1R Etosha 18 RIP 0-2 cm 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	31.0

Phase Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	21.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	48.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Silicate Hydroxide Hydrate |
| --- | --- | --- | --- | --- |
| 1 550c | 31.0 | 21.0 | 48.0 | 0.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7637.0000 | 7653.7953 | 7637.0000 |
| 2.0164 | 7708.5664 | 7605.4635 | 7579.0014 |
| 2.0274 | 7510.6893 | 7548.3293 | 7521.0027 |
| 2.0384 | 7419.8850 | 7491.2376 | 7463.0041 |
| 2.0494 | 7449.0472 | 7434.1913 | 7405.0055 |
| 2.0604 | 7555.4911 | 7377.1934 | 7347.0069 |
| 2.0714 | 7394.1888 | 7320.2472 | 7289.0082 |
| 2.0824 | 7392.3456 | 7263.3563 | 7231.0096 |
| 2.0934 | 7452.1898 | 7206.5245 | 7173.0110 |
| 2.1044 | 7213.9956 | 7149.7562 | 7115.0124 |
| 2.1154 | 7413.7817 | 7093.0558 | 7057.0137 |
| 2.1264 | 7330.2886 | 7036.4285 | 6999.0151 |
| 2.1374 | 7232.4867 | 6979.8798 | 6941.0165 |
| 2.1484 | 7281.2552 | 6923.4157 | 6883.0179 |
| 2.1594 | 7051.5133 | 6867.0429 | 6825.0192 |
| 2.1704 | 6996.9115 | 6810.7687 | 6767.0206 |
| 2.1814 | 7087.3599 | 6754.6014 | 6709.0220 |
| 2.1924 | 7079.6573 | 6698.5299 | 6651.0234 |
| 2.2034 | 7003.8230 | 6642.4927 | 6592.8925 |
| 2.2144 | 6962.3953 | 6586.5731 | 6534.7616 |
| 2.2254 | 6886.2320 | 6530.8047 | 6476.6308 |
| 2.2364 | 6764.2360 | 6475.2029 | 6418.4999 |
| 2.2474 | 6872.4346 | 6419.7857 | 6360.3690 |
| 2.2584 | 6765.1175 | 6364.5745 | 6302.2382 |
| 2.2694 | 6834.5752 | 6309.5953 | 6244.1073 |
| 2.2804 | 6834.7547 | 6254.8793 | 6185.9764 |
| 2.2914 | 6837.5890 | 6200.4651 | 6127.8456 |
| 2.3024 | 6710.6947 | 6146.4007 | 6069.7147 |
| 2.3134 | 6582.4474 | 6092.7457 | 6011.5838 |
| 2.3244 | 6640.3761 | 6039.5745 | 5953.4529 |
| 2.3354 | 6653.2360 | 5986.9803 | 5895.3221 |
| 2.3464 | 6701.1898 | 5935.0791 | 5837.1912 |
| 2.3574 | 6632.4631 | 5884.0144 | 5779.0603 |
| 2.3684 | 6528.6991 | 5833.9624 | 5720.9295 |
| 2.3794 | 6495.0157 | 5785.1378 | 5662.7986 |
| 2.3904 | 6532.2601 | 5737.7981 | 5604.6677 |
| 2.4014 | 6546.5664 | 5692.2488 | 5546.5369 |
| 2.4124 | 6383.0585 | 5648.8464 | 5488.4060 |
| 2.4234 | 6331.0895 | 5607.9996 | 5430.2751 |
| 2.4344 | 6316.9410 | 5570.1681 | 5372.1443 |
| 2.4454 | 6377.1446 | 5535.8582 | 5314.0134 |
| 2.4564 | 6320.1745 | 5505.6137 | 5255.8825 |
| 2.4674 | 6197.3953 | 5480.0027 | 5197.7517 |
| 2.4784 | 6227.9012 | 5459.5993 | 5139.6208 |
| 2.4894 | 6188.7965 | 5444.9601 | 5081.4899 |
| 2.5004 | 6177.2743 | 5436.5966 | 5023.3591 |
| 2.5114 | 6131.4612 | 5434.9426 | 4965.2282 |
| 2.5224 | 6123.2385 | 5440.3191 | 4907.0973 |
| 2.5334 | 6114.1917 | 5452.8953 | 4848.9665 |
| 2.5444 | 6030.3761 | 5472.6485 | 4790.8356 |
| 2.5554 | 6099.1613 | 5499.3207 | 4732.7047 |
| 2.5664 | 6054.1681 | 5532.3519 | 4674.5739 |
| 2.5774 | 6065.6136 | 5570.7961 | 4616.3107 |
| 2.5884 | 6076.7773 | 5613.4567 | 4558.0476 |
| 2.5994 | 5976.0354 | 5658.6246 | 4499.7845 |
| 2.6104 | 5902.2276 | 5704.0405 | 4441.5214 |
| 2.6214 | 5871.8574 | 5746.8606 | 4383.2583 |
| 2.6324 | 5925.9513 | 5783.6487 | 4324.9952 |
| 2.6434 | 5922.7719 | 5810.4622 | 4266.7321 |
| 2.6544 | 5807.3004 | 5823.0850 | 4208.4690 |
| 2.6654 | 5759.1504 | 5817.4331 | 4150.2059 |
| 2.6764 | 5535.5722 | 5790.0987 | 4091.9428 |
| 2.6874 | 5440.6627 | 5738.9153 | 4033.6796 |
| 2.6984 | 5416.9646 | 5663.3672 | 3975.4165 |
| 2.7094 | 5341.2035 | 5564.6938 | 3917.1534 |
| 2.7204 | 5268.4725 | 5445.6456 | 3858.8903 |
| 2.7314 | 4946.7404 | 5309.9878 | 3800.6272 |
| 2.7424 | 4778.6504 | 5161.9231 | 3742.3641 |
| 2.7534 | 4701.1662 | 5005.5703 | 3684.1010 |
| 2.7644 | 4539.8894 | 4844.5912 | 3625.6744 |
| 2.7754 | 4357.2723 | 4682.2663 | 3567.2478 |
| 2.7864 | 4224.6622 | 4521.2137 | 3508.8213 |
| 2.7974 | 4124.9292 | 4363.4611 | 3450.3947 |
| 2.8084 | 3930.0644 | 4210.5346 | 3391.9681 |
| 2.8194 | 3687.9823 | 4063.5278 | 3333.5416 |
| 2.8304 | 3596.8628 | 3923.1668 | 3275.1150 |
| 2.8414 | 3466.7620 | 3789.8665 | 3216.6884 |
| 2.8524 | 3399.3225 | 3663.7797 | 3158.2618 |
| 2.8634 | 3154.4070 | 3544.8430 | 3099.8353 |
| 2.8744 | 3109.0442 | 3432.8181 | 3041.4087 |
| 2.8854 | 3022.4543 | 3327.3319 | 2982.9821 |
| 2.8964 | 2994.1195 | 3227.9135 | 2924.5556 |
| 2.9074 | 2922.8663 | 3134.0286 | 2866.1290 |
| 2.9184 | 2901.0614 | 3045.1098 | 2807.7024 |
| 2.9294 | 2659.7345 | 2960.5830 | 2749.2759 |
| 2.9404 | 2626.2055 | 2885.1214 | 2690.8493 |
| 2.9514 | 2715.4867 | 2836.8213 | 2666.7478 |
| 2.9624 | 2699.9292 | 2796.5696 | 2642.6463 |
| 2.9734 | 2604.1023 | 2758.6945 | 2618.5449 |
| 2.9844 | 2593.6244 | 2722.8093 | 2594.4434 |
| 2.9954 | 2580.0177 | 2688.5794 | 2570.3419 |
| 3.0064 | 2500.7394 | 2655.7198 | 2546.2405 |
| 3.0174 | 2528.9380 | 2623.9919 | 2522.1390 |
| 3.0284 | 2467.1209 | 2593.1978 | 2498.0375 |
| 3.0394 | 2381.5733 | 2563.1758 | 2473.9361 |
| 3.0504 | 2393.1204 | 2533.7945 | 2449.8346 |
| 3.0614 | 2365.6962 | 2504.9484 | 2425.7331 |
| 3.0724 | 2418.8078 | 2476.5525 | 2401.6317 |
| 3.0834 | 2403.2743 | 2448.5390 | 2377.5302 |
| 3.0944 | 2344.9159 | 2420.8538 | 2353.4287 |
| 3.1054 | 2332.7522 | 2393.4531 | 2329.3273 |
| 3.1164 | 2299.6893 | 2366.3016 | 2305.2258 |
| 3.1274 | 2282.4926 | 2340.0719 | 2281.1243 |
| 3.1384 | 2273.5526 | 2317.2374 | 2261.6245 |
| 3.1494 | 2222.6686 | 2295.2810 | 2242.1247 |
| 3.1604 | 2137.8982 | 2273.4843 | 2222.6249 |
| 3.1714 | 2149.0452 | 2251.8330 | 2203.1251 |
| 3.1824 | 2204.2729 | 2230.3144 | 2183.6253 |
| 3.1934 | 2165.1858 | 2208.9175 | 2164.1255 |
| 3.2044 | 2099.8850 | 2187.6326 | 2144.6257 |
| 3.2154 | 2107.7129 | 2166.4509 | 2125.1258 |
| 3.2264 | 2129.7920 | 2145.3647 | 2105.6260 |
| 3.2374 | 2094.0787 | 2124.3669 | 2086.1262 |
| 3.2484 | 2041.3889 | 2103.4511 | 2066.6264 |
| 3.2594 | 1984.9941 | 2082.6115 | 2047.1266 |
| 3.2704 | 2004.3274 | 2061.8428 | 2027.6268 |
| 3.2814 | 2015.1376 | 2041.1400 | 2008.1270 |
| 3.2924 | 1956.3363 | 2020.4988 | 1988.6272 |
| 3.3034 | 1953.0275 | 1999.9151 | 1969.1274 |
| 3.3144 | 1984.0462 | 1980.3458 | 1949.6276 |
| 3.3254 | 1949.5280 | 1965.2064 | 1936.4287 |
| 3.3364 | 1854.4302 | 1951.0747 | 1923.2298 |
| 3.3474 | 1839.4386 | 1936.9872 | 1910.0309 |
| 3.3584 | 1881.5280 | 1922.9411 | 1896.8320 |
| 3.3694 | 1882.4395 | 1908.9339 | 1883.6331 |
| 3.3804 | 1879.5447 | 1894.9634 | 1870.4342 |
| 3.3914 | 1837.4071 | 1881.0273 | 1857.2353 |
| 3.4024 | 1792.7566 | 1867.1236 | 1844.0364 |
| 3.4134 | 1793.0639 | 1853.2506 | 1830.8375 |
| 3.4244 | 1836.6918 | 1839.4063 | 1817.6386 |
| 3.4354 | 1841.4562 | 1825.5894 | 1804.4397 |
| 3.4464 | 1782.7999 | 1811.7982 | 1791.2408 |
| 3.4574 | 1773.1623 | 1798.0313 | 1778.0419 |
| 3.4684 | 1787.2694 | 1784.2875 | 1764.8430 |
| 3.4794 | 1730.4169 | 1770.5655 | 1751.6441 |
| 3.4904 | 1743.8319 | 1756.8641 | 1738.4452 |
| 3.5014 | 1730.7345 | 1743.4906 | 1725.2463 |
| 3.5124 | 1722.5742 | 1731.5409 | 1714.0690 |
| 3.5234 | 1685.2301 | 1719.9170 | 1702.8917 |
| 3.5344 | 1642.9125 | 1708.3100 | 1691.7144 |
| 3.5454 | 1707.2370 | 1696.7189 | 1680.5371 |
| 3.5564 | 1672.9587 | 1685.1430 | 1669.3597 |
| 3.5674 | 1637.3294 | 1673.5815 | 1658.1824 |
| 3.5784 | 1560.2684 | 1662.0339 | 1647.0051 |
| 3.5894 | 1593.2036 | 1650.4993 | 1635.8278 |
| 3.6004 | 1593.5737 | 1638.9773 | 1624.6505 |
| 3.6114 | 1561.9872 | 1627.4672 | 1613.4731 |
| 3.6224 | 1577.5900 | 1615.9685 | 1602.2958 |
| 3.6334 | 1556.7896 | 1604.4807 | 1591.1185 |
| 3.6444 | 1580.0978 | 1593.0033 | 1579.9412 |
| 3.6554 | 1545.5044 | 1581.5359 | 1568.7639 |
| 3.6664 | 1611.6116 | 1570.0779 | 1557.5865 |
| 3.6774 | 1558.8820 | 1558.6291 | 1546.4092 |
| 3.6884 | 1543.7168 | 1547.1890 | 1535.2319 |
| 3.6994 | 1526.0364 | 1535.7572 | 1524.0546 |
| 3.7104 | 1422.6273 | 1524.3335 | 1512.8773 |
| 3.7214 | 1473.4661 | 1512.9174 | 1501.6999 |
| 3.7324 | 1368.3662 | 1501.5086 | 1490.5226 |
| 3.7434 | 1501.2980 | 1490.1070 | 1479.3453 |
| 3.7544 | 1386.8982 | 1478.7120 | 1468.1680 |
| 3.7654 | 1446.7267 | 1467.3236 | 1456.9907 |
| 3.7764 | 1461.7252 | 1455.9415 | 1445.8133 |
| 3.7874 | 1418.3894 | 1444.5654 | 1434.6360 |
| 3.7984 | 1359.3476 | 1433.1950 | 1423.4587 |
| 3.8094 | 1459.4965 | 1421.8302 | 1412.2814 |
| 3.8204 | 1426.5147 | 1410.4707 | 1401.1041 |
| 3.8314 | 1377.2576 | 1399.1164 | 1389.9267 |
| 3.8424 | 1427.1598 | 1387.7670 | 1378.7494 |
| 3.8534 | 1357.0265 | 1376.4224 | 1367.5721 |
| 3.8644 | 1341.4562 | 1365.0824 | 1356.3948 |
| 3.8754 | 1326.8476 | 1354.5075 | 1345.2175 |
| 3.8864 | 1363.8628 | 1347.4044 | 1339.0289 |
| 3.8974 | 1349.6765 | 1341.0660 | 1332.8404 |
| 3.9084 | 1380.3141 | 1334.7316 | 1326.6519 |
| 3.9194 | 1341.2773 | 1328.4010 | 1320.4633 |
| 3.9304 | 1344.3584 | 1322.0741 | 1314.2748 |
| 3.9414 | 1350.8574 | 1315.7508 | 1308.0863 |
| 3.9524 | 1345.8776 | 1309.4310 | 1301.8978 |
| 3.9634 | 1338.7315 | 1303.1144 | 1295.7092 |
| 3.9744 | 1290.6003 | 1296.8012 | 1289.5207 |
| 3.9854 | 1295.3363 | 1290.4910 | 1283.3322 |
| 3.9964 | 1300.4051 | 1284.1838 | 1277.1436 |
| 4.0074 | 1276.8623 | 1277.8796 | 1270.9551 |
| 4.0184 | 1257.4513 | 1271.5782 | 1264.7666 |
| 4.0294 | 1290.7837 | 1265.2795 | 1258.5780 |
| 4.0404 | 1234.5939 | 1258.9834 | 1252.3895 |
| 4.0514 | 1216.7286 | 1252.6900 | 1246.2010 |
| 4.0624 | 1250.5497 | 1246.6760 | 1240.0125 |
| 4.0734 | 1261.5034 | 1241.9273 | 1235.6408 |
| 4.0844 | 1222.4336 | 1237.4579 | 1231.2692 |
| 4.0954 | 1205.4002 | 1232.9908 | 1226.8976 |
| 4.1064 | 1216.8771 | 1228.5259 | 1222.5260 |
| 4.1174 | 1211.8348 | 1224.0631 | 1218.1543 |
| 4.1284 | 1214.3200 | 1219.6023 | 1213.7827 |
| 4.1394 | 1184.8407 | 1215.1436 | 1209.4111 |
| 4.1504 | 1193.1136 | 1210.6868 | 1205.0394 |
| 4.1614 | 1203.0875 | 1206.2318 | 1200.6678 |
| 4.1724 | 1236.6239 | 1201.7787 | 1196.2962 |
| 4.1834 | 1218.3982 | 1197.3274 | 1191.9246 |
| 4.1944 | 1203.8520 | 1192.8778 | 1187.5529 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 1 550c | 2.0054 | 29.9894 | 0.0110 | 4/25/2024 3:30:03 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6829 | 1523.33 | 0.2381 | 32.90404 | 100.00 |
| 8.6665 | 1016.18 | 0.1515 | 10.19493 | 66.71 |
| 10.6278 | 67.29 | 0.5196 | 8.31745 | 4.42 |
| 15.8335 | 562.77 | 0.2165 | 5.59266 | 36.94 |
| 17.5925 | 54.63 | 0.2598 | 5.03724 | 3.59 |
| 18.2852 | 61.12 | 0.1299 | 4.84794 | 4.01 |
| 19.5641 | 68.83 | 0.3464 | 4.53381 | 4.52 |
| 20.2034 | 64.31 | 0.2598 | 4.39178 | 4.22 |
| 26.0026 | 354.80 | 0.1082 | 3.42396 | 23.29 |
| 26.6701 | 116.08 | 0.2165 | 3.33976 | 7.62 |
| 27.5077 | 78.24 | 0.5196 | 3.23994 | 5.14 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-083-1730 | 68 | Sodium Aluminum Silicate Hydrate | Na14.96 Al15.36 Si32.64 O96 ( H2 O )16 | Analcime | 31 |
| * | 04-015-8329 | 40 | Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Na0.01 Ca0.01 Mg2.04 Fe0.11 Al2.12 Si7.8 O20 ( O H )2 ( H2 O )8 | Palygorskite-M | 21 |
| * | 04-025-4215 | 44 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 48 |
| * | 01-075-8323 | No Matching Lines | Magnesium Silicate Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ) ( H2 O )11.82 | Sepiolite | - |

Anchor Scan Parameters

Dataset Name	1 550c

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\REP 1\1 550c.xrdml

Sample Identification	1 550c

Measurement Start Date/Time	4/25/2024 3:30:03 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes