1R Etosha 18 RIP 0-2 cm  400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	8.0

Phase Potassium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide

Weight fraction/ %	51.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	7.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	7.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	18.0

Phase Potassium Manganese Silicate Hydroxide Hydrate

Weight fraction/ %	6.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicon Oxide Hydrate | Potassium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide | Magnesium Silicate Hydroxide Hydrate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Manganese Silicate Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 400c | 8.0 | 51.0 | 3.0 | 7.0 | 7.0 | 18.0 | 6.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7237.0000 | 7248.7184 | 7237.0000 |
| 2.0164 | 7203.5329 | 7197.2198 | 7184.4002 |
| 2.0274 | 7166.0983 | 7145.0169 | 7131.8004 |
| 2.0384 | 7171.4749 | 7092.8326 | 7079.2006 |
| 2.0494 | 7213.3432 | 7040.6680 | 7026.6008 |
| 2.0604 | 7266.2006 | 6988.5245 | 6974.0010 |
| 2.0714 | 7089.3923 | 6936.4034 | 6921.4011 |
| 2.0824 | 7115.9110 | 6884.3061 | 6868.8013 |
| 2.0934 | 6939.8869 | 6832.2344 | 6816.2015 |
| 2.1044 | 6921.9823 | 6780.1898 | 6763.6017 |
| 2.1154 | 7127.5909 | 6728.1743 | 6711.0019 |
| 2.1264 | 6910.5029 | 6676.1900 | 6658.4021 |
| 2.1374 | 6794.6814 | 6624.2391 | 6605.8023 |
| 2.1484 | 6919.6804 | 6572.3240 | 6553.2025 |
| 2.1594 | 6904.7502 | 6520.4474 | 6500.6027 |
| 2.1704 | 6831.5973 | 6468.6122 | 6448.0029 |
| 2.1814 | 6774.0708 | 6416.8216 | 6395.4031 |
| 2.1924 | 6748.4912 | 6365.0772 | 6342.8033 |
| 2.2034 | 6857.5133 | 6313.2580 | 6290.0731 |
| 2.2144 | 6686.5093 | 6261.4932 | 6237.3430 |
| 2.2254 | 6626.1858 | 6209.7891 | 6184.6129 |
| 2.2364 | 6687.9926 | 6158.1510 | 6131.8827 |
| 2.2474 | 6559.7502 | 6106.5844 | 6079.1526 |
| 2.2584 | 6549.7252 | 6055.0959 | 6026.4225 |
| 2.2694 | 6605.5605 | 6003.6922 | 5973.6924 |
| 2.2804 | 6547.0487 | 5952.3814 | 5920.9622 |
| 2.2914 | 6468.2370 | 5901.1721 | 5868.2321 |
| 2.3024 | 6462.3805 | 5850.0743 | 5815.5020 |
| 2.3134 | 6457.5192 | 5799.0989 | 5762.7719 |
| 2.3244 | 6473.6731 | 5748.2587 | 5710.0417 |
| 2.3354 | 6414.6578 | 5697.5683 | 5657.3116 |
| 2.3464 | 6303.8466 | 5647.0445 | 5604.5815 |
| 2.3574 | 6226.7325 | 5596.7073 | 5551.8514 |
| 2.3684 | 6324.0089 | 5546.5806 | 5499.1212 |
| 2.3794 | 6389.6283 | 5496.6935 | 5446.3911 |
| 2.3904 | 6260.5890 | 5447.0824 | 5393.6610 |
| 2.4014 | 6204.9381 | 5397.7935 | 5340.9308 |
| 2.4124 | 6278.1028 | 5348.8861 | 5288.2007 |
| 2.4234 | 6176.2232 | 5300.4376 | 5235.4706 |
| 2.4344 | 6145.8791 | 5252.5496 | 5182.7405 |
| 2.4454 | 6130.4572 | 5205.3553 | 5130.0103 |
| 2.4564 | 6013.2517 | 5159.0289 | 5077.2802 |
| 2.4674 | 6045.5162 | 5113.7962 | 5024.5501 |
| 2.4784 | 6061.8555 | 5069.9464 | 4971.8200 |
| 2.4894 | 5975.4100 | 5027.8432 | 4919.0898 |
| 2.5004 | 5908.2522 | 4987.9360 | 4866.3597 |
| 2.5114 | 5929.7847 | 4950.7665 | 4813.6296 |
| 2.5224 | 5928.6455 | 4916.9710 | 4760.8995 |
| 2.5334 | 5806.5959 | 4887.2751 | 4708.1693 |
| 2.5444 | 5805.1008 | 4862.4775 | 4655.4392 |
| 2.5554 | 5881.3530 | 4843.4222 | 4602.7091 |
| 2.5664 | 5776.8997 | 4830.9562 | 4549.9789 |
| 2.5774 | 5788.4484 | 4825.7527 | 4497.1185 |
| 2.5884 | 5686.4749 | 4828.6182 | 4444.2581 |
| 2.5994 | 5676.0266 | 4840.0419 | 4391.3976 |
| 2.6104 | 5775.2208 | 4860.2332 | 4338.5372 |
| 2.6214 | 5695.1839 | 4889.0316 | 4285.6767 |
| 2.6324 | 5595.2581 | 4925.8087 | 4232.8163 |
| 2.6434 | 5459.2261 | 4969.3569 | 4179.9558 |
| 2.6544 | 5496.3948 | 5017.7596 | 4127.0954 |
| 2.6654 | 5405.5811 | 5068.2431 | 4074.2349 |
| 2.6764 | 5359.0010 | 5117.0299 | 4021.3745 |
| 2.6874 | 5194.1603 | 5159.2648 | 3968.5141 |
| 2.6984 | 5123.6416 | 5189.1433 | 3915.6536 |
| 2.7094 | 5174.6372 | 5200.4097 | 3862.7932 |
| 2.7204 | 5007.8466 | 5187.3087 | 3809.9327 |
| 2.7314 | 4970.1121 | 5145.8237 | 3757.0723 |
| 2.7424 | 4696.9508 | 5074.7383 | 3704.2118 |
| 2.7534 | 4602.0610 | 4975.9855 | 3651.3514 |
| 2.7644 | 4484.7492 | 4853.9446 | 3598.3299 |
| 2.7754 | 4292.0649 | 4714.7474 | 3545.3083 |
| 2.7864 | 4120.0103 | 4564.6145 | 3492.2868 |
| 2.7974 | 3916.6991 | 4409.1568 | 3439.2653 |
| 2.8084 | 3803.2753 | 4252.9793 | 3386.2438 |
| 2.8194 | 3720.2370 | 4099.6142 | 3333.2222 |
| 2.8304 | 3585.7876 | 3951.6215 | 3280.2007 |
| 2.8414 | 3543.2399 | 3810.7396 | 3227.1792 |
| 2.8524 | 3295.8795 | 3678.0304 | 3174.1576 |
| 2.8634 | 3184.2124 | 3554.0036 | 3121.1361 |
| 2.8744 | 3184.8550 | 3438.7250 | 3068.1146 |
| 2.8854 | 3018.8250 | 3331.9126 | 3015.0931 |
| 2.8964 | 3003.0575 | 3233.0261 | 2962.0715 |
| 2.9074 | 2861.5437 | 3141.3505 | 2909.0500 |
| 2.9184 | 2803.4154 | 3056.0701 | 2856.0285 |
| 2.9294 | 2773.9616 | 2976.3331 | 2803.0070 |
| 2.9404 | 2746.2660 | 2901.6123 | 2749.9854 |
| 2.9514 | 2802.8830 | 2852.7655 | 2719.5343 |
| 2.9624 | 2587.8024 | 2807.4457 | 2689.0832 |
| 2.9734 | 2606.4503 | 2764.7288 | 2658.6321 |
| 2.9844 | 2550.1977 | 2724.0949 | 2628.1809 |
| 2.9954 | 2594.4956 | 2685.1155 | 2597.7298 |
| 3.0064 | 2467.0806 | 2647.4453 | 2567.2787 |
| 3.0174 | 2480.3225 | 2610.8110 | 2536.8276 |
| 3.0284 | 2418.2891 | 2574.9997 | 2506.3764 |
| 3.0394 | 2423.1445 | 2539.8478 | 2475.9253 |
| 3.0504 | 2377.8501 | 2505.2301 | 2445.4742 |
| 3.0614 | 2371.3068 | 2471.0514 | 2415.0231 |
| 3.0724 | 2267.1962 | 2437.2389 | 2384.5719 |
| 3.0834 | 2246.0433 | 2403.7369 | 2354.1208 |
| 3.0944 | 2305.3540 | 2370.5015 | 2323.6697 |
| 3.1054 | 2237.5418 | 2337.4985 | 2293.2186 |
| 3.1164 | 2229.9651 | 2304.7000 | 2262.7675 |
| 3.1274 | 2220.8938 | 2272.2495 | 2232.3163 |
| 3.1384 | 2250.2660 | 2251.7589 | 2213.9955 |
| 3.1494 | 2208.7030 | 2231.5808 | 2195.6747 |
| 3.1604 | 2114.1092 | 2211.5349 | 2177.3539 |
| 3.1714 | 2143.7316 | 2191.6088 | 2159.0331 |
| 3.1824 | 2129.2060 | 2171.7916 | 2140.7123 |
| 3.1934 | 2108.7876 | 2152.0739 | 2122.3915 |
| 3.2044 | 2079.4218 | 2132.4471 | 2104.0707 |
| 3.2154 | 2121.9440 | 2112.9035 | 2085.7498 |
| 3.2264 | 2126.5575 | 2093.4363 | 2067.4290 |
| 3.2374 | 2104.1062 | 2074.0394 | 2049.1082 |
| 3.2484 | 2062.0000 | 2054.7072 | 2030.7874 |
| 3.2594 | 2039.8702 | 2035.4346 | 2012.4666 |
| 3.2704 | 1945.8840 | 2016.2171 | 1994.1458 |
| 3.2814 | 1948.1505 | 1997.0506 | 1975.8250 |
| 3.2924 | 1985.2876 | 1977.9313 | 1957.5042 |
| 3.3034 | 1946.0393 | 1958.8558 | 1939.1834 |
| 3.3144 | 1898.4661 | 1939.9045 | 1920.8625 |
| 3.3254 | 1885.7965 | 1926.9073 | 1908.6250 |
| 3.3364 | 1928.0526 | 1914.0289 | 1896.3874 |
| 3.3474 | 1937.0088 | 1901.1832 | 1884.1498 |
| 3.3584 | 1883.9852 | 1888.3683 | 1871.9123 |
| 3.3694 | 1838.3314 | 1875.5820 | 1859.6747 |
| 3.3804 | 1837.1455 | 1862.8224 | 1847.4371 |
| 3.3914 | 1841.1947 | 1850.0880 | 1835.1995 |
| 3.4024 | 1825.0492 | 1837.3771 | 1822.9620 |
| 3.4134 | 1828.7709 | 1824.6883 | 1810.7244 |
| 3.4244 | 1801.5973 | 1812.0202 | 1798.4868 |
| 3.4354 | 1724.5752 | 1799.3716 | 1786.2492 |
| 3.4464 | 1720.6760 | 1786.7413 | 1774.0117 |
| 3.4574 | 1776.9676 | 1774.1283 | 1761.7741 |
| 3.4684 | 1716.2183 | 1761.5316 | 1749.5365 |
| 3.4794 | 1681.5870 | 1748.9502 | 1737.2990 |
| 3.4904 | 1711.4159 | 1736.3833 | 1725.0614 |
| 3.5014 | 1723.6716 | 1723.8311 | 1712.8238 |
| 3.5124 | 1725.3677 | 1711.3666 | 1700.6630 |
| 3.5234 | 1696.7611 | 1698.9153 | 1688.5022 |
| 3.5344 | 1544.4341 | 1686.4757 | 1676.3413 |
| 3.5454 | 1601.5989 | 1674.0471 | 1664.1805 |
| 3.5564 | 1601.2846 | 1661.6289 | 1652.0197 |
| 3.5674 | 1630.4651 | 1649.2205 | 1639.8589 |
| 3.5784 | 1608.8766 | 1636.8216 | 1627.6981 |
| 3.5894 | 1622.4071 | 1624.4316 | 1615.5372 |
| 3.6004 | 1553.3441 | 1612.0502 | 1603.3764 |
| 3.6114 | 1556.6293 | 1599.6767 | 1591.2156 |
| 3.6224 | 1550.8982 | 1587.3110 | 1579.0548 |
| 3.6334 | 1517.6942 | 1574.9526 | 1566.8939 |
| 3.6444 | 1546.7488 | 1562.6012 | 1554.7331 |
| 3.6554 | 1539.6578 | 1550.2565 | 1542.5723 |
| 3.6664 | 1509.6096 | 1537.9180 | 1530.4115 |
| 3.6774 | 1502.3953 | 1525.5857 | 1518.2506 |
| 3.6884 | 1527.5354 | 1514.3607 | 1506.0898 |
| 3.6994 | 1458.6814 | 1505.5899 | 1498.5808 |
| 3.7104 | 1531.4602 | 1497.9260 | 1491.0717 |
| 3.7214 | 1469.3599 | 1490.2671 | 1483.5627 |
| 3.7324 | 1431.3904 | 1482.6131 | 1476.0537 |
| 3.7434 | 1386.6106 | 1474.9637 | 1468.5446 |
| 3.7544 | 1448.8909 | 1467.3188 | 1461.0356 |
| 3.7654 | 1460.6991 | 1459.6781 | 1453.5266 |
| 3.7764 | 1401.2896 | 1452.0415 | 1446.0175 |
| 3.7874 | 1389.0973 | 1444.4088 | 1438.5085 |
| 3.7984 | 1423.0413 | 1436.7799 | 1430.9995 |
| 3.8094 | 1434.2920 | 1429.1546 | 1423.4904 |
| 3.8204 | 1390.5044 | 1421.5327 | 1415.9814 |
| 3.8314 | 1407.7581 | 1413.9142 | 1408.4724 |
| 3.8424 | 1402.9469 | 1406.2989 | 1400.9633 |
| 3.8534 | 1421.2330 | 1398.6866 | 1393.4543 |
| 3.8644 | 1433.8284 | 1391.0773 | 1385.9452 |
| 3.8754 | 1376.6529 | 1383.4709 | 1378.4362 |
| 3.8864 | 1416.9779 | 1375.8672 | 1370.9272 |
| 3.8974 | 1352.7188 | 1368.2661 | 1363.4181 |
| 3.9084 | 1338.9169 | 1360.6676 | 1355.9091 |
| 3.9194 | 1359.2065 | 1353.0715 | 1348.4001 |
| 3.9304 | 1319.5659 | 1345.4778 | 1340.8910 |
| 3.9414 | 1325.8387 | 1337.8864 | 1333.3820 |
| 3.9524 | 1286.8083 | 1330.2971 | 1325.8730 |
| 3.9634 | 1298.1219 | 1322.7100 | 1318.3639 |
| 3.9744 | 1297.2036 | 1315.1249 | 1310.8549 |
| 3.9854 | 1314.3186 | 1307.5418 | 1303.3459 |
| 3.9964 | 1265.3830 | 1299.9606 | 1295.8368 |
| 4.0074 | 1268.0384 | 1292.3813 | 1288.3278 |
| 4.0184 | 1329.2787 | 1284.8037 | 1280.8187 |
| 4.0294 | 1293.9843 | 1277.2279 | 1273.3097 |
| 4.0404 | 1265.2247 | 1269.6537 | 1265.8007 |
| 4.0514 | 1236.0030 | 1262.0811 | 1258.2916 |
| 4.0624 | 1260.3978 | 1254.6647 | 1250.7826 |
| 4.0734 | 1277.1032 | 1247.5937 | 1243.9267 |
| 4.0844 | 1204.9248 | 1240.6787 | 1237.0707 |
| 4.0954 | 1201.4120 | 1233.7651 | 1230.2148 |
| 4.1064 | 1234.6042 | 1226.8529 | 1223.3588 |
| 4.1174 | 1251.3186 | 1219.9421 | 1216.5029 |
| 4.1284 | 1250.4400 | 1213.0325 | 1209.6469 |
| 4.1394 | 1215.2389 | 1206.1241 | 1202.7910 |
| 4.1504 | 1176.4454 | 1199.2170 | 1195.9350 |
| 4.1614 | 1187.6342 | 1192.3110 | 1189.0791 |
| 4.1724 | 1206.7306 | 1185.4062 | 1182.2231 |
| 4.1834 | 1160.1770 | 1178.5024 | 1175.3672 |
| 4.1944 | 1153.4573 | 1171.5998 | 1168.5112 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 1 400c | 2.0054 | 29.9894 | 0.0110 | 4/25/2024 1:39:47 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7279 | 1240.10 | 0.1948 | 32.36131 | 100.00 |
| 7.1344 | 1156.66 | 0.1732 | 12.38043 | 93.27 |
| 8.7085 | 757.33 | 0.1515 | 10.14578 | 61.07 |
| 10.4493 | 41.92 | 0.3464 | 8.45912 | 3.38 |
| 15.7055 | 1002.82 | 0.1299 | 5.63796 | 80.87 |
| 17.6191 | 59.53 | 0.2598 | 5.02970 | 4.80 |
| 18.1826 | 152.32 | 0.1082 | 4.87505 | 12.28 |
| 19.5512 | 83.45 | 0.3464 | 4.53677 | 6.73 |
| 21.0045 | 13.60 | 0.3464 | 4.22605 | 1.10 |
| 24.1995 | 60.27 | 0.1299 | 3.67484 | 4.86 |
| 25.8778 | 751.23 | 0.1191 | 3.44019 | 60.58 |
| 26.6871 | 179.22 | 0.3031 | 3.33767 | 14.45 |
| 27.4658 | 66.72 | 0.1732 | 3.24479 | 5.38 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-009-3254 | 36 | Sodium Aluminum Silicon Oxide Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 8 |
| * | 04-016-6884 | 16 | Potassium Magnesium Manganese Aluminum Iron Silicon Oxide Hydroxide | K0.8 Mg2.6 Mn0.1 Fe0.2 Al1.3 Si2.8 O10 ( O H )2 | Muscovite-1M | 51 |
| * | 01-075-8323 | 24 | Magnesium Silicate Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ) ( H2 O )11.82 | Sepiolite | 3 |
| * | 04-015-2963 | 25 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 7 |
| * | 01-082-8023 | 23 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 7 |
| * | 04-025-4215 | 27 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 18 |
| * | 01-089-6415 | 38 | Potassium Manganese Silicate Hydroxide Hydrate | K3.68 Mn15.904 Si25.472 O64 ( O H )9.376 ( H2 O )7.024 | Ganophyllite | 6 |

Anchor Scan Parameters

Dataset Name	1 400c

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\REP 1\1 400c.xrdml

Sample Identification	1 400c

Measurement Start Date/Time	4/25/2024 1:39:47 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes