2 Etosha 18 SS 0-2 cm 550

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	17.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	25.0

Phase Potassium Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	20.0

Phase Silicon Oxide

Weight fraction/ %	8.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	30.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Aluminum Silicate Hydroxide | Silicon Oxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- |
| 2 Etosha18 SS 0-2cm S1 550C | 17.0 | 25.0 | 20.0 | 8.0 | 30.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 9379.0000 | 9356.0274 | 9379.0000 |
| 2.0164 | 9345.6401 | 9324.9166 | 9312.3317 |
| 2.0274 | 9157.4995 | 9258.6675 | 9245.6633 |
| 2.0384 | 9214.1239 | 9192.4395 | 9178.9950 |
| 2.0494 | 9127.6431 | 9126.2342 | 9112.3266 |
| 2.0604 | 8905.2345 | 9060.0530 | 9045.6583 |
| 2.0714 | 8874.7257 | 8993.8977 | 8978.9900 |
| 2.0824 | 9019.2468 | 8927.7702 | 8912.3216 |
| 2.0934 | 8973.0875 | 8861.6724 | 8845.6533 |
| 2.1044 | 8815.3451 | 8795.6066 | 8778.9849 |
| 2.1154 | 8793.1396 | 8729.5751 | 8712.3166 |
| 2.1264 | 8801.1962 | 8663.5807 | 8645.6482 |
| 2.1374 | 8858.9616 | 8597.6261 | 8578.9799 |
| 2.1484 | 8654.7380 | 8531.7147 | 8512.3116 |
| 2.1594 | 8583.6234 | 8465.8499 | 8445.6432 |
| 2.1704 | 8585.1121 | 8400.0355 | 8378.9749 |
| 2.1814 | 8586.7817 | 8334.2759 | 8312.3065 |
| 2.1924 | 8443.8658 | 8268.4993 | 8245.6382 |
| 2.2034 | 8401.2478 | 8202.7953 | 8178.8248 |
| 2.2144 | 8328.2630 | 8137.0854 | 8112.0113 |
| 2.2254 | 8434.1672 | 8071.4525 | 8045.1979 |
| 2.2364 | 8372.5103 | 8005.9039 | 7978.3844 |
| 2.2474 | 8237.6539 | 7940.4477 | 7911.5710 |
| 2.2584 | 8191.5005 | 7875.0931 | 7844.7575 |
| 2.2694 | 8290.6844 | 7809.8502 | 7777.9441 |
| 2.2804 | 8018.0865 | 7744.7306 | 7711.1306 |
| 2.2914 | 7926.4091 | 7679.7474 | 7644.3172 |
| 2.3024 | 8040.6549 | 7614.9156 | 7577.5037 |
| 2.3134 | 8072.4995 | 7550.2522 | 7510.6903 |
| 2.3244 | 8067.3953 | 7485.7772 | 7443.8768 |
| 2.3354 | 7906.5280 | 7421.5139 | 7377.0634 |
| 2.3464 | 7869.2979 | 7357.4899 | 7310.2500 |
| 2.3574 | 7841.3068 | 7293.7389 | 7243.4365 |
| 2.3684 | 7696.0856 | 7230.3029 | 7176.6231 |
| 2.3794 | 7766.1799 | 7167.2351 | 7109.8096 |
| 2.3904 | 7772.5772 | 7104.6051 | 7042.9962 |
| 2.4014 | 7746.2389 | 7042.5051 | 6976.1827 |
| 2.4124 | 7584.2419 | 6981.0595 | 6909.3693 |
| 2.4234 | 7455.7552 | 6920.4370 | 6842.5558 |
| 2.4344 | 7509.5649 | 6860.8661 | 6775.7424 |
| 2.4454 | 7580.4110 | 6802.6542 | 6708.9289 |
| 2.4564 | 7428.2448 | 6746.2089 | 6642.1155 |
| 2.4674 | 7392.3658 | 6692.0605 | 6575.3020 |
| 2.4784 | 7432.6731 | 6640.8825 | 6508.4886 |
| 2.4894 | 7334.6342 | 6593.5058 | 6441.6752 |
| 2.5004 | 7297.2920 | 6550.9221 | 6374.8617 |
| 2.5114 | 7226.0570 | 6514.2700 | 6308.0483 |
| 2.5224 | 7193.3260 | 6484.7985 | 6241.2348 |
| 2.5334 | 7168.3628 | 6463.8029 | 6174.4214 |
| 2.5444 | 7145.2611 | 6452.5328 | 6107.6079 |
| 2.5554 | 7068.1190 | 6452.0715 | 6040.7945 |
| 2.5664 | 7064.4012 | 6463.1161 | 5973.9810 |
| 2.5774 | 6988.9036 | 6486.0523 | 5907.0225 |
| 2.5884 | 6938.7714 | 6520.4480 | 5840.0639 |
| 2.5994 | 6928.7345 | 6565.1860 | 5773.1054 |
| 2.6104 | 6894.6357 | 6618.0017 | 5706.1468 |
| 2.6214 | 6718.8731 | 6675.2946 | 5639.1883 |
| 2.6324 | 6777.4115 | 6731.8500 | 5572.2297 |
| 2.6434 | 6776.2566 | 6780.6605 | 5505.2712 |
| 2.6544 | 6631.1711 | 6813.1239 | 5438.3126 |
| 2.6654 | 6646.2094 | 6819.9757 | 5371.3541 |
| 2.6764 | 6515.7999 | 6792.8064 | 5304.3955 |
| 2.6874 | 6398.7021 | 6726.6177 | 5237.4370 |
| 2.6984 | 6389.6150 | 6621.3437 | 5170.4784 |
| 2.7094 | 6237.2478 | 6481.8130 | 5103.5199 |
| 2.7204 | 6024.0314 | 6316.2235 | 5036.5613 |
| 2.7314 | 5830.9262 | 6133.9171 | 4969.6028 |
| 2.7424 | 5773.7655 | 5943.5700 | 4902.6442 |
| 2.7534 | 5583.4542 | 5752.1498 | 4835.6857 |
| 2.7644 | 5516.4690 | 5565.0950 | 4768.5478 |
| 2.7754 | 5301.0688 | 5385.9029 | 4701.4099 |
| 2.7864 | 5294.9253 | 5216.9939 | 4634.2720 |
| 2.7974 | 5259.1770 | 5059.5960 | 4567.1340 |
| 2.8084 | 4929.1966 | 4914.0842 | 4499.9961 |
| 2.8194 | 4922.0148 | 4780.1774 | 4432.8582 |
| 2.8304 | 4846.6445 | 4657.1163 | 4365.7203 |
| 2.8414 | 4605.5359 | 4543.8259 | 4298.5824 |
| 2.8524 | 4412.0211 | 4439.0602 | 4231.4445 |
| 2.8634 | 4416.3805 | 4341.5232 | 4164.3066 |
| 2.8744 | 4261.6411 | 4249.9625 | 4097.1687 |
| 2.8854 | 4284.5320 | 4163.2346 | 4030.0308 |
| 2.8964 | 4234.2257 | 4080.3416 | 3962.8929 |
| 2.9074 | 3964.8830 | 4000.4464 | 3895.7549 |
| 2.9184 | 3822.3471 | 3922.8699 | 3828.6170 |
| 2.9294 | 3741.6755 | 3847.0768 | 3761.4791 |
| 2.9404 | 3724.9311 | 3791.6435 | 3694.3412 |
| 2.9514 | 3583.0679 | 3729.6375 | 3657.5455 |
| 2.9624 | 3722.2551 | 3687.4496 | 3620.7498 |
| 2.9734 | 3571.7158 | 3645.9212 | 3583.9540 |
| 2.9844 | 3501.3756 | 3604.9267 | 3547.1583 |
| 2.9954 | 3501.1770 | 3564.3728 | 3510.3626 |
| 3.0064 | 3456.6775 | 3524.1893 | 3473.5669 |
| 3.0174 | 3352.9685 | 3484.3225 | 3436.7711 |
| 3.0284 | 3267.1342 | 3444.7301 | 3399.9754 |
| 3.0394 | 3240.5447 | 3405.3781 | 3363.1797 |
| 3.0504 | 3283.6470 | 3366.2388 | 3326.3840 |
| 3.0614 | 3268.4395 | 3327.2885 | 3289.5882 |
| 3.0724 | 3262.8894 | 3288.5075 | 3252.7925 |
| 3.0834 | 3221.8171 | 3249.8785 | 3215.9968 |
| 3.0944 | 3245.0398 | 3211.3864 | 3179.2010 |
| 3.1054 | 3166.4857 | 3173.0180 | 3142.4053 |
| 3.1164 | 3076.0339 | 3134.7619 | 3105.6096 |
| 3.1274 | 3047.9557 | 3107.4509 | 3068.8139 |
| 3.1384 | 3044.3196 | 3075.8733 | 3049.3452 |
| 3.1494 | 3063.1740 | 3055.2236 | 3029.8766 |
| 3.1604 | 3063.8304 | 3034.6512 | 3010.4080 |
| 3.1714 | 3022.0403 | 3014.1496 | 2990.9393 |
| 3.1824 | 2968.5034 | 2993.7130 | 2971.4707 |
| 3.1934 | 2961.2301 | 2973.3360 | 2952.0021 |
| 3.2044 | 2964.7974 | 2953.0141 | 2932.5335 |
| 3.2154 | 2902.8093 | 2932.7428 | 2913.0648 |
| 3.2264 | 2929.5914 | 2912.5183 | 2893.5962 |
| 3.2374 | 2873.0659 | 2892.3370 | 2874.1276 |
| 3.2484 | 2841.8333 | 2872.1958 | 2854.6589 |
| 3.2594 | 2817.7670 | 2852.0918 | 2835.1903 |
| 3.2704 | 2779.4995 | 2832.0223 | 2815.7217 |
| 3.2814 | 2750.7030 | 2811.9849 | 2796.2530 |
| 3.2924 | 2780.5974 | 2791.9773 | 2776.7844 |
| 3.3034 | 2782.6745 | 2771.9977 | 2757.3158 |
| 3.3144 | 2714.2419 | 2754.4391 | 2737.8472 |
| 3.3254 | 2699.5723 | 2735.9420 | 2722.2059 |
| 3.3364 | 2723.8722 | 2719.8627 | 2706.5647 |
| 3.3474 | 2675.0531 | 2703.8047 | 2690.9235 |
| 3.3584 | 2607.6932 | 2687.7666 | 2675.2822 |
| 3.3694 | 2601.2891 | 2671.7473 | 2659.6410 |
| 3.3804 | 2645.0831 | 2655.7455 | 2643.9997 |
| 3.3914 | 2686.7788 | 2639.7603 | 2628.3585 |
| 3.4024 | 2648.5619 | 2623.7906 | 2612.7173 |
| 3.4134 | 2600.9616 | 2607.8356 | 2597.0760 |
| 3.4244 | 2572.0914 | 2591.8944 | 2581.4348 |
| 3.4354 | 2545.4454 | 2575.9662 | 2565.7936 |
| 3.4464 | 2481.4783 | 2560.0504 | 2550.1523 |
| 3.4574 | 2535.0059 | 2544.1462 | 2534.5111 |
| 3.4684 | 2538.2232 | 2528.2530 | 2518.8699 |
| 3.4794 | 2490.2370 | 2512.3702 | 2503.2286 |
| 3.4904 | 2420.6637 | 2496.4973 | 2487.5874 |
| 3.5014 | 2477.9774 | 2480.8297 | 2471.9462 |
| 3.5124 | 2523.0516 | 2465.0922 | 2456.6180 |
| 3.5234 | 2420.9675 | 2449.5590 | 2441.2898 |
| 3.5344 | 2451.8048 | 2434.0339 | 2425.9616 |
| 3.5454 | 2442.6381 | 2418.5164 | 2410.6334 |
| 3.5564 | 2365.4248 | 2403.0062 | 2395.3052 |
| 3.5674 | 2287.1003 | 2387.5028 | 2379.9770 |
| 3.5784 | 2332.3978 | 2372.0061 | 2364.6488 |
| 3.5894 | 2324.5133 | 2356.5156 | 2349.3206 |
| 3.6004 | 2359.0212 | 2341.0312 | 2333.9925 |
| 3.6114 | 2316.1799 | 2325.5524 | 2318.6643 |
| 3.6224 | 2293.1254 | 2310.0791 | 2303.3361 |
| 3.6334 | 2217.2832 | 2294.6111 | 2288.0079 |
| 3.6444 | 2234.2547 | 2279.1480 | 2272.6797 |
| 3.6554 | 2166.7581 | 2263.6897 | 2257.3515 |
| 3.6664 | 2216.3402 | 2248.2360 | 2242.0233 |
| 3.6774 | 2214.8446 | 2232.7867 | 2226.6951 |
| 3.6884 | 2207.7168 | 2220.1420 | 2211.3669 |
| 3.6994 | 2214.1426 | 2206.3755 | 2200.5137 |
| 3.7104 | 2215.0000 | 2195.4132 | 2189.6604 |
| 3.7214 | 2202.1563 | 2184.4547 | 2178.8071 |
| 3.7324 | 2242.8363 | 2173.4998 | 2167.9539 |
| 3.7434 | 2178.1770 | 2162.5483 | 2157.1006 |
| 3.7544 | 2075.7094 | 2151.6001 | 2146.2473 |
| 3.7654 | 2158.9577 | 2140.6551 | 2135.3940 |
| 3.7764 | 2114.0359 | 2129.7131 | 2124.5408 |
| 3.7874 | 2112.0088 | 2118.7742 | 2113.6875 |
| 3.7984 | 2056.2375 | 2107.8381 | 2102.8342 |
| 3.8094 | 2124.3707 | 2096.9047 | 2091.9810 |
| 3.8204 | 2082.6740 | 2085.9741 | 2081.1277 |
| 3.8314 | 2004.8624 | 2075.0460 | 2070.2744 |
| 3.8424 | 2070.5275 | 2064.1204 | 2059.4212 |
| 3.8534 | 2028.4012 | 2053.1972 | 2048.5679 |
| 3.8644 | 2063.5403 | 2042.2763 | 2037.7146 |
| 3.8754 | 2067.7630 | 2031.3577 | 2026.8613 |
| 3.8864 | 2041.1327 | 2020.4413 | 2016.0081 |
| 3.8974 | 2001.2969 | 2009.5271 | 2005.1548 |
| 3.9084 | 1955.4838 | 1998.6149 | 1994.3015 |
| 3.9194 | 1953.1800 | 1987.7047 | 1983.4483 |
| 3.9304 | 2006.7168 | 1976.7964 | 1972.5950 |
| 3.9414 | 2010.9007 | 1965.8901 | 1961.7417 |
| 3.9524 | 1953.2979 | 1954.9856 | 1950.8884 |
| 3.9634 | 1945.6804 | 1944.0829 | 1940.0352 |
| 3.9744 | 1934.2036 | 1933.1820 | 1929.1819 |
| 3.9854 | 1944.3097 | 1922.2829 | 1918.3286 |
| 3.9964 | 1890.9523 | 1911.3853 | 1907.4754 |
| 4.0074 | 1932.9666 | 1900.4895 | 1896.6221 |
| 4.0184 | 1880.7802 | 1889.5952 | 1885.7688 |
| 4.0294 | 1845.2920 | 1878.7026 | 1874.9155 |
| 4.0404 | 1805.1632 | 1867.8115 | 1864.0623 |
| 4.0514 | 1788.0797 | 1856.9219 | 1853.2090 |
| 4.0624 | 1900.6180 | 1847.4436 | 1842.3557 |
| 4.0734 | 1841.7856 | 1837.3999 | 1833.7553 |
| 4.0844 | 1840.5974 | 1828.7676 | 1825.1548 |
| 4.0954 | 1834.4759 | 1820.1366 | 1816.5543 |
| 4.1064 | 1760.2674 | 1811.5071 | 1807.9539 |
| 4.1174 | 1750.6372 | 1802.8790 | 1799.3534 |
| 4.1284 | 1771.2104 | 1794.2522 | 1790.7529 |
| 4.1394 | 1767.6971 | 1785.6268 | 1782.1525 |
| 4.1504 | 1735.7006 | 1777.0028 | 1773.5520 |
| 4.1614 | 1727.6352 | 1768.3801 | 1764.9515 |
| 4.1724 | 1753.9548 | 1759.7588 | 1756.3510 |
| 4.1834 | 1759.4602 | 1751.1388 | 1747.7506 |
| 4.1944 | 1747.8918 | 1742.5202 | 1739.1501 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 2 Etosha18 SS 0-2cm S1 550C | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 11:15:21 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6799 | 1337.93 | 0.1732 | 32.94053 | 100.00 |
| 5.2534 | 108.15 | 0.2598 | 16.80835 | 8.08 |
| 8.7119 | 729.79 | 0.1732 | 10.14182 | 54.55 |
| 10.5198 | 40.26 | 0.5196 | 8.40265 | 3.01 |
| 15.9524 | 425.69 | 0.1515 | 5.55124 | 31.82 |
| 17.6533 | 45.43 | 0.2598 | 5.02001 | 3.40 |
| 18.3285 | 24.08 | 0.3464 | 4.83657 | 1.80 |
| 19.8873 | 23.60 | 0.8659 | 4.46087 | 1.76 |
| 26.2156 | 224.16 | 0.2165 | 3.39662 | 16.75 |
| 27.4623 | 75.76 | 0.2598 | 3.24519 | 5.66 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-017-4317 | 52 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 17 |
| * | 04-011-6233 | 44 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 25 |
| * | 00-042-1339 | 27 | Potassium Magnesium Aluminum Silicate Hydroxide | K Mg3 ( Si3 Al ) O10 ( O H )2 | Phlogopite-2M1 | 20 |
| * | 01-085-9814 | 8 | Silicon Oxide | Si O2 | Zeolite SSZ-70 | 8 |
| * | 04-025-4215 | 17 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 30 |

Anchor Scan Parameters

Dataset Name	2 Etosha18 SS 0-2cm S1 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 2\2 Etosha18 SS 0-2cm S1 550C.xrdml

Sample Identification	2 Etosha18 SS 0-2cm S1 550C

Measurement Start Date/Time	12/7/2023 11:15:21 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes