2 Etosha 18 SS 0-2 cm 400

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	12.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	32.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	5.0

Phase Potassium Sodium Barium Iron Magnesium Manganese Titanium Aluminum Fluoride Silicate Hydroxide

Weight fraction/ %	25.0

Phase Silicon Oxide

Weight fraction/ %	8.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	18.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Magnesium Silicate Hydroxide Hydrate | Potassium Sodium Barium Iron Magnesium Manganese Titanium Aluminum Fluoride Silicate Hydroxide | Silicon Oxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- |
| 2 Etosha18 SS 0-2cm S1 400C | 12.0 | 32.0 | 5.0 | 25.0 | 8.0 | 18.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5922.0000 | 5909.4351 | 5922.0000 |
| 2.0164 | 5881.2581 | 5884.2388 | 5884.2388 |
| 2.0274 | 5900.5251 | 5846.4777 | 5846.4777 |
| 2.0384 | 5844.3968 | 5808.7165 | 5808.7165 |
| 2.0494 | 5896.4789 | 5770.9553 | 5770.9553 |
| 2.0604 | 5690.8491 | 5733.1942 | 5733.1942 |
| 2.0714 | 5660.0649 | 5695.4330 | 5695.4330 |
| 2.0824 | 5682.9887 | 5657.6719 | 5657.6719 |
| 2.0934 | 5635.1691 | 5619.9107 | 5619.9107 |
| 2.1044 | 5485.6858 | 5582.1495 | 5582.1495 |
| 2.1154 | 5462.0619 | 5544.3884 | 5544.3884 |
| 2.1264 | 5540.5944 | 5506.6272 | 5506.6272 |
| 2.1374 | 5507.4690 | 5468.8660 | 5468.8660 |
| 2.1484 | 5352.4110 | 5431.1049 | 5431.1049 |
| 2.1594 | 5443.8348 | 5393.3437 | 5393.3437 |
| 2.1704 | 5330.2006 | 5355.5825 | 5355.5825 |
| 2.1814 | 5302.1888 | 5317.8214 | 5317.8214 |
| 2.1924 | 5350.6436 | 5281.6870 | 5280.0602 |
| 2.2034 | 5175.2655 | 5245.7717 | 5245.7717 |
| 2.2144 | 5189.0664 | 5211.4832 | 5211.4832 |
| 2.2254 | 5074.2242 | 5177.1947 | 5177.1947 |
| 2.2364 | 5117.8053 | 5142.9063 | 5142.9063 |
| 2.2474 | 5044.5673 | 5108.6178 | 5108.6178 |
| 2.2584 | 4885.1057 | 5074.3293 | 5074.3293 |
| 2.2694 | 4873.8643 | 5040.0408 | 5040.0408 |
| 2.2804 | 4899.9326 | 5005.7523 | 5005.7523 |
| 2.2914 | 4930.9764 | 4971.4638 | 4971.4638 |
| 2.3024 | 5012.4159 | 4937.1753 | 4937.1753 |
| 2.3134 | 4962.2665 | 4902.8868 | 4902.8868 |
| 2.3244 | 4939.7822 | 4868.5983 | 4868.5983 |
| 2.3354 | 4886.9528 | 4834.3098 | 4834.3098 |
| 2.3464 | 4766.6145 | 4800.0214 | 4800.0214 |
| 2.3574 | 4723.4602 | 4765.7329 | 4765.7329 |
| 2.3684 | 4709.8879 | 4731.4444 | 4731.4444 |
| 2.3794 | 4702.5969 | 4702.2384 | 4697.1559 |
| 2.3904 | 4697.3850 | 4673.7168 | 4673.7168 |
| 2.4014 | 4661.6460 | 4650.2777 | 4650.2777 |
| 2.4124 | 4564.6013 | 4626.8385 | 4626.8385 |
| 2.4234 | 4512.1613 | 4603.3994 | 4603.3994 |
| 2.4344 | 4560.0664 | 4579.9603 | 4579.9603 |
| 2.4454 | 4562.6421 | 4556.5212 | 4556.5212 |
| 2.4564 | 4498.5673 | 4533.0821 | 4533.0821 |
| 2.4674 | 4466.1976 | 4509.6430 | 4509.6430 |
| 2.4784 | 4451.5895 | 4486.2039 | 4486.2039 |
| 2.4894 | 4484.8968 | 4462.7647 | 4462.7647 |
| 2.5004 | 4441.5487 | 4439.3256 | 4439.3256 |
| 2.5114 | 4416.8427 | 4415.8865 | 4415.8865 |
| 2.5224 | 4345.1971 | 4392.4474 | 4392.4474 |
| 2.5334 | 4325.1269 | 4369.0083 | 4369.0083 |
| 2.5444 | 4325.0349 | 4345.5692 | 4345.5692 |
| 2.5554 | 4284.3235 | 4322.1301 | 4322.1301 |
| 2.5664 | 4344.6991 | 4302.9808 | 4298.6909 |
| 2.5774 | 4251.4208 | 4284.4092 | 4284.4092 |
| 2.5884 | 4275.6682 | 4270.1275 | 4270.1275 |
| 2.5994 | 4297.8053 | 4255.8457 | 4255.8457 |
| 2.6104 | 4208.9911 | 4241.5640 | 4241.5640 |
| 2.6214 | 4196.0256 | 4227.2822 | 4227.2822 |
| 2.6324 | 4186.3835 | 4213.0005 | 4213.0005 |
| 2.6434 | 4206.5152 | 4198.7187 | 4198.7187 |
| 2.6544 | 4173.0393 | 4184.4370 | 4184.4370 |
| 2.6654 | 4052.7551 | 4170.1553 | 4170.1553 |
| 2.6764 | 4095.4740 | 4155.8735 | 4155.8735 |
| 2.6874 | 4097.6145 | 4141.5918 | 4141.5918 |
| 2.6984 | 4198.4071 | 4127.3100 | 4127.3100 |
| 2.7094 | 4108.8594 | 4113.0283 | 4113.0283 |
| 2.7204 | 4179.8594 | 4098.7466 | 4098.7466 |
| 2.7314 | 4140.2920 | 4084.4648 | 4084.4648 |
| 2.7424 | 4027.0034 | 4070.1831 | 4070.1831 |
| 2.7534 | 4056.1475 | 4055.9013 | 4055.9013 |
| 2.7644 | 4087.2021 | 4041.6196 | 4041.6196 |
| 2.7754 | 4132.2979 | 4027.3378 | 4027.3378 |
| 2.7864 | 4049.1155 | 4013.0561 | 4013.0561 |
| 2.7974 | 3906.7964 | 3998.7744 | 3998.7744 |
| 2.8084 | 3974.3412 | 3984.4926 | 3984.4926 |
| 2.8194 | 3937.6136 | 3970.2109 | 3970.2109 |
| 2.8304 | 3917.3289 | 3955.9291 | 3955.9291 |
| 2.8414 | 3831.9292 | 3941.6474 | 3941.6474 |
| 2.8524 | 3984.9971 | 3927.3657 | 3927.3657 |
| 2.8634 | 3977.7021 | 3913.0839 | 3913.0839 |
| 2.8744 | 3868.2488 | 3898.8022 | 3898.8022 |
| 2.8854 | 3847.3009 | 3884.5204 | 3884.5204 |
| 2.8964 | 3788.2611 | 3870.2387 | 3870.2387 |
| 2.9074 | 3894.0324 | 3855.9569 | 3855.9569 |
| 2.9184 | 3773.8948 | 3841.6752 | 3841.6752 |
| 2.9294 | 3864.3127 | 3827.3935 | 3827.3935 |
| 2.9404 | 3816.1922 | 3813.0620 | 3813.1117 |
| 2.9514 | 3852.4493 | 3799.1592 | 3798.7239 |
| 2.9624 | 3684.5856 | 3784.8534 | 3784.3360 |
| 2.9734 | 3774.1426 | 3770.6863 | 3769.9482 |
| 2.9844 | 3790.1927 | 3756.3422 | 3755.5604 |
| 2.9954 | 3814.9469 | 3741.9584 | 3741.1725 |
| 3.0064 | 3763.5261 | 3727.5746 | 3726.7847 |
| 3.0174 | 3752.9380 | 3713.1908 | 3712.3969 |
| 3.0284 | 3697.8451 | 3698.8071 | 3698.0090 |
| 3.0394 | 3661.2734 | 3684.4234 | 3683.6212 |
| 3.0504 | 3725.4852 | 3670.0397 | 3669.2334 |
| 3.0614 | 3698.4248 | 3655.6561 | 3654.8455 |
| 3.0724 | 3644.1106 | 3641.2725 | 3640.4577 |
| 3.0834 | 3682.1150 | 3626.8889 | 3626.0698 |
| 3.0944 | 3638.2876 | 3612.5054 | 3611.6820 |
| 3.1054 | 3633.9656 | 3598.1218 | 3597.2942 |
| 3.1164 | 3568.5880 | 3583.7384 | 3582.9063 |
| 3.1274 | 3603.8436 | 3569.7307 | 3568.5185 |
| 3.1384 | 3506.6411 | 3555.7736 | 3554.9327 |
| 3.1494 | 3550.7374 | 3542.1923 | 3541.3469 |
| 3.1604 | 3446.6106 | 3528.6110 | 3527.7612 |
| 3.1714 | 3503.2920 | 3515.0298 | 3514.1754 |
| 3.1824 | 3444.3874 | 3501.4486 | 3500.5896 |
| 3.1934 | 3450.8584 | 3487.8674 | 3487.0039 |
| 3.2044 | 3409.3451 | 3474.2863 | 3473.4181 |
| 3.2154 | 3433.7355 | 3460.7052 | 3459.8323 |
| 3.2264 | 3453.0738 | 3447.1242 | 3446.2465 |
| 3.2374 | 3500.4041 | 3433.5432 | 3432.6608 |
| 3.2484 | 3424.8889 | 3419.9622 | 3419.0750 |
| 3.2594 | 3355.3717 | 3406.3813 | 3405.4892 |
| 3.2704 | 3374.0777 | 3392.8004 | 3391.9034 |
| 3.2814 | 3402.2665 | 3379.2195 | 3378.3177 |
| 3.2924 | 3361.6681 | 3365.6387 | 3364.7319 |
| 3.3034 | 3369.0207 | 3352.0579 | 3351.1461 |
| 3.3144 | 3372.3913 | 3338.4772 | 3337.5603 |
| 3.3254 | 3293.8318 | 3324.8965 | 3323.9746 |
| 3.3364 | 3294.6962 | 3311.3159 | 3310.3888 |
| 3.3474 | 3377.9695 | 3297.7353 | 3296.8030 |
| 3.3584 | 3339.3952 | 3284.1547 | 3283.2172 |
| 3.3694 | 3247.3196 | 3270.5742 | 3269.6315 |
| 3.3804 | 3255.1101 | 3256.9937 | 3256.0457 |
| 3.3914 | 3346.7434 | 3243.4133 | 3242.4599 |
| 3.4024 | 3337.1720 | 3229.8329 | 3228.8742 |
| 3.4134 | 3234.6873 | 3216.2526 | 3215.2884 |
| 3.4244 | 3199.6844 | 3202.6723 | 3201.7026 |
| 3.4354 | 3153.9774 | 3189.0921 | 3188.1168 |
| 3.4464 | 3160.0482 | 3175.5119 | 3174.5311 |
| 3.4574 | 3186.8673 | 3161.9317 | 3160.9453 |
| 3.4684 | 3191.8083 | 3148.3516 | 3147.3595 |
| 3.4794 | 3115.7129 | 3134.7716 | 3133.7737 |
| 3.4904 | 3124.4248 | 3121.1916 | 3120.1880 |
| 3.5014 | 3137.5683 | 3108.4163 | 3106.6022 |
| 3.5124 | 3065.3481 | 3095.7493 | 3094.7340 |
| 3.5234 | 3050.3156 | 3083.8870 | 3082.8657 |
| 3.5344 | 3092.4228 | 3072.0247 | 3070.9975 |
| 3.5454 | 3036.3667 | 3060.1625 | 3059.1292 |
| 3.5564 | 2990.6740 | 3048.3647 | 3047.2610 |
| 3.5674 | 3027.2291 | 3036.5284 | 3035.3927 |
| 3.5784 | 2998.0580 | 3024.7000 | 3023.5245 |
| 3.5894 | 3090.2478 | 3012.8523 | 3011.6563 |
| 3.6004 | 3042.9975 | 3000.9922 | 2999.7880 |
| 3.6114 | 3025.7670 | 2989.1321 | 2987.9198 |
| 3.6224 | 2902.7551 | 2977.2722 | 2976.0515 |
| 3.6334 | 2929.5162 | 2965.4123 | 2964.1833 |
| 3.6444 | 3004.3525 | 2953.5525 | 2952.3151 |
| 3.6554 | 2960.4749 | 2941.6929 | 2940.4468 |
| 3.6664 | 2983.3820 | 2929.8333 | 2928.5786 |
| 3.6774 | 3042.8309 | 2917.9738 | 2916.7103 |
| 3.6884 | 2995.5265 | 2906.1145 | 2904.8421 |
| 3.6994 | 2863.0049 | 2894.2552 | 2892.9739 |
| 3.7104 | 2914.0733 | 2882.3961 | 2881.1056 |
| 3.7214 | 2898.9823 | 2870.5370 | 2869.2374 |
| 3.7324 | 2903.5079 | 2858.6781 | 2857.3691 |
| 3.7434 | 2865.3786 | 2846.8193 | 2845.5009 |
| 3.7544 | 2858.2286 | 2834.9606 | 2833.6327 |
| 3.7654 | 2804.8387 | 2823.1020 | 2821.7644 |
| 3.7764 | 2777.5496 | 2811.2436 | 2809.8962 |
| 3.7874 | 2820.6106 | 2799.3852 | 2798.0279 |
| 3.7984 | 2803.0103 | 2787.5270 | 2786.1597 |
| 3.8094 | 2806.0000 | 2775.6689 | 2774.2914 |
| 3.8204 | 2804.2625 | 2763.8110 | 2762.4232 |
| 3.8314 | 2747.6687 | 2751.9532 | 2750.5550 |
| 3.8424 | 2829.6342 | 2740.0955 | 2738.6867 |
| 3.8534 | 2731.7670 | 2728.2379 | 2726.8185 |
| 3.8644 | 2710.5265 | 2716.3805 | 2714.9502 |
| 3.8754 | 2676.4268 | 2704.4714 | 2703.0820 |
| 3.8864 | 2754.4425 | 2692.5555 | 2691.1030 |
| 3.8974 | 2766.0767 | 2680.5878 | 2679.1241 |
| 3.9084 | 2692.9169 | 2668.6203 | 2667.1451 |
| 3.9194 | 2707.9380 | 2656.6529 | 2655.1662 |
| 3.9304 | 2625.6042 | 2644.6857 | 2643.1872 |
| 3.9414 | 2600.4858 | 2632.7187 | 2631.2083 |
| 3.9524 | 2673.2404 | 2620.7518 | 2619.2293 |
| 3.9634 | 2604.6657 | 2608.7851 | 2607.2503 |
| 3.9744 | 2559.0059 | 2596.8186 | 2595.2714 |
| 3.9854 | 2596.5929 | 2584.8523 | 2583.2924 |
| 3.9964 | 2573.2783 | 2572.8861 | 2571.3135 |
| 4.0074 | 2610.8338 | 2560.9202 | 2559.3345 |
| 4.0184 | 2573.9646 | 2548.9544 | 2547.3555 |
| 4.0294 | 2586.9833 | 2536.9888 | 2535.3766 |
| 4.0404 | 2510.2247 | 2525.0235 | 2523.3976 |
| 4.0514 | 2496.1682 | 2513.0583 | 2511.4187 |
| 4.0624 | 2521.9897 | 2501.3713 | 2499.4397 |
| 4.0734 | 2485.4179 | 2489.7220 | 2488.0541 |
| 4.0844 | 2489.4469 | 2478.3508 | 2476.6684 |
| 4.0954 | 2520.2242 | 2466.9799 | 2465.2828 |
| 4.1064 | 2558.8077 | 2455.6091 | 2453.8971 |
| 4.1174 | 2485.4012 | 2444.2387 | 2442.5115 |
| 4.1284 | 2456.2974 | 2432.8685 | 2431.1258 |
| 4.1394 | 2403.3904 | 2421.4985 | 2419.7402 |
| 4.1504 | 2399.4410 | 2410.1288 | 2408.3545 |
| 4.1614 | 2442.4985 | 2398.7594 | 2396.9689 |
| 4.1724 | 2466.2134 | 2387.3903 | 2385.5832 |
| 4.1834 | 2419.9646 | 2376.0215 | 2374.1976 |
| 4.1944 | 2381.4307 | 2364.6529 | 2362.8119 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 2 Etosha18 SS 0-2cm S1 400C | 2.0054 | 29.9894 | 0.0110 | 12/5/2023 12:00:08 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.2909 | 95.06 | 0.1732 | 16.68912 | 13.20 |
| 7.2781 | 547.10 | 0.4330 | 12.13632 | 75.97 |
| 8.8013 | 608.99 | 0.1732 | 10.03908 | 84.56 |
| 10.6584 | 41.96 | 0.4330 | 8.29368 | 5.83 |
| 15.8495 | 720.17 | 0.0541 | 5.58704 | 100.00 |
| 17.6705 | 53.49 | 0.2165 | 5.01518 | 7.43 |
| 18.3035 | 65.72 | 0.1299 | 4.84312 | 9.13 |
| 19.7935 | 42.20 | 0.7793 | 4.48178 | 5.86 |
| 23.4352 | 27.05 | 0.2598 | 3.79292 | 3.76 |
| 24.3184 | 49.44 | 0.1299 | 3.65714 | 6.87 |
| 26.0049 | 519.69 | 0.0758 | 3.42367 | 72.16 |
| 26.7775 | 169.42 | 0.1299 | 3.32660 | 23.52 |
| 27.5511 | 89.53 | 0.2165 | 3.23494 | 12.43 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-017-4317 | 24 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 12 |
| * | 04-011-6751 | 63 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 32 |
| * | 01-075-8323 | 24 | Magnesium Silicate Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ) ( H2 O )11.82 | Sepiolite | 5 |
| * | 01-076-2511 | 16 | Potassium Sodium Barium Iron Magnesium Manganese Titanium Aluminum Fluoride Silicate Hydroxide | ( Na0.163 K1.762 Ca0.003 Ba0.072 ) ( Al0.232 Fe1.765 Mg3.703 Mn0.018 Ti0.282 ) ( Si5.305 Al2.695 O21.116 ( O H )2.851 F0.033 ) | Phlogopite-1M | 25 |
| * | 01-085-9814 | 14 | Silicon Oxide | Si O2 | Zeolite SSZ-70 | 8 |
| * | 04-025-4215 | 6 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 18 |

Anchor Scan Parameters

Dataset Name	2 Etosha18 SS 0-2cm S1 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 2\2 Etosha18 SS 0-2cm S1 400C.xrdml

Sample Identification	2 Etosha18 SS 0-2cm S1 400C

Measurement Start Date/Time	12/5/2023 12:00:08 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes