2 Etosha 18 SS 0-2 cm GLYCOLATED

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	14.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	20.0

Phase Potassium Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	20.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	19.0

Phase Silicon Oxide

Weight fraction/ %	17.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	11.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Aluminum Silicate Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Silicon Oxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- |
| 2 Etosha18 SS 0-2cm S1 GLYCOLATED | 14.0 | 20.0 | 20.0 | 19.0 | 17.0 | 11.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5172.0000 | 5167.6845 | 5172.0000 |
| 2.0164 | 5034.4503 | 5144.5139 | 5135.4823 |
| 2.0274 | 5144.5841 | 5108.3445 | 5098.9645 |
| 2.0384 | 4893.7242 | 5072.2008 | 5062.4468 |
| 2.0494 | 4992.2783 | 5036.0862 | 5025.9291 |
| 2.0604 | 5008.8879 | 5000.0047 | 4989.4113 |
| 2.0714 | 4882.4189 | 4963.9606 | 4952.8936 |
| 2.0824 | 4860.5826 | 4927.9593 | 4916.3759 |
| 2.0934 | 4963.4621 | 4892.0067 | 4879.8582 |
| 2.1044 | 4863.9425 | 4856.1096 | 4843.3404 |
| 2.1154 | 4767.4916 | 4820.2760 | 4806.8227 |
| 2.1264 | 4756.6686 | 4784.5147 | 4770.3050 |
| 2.1374 | 4664.2625 | 4748.8358 | 4733.7872 |
| 2.1484 | 4674.8599 | 4713.2504 | 4697.2695 |
| 2.1594 | 4757.1298 | 4677.7709 | 4660.7518 |
| 2.1704 | 4737.9144 | 4642.4111 | 4624.2340 |
| 2.1814 | 4558.1170 | 4607.1859 | 4587.7163 |
| 2.1924 | 4514.5379 | 4576.2092 | 4551.1986 |
| 2.2034 | 4477.0177 | 4548.6964 | 4526.1724 |
| 2.2144 | 4560.1077 | 4525.4676 | 4501.1461 |
| 2.2254 | 4552.1436 | 4502.4442 | 4476.1199 |
| 2.2364 | 4458.4558 | 4479.6457 | 4451.0937 |
| 2.2474 | 4504.6126 | 4457.0921 | 4426.0675 |
| 2.2584 | 4425.5998 | 4434.8034 | 4401.0413 |
| 2.2694 | 4407.9322 | 4412.7990 | 4376.0150 |
| 2.2804 | 4481.9302 | 4391.0974 | 4350.9888 |
| 2.2914 | 4357.9784 | 4369.7159 | 4325.9626 |
| 2.3024 | 4371.7566 | 4348.6696 | 4300.9364 |
| 2.3134 | 4318.6106 | 4327.9712 | 4275.9101 |
| 2.3244 | 4292.1485 | 4307.6302 | 4250.8839 |
| 2.3354 | 4228.3717 | 4287.6524 | 4225.8577 |
| 2.3464 | 4171.4366 | 4268.0390 | 4200.8315 |
| 2.3574 | 4246.7198 | 4248.7861 | 4175.8053 |
| 2.3684 | 4252.3776 | 4229.8839 | 4150.7790 |
| 2.3794 | 4216.1504 | 4211.2835 | 4125.7528 |
| 2.3904 | 4157.3850 | 4192.9675 | 4100.6354 |
| 2.4014 | 4147.7522 | 4174.8971 | 4075.5181 |
| 2.4124 | 4162.2763 | 4157.0631 | 4050.4007 |
| 2.4234 | 4113.0846 | 4139.4135 | 4025.2833 |
| 2.4344 | 4113.6298 | 4121.8845 | 4000.1659 |
| 2.4454 | 4097.0128 | 4104.3994 | 3975.0485 |
| 2.4564 | 4021.1259 | 4086.8680 | 3949.9312 |
| 2.4674 | 3996.2183 | 4069.1853 | 3924.8138 |
| 2.4784 | 3971.2129 | 4051.2325 | 3899.6964 |
| 2.4894 | 3911.6136 | 4032.8775 | 3874.5790 |
| 2.5004 | 3816.1549 | 4013.9779 | 3849.4616 |
| 2.5114 | 3910.6893 | 3994.3862 | 3824.3442 |
| 2.5224 | 3944.3436 | 3973.9561 | 3799.2269 |
| 2.5334 | 3856.9321 | 3952.5515 | 3774.1095 |
| 2.5444 | 3845.6701 | 3930.0564 | 3748.9921 |
| 2.5554 | 3787.3264 | 3906.3838 | 3723.8747 |
| 2.5664 | 3777.4764 | 3881.4845 | 3698.7573 |
| 2.5774 | 3712.3559 | 3855.3509 | 3673.6400 |
| 2.5884 | 3738.2625 | 3828.0186 | 3648.5226 |
| 2.5994 | 3781.9823 | 3799.5622 | 3623.4052 |
| 2.6104 | 3770.4798 | 3770.0889 | 3598.2878 |
| 2.6214 | 3711.6893 | 3739.7293 | 3573.1704 |
| 2.6324 | 3545.0796 | 3708.6270 | 3548.0531 |
| 2.6434 | 3547.4464 | 3676.9303 | 3522.9357 |
| 2.6544 | 3562.1224 | 3644.7838 | 3497.8183 |
| 2.6654 | 3550.6254 | 3612.3236 | 3472.7009 |
| 2.6764 | 3523.2581 | 3579.6735 | 3447.5835 |
| 2.6874 | 3524.1445 | 3546.9431 | 3422.4662 |
| 2.6984 | 3491.3805 | 3514.2276 | 3397.3488 |
| 2.7094 | 3459.7611 | 3481.6082 | 3372.2314 |
| 2.7204 | 3354.1352 | 3449.1529 | 3347.1140 |
| 2.7314 | 3309.5310 | 3416.9178 | 3321.9966 |
| 2.7424 | 3338.7635 | 3384.9478 | 3296.8792 |
| 2.7534 | 3337.6421 | 3353.2459 | 3271.7619 |
| 2.7644 | 3323.2788 | 3321.8450 | 3246.5533 |
| 2.7754 | 3284.0039 | 3290.7576 | 3221.3448 |
| 2.7864 | 3198.5875 | 3260.0282 | 3196.1362 |
| 2.7974 | 3217.9735 | 3229.6627 | 3170.9277 |
| 2.8084 | 3122.4056 | 3199.6613 | 3145.7192 |
| 2.8194 | 3178.3058 | 3170.0198 | 3120.5106 |
| 2.8304 | 3058.7094 | 3140.7299 | 3095.3021 |
| 2.8414 | 3082.5624 | 3111.7800 | 3070.0935 |
| 2.8524 | 2931.6814 | 3083.1556 | 3044.8850 |
| 2.8634 | 3010.2419 | 3054.8403 | 3019.6765 |
| 2.8744 | 3046.0428 | 3026.8157 | 2994.4679 |
| 2.8854 | 2918.1898 | 2999.0628 | 2969.2594 |
| 2.8964 | 2960.8009 | 2971.5618 | 2944.0508 |
| 2.9074 | 3043.2999 | 2944.2925 | 2918.8423 |
| 2.9184 | 2952.4198 | 2917.2354 | 2893.6338 |
| 2.9294 | 2829.2389 | 2890.3710 | 2868.4252 |
| 2.9404 | 2893.0472 | 2863.6406 | 2843.2167 |
| 2.9514 | 2826.4641 | 2837.0345 | 2817.8955 |
| 2.9624 | 2767.2375 | 2810.5283 | 2792.5743 |
| 2.9734 | 2762.0600 | 2784.1468 | 2767.2531 |
| 2.9844 | 2821.2537 | 2757.8759 | 2741.9319 |
| 2.9954 | 2828.5575 | 2731.7028 | 2716.6107 |
| 3.0064 | 2711.6210 | 2705.6158 | 2691.2895 |
| 3.0174 | 2725.0757 | 2679.6046 | 2665.9683 |
| 3.0284 | 2603.3112 | 2653.6599 | 2640.6471 |
| 3.0394 | 2681.2104 | 2627.7735 | 2615.3259 |
| 3.0504 | 2551.8973 | 2601.9382 | 2590.0047 |
| 3.0614 | 2605.2802 | 2576.1477 | 2564.6835 |
| 3.0724 | 2604.3068 | 2550.3966 | 2539.3623 |
| 3.0834 | 2597.6381 | 2524.6802 | 2514.0411 |
| 3.0944 | 2539.8540 | 2498.9943 | 2488.7199 |
| 3.1054 | 2524.1140 | 2473.3355 | 2463.3987 |
| 3.1164 | 2404.3451 | 2447.7007 | 2438.0775 |
| 3.1274 | 2421.2979 | 2426.0313 | 2412.7563 |
| 3.1384 | 2408.6578 | 2407.5533 | 2398.4951 |
| 3.1494 | 2350.0610 | 2393.0366 | 2384.2339 |
| 3.1604 | 2383.2788 | 2378.5356 | 2369.9726 |
| 3.1714 | 2422.8918 | 2364.0489 | 2355.7114 |
| 3.1824 | 2372.3151 | 2349.5753 | 2341.4501 |
| 3.1934 | 2376.2743 | 2335.1138 | 2327.1889 |
| 3.2044 | 2349.3672 | 2320.6634 | 2312.9276 |
| 3.2154 | 2319.9056 | 2306.2233 | 2298.6664 |
| 3.2264 | 2344.8333 | 2291.7928 | 2284.4051 |
| 3.2374 | 2274.1298 | 2277.3714 | 2270.1439 |
| 3.2484 | 2233.2222 | 2262.9583 | 2255.8826 |
| 3.2594 | 2205.3157 | 2248.5531 | 2241.6214 |
| 3.2704 | 2290.0487 | 2234.1554 | 2227.3602 |
| 3.2814 | 2314.6529 | 2219.7647 | 2213.0989 |
| 3.2924 | 2237.1106 | 2205.3807 | 2198.8377 |
| 3.3034 | 2221.5979 | 2191.0029 | 2184.5764 |
| 3.3144 | 2189.7433 | 2178.6523 | 2170.3152 |
| 3.3254 | 2075.8732 | 2166.7028 | 2160.4915 |
| 3.3364 | 2132.3624 | 2156.7797 | 2150.6679 |
| 3.3474 | 2160.5172 | 2146.8619 | 2140.8442 |
| 3.3584 | 2129.1814 | 2136.9490 | 2131.0206 |
| 3.3694 | 2114.9518 | 2127.0408 | 2121.1969 |
| 3.3804 | 2117.7547 | 2117.1371 | 2111.3733 |
| 3.3914 | 2114.4159 | 2107.2378 | 2101.5496 |
| 3.4024 | 2086.5614 | 2097.3426 | 2091.7259 |
| 3.4134 | 2064.4140 | 2087.4514 | 2081.9023 |
| 3.4244 | 2051.0457 | 2077.5640 | 2072.0786 |
| 3.4354 | 2041.6087 | 2067.6803 | 2062.2550 |
| 3.4464 | 2065.0153 | 2057.8002 | 2052.4313 |
| 3.4574 | 2063.5723 | 2047.9235 | 2042.6077 |
| 3.4684 | 2025.0728 | 2038.0501 | 2032.7840 |
| 3.4794 | 2022.5870 | 2028.1799 | 2022.9604 |
| 3.4904 | 2047.8009 | 2018.3129 | 2013.1367 |
| 3.5014 | 2032.1514 | 2008.4488 | 2003.3131 |
| 3.5124 | 2011.7935 | 1998.5877 | 1993.4894 |
| 3.5234 | 1987.8112 | 1988.7294 | 1983.6658 |
| 3.5344 | 1915.2389 | 1978.8739 | 1973.8421 |
| 3.5454 | 1881.7925 | 1969.0210 | 1964.0185 |
| 3.5564 | 1882.6652 | 1959.1708 | 1954.1948 |
| 3.5674 | 1902.6332 | 1949.3232 | 1944.3712 |
| 3.5784 | 1905.9695 | 1939.4780 | 1934.5475 |
| 3.5894 | 1909.6195 | 1929.6354 | 1924.7238 |
| 3.6004 | 1907.0890 | 1919.7951 | 1914.9002 |
| 3.6114 | 1880.5762 | 1909.9572 | 1905.0765 |
| 3.6224 | 1895.7832 | 1900.1217 | 1895.2529 |
| 3.6334 | 1856.7699 | 1890.2884 | 1885.4292 |
| 3.6444 | 1832.0354 | 1880.4575 | 1875.6056 |
| 3.6554 | 1869.4956 | 1870.6287 | 1865.7819 |
| 3.6664 | 1841.0501 | 1860.8022 | 1855.9583 |
| 3.6774 | 1855.8378 | 1850.9779 | 1846.1346 |
| 3.6884 | 1827.3009 | 1841.5577 | 1836.3110 |
| 3.6994 | 1816.7502 | 1832.2182 | 1827.3698 |
| 3.7104 | 1849.4892 | 1823.2829 | 1818.4286 |
| 3.7214 | 1800.7079 | 1814.3497 | 1809.4874 |
| 3.7324 | 1802.5079 | 1805.4187 | 1800.5462 |
| 3.7434 | 1846.3314 | 1796.4898 | 1791.6050 |
| 3.7544 | 1714.4469 | 1787.5630 | 1782.6638 |
| 3.7654 | 1785.3255 | 1778.6384 | 1773.7226 |
| 3.7764 | 1794.8520 | 1769.7160 | 1764.7814 |
| 3.7874 | 1793.0177 | 1760.7957 | 1755.8402 |
| 3.7984 | 1689.1239 | 1751.8777 | 1746.8990 |
| 3.8094 | 1725.2203 | 1742.9618 | 1737.9578 |
| 3.8204 | 1739.3083 | 1734.0482 | 1729.0166 |
| 3.8314 | 1749.3550 | 1725.1368 | 1720.0755 |
| 3.8424 | 1733.0531 | 1716.2278 | 1711.1343 |
| 3.8534 | 1713.5988 | 1707.3210 | 1702.1931 |
| 3.8644 | 1674.9862 | 1698.4166 | 1693.2519 |
| 3.8754 | 1633.8899 | 1691.8359 | 1684.3107 |
| 3.8864 | 1710.5133 | 1685.7119 | 1680.4665 |
| 3.8974 | 1757.9626 | 1681.9118 | 1676.6222 |
| 3.9084 | 1685.5595 | 1678.1141 | 1672.7780 |
| 3.9194 | 1717.3451 | 1674.3191 | 1668.9338 |
| 3.9304 | 1671.0192 | 1670.5266 | 1665.0896 |
| 3.9414 | 1649.6922 | 1666.7369 | 1661.2454 |
| 3.9524 | 1681.1917 | 1662.9499 | 1657.4011 |
| 3.9634 | 1643.7728 | 1659.1658 | 1653.5569 |
| 3.9744 | 1555.8083 | 1655.3845 | 1649.7127 |
| 3.9854 | 1628.3097 | 1651.6062 | 1645.8685 |
| 3.9964 | 1656.5379 | 1647.8310 | 1642.0243 |
| 4.0074 | 1657.0894 | 1644.0589 | 1638.1801 |
| 4.0184 | 1579.2050 | 1640.2901 | 1634.3358 |
| 4.0294 | 1621.3382 | 1636.5247 | 1630.4916 |
| 4.0404 | 1612.6431 | 1632.7627 | 1626.6474 |
| 4.0514 | 1625.2979 | 1629.0043 | 1622.8032 |
| 4.0624 | 1654.6544 | 1625.2070 | 1618.9590 |
| 4.0734 | 1661.0177 | 1621.4052 | 1615.0213 |
| 4.0844 | 1626.4469 | 1617.5648 | 1611.0836 |
| 4.0954 | 1624.0295 | 1613.7285 | 1607.1459 |
| 4.1064 | 1629.1337 | 1609.8965 | 1603.2082 |
| 4.1174 | 1607.4041 | 1606.0689 | 1599.2706 |
| 4.1284 | 1589.0939 | 1602.2459 | 1595.3329 |
| 4.1394 | 1575.6234 | 1598.4278 | 1591.3952 |
| 4.1504 | 1567.5988 | 1594.6146 | 1587.4575 |
| 4.1614 | 1603.3638 | 1590.8067 | 1583.5198 |
| 4.1724 | 1582.0398 | 1587.0042 | 1579.5822 |
| 4.1834 | 1556.8673 | 1583.2075 | 1575.6445 |
| 4.1944 | 1570.9317 | 1579.4167 | 1571.7068 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 2 Etosha18 SS 0-2cm S1 GLYCOLATED | 2.0054 | 29.9894 | 0.0110 | 12/1/2023 9:37:13 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.5607 | 162.43 | 0.3464 | 34.47410 | 17.62 |
| 5.0377 | 193.03 | 0.4330 | 17.52746 | 20.94 |
| 7.0664 | 921.87 | 0.1948 | 12.49936 | 100.00 |
| 8.7007 | 410.07 | 0.1299 | 10.15492 | 44.48 |
| 15.7226 | 669.74 | 0.0541 | 5.63186 | 72.65 |
| 17.6320 | 40.79 | 0.2598 | 5.02603 | 4.42 |
| 18.1882 | 111.63 | 0.0758 | 4.87356 | 12.11 |
| 19.7630 | 64.68 | 0.6927 | 4.48864 | 7.02 |
| 25.8740 | 634.14 | 0.0758 | 3.44068 | 68.79 |
| 26.7701 | 111.85 | 0.1732 | 3.32751 | 12.13 |
| 27.4657 | 55.21 | 0.1299 | 3.24480 | 5.99 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-017-4317 | 28 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 14 |
| * | 01-072-4625 | 42 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 20 |
| * | 00-042-1339 | 20 | Potassium Magnesium Aluminum Silicate Hydroxide | K Mg3 ( Si3 Al ) O10 ( O H )2 | Phlogopite-2M1 | 20 |
| * | 01-082-8023 | 20 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 19 |
| * | 01-085-9814 | 8 | Silicon Oxide | Si O2 | Zeolite SSZ-70 | 17 |
| * | 04-025-4215 | 9 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 11 |

Anchor Scan Parameters

Dataset Name	2 Etosha18 SS 0-2cm S1 GLYCOLATED

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 2\2 Etosha18 SS 0-2cm S1 GLYCOLATED.xrdml

Sample Identification	2 Etosha18 SS 0-2cm S1 GLYCOLATED

Measurement Start Date/Time	12/1/2023 9:37:13 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes