20 Etosha 22 HS crt 0-0.1 cm S4 400C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	13.0

Phase Tin Oxide

Weight fraction/ %	2.0

Phase Titanium Oxide

Weight fraction/ %	6.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	15.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	10.0

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	11.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	43.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Tin Oxide | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Silicate Hydroxide Hydrate | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 20 Etosha22 HS crt 0-0.1cm S4 400C | 13.0 | 2.0 | 6.0 | 15.0 | 10.0 | 11.0 | 43.0 | 0.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8983.0000 | 8994.1122 | 8983.0000 |
| 2.0164 | 8718.4882 | 8936.9518 | 8916.2431 |
| 2.0274 | 8597.2950 | 8870.8541 | 8849.4862 |
| 2.0384 | 8610.4381 | 8804.7880 | 8782.7292 |
| 2.0494 | 8634.6273 | 8738.7557 | 8715.9723 |
| 2.0604 | 8385.2797 | 8672.7594 | 8649.2154 |
| 2.0714 | 8505.6136 | 8606.8014 | 8582.4585 |
| 2.0824 | 8264.2738 | 8540.8844 | 8515.7016 |
| 2.0934 | 8528.2380 | 8475.0111 | 8448.9447 |
| 2.1044 | 8290.6726 | 8409.1846 | 8382.1877 |
| 2.1154 | 8279.6313 | 8343.4083 | 8315.4308 |
| 2.1264 | 8264.5615 | 8277.6858 | 8248.6739 |
| 2.1374 | 8217.4484 | 8212.0210 | 8181.9170 |
| 2.1484 | 8374.9607 | 8146.4183 | 8115.1601 |
| 2.1594 | 8166.2379 | 8080.8823 | 8048.4031 |
| 2.1704 | 7977.8628 | 8015.4183 | 7981.6462 |
| 2.1814 | 8173.0826 | 7950.0320 | 7914.8893 |
| 2.1924 | 7978.3427 | 7884.7092 | 7848.1324 |
| 2.2034 | 8035.5929 | 7819.3660 | 7781.2235 |
| 2.2144 | 7963.4975 | 7754.1008 | 7714.3145 |
| 2.2254 | 7823.7542 | 7688.9426 | 7647.4056 |
| 2.2364 | 7790.2198 | 7623.9007 | 7580.4967 |
| 2.2474 | 7720.3363 | 7558.9857 | 7513.5877 |
| 2.2584 | 7787.4135 | 7494.2095 | 7446.6788 |
| 2.2694 | 7746.7522 | 7429.5856 | 7379.7699 |
| 2.2804 | 7684.6332 | 7365.1296 | 7312.8610 |
| 2.2914 | 7739.2193 | 7300.8593 | 7245.9520 |
| 2.3024 | 7681.1770 | 7236.7960 | 7179.0431 |
| 2.3134 | 7710.7021 | 7172.9651 | 7112.1342 |
| 2.3244 | 7634.4951 | 7109.3971 | 7045.2252 |
| 2.3354 | 7606.1829 | 7046.1301 | 6978.3163 |
| 2.3464 | 7584.2920 | 6983.2112 | 6911.4074 |
| 2.3574 | 7554.2576 | 6920.7003 | 6844.4985 |
| 2.3684 | 7360.3481 | 6858.6734 | 6777.5895 |
| 2.3794 | 7290.4769 | 6797.2275 | 6710.6806 |
| 2.3904 | 7295.3397 | 6736.4866 | 6643.7717 |
| 2.4014 | 7324.1770 | 6676.6084 | 6576.8627 |
| 2.4124 | 7379.9902 | 6617.7922 | 6509.9538 |
| 2.4234 | 7416.2507 | 6560.2873 | 6443.0449 |
| 2.4344 | 7316.2684 | 6504.4013 | 6376.1360 |
| 2.4454 | 7146.2743 | 6450.5084 | 6309.2270 |
| 2.4564 | 7165.0393 | 6399.0554 | 6242.3181 |
| 2.4674 | 7175.1622 | 6350.5656 | 6175.4092 |
| 2.4784 | 7093.3235 | 6305.6378 | 6108.5002 |
| 2.4894 | 6948.9400 | 6264.9402 | 6041.5913 |
| 2.5004 | 6941.2257 | 6229.1970 | 5974.6824 |
| 2.5114 | 6996.2655 | 6199.1670 | 5907.7735 |
| 2.5224 | 6978.5383 | 6175.6135 | 5840.8645 |
| 2.5334 | 6909.2124 | 6159.2649 | 5773.9556 |
| 2.5444 | 6857.9322 | 6150.7679 | 5707.0467 |
| 2.5554 | 6837.3963 | 6150.6334 | 5640.1377 |
| 2.5664 | 6770.5693 | 6159.1563 | 5573.2288 |
| 2.5774 | 6702.6824 | 6176.3012 | 5506.1679 |
| 2.5884 | 6664.1544 | 6201.8864 | 5439.1069 |
| 2.5994 | 6722.6903 | 6235.2575 | 5372.0460 |
| 2.6104 | 6697.8353 | 6275.2538 | 5304.9851 |
| 2.6214 | 6641.4680 | 6320.1330 | 5237.9241 |
| 2.6324 | 6544.9292 | 6367.4622 | 5170.8632 |
| 2.6434 | 6502.5841 | 6414.0107 | 5103.8023 |
| 2.6544 | 6445.6121 | 6455.6803 | 5036.7413 |
| 2.6654 | 6363.0531 | 6487.5455 | 4969.6804 |
| 2.6764 | 6429.4710 | 6504.1014 | 4902.6194 |
| 2.6874 | 6381.2714 | 6499.8002 | 4835.5585 |
| 2.6984 | 6216.8451 | 6469.8625 | 4768.4976 |
| 2.7094 | 6109.1367 | 6411.1862 | 4701.4366 |
| 2.7204 | 6025.4887 | 6323.0376 | 4634.3757 |
| 2.7314 | 5764.8259 | 6207.2271 | 4567.3147 |
| 2.7424 | 5580.3574 | 6067.6878 | 4500.2538 |
| 2.7534 | 5575.5664 | 5909.5773 | 4433.1929 |
| 2.7644 | 5186.4896 | 5738.5401 | 4365.9440 |
| 2.7754 | 5056.6342 | 5559.8592 | 4298.6952 |
| 2.7864 | 4991.1495 | 5378.1907 | 4231.4464 |
| 2.7974 | 4791.8495 | 5197.2540 | 4164.1975 |
| 2.8084 | 4670.9946 | 5019.9210 | 4096.9487 |
| 2.8194 | 4522.6598 | 4848.3100 | 4029.6999 |
| 2.8304 | 4296.0575 | 4683.8973 | 3962.4510 |
| 2.8414 | 4099.5831 | 4527.6204 | 3895.2022 |
| 2.8524 | 4040.6259 | 4379.9694 | 3827.9534 |
| 2.8634 | 3852.0118 | 4241.0651 | 3760.7045 |
| 2.8744 | 3876.0428 | 4110.7307 | 3693.4557 |
| 2.8854 | 3671.4936 | 3988.5579 | 3626.2069 |
| 2.8964 | 3537.5796 | 3873.9698 | 3558.9580 |
| 2.9074 | 3553.6539 | 3766.2774 | 3491.7092 |
| 2.9184 | 3506.8353 | 3664.7317 | 3424.4604 |
| 2.9294 | 3347.5162 | 3568.5669 | 3357.2116 |
| 2.9404 | 3189.0108 | 3498.7999 | 3289.9627 |
| 2.9514 | 3291.8938 | 3421.2749 | 3254.5521 |
| 2.9624 | 3222.6829 | 3368.8062 | 3219.1414 |
| 2.9734 | 3194.0639 | 3319.0634 | 3183.7307 |
| 2.9844 | 3078.5123 | 3271.5566 | 3148.3201 |
| 2.9954 | 3144.5221 | 3225.8712 | 3112.9094 |
| 3.0064 | 3072.4641 | 3181.6629 | 3077.4987 |
| 3.0174 | 2933.2379 | 3138.6504 | 3042.0881 |
| 3.0284 | 2879.4351 | 3096.6074 | 3006.6774 |
| 3.0394 | 2896.2124 | 3055.3536 | 2971.2667 |
| 3.0504 | 2841.9941 | 3014.7470 | 2935.8561 |
| 3.0614 | 2838.0796 | 2974.6761 | 2900.4454 |
| 3.0724 | 2841.6544 | 2935.0537 | 2865.0348 |
| 3.0834 | 2819.0246 | 2895.8113 | 2829.6241 |
| 3.0944 | 2759.7212 | 2856.8952 | 2794.2134 |
| 3.1054 | 2757.4238 | 2818.2624 | 2758.8028 |
| 3.1164 | 2663.4135 | 2779.8785 | 2723.3921 |
| 3.1274 | 2676.9056 | 2755.0079 | 2687.9814 |
| 3.1384 | 2730.2743 | 2723.1950 | 2672.0165 |
| 3.1494 | 2636.2517 | 2704.8523 | 2656.0515 |
| 3.1604 | 2627.3466 | 2686.6704 | 2640.0865 |
| 3.1714 | 2662.0521 | 2668.7307 | 2624.1216 |
| 3.1824 | 2588.9754 | 2650.8806 | 2608.1566 |
| 3.1934 | 2608.7788 | 2633.1037 | 2592.1917 |
| 3.2044 | 2578.6740 | 2615.4373 | 2576.2267 |
| 3.2154 | 2563.3048 | 2597.8740 | 2560.2617 |
| 3.2264 | 2541.2610 | 2580.4058 | 2544.2968 |
| 3.2374 | 2468.1023 | 2563.0253 | 2528.3318 |
| 3.2484 | 2522.0000 | 2545.7260 | 2512.3668 |
| 3.2594 | 2512.7079 | 2528.5018 | 2496.4019 |
| 3.2704 | 2462.2788 | 2511.3473 | 2480.4369 |
| 3.2814 | 2458.7030 | 2494.2575 | 2464.4719 |
| 3.2924 | 2458.8097 | 2477.2278 | 2448.5070 |
| 3.3034 | 2433.9331 | 2460.2541 | 2432.5420 |
| 3.3144 | 2436.6087 | 2443.3326 | 2416.5771 |
| 3.3254 | 2421.6076 | 2426.4599 | 2400.6121 |
| 3.3364 | 2350.9218 | 2409.6326 | 2384.6471 |
| 3.3474 | 2347.9862 | 2392.8478 | 2368.6822 |
| 3.3584 | 2306.2138 | 2376.1029 | 2352.7172 |
| 3.3694 | 2261.3855 | 2359.3953 | 2336.7522 |
| 3.3804 | 2266.8545 | 2342.7227 | 2320.7873 |
| 3.3914 | 2235.3717 | 2326.0829 | 2304.8223 |
| 3.4024 | 2215.4877 | 2309.4741 | 2288.8574 |
| 3.4134 | 2256.2616 | 2292.8943 | 2272.8924 |
| 3.4244 | 2230.1298 | 2276.3419 | 2256.9274 |
| 3.4354 | 2214.1200 | 2259.8152 | 2240.9625 |
| 3.4464 | 2241.2026 | 2243.3129 | 2224.9975 |
| 3.4574 | 2247.7552 | 2226.8335 | 2209.0325 |
| 3.4684 | 2227.9587 | 2210.3758 | 2193.0676 |
| 3.4794 | 2202.7660 | 2193.9386 | 2177.1026 |
| 3.4904 | 2198.2965 | 2177.5208 | 2161.1376 |
| 3.5014 | 2152.9892 | 2165.1553 | 2145.1727 |
| 3.5124 | 2085.5482 | 2150.6406 | 2135.1089 |
| 3.5234 | 2091.4543 | 2140.1762 | 2125.0451 |
| 3.5344 | 2119.2945 | 2129.7275 | 2114.9813 |
| 3.5454 | 2119.5133 | 2119.2937 | 2104.9175 |
| 3.5564 | 2086.2124 | 2108.8740 | 2094.8538 |
| 3.5674 | 2083.9440 | 2098.4677 | 2084.7900 |
| 3.5784 | 2113.5167 | 2088.0743 | 2074.7262 |
| 3.5894 | 1997.2743 | 2077.6929 | 2064.6624 |
| 3.6004 | 2078.1126 | 2067.3232 | 2054.5986 |
| 3.6114 | 2091.9321 | 2056.9645 | 2044.5348 |
| 3.6224 | 2132.9867 | 2046.6163 | 2034.4711 |
| 3.6334 | 2017.0432 | 2036.2782 | 2024.4073 |
| 3.6444 | 1993.9882 | 2025.9497 | 2014.3435 |
| 3.6554 | 1899.6666 | 2015.6304 | 2004.2797 |
| 3.6664 | 1978.7223 | 2005.3198 | 1994.2159 |
| 3.6774 | 1969.8210 | 1995.0176 | 1984.1521 |
| 3.6884 | 2007.3850 | 1985.7787 | 1974.0883 |
| 3.6994 | 1946.9311 | 1975.9806 | 1965.5683 |
| 3.7104 | 1946.2409 | 1967.2452 | 1957.0483 |
| 3.7214 | 1960.7611 | 1958.5168 | 1948.5282 |
| 3.7324 | 1869.0305 | 1949.7952 | 1940.0082 |
| 3.7434 | 1891.2016 | 1941.0801 | 1931.4881 |
| 3.7544 | 1850.0575 | 1932.3712 | 1922.9681 |
| 3.7654 | 1851.8663 | 1923.6683 | 1914.4481 |
| 3.7764 | 1896.0487 | 1914.9711 | 1905.9280 |
| 3.7874 | 1792.9292 | 1906.2794 | 1897.4080 |
| 3.7984 | 1859.9484 | 1897.5930 | 1888.8879 |
| 3.8094 | 1846.1642 | 1888.9117 | 1880.3679 |
| 3.8204 | 1918.2714 | 1880.2353 | 1871.8479 |
| 3.8314 | 1889.2507 | 1871.5637 | 1863.3278 |
| 3.8424 | 1802.3673 | 1862.8966 | 1854.8078 |
| 3.8534 | 1842.0147 | 1854.2339 | 1846.2877 |
| 3.8644 | 1802.3191 | 1845.5755 | 1837.7677 |
| 3.8754 | 1850.6795 | 1836.9211 | 1829.2476 |
| 3.8864 | 1924.8539 | 1828.2706 | 1820.7276 |
| 3.8974 | 1804.7906 | 1819.6240 | 1812.2076 |
| 3.9084 | 1829.4911 | 1810.9810 | 1803.6875 |
| 3.9194 | 1750.0708 | 1802.3416 | 1795.1675 |
| 3.9304 | 1785.8495 | 1793.7057 | 1786.6474 |
| 3.9414 | 1744.0806 | 1785.0730 | 1778.1274 |
| 3.9524 | 1751.6607 | 1776.4436 | 1769.6074 |
| 3.9634 | 1694.6342 | 1767.8173 | 1761.0873 |
| 3.9744 | 1718.7999 | 1759.1940 | 1752.5673 |
| 3.9854 | 1724.1593 | 1750.5736 | 1744.0472 |
| 3.9964 | 1733.9685 | 1741.9560 | 1735.5272 |
| 4.0074 | 1695.8722 | 1733.3412 | 1727.0071 |
| 4.0184 | 1701.0501 | 1724.7291 | 1718.4871 |
| 4.0294 | 1666.7395 | 1716.1196 | 1709.9671 |
| 4.0404 | 1710.7139 | 1707.5126 | 1701.4470 |
| 4.0514 | 1700.5693 | 1698.9080 | 1692.9270 |
| 4.0624 | 1677.9007 | 1691.6528 | 1684.4069 |
| 4.0734 | 1655.6824 | 1683.6765 | 1677.8574 |
| 4.0844 | 1698.5708 | 1677.0494 | 1671.3079 |
| 4.0954 | 1664.5585 | 1670.4245 | 1664.7584 |
| 4.1064 | 1643.9892 | 1663.8018 | 1658.2088 |
| 4.1174 | 1661.0442 | 1657.1811 | 1651.6593 |
| 4.1284 | 1627.9513 | 1650.5625 | 1645.1098 |
| 4.1394 | 1627.9164 | 1643.9459 | 1638.5603 |
| 4.1504 | 1628.0206 | 1637.3313 | 1632.0108 |
| 4.1614 | 1585.7729 | 1630.7185 | 1625.4612 |
| 4.1724 | 1591.5841 | 1624.1077 | 1618.9117 |
| 4.1834 | 1641.8938 | 1617.4986 | 1612.3622 |
| 4.1944 | 1648.5162 | 1610.8914 | 1605.8127 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 20 Etosha22 HS crt 0-0.1cm S4 400C | 2.0054 | 29.9894 | 0.0110 | 12/12/2023 12:27:50 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7048 | 1527.99 | 0.2165 | 32.63755 | 100.00 |
| 5.3322 | 105.19 | 0.2165 | 16.56018 | 6.88 |
| 6.9753 | 1073.96 | 0.2165 | 12.66243 | 70.29 |
| 7.1716 | 988.95 | 0.2165 | 12.31628 | 64.72 |
| 8.6882 | 704.69 | 0.1299 | 10.16942 | 46.12 |
| 13.1877 | 13.54 | 0.5196 | 6.70815 | 0.89 |
| 15.7667 | 546.17 | 0.0974 | 5.61618 | 35.74 |
| 17.5881 | 43.67 | 0.3464 | 5.03849 | 2.86 |
| 18.2617 | 50.91 | 0.1515 | 4.85413 | 3.33 |
| 19.5618 | 36.95 | 0.3464 | 4.53434 | 2.42 |
| 24.2025 | 24.71 | 0.2598 | 3.67439 | 1.62 |
| 25.9332 | 347.42 | 0.1515 | 3.43297 | 22.74 |
| 26.6771 | 192.79 | 0.2165 | 3.33890 | 12.62 |
| 27.4906 | 222.18 | 0.1515 | 3.24192 | 14.54 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-072-4625 | 53 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 13 |
| * | 01-070-4177 | 47 | Tin Oxide | Sn O2 | Cassiterite | 2 |
| * | 04-008-7810 | 45 | Titanium Oxide | Ti O2 | Rutile | 6 |
| * | 04-017-4317 | 32 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 15 |
| * | 01-080-5019 | 20 | Magnesium Silicate Hydroxide Hydrate | Mg7.68 ( Si12 O30 ) ( O H )4 ( H2 O )4 ( H2 O )6 | Sepiolite | 10 |
| * | 04-016-6876 | 33 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 11 |
| * | 04-025-4215 | 24 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 43 |
| * | 04-017-7291 | No Matching Lines | Sodium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Na0.930 Mg2.810 Fe0.065 Al1.185 Si2.895 O10 ( O H )2 ( H2 O )3 | Vermiculite | - |

Anchor Scan Parameters

Dataset Name	20 Etosha22 HS crt 0-0.1cm S4 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 20\20 Etosha22 HS crt 0-0.1cm S4 400C.xrdml

Sample Identification	20 Etosha22 HS crt 0-0.1cm S4 400C

Measurement Start Date/Time	12/12/2023 12:27:50 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes