20 Etosha 22 HS crt 0-0.1 cm S4 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	4.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	14.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	14.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	34.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	34.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- |
| 20 Etosha22 HS crt 0-0.1cm S4 550C | 4.0 | 14.0 | 14.0 | 34.0 | 34.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 9004.0000 | 9013.4080 | 9004.0000 |
| 2.0164 | 8671.2906 | 8972.2173 | 8936.8692 |
| 2.0274 | 8774.6804 | 8906.2520 | 8869.7384 |
| 2.0384 | 8752.7817 | 8840.3444 | 8802.6076 |
| 2.0494 | 8515.0482 | 8774.4985 | 8735.4768 |
| 2.0604 | 8571.6647 | 8708.7183 | 8668.3460 |
| 2.0714 | 8530.2478 | 8643.0084 | 8601.2152 |
| 2.0824 | 8455.1608 | 8577.3737 | 8534.0843 |
| 2.0934 | 8410.2507 | 8511.8195 | 8466.9535 |
| 2.1044 | 8281.1947 | 8446.3518 | 8399.8227 |
| 2.1154 | 8317.2340 | 8380.9768 | 8332.6919 |
| 2.1264 | 8217.3776 | 8315.7018 | 8265.5611 |
| 2.1374 | 8194.6106 | 8250.5344 | 8198.4303 |
| 2.1484 | 8123.1598 | 8185.4835 | 8131.2995 |
| 2.1594 | 8133.1200 | 8120.5589 | 8064.1687 |
| 2.1704 | 8155.2448 | 8055.7716 | 7997.0379 |
| 2.1814 | 8052.1170 | 7991.1343 | 7929.9071 |
| 2.1924 | 8017.3137 | 7926.6032 | 7862.7763 |
| 2.2034 | 8015.8938 | 7862.2127 | 7795.4879 |
| 2.2144 | 8044.1863 | 7797.9656 | 7728.1995 |
| 2.2254 | 7858.5418 | 7733.9441 | 7660.9111 |
| 2.2364 | 7882.4897 | 7670.1769 | 7593.6227 |
| 2.2474 | 7909.1848 | 7606.6988 | 7526.3344 |
| 2.2584 | 7748.8732 | 7543.5525 | 7459.0460 |
| 2.2694 | 7792.8643 | 7480.7899 | 7391.7576 |
| 2.2804 | 7798.6524 | 7418.4750 | 7324.4692 |
| 2.2914 | 7700.2497 | 7356.6862 | 7257.1808 |
| 2.3024 | 7632.6195 | 7295.5192 | 7189.8924 |
| 2.3134 | 7618.2085 | 7235.0907 | 7122.6041 |
| 2.3244 | 7579.2281 | 7175.5419 | 7055.3157 |
| 2.3354 | 7599.1829 | 7117.0423 | 6988.0273 |
| 2.3464 | 7518.6145 | 7059.7932 | 6920.7389 |
| 2.3574 | 7434.9489 | 7004.0315 | 6853.4505 |
| 2.3684 | 7412.8333 | 6950.0324 | 6786.1621 |
| 2.3794 | 7385.5555 | 6898.1109 | 6718.8738 |
| 2.3904 | 7396.3919 | 6848.6228 | 6651.5854 |
| 2.4014 | 7455.7964 | 6801.9628 | 6584.2970 |
| 2.4124 | 7297.5477 | 6758.5609 | 6517.0086 |
| 2.4234 | 7320.2812 | 6718.8761 | 6449.7202 |
| 2.4344 | 7337.1239 | 6683.3867 | 6382.4318 |
| 2.4454 | 7256.8122 | 6652.5780 | 6315.1435 |
| 2.4564 | 7208.2439 | 6626.9259 | 6247.8551 |
| 2.4674 | 7225.0619 | 6606.8780 | 6180.5667 |
| 2.4784 | 7104.7114 | 6592.8322 | 6113.2783 |
| 2.4894 | 7122.0285 | 6585.1114 | 6045.9899 |
| 2.5004 | 7178.7301 | 6583.9383 | 5978.7015 |
| 2.5114 | 7131.7345 | 6589.4067 | 5911.4132 |
| 2.5224 | 7008.5078 | 6601.4527 | 5844.1248 |
| 2.5334 | 6938.7994 | 6619.8236 | 5776.8364 |
| 2.5444 | 7001.8058 | 6644.0438 | 5709.5480 |
| 2.5554 | 7010.9597 | 6673.3782 | 5642.2596 |
| 2.5664 | 6940.7183 | 6706.7311 | 5574.9712 |
| 2.5774 | 6845.7257 | 6742.7327 | 5507.5253 |
| 2.5884 | 6820.4228 | 6779.5798 | 5440.0793 |
| 2.5994 | 6800.1150 | 6815.1011 | 5372.6334 |
| 2.6104 | 6766.0438 | 6846.6027 | 5305.1874 |
| 2.6214 | 6678.9105 | 6870.9522 | 5237.7415 |
| 2.6324 | 6548.0192 | 6884.6862 | 5170.2955 |
| 2.6434 | 6636.0315 | 6884.2254 | 5102.8495 |
| 2.6544 | 6586.4759 | 6866.2034 | 5035.4036 |
| 2.6654 | 6568.6490 | 6827.8719 | 4967.9576 |
| 2.6764 | 6428.2984 | 6767.4982 | 4900.5117 |
| 2.6874 | 6318.7984 | 6684.6476 | 4833.0657 |
| 2.6984 | 6205.5310 | 6580.2569 | 4765.6197 |
| 2.7094 | 5999.4356 | 6456.4773 | 4698.1738 |
| 2.7204 | 5840.7492 | 6316.4362 | 4630.7278 |
| 2.7314 | 5670.2271 | 6163.4873 | 4563.2819 |
| 2.7424 | 5716.8796 | 6001.1858 | 4495.8359 |
| 2.7534 | 5539.2605 | 5832.8694 | 4428.3900 |
| 2.7644 | 5297.4601 | 5661.5420 | 4360.7492 |
| 2.7754 | 5045.9066 | 5489.7035 | 4293.1085 |
| 2.7864 | 4874.8643 | 5319.4861 | 4225.4678 |
| 2.7974 | 4822.2566 | 5152.5213 | 4157.8270 |
| 2.8084 | 4512.9360 | 4990.0596 | 4090.1863 |
| 2.8194 | 4382.4985 | 4833.0202 | 4022.5456 |
| 2.8304 | 4197.8525 | 4682.0367 | 3954.9048 |
| 2.8414 | 4154.9764 | 4537.4971 | 3887.2641 |
| 2.8524 | 4039.4307 | 4399.5799 | 3819.6234 |
| 2.8634 | 3828.7964 | 4268.2866 | 3751.9826 |
| 2.8744 | 3700.5678 | 4143.4718 | 3684.3419 |
| 2.8854 | 3675.3677 | 4024.8722 | 3616.7012 |
| 2.8964 | 3598.3407 | 3912.1339 | 3549.0604 |
| 2.9074 | 3541.0482 | 3804.8378 | 3481.4197 |
| 2.9184 | 3420.3953 | 3702.5232 | 3413.7790 |
| 2.9294 | 3387.9823 | 3604.7084 | 3346.1382 |
| 2.9404 | 3291.0654 | 3523.9939 | 3278.4975 |
| 2.9514 | 3144.9390 | 3456.0307 | 3246.2344 |
| 2.9624 | 3177.0000 | 3404.2461 | 3213.9713 |
| 2.9734 | 3175.7758 | 3355.1379 | 3181.7082 |
| 2.9844 | 3141.5290 | 3308.3257 | 3149.4451 |
| 2.9954 | 2955.5752 | 3263.4687 | 3117.1820 |
| 3.0064 | 3048.8530 | 3220.2669 | 3084.9189 |
| 3.0174 | 3013.8151 | 3178.4597 | 3052.6559 |
| 3.0284 | 2981.8510 | 3137.8239 | 3020.3928 |
| 3.0394 | 2942.5516 | 3098.1704 | 2988.1297 |
| 3.0504 | 2872.2149 | 3059.3407 | 2955.8666 |
| 3.0614 | 2906.8820 | 3021.2033 | 2923.6035 |
| 3.0724 | 2883.9980 | 2983.6497 | 2891.3404 |
| 3.0834 | 2895.5919 | 2946.5910 | 2859.0773 |
| 3.0944 | 2832.9823 | 2909.9545 | 2826.8142 |
| 3.1054 | 2738.0836 | 2873.6812 | 2794.5511 |
| 3.1164 | 2725.5855 | 2837.7226 | 2762.2880 |
| 3.1274 | 2718.8319 | 2806.0806 | 2730.0249 |
| 3.1384 | 2766.3176 | 2777.5254 | 2708.6881 |
| 3.1494 | 2696.1386 | 2753.2275 | 2687.3512 |
| 3.1604 | 2645.7021 | 2729.1234 | 2666.0143 |
| 3.1714 | 2609.9774 | 2705.1942 | 2644.6774 |
| 3.1824 | 2601.1146 | 2681.4240 | 2623.3405 |
| 3.1934 | 2617.5310 | 2657.7988 | 2602.0036 |
| 3.2044 | 2546.1288 | 2634.3066 | 2580.6667 |
| 3.2154 | 2487.3343 | 2610.9370 | 2559.3298 |
| 3.2264 | 2441.3156 | 2587.6805 | 2537.9930 |
| 3.2374 | 2487.2724 | 2564.5287 | 2516.6561 |
| 3.2484 | 2502.6111 | 2541.4741 | 2495.3192 |
| 3.2594 | 2462.8525 | 2518.5099 | 2473.9823 |
| 3.2704 | 2403.7119 | 2495.6299 | 2452.6454 |
| 3.2814 | 2447.7139 | 2472.8284 | 2431.3085 |
| 3.2924 | 2446.7743 | 2450.1003 | 2409.9716 |
| 3.3034 | 2371.5221 | 2427.4408 | 2388.6347 |
| 3.3144 | 2314.0462 | 2406.2409 | 2367.2979 |
| 3.3254 | 2364.5399 | 2386.0833 | 2349.7338 |
| 3.3364 | 2410.2030 | 2367.3775 | 2332.1698 |
| 3.3474 | 2341.0403 | 2348.7248 | 2314.6057 |
| 3.3584 | 2329.6844 | 2330.1220 | 2297.0417 |
| 3.3694 | 2313.4523 | 2311.5661 | 2279.4777 |
| 3.3804 | 2230.6258 | 2293.0543 | 2261.9136 |
| 3.3914 | 2237.3452 | 2274.5842 | 2244.3496 |
| 3.4024 | 2176.5142 | 2256.1534 | 2226.7855 |
| 3.4134 | 2152.0197 | 2237.7596 | 2209.2215 |
| 3.4244 | 2143.1563 | 2219.4009 | 2191.6575 |
| 3.4354 | 2130.3265 | 2201.0753 | 2174.0934 |
| 3.4464 | 2151.9317 | 2182.7810 | 2156.5294 |
| 3.4574 | 2151.3982 | 2164.5164 | 2138.9653 |
| 3.4684 | 2097.2232 | 2146.2800 | 2121.4013 |
| 3.4794 | 2101.6441 | 2128.0701 | 2103.8373 |
| 3.4904 | 2132.5266 | 2109.8856 | 2086.2732 |
| 3.5014 | 2033.5614 | 2094.0478 | 2068.7092 |
| 3.5124 | 2053.8068 | 2079.8673 | 2057.4250 |
| 3.5234 | 2045.9262 | 2068.0312 | 2046.1408 |
| 3.5344 | 1995.4110 | 2056.2157 | 2034.8566 |
| 3.5454 | 1981.2793 | 2044.4199 | 2023.5724 |
| 3.5564 | 2088.7567 | 2032.6428 | 2012.2882 |
| 3.5674 | 2069.1190 | 2020.8835 | 2001.0041 |
| 3.5784 | 1977.0260 | 2009.1413 | 1989.7199 |
| 3.5894 | 1975.5575 | 1997.4153 | 1978.4357 |
| 3.6004 | 1967.9203 | 1985.7047 | 1967.1515 |
| 3.6114 | 1967.1780 | 1974.0090 | 1955.8673 |
| 3.6224 | 1897.8097 | 1962.3274 | 1944.5831 |
| 3.6334 | 1919.4966 | 1950.6594 | 1933.2989 |
| 3.6444 | 1952.1096 | 1939.0042 | 1922.0147 |
| 3.6554 | 1886.9764 | 1927.3615 | 1910.7306 |
| 3.6664 | 1913.3737 | 1915.7307 | 1899.4464 |
| 3.6774 | 1900.0305 | 1904.1112 | 1888.1622 |
| 3.6884 | 1890.8363 | 1892.6950 | 1876.8780 |
| 3.6994 | 1831.0737 | 1881.4248 | 1866.1141 |
| 3.7104 | 1870.1608 | 1870.3570 | 1855.3502 |
| 3.7214 | 1837.3864 | 1859.2988 | 1844.5864 |
| 3.7324 | 1901.8678 | 1848.2499 | 1833.8225 |
| 3.7434 | 1823.1632 | 1837.2099 | 1823.0586 |
| 3.7544 | 1797.0059 | 1826.1784 | 1812.2948 |
| 3.7654 | 1816.2979 | 1815.1551 | 1801.5309 |
| 3.7764 | 1737.7124 | 1804.1398 | 1790.7670 |
| 3.7874 | 1710.2301 | 1793.1320 | 1780.0031 |
| 3.7984 | 1878.5319 | 1782.1316 | 1769.2393 |
| 3.8094 | 1743.3461 | 1771.1383 | 1758.4754 |
| 3.8204 | 1762.6740 | 1760.1518 | 1747.7115 |
| 3.8314 | 1684.7414 | 1749.1718 | 1736.9477 |
| 3.8424 | 1747.1593 | 1738.1982 | 1726.1838 |
| 3.8534 | 1698.8555 | 1727.2307 | 1715.4199 |
| 3.8644 | 1729.8112 | 1716.2691 | 1704.6560 |
| 3.8754 | 1620.5271 | 1706.9262 | 1693.8922 |
| 3.8864 | 1743.4203 | 1698.2141 | 1686.9795 |
| 3.8974 | 1694.7876 | 1691.1202 | 1680.0668 |
| 3.9084 | 1639.8447 | 1684.0316 | 1673.1542 |
| 3.9194 | 1692.2655 | 1676.9479 | 1666.2415 |
| 3.9304 | 1634.5285 | 1669.8691 | 1659.3288 |
| 3.9414 | 1621.6922 | 1662.7949 | 1652.4161 |
| 3.9524 | 1639.5014 | 1655.7253 | 1645.5035 |
| 3.9634 | 1577.4002 | 1648.6601 | 1638.5908 |
| 3.9744 | 1632.7945 | 1641.5992 | 1631.6781 |
| 3.9854 | 1595.2213 | 1634.5424 | 1624.7654 |
| 3.9964 | 1618.6298 | 1627.4897 | 1617.8528 |
| 4.0074 | 1606.0521 | 1620.4409 | 1610.9401 |
| 4.0184 | 1612.9705 | 1613.3958 | 1604.0274 |
| 4.0294 | 1636.1996 | 1606.3545 | 1597.1148 |
| 4.0404 | 1612.3446 | 1599.3168 | 1590.2021 |
| 4.0514 | 1593.1327 | 1592.2826 | 1583.2894 |
| 4.0624 | 1574.2094 | 1585.2518 | 1576.3767 |
| 4.0734 | 1578.0787 | 1578.2244 | 1569.4641 |
| 4.0844 | 1587.9248 | 1571.2002 | 1562.5514 |
| 4.0954 | 1556.2468 | 1564.1792 | 1555.6387 |
| 4.1064 | 1507.8825 | 1557.1613 | 1548.7260 |
| 4.1174 | 1515.5458 | 1550.1464 | 1541.8134 |
| 4.1284 | 1589.2783 | 1543.1345 | 1534.9007 |
| 4.1394 | 1547.6293 | 1536.1255 | 1527.9880 |
| 4.1504 | 1479.8908 | 1529.1193 | 1521.0753 |
| 4.1614 | 1505.1318 | 1522.1159 | 1514.1627 |
| 4.1724 | 1496.4793 | 1515.1153 | 1507.2500 |
| 4.1834 | 1467.7788 | 1508.1173 | 1500.3373 |
| 4.1944 | 1538.0551 | 1501.1220 | 1493.4247 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 20 Etosha22 HS crt 0-0.1cm S4 550C | 2.0054 | 29.9894 | 0.0110 | 12/12/2023 2:46:28 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6722 | 1667.10 | 0.2598 | 33.03603 | 100.00 |
| 5.3108 | 115.77 | 0.2598 | 16.62661 | 6.94 |
| 8.6551 | 799.34 | 0.1082 | 10.20827 | 47.95 |
| 10.5251 | 37.37 | 0.4330 | 8.39841 | 2.24 |
| 15.9810 | 255.66 | 0.1299 | 5.54137 | 15.34 |
| 17.6907 | 17.95 | 0.6927 | 5.00949 | 1.08 |
| 19.8781 | 13.99 | 0.6927 | 4.46290 | 0.84 |
| 26.2360 | 186.25 | 0.2165 | 3.39403 | 11.17 |
| 26.7499 | 81.06 | 0.1732 | 3.32998 | 4.86 |
| 27.5161 | 221.85 | 0.0866 | 3.23897 | 13.31 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-016-2838 | 52 | Titanium Oxide | Ti O2 | Rutile | 4 |
| * | 04-017-4317 | 36 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 14 |
| * | 04-011-6233 | 27 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 14 |
| * | 04-023-1517 | 17 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.9 Na0.15 Mg1.61 Ti0.28 Fe0.92 Al1.44 Si2.75 O11.32 ( O H )0.39 F0.29 | Phlogopite-1M | 34 |
| * | 04-025-4215 | 21 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 34 |

Anchor Scan Parameters

Dataset Name	20 Etosha22 HS crt 0-0.1cm S4 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 20\20 Etosha22 HS crt 0-0.1cm S4 550C.xrdml

Sample Identification	20 Etosha22 HS crt 0-0.1cm S4 550C

Measurement Start Date/Time	12/12/2023 2:46:28 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes