20 Etosha 22 HS crt 0-0.1 cm S4 glycol

Graphics

Graphics

Graphics

Quantitative Results

Phase Tin Oxide

Weight fraction/ %	2.0

Phase Titanium Oxide

Weight fraction/ %	3.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	12.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	7.0

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	8.0

Phase Potassium Magnesium Aluminum Fluoride Silicate Hydroxide

Weight fraction/ %	23.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	34.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	11.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Tin Oxide | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Potassium Magnesium Aluminum Fluoride Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Magnesium Silicon Oxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 20 Etosha22 HScrt 0-0.1cm S4 glycol | 2.0 | 3.0 | 12.0 | 7.0 | 8.0 | 23.0 | 34.0 | 11.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8522.0000 | 8511.7920 | 8522.0000 |
| 2.0164 | 8504.2301 | 8473.6153 | 8461.3202 |
| 2.0274 | 8360.7463 | 8413.2330 | 8400.6405 |
| 2.0384 | 8310.4469 | 8352.8636 | 8339.9607 |
| 2.0494 | 8302.7847 | 8292.5080 | 8279.2809 |
| 2.0604 | 8422.0777 | 8232.1669 | 8218.6012 |
| 2.0714 | 8235.7227 | 8171.8414 | 8157.9214 |
| 2.0824 | 8176.1495 | 8111.5324 | 8097.2417 |
| 2.0934 | 8136.9105 | 8051.2409 | 8036.5619 |
| 2.1044 | 8310.0531 | 7990.9682 | 7975.8821 |
| 2.1154 | 8005.5025 | 7930.7155 | 7915.2024 |
| 2.1264 | 7974.9843 | 7870.4842 | 7854.5226 |
| 2.1374 | 8111.2330 | 7810.2757 | 7793.8428 |
| 2.1484 | 8022.1563 | 7750.0918 | 7733.1631 |
| 2.1594 | 7862.5880 | 7689.9342 | 7672.4833 |
| 2.1704 | 7775.8437 | 7629.8049 | 7611.8035 |
| 2.1814 | 7813.1052 | 7569.7059 | 7551.1238 |
| 2.1924 | 7944.5369 | 7509.5728 | 7490.4440 |
| 2.2034 | 7976.5133 | 7449.4261 | 7429.5819 |
| 2.2144 | 7912.4253 | 7389.2507 | 7368.7198 |
| 2.2254 | 7852.4848 | 7329.1164 | 7307.8576 |
| 2.2364 | 7754.6755 | 7269.0267 | 7246.9955 |
| 2.2474 | 7724.1888 | 7208.9853 | 7186.1334 |
| 2.2584 | 7697.1229 | 7148.9964 | 7125.2712 |
| 2.2694 | 7628.6903 | 7089.0646 | 7064.4091 |
| 2.2804 | 7606.4744 | 7029.1951 | 7003.5470 |
| 2.2914 | 7549.5280 | 6969.3935 | 6942.6848 |
| 2.3024 | 7487.2743 | 6909.6663 | 6881.8227 |
| 2.3134 | 7494.3835 | 6850.0207 | 6820.9606 |
| 2.3244 | 7430.6234 | 6790.4647 | 6760.0985 |
| 2.3354 | 7401.4366 | 6731.0073 | 6699.2363 |
| 2.3464 | 7338.1254 | 6671.6588 | 6638.3742 |
| 2.3574 | 7216.2517 | 6612.4307 | 6577.5121 |
| 2.3684 | 7192.5855 | 6553.3364 | 6516.6499 |
| 2.3794 | 7098.3727 | 6494.3371 | 6455.7878 |
| 2.3904 | 7115.2793 | 6435.4648 | 6394.7781 |
| 2.4014 | 7076.2743 | 6376.7259 | 6333.7685 |
| 2.4124 | 7065.4720 | 6318.1992 | 6272.7588 |
| 2.4234 | 7122.4789 | 6259.9151 | 6211.7491 |
| 2.4344 | 7080.5192 | 6201.9113 | 6150.7395 |
| 2.4454 | 7032.7325 | 6144.2362 | 6089.7298 |
| 2.4564 | 6999.1106 | 6086.9533 | 6028.7201 |
| 2.4674 | 6973.2301 | 6030.1468 | 5967.7105 |
| 2.4784 | 6988.1293 | 5973.9308 | 5906.7008 |
| 2.4894 | 6969.5615 | 5918.4598 | 5845.6911 |
| 2.5004 | 6824.0442 | 5863.9431 | 5784.6814 |
| 2.5114 | 6723.4808 | 5810.6617 | 5723.6718 |
| 2.5224 | 6746.1750 | 5758.9866 | 5662.6621 |
| 2.5334 | 6749.7404 | 5709.3987 | 5601.6524 |
| 2.5444 | 6680.7625 | 5662.5055 | 5540.6428 |
| 2.5554 | 6571.3992 | 5619.0517 | 5479.6331 |
| 2.5664 | 6606.1018 | 5579.9201 | 5418.6234 |
| 2.5774 | 6648.8043 | 5546.1153 | 5357.6138 |
| 2.5884 | 6424.8638 | 5518.7286 | 5296.6041 |
| 2.5994 | 6555.5576 | 5498.8774 | 5235.5944 |
| 2.6104 | 6471.7615 | 5487.6209 | 5174.5848 |
| 2.6214 | 6572.6716 | 5485.8520 | 5113.5751 |
| 2.6324 | 6399.8775 | 5494.1694 | 5052.5654 |
| 2.6434 | 6372.5457 | 5512.7356 | 4991.5558 |
| 2.6544 | 6309.1018 | 5541.1208 | 4930.5461 |
| 2.6654 | 6264.6254 | 5578.1298 | 4869.5364 |
| 2.6764 | 6199.0206 | 5621.6003 | 4808.5268 |
| 2.6874 | 6053.0246 | 5668.1681 | 4747.5171 |
| 2.6984 | 6003.1593 | 5713.0314 | 4686.5074 |
| 2.7094 | 5896.9518 | 5749.8351 | 4625.4977 |
| 2.7204 | 5658.0855 | 5770.9281 | 4564.4881 |
| 2.7314 | 5722.6254 | 5768.2908 | 4503.4784 |
| 2.7424 | 5495.5383 | 5735.1952 | 4442.4687 |
| 2.7534 | 5439.3284 | 5668.0453 | 4381.4591 |
| 2.7644 | 5224.4351 | 5567.6660 | 4320.3019 |
| 2.7754 | 5168.7925 | 5438.9217 | 4259.1447 |
| 2.7864 | 4845.7320 | 5289.2702 | 4197.9875 |
| 2.7974 | 4752.9823 | 5126.7417 | 4136.8303 |
| 2.8084 | 4588.1873 | 4958.5810 | 4075.6730 |
| 2.8194 | 4475.4080 | 4790.5898 | 4014.5158 |
| 2.8304 | 4206.0442 | 4627.0355 | 3953.3586 |
| 2.8414 | 4145.7011 | 4470.8286 | 3892.2014 |
| 2.8524 | 4067.2871 | 4323.7645 | 3831.0442 |
| 2.8634 | 3934.5339 | 4186.7467 | 3769.8870 |
| 2.8744 | 3825.1037 | 4059.9770 | 3708.7298 |
| 2.8854 | 3908.5290 | 3943.1216 | 3647.5726 |
| 2.8964 | 3703.9159 | 3835.4622 | 3586.4154 |
| 2.9074 | 3561.0236 | 3736.0339 | 3525.2582 |
| 2.9184 | 3561.0570 | 3643.7459 | 3464.1010 |
| 2.9294 | 3415.9557 | 3557.4823 | 3402.9438 |
| 2.9404 | 3349.1391 | 3486.7284 | 3341.7866 |
| 2.9514 | 3228.5054 | 3427.6832 | 3309.4455 |
| 2.9624 | 3287.8879 | 3382.3491 | 3277.1045 |
| 2.9734 | 3093.0797 | 3339.4798 | 3244.7635 |
| 2.9844 | 3183.7183 | 3298.5147 | 3212.4225 |
| 2.9954 | 3178.2389 | 3259.0137 | 3180.0814 |
| 3.0064 | 3148.8387 | 3220.6400 | 3147.7404 |
| 3.0174 | 3113.8545 | 3183.1401 | 3115.3994 |
| 3.0284 | 3149.6607 | 3146.3257 | 3083.0583 |
| 3.0394 | 2932.0000 | 3110.0583 | 3050.7173 |
| 3.0504 | 2937.7001 | 3074.2352 | 3018.3763 |
| 3.0614 | 2957.3628 | 3038.7805 | 2986.0353 |
| 3.0724 | 2906.8505 | 3003.6366 | 2953.6942 |
| 3.0834 | 2870.6352 | 2968.7593 | 2921.3532 |
| 3.0944 | 2904.4115 | 2934.1138 | 2889.0122 |
| 3.1054 | 2861.6499 | 2899.6718 | 2856.6711 |
| 3.1164 | 2788.9985 | 2865.4102 | 2824.3301 |
| 3.1274 | 2747.1003 | 2836.1069 | 2791.9891 |
| 3.1384 | 2810.0206 | 2810.4554 | 2772.7508 |
| 3.1494 | 2779.9302 | 2789.7310 | 2753.5125 |
| 3.1604 | 2749.1209 | 2769.1236 | 2734.2742 |
| 3.1714 | 2677.7551 | 2748.6221 | 2715.0359 |
| 3.1824 | 2626.3560 | 2728.2169 | 2695.7977 |
| 3.1934 | 2740.5221 | 2707.8992 | 2676.5594 |
| 3.2044 | 2682.3097 | 2687.6613 | 2657.3211 |
| 3.2154 | 2605.3677 | 2667.4964 | 2638.0828 |
| 3.2264 | 2622.3230 | 2647.3983 | 2618.8445 |
| 3.2374 | 2654.9361 | 2627.3617 | 2599.6062 |
| 3.2484 | 2571.6666 | 2607.3815 | 2580.3679 |
| 3.2594 | 2465.9587 | 2587.4534 | 2561.1296 |
| 3.2704 | 2502.0590 | 2567.5732 | 2541.8914 |
| 3.2814 | 2543.8299 | 2547.7376 | 2522.6531 |
| 3.2924 | 2470.4115 | 2527.9431 | 2503.4148 |
| 3.3034 | 2457.0600 | 2508.1868 | 2484.1765 |
| 3.3144 | 2466.5231 | 2491.5031 | 2464.9382 |
| 3.3254 | 2453.3009 | 2477.0728 | 2453.9942 |
| 3.3364 | 2484.0285 | 2465.7105 | 2443.0503 |
| 3.3474 | 2498.5241 | 2454.3770 | 2432.1063 |
| 3.3584 | 2458.1342 | 2443.0705 | 2421.1623 |
| 3.3694 | 2460.2950 | 2431.7895 | 2410.2183 |
| 3.3804 | 2438.9897 | 2420.5322 | 2399.2743 |
| 3.3914 | 2398.2212 | 2409.2973 | 2388.3304 |
| 3.4024 | 2409.5118 | 2398.0836 | 2377.3864 |
| 3.4134 | 2464.1278 | 2386.8898 | 2366.4424 |
| 3.4244 | 2433.6888 | 2375.7148 | 2355.4984 |
| 3.4354 | 2343.1730 | 2364.5577 | 2344.5544 |
| 3.4464 | 2306.1190 | 2353.4174 | 2333.6104 |
| 3.4574 | 2293.6637 | 2342.2933 | 2322.6665 |
| 3.4684 | 2275.9405 | 2331.1844 | 2311.7225 |
| 3.4794 | 2224.3569 | 2320.0900 | 2300.7785 |
| 3.4904 | 2284.3894 | 2309.0096 | 2289.8345 |
| 3.5014 | 2310.5388 | 2298.9790 | 2278.8905 |
| 3.5124 | 2267.8063 | 2289.7190 | 2270.7775 |
| 3.5234 | 2265.2271 | 2281.5077 | 2262.6645 |
| 3.5344 | 2205.1135 | 2273.3081 | 2254.5515 |
| 3.5454 | 2174.3963 | 2265.1198 | 2246.4385 |
| 3.5564 | 2261.6977 | 2256.9424 | 2238.3254 |
| 3.5674 | 2179.2192 | 2248.7754 | 2230.2124 |
| 3.5784 | 2181.6691 | 2240.6186 | 2222.0994 |
| 3.5894 | 2184.9911 | 2232.4716 | 2213.9864 |
| 3.6004 | 2129.5924 | 2224.3341 | 2205.8733 |
| 3.6114 | 2227.8181 | 2216.2059 | 2197.7603 |
| 3.6224 | 2210.2065 | 2208.0867 | 2189.6473 |
| 3.6334 | 2130.1976 | 2199.9763 | 2181.5343 |
| 3.6444 | 2122.4823 | 2191.8745 | 2173.4213 |
| 3.6554 | 2190.6490 | 2183.7811 | 2165.3082 |
| 3.6664 | 2120.8289 | 2175.6959 | 2157.1952 |
| 3.6774 | 2141.7296 | 2167.6188 | 2149.0822 |
| 3.6884 | 2139.0752 | 2162.3363 | 2140.9692 |
| 3.6994 | 2170.1416 | 2156.8705 | 2138.2383 |
| 3.7104 | 2070.8171 | 2154.1991 | 2135.5075 |
| 3.7214 | 2078.3481 | 2151.5353 | 2132.7766 |
| 3.7324 | 2053.9685 | 2148.8791 | 2130.0458 |
| 3.7434 | 2016.2045 | 2146.2304 | 2127.3149 |
| 3.7544 | 2062.6682 | 2143.5891 | 2124.5841 |
| 3.7654 | 2163.5900 | 2140.9552 | 2121.8533 |
| 3.7764 | 2065.1986 | 2138.3287 | 2119.1224 |
| 3.7874 | 2122.4690 | 2135.7095 | 2116.3916 |
| 3.7984 | 2150.7797 | 2133.0976 | 2113.6607 |
| 3.8094 | 2085.9774 | 2130.4932 | 2110.9299 |
| 3.8204 | 2024.0738 | 2127.8960 | 2108.1990 |
| 3.8314 | 2096.0806 | 2125.3063 | 2105.4682 |
| 3.8424 | 2099.9464 | 2122.7240 | 2102.7374 |
| 3.8534 | 2133.1829 | 2120.1491 | 2100.0065 |
| 3.8644 | 2103.9125 | 2117.5818 | 2097.2757 |
| 3.8754 | 2070.4002 | 2114.9188 | 2094.5448 |
| 3.8864 | 2103.3717 | 2112.3247 | 2091.6688 |
| 3.8974 | 2080.5595 | 2109.6352 | 2088.7928 |
| 3.9084 | 2010.8304 | 2106.9534 | 2085.9168 |
| 3.9194 | 1995.0325 | 2104.2796 | 2083.0407 |
| 3.9304 | 2082.9430 | 2101.6139 | 2080.1647 |
| 3.9414 | 2111.2271 | 2098.9563 | 2077.2887 |
| 3.9524 | 2058.9838 | 2096.3070 | 2074.4127 |
| 3.9634 | 2066.8023 | 2093.6662 | 2071.5367 |
| 3.9744 | 2048.8043 | 2091.0340 | 2068.6606 |
| 3.9854 | 2094.6195 | 2088.4105 | 2065.7846 |
| 3.9964 | 2128.3830 | 2085.7960 | 2062.9086 |
| 4.0074 | 2095.2556 | 2083.1906 | 2060.0326 |
| 4.0184 | 2050.5015 | 2080.5945 | 2057.1565 |
| 4.0294 | 2071.7552 | 2078.0080 | 2054.2805 |
| 4.0404 | 2125.0462 | 2075.4312 | 2051.4045 |
| 4.0514 | 2089.1327 | 2072.8644 | 2048.5285 |
| 4.0624 | 2082.7434 | 2070.1978 | 2045.6525 |
| 4.0734 | 2098.0570 | 2067.6070 | 2042.6216 |
| 4.0844 | 2073.0929 | 2064.9170 | 2039.5908 |
| 4.0954 | 2080.0767 | 2062.2380 | 2036.5600 |
| 4.1064 | 2077.4975 | 2059.5705 | 2033.5291 |
| 4.1174 | 2043.7935 | 2056.9146 | 2030.4983 |
| 4.1284 | 2086.4435 | 2054.2708 | 2027.4675 |
| 4.1394 | 2102.4602 | 2051.6395 | 2024.4366 |
| 4.1504 | 2126.6475 | 2049.0209 | 2021.4058 |
| 4.1614 | 2121.4582 | 2046.4155 | 2018.3750 |
| 4.1724 | 2081.8481 | 2043.8238 | 2015.3441 |
| 4.1834 | 2088.3628 | 2041.2462 | 2012.3133 |
| 4.1944 | 2096.1613 | 2038.6831 | 2009.2825 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 20 Etosha22 HScrt 0-0.1cm S4 glycol | 2.0054 | 29.9894 | 0.0110 | 12/13/2023 9:19:31 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7437 | 1155.02 | 0.1732 | 32.17472 | 100.00 |
| 5.2973 | 918.05 | 0.5196 | 16.66913 | 79.48 |
| 6.8231 | 1005.75 | 0.1515 | 12.94460 | 87.08 |
| 7.0436 | 1126.70 | 0.1732 | 12.53977 | 97.55 |
| 8.7084 | 632.16 | 0.1299 | 10.14589 | 54.73 |
| 15.7079 | 815.68 | 0.0974 | 5.63708 | 70.62 |
| 17.5471 | 67.28 | 0.2165 | 5.05016 | 5.82 |
| 18.1510 | 148.64 | 0.1515 | 4.88347 | 12.87 |
| 19.5388 | 51.43 | 0.6061 | 4.53963 | 4.45 |
| 22.3922 | 34.86 | 0.2598 | 3.96718 | 3.02 |
| 24.1305 | 29.54 | 0.2598 | 3.68520 | 2.56 |
| 25.8711 | 806.46 | 0.0758 | 3.44106 | 69.82 |
| 26.6611 | 274.11 | 0.1732 | 3.34087 | 23.73 |
| 27.4852 | 159.51 | 0.1732 | 3.24254 | 13.81 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-070-4177 | 51 | Tin Oxide | Sn O2 | Cassiterite | 2 |
| * | 04-008-7810 | 44 | Titanium Oxide | Ti O2 | Rutile | 3 |
| * | 04-017-4317 | 43 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 12 |
| * | 01-072-4625 | 30 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 7 |
| * | 04-016-6876 | 39 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 8 |
| * | 00-034-0159 | 21 | Potassium Magnesium Aluminum Fluoride Silicate Hydroxide | K Mg3 Si3 Al O10 ( F , O H )2 | Phlogopite-1M | 23 |
| * | 04-025-4215 | 18 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 34 |
| * | 01-082-8023 | 27 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 11 |

Anchor Scan Parameters

Dataset Name	20 Etosha22 HScrt 0-0.1cm S4 glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 20\20 Etosha22 HScrt 0-0.1cm S4 glycol.xrdml

Sample Identification	20 Etosha22 HScrt 0-0.1cm S4

Measurement Start Date/Time	12/13/2023 9:19:31 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes