20 Etosha 22 HS crt 0-0.1 cm S4 regular

Graphics

Graphics

Graphics

Quantitative Results

Phase Tin Oxide

Weight fraction/ %	2.0

Phase Titanium Oxide

Weight fraction/ %	5.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	11.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	11.0

Phase Sodium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	7.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	43.0

Phase Potassium Manganese Silicate Hydroxide Hydrate

Weight fraction/ %	18.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Tin Oxide | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Silicon Oxide Hydroxide Hydrate | Sodium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Manganese Silicate Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 20 Etosha22 HS crt 0-0.1cm S4 | 2.0 | 5.0 | 11.0 | 11.0 | 4.0 | 7.0 | 43.0 | 18.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8742.0000 | 8702.2998 | 8742.0000 |
| 2.0164 | 8565.6883 | 8695.2478 | 8677.8196 |
| 2.0274 | 8615.8623 | 8631.5412 | 8613.6392 |
| 2.0384 | 8412.9956 | 8567.8559 | 8549.4588 |
| 2.0494 | 8438.8525 | 8504.1935 | 8485.2784 |
| 2.0604 | 8429.4243 | 8440.5552 | 8421.0979 |
| 2.0714 | 8325.1652 | 8376.9426 | 8356.9175 |
| 2.0824 | 8287.5826 | 8313.3574 | 8292.7371 |
| 2.0934 | 8382.6942 | 8249.8014 | 8228.5567 |
| 2.1044 | 8235.3938 | 8186.2765 | 8164.3763 |
| 2.1154 | 8307.4572 | 8122.7849 | 8100.1959 |
| 2.1264 | 8172.3265 | 8059.3287 | 8036.0155 |
| 2.1374 | 8160.1770 | 7995.9106 | 7971.8351 |
| 2.1484 | 7962.4361 | 7932.5331 | 7907.6547 |
| 2.1594 | 8105.6401 | 7869.1994 | 7843.4742 |
| 2.1704 | 7987.2743 | 7805.9124 | 7779.2938 |
| 2.1814 | 8042.2635 | 7742.6759 | 7715.1134 |
| 2.1924 | 8008.8215 | 7679.3203 | 7650.9330 |
| 2.2034 | 7922.7434 | 7616.1735 | 7586.5564 |
| 2.2144 | 7855.9282 | 7552.9165 | 7522.1798 |
| 2.2254 | 7855.9115 | 7489.7276 | 7457.8032 |
| 2.2364 | 7866.4100 | 7426.6125 | 7393.4266 |
| 2.2474 | 7707.2094 | 7363.5774 | 7329.0501 |
| 2.2584 | 7632.6844 | 7300.6292 | 7264.6735 |
| 2.2694 | 7611.4513 | 7237.7755 | 7200.2969 |
| 2.2804 | 7717.8628 | 7175.0251 | 7135.9203 |
| 2.2914 | 7577.6588 | 7112.3875 | 7071.5437 |
| 2.3024 | 7608.6770 | 7049.8739 | 7007.1671 |
| 2.3134 | 7546.5270 | 6987.4969 | 6942.7905 |
| 2.3244 | 7444.4853 | 6925.2713 | 6878.4139 |
| 2.3354 | 7459.4749 | 6863.2146 | 6814.0373 |
| 2.3464 | 7421.6116 | 6801.3476 | 6749.6607 |
| 2.3574 | 7374.0924 | 6739.6958 | 6685.2842 |
| 2.3684 | 7357.3835 | 6678.2904 | 6620.9076 |
| 2.3794 | 7314.1485 | 6617.0307 | 6556.5310 |
| 2.3904 | 7301.9813 | 6556.2279 | 6491.9957 |
| 2.4014 | 7286.5929 | 6495.6834 | 6427.4604 |
| 2.4124 | 7270.7847 | 6435.6183 | 6362.9251 |
| 2.4234 | 7175.4553 | 6376.1354 | 6298.3898 |
| 2.4344 | 7081.3864 | 6317.3657 | 6233.8545 |
| 2.4454 | 7043.1976 | 6259.4744 | 6169.3192 |
| 2.4564 | 7086.4567 | 6202.6676 | 6104.7839 |
| 2.4674 | 7130.0413 | 6147.1994 | 6040.2486 |
| 2.4784 | 7148.5172 | 6093.3776 | 5975.7133 |
| 2.4894 | 7049.3687 | 6041.5692 | 5911.1780 |
| 2.5004 | 6936.2212 | 5992.2022 | 5846.6427 |
| 2.5114 | 6892.6077 | 5945.7647 | 5782.1074 |
| 2.5224 | 6843.7856 | 5902.7995 | 5717.5721 |
| 2.5334 | 6800.5605 | 5863.8917 | 5653.0368 |
| 2.5444 | 6850.6126 | 5829.6513 | 5588.5015 |
| 2.5554 | 6817.3264 | 5800.6878 | 5523.9662 |
| 2.5664 | 6676.4661 | 5777.5778 | 5459.4309 |
| 2.5774 | 6689.9440 | 5760.8267 | 5394.8956 |
| 2.5884 | 6699.3830 | 5750.8243 | 5330.3602 |
| 2.5994 | 6728.7965 | 5747.7969 | 5265.8249 |
| 2.6104 | 6691.8353 | 5751.7550 | 5201.2896 |
| 2.6214 | 6687.7788 | 5762.4378 | 5136.7543 |
| 2.6324 | 6546.2714 | 5779.2532 | 5072.2190 |
| 2.6434 | 6489.5546 | 5801.2088 | 5007.6837 |
| 2.6544 | 6407.4297 | 5826.8340 | 4943.1484 |
| 2.6654 | 6394.9115 | 5854.0920 | 4878.6131 |
| 2.6764 | 6276.0413 | 5880.2970 | 4814.0778 |
| 2.6874 | 6170.7502 | 5902.0689 | 4749.5425 |
| 2.6984 | 6106.0885 | 5915.3864 | 4685.0072 |
| 2.7094 | 5968.7129 | 5915.8170 | 4620.4719 |
| 2.7204 | 5799.1839 | 5898.9787 | 4555.9366 |
| 2.7314 | 5704.9705 | 5861.2050 | 4491.4013 |
| 2.7424 | 5569.1219 | 5800.2559 | 4426.8660 |
| 2.7534 | 5448.5555 | 5715.6777 | 4362.3307 |
| 2.7644 | 5342.6475 | 5609.4214 | 4297.6367 |
| 2.7754 | 5108.4651 | 5484.5308 | 4232.9427 |
| 2.7864 | 4995.3328 | 5345.3930 | 4168.2487 |
| 2.7974 | 4727.3628 | 5196.4911 | 4103.5547 |
| 2.8084 | 4527.1121 | 5042.0095 | 4038.8607 |
| 2.8194 | 4445.2419 | 4885.5364 | 3974.1666 |
| 2.8304 | 4339.4425 | 4729.9656 | 3909.4726 |
| 2.8414 | 4058.2369 | 4577.5207 | 3844.7786 |
| 2.8524 | 3981.2689 | 4429.8323 | 3780.0846 |
| 2.8634 | 3820.7728 | 4288.0269 | 3715.3906 |
| 2.8744 | 3844.1008 | 4152.8085 | 3650.6966 |
| 2.8854 | 3684.7247 | 4024.5302 | 3586.0026 |
| 2.8964 | 3546.6017 | 3903.2564 | 3521.3086 |
| 2.9074 | 3400.5192 | 3788.8199 | 3456.6145 |
| 2.9184 | 3463.8028 | 3680.8743 | 3391.9205 |
| 2.9294 | 3353.6578 | 3578.9440 | 3327.2265 |
| 2.9404 | 3251.9867 | 3509.7858 | 3262.5325 |
| 2.9514 | 3200.6735 | 3421.7805 | 3228.7728 |
| 2.9624 | 3067.7832 | 3365.3308 | 3195.0130 |
| 2.9734 | 3121.3903 | 3312.5252 | 3161.2533 |
| 2.9844 | 3003.3147 | 3262.8064 | 3127.4935 |
| 2.9954 | 3015.2566 | 3215.6692 | 3093.7338 |
| 3.0064 | 2996.4405 | 3170.6669 | 3059.9741 |
| 3.0174 | 2906.9233 | 3127.4146 | 3026.2143 |
| 3.0284 | 2919.6947 | 3085.5869 | 2992.4546 |
| 3.0394 | 2841.3982 | 3044.9143 | 2958.6949 |
| 3.0504 | 2841.1204 | 3005.1770 | 2924.9351 |
| 3.0614 | 2792.1032 | 2966.1983 | 2891.1754 |
| 3.0724 | 2751.9980 | 2927.8378 | 2857.4156 |
| 3.0834 | 2781.3855 | 2889.9847 | 2823.6559 |
| 3.0944 | 2805.9779 | 2852.5522 | 2789.8962 |
| 3.1054 | 2738.2812 | 2815.4724 | 2756.1364 |
| 3.1164 | 2639.8643 | 2778.6920 | 2722.3767 |
| 3.1274 | 2725.0324 | 2755.7242 | 2688.6169 |
| 3.1384 | 2679.1382 | 2721.2200 | 2670.2076 |
| 3.1494 | 2655.3559 | 2700.5880 | 2651.7983 |
| 3.1604 | 2608.4528 | 2680.2162 | 2633.3890 |
| 3.1714 | 2611.0914 | 2659.8707 | 2614.9796 |
| 3.1824 | 2577.8009 | 2639.5949 | 2596.5703 |
| 3.1934 | 2531.9381 | 2619.4468 | 2578.1610 |
| 3.2044 | 2553.2193 | 2599.4149 | 2559.7516 |
| 3.2154 | 2514.3923 | 2579.4891 | 2541.3423 |
| 3.2264 | 2503.5914 | 2559.6605 | 2522.9330 |
| 3.2374 | 2477.5703 | 2539.9212 | 2504.5237 |
| 3.2484 | 2464.5555 | 2520.2641 | 2486.1143 |
| 3.2594 | 2405.0118 | 2500.6827 | 2467.7050 |
| 3.2704 | 2397.7689 | 2481.1712 | 2449.2957 |
| 3.2814 | 2373.0393 | 2461.7245 | 2430.8863 |
| 3.2924 | 2395.6637 | 2442.3377 | 2412.4770 |
| 3.3034 | 2412.9331 | 2423.0066 | 2394.0677 |
| 3.3144 | 2381.3736 | 2404.4149 | 2375.6584 |
| 3.3254 | 2342.7551 | 2385.2746 | 2358.0278 |
| 3.3364 | 2314.7699 | 2366.8668 | 2340.3972 |
| 3.3474 | 2325.4985 | 2348.5008 | 2322.7666 |
| 3.3584 | 2292.7094 | 2330.1738 | 2305.1360 |
| 3.3694 | 2247.4218 | 2311.8832 | 2287.5054 |
| 3.3804 | 2211.8628 | 2293.6268 | 2269.8748 |
| 3.3914 | 2215.1416 | 2275.4024 | 2252.2443 |
| 3.4024 | 2223.2198 | 2257.2079 | 2234.6137 |
| 3.4134 | 2187.6303 | 2239.0417 | 2216.9831 |
| 3.4244 | 2151.0192 | 2220.9018 | 2199.3525 |
| 3.4354 | 2109.1081 | 2202.7869 | 2181.7219 |
| 3.4464 | 2133.5393 | 2184.6954 | 2164.0913 |
| 3.4574 | 2148.9292 | 2166.6260 | 2146.4607 |
| 3.4684 | 2154.9636 | 2148.5775 | 2128.8301 |
| 3.4794 | 2159.7650 | 2130.5486 | 2111.1995 |
| 3.4904 | 2083.5000 | 2112.5384 | 2093.5690 |
| 3.5014 | 2062.4612 | 2101.4130 | 2075.9384 |
| 3.5124 | 2034.0708 | 2084.3464 | 2066.0845 |
| 3.5234 | 2079.6549 | 2074.1629 | 2056.2306 |
| 3.5344 | 2123.2945 | 2063.9944 | 2046.3767 |
| 3.5454 | 2020.4464 | 2053.8401 | 2036.5228 |
| 3.5564 | 2045.4396 | 2043.6993 | 2026.6689 |
| 3.5674 | 2041.6775 | 2033.5714 | 2016.8150 |
| 3.5784 | 1969.8751 | 2023.4556 | 2006.9611 |
| 3.5894 | 1911.5044 | 2013.3515 | 1997.1072 |
| 3.6004 | 2004.0330 | 2003.2585 | 1987.2534 |
| 3.6114 | 1999.6313 | 1993.1761 | 1977.3995 |
| 3.6224 | 2022.4646 | 1983.1037 | 1967.5456 |
| 3.6334 | 1958.7404 | 1973.0410 | 1957.6917 |
| 3.6444 | 1964.6155 | 1962.9875 | 1947.8378 |
| 3.6554 | 1906.5693 | 1952.9428 | 1937.9839 |
| 3.6664 | 1915.5428 | 1942.9065 | 1928.1300 |
| 3.6774 | 1935.4966 | 1932.8783 | 1918.2761 |
| 3.6884 | 1898.3761 | 1924.4263 | 1908.4222 |
| 3.6994 | 1905.4995 | 1914.6210 | 1900.3445 |
| 3.7104 | 1877.1313 | 1906.3913 | 1892.2668 |
| 3.7214 | 1929.9617 | 1898.1684 | 1884.1891 |
| 3.7324 | 1842.9601 | 1889.9521 | 1876.1114 |
| 3.7434 | 1867.0856 | 1881.7422 | 1868.0337 |
| 3.7544 | 1889.9941 | 1873.5383 | 1859.9560 |
| 3.7654 | 1817.5408 | 1865.3403 | 1851.8783 |
| 3.7764 | 1816.9577 | 1857.1480 | 1843.8006 |
| 3.7874 | 1813.0354 | 1848.9612 | 1835.7229 |
| 3.7984 | 1868.9553 | 1840.7797 | 1827.6451 |
| 3.8094 | 1854.7256 | 1832.6032 | 1819.5674 |
| 3.8204 | 1773.8790 | 1824.4317 | 1811.4897 |
| 3.8314 | 1738.3865 | 1816.2649 | 1803.4120 |
| 3.8424 | 1815.9489 | 1808.1028 | 1795.3343 |
| 3.8534 | 1766.3216 | 1799.9452 | 1787.2566 |
| 3.8644 | 1836.8250 | 1791.7919 | 1779.1789 |
| 3.8754 | 1765.8633 | 1783.6429 | 1771.1012 |
| 3.8864 | 1782.1770 | 1775.4979 | 1763.0235 |
| 3.8974 | 1678.0108 | 1767.3569 | 1754.9458 |
| 3.9084 | 1748.0000 | 1759.2198 | 1746.8681 |
| 3.9194 | 1745.7817 | 1751.0865 | 1738.7903 |
| 3.9304 | 1728.9813 | 1742.9569 | 1730.7126 |
| 3.9414 | 1723.5890 | 1734.8309 | 1722.6349 |
| 3.9524 | 1765.7994 | 1726.7084 | 1714.5572 |
| 3.9634 | 1688.7562 | 1718.5893 | 1706.4795 |
| 3.9744 | 1706.6008 | 1710.4736 | 1698.4018 |
| 3.9854 | 1691.5486 | 1702.3612 | 1690.3241 |
| 3.9964 | 1635.3668 | 1694.2520 | 1682.2464 |
| 4.0074 | 1711.2606 | 1686.1459 | 1674.1687 |
| 4.0184 | 1690.7655 | 1678.0430 | 1666.0910 |
| 4.0294 | 1671.8614 | 1669.9431 | 1658.0133 |
| 4.0404 | 1652.0462 | 1661.8462 | 1649.9355 |
| 4.0514 | 1618.4218 | 1653.7523 | 1641.8578 |
| 4.0624 | 1626.9946 | 1649.5697 | 1633.7801 |
| 4.0734 | 1656.9105 | 1641.9992 | 1630.1285 |
| 4.0844 | 1627.0752 | 1638.3399 | 1626.4768 |
| 4.0954 | 1633.9410 | 1634.6835 | 1622.8251 |
| 4.1064 | 1624.7753 | 1631.0298 | 1619.1735 |
| 4.1174 | 1626.6460 | 1627.3789 | 1615.5218 |
| 4.1284 | 1583.9513 | 1623.7307 | 1611.8702 |
| 4.1394 | 1561.2330 | 1620.0852 | 1608.2185 |
| 4.1504 | 1566.6800 | 1616.4425 | 1604.5668 |
| 4.1614 | 1593.4995 | 1612.8024 | 1600.9152 |
| 4.1724 | 1620.6455 | 1609.1650 | 1597.2635 |
| 4.1834 | 1635.9911 | 1605.5303 | 1593.6119 |
| 4.1944 | 1626.1347 | 1601.8982 | 1589.9602 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 20 Etosha22 HS crt 0-0.1cm S4 | 2.0054 | 29.9894 | 0.0110 | 12/12/2023 9:47:11 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7363 | 1226.44 | 0.2165 | 32.26173 | 82.15 |
| 5.3158 | 280.21 | 0.2165 | 16.61103 | 18.77 |
| 7.0974 | 1492.87 | 0.5196 | 12.44492 | 100.00 |
| 8.6888 | 414.51 | 0.2165 | 10.16880 | 27.77 |
| 13.1475 | 14.95 | 0.6927 | 6.72855 | 1.00 |
| 15.7107 | 564.91 | 0.0866 | 5.63610 | 37.84 |
| 17.6244 | 31.39 | 0.2598 | 5.02819 | 2.10 |
| 18.1670 | 74.99 | 0.1082 | 4.87920 | 5.02 |
| 19.5390 | 46.06 | 0.3464 | 4.53958 | 3.09 |
| 25.8475 | 457.31 | 0.0649 | 3.44415 | 30.63 |
| 26.6430 | 215.01 | 0.1082 | 3.34309 | 14.40 |
| 27.4639 | 207.68 | 0.1732 | 3.24500 | 13.91 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-070-4177 | 53 | Tin Oxide | Sn O2 | Cassiterite | 2 |
| * | 04-003-0648 | 50 | Titanium Oxide | Ti O2 | Rutile | 5 |
| * | 04-017-4317 | 34 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 11 |
| * | 04-016-3203 | 23 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 11 |
| * | 04-017-7291 | 17 | Sodium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Na0.930 Mg2.810 Fe0.065 Al1.185 Si2.895 O10 ( O H )2 ( H2 O )3 | Vermiculite | 4 |
| * | 01-072-4625 | 23 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 7 |
| * | 04-025-4215 | 22 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 43 |
| * | 01-089-6415 | 41 | Potassium Manganese Silicate Hydroxide Hydrate | K3.68 Mn15.904 Si25.472 O64 ( O H )9.376 ( H2 O )7.024 | Ganophyllite | 18 |

Anchor Scan Parameters

Dataset Name	20 Etosha22 HS crt 0-0.1cm S4

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 20\20 Etosha22 HS crt 0-0.1cm S4.xrdml

Sample Identification	20 Etosha22 HS crt 0-0.1cm S4

Measurement Start Date/Time	12/12/2023 9:47:11 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes