21 Etosha 22 Hssub 0.1-2.5 cm S4 REGULAR REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Tin Oxide

Weight fraction/ %	2.0

Phase Titanium Oxide

Weight fraction/ %	11.0

Phase Potassium Manganese Silicate Hydroxide Hydrate

Weight fraction/ %	5.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	6.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	14.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	20.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	28.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	11.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	3.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Tin Oxide | Titanium Oxide | Potassium Manganese Silicate Hydroxide Hydrate | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Aluminum Silicate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 21 Etosha22 HSsub 0.1-2.5cm S4 | 2.0 | 11.0 | 5.0 | 6.0 | 14.0 | 20.0 | 28.0 | 11.0 | 3.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8324.0000 | 8307.3984 | 8324.0000 |
| 2.0164 | 8309.5285 | 8274.7947 | 8263.6490 |
| 2.0274 | 8353.8682 | 8214.8091 | 8203.2980 |
| 2.0384 | 8422.0265 | 8154.8417 | 8142.9469 |
| 2.0494 | 8265.0659 | 8094.8937 | 8082.5959 |
| 2.0604 | 8243.8658 | 8034.9665 | 8022.2449 |
| 2.0714 | 8182.0619 | 7975.0614 | 7961.8939 |
| 2.0824 | 8007.7743 | 7915.1801 | 7901.5429 |
| 2.0934 | 8017.1799 | 7855.3243 | 7841.1918 |
| 2.1044 | 8047.4690 | 7795.4957 | 7780.8408 |
| 2.1154 | 8174.5015 | 7735.6965 | 7720.4898 |
| 2.1264 | 7943.0438 | 7675.9289 | 7660.1388 |
| 2.1374 | 7821.3894 | 7616.1953 | 7599.7878 |
| 2.1484 | 7893.4794 | 7556.4984 | 7539.4368 |
| 2.1594 | 7913.0354 | 7496.8412 | 7479.0857 |
| 2.1704 | 7953.1490 | 7437.2268 | 7418.7347 |
| 2.1814 | 7788.4523 | 7377.6589 | 7358.3837 |
| 2.1924 | 7835.6431 | 7318.0793 | 7298.0327 |
| 2.2034 | 7725.2124 | 7258.5419 | 7237.5448 |
| 2.2144 | 7767.7552 | 7199.0021 | 7177.0569 |
| 2.2254 | 7614.1406 | 7139.5274 | 7116.5690 |
| 2.2364 | 7666.3525 | 7080.1239 | 7056.0811 |
| 2.2474 | 7643.5202 | 7020.7983 | 6995.5932 |
| 2.2584 | 7641.2709 | 6961.5581 | 6935.1053 |
| 2.2694 | 7529.4307 | 6902.4120 | 6874.6174 |
| 2.2804 | 7489.6254 | 6843.3694 | 6814.1295 |
| 2.2914 | 7466.9282 | 6784.4412 | 6753.6416 |
| 2.3024 | 7340.8363 | 6725.6396 | 6693.1537 |
| 2.3134 | 7215.2124 | 6666.9785 | 6632.6658 |
| 2.3244 | 7338.7119 | 6608.4737 | 6572.1779 |
| 2.3354 | 7261.6224 | 6550.1433 | 6511.6900 |
| 2.3464 | 7340.4744 | 6492.0082 | 6451.2021 |
| 2.3574 | 7315.9538 | 6434.0922 | 6390.7142 |
| 2.3684 | 7196.5428 | 6376.4235 | 6330.2263 |
| 2.3794 | 7122.6539 | 6319.0348 | 6269.7384 |
| 2.3904 | 7197.1436 | 6261.9652 | 6209.2505 |
| 2.4014 | 7091.2478 | 6205.2623 | 6148.7626 |
| 2.4124 | 7049.1957 | 6148.9852 | 6088.2747 |
| 2.4234 | 7089.0718 | 6093.2098 | 6027.7868 |
| 2.4344 | 7081.6195 | 6038.0362 | 5967.2989 |
| 2.4454 | 7046.3343 | 5983.6009 | 5906.8110 |
| 2.4564 | 7051.7006 | 5930.0942 | 5846.3231 |
| 2.4674 | 6924.7138 | 5877.7849 | 5785.8352 |
| 2.4784 | 6852.8211 | 5827.0534 | 5725.3473 |
| 2.4894 | 6887.8781 | 5778.4345 | 5664.8594 |
| 2.5004 | 6823.6239 | 5732.6666 | 5604.3715 |
| 2.5114 | 6802.3078 | 5690.7436 | 5543.8836 |
| 2.5224 | 6709.9061 | 5653.9603 | 5483.3957 |
| 2.5334 | 6598.8319 | 5623.9385 | 5422.9078 |
| 2.5444 | 6535.6598 | 5602.6167 | 5362.4199 |
| 2.5554 | 6562.0079 | 5592.1859 | 5301.9320 |
| 2.5664 | 6547.6136 | 5594.8950 | 5241.4441 |
| 2.5774 | 6630.5703 | 5613.0150 | 5180.8193 |
| 2.5884 | 6464.3495 | 5648.3458 | 5120.1946 |
| 2.5994 | 6440.8938 | 5702.0827 | 5059.5698 |
| 2.6104 | 6536.2925 | 5774.2522 | 4998.9450 |
| 2.6214 | 6474.0275 | 5863.3397 | 4938.3202 |
| 2.6324 | 6406.5752 | 5965.7919 | 4877.6954 |
| 2.6434 | 6279.9390 | 6075.4230 | 4817.0707 |
| 2.6544 | 6287.6627 | 6182.7754 | 4756.4459 |
| 2.6654 | 6312.4248 | 6274.7600 | 4695.8211 |
| 2.6764 | 6200.7871 | 6335.3670 | 4635.1963 |
| 2.6874 | 6121.8496 | 6348.5317 | 4574.5715 |
| 2.6984 | 5929.3540 | 6302.9811 | 4513.9468 |
| 2.7094 | 5946.2232 | 6195.2569 | 4453.3220 |
| 2.7204 | 5712.5418 | 6033.8361 | 4392.6972 |
| 2.7314 | 5649.0000 | 5832.9410 | 4332.0724 |
| 2.7424 | 5311.3647 | 5609.4948 | 4271.4477 |
| 2.7534 | 5203.8967 | 5378.1019 | 4210.8229 |
| 2.7644 | 5044.3451 | 5149.9737 | 4150.0289 |
| 2.7754 | 4911.1740 | 4932.6700 | 4089.2349 |
| 2.7864 | 4815.4602 | 4730.9507 | 4028.4410 |
| 2.7974 | 4597.8053 | 4547.1988 | 3967.6470 |
| 2.8084 | 4411.2900 | 4382.0387 | 3906.8530 |
| 2.8194 | 4369.3520 | 4234.7948 | 3846.0590 |
| 2.8304 | 4197.3835 | 4103.9002 | 3785.2651 |
| 2.8414 | 3986.8348 | 3987.2639 | 3724.4711 |
| 2.8524 | 3902.9656 | 3882.5835 | 3663.6771 |
| 2.8634 | 3777.2448 | 3787.5899 | 3602.8832 |
| 2.8744 | 3609.8441 | 3700.2148 | 3542.0892 |
| 2.8854 | 3447.6745 | 3618.6850 | 3481.2952 |
| 2.8964 | 3563.4735 | 3541.5557 | 3420.5012 |
| 2.9074 | 3373.0954 | 3467.6989 | 3359.7073 |
| 2.9184 | 3258.8387 | 3396.2649 | 3298.9133 |
| 2.9294 | 3250.6106 | 3326.6316 | 3238.1193 |
| 2.9404 | 3232.1101 | 3271.6912 | 3177.3253 |
| 2.9514 | 3084.2016 | 3220.4940 | 3145.9100 |
| 2.9624 | 3066.5634 | 3183.4519 | 3114.4946 |
| 2.9734 | 3010.9174 | 3147.0686 | 3083.0792 |
| 2.9844 | 3053.9671 | 3111.2292 | 3051.6639 |
| 2.9954 | 3030.7256 | 3075.8479 | 3020.2485 |
| 3.0064 | 2912.1278 | 3040.8588 | 2988.8331 |
| 3.0174 | 2854.5919 | 3006.2094 | 2957.4178 |
| 3.0284 | 2820.5841 | 2971.8572 | 2926.0024 |
| 3.0394 | 2879.3019 | 2937.7666 | 2894.5870 |
| 3.0504 | 2894.6907 | 2903.9076 | 2863.1717 |
| 3.0614 | 2775.7994 | 2870.2545 | 2831.7563 |
| 3.0724 | 2767.0836 | 2836.7850 | 2800.3409 |
| 3.0834 | 2696.0000 | 2803.4800 | 2768.9256 |
| 3.0944 | 2703.8053 | 2770.3225 | 2737.5102 |
| 3.1054 | 2723.9813 | 2737.2979 | 2706.0948 |
| 3.1164 | 2686.6200 | 2704.3931 | 2674.6795 |
| 3.1274 | 2644.3599 | 2675.9952 | 2643.2641 |
| 3.1384 | 2593.3918 | 2648.5871 | 2621.5372 |
| 3.1494 | 2546.0266 | 2625.6669 | 2599.8103 |
| 3.1604 | 2572.7965 | 2602.8280 | 2578.0834 |
| 3.1714 | 2502.1150 | 2580.0633 | 2556.3565 |
| 3.1824 | 2436.0477 | 2557.3665 | 2534.6296 |
| 3.1934 | 2464.5841 | 2534.7319 | 2512.9027 |
| 3.2044 | 2428.9150 | 2512.1544 | 2491.1758 |
| 3.2154 | 2490.7601 | 2489.6293 | 2469.4489 |
| 3.2264 | 2481.9779 | 2467.1526 | 2447.7220 |
| 3.2374 | 2457.2340 | 2444.7204 | 2425.9951 |
| 3.2484 | 2430.7778 | 2422.3293 | 2404.2682 |
| 3.2594 | 2360.8879 | 2399.9764 | 2382.5413 |
| 3.2704 | 2299.0383 | 2377.6587 | 2360.8144 |
| 3.2814 | 2332.0217 | 2355.3738 | 2339.0875 |
| 3.2924 | 2370.2301 | 2333.1193 | 2317.3606 |
| 3.3034 | 2299.1111 | 2310.8931 | 2295.6337 |
| 3.3144 | 2271.2350 | 2289.5930 | 2273.9068 |
| 3.3254 | 2242.6106 | 2268.4999 | 2254.1618 |
| 3.3364 | 2198.1819 | 2248.3295 | 2234.4168 |
| 3.3474 | 2210.0206 | 2228.1806 | 2214.6718 |
| 3.3584 | 2211.0074 | 2208.0518 | 2194.9269 |
| 3.3694 | 2226.2350 | 2187.9418 | 2175.1819 |
| 3.3804 | 2185.5988 | 2167.8494 | 2155.4369 |
| 3.3914 | 2139.0885 | 2147.7736 | 2135.6919 |
| 3.4024 | 2100.7566 | 2127.7134 | 2115.9469 |
| 3.4134 | 2093.6116 | 2107.6679 | 2096.2019 |
| 3.4244 | 2053.8141 | 2087.6361 | 2076.4570 |
| 3.4354 | 2020.7935 | 2067.6173 | 2056.7120 |
| 3.4464 | 2073.8609 | 2047.6108 | 2036.9670 |
| 3.4574 | 2064.6755 | 2027.6158 | 2017.2220 |
| 3.4684 | 1999.0133 | 2007.6318 | 1997.4770 |
| 3.4794 | 1993.4690 | 1987.6581 | 1977.7320 |
| 3.4904 | 1975.3097 | 1967.6943 | 1957.9871 |
| 3.5014 | 1946.8967 | 1950.6061 | 1938.2421 |
| 3.5124 | 1922.2193 | 1934.1076 | 1924.8109 |
| 3.5234 | 1848.5604 | 1920.4839 | 1911.3797 |
| 3.5344 | 1886.5949 | 1906.8682 | 1897.9485 |
| 3.5454 | 1892.3776 | 1893.3539 | 1884.5173 |
| 3.5564 | 1911.8555 | 1879.7806 | 1871.0861 |
| 3.5674 | 1866.8456 | 1866.2353 | 1857.6549 |
| 3.5784 | 1810.8766 | 1852.6631 | 1844.2237 |
| 3.5894 | 1884.4602 | 1839.0838 | 1830.7925 |
| 3.6004 | 1894.3559 | 1825.5105 | 1817.3613 |
| 3.6114 | 1802.6057 | 1811.9428 | 1803.9302 |
| 3.6224 | 1774.3525 | 1798.3805 | 1790.4990 |
| 3.6334 | 1831.9735 | 1784.8234 | 1777.0678 |
| 3.6444 | 1769.3456 | 1771.2712 | 1763.6366 |
| 3.6554 | 1786.9027 | 1757.7238 | 1750.2054 |
| 3.6664 | 1752.7704 | 1744.1808 | 1736.7742 |
| 3.6774 | 1769.4425 | 1730.6422 | 1723.3430 |
| 3.6884 | 1721.0487 | 1717.9859 | 1709.9118 |
| 3.6994 | 1615.7895 | 1705.5115 | 1698.4148 |
| 3.7104 | 1703.5625 | 1693.9190 | 1686.9177 |
| 3.7214 | 1738.7699 | 1682.3301 | 1675.4207 |
| 3.7324 | 1661.9759 | 1670.7448 | 1663.9236 |
| 3.7434 | 1654.1160 | 1659.1629 | 1652.4266 |
| 3.7544 | 1642.5487 | 1647.5843 | 1640.9295 |
| 3.7654 | 1598.5044 | 1636.0088 | 1629.4325 |
| 3.7764 | 1639.0910 | 1624.4364 | 1617.9354 |
| 3.7874 | 1557.7345 | 1612.8668 | 1606.4384 |
| 3.7984 | 1615.0860 | 1601.3001 | 1594.9413 |
| 3.8094 | 1640.0787 | 1589.7361 | 1583.4443 |
| 3.8204 | 1642.9823 | 1578.1748 | 1571.9472 |
| 3.8314 | 1570.4198 | 1566.6160 | 1560.4502 |
| 3.8424 | 1507.5796 | 1555.0596 | 1548.9531 |
| 3.8534 | 1489.4632 | 1543.5056 | 1537.4561 |
| 3.8644 | 1591.5968 | 1531.9539 | 1525.9590 |
| 3.8754 | 1521.2733 | 1521.1801 | 1514.4620 |
| 3.8864 | 1465.9513 | 1510.5657 | 1504.6734 |
| 3.8974 | 1484.0157 | 1500.7290 | 1494.8849 |
| 3.9084 | 1420.3574 | 1490.8943 | 1485.0963 |
| 3.9194 | 1414.1298 | 1481.0616 | 1475.3078 |
| 3.9304 | 1445.3963 | 1471.2309 | 1465.5192 |
| 3.9414 | 1428.2891 | 1461.4020 | 1455.7307 |
| 3.9524 | 1375.3761 | 1451.5749 | 1445.9421 |
| 3.9634 | 1447.4218 | 1441.7496 | 1436.1536 |
| 3.9744 | 1406.0000 | 1431.9261 | 1426.3650 |
| 3.9854 | 1416.1947 | 1422.1042 | 1416.5765 |
| 3.9964 | 1444.1140 | 1412.2840 | 1406.7879 |
| 4.0074 | 1405.7345 | 1402.4654 | 1396.9994 |
| 4.0184 | 1377.2935 | 1392.6483 | 1387.2108 |
| 4.0294 | 1341.3697 | 1382.8328 | 1377.4223 |
| 4.0404 | 1361.9877 | 1373.0188 | 1367.6337 |
| 4.0514 | 1362.2979 | 1363.2063 | 1357.8452 |
| 4.0624 | 1357.0368 | 1354.6660 | 1348.0566 |
| 4.0734 | 1319.3039 | 1346.3847 | 1341.0672 |
| 4.0844 | 1355.1725 | 1339.3755 | 1334.0777 |
| 4.0954 | 1326.6942 | 1332.3678 | 1327.0883 |
| 4.1064 | 1338.4331 | 1325.3614 | 1320.0988 |
| 4.1174 | 1316.7286 | 1318.3563 | 1313.1093 |
| 4.1284 | 1328.8034 | 1311.3525 | 1306.1199 |
| 4.1394 | 1364.9478 | 1304.3501 | 1299.1304 |
| 4.1504 | 1279.0767 | 1297.3489 | 1292.1409 |
| 4.1614 | 1303.2271 | 1290.3490 | 1285.1515 |
| 4.1724 | 1302.8933 | 1283.3503 | 1278.1620 |
| 4.1834 | 1286.1239 | 1276.3529 | 1271.1725 |
| 4.1944 | 1239.4611 | 1269.3568 | 1264.1831 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 21 Etosha22 HSsub 0.1-2.5cm S4 | 2.0054 | 29.9894 | 0.0110 | 12/12/2023 9:57:38 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6932 | 1603.31 | 0.1515 | 32.77766 | 100.00 |
| 5.2793 | 128.26 | 0.1732 | 16.72591 | 8.00 |
| 7.0218 | 734.27 | 0.4330 | 12.57867 | 45.80 |
| 8.7040 | 516.65 | 0.1732 | 10.15107 | 32.22 |
| 13.5014 | 37.97 | 0.1299 | 6.55299 | 2.37 |
| 15.6818 | 921.17 | 0.1082 | 5.64642 | 57.45 |
| 17.6009 | 64.95 | 0.1732 | 5.03486 | 4.05 |
| 18.1537 | 132.09 | 0.1082 | 4.88276 | 8.24 |
| 19.6025 | 27.09 | 0.5196 | 4.52501 | 1.69 |
| 22.3625 | 21.46 | 0.2598 | 3.97239 | 1.34 |
| 23.3550 | 28.70 | 0.2598 | 3.80578 | 1.79 |
| 24.1665 | 29.61 | 0.1732 | 3.67978 | 1.85 |
| 25.8939 | 661.28 | 0.1082 | 3.43808 | 41.24 |
| 26.6262 | 405.12 | 0.1515 | 3.34517 | 25.27 |
| 27.5022 | 706.40 | 0.0433 | 3.24058 | 44.06 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-070-4177 | 55 | Tin Oxide | Sn O2 | Cassiterite | 2 |
| * | 04-016-2838 | 52 | Titanium Oxide | Ti O2 | Rutile | 11 |
| * | 01-089-6415 | 48 | Potassium Manganese Silicate Hydroxide Hydrate | K3.68 Mn15.904 Si25.472 O64 ( O H )9.376 ( H2 O )7.024 | Ganophyllite | 5 |
| * | 04-017-4317 | 47 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 6 |
| * | 04-011-6756 | 27 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 14 |
| * | 04-013-9383 | 19 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 Al Si3 O10 ( O H ) F | Phlogopite-2M1 | 20 |
| * | 04-025-4215 | 35 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 28 |
| * | 04-013-2099 | 19 | Potassium Aluminum Silicate | K8 Al8 Si16 O48 | Leucite | 11 |
|  | 01-081-8598 | 25 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2 Al2 ) Si8 O20 ( H2 O )4 ( O H )2 ( H2 O )3.84 | Palygorskite-M | 3 |

Anchor Scan Parameters

Dataset Name	21 Etosha22 HSsub 0.1-2.5cm S4

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 21\21 Etosha22 HSsub 0.1-2.5cm S4.xrdml

Sample Identification	21 Etosha22 HSsub 0.1-2.5cm S4

Measurement Start Date/Time	12/12/2023 9:57:38 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes