This is the simple example template containing only headers for each report item and the bookmarks. The invisible bookmarks are indicated by text between brackets.

Modify it according to your own needs and standards.

## Measurement Conditions:  (Bookmark 1)

## Main Graphics, Analyze View: (Bookmark 2)

## Peak List: (Bookmark 3)

Phase Tin Oxide

Weight fraction/ %	2.0

Phase Titanium Oxide

Weight fraction/ %	6.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	9.0

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Sodium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	10.0

Phase Potassium Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	11.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	37.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	15.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	8.0

| Scan name | Tin Oxide | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Sodium Aluminum Silicon Oxide Hydrate | Potassium Magnesium Aluminum Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Aluminum Silicate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 21 Etosha22 HSsub 0.1-2.5cm glycol | 2.0 | 6.0 | 9.0 | 3.0 | 10.0 | 11.0 | 37.0 | 15.0 | 8.0 |

## Pattern List: (Bookmark 4)

## Document History: (Bookmark 5)

More items… (Bookmark 6)

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8853.0000 | 8829.5212 | 8853.0000 |
| 2.0164 | 8734.4346 | 8804.5831 | 8787.8120 |
| 2.0274 | 8687.4759 | 8739.8873 | 8722.6239 |
| 2.0384 | 8619.7729 | 8675.2147 | 8657.4359 |
| 2.0494 | 8443.0944 | 8610.5669 | 8592.2478 |
| 2.0604 | 8665.5693 | 8545.9454 | 8527.0598 |
| 2.0714 | 8500.2183 | 8481.3520 | 8461.8717 |
| 2.0824 | 8597.1578 | 8416.7887 | 8396.6837 |
| 2.0934 | 8384.8073 | 8352.2573 | 8331.4956 |
| 2.1044 | 8292.1372 | 8287.7602 | 8266.3076 |
| 2.1154 | 8439.4857 | 8223.2998 | 8201.1195 |
| 2.1264 | 8370.9621 | 8158.8788 | 8135.9315 |
| 2.1374 | 8247.5516 | 8094.4999 | 8070.7434 |
| 2.1484 | 8324.7129 | 8030.1665 | 8005.5554 |
| 2.1594 | 8217.8210 | 7965.8818 | 7940.3673 |
| 2.1704 | 8221.9454 | 7901.6498 | 7875.1793 |
| 2.1814 | 7853.2439 | 7837.4745 | 7809.9912 |
| 2.1924 | 8124.9985 | 7773.2388 | 7744.8032 |
| 2.2034 | 8205.2389 | 7709.1134 | 7679.4158 |
| 2.2144 | 7955.5565 | 7644.9382 | 7614.0285 |
| 2.2254 | 7996.5900 | 7580.8409 | 7548.6411 |
| 2.2364 | 7864.1003 | 7516.8284 | 7483.2537 |
| 2.2474 | 7898.9902 | 7452.9082 | 7417.8664 |
| 2.2584 | 7853.7635 | 7389.0885 | 7352.4790 |
| 2.2694 | 7863.3156 | 7325.3789 | 7287.0916 |
| 2.2804 | 7772.1593 | 7261.7897 | 7221.7043 |
| 2.2914 | 7650.0197 | 7198.3328 | 7156.3169 |
| 2.3024 | 7675.0310 | 7135.0214 | 7090.9296 |
| 2.3134 | 7666.8505 | 7071.8710 | 7025.5422 |
| 2.3244 | 7668.0197 | 7008.8991 | 6960.1548 |
| 2.3354 | 7652.2124 | 6946.1262 | 6894.7675 |
| 2.3464 | 7638.8540 | 6883.5767 | 6829.3801 |
| 2.3574 | 7555.9361 | 6821.2802 | 6763.9927 |
| 2.3684 | 7458.8319 | 6759.2729 | 6698.6054 |
| 2.3794 | 7470.2527 | 6697.5019 | 6633.2180 |
| 2.3904 | 7431.4154 | 6636.1591 | 6567.6694 |
| 2.4014 | 7354.7611 | 6575.1858 | 6502.1208 |
| 2.4124 | 7469.6750 | 6514.7785 | 6436.5722 |
| 2.4234 | 7386.5172 | 6455.0658 | 6371.0236 |
| 2.4344 | 7191.6696 | 6396.2165 | 6305.4749 |
| 2.4454 | 7166.0767 | 6338.4505 | 6239.9263 |
| 2.4564 | 7228.7630 | 6282.0514 | 6174.3777 |
| 2.4674 | 7301.2537 | 6227.3797 | 6108.8291 |
| 2.4784 | 7256.2738 | 6174.8863 | 6043.2805 |
| 2.4894 | 7204.0924 | 6125.1224 | 5977.7319 |
| 2.5004 | 7060.2964 | 6078.7466 | 5912.1833 |
| 2.5114 | 6958.6499 | 6036.5238 | 5846.6346 |
| 2.5224 | 6927.5821 | 5999.3154 | 5781.0860 |
| 2.5334 | 6976.8466 | 5968.0560 | 5715.5374 |
| 2.5444 | 6923.4223 | 5943.7167 | 5649.9888 |
| 2.5554 | 6975.6087 | 5927.2525 | 5584.4402 |
| 2.5664 | 6910.8407 | 5919.5353 | 5518.8916 |
| 2.5774 | 6831.1957 | 5921.2728 | 5453.3430 |
| 2.5884 | 6789.3545 | 5932.9179 | 5387.7943 |
| 2.5994 | 6822.4159 | 5954.5686 | 5322.2457 |
| 2.6104 | 6782.0472 | 5985.8607 | 5256.6971 |
| 2.6214 | 6721.4680 | 6025.8499 | 5191.1485 |
| 2.6324 | 6562.5767 | 6072.8769 | 5125.5999 |
| 2.6434 | 6650.4179 | 6124.4117 | 5060.0513 |
| 2.6544 | 6576.1180 | 6176.8829 | 4994.5027 |
| 2.6654 | 6461.5782 | 6225.5374 | 4928.9540 |
| 2.6764 | 6364.7743 | 6264.4322 | 4863.4054 |
| 2.6874 | 6304.9459 | 6286.7247 | 4797.8568 |
| 2.6984 | 6002.8495 | 6285.4195 | 4732.3082 |
| 2.7094 | 6094.9912 | 6254.5750 | 4666.7596 |
| 2.7204 | 5960.0477 | 6190.6591 | 4601.2110 |
| 2.7314 | 5750.9469 | 6093.4954 | 4535.6624 |
| 2.7424 | 5647.9435 | 5966.3152 | 4470.1137 |
| 2.7534 | 5530.3618 | 5814.7890 | 4404.5651 |
| 2.7644 | 5288.6504 | 5646.0108 | 4338.8553 |
| 2.7754 | 5088.1101 | 5466.7528 | 4273.1454 |
| 2.7864 | 4895.3210 | 5283.1668 | 4207.4355 |
| 2.7974 | 4723.2124 | 5100.1241 | 4141.7257 |
| 2.8084 | 4680.6716 | 4921.3034 | 4076.0158 |
| 2.8194 | 4361.4808 | 4749.3253 | 4010.3059 |
| 2.8304 | 4271.0029 | 4585.9236 | 3944.5961 |
| 2.8414 | 4249.1858 | 4432.1033 | 3878.8862 |
| 2.8524 | 4044.5216 | 4288.2778 | 3813.1763 |
| 2.8634 | 3856.5988 | 4154.3875 | 3747.4665 |
| 2.8744 | 3809.1893 | 4030.0086 | 3681.7566 |
| 2.8854 | 3613.3097 | 3914.4531 | 3616.0467 |
| 2.8964 | 3451.7035 | 3806.8608 | 3550.3369 |
| 2.9074 | 3442.7168 | 3706.2811 | 3484.6270 |
| 2.9184 | 3406.4557 | 3611.7417 | 3418.9172 |
| 2.9294 | 3374.7109 | 3522.3025 | 3353.2073 |
| 2.9404 | 3219.7291 | 3456.2997 | 3287.4974 |
| 2.9514 | 3272.5821 | 3386.8141 | 3253.2608 |
| 2.9624 | 3184.6637 | 3339.3213 | 3219.0242 |
| 2.9734 | 3192.7994 | 3294.0540 | 3184.7875 |
| 2.9844 | 3037.1318 | 3250.5525 | 3150.5509 |
| 2.9954 | 3065.0000 | 3208.4481 | 3116.3143 |
| 3.0064 | 2966.1327 | 3167.4507 | 3082.0777 |
| 3.0174 | 2981.6077 | 3127.3348 | 3047.8410 |
| 3.0284 | 2965.9808 | 3087.9276 | 3013.6044 |
| 3.0394 | 2884.2714 | 3049.0970 | 2979.3678 |
| 3.0504 | 2864.3353 | 3010.7424 | 2945.1312 |
| 3.0614 | 2846.2065 | 2972.7868 | 2910.8945 |
| 3.0724 | 2765.9961 | 2935.1708 | 2876.6579 |
| 3.0834 | 2797.1603 | 2897.8480 | 2842.4213 |
| 3.0944 | 2758.0354 | 2860.7813 | 2808.1847 |
| 3.1054 | 2756.6283 | 2823.9408 | 2773.9481 |
| 3.1164 | 2699.7920 | 2787.3015 | 2739.7114 |
| 3.1274 | 2665.4454 | 2758.0925 | 2705.4748 |
| 3.1384 | 2716.4371 | 2726.4270 | 2683.1186 |
| 3.1494 | 2726.5732 | 2702.1584 | 2660.7625 |
| 3.1604 | 2635.8422 | 2678.0235 | 2638.4063 |
| 3.1714 | 2565.7483 | 2654.0103 | 2616.0502 |
| 3.1824 | 2588.4489 | 2630.1081 | 2593.6940 |
| 3.1934 | 2562.9292 | 2606.3077 | 2571.3379 |
| 3.2044 | 2541.7837 | 2582.6004 | 2548.9817 |
| 3.2154 | 2496.9685 | 2558.9788 | 2526.6256 |
| 3.2264 | 2492.4056 | 2535.4360 | 2504.2694 |
| 3.2374 | 2456.5447 | 2511.9658 | 2481.9133 |
| 3.2484 | 2475.1667 | 2488.5627 | 2459.5571 |
| 3.2594 | 2445.7079 | 2465.2215 | 2437.2010 |
| 3.2704 | 2394.8653 | 2441.9377 | 2414.8448 |
| 3.2814 | 2381.7620 | 2418.7072 | 2392.4886 |
| 3.2924 | 2403.1018 | 2395.5261 | 2370.1325 |
| 3.3034 | 2384.0049 | 2372.3910 | 2347.7763 |
| 3.3144 | 2327.2670 | 2354.3623 | 2325.4202 |
| 3.3254 | 2287.0590 | 2334.5442 | 2311.3620 |
| 3.3364 | 2236.6421 | 2319.8270 | 2297.3039 |
| 3.3474 | 2274.9764 | 2305.1446 | 2283.2458 |
| 3.3584 | 2334.8260 | 2290.4947 | 2269.1876 |
| 3.3694 | 2323.9282 | 2275.8754 | 2255.1295 |
| 3.3804 | 2308.2099 | 2261.2846 | 2241.0713 |
| 3.3914 | 2258.1239 | 2246.7207 | 2227.0132 |
| 3.4024 | 2185.5369 | 2232.1821 | 2212.9550 |
| 3.4134 | 2176.7198 | 2217.6672 | 2198.8969 |
| 3.4244 | 2134.6696 | 2203.1746 | 2184.8388 |
| 3.4354 | 2115.9567 | 2188.7031 | 2170.7806 |
| 3.4464 | 2166.7090 | 2174.2516 | 2156.7225 |
| 3.4574 | 2141.7168 | 2159.8188 | 2142.6643 |
| 3.4684 | 2113.8083 | 2145.4038 | 2128.6062 |
| 3.4794 | 2076.5329 | 2131.0056 | 2114.5480 |
| 3.4904 | 2127.5222 | 2116.6233 | 2100.4899 |
| 3.5014 | 2091.7974 | 2102.2562 | 2086.4318 |
| 3.5124 | 2058.0516 | 2087.9034 | 2072.3736 |
| 3.5234 | 2065.2655 | 2073.5642 | 2058.3155 |
| 3.5344 | 2020.5334 | 2059.2379 | 2044.2573 |
| 3.5454 | 1944.0609 | 2044.9240 | 2030.1992 |
| 3.5564 | 1923.4661 | 2030.6218 | 2016.1410 |
| 3.5674 | 1989.5890 | 2016.3308 | 2002.0829 |
| 3.5784 | 1955.1784 | 2002.0505 | 1988.0248 |
| 3.5894 | 1989.3540 | 1987.7804 | 1973.9666 |
| 3.6004 | 1965.1077 | 1973.5200 | 1959.9085 |
| 3.6114 | 2068.4071 | 1959.2690 | 1945.8503 |
| 3.6224 | 1977.7890 | 1945.0268 | 1931.7922 |
| 3.6334 | 1949.8191 | 1930.7933 | 1917.7340 |
| 3.6444 | 1931.7099 | 1916.5679 | 1903.6759 |
| 3.6554 | 1962.5900 | 1902.3504 | 1889.6177 |
| 3.6664 | 1928.7704 | 1888.1405 | 1875.5596 |
| 3.6774 | 1840.3854 | 1873.9379 | 1861.5015 |
| 3.6884 | 1846.4912 | 1862.4822 | 1847.4433 |
| 3.6994 | 1847.2144 | 1850.0435 | 1837.8753 |
| 3.7104 | 1803.5546 | 1840.3512 | 1828.3072 |
| 3.7214 | 1930.1888 | 1830.6652 | 1818.7391 |
| 3.7324 | 1889.9371 | 1820.9853 | 1809.1710 |
| 3.7434 | 1940.6352 | 1811.3113 | 1799.6030 |
| 3.7544 | 1791.3156 | 1801.6430 | 1790.0349 |
| 3.7654 | 1784.0000 | 1791.9802 | 1780.4668 |
| 3.7764 | 1763.4439 | 1782.3227 | 1770.8988 |
| 3.7874 | 1778.8584 | 1772.6704 | 1761.3307 |
| 3.7984 | 1765.9897 | 1763.0232 | 1751.7626 |
| 3.8094 | 1762.3864 | 1753.3809 | 1742.1946 |
| 3.8204 | 1725.6254 | 1743.7434 | 1732.6265 |
| 3.8314 | 1778.2507 | 1734.1106 | 1723.0584 |
| 3.8424 | 1687.0010 | 1724.4823 | 1713.4904 |
| 3.8534 | 1653.4012 | 1714.8585 | 1703.9223 |
| 3.8644 | 1687.4597 | 1705.2391 | 1694.3542 |
| 3.8754 | 1682.4317 | 1698.7298 | 1684.7861 |
| 3.8864 | 1698.9336 | 1691.1027 | 1680.3079 |
| 3.8974 | 1709.3844 | 1686.5857 | 1675.8296 |
| 3.9084 | 1664.0649 | 1682.0727 | 1671.3514 |
| 3.9194 | 1696.1563 | 1677.5636 | 1666.8731 |
| 3.9304 | 1636.3584 | 1673.0585 | 1662.3948 |
| 3.9414 | 1641.8781 | 1668.5573 | 1657.9166 |
| 3.9524 | 1629.4204 | 1664.0599 | 1653.4383 |
| 3.9634 | 1630.6391 | 1659.5663 | 1648.9601 |
| 3.9744 | 1658.1952 | 1655.0764 | 1644.4818 |
| 3.9854 | 1618.1504 | 1650.5903 | 1640.0035 |
| 3.9964 | 1619.4936 | 1646.1078 | 1635.5253 |
| 4.0074 | 1631.6824 | 1641.6291 | 1631.0470 |
| 4.0184 | 1616.5133 | 1637.1540 | 1626.5688 |
| 4.0294 | 1625.4936 | 1632.6825 | 1622.0905 |
| 4.0404 | 1667.9139 | 1628.2147 | 1617.6122 |
| 4.0514 | 1604.2743 | 1623.7505 | 1613.1340 |
| 4.0624 | 1595.7434 | 1619.2899 | 1608.6557 |
| 4.0734 | 1627.2144 | 1614.8330 | 1604.1775 |
| 4.0844 | 1626.1416 | 1610.3798 | 1599.6992 |
| 4.0954 | 1606.0649 | 1605.9303 | 1595.2209 |
| 4.1064 | 1608.5349 | 1601.4844 | 1590.7427 |
| 4.1174 | 1554.3658 | 1597.0423 | 1586.2644 |
| 4.1284 | 1545.3304 | 1592.6040 | 1581.7862 |
| 4.1394 | 1596.4563 | 1588.1694 | 1577.3079 |
| 4.1504 | 1592.6076 | 1583.7387 | 1572.8296 |
| 4.1614 | 1558.0905 | 1579.3119 | 1568.3514 |
| 4.1724 | 1583.3815 | 1574.8891 | 1563.8731 |
| 4.1834 | 1599.1593 | 1570.4703 | 1559.3948 |
| 4.1944 | 1554.6775 | 1566.0555 | 1554.9166 |

More items… (Bookmark 7)

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 21 Etosha22 HSsub 0.1-2.5cm glycol | 2.0054 | 29.9894 | 0.0110 | 12/13/2023 9:29:58 AM |

More items… (Bookmark 8)

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7132 | 1423.58 | 0.1948 | 32.53646 | 100.00 |
| 5.2958 | 294.22 | 0.3897 | 16.67389 | 20.67 |
| 7.0263 | 482.28 | 0.5628 | 12.57063 | 33.88 |
| 8.6850 | 569.58 | 0.0758 | 10.17321 | 40.01 |
| 15.7065 | 917.21 | 0.0866 | 5.63760 | 64.43 |
| 17.6140 | 61.88 | 0.1299 | 5.03114 | 4.35 |
| 18.1683 | 135.44 | 0.1082 | 4.87887 | 9.51 |
| 19.6769 | 29.63 | 0.6061 | 4.50808 | 2.08 |
| 22.4143 | 33.27 | 0.1299 | 3.96333 | 2.34 |
| 23.3307 | 27.21 | 0.2165 | 3.80968 | 1.91 |
| 24.1775 | 37.50 | 0.1299 | 3.67813 | 2.63 |
| 25.8579 | 783.89 | 0.0974 | 3.44279 | 55.06 |
| 26.6448 | 257.65 | 0.1732 | 3.34287 | 18.10 |
| 27.5007 | 283.66 | 0.1732 | 3.24075 | 19.93 |

More items… (Bookmark 9)

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-003-0649 | 51 | Tin Oxide | Sn O2 | Cassiterite | 2 |
| * | 04-016-2838 | 48 | Titanium Oxide | Ti O2 | Rutile | 6 |
| * | 04-017-4317 | 38 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 9 |
| * | 04-016-6876 | 28 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 3 |
| * | 04-012-1749 | 26 | Sodium Aluminum Silicon Oxide Hydrate | Na7.7 Al7.7 Si16.3 O48 ( H2 O )8 | Analcime | 10 |
| * | 00-042-1339 | 19 | Potassium Magnesium Aluminum Silicate Hydroxide | K Mg3 ( Si3 Al ) O10 ( O H )2 | Phlogopite-2M1 | 11 |
| * | 04-025-4215 | 22 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 37 |
| * | 04-013-2099 | 5 | Potassium Aluminum Silicate | K8 Al8 Si16 O48 | Leucite | 15 |
| * | 04-013-5979 | 16 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 8 |

More items… (Bookmark 10)

Dataset Name	21 Etosha22 HSsub 0.1-2.5cm glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 21\21 Etosha22 HSsub 0.1-2.5cm glycol.xrdml

Sample Identification	21 Etosha22 HSsub 0.1-2.5cm glycol

Measurement Start Date/Time	12/13/2023 9:29:58 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes

More items… (Bookmark 11)

More items… (Bookmark 12)

More items… (Bookmark 13)

More items… (Bookmark 14)

More items… (Bookmark 15)