23 Etosha 23 CRT 0-0.1 cm S5 REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Silicon Oxide

Weight fraction/ %	6.0

Phase Titanium Oxide

Weight fraction/ %	14.0

Phase Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	12.0

Phase Sodium Calcium Magnesium Aluminum Iron Titanium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	6.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	5.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	7.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	9.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	38.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Silicon Oxide | Titanium Oxide | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | Sodium Calcium Magnesium Aluminum Iron Titanium Aluminum Silicon Oxide Hydroxide Hydrate | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Silicon Oxide Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Potassium Aluminum Silicate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 23 Etosha22 crt 0-0.1cm S5 | 6.0 | 14.0 | 12.0 | 2.0 | 6.0 | 5.0 | 7.0 | 9.0 | 38.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8473.0000 | 8455.9447 | 8473.0000 |
| 2.0164 | 8444.2547 | 8428.0940 | 8411.4959 |
| 2.0274 | 8299.7965 | 8367.0689 | 8349.9919 |
| 2.0384 | 8134.6224 | 8306.0667 | 8288.4878 |
| 2.0494 | 8181.5723 | 8245.0886 | 8226.9838 |
| 2.0604 | 8255.7424 | 8184.1365 | 8165.4797 |
| 2.0714 | 8037.4838 | 8123.2119 | 8103.9756 |
| 2.0824 | 8021.9661 | 8062.3167 | 8042.4716 |
| 2.0934 | 7939.3727 | 8001.4530 | 7980.9675 |
| 2.1044 | 8028.7035 | 7940.6230 | 7919.4635 |
| 2.1154 | 7764.1957 | 7879.8292 | 7857.9594 |
| 2.1264 | 7787.5408 | 7819.0740 | 7796.4553 |
| 2.1374 | 7783.0354 | 7758.3604 | 7734.9513 |
| 2.1484 | 7724.8564 | 7697.6916 | 7673.4472 |
| 2.1594 | 7677.3471 | 7637.0709 | 7611.9431 |
| 2.1704 | 7720.0487 | 7576.5021 | 7550.4391 |
| 2.1814 | 7570.8328 | 7515.9894 | 7488.9350 |
| 2.1924 | 7627.5069 | 7455.4568 | 7427.4310 |
| 2.2034 | 7652.6106 | 7395.0016 | 7365.7777 |
| 2.2144 | 7555.7960 | 7334.5371 | 7304.1245 |
| 2.2254 | 7641.9764 | 7274.1498 | 7242.4713 |
| 2.2364 | 7576.6490 | 7213.8466 | 7180.8181 |
| 2.2474 | 7572.9961 | 7153.6350 | 7119.1649 |
| 2.2584 | 7397.3461 | 7093.5234 | 7057.5117 |
| 2.2694 | 7417.8083 | 7033.5213 | 6995.8584 |
| 2.2804 | 7442.6175 | 6973.6391 | 6934.2052 |
| 2.2914 | 7343.2763 | 6913.8890 | 6872.5520 |
| 2.3024 | 7370.8496 | 6854.2843 | 6810.8988 |
| 2.3134 | 7284.2144 | 6794.8408 | 6749.2456 |
| 2.3244 | 7280.9208 | 6735.5765 | 6687.5923 |
| 2.3354 | 7295.0059 | 6676.5127 | 6625.9391 |
| 2.3464 | 7230.4144 | 6617.6748 | 6564.2859 |
| 2.3574 | 7140.6116 | 6559.0940 | 6502.6327 |
| 2.3684 | 7184.2655 | 6500.8088 | 6440.9795 |
| 2.3794 | 7088.5103 | 6442.8682 | 6379.3263 |
| 2.3904 | 6979.3019 | 6385.3349 | 6317.6730 |
| 2.4014 | 6903.5841 | 6328.2908 | 6256.0198 |
| 2.4124 | 6882.8584 | 6271.8433 | 6194.3666 |
| 2.4234 | 6931.4916 | 6216.1330 | 6132.7134 |
| 2.4344 | 6851.9911 | 6161.3441 | 6071.0602 |
| 2.4454 | 6841.2576 | 6107.7156 | 6009.4069 |
| 2.4564 | 6894.8029 | 6055.5538 | 5947.7537 |
| 2.4674 | 6828.7227 | 6005.2449 | 5886.1005 |
| 2.4784 | 6763.7679 | 5957.2667 | 5824.4473 |
| 2.4894 | 6704.3078 | 5912.1968 | 5762.7941 |
| 2.5004 | 6633.4248 | 5870.7157 | 5701.1409 |
| 2.5114 | 6620.0383 | 5833.6017 | 5639.4876 |
| 2.5224 | 6456.2256 | 5801.7151 | 5577.8344 |
| 2.5334 | 6596.1475 | 5775.9692 | 5516.1812 |
| 2.5444 | 6573.0604 | 5757.2879 | 5454.5280 |
| 2.5554 | 6546.2449 | 5746.5474 | 5392.8748 |
| 2.5664 | 6534.5251 | 5744.4250 | 5331.2215 |
| 2.5774 | 6328.5772 | 5751.5700 | 5269.4192 |
| 2.5884 | 6291.4169 | 5768.1550 | 5207.6168 |
| 2.5994 | 6329.9558 | 5794.1350 | 5145.8144 |
| 2.6104 | 6418.1490 | 5828.8882 | 5084.0120 |
| 2.6214 | 6363.0147 | 5871.1768 | 5022.2097 |
| 2.6324 | 6275.8628 | 5919.0086 | 4960.4073 |
| 2.6434 | 6132.9587 | 5969.4776 | 4898.6049 |
| 2.6544 | 6090.9769 | 6018.6034 | 4836.8026 |
| 2.6654 | 6143.4100 | 6061.2390 | 4775.0002 |
| 2.6764 | 6152.0029 | 6091.1828 | 4713.1978 |
| 2.6874 | 5969.9193 | 6101.6712 | 4651.3954 |
| 2.6984 | 5884.5752 | 6086.3579 | 4589.5931 |
| 2.7094 | 5820.9361 | 6040.6314 | 4527.7907 |
| 2.7204 | 5638.2271 | 5962.8009 | 4465.9883 |
| 2.7314 | 5561.9292 | 5854.5734 | 4404.1859 |
| 2.7424 | 5335.7723 | 5720.5641 | 4342.3836 |
| 2.7534 | 5146.0796 | 5567.0102 | 4280.5812 |
| 2.7644 | 5050.1534 | 5400.7749 | 4218.5944 |
| 2.7754 | 4890.0157 | 5227.9350 | 4156.6077 |
| 2.7864 | 4762.1529 | 5053.7328 | 4094.6209 |
| 2.7974 | 4500.9823 | 4882.1495 | 4032.6342 |
| 2.8084 | 4338.8992 | 4716.0948 | 3970.6475 |
| 2.8194 | 4221.2222 | 4557.5646 | 3908.6607 |
| 2.8304 | 4023.8687 | 4407.8001 | 3846.6740 |
| 2.8414 | 4073.3884 | 4267.4259 | 3784.6872 |
| 2.8524 | 3943.6096 | 4136.5695 | 3722.7005 |
| 2.8634 | 3794.1121 | 4014.9675 | 3660.7137 |
| 2.8744 | 3734.5954 | 3902.0642 | 3598.7270 |
| 2.8854 | 3666.1367 | 3797.1026 | 3536.7403 |
| 2.8964 | 3460.9070 | 3699.2073 | 3474.7535 |
| 2.9074 | 3506.4346 | 3607.4550 | 3412.7668 |
| 2.9184 | 3308.5364 | 3520.9325 | 3350.7800 |
| 2.9294 | 3285.0265 | 3438.7797 | 3288.7933 |
| 2.9404 | 3249.7812 | 3375.5574 | 3226.8065 |
| 2.9514 | 3122.6460 | 3312.9876 | 3193.2394 |
| 2.9624 | 3209.8997 | 3268.0897 | 3159.6723 |
| 2.9734 | 3126.1229 | 3225.0469 | 3126.1051 |
| 2.9844 | 3094.2011 | 3183.4725 | 3092.5380 |
| 2.9954 | 2996.2655 | 3143.0600 | 3058.9709 |
| 3.0064 | 3042.1278 | 3103.5702 | 3025.4037 |
| 3.0174 | 2981.5841 | 3064.8186 | 2991.8366 |
| 3.0284 | 2916.7109 | 3026.6644 | 2958.2694 |
| 3.0394 | 2899.2714 | 2989.0000 | 2924.7023 |
| 3.0504 | 2854.8584 | 2951.7435 | 2891.1352 |
| 3.0614 | 2755.6932 | 2914.8320 | 2857.5680 |
| 3.0724 | 2829.8156 | 2878.2164 | 2824.0009 |
| 3.0834 | 2729.4562 | 2841.8582 | 2790.4337 |
| 3.0944 | 2670.0841 | 2805.7261 | 2756.8666 |
| 3.1054 | 2697.8270 | 2769.7947 | 2723.2995 |
| 3.1164 | 2749.2738 | 2734.0426 | 2689.7323 |
| 3.1274 | 2641.7492 | 2706.3859 | 2656.1652 |
| 3.1384 | 2597.3835 | 2677.7067 | 2637.2980 |
| 3.1494 | 2600.8082 | 2657.0937 | 2618.4308 |
| 3.1604 | 2559.9322 | 2636.6008 | 2599.5636 |
| 3.1714 | 2556.3599 | 2616.2174 | 2580.6964 |
| 3.1824 | 2565.3274 | 2595.9342 | 2561.8292 |
| 3.1934 | 2549.7257 | 2575.7428 | 2542.9620 |
| 3.2044 | 2519.2193 | 2555.6355 | 2524.0949 |
| 3.2154 | 2490.2488 | 2535.6056 | 2505.2277 |
| 3.2264 | 2531.4720 | 2515.6469 | 2486.3605 |
| 3.2374 | 2473.0570 | 2495.7540 | 2467.4933 |
| 3.2484 | 2388.2778 | 2475.9218 | 2448.6261 |
| 3.2594 | 2385.4100 | 2456.1457 | 2429.7589 |
| 3.2704 | 2300.9907 | 2436.4217 | 2410.8917 |
| 3.2814 | 2308.2075 | 2416.7459 | 2392.0245 |
| 3.2924 | 2309.0177 | 2397.1150 | 2373.1573 |
| 3.3034 | 2358.9744 | 2377.5258 | 2354.2902 |
| 3.3144 | 2369.7792 | 2357.9754 | 2335.4230 |
| 3.3254 | 2325.6018 | 2338.4613 | 2316.5558 |
| 3.3364 | 2298.3835 | 2318.9809 | 2297.6886 |
| 3.3474 | 2243.0393 | 2299.5322 | 2278.8214 |
| 3.3584 | 2168.1976 | 2280.1131 | 2259.9542 |
| 3.3694 | 2165.9214 | 2260.7216 | 2241.0870 |
| 3.3804 | 2159.6716 | 2241.3561 | 2222.2198 |
| 3.3914 | 2151.9469 | 2222.0150 | 2203.3526 |
| 3.4024 | 2192.9995 | 2202.6969 | 2184.4854 |
| 3.4134 | 2138.1966 | 2183.4002 | 2165.6183 |
| 3.4244 | 2125.5738 | 2164.1239 | 2146.7511 |
| 3.4354 | 2125.7060 | 2144.8666 | 2127.8839 |
| 3.4464 | 2063.2910 | 2125.6274 | 2109.0167 |
| 3.4574 | 2066.4985 | 2106.4052 | 2090.1495 |
| 3.4684 | 2071.0364 | 2087.1991 | 2071.2823 |
| 3.4794 | 2011.2399 | 2068.0082 | 2052.4151 |
| 3.4904 | 2069.3673 | 2048.8317 | 2033.5479 |
| 3.5014 | 1990.4287 | 2030.6959 | 2014.6807 |
| 3.5124 | 1995.6519 | 2012.4219 | 1997.7167 |
| 3.5234 | 1987.7109 | 1995.1873 | 1980.7526 |
| 3.5344 | 1952.5801 | 1977.9643 | 1963.7886 |
| 3.5454 | 1916.1701 | 1960.7524 | 1946.8245 |
| 3.5564 | 1883.7419 | 1943.5510 | 1929.8605 |
| 3.5674 | 1925.9371 | 1926.4309 | 1912.8964 |
| 3.5784 | 1947.5457 | 1909.3659 | 1895.9324 |
| 3.5894 | 1872.0088 | 1892.2315 | 1878.9683 |
| 3.6004 | 1858.3864 | 1875.1288 | 1862.0043 |
| 3.6114 | 1853.8496 | 1857.9766 | 1845.0402 |
| 3.6224 | 1780.1961 | 1840.8323 | 1828.0762 |
| 3.6334 | 1817.0590 | 1823.6956 | 1811.1121 |
| 3.6444 | 1806.5531 | 1806.5662 | 1794.1481 |
| 3.6554 | 1800.3127 | 1789.4437 | 1777.1840 |
| 3.6664 | 1711.8372 | 1772.3279 | 1760.2200 |
| 3.6774 | 1767.3275 | 1755.2185 | 1743.2559 |
| 3.6884 | 1699.6327 | 1742.7593 | 1726.2919 |
| 3.6994 | 1717.5703 | 1729.6222 | 1717.9323 |
| 3.7104 | 1759.9199 | 1721.1349 | 1709.5727 |
| 3.7214 | 1717.2124 | 1712.6530 | 1701.2131 |
| 3.7324 | 1739.0315 | 1704.1763 | 1692.8536 |
| 3.7434 | 1735.3481 | 1695.7046 | 1684.4940 |
| 3.7544 | 1649.1150 | 1687.2378 | 1676.1344 |
| 3.7654 | 1635.3343 | 1678.7756 | 1667.7748 |
| 3.7764 | 1643.8097 | 1670.3179 | 1659.4152 |
| 3.7874 | 1705.4513 | 1661.8645 | 1651.0557 |
| 3.7984 | 1608.2134 | 1653.4153 | 1642.6961 |
| 3.8094 | 1669.6696 | 1644.9702 | 1634.3365 |
| 3.8204 | 1648.5236 | 1636.5290 | 1625.9769 |
| 3.8314 | 1630.3874 | 1628.0915 | 1617.6173 |
| 3.8424 | 1593.8412 | 1619.6577 | 1609.2577 |
| 3.8534 | 1625.8967 | 1611.2274 | 1600.8982 |
| 3.8644 | 1608.6878 | 1602.8006 | 1592.5386 |
| 3.8754 | 1594.6106 | 1594.3771 | 1584.1790 |
| 3.8864 | 1605.7079 | 1585.9568 | 1575.8194 |
| 3.8974 | 1562.9921 | 1577.5397 | 1567.4598 |
| 3.9084 | 1583.5128 | 1569.1256 | 1559.1003 |
| 3.9194 | 1514.8820 | 1560.7145 | 1550.7407 |
| 3.9304 | 1531.6042 | 1552.3063 | 1542.3811 |
| 3.9414 | 1499.7935 | 1543.9009 | 1534.0215 |
| 3.9524 | 1536.3097 | 1535.4982 | 1525.6619 |
| 3.9634 | 1472.5634 | 1527.0982 | 1517.3024 |
| 3.9744 | 1472.7989 | 1518.7009 | 1508.9428 |
| 3.9854 | 1467.3982 | 1510.3061 | 1500.5832 |
| 3.9964 | 1461.1268 | 1501.9137 | 1492.2236 |
| 4.0074 | 1412.5880 | 1493.5239 | 1483.8640 |
| 4.0184 | 1462.2611 | 1485.1364 | 1475.5044 |
| 4.0294 | 1448.6460 | 1476.7512 | 1467.1449 |
| 4.0404 | 1439.8092 | 1468.3684 | 1458.7853 |
| 4.0514 | 1440.0089 | 1459.9878 | 1450.4257 |
| 4.0624 | 1450.2252 | 1451.6544 | 1442.0661 |
| 4.0734 | 1439.3107 | 1443.3081 | 1433.7813 |
| 4.0844 | 1423.5265 | 1435.0089 | 1425.4965 |
| 4.0954 | 1398.0531 | 1426.7118 | 1417.2118 |
| 4.1064 | 1395.8397 | 1418.4168 | 1408.9270 |
| 4.1174 | 1387.5104 | 1410.1238 | 1400.6422 |
| 4.1284 | 1414.3200 | 1401.8329 | 1392.3574 |
| 4.1394 | 1362.1573 | 1393.5440 | 1384.0726 |
| 4.1504 | 1350.3805 | 1385.2571 | 1375.7878 |
| 4.1614 | 1369.5438 | 1376.9721 | 1367.5030 |
| 4.1724 | 1345.2315 | 1368.6891 | 1359.2182 |
| 4.1834 | 1327.8319 | 1360.4081 | 1350.9334 |
| 4.1944 | 1371.6091 | 1352.1290 | 1342.6486 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 23 Etosha22 crt 0-0.1cm S5 | 2.0054 | 29.9894 | 0.0110 | 12/12/2023 10:18:32 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7072 | 1349.67 | 0.1948 | 32.60844 | 100.00 |
| 5.3056 | 199.29 | 0.1732 | 16.64290 | 14.77 |
| 7.0819 | 902.64 | 0.6061 | 12.47199 | 66.88 |
| 8.7175 | 228.42 | 0.1732 | 10.13532 | 16.92 |
| 13.5184 | 21.07 | 0.1732 | 6.54477 | 1.56 |
| 15.7192 | 239.86 | 0.0974 | 5.63305 | 17.77 |
| 17.6906 | 14.67 | 0.6927 | 5.00953 | 1.09 |
| 19.5849 | 16.31 | 0.5196 | 4.52904 | 1.21 |
| 25.8862 | 191.64 | 0.0758 | 3.43909 | 14.20 |
| 26.6506 | 210.86 | 0.1515 | 3.34216 | 15.62 |
| 27.4573 | 481.95 | 0.1732 | 3.24577 | 35.71 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-070-7345 | 40 | Silicon Oxide | Si O2 | Quartz | 6 |
| * | 04-008-7810 | 56 | Titanium Oxide | Ti O2 | Rutile | 14 |
| * | 04-016-0693 | 38 | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | K0.3 Na0.4 Ca0.3 Mn3.9 Fe0.1 Al1.4 Si5.3 O16 ( O H )2.7 ( H2 O )3.5 | Ganophyllite | 12 |
| * | 01-078-4316 | 15 | Sodium Calcium Magnesium Aluminum Iron Titanium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2.46 Al0.3 Fe0.22 Ti0.021 )2 ( Mg0.38 Ca0.03 Na0.02 )2 ( ( Si2.83 Al1.17 ) O10 )2 ( O H )4 ( H2 O )3.4 | Vermiculite | 2 |
| * | 04-017-4317 | 21 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 6 |
| * | 01-080-5781 | 13 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ( H2 O )3.92 ) ( H2 O )7.72 | Sepiolite | 5 |
| * | 04-011-6756 | 20 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 7 |
| * | 04-013-2099 | 17 | Potassium Aluminum Silicate | K8 Al8 Si16 O48 | Leucite | 9 |
| * | 04-025-4215 | 22 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 38 |

Anchor Scan Parameters

Dataset Name	23 Etosha22 crt 0-0.1cm S5

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 23\23 Etosha22 crt 0-0.1cm S5.xrdml

Sample Identification	23 Etosha22 crt 0-0.1cm S5

Measurement Start Date/Time	12/12/2023 10:18:32 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes