24 Etosha 22 sub 0.1-5 cm S5 400 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	9.0

Phase Titanium Oxide

Weight fraction/ %	3.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	18.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	28.0

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	7.0

Phase Magnesium Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	13.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	22.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Magnesium Aluminum Silicate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 24 Etosha22 sub 0.1-5cm S5 400C | 9.0 | 3.0 | 18.0 | 28.0 | 7.0 | 13.0 | 22.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8394.0000 | 8389.0066 | 8394.0000 |
| 2.0164 | 8082.3564 | 8352.9825 | 8332.4737 |
| 2.0274 | 8111.7129 | 8292.1031 | 8270.9473 |
| 2.0384 | 8136.3864 | 8231.2544 | 8209.4210 |
| 2.0494 | 8030.8889 | 8170.4384 | 8147.8946 |
| 2.0604 | 7810.4076 | 8109.6573 | 8086.3683 |
| 2.0714 | 7742.2566 | 8048.9134 | 8024.8419 |
| 2.0824 | 7937.4046 | 7988.2090 | 7963.3156 |
| 2.0934 | 7713.1131 | 7927.5470 | 7901.7892 |
| 2.1044 | 7759.6681 | 7866.9301 | 7840.2629 |
| 2.1154 | 7753.5585 | 7806.3616 | 7778.7365 |
| 2.1264 | 7713.1814 | 7745.8450 | 7717.2102 |
| 2.1374 | 7605.0678 | 7685.3839 | 7655.6838 |
| 2.1484 | 7567.7163 | 7624.9825 | 7594.1575 |
| 2.1594 | 7564.9646 | 7564.6453 | 7532.6311 |
| 2.1704 | 7523.5605 | 7504.3771 | 7471.1048 |
| 2.1814 | 7672.7148 | 7444.1835 | 7409.5784 |
| 2.1924 | 7564.2532 | 7384.0038 | 7348.0521 |
| 2.2034 | 7600.5398 | 7323.8799 | 7286.3615 |
| 2.2144 | 7487.8687 | 7263.7840 | 7224.6709 |
| 2.2254 | 7333.3058 | 7203.7909 | 7162.9803 |
| 2.2364 | 7240.7434 | 7143.9099 | 7101.2897 |
| 2.2474 | 7295.7188 | 7084.1517 | 7039.5991 |
| 2.2584 | 7315.5880 | 7024.5286 | 6977.9085 |
| 2.2694 | 7147.3097 | 6965.0551 | 6916.2179 |
| 2.2804 | 7189.4985 | 6905.7483 | 6854.5273 |
| 2.2914 | 7263.9892 | 6846.6286 | 6792.8367 |
| 2.3024 | 7245.4911 | 6787.7209 | 6731.1461 |
| 2.3134 | 7155.0718 | 6729.0556 | 6669.4556 |
| 2.3244 | 7088.7026 | 6670.6704 | 6607.7650 |
| 2.3354 | 7049.8555 | 6612.6124 | 6546.0744 |
| 2.3464 | 7072.8088 | 6554.9401 | 6484.3838 |
| 2.3574 | 6980.6509 | 6497.7268 | 6422.6932 |
| 2.3684 | 6903.3510 | 6441.0640 | 6361.0026 |
| 2.3794 | 6935.7778 | 6385.0112 | 6299.3120 |
| 2.3904 | 6928.9356 | 6329.7362 | 6237.4885 |
| 2.4014 | 6944.1681 | 6275.3808 | 6175.6650 |
| 2.4124 | 6824.9803 | 6222.2038 | 6113.8416 |
| 2.4234 | 6816.2330 | 6170.4491 | 6052.0181 |
| 2.4344 | 6795.3289 | 6120.4024 | 5990.1946 |
| 2.4454 | 6776.6057 | 6072.3929 | 5928.3711 |
| 2.4564 | 6809.8348 | 6026.7926 | 5866.5477 |
| 2.4674 | 6685.7551 | 5984.0136 | 5804.7242 |
| 2.4784 | 6652.9504 | 5944.5010 | 5742.9007 |
| 2.4894 | 6686.2045 | 5908.7237 | 5681.0773 |
| 2.5004 | 6644.4292 | 5877.1592 | 5619.2538 |
| 2.5114 | 6607.2114 | 5850.2761 | 5557.4303 |
| 2.5224 | 6556.7615 | 5828.5111 | 5495.6068 |
| 2.5334 | 6522.7404 | 5812.2437 | 5433.7834 |
| 2.5444 | 6491.7050 | 5801.7665 | 5371.9599 |
| 2.5554 | 6457.1780 | 5797.2545 | 5310.1364 |
| 2.5664 | 6449.7611 | 5798.7315 | 5248.3129 |
| 2.5774 | 6428.9911 | 5806.0348 | 5186.4895 |
| 2.5884 | 6348.9031 | 5818.7773 | 5124.6660 |
| 2.5994 | 6281.8053 | 5836.3051 | 5062.8425 |
| 2.6104 | 6304.5325 | 5857.6497 | 5001.0190 |
| 2.6214 | 6236.9626 | 5881.4730 | 4939.1956 |
| 2.6324 | 6120.2345 | 5906.0100 | 4877.3721 |
| 2.6434 | 6048.5044 | 5929.0178 | 4815.5486 |
| 2.6544 | 6053.3048 | 5947.7566 | 4753.7252 |
| 2.6654 | 6131.7965 | 5959.0380 | 4691.9017 |
| 2.6764 | 6085.7733 | 5959.3860 | 4630.0782 |
| 2.6874 | 5881.3953 | 5945.3398 | 4568.2547 |
| 2.6984 | 5794.0265 | 5913.8863 | 4506.4313 |
| 2.7094 | 5587.5565 | 5862.9367 | 4444.6078 |
| 2.7204 | 5562.7611 | 5791.7105 | 4382.7843 |
| 2.7314 | 5479.1445 | 5700.8898 | 4320.9608 |
| 2.7424 | 5338.5924 | 5592.4820 | 4259.1374 |
| 2.7534 | 5207.6902 | 5469.3942 | 4197.3139 |
| 2.7644 | 5064.0280 | 5335.0943 | 4135.3575 |
| 2.7754 | 4777.0049 | 5193.0362 | 4073.4012 |
| 2.7864 | 4599.6096 | 5046.4861 | 4011.4448 |
| 2.7974 | 4526.0177 | 4898.2176 | 3949.4885 |
| 2.8084 | 4424.7891 | 4750.5091 | 3887.5321 |
| 2.8194 | 4228.4542 | 4605.1597 | 3825.5758 |
| 2.8304 | 3909.4837 | 4463.5377 | 3763.6194 |
| 2.8414 | 3979.2803 | 4326.6377 | 3701.6631 |
| 2.8524 | 3753.1829 | 4195.1357 | 3639.7067 |
| 2.8634 | 3700.6932 | 4069.4378 | 3577.7504 |
| 2.8744 | 3566.9449 | 3949.7223 | 3515.7940 |
| 2.8854 | 3458.7719 | 3835.9784 | 3453.8377 |
| 2.8964 | 3519.7212 | 3728.0413 | 3391.8813 |
| 2.9074 | 3295.2203 | 3625.6261 | 3329.9250 |
| 2.9184 | 3322.1534 | 3528.3592 | 3267.9686 |
| 2.9294 | 3276.2950 | 3435.8072 | 3206.0123 |
| 2.9404 | 3130.0944 | 3360.7366 | 3144.0559 |
| 2.9514 | 3008.7335 | 3295.6893 | 3114.8190 |
| 2.9624 | 3075.1460 | 3247.1762 | 3085.5821 |
| 2.9734 | 2919.4277 | 3201.5166 | 3056.3452 |
| 2.9844 | 2957.7183 | 3158.2959 | 3027.1083 |
| 2.9954 | 2956.2743 | 3117.1389 | 2997.8713 |
| 3.0064 | 2964.5118 | 3077.7133 | 2968.6344 |
| 3.0174 | 2933.7070 | 3039.7301 | 2939.3975 |
| 3.0284 | 2817.2345 | 3002.9425 | 2910.1606 |
| 3.0394 | 2634.6342 | 2967.1425 | 2880.9237 |
| 3.0504 | 2771.4852 | 2932.1577 | 2851.6868 |
| 3.0614 | 2757.7404 | 2897.8463 | 2822.4499 |
| 3.0724 | 2730.0855 | 2864.0932 | 2793.2129 |
| 3.0834 | 2669.4966 | 2830.8055 | 2763.9760 |
| 3.0944 | 2772.2699 | 2797.9086 | 2734.7391 |
| 3.1054 | 2703.2911 | 2765.3430 | 2705.5022 |
| 3.1164 | 2697.2404 | 2733.0607 | 2676.2653 |
| 3.1274 | 2632.4366 | 2706.0777 | 2647.0284 |
| 3.1384 | 2585.2247 | 2681.6967 | 2630.2876 |
| 3.1494 | 2618.0344 | 2662.5587 | 2613.5469 |
| 3.1604 | 2566.9513 | 2643.5888 | 2596.8062 |
| 3.1714 | 2536.4740 | 2624.7697 | 2580.0654 |
| 3.1824 | 2525.7409 | 2606.0867 | 2563.3247 |
| 3.1934 | 2431.6106 | 2587.5275 | 2546.5839 |
| 3.2044 | 2485.5123 | 2569.0811 | 2529.8432 |
| 3.2154 | 2468.0944 | 2550.7382 | 2513.1025 |
| 3.2264 | 2403.0929 | 2532.4903 | 2496.3617 |
| 3.2374 | 2392.1957 | 2514.3301 | 2479.6210 |
| 3.2484 | 2364.3889 | 2496.2507 | 2462.8803 |
| 3.2594 | 2354.4012 | 2478.3167 | 2446.1395 |
| 3.2704 | 2375.2601 | 2461.6831 | 2429.3988 |
| 3.2814 | 2389.5241 | 2443.8557 | 2412.6580 |
| 3.2924 | 2355.9823 | 2426.7052 | 2395.9173 |
| 3.3034 | 2362.3186 | 2408.9625 | 2379.1766 |
| 3.3144 | 2389.6868 | 2392.6369 | 2362.4358 |
| 3.3254 | 2339.9823 | 2377.0048 | 2349.0697 |
| 3.3364 | 2326.4902 | 2362.7832 | 2335.7036 |
| 3.3474 | 2347.0197 | 2348.6042 | 2322.3375 |
| 3.3584 | 2311.1342 | 2334.4651 | 2308.9714 |
| 3.3694 | 2297.5723 | 2320.3635 | 2295.6054 |
| 3.3804 | 2266.8171 | 2306.2969 | 2282.2393 |
| 3.3914 | 2239.5487 | 2292.2634 | 2268.8732 |
| 3.4024 | 2256.8289 | 2278.2609 | 2255.5071 |
| 3.4134 | 2210.9547 | 2264.2875 | 2242.1410 |
| 3.4244 | 2205.6460 | 2250.3417 | 2228.7749 |
| 3.4354 | 2191.7492 | 2236.4218 | 2215.4088 |
| 3.4464 | 2170.7114 | 2222.5263 | 2202.0427 |
| 3.4574 | 2187.4484 | 2208.6540 | 2188.6766 |
| 3.4684 | 2175.9587 | 2194.8035 | 2175.3105 |
| 3.4794 | 2184.4100 | 2180.9736 | 2161.9444 |
| 3.4904 | 2144.8938 | 2167.1633 | 2148.5783 |
| 3.5014 | 2090.1219 | 2154.5807 | 2135.2122 |
| 3.5124 | 2140.9681 | 2142.5869 | 2124.8357 |
| 3.5234 | 2143.8495 | 2131.8189 | 2114.4592 |
| 3.5344 | 2151.8368 | 2121.0667 | 2104.0827 |
| 3.5454 | 2070.6273 | 2110.3296 | 2093.7062 |
| 3.5564 | 2045.5295 | 2099.6067 | 2083.3297 |
| 3.5674 | 2036.3294 | 2088.8974 | 2072.9532 |
| 3.5784 | 2090.3368 | 2078.2010 | 2062.5767 |
| 3.5894 | 2048.1770 | 2067.5169 | 2052.2002 |
| 3.6004 | 2016.7026 | 2056.8446 | 2041.8237 |
| 3.6114 | 2028.0954 | 2046.1834 | 2031.4472 |
| 3.6224 | 2049.7493 | 2035.5329 | 2021.0707 |
| 3.6334 | 1995.8456 | 2024.8926 | 2010.6942 |
| 3.6444 | 2021.2429 | 2014.2621 | 2000.3177 |
| 3.6554 | 1942.9469 | 2003.6408 | 1989.9412 |
| 3.6664 | 1982.6367 | 1993.0284 | 1979.5647 |
| 3.6774 | 1976.3717 | 1982.4246 | 1969.1882 |
| 3.6884 | 1931.7345 | 1973.7483 | 1958.8117 |
| 3.6994 | 1969.7483 | 1965.9867 | 1953.1809 |
| 3.7104 | 1963.2335 | 1960.1521 | 1947.5501 |
| 3.7214 | 1930.8082 | 1954.3246 | 1941.9194 |
| 3.7324 | 1966.1175 | 1948.5040 | 1936.2886 |
| 3.7434 | 1905.8869 | 1942.6900 | 1930.6578 |
| 3.7544 | 1964.9823 | 1936.8823 | 1925.0271 |
| 3.7654 | 1865.5437 | 1931.0807 | 1919.3963 |
| 3.7764 | 1950.0974 | 1925.2850 | 1913.7656 |
| 3.7874 | 1895.5044 | 1919.4949 | 1908.1348 |
| 3.7984 | 1899.2960 | 1913.7103 | 1902.5040 |
| 3.8094 | 1983.3638 | 1907.9309 | 1896.8733 |
| 3.8204 | 1880.0752 | 1902.1565 | 1891.2425 |
| 3.8314 | 1851.3865 | 1896.3869 | 1885.6117 |
| 3.8424 | 1927.2129 | 1890.6220 | 1879.9810 |
| 3.8534 | 1841.7788 | 1884.8616 | 1874.3502 |
| 3.8644 | 1857.0138 | 1879.1056 | 1868.7194 |
| 3.8754 | 1896.3205 | 1873.5053 | 1863.0887 |
| 3.8864 | 1816.5487 | 1867.9807 | 1857.8328 |
| 3.8974 | 1891.4297 | 1862.6117 | 1852.5768 |
| 3.9084 | 1883.5885 | 1857.2464 | 1847.3209 |
| 3.9194 | 1853.8997 | 1851.8848 | 1842.0650 |
| 3.9304 | 1819.1696 | 1846.5267 | 1836.8091 |
| 3.9414 | 1844.8348 | 1841.1721 | 1831.5532 |
| 3.9524 | 1879.9100 | 1835.8207 | 1826.2973 |
| 3.9634 | 1865.5782 | 1830.4726 | 1821.0413 |
| 3.9744 | 1872.3829 | 1825.1275 | 1815.7854 |
| 3.9854 | 1742.7080 | 1819.7855 | 1810.5295 |
| 3.9964 | 1801.2876 | 1814.4464 | 1805.2736 |
| 4.0074 | 1878.7296 | 1809.1102 | 1800.0177 |
| 4.0184 | 1816.0590 | 1803.7767 | 1794.7618 |
| 4.0294 | 1759.9233 | 1798.4458 | 1789.5058 |
| 4.0404 | 1791.8122 | 1793.1176 | 1784.2499 |
| 4.0514 | 1822.9646 | 1787.7919 | 1778.9940 |
| 4.0624 | 1768.9685 | 1783.4738 | 1773.7381 |
| 4.0734 | 1756.5890 | 1779.6331 | 1770.9675 |
| 4.0844 | 1721.9027 | 1776.7998 | 1768.1969 |
| 4.0954 | 1790.4415 | 1773.9688 | 1765.4263 |
| 4.1064 | 1795.3692 | 1771.1400 | 1762.6557 |
| 4.1174 | 1729.5221 | 1768.3134 | 1759.8851 |
| 4.1284 | 1724.6991 | 1765.4888 | 1757.1144 |
| 4.1394 | 1736.0000 | 1762.6663 | 1754.3438 |
| 4.1504 | 1772.5015 | 1759.8458 | 1751.5732 |
| 4.1614 | 1797.3215 | 1757.0272 | 1748.8026 |
| 4.1724 | 1777.4376 | 1754.2106 | 1746.0320 |
| 4.1834 | 1786.2832 | 1751.3957 | 1743.2614 |
| 4.1944 | 1780.7552 | 1748.5827 | 1740.4908 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 24 Etosha22 sub 0.1-5cm S5 400C | 2.0054 | 29.9894 | 0.0110 | 12/12/2023 1:09:39 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7076 | 1266.86 | 0.2381 | 32.60371 | 73.20 |
| 7.1660 | 1458.93 | 0.3897 | 12.32597 | 84.30 |
| 8.6964 | 1730.73 | 0.1948 | 10.15987 | 100.00 |
| 13.1938 | 24.59 | 0.6927 | 6.70506 | 1.42 |
| 15.7291 | 873.95 | 0.1407 | 5.62955 | 50.50 |
| 17.5710 | 128.71 | 0.2165 | 5.04336 | 7.44 |
| 18.2339 | 125.13 | 0.0649 | 4.86146 | 7.23 |
| 19.5158 | 33.22 | 0.3464 | 4.54493 | 1.92 |
| 22.3747 | 36.81 | 0.1732 | 3.97024 | 2.13 |
| 23.3551 | 27.58 | 0.1299 | 3.80575 | 1.59 |
| 24.1938 | 43.21 | 0.2598 | 3.67569 | 2.50 |
| 25.9178 | 560.13 | 0.1299 | 3.43497 | 32.36 |
| 26.6472 | 401.66 | 0.2381 | 3.34258 | 23.21 |
| 27.4844 | 242.41 | 0.1299 | 3.24264 | 14.01 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-072-4625 | 49 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 9 |
| * | 04-008-7810 | 51 | Titanium Oxide | Ti O2 | Rutile | 3 |
| * | 04-017-4317 | 45 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 18 |
| * | 04-014-4592 | 23 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.923 Na0.066 Mg1.488 Ti0.208 Fe1.148 Al1.443 Si2.715 O10.282 ( O H )1.421 F0.297 | Phlogopite-1M, Fe+2-bearing | 28 |
| * | 04-016-6876 | 29 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 7 |
| * | 00-034-0166 | 5 | Magnesium Aluminum Silicate Hydroxide Hydrate | ( Mg , Al )3 ( Si , Al )4 O10 ( O H )2 ·4 H2 O | Vermiculite-2M | 13 |
| * | 04-025-4215 | 23 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 22 |

Anchor Scan Parameters

Dataset Name	24 Etosha22 sub 0.1-5cm S5 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 24\24 Etosha22 sub 0.1-5cm S5 400C.xrdml

Sample Identification	24 Etosha22 sub 0.1-5cm S5 400C

Measurement Start Date/Time	12/12/2023 1:09:39 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes