24 Etosha 22 sub 0.1-5 cm S5 550 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	37.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	10.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Deuterate Hydrate

Weight fraction/ %	28.0

Phase Potassium Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Fluoride Hydroxide

Weight fraction/ %	10.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	15.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Sodium Aluminum Silicate Hydrate | Magnesium Aluminum Silicon Oxide Hydroxide Deuterate Hydrate | Magnesium Aluminum Iron Aluminum Silicate Hydroxide Hydrate | Potassium Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Fluoride Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- |
| 24 Etosha22 sub 0.1-5cm S5 550C | 37.0 | 10.0 | 28.0 | 0.0 | 10.0 | 15.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7758.0000 | 7748.4371 | 7758.0000 |
| 2.0164 | 7749.9464 | 7708.4407 | 7705.6280 |
| 2.0274 | 7825.5575 | 7656.1643 | 7653.2560 |
| 2.0384 | 7805.0870 | 7603.8929 | 7600.8840 |
| 2.0494 | 7723.2970 | 7551.6268 | 7548.5120 |
| 2.0604 | 7605.5639 | 7499.3664 | 7496.1400 |
| 2.0714 | 7495.0973 | 7447.1121 | 7443.7681 |
| 2.0824 | 7538.8181 | 7394.8643 | 7391.3961 |
| 2.0934 | 7568.4661 | 7342.6236 | 7339.0241 |
| 2.1044 | 7362.3717 | 7290.3904 | 7286.6521 |
| 2.1154 | 7296.5644 | 7238.1654 | 7234.2801 |
| 2.1264 | 7315.7807 | 7185.9493 | 7181.9081 |
| 2.1374 | 7284.4071 | 7133.7427 | 7129.5361 |
| 2.1484 | 7325.6499 | 7081.5464 | 7077.1641 |
| 2.1594 | 7279.7729 | 7029.3614 | 7024.7921 |
| 2.1704 | 7239.1003 | 6977.1885 | 6972.4201 |
| 2.1814 | 7214.5733 | 6925.0289 | 6920.0481 |
| 2.1924 | 7216.6121 | 6872.8511 | 6867.6761 |
| 2.2034 | 7186.7257 | 6820.6149 | 6815.1645 |
| 2.2144 | 7159.8501 | 6768.3633 | 6762.6529 |
| 2.2254 | 7148.3038 | 6716.1307 | 6710.1412 |
| 2.2364 | 6960.4926 | 6663.9190 | 6657.6296 |
| 2.2474 | 7071.8525 | 6611.7303 | 6605.1179 |
| 2.2584 | 6946.8958 | 6559.5671 | 6552.6063 |
| 2.2694 | 6841.2330 | 6507.4320 | 6500.0946 |
| 2.2804 | 6940.8383 | 6455.3283 | 6447.5830 |
| 2.2914 | 6907.3432 | 6403.2593 | 6395.0713 |
| 2.3024 | 6779.4602 | 6351.2293 | 6342.5597 |
| 2.3134 | 6715.4612 | 6299.2428 | 6290.0480 |
| 2.3244 | 6706.9208 | 6247.3053 | 6237.5364 |
| 2.3354 | 6687.8201 | 6195.4230 | 6185.0247 |
| 2.3464 | 6671.1957 | 6143.6032 | 6132.5131 |
| 2.3574 | 6643.4503 | 6091.8543 | 6080.0015 |
| 2.3684 | 6567.7212 | 6040.1865 | 6027.4898 |
| 2.3794 | 6575.3599 | 5988.6113 | 5974.9782 |
| 2.3904 | 6564.9243 | 5937.1430 | 5922.4665 |
| 2.4014 | 6589.8849 | 5885.7981 | 5869.9549 |
| 2.4124 | 6548.0098 | 5834.5968 | 5817.4432 |
| 2.4234 | 6473.9174 | 5783.5633 | 5764.9316 |
| 2.4344 | 6369.6696 | 5732.7274 | 5712.4199 |
| 2.4454 | 6357.8427 | 5682.1254 | 5659.9083 |
| 2.4564 | 6372.7793 | 5631.8024 | 5607.3966 |
| 2.4674 | 6365.1534 | 5581.8145 | 5554.8850 |
| 2.4784 | 6326.5855 | 5532.2329 | 5502.3733 |
| 2.4894 | 6228.4916 | 5483.1488 | 5449.8617 |
| 2.5004 | 6256.2788 | 5434.6815 | 5397.3501 |
| 2.5114 | 6232.2261 | 5386.9944 | 5344.8384 |
| 2.5224 | 6198.3019 | 5340.3258 | 5292.3268 |
| 2.5334 | 6191.3923 | 5295.0557 | 5239.8151 |
| 2.5444 | 6066.8540 | 5251.8442 | 5187.3035 |
| 2.5554 | 6021.3638 | 5211.8912 | 5134.7918 |
| 2.5664 | 5997.1504 | 5177.3274 | 5082.2802 |
| 2.5774 | 5948.8781 | 5151.7929 | 5029.6289 |
| 2.5884 | 5908.2458 | 5141.0149 | 4976.9776 |
| 2.5994 | 5942.1239 | 5152.7098 | 4924.3263 |
| 2.6104 | 5915.9754 | 5195.5840 | 4871.6750 |
| 2.6214 | 5766.0413 | 5276.6291 | 4819.0237 |
| 2.6324 | 5803.5797 | 5397.5720 | 4766.3724 |
| 2.6434 | 5779.1278 | 5549.8923 | 4713.7211 |
| 2.6544 | 5763.8776 | 5708.4582 | 4661.0698 |
| 2.6654 | 5731.8643 | 5826.3174 | 4608.4185 |
| 2.6764 | 5664.2679 | 5845.2799 | 4555.7672 |
| 2.6874 | 5452.4405 | 5735.1208 | 4503.1159 |
| 2.6984 | 5440.7832 | 5521.4472 | 4450.4646 |
| 2.7094 | 5302.3943 | 5260.5949 | 4397.8133 |
| 2.7204 | 5241.0270 | 5001.0624 | 4345.1620 |
| 2.7314 | 5016.9734 | 4770.4592 | 4292.5107 |
| 2.7424 | 4888.5909 | 4579.1785 | 4239.8594 |
| 2.7534 | 4785.9135 | 4426.5178 | 4187.2081 |
| 2.7644 | 4778.3289 | 4305.8259 | 4134.3841 |
| 2.7754 | 4699.1249 | 4208.6078 | 4081.5602 |
| 2.7864 | 4531.5383 | 4127.0596 | 4028.7363 |
| 2.7974 | 4411.6549 | 4055.2478 | 3975.9124 |
| 2.8084 | 4349.6514 | 3989.2615 | 3923.0885 |
| 2.8194 | 4144.8112 | 3926.7698 | 3870.2645 |
| 2.8304 | 4016.2242 | 3866.4683 | 3817.4406 |
| 2.8414 | 4049.9695 | 3807.6386 | 3764.6167 |
| 2.8524 | 3926.1809 | 3749.8706 | 3711.7928 |
| 2.8634 | 3776.1534 | 3692.9103 | 3658.9688 |
| 2.8744 | 3688.4366 | 3636.5862 | 3606.1449 |
| 2.8854 | 3599.4710 | 3580.7736 | 3553.3210 |
| 2.8964 | 3575.1018 | 3525.3782 | 3500.4971 |
| 2.9074 | 3408.2360 | 3470.3265 | 3447.6732 |
| 2.9184 | 3436.9720 | 3415.5605 | 3394.8492 |
| 2.9294 | 3381.0944 | 3361.0339 | 3342.0253 |
| 2.9404 | 3209.4740 | 3312.1325 | 3289.2014 |
| 2.9514 | 3297.7001 | 3275.6769 | 3259.4984 |
| 2.9624 | 3171.0383 | 3244.7912 | 3229.7954 |
| 2.9734 | 3092.5506 | 3214.0315 | 3200.0924 |
| 2.9844 | 3100.4218 | 3183.3805 | 3170.3894 |
| 2.9954 | 3009.5929 | 3152.8241 | 3140.6864 |
| 3.0064 | 3013.0472 | 3122.3500 | 3110.9835 |
| 3.0174 | 2934.1613 | 3091.9482 | 3081.2805 |
| 3.0284 | 2907.5797 | 3061.6100 | 3051.5775 |
| 3.0394 | 2932.9213 | 3031.3279 | 3021.8745 |
| 3.0504 | 2882.1263 | 3001.0955 | 2992.1715 |
| 3.0614 | 2874.6313 | 2970.9074 | 2962.4685 |
| 3.0724 | 2957.5536 | 2940.7588 | 2932.7655 |
| 3.0834 | 2811.5438 | 2910.6456 | 2903.0625 |
| 3.0944 | 2859.8584 | 2880.5641 | 2873.3596 |
| 3.1054 | 2837.3068 | 2850.5112 | 2843.6566 |
| 3.1164 | 2872.7905 | 2820.4842 | 2813.9536 |
| 3.1274 | 2756.2094 | 2794.1096 | 2784.2506 |
| 3.1384 | 2734.7011 | 2775.9700 | 2770.0196 |
| 3.1494 | 2728.8879 | 2761.4787 | 2755.7886 |
| 3.1604 | 2785.1740 | 2747.0051 | 2741.5576 |
| 3.1714 | 2734.8741 | 2732.5474 | 2727.3266 |
| 3.1824 | 2756.7817 | 2718.1045 | 2713.0956 |
| 3.1934 | 2784.6460 | 2703.6750 | 2698.8646 |
| 3.2044 | 2762.4906 | 2689.2579 | 2684.6336 |
| 3.2154 | 2649.8004 | 2674.8521 | 2670.4026 |
| 3.2264 | 2642.6844 | 2660.4569 | 2656.1716 |
| 3.2374 | 2596.3510 | 2646.0713 | 2641.9406 |
| 3.2484 | 2596.3333 | 2631.6948 | 2627.7096 |
| 3.2594 | 2620.2271 | 2617.3265 | 2613.4786 |
| 3.2704 | 2592.6529 | 2602.9659 | 2599.2476 |
| 3.2814 | 2537.8319 | 2588.6124 | 2585.0166 |
| 3.2924 | 2543.8761 | 2574.2656 | 2570.7856 |
| 3.3034 | 2548.1524 | 2559.9250 | 2556.5546 |
| 3.3144 | 2555.7011 | 2547.0357 | 2542.3236 |
| 3.3254 | 2539.5782 | 2537.4232 | 2534.2550 |
| 3.3364 | 2525.2827 | 2529.2613 | 2526.1864 |
| 3.3474 | 2500.5329 | 2521.1041 | 2518.1179 |
| 3.3584 | 2521.7626 | 2512.9513 | 2510.0493 |
| 3.3694 | 2535.2173 | 2504.8027 | 2501.9807 |
| 3.3804 | 2504.8274 | 2496.6579 | 2493.9121 |
| 3.3914 | 2552.8938 | 2488.5169 | 2485.8436 |
| 3.4024 | 2564.8786 | 2480.3793 | 2477.7750 |
| 3.4134 | 2488.1013 | 2472.2450 | 2469.7064 |
| 3.4244 | 2420.4071 | 2464.1137 | 2461.6378 |
| 3.4354 | 2420.9351 | 2455.9854 | 2453.5693 |
| 3.4464 | 2451.9140 | 2447.8598 | 2445.5007 |
| 3.4574 | 2460.2655 | 2439.7368 | 2437.4321 |
| 3.4684 | 2466.8859 | 2431.6162 | 2429.3635 |
| 3.4794 | 2450.6490 | 2423.4980 | 2421.2950 |
| 3.4904 | 2419.2212 | 2415.3820 | 2413.2264 |
| 3.5014 | 2470.7857 | 2407.2681 | 2405.1578 |
| 3.5124 | 2413.4641 | 2399.1562 | 2397.0892 |
| 3.5234 | 2392.4926 | 2391.0461 | 2389.0207 |
| 3.5344 | 2418.0030 | 2382.9379 | 2380.9521 |
| 3.5454 | 2393.2871 | 2373.9328 | 2372.8835 |
| 3.5564 | 2355.3436 | 2365.2264 | 2364.8149 |
| 3.5674 | 2378.0492 | 2357.0714 | 2356.7464 |
| 3.5784 | 2299.6008 | 2349.0072 | 2348.6778 |
| 3.5894 | 2341.0620 | 2340.9431 | 2340.6092 |
| 3.6004 | 2370.6042 | 2332.8790 | 2332.5406 |
| 3.6114 | 2350.7542 | 2324.8151 | 2324.4721 |
| 3.6224 | 2379.6918 | 2316.7513 | 2316.4035 |
| 3.6334 | 2282.3392 | 2308.6876 | 2308.3349 |
| 3.6444 | 2292.2547 | 2300.6240 | 2300.2663 |
| 3.6554 | 2289.7198 | 2292.5604 | 2292.1978 |
| 3.6664 | 2318.8142 | 2284.4970 | 2284.1292 |
| 3.6774 | 2313.5811 | 2276.4337 | 2276.0606 |
| 3.6884 | 2242.4380 | 2269.5035 | 2267.9920 |
| 3.6994 | 2245.4995 | 2265.1377 | 2264.7537 |
| 3.7104 | 2243.3795 | 2261.9050 | 2261.5153 |
| 3.7214 | 2194.3776 | 2258.6724 | 2258.2770 |
| 3.7324 | 2210.4533 | 2255.4399 | 2255.0386 |
| 3.7434 | 2278.8810 | 2252.2075 | 2251.8002 |
| 3.7544 | 2303.9941 | 2248.9753 | 2248.5619 |
| 3.7654 | 2270.2035 | 2245.7432 | 2245.3235 |
| 3.7764 | 2192.6489 | 2242.5113 | 2242.0851 |
| 3.7874 | 2244.5221 | 2239.2795 | 2238.8468 |
| 3.7984 | 2243.1101 | 2236.0479 | 2235.6084 |
| 3.8094 | 2275.4720 | 2232.8164 | 2232.3701 |
| 3.8204 | 2304.6917 | 2229.5851 | 2229.1317 |
| 3.8314 | 2288.9606 | 2226.3540 | 2225.8933 |
| 3.8424 | 2166.4223 | 2223.1230 | 2222.6550 |
| 3.8534 | 2127.5930 | 2219.8923 | 2219.4166 |
| 3.8644 | 2234.4528 | 2216.6617 | 2216.1782 |
| 3.8754 | 2204.4474 | 2213.4043 | 2212.9399 |
| 3.8864 | 2216.6328 | 2210.1346 | 2209.6351 |
| 3.8974 | 2288.5625 | 2206.8382 | 2206.3304 |
| 3.9084 | 2305.4262 | 2203.5420 | 2203.0256 |
| 3.9194 | 2186.8437 | 2200.2461 | 2199.7208 |
| 3.9304 | 2242.2645 | 2196.9503 | 2196.4161 |
| 3.9414 | 2196.2891 | 2193.6548 | 2193.1113 |
| 3.9524 | 2118.4528 | 2190.3595 | 2189.8066 |
| 3.9634 | 2090.8879 | 2187.0645 | 2186.5018 |
| 3.9744 | 2125.8004 | 2183.7697 | 2183.1971 |
| 3.9854 | 2144.7168 | 2180.4752 | 2179.8923 |
| 3.9964 | 2202.5506 | 2177.1810 | 2176.5875 |
| 4.0074 | 2200.5261 | 2173.8871 | 2173.2828 |
| 4.0184 | 2176.8156 | 2170.5934 | 2169.9780 |
| 4.0294 | 2129.6165 | 2167.3001 | 2166.6733 |
| 4.0404 | 2177.6062 | 2164.0071 | 2163.3685 |
| 4.0514 | 2173.7375 | 2160.7144 | 2160.0637 |
| 4.0624 | 2181.0683 | 2157.3718 | 2156.7590 |
| 4.0734 | 2127.4396 | 2154.0063 | 2153.3305 |
| 4.0844 | 2154.9734 | 2150.5910 | 2149.9020 |
| 4.0954 | 2110.3176 | 2147.1760 | 2146.4735 |
| 4.1064 | 2103.6096 | 2143.7615 | 2143.0449 |
| 4.1174 | 2124.3924 | 2140.3473 | 2139.6164 |
| 4.1284 | 2166.0000 | 2136.9336 | 2136.1879 |
| 4.1394 | 2166.0000 | 2133.5203 | 2132.7594 |
| 4.1504 | 2151.3200 | 2130.1075 | 2129.3309 |
| 4.1614 | 2131.8633 | 2126.6952 | 2125.9024 |
| 4.1724 | 2134.3146 | 2123.2834 | 2122.4739 |
| 4.1834 | 2105.9823 | 2119.8722 | 2119.0454 |
| 4.1944 | 2129.0777 | 2116.4615 | 2115.6169 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 24 Etosha22 sub 0.1-5cm S5 550C | 2.0054 | 29.9894 | 0.0110 | 12/12/2023 3:28:17 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6749 | 1163.69 | 0.0866 | 33.00184 | 59.65 |
| 5.2012 | 92.02 | 0.2598 | 16.97702 | 4.72 |
| 8.7166 | 1950.77 | 0.1299 | 10.13638 | 100.00 |
| 10.6076 | 34.68 | 0.3464 | 8.33324 | 1.78 |
| 15.9920 | 441.87 | 0.1515 | 5.53756 | 22.65 |
| 17.6443 | 144.96 | 0.1732 | 5.02256 | 7.43 |
| 19.6325 | 17.55 | 0.6927 | 4.51816 | 0.90 |
| 22.4773 | 32.19 | 0.2598 | 3.95235 | 1.65 |
| 26.2430 | 340.99 | 0.1948 | 3.39314 | 17.48 |
| 26.6887 | 268.09 | 0.1732 | 3.33747 | 13.74 |
| 27.5160 | 334.27 | 0.2165 | 3.23898 | 17.14 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-015-8233 | 56 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.87 Na0.04 Mg1.14 Ti0.1 Fe1.23 Al1.73 Si2.66 O10.16 ( O H )1.76 F0.08 | Biotite-1M | 37 |
| * | 04-011-6233 | 22 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 10 |
| * | 04-014-3289 | 25 | Magnesium Aluminum Silicon Oxide Hydroxide Deuterate Hydrate | Mg1.16 Al0.84 Si4 O10 ( O H ) ( H2 O )2 ( D2 O )2.5 | Palygorskite-M | 28 |
| * | 01-077-0022 | No Matching Lines | Magnesium Aluminum Iron Aluminum Silicate Hydroxide Hydrate | ( Mg2.36 Fe0.48 Al0.16 ) Mg0.32 ( Al1.28 Si2.72 O10 ) ( O H )2 ( H2 O )4.32 | Vermiculite-2M | - |
| * | 04-023-2279 | 14 | Potassium Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Fluoride Hydroxide | K0.22 Na0.4 Ca1.66 Mg2.2 Fe2.94 Al1.11 Si6.89 O22 ( O H )0.37 F1.63 | Magnesio-ferri-fluoro-hornblende | 10 |
| * | 04-025-4215 | 43 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 15 |

Anchor Scan Parameters

Dataset Name	24 Etosha22 sub 0.1-5cm S5 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 24\24 Etosha22 sub 0.1-5cm S5 550C.xrdml

Sample Identification	24 Etosha22 sub 0.1-5cm S5 550C

Measurement Start Date/Time	12/12/2023 3:28:17 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes