24 Etosha 22 sub 0.1-5 cm S5 glycol report

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	16.0

Phase Potassium Manganese Silicate Hydroxide Hydrate

Weight fraction/ %	10.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	14.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	35.0

Phase Sodium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Sodium Calcium Iron Silicate Hydroxide

Weight fraction/ %	5.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	18.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Manganese Silicate Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Sodium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Sodium Calcium Iron Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 24 Etosha22 sub 0.1-5cm S5 glycol | 16.0 | 10.0 | 14.0 | 35.0 | 2.0 | 5.0 | 18.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7857.0000 | 7867.0182 | 7857.0000 |
| 2.0164 | 8059.3899 | 7830.2592 | 7807.9762 |
| 2.0274 | 7929.3363 | 7781.4636 | 7758.9525 |
| 2.0384 | 7896.6578 | 7732.6745 | 7709.9287 |
| 2.0494 | 7731.5408 | 7683.8921 | 7660.9050 |
| 2.0604 | 7746.1790 | 7635.1170 | 7611.8812 |
| 2.0714 | 7801.4454 | 7586.3496 | 7562.8574 |
| 2.0824 | 7687.2891 | 7537.5904 | 7513.8337 |
| 2.0934 | 7622.3913 | 7488.8400 | 7464.8099 |
| 2.1044 | 7657.3274 | 7440.0989 | 7415.7862 |
| 2.1154 | 7468.1062 | 7391.3678 | 7366.7624 |
| 2.1264 | 7477.6224 | 7342.6475 | 7317.7386 |
| 2.1374 | 7462.4838 | 7293.9387 | 7268.7149 |
| 2.1484 | 7315.7989 | 7245.2424 | 7219.6911 |
| 2.1594 | 7322.4090 | 7196.5595 | 7170.6673 |
| 2.1704 | 7309.2950 | 7147.8912 | 7121.6436 |
| 2.1814 | 7193.1170 | 7099.2386 | 7072.6198 |
| 2.1924 | 7188.1932 | 7050.5631 | 7023.5961 |
| 2.2034 | 7262.2832 | 7001.8233 | 6974.4092 |
| 2.2144 | 7215.4012 | 6953.0639 | 6925.2224 |
| 2.2254 | 7149.2035 | 6904.3268 | 6876.0356 |
| 2.2364 | 6983.3643 | 6855.6142 | 6826.8488 |
| 2.2474 | 7169.6677 | 6806.9286 | 6777.6620 |
| 2.2584 | 7163.4666 | 6758.2728 | 6728.4751 |
| 2.2694 | 6905.4189 | 6709.6500 | 6679.2883 |
| 2.2804 | 6951.0108 | 6661.0640 | 6630.1015 |
| 2.2914 | 6918.2999 | 6612.5189 | 6580.9147 |
| 2.3024 | 6860.1195 | 6564.0197 | 6531.7278 |
| 2.3134 | 6850.3953 | 6515.5720 | 6482.5410 |
| 2.3244 | 6960.6637 | 6467.1824 | 6433.3542 |
| 2.3354 | 6901.9115 | 6418.8586 | 6384.1674 |
| 2.3464 | 6737.6219 | 6370.6096 | 6334.9805 |
| 2.3574 | 6812.9508 | 6322.4463 | 6285.7937 |
| 2.3684 | 6796.3053 | 6274.3811 | 6236.6069 |
| 2.3794 | 6612.6136 | 6226.3971 | 6187.4201 |
| 2.3904 | 6578.1131 | 6178.4777 | 6138.1013 |
| 2.4014 | 6568.0000 | 6130.6798 | 6088.7826 |
| 2.4124 | 6503.6357 | 6083.0627 | 6039.4638 |
| 2.4234 | 6445.4857 | 6035.6597 | 5990.1451 |
| 2.4344 | 6456.7375 | 5988.5119 | 5940.8264 |
| 2.4454 | 6479.5113 | 5941.6708 | 5891.5076 |
| 2.4564 | 6389.7797 | 5895.2015 | 5842.1889 |
| 2.4674 | 6335.1563 | 5849.1877 | 5792.8701 |
| 2.4784 | 6265.0762 | 5803.7398 | 5743.5514 |
| 2.4894 | 6298.0089 | 5759.0098 | 5694.2326 |
| 2.5004 | 6275.3761 | 5715.2222 | 5644.9139 |
| 2.5114 | 6216.6116 | 5672.7401 | 5595.5952 |
| 2.5224 | 6140.2365 | 5632.2010 | 5546.2764 |
| 2.5334 | 6075.4602 | 5594.7678 | 5496.9577 |
| 2.5444 | 6103.7153 | 5562.5283 | 5447.6389 |
| 2.5554 | 6165.1750 | 5538.9966 | 5398.3202 |
| 2.5664 | 6100.1077 | 5529.5115 | 5349.0014 |
| 2.5774 | 5951.4080 | 5541.1203 | 5299.6827 |
| 2.5884 | 5886.2743 | 5581.4537 | 5250.3640 |
| 2.5994 | 5948.3628 | 5656.3077 | 5201.0452 |
| 2.6104 | 6011.3923 | 5766.0667 | 5151.7265 |
| 2.6214 | 5947.9105 | 5901.1783 | 5102.4077 |
| 2.6324 | 5855.5516 | 6036.4812 | 5053.0890 |
| 2.6434 | 5937.9322 | 6127.2758 | 5003.7702 |
| 2.6544 | 5942.5659 | 6122.0372 | 4954.4515 |
| 2.6654 | 5796.7315 | 6000.7997 | 4905.1328 |
| 2.6764 | 5657.7802 | 5795.3547 | 4855.8140 |
| 2.6874 | 5627.0000 | 5558.4311 | 4806.4953 |
| 2.6984 | 5489.9425 | 5329.9623 | 4757.1765 |
| 2.7094 | 5372.1239 | 5130.5504 | 4707.8578 |
| 2.7204 | 5334.2227 | 4966.7096 | 4658.5390 |
| 2.7314 | 5290.2507 | 4836.2755 | 4609.2203 |
| 2.7424 | 5164.0629 | 4732.6789 | 4559.9015 |
| 2.7534 | 5017.8102 | 4648.2240 | 4510.5828 |
| 2.7644 | 4828.6239 | 4576.2036 | 4461.1321 |
| 2.7754 | 4981.3992 | 4511.7967 | 4411.6815 |
| 2.7864 | 4805.9238 | 4451.9335 | 4362.2308 |
| 2.7974 | 4697.2389 | 4394.8091 | 4312.7802 |
| 2.8084 | 4510.2424 | 4339.4275 | 4263.3295 |
| 2.8194 | 4498.1858 | 4285.2405 | 4213.8788 |
| 2.8304 | 4524.8112 | 4231.9300 | 4164.4282 |
| 2.8414 | 4370.0678 | 4179.2950 | 4114.9775 |
| 2.8524 | 4260.5732 | 4127.1962 | 4065.5268 |
| 2.8634 | 4255.0000 | 4075.5315 | 4016.0762 |
| 2.8744 | 4019.0486 | 4024.2224 | 3966.6255 |
| 2.8854 | 3942.1868 | 3973.2079 | 3917.1748 |
| 2.8964 | 4034.5841 | 3922.4396 | 3867.7242 |
| 2.9074 | 3994.3726 | 3871.8787 | 3818.2735 |
| 2.9184 | 3664.8948 | 3821.4938 | 3768.8229 |
| 2.9294 | 3753.5280 | 3771.2594 | 3719.3722 |
| 2.9404 | 3650.5816 | 3725.5658 | 3669.9215 |
| 2.9514 | 3659.3500 | 3689.1194 | 3638.4281 |
| 2.9624 | 3593.8009 | 3657.1821 | 3606.9347 |
| 2.9734 | 3519.6745 | 3625.3306 | 3575.4413 |
| 2.9844 | 3473.0659 | 3593.5550 | 3543.9479 |
| 2.9954 | 3486.2035 | 3561.8466 | 3512.4545 |
| 3.0064 | 3422.2463 | 3530.1981 | 3480.9611 |
| 3.0174 | 3370.0383 | 3498.6034 | 3449.4677 |
| 3.0284 | 3353.5664 | 3467.0571 | 3417.9742 |
| 3.0394 | 3338.4376 | 3435.5547 | 3386.4808 |
| 3.0504 | 3353.4144 | 3404.0923 | 3354.9874 |
| 3.0614 | 3291.0767 | 3372.6664 | 3323.4940 |
| 3.0724 | 3324.5049 | 3341.2740 | 3292.0006 |
| 3.0834 | 3246.6391 | 3309.9126 | 3260.5072 |
| 3.0944 | 3153.6372 | 3278.5800 | 3229.0138 |
| 3.1054 | 3177.8948 | 3247.2741 | 3197.5204 |
| 3.1164 | 3194.3796 | 3215.9933 | 3166.0270 |
| 3.1274 | 3167.2006 | 3188.5557 | 3134.5335 |
| 3.1384 | 3054.4041 | 3169.0504 | 3118.5896 |
| 3.1494 | 3061.4091 | 3153.3858 | 3102.6456 |
| 3.1604 | 3047.1253 | 3137.7413 | 3086.7016 |
| 3.1714 | 2935.4572 | 3122.1159 | 3070.7576 |
| 3.1824 | 3005.3614 | 3106.5088 | 3054.8136 |
| 3.1934 | 3116.1504 | 3090.9194 | 3038.8696 |
| 3.2044 | 2969.3727 | 3075.3471 | 3022.9256 |
| 3.2154 | 2942.1681 | 3059.7914 | 3006.9816 |
| 3.2264 | 2964.0295 | 3044.2517 | 2991.0377 |
| 3.2374 | 2972.4169 | 3028.7277 | 2975.0937 |
| 3.2484 | 2964.8889 | 3013.2191 | 2959.1497 |
| 3.2594 | 2970.3009 | 2997.7255 | 2943.2057 |
| 3.2704 | 2891.4705 | 2982.2468 | 2927.2617 |
| 3.2814 | 2825.0285 | 2966.7828 | 2911.3177 |
| 3.2924 | 2835.9956 | 2951.3332 | 2895.3737 |
| 3.3034 | 2906.2586 | 2935.8980 | 2879.4298 |
| 3.3144 | 2903.3451 | 2920.4771 | 2863.4858 |
| 3.3254 | 2830.3333 | 2905.0703 | 2847.5418 |
| 3.3364 | 2796.8225 | 2889.6778 | 2831.5978 |
| 3.3474 | 2757.0659 | 2874.2994 | 2815.6538 |
| 3.3584 | 2727.3614 | 2858.9352 | 2799.7098 |
| 3.3694 | 2779.7709 | 2843.5853 | 2783.7658 |
| 3.3804 | 2733.8525 | 2828.2497 | 2767.8218 |
| 3.3914 | 2748.4868 | 2812.9284 | 2751.8779 |
| 3.4024 | 2769.7812 | 2797.6217 | 2735.9339 |
| 3.4134 | 2737.2675 | 2782.3296 | 2719.9899 |
| 3.4244 | 2740.6121 | 2767.0522 | 2704.0459 |
| 3.4354 | 2732.2497 | 2751.7897 | 2688.1019 |
| 3.4464 | 2691.2733 | 2736.5424 | 2672.1579 |
| 3.4574 | 2666.6431 | 2721.3103 | 2656.2139 |
| 3.4684 | 2657.0182 | 2706.0938 | 2640.2699 |
| 3.4794 | 2664.6460 | 2690.8930 | 2624.3260 |
| 3.4904 | 2636.0575 | 2675.7081 | 2608.3820 |
| 3.5014 | 2553.5280 | 2663.6038 | 2592.4380 |
| 3.5124 | 2550.7227 | 2657.8350 | 2588.9681 |
| 3.5234 | 2628.0472 | 2654.2425 | 2585.4983 |
| 3.5344 | 2582.3205 | 2651.1673 | 2582.0284 |
| 3.5454 | 2575.7847 | 2648.5747 | 2578.5585 |
| 3.5564 | 2573.2714 | 2645.9986 | 2575.0887 |
| 3.5674 | 2624.8997 | 2643.4394 | 2571.6188 |
| 3.5784 | 2602.3309 | 2640.8977 | 2568.1489 |
| 3.5894 | 2545.1150 | 2638.3738 | 2564.6791 |
| 3.6004 | 2493.6721 | 2635.8682 | 2561.2092 |
| 3.6114 | 2520.3412 | 2633.3814 | 2557.7393 |
| 3.6224 | 2536.4543 | 2630.9139 | 2554.2695 |
| 3.6334 | 2604.3452 | 2628.4661 | 2550.7996 |
| 3.6444 | 2594.0590 | 2626.0387 | 2547.3298 |
| 3.6554 | 2517.2891 | 2623.6321 | 2543.8599 |
| 3.6664 | 2540.8058 | 2621.2470 | 2540.3900 |
| 3.6774 | 2572.1790 | 2618.8839 | 2536.9202 |
| 3.6884 | 2539.8982 | 2616.8554 | 2533.4503 |
| 3.6994 | 2488.5732 | 2615.4961 | 2531.2503 |
| 3.7104 | 2542.7375 | 2614.4728 | 2529.0503 |
| 3.7214 | 2532.4867 | 2613.4741 | 2526.8503 |
| 3.7324 | 2536.5782 | 2612.5008 | 2524.6503 |
| 3.7434 | 2514.3923 | 2611.5536 | 2522.4503 |
| 3.7544 | 2499.6401 | 2610.6333 | 2520.2503 |
| 3.7654 | 2520.2645 | 2609.7409 | 2518.0503 |
| 3.7764 | 2535.6829 | 2608.8770 | 2515.8503 |
| 3.7874 | 2500.3186 | 2608.0427 | 2513.6503 |
| 3.7984 | 2547.9277 | 2607.2390 | 2511.4503 |
| 3.8094 | 2527.5978 | 2606.4668 | 2509.2503 |
| 3.8204 | 2563.0944 | 2605.7272 | 2507.0503 |
| 3.8314 | 2495.0649 | 2605.0213 | 2504.8503 |
| 3.8424 | 2450.2099 | 2604.3504 | 2502.6503 |
| 3.8534 | 2480.5664 | 2603.7157 | 2500.4503 |
| 3.8644 | 2599.8318 | 2603.1186 | 2498.2503 |
| 3.8754 | 2549.9105 | 2602.5216 | 2496.0503 |
| 3.8864 | 2535.3628 | 2601.8848 | 2493.6924 |
| 3.8974 | 2431.6529 | 2601.2512 | 2491.3344 |
| 3.9084 | 2559.7365 | 2600.6615 | 2488.9764 |
| 3.9194 | 2552.2478 | 2600.1175 | 2486.6185 |
| 3.9304 | 2583.6967 | 2599.6210 | 2484.2605 |
| 3.9414 | 2705.9007 | 2599.1743 | 2481.9026 |
| 3.9524 | 2642.1549 | 2598.7795 | 2479.5446 |
| 3.9634 | 2614.6952 | 2598.4391 | 2477.1867 |
| 3.9744 | 2631.5983 | 2598.1556 | 2474.8287 |
| 3.9854 | 2603.7699 | 2597.9318 | 2472.4708 |
| 3.9964 | 2579.3098 | 2597.7706 | 2470.1128 |
| 4.0074 | 2683.8722 | 2597.6753 | 2467.7549 |
| 4.0184 | 2681.5722 | 2597.6492 | 2465.3969 |
| 4.0294 | 2603.0305 | 2597.6960 | 2463.0389 |
| 4.0404 | 2566.2709 | 2597.8197 | 2460.6810 |
| 4.0514 | 2561.7965 | 2598.0245 | 2458.3230 |
| 4.0624 | 2677.7227 | 2598.2369 | 2455.9651 |
| 4.0734 | 2654.3825 | 2598.5369 | 2453.4481 |
| 4.0844 | 2686.2079 | 2598.8547 | 2450.9310 |
| 4.0954 | 2604.3176 | 2599.2740 | 2448.4140 |
| 4.1064 | 2671.2990 | 2599.8009 | 2445.8970 |
| 4.1174 | 2763.0944 | 2600.4420 | 2443.3799 |
| 4.1284 | 2689.4661 | 2601.2042 | 2440.8629 |
| 4.1394 | 2675.0855 | 2602.0950 | 2438.3459 |
| 4.1504 | 2705.0679 | 2603.1225 | 2435.8289 |
| 4.1614 | 2786.4110 | 2604.2953 | 2433.3118 |
| 4.1724 | 2814.0885 | 2605.6227 | 2430.7948 |
| 4.1834 | 2883.0973 | 2607.1144 | 2428.2778 |
| 4.1944 | 2851.6907 | 2608.7811 | 2425.7607 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 24 Etosha22 sub 0.1-5cm S5 glycol | 2.0054 | 29.9894 | 0.0110 | 12/13/2023 10:01:20 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6508 | 1020.93 | 0.0866 | 33.30189 | 38.68 |
| 5.1996 | 2639.61 | 0.7360 | 16.98206 | 100.00 |
| 6.9970 | 1560.80 | 0.1515 | 12.62319 | 59.13 |
| 8.7131 | 1061.61 | 0.1515 | 10.14050 | 40.22 |
| 10.3388 | 63.92 | 0.6061 | 8.54929 | 2.42 |
| 15.7084 | 1097.19 | 0.1082 | 5.63692 | 41.57 |
| 17.6158 | 151.23 | 0.1732 | 5.03062 | 5.73 |
| 18.1894 | 193.87 | 0.0866 | 4.87325 | 7.34 |
| 19.5698 | 66.47 | 0.5196 | 4.53251 | 2.52 |
| 20.8935 | 37.79 | 0.2598 | 4.24825 | 1.43 |
| 22.3890 | 63.26 | 0.1299 | 3.96774 | 2.40 |
| 23.3838 | 40.26 | 0.2598 | 3.80114 | 1.53 |
| 25.8773 | 1345.37 | 0.1082 | 3.44026 | 50.97 |
| 26.6753 | 660.06 | 0.1732 | 3.33913 | 25.01 |
| 27.5006 | 180.60 | 0.1299 | 3.24076 | 6.84 |
| 29.3549 | 69.92 | 0.1732 | 3.04012 | 2.65 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-017-4317 | 49 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 16 |
| * | 01-089-6415 | 43 | Potassium Manganese Silicate Hydroxide Hydrate | K3.68 Mn15.904 Si25.472 O64 ( O H )9.376 ( H2 O )7.024 | Ganophyllite | 10 |
| * | 04-011-6751 | 16 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 14 |
| * | 04-015-8177 | 32 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.9 Na0.1 Mg1.98 Ti0.18 Fe0.66 Al1.42 Si2.75 O10.66 ( O H )1.2 F0.14 | Phlogopite-1M | 35 |
| * | 04-017-7291 | 19 | Sodium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Na0.930 Mg2.810 Fe0.065 Al1.185 Si2.895 O10 ( O H )2 ( H2 O )3 | Vermiculite | 2 |
| * | 01-080-0281 | 7 | Sodium Calcium Iron Silicate Hydroxide | Na Ca2 Fe5 Si8 O22 ( O H )2 | Ferro-ferri-hornblende | 5 |
| * | 04-025-4215 | 38 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 18 |

Anchor Scan Parameters

Dataset Name	24 Etosha22 sub 0.1-5cm S5 glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 24\24 Etosha22 sub 0.1-5cm S5 glycol.xrdml

Sample Identification	24 Etosha22 sub 0.1-5cm S5 glycol

Measurement Start Date/Time	12/13/2023 10:01:20 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes