24 Etosha 22 sub 0.1-5 cm S5 REGULAR REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	16.0

Phase Titanium Oxide

Weight fraction/ %	3.0

Phase Potassium Manganese Silicate Hydroxide Hydrate

Weight fraction/ %	28.0

Phase Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	6.0

Phase Magnesium Silicate Hydroxide

Weight fraction/ %	4.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	23.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	20.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Titanium Oxide | Potassium Manganese Silicate Hydroxide Hydrate | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | Magnesium Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 24 Etosha22 sub 0.1-5cm S5 | 16.0 | 3.0 | 28.0 | 6.0 | 4.0 | 23.0 | 20.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7941.0000 | 7943.8517 | 7941.0000 |
| 2.0164 | 8028.2424 | 7901.5406 | 7884.7095 |
| 2.0274 | 7883.8535 | 7845.7590 | 7828.4189 |
| 2.0384 | 7763.0192 | 7790.0035 | 7772.1284 |
| 2.0494 | 7868.8850 | 7734.2758 | 7715.8379 |
| 2.0604 | 7878.6868 | 7678.5778 | 7659.5474 |
| 2.0714 | 7753.7257 | 7622.9117 | 7603.2568 |
| 2.0824 | 7591.1298 | 7567.2799 | 7546.9663 |
| 2.0934 | 7626.6421 | 7511.6849 | 7490.6758 |
| 2.1044 | 7579.3142 | 7456.1297 | 7434.3853 |
| 2.1154 | 7766.4503 | 7400.6172 | 7378.0947 |
| 2.1264 | 7424.7321 | 7345.1509 | 7321.8042 |
| 2.1374 | 7454.4100 | 7289.7345 | 7265.5137 |
| 2.1484 | 7428.9498 | 7234.3721 | 7209.2232 |
| 2.1594 | 7320.0551 | 7179.0684 | 7152.9326 |
| 2.1704 | 7369.3024 | 7123.8284 | 7096.6421 |
| 2.1814 | 7435.8201 | 7068.6575 | 7040.3516 |
| 2.1924 | 7381.2704 | 7013.5206 | 6984.0611 |
| 2.2034 | 7221.0973 | 6958.3758 | 6927.5970 |
| 2.2144 | 7294.0782 | 6903.2794 | 6871.1329 |
| 2.2254 | 7186.8761 | 6848.2819 | 6814.6689 |
| 2.2364 | 7137.3260 | 6793.3929 | 6758.2048 |
| 2.2474 | 7193.5152 | 6738.6232 | 6701.7407 |
| 2.2584 | 7170.7729 | 6683.9853 | 6645.2767 |
| 2.2694 | 7082.8053 | 6629.4931 | 6588.8126 |
| 2.2804 | 7047.1052 | 6575.1624 | 6532.3485 |
| 2.2914 | 6980.1868 | 6521.0116 | 6475.8845 |
| 2.3024 | 6864.6593 | 6467.0617 | 6419.4204 |
| 2.3134 | 6736.2724 | 6413.3376 | 6362.9563 |
| 2.3244 | 6781.1981 | 6359.8685 | 6306.4923 |
| 2.3354 | 6791.9440 | 6306.6903 | 6250.0282 |
| 2.3464 | 6821.9592 | 6253.8473 | 6193.5641 |
| 2.3574 | 6854.4680 | 6201.3957 | 6137.1001 |
| 2.3684 | 6738.1799 | 6149.4090 | 6080.6360 |
| 2.3794 | 6673.8791 | 6097.9508 | 6024.1719 |
| 2.3904 | 6707.4680 | 6047.1126 | 5967.5675 |
| 2.4014 | 6597.9911 | 5997.1116 | 5910.9630 |
| 2.4124 | 6585.1298 | 5948.2222 | 5854.3586 |
| 2.4234 | 6608.5398 | 5900.7684 | 5797.7541 |
| 2.4344 | 6476.1888 | 5855.1806 | 5741.1496 |
| 2.4454 | 6520.3117 | 5812.0193 | 5684.5452 |
| 2.4564 | 6628.5433 | 5771.9974 | 5627.9407 |
| 2.4674 | 6567.4071 | 5735.9968 | 5571.3362 |
| 2.4784 | 6392.9548 | 5705.0718 | 5514.7318 |
| 2.4894 | 6378.4474 | 5680.4367 | 5458.1273 |
| 2.5004 | 6441.5973 | 5663.4270 | 5401.5229 |
| 2.5114 | 6393.8574 | 5655.4340 | 5344.9184 |
| 2.5224 | 6262.4838 | 5657.8064 | 5288.3139 |
| 2.5334 | 6203.7493 | 5671.7235 | 5231.7095 |
| 2.5444 | 6273.6239 | 5698.0420 | 5175.1050 |
| 2.5554 | 6234.9518 | 5737.1226 | 5118.5005 |
| 2.5664 | 6160.2994 | 5788.6413 | 5061.8961 |
| 2.5774 | 6029.9557 | 5851.3795 | 5005.2916 |
| 2.5884 | 6118.7365 | 5922.9850 | 4948.6871 |
| 2.5994 | 6104.0973 | 5999.6899 | 4892.0827 |
| 2.6104 | 5993.4833 | 6076.0101 | 4835.4782 |
| 2.6214 | 6047.2842 | 6144.5395 | 4778.8738 |
| 2.6324 | 6043.6652 | 6196.1093 | 4722.2693 |
| 2.6434 | 6025.2871 | 6220.6882 | 4665.6648 |
| 2.6544 | 5962.6352 | 6209.2302 | 4609.0604 |
| 2.6654 | 5767.1711 | 6156.0652 | 4552.4559 |
| 2.6764 | 5819.9627 | 6060.7301 | 4495.8514 |
| 2.6874 | 5747.5034 | 5928.1373 | 4439.2470 |
| 2.6984 | 5523.2876 | 5766.9633 | 4382.6425 |
| 2.7094 | 5394.0570 | 5587.2498 | 4326.0380 |
| 2.7204 | 5347.6357 | 5398.4050 | 4269.4336 |
| 2.7314 | 5217.6961 | 5208.1481 | 4212.8291 |
| 2.7424 | 5079.4744 | 5022.2598 | 4156.2247 |
| 2.7534 | 5061.8505 | 4844.7067 | 4099.6202 |
| 2.7644 | 4895.0796 | 4678.0528 | 4042.8753 |
| 2.7754 | 4616.3520 | 4523.6651 | 3986.1305 |
| 2.7864 | 4467.7896 | 4382.0434 | 3929.3856 |
| 2.7974 | 4525.4513 | 4252.9206 | 3872.6407 |
| 2.8084 | 4232.6278 | 4135.5055 | 3815.8959 |
| 2.8194 | 4127.9656 | 4028.6582 | 3759.1510 |
| 2.8304 | 3901.6047 | 3931.0466 | 3702.4062 |
| 2.8414 | 3946.5202 | 3841.2785 | 3645.6613 |
| 2.8524 | 3788.2173 | 3758.0035 | 3588.9164 |
| 2.8634 | 3696.5516 | 3679.9850 | 3532.1716 |
| 2.8744 | 3478.4105 | 3606.1414 | 3475.4267 |
| 2.8854 | 3532.9636 | 3535.5638 | 3418.6819 |
| 2.8964 | 3329.9070 | 3467.5133 | 3361.9370 |
| 2.9074 | 3279.8112 | 3401.4068 | 3305.1921 |
| 2.9184 | 3257.0280 | 3336.7952 | 3248.4473 |
| 2.9294 | 3299.3746 | 3273.3396 | 3191.7024 |
| 2.9404 | 3071.8658 | 3219.3818 | 3134.9576 |
| 2.9514 | 3065.0649 | 3172.8688 | 3102.1285 |
| 2.9624 | 3003.5354 | 3135.5299 | 3069.2995 |
| 2.9734 | 3045.5319 | 3098.6694 | 3036.4705 |
| 2.9844 | 2976.6755 | 3062.2105 | 3003.6414 |
| 2.9954 | 2910.8850 | 3026.0949 | 2970.8124 |
| 3.0064 | 2929.2507 | 2990.2765 | 2937.9834 |
| 3.0174 | 2761.0462 | 2954.7185 | 2905.1544 |
| 3.0284 | 2764.1372 | 2919.3906 | 2872.3253 |
| 3.0394 | 2743.4857 | 2884.2675 | 2839.4963 |
| 3.0504 | 2768.4002 | 2849.3275 | 2806.6673 |
| 3.0614 | 2805.0265 | 2814.5520 | 2773.8383 |
| 3.0724 | 2710.5398 | 2779.9248 | 2741.0092 |
| 3.0834 | 2701.7267 | 2745.4316 | 2708.1802 |
| 3.0944 | 2682.3716 | 2711.0598 | 2675.3512 |
| 3.1054 | 2559.0344 | 2676.7984 | 2642.5222 |
| 3.1164 | 2634.5506 | 2642.6375 | 2609.6931 |
| 3.1274 | 2578.1357 | 2613.4639 | 2576.8641 |
| 3.1384 | 2549.1485 | 2588.2063 | 2557.6584 |
| 3.1494 | 2532.7217 | 2567.9210 | 2538.4526 |
| 3.1604 | 2535.1962 | 2547.7062 | 2519.2469 |
| 3.1714 | 2503.3264 | 2527.5561 | 2500.0411 |
| 3.1824 | 2435.6357 | 2507.4658 | 2480.8354 |
| 3.1934 | 2437.5575 | 2487.4305 | 2461.6296 |
| 3.2044 | 2384.9204 | 2467.4461 | 2442.4239 |
| 3.2154 | 2422.2694 | 2447.5087 | 2423.2181 |
| 3.2264 | 2320.0074 | 2427.6150 | 2404.0124 |
| 3.2374 | 2317.2085 | 2407.7618 | 2384.8066 |
| 3.2484 | 2322.0000 | 2387.9462 | 2365.6009 |
| 3.2594 | 2315.2832 | 2368.1656 | 2346.3951 |
| 3.2704 | 2286.1834 | 2348.4177 | 2327.1894 |
| 3.2814 | 2290.2556 | 2328.7003 | 2307.9836 |
| 3.2924 | 2278.7390 | 2309.0113 | 2288.7779 |
| 3.3034 | 2325.5959 | 2289.3490 | 2269.5721 |
| 3.3144 | 2271.8112 | 2271.3038 | 2250.3664 |
| 3.3254 | 2163.3333 | 2254.5283 | 2235.5912 |
| 3.3364 | 2175.6210 | 2239.3670 | 2220.8161 |
| 3.3474 | 2211.5388 | 2224.2263 | 2206.0410 |
| 3.3584 | 2166.3702 | 2209.1051 | 2191.2658 |
| 3.3694 | 2134.2714 | 2194.0022 | 2176.4907 |
| 3.3804 | 2097.1268 | 2178.9165 | 2161.7156 |
| 3.3914 | 2078.3186 | 2163.8472 | 2146.9405 |
| 3.4024 | 2116.8771 | 2148.7933 | 2132.1653 |
| 3.4134 | 2128.4965 | 2133.7540 | 2117.3902 |
| 3.4244 | 2018.4837 | 2118.7285 | 2102.6151 |
| 3.4354 | 1933.2714 | 2103.7161 | 2087.8400 |
| 3.4464 | 1979.7926 | 2088.7161 | 2073.0648 |
| 3.4574 | 2000.5723 | 2073.7279 | 2058.2897 |
| 3.4684 | 1992.5388 | 2058.7510 | 2043.5146 |
| 3.4794 | 2019.2330 | 2043.7847 | 2028.7394 |
| 3.4904 | 2029.0442 | 2028.8286 | 2013.9643 |
| 3.5014 | 1998.7935 | 2014.2360 | 1999.1892 |
| 3.5124 | 1974.0580 | 1999.9296 | 1985.3985 |
| 3.5234 | 1946.0265 | 1985.9858 | 1971.6079 |
| 3.5344 | 1923.2478 | 1972.0505 | 1957.8172 |
| 3.5454 | 1881.2419 | 1958.1233 | 1944.0266 |
| 3.5564 | 1930.7744 | 1944.2038 | 1930.2359 |
| 3.5674 | 1898.1003 | 1930.2918 | 1916.4453 |
| 3.5784 | 1807.0260 | 1916.3869 | 1902.6546 |
| 3.5894 | 1871.7699 | 1902.4889 | 1888.8640 |
| 3.6004 | 1862.0187 | 1888.5975 | 1875.0733 |
| 3.6114 | 1910.7925 | 1874.7124 | 1861.2827 |
| 3.6224 | 1809.8230 | 1860.8334 | 1847.4920 |
| 3.6334 | 1811.4867 | 1846.9604 | 1833.7014 |
| 3.6444 | 1807.1922 | 1833.0931 | 1819.9107 |
| 3.6554 | 1778.0029 | 1819.2312 | 1806.1201 |
| 3.6664 | 1803.8142 | 1805.3747 | 1792.3294 |
| 3.6774 | 1779.4798 | 1791.5233 | 1778.5388 |
| 3.6884 | 1738.0177 | 1780.0402 | 1764.7481 |
| 3.6994 | 1750.8564 | 1770.4118 | 1757.5338 |
| 3.7104 | 1799.1608 | 1763.1514 | 1750.3196 |
| 3.7214 | 1704.9203 | 1755.8955 | 1743.1053 |
| 3.7324 | 1760.1490 | 1748.6441 | 1735.8910 |
| 3.7434 | 1691.5251 | 1741.3969 | 1728.6767 |
| 3.7544 | 1744.2567 | 1734.1541 | 1721.4624 |
| 3.7654 | 1669.6745 | 1726.9153 | 1714.2482 |
| 3.7764 | 1709.0910 | 1719.6805 | 1707.0339 |
| 3.7874 | 1682.2478 | 1712.4497 | 1699.8196 |
| 3.7984 | 1742.7281 | 1705.2228 | 1692.6053 |
| 3.8094 | 1664.4563 | 1697.9996 | 1685.3910 |
| 3.8204 | 1692.2434 | 1690.7800 | 1678.1767 |
| 3.8314 | 1665.1534 | 1683.5642 | 1670.9625 |
| 3.8424 | 1647.1042 | 1676.3519 | 1663.7482 |
| 3.8534 | 1684.3510 | 1669.1430 | 1656.5339 |
| 3.8644 | 1672.3756 | 1661.9377 | 1649.3196 |
| 3.8754 | 1640.2842 | 1655.6245 | 1642.1053 |
| 3.8864 | 1628.6239 | 1650.0105 | 1637.3644 |
| 3.8974 | 1588.5172 | 1645.2885 | 1632.6235 |
| 3.9084 | 1588.8771 | 1640.5699 | 1627.8826 |
| 3.9194 | 1661.9882 | 1635.8544 | 1623.1416 |
| 3.9304 | 1609.1696 | 1631.1422 | 1618.4007 |
| 3.9414 | 1627.9794 | 1626.4332 | 1613.6598 |
| 3.9524 | 1622.4690 | 1621.7273 | 1608.9189 |
| 3.9634 | 1602.8614 | 1617.0246 | 1604.1779 |
| 3.9744 | 1712.5904 | 1612.3250 | 1599.4370 |
| 3.9854 | 1627.9911 | 1607.6284 | 1594.6961 |
| 3.9964 | 1592.1140 | 1602.9350 | 1589.9551 |
| 4.0074 | 1566.0570 | 1598.2447 | 1585.2142 |
| 4.0184 | 1579.7861 | 1593.5574 | 1580.4733 |
| 4.0294 | 1551.8928 | 1588.8732 | 1575.7324 |
| 4.0404 | 1587.6800 | 1584.1921 | 1570.9914 |
| 4.0514 | 1604.5546 | 1579.5140 | 1566.2505 |
| 4.0624 | 1552.1258 | 1575.4227 | 1561.5096 |
| 4.0734 | 1521.4789 | 1571.7913 | 1558.3928 |
| 4.0844 | 1568.9557 | 1568.7466 | 1555.2760 |
| 4.0954 | 1558.3825 | 1565.7050 | 1552.1591 |
| 4.1064 | 1592.3796 | 1562.6665 | 1549.0423 |
| 4.1174 | 1599.4484 | 1559.6312 | 1545.9255 |
| 4.1284 | 1550.2783 | 1556.5991 | 1542.8087 |
| 4.1394 | 1547.4602 | 1553.5701 | 1539.6919 |
| 4.1504 | 1558.1578 | 1550.5443 | 1536.5751 |
| 4.1614 | 1567.2271 | 1547.5218 | 1533.4583 |
| 4.1724 | 1567.3146 | 1544.5025 | 1530.3414 |
| 4.1834 | 1576.2743 | 1541.4866 | 1527.2246 |
| 4.1944 | 1569.1499 | 1538.4739 | 1524.1078 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 24 Etosha22 sub 0.1-5cm S5 | 2.0054 | 29.9894 | 0.0110 | 12/12/2023 10:29:00 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6586 | 1436.36 | 0.1732 | 33.20469 | 43.79 |
| 5.9798 | 1446.99 | 0.4330 | 14.76814 | 44.12 |
| 7.0360 | 3280.00 | 0.2165 | 12.55332 | 100.00 |
| 8.7092 | 987.95 | 0.1948 | 10.14496 | 30.12 |
| 13.0001 | 18.11 | 0.5196 | 6.80454 | 0.55 |
| 15.6882 | 824.92 | 0.0649 | 5.64413 | 25.15 |
| 17.5572 | 116.21 | 0.1732 | 5.04726 | 3.54 |
| 18.1459 | 164.46 | 0.0649 | 4.88485 | 5.01 |
| 19.6061 | 57.20 | 0.5196 | 4.52420 | 1.74 |
| 22.3563 | 26.42 | 0.2598 | 3.97348 | 0.81 |
| 23.3237 | 31.89 | 0.2598 | 3.81080 | 0.97 |
| 25.8509 | 797.23 | 0.0974 | 3.44371 | 24.31 |
| 26.6085 | 391.75 | 0.1515 | 3.34735 | 11.94 |
| 27.4641 | 187.08 | 0.1299 | 3.24498 | 5.70 |
| 29.3067 | 55.55 | 0.1299 | 3.04502 | 1.69 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-017-4317 | 49 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 16 |
| * | 04-007-4874 | 47 | Titanium Oxide | Ti O2 | Rutile | 3 |
| * | 01-089-6415 | 50 | Potassium Manganese Silicate Hydroxide Hydrate | K3.68 Mn15.904 Si25.472 O64 ( O H )9.376 ( H2 O )7.024 | Ganophyllite | 28 |
| * | 04-024-8347 | 18 | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | K0.19 Na7.69 Ca0.06 Al8 Si16 O48 ( H2 O )8 | Analcime | 6 |
| * | 01-074-1732 | 28 | Magnesium Silicate Hydroxide | Mg3 ( Si4 O10 ) ( O H )2 | Vermiculite-2M | 4 |
| * | 04-025-4215 | 40 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 23 |
| * | 04-014-4592 | 36 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.923 Na0.066 Mg1.488 Ti0.208 Fe1.148 Al1.443 Si2.715 O10.282 ( O H )1.421 F0.297 | Phlogopite-1M, Fe+2-bearing | 20 |

Anchor Scan Parameters

Dataset Name	24 Etosha22 sub 0.1-5cm S5

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 24\24 Etosha22 sub 0.1-5cm S5.xrdml

Sample Identification	24 Etosha22 sub 0.1-5cm S5

Measurement Start Date/Time	12/12/2023 10:29:00 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes