25 Etosha 22 sub 5-15 cm S5 550 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	41.0

Phase Potassium Sodium Magnesium Manganese Aluminum Iron Titanium Fluoride Aluminum Iron Silicate Hydroxide

Weight fraction/ %	26.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	9.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	10.0

Phase Potassium Sodium Aluminum Silicate

Weight fraction/ %	14.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Potassium Sodium Magnesium Manganese Aluminum Iron Titanium Fluoride Aluminum Iron Silicate Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Potassium Aluminum Silicate | Potassium Sodium Aluminum Silicate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Sulfate Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 25 Etosha22 sub 5-15cm S5 550C | 41.0 | 26.0 | 9.0 | 0.0 | 10.0 | 14.0 | 0.0 | 0.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6322.0000 | 6322.0000 | 6322.0000 |
| 2.0164 | 6495.2960 | 6284.7607 | 6284.7607 |
| 2.0274 | 6277.5084 | 6247.5214 | 6247.5214 |
| 2.0384 | 6257.2625 | 6210.2821 | 6210.2821 |
| 2.0494 | 6239.7207 | 6173.0428 | 6173.0428 |
| 2.0604 | 6264.2734 | 6135.8035 | 6135.8035 |
| 2.0714 | 6135.1298 | 6098.5642 | 6098.5642 |
| 2.0824 | 6171.9435 | 6061.3249 | 6061.3249 |
| 2.0934 | 6000.6922 | 6024.0856 | 6024.0856 |
| 2.1044 | 5918.3496 | 5986.8463 | 5986.8463 |
| 2.1154 | 6066.8928 | 5949.6070 | 5949.6070 |
| 2.1264 | 5906.4617 | 5912.3677 | 5912.3677 |
| 2.1374 | 5933.3776 | 5875.1284 | 5875.1284 |
| 2.1484 | 5900.1922 | 5837.8891 | 5837.8891 |
| 2.1594 | 5756.7601 | 5800.6498 | 5800.6498 |
| 2.1704 | 5692.4145 | 5763.4104 | 5763.4104 |
| 2.1814 | 5785.7738 | 5726.1711 | 5726.1711 |
| 2.1924 | 5706.3894 | 5688.9318 | 5688.9318 |
| 2.2034 | 5579.0443 | 5658.2349 | 5658.2349 |
| 2.2144 | 5655.8201 | 5627.5380 | 5627.5380 |
| 2.2254 | 5688.0315 | 5596.8411 | 5596.8411 |
| 2.2364 | 5536.4174 | 5566.1443 | 5566.1443 |
| 2.2474 | 5477.6077 | 5535.4474 | 5535.4474 |
| 2.2584 | 5404.6750 | 5504.7505 | 5504.7505 |
| 2.2694 | 5403.3805 | 5474.0536 | 5474.0536 |
| 2.2804 | 5367.2453 | 5443.3567 | 5443.3567 |
| 2.2914 | 5354.1849 | 5412.6598 | 5412.6598 |
| 2.3024 | 5396.5841 | 5381.9629 | 5381.9629 |
| 2.3134 | 5343.4887 | 5351.2660 | 5351.2660 |
| 2.3244 | 5234.0900 | 5320.5691 | 5320.5691 |
| 2.3354 | 5314.8142 | 5289.8722 | 5289.8722 |
| 2.3464 | 5252.6657 | 5259.1753 | 5259.1753 |
| 2.3574 | 5234.5605 | 5228.4784 | 5228.4784 |
| 2.3684 | 5213.1047 | 5197.7815 | 5197.7815 |
| 2.3794 | 5170.4041 | 5167.0846 | 5167.0846 |
| 2.3904 | 5136.6150 | 5147.5017 | 5147.5017 |
| 2.4014 | 5071.4690 | 5127.9188 | 5127.9188 |
| 2.4124 | 4991.8289 | 5108.3359 | 5108.3359 |
| 2.4234 | 5039.9518 | 5088.7530 | 5088.7530 |
| 2.4344 | 5041.5118 | 5069.1701 | 5069.1701 |
| 2.4454 | 5035.1740 | 5049.5872 | 5049.5872 |
| 2.4564 | 5032.8269 | 5030.0043 | 5030.0043 |
| 2.4674 | 5013.0649 | 5010.4214 | 5010.4214 |
| 2.4784 | 5009.7148 | 4990.8385 | 4990.8385 |
| 2.4894 | 4926.0423 | 4971.2556 | 4971.2556 |
| 2.5004 | 4941.9646 | 4951.6727 | 4951.6727 |
| 2.5114 | 5004.4769 | 4932.0898 | 4932.0898 |
| 2.5224 | 4946.1204 | 4912.5069 | 4912.5069 |
| 2.5334 | 4882.4012 | 4892.9240 | 4892.9240 |
| 2.5444 | 4797.9444 | 4873.3411 | 4873.3411 |
| 2.5554 | 4878.9833 | 4853.7582 | 4853.7582 |
| 2.5664 | 4828.2433 | 4834.1753 | 4834.1753 |
| 2.5774 | 4797.0177 | 4824.7346 | 4824.7346 |
| 2.5884 | 4907.6854 | 4815.2939 | 4815.2939 |
| 2.5994 | 4855.4336 | 4805.8532 | 4805.8532 |
| 2.6104 | 4803.9720 | 4796.4125 | 4796.4125 |
| 2.6214 | 4873.8948 | 4786.9717 | 4786.9717 |
| 2.6324 | 4901.0959 | 4777.5310 | 4777.5310 |
| 2.6434 | 4876.9007 | 4768.0903 | 4768.0903 |
| 2.6544 | 4751.9725 | 4758.6496 | 4758.6496 |
| 2.6654 | 4851.8053 | 4749.2089 | 4749.2089 |
| 2.6764 | 4855.0157 | 4739.7681 | 4739.7681 |
| 2.6874 | 4839.7620 | 4730.3274 | 4730.3274 |
| 2.6984 | 4771.0841 | 4720.8867 | 4720.8867 |
| 2.7094 | 4716.3884 | 4711.4460 | 4711.4460 |
| 2.7204 | 4704.6032 | 4702.0052 | 4702.0052 |
| 2.7314 | 4817.5693 | 4692.5645 | 4692.5645 |
| 2.7424 | 4846.4705 | 4683.1238 | 4683.1238 |
| 2.7534 | 4824.4336 | 4673.6831 | 4673.6831 |
| 2.7644 | 4732.6475 | 4664.1285 | 4664.1285 |
| 2.7754 | 4690.3284 | 4654.5739 | 4654.5739 |
| 2.7864 | 4708.6893 | 4645.0194 | 4645.0194 |
| 2.7974 | 4819.9646 | 4635.4648 | 4635.4648 |
| 2.8084 | 4655.4479 | 4625.9102 | 4625.9102 |
| 2.8194 | 4768.7021 | 4616.3557 | 4616.3557 |
| 2.8304 | 4792.1401 | 4606.8011 | 4606.8011 |
| 2.8414 | 4827.5624 | 4597.2465 | 4597.2465 |
| 2.8524 | 4906.6593 | 4587.6920 | 4587.6920 |
| 2.8634 | 4871.6932 | 4578.1374 | 4578.1374 |
| 2.8744 | 4728.2350 | 4568.5828 | 4568.5828 |
| 2.8854 | 4729.8997 | 4559.0283 | 4559.0283 |
| 2.8964 | 4782.7655 | 4549.4737 | 4549.4737 |
| 2.9074 | 4857.0315 | 4539.9191 | 4539.9191 |
| 2.9184 | 4859.7099 | 4530.3645 | 4530.3645 |
| 2.9294 | 4793.3333 | 4520.8100 | 4520.8100 |
| 2.9404 | 4684.0447 | 4511.2554 | 4511.2554 |
| 2.9514 | 4680.2665 | 4501.5775 | 4501.5775 |
| 2.9624 | 4610.2493 | 4491.8996 | 4491.8996 |
| 2.9734 | 4716.5929 | 4482.2217 | 4482.2217 |
| 2.9844 | 4672.6342 | 4472.5438 | 4472.5438 |
| 2.9954 | 4708.3097 | 4462.8659 | 4462.8659 |
| 3.0064 | 4565.0998 | 4453.1880 | 4453.1880 |
| 3.0174 | 4681.7699 | 4443.5101 | 4443.5101 |
| 3.0284 | 4736.2507 | 4433.8322 | 4433.8322 |
| 3.0394 | 4612.4877 | 4424.1543 | 4424.1543 |
| 3.0504 | 4705.7910 | 4414.4764 | 4414.4764 |
| 3.0614 | 4659.5634 | 4404.7985 | 4404.7985 |
| 3.0724 | 4634.4912 | 4395.1206 | 4395.1206 |
| 3.0834 | 4706.5024 | 4385.4427 | 4385.4427 |
| 3.0944 | 4625.9381 | 4375.7648 | 4375.7648 |
| 3.1054 | 4662.2262 | 4366.0869 | 4366.0869 |
| 3.1164 | 4673.4464 | 4356.4090 | 4356.4090 |
| 3.1274 | 4580.8672 | 4346.7311 | 4346.7311 |
| 3.1384 | 4561.4474 | 4336.9180 | 4336.9180 |
| 3.1494 | 4560.2950 | 4327.1048 | 4327.1048 |
| 3.1604 | 4543.8068 | 4317.2917 | 4317.2917 |
| 3.1714 | 4602.2350 | 4307.4786 | 4307.4786 |
| 3.1824 | 4559.9563 | 4297.6654 | 4297.6654 |
| 3.1934 | 4631.8761 | 4287.8523 | 4287.8523 |
| 3.2044 | 4512.2468 | 4278.0392 | 4278.0392 |
| 3.2154 | 4455.9705 | 4268.2260 | 4268.2260 |
| 3.2264 | 4517.1047 | 4258.4129 | 4258.4129 |
| 3.2374 | 4442.4936 | 4248.5997 | 4248.5997 |
| 3.2484 | 4425.2222 | 4238.7866 | 4238.7866 |
| 3.2594 | 4438.9086 | 4228.9735 | 4228.9735 |
| 3.2704 | 4497.7212 | 4219.1603 | 4219.1603 |
| 3.2814 | 4461.7011 | 4209.3472 | 4209.3472 |
| 3.2924 | 4421.7699 | 4199.5341 | 4199.5341 |
| 3.3034 | 4487.0344 | 4189.7209 | 4189.7209 |
| 3.3144 | 4442.5334 | 4179.8720 | 4179.9078 |
| 3.3254 | 4338.8732 | 4169.9491 | 4169.9491 |
| 3.3364 | 4392.9263 | 4159.9905 | 4159.9905 |
| 3.3474 | 4396.0393 | 4150.0318 | 4150.0318 |
| 3.3584 | 4376.9838 | 4140.0732 | 4140.0732 |
| 3.3694 | 4413.7709 | 4130.1145 | 4130.1145 |
| 3.3804 | 4423.0998 | 4120.1559 | 4120.1559 |
| 3.3914 | 4380.1416 | 4110.1972 | 4110.1972 |
| 3.4024 | 4389.3894 | 4100.2386 | 4100.2386 |
| 3.4134 | 4374.5664 | 4090.2799 | 4090.2799 |
| 3.4244 | 4440.1284 | 4080.3212 | 4080.3212 |
| 3.4354 | 4373.4975 | 4070.3626 | 4070.3626 |
| 3.4464 | 4343.2331 | 4060.4039 | 4060.4039 |
| 3.4574 | 4340.6755 | 4050.4453 | 4050.4453 |
| 3.4684 | 4346.7355 | 4040.4866 | 4040.4866 |
| 3.4794 | 4344.2960 | 4030.5280 | 4030.5280 |
| 3.4904 | 4282.2345 | 4020.5693 | 4020.5693 |
| 3.5014 | 4268.0885 | 4010.5732 | 4010.6107 |
| 3.5124 | 4330.7616 | 4000.4998 | 4000.4998 |
| 3.5234 | 4263.0177 | 3990.3889 | 3990.3889 |
| 3.5344 | 4345.2714 | 3980.2781 | 3980.2781 |
| 3.5454 | 4315.2763 | 3970.1672 | 3970.1672 |
| 3.5564 | 4306.7242 | 3960.0563 | 3960.0563 |
| 3.5674 | 4241.2124 | 3949.9454 | 3949.9454 |
| 3.5784 | 4199.3323 | 3939.8346 | 3939.8346 |
| 3.5894 | 4133.9469 | 3929.7237 | 3929.7237 |
| 3.6004 | 4161.3678 | 3919.6128 | 3919.6128 |
| 3.6114 | 4134.2753 | 3909.5020 | 3909.5020 |
| 3.6224 | 4174.8275 | 3899.3911 | 3899.3911 |
| 3.6334 | 4128.0265 | 3889.2802 | 3889.2802 |
| 3.6444 | 4112.5059 | 3879.1694 | 3879.1694 |
| 3.6554 | 4082.4720 | 3869.0585 | 3869.0585 |
| 3.6664 | 4106.1023 | 3858.9476 | 3858.9476 |
| 3.6774 | 4109.2635 | 3848.8368 | 3848.8368 |
| 3.6884 | 4078.1814 | 3838.6900 | 3838.7259 |
| 3.6994 | 4096.3206 | 3828.4690 | 3828.4690 |
| 3.7104 | 4089.9489 | 3818.2120 | 3818.2120 |
| 3.7214 | 4076.1563 | 3807.9551 | 3807.9551 |
| 3.7324 | 3936.4754 | 3797.6982 | 3797.6982 |
| 3.7434 | 4063.5300 | 3787.4412 | 3787.4412 |
| 3.7544 | 4009.0177 | 3777.1843 | 3777.1843 |
| 3.7654 | 3977.0029 | 3766.9274 | 3766.9274 |
| 3.7764 | 4028.8584 | 3756.6704 | 3756.6704 |
| 3.7874 | 4025.0442 | 3746.4135 | 3746.4135 |
| 3.7984 | 3991.8382 | 3736.1566 | 3736.1566 |
| 3.8094 | 3946.0856 | 3725.8997 | 3725.8997 |
| 3.8204 | 4012.5988 | 3715.6427 | 3715.6427 |
| 3.8314 | 3961.7020 | 3705.3858 | 3705.3858 |
| 3.8424 | 3912.2080 | 3695.1289 | 3695.1289 |
| 3.8534 | 3992.5663 | 3684.8719 | 3684.8719 |
| 3.8644 | 3807.3363 | 3674.6150 | 3674.6150 |
| 3.8754 | 3899.7522 | 3664.3242 | 3664.3581 |
| 3.8864 | 3824.3717 | 3653.9636 | 3653.9636 |
| 3.8974 | 3811.2547 | 3643.5690 | 3643.5690 |
| 3.9084 | 3830.2237 | 3633.1745 | 3633.1745 |
| 3.9194 | 3881.7994 | 3622.7800 | 3622.7800 |
| 3.9304 | 3810.9808 | 3612.3855 | 3612.3855 |
| 3.9414 | 3827.0845 | 3601.9910 | 3601.9910 |
| 3.9524 | 3761.4366 | 3591.5964 | 3591.5964 |
| 3.9634 | 3744.1318 | 3581.2019 | 3581.2019 |
| 3.9744 | 3749.5939 | 3570.8074 | 3570.8074 |
| 3.9854 | 3704.6726 | 3560.4129 | 3560.4129 |
| 3.9964 | 3729.4145 | 3550.0184 | 3550.0184 |
| 4.0074 | 3749.3127 | 3539.6238 | 3539.6238 |
| 4.0184 | 3726.0147 | 3529.2293 | 3529.2293 |
| 4.0294 | 3728.5241 | 3518.8348 | 3518.8348 |
| 4.0404 | 3774.1662 | 3508.4403 | 3508.4403 |
| 4.0514 | 3720.5073 | 3498.0458 | 3498.0458 |
| 4.0624 | 3639.4553 | 3487.6188 | 3487.6512 |
| 4.0734 | 3680.6961 | 3477.1247 | 3477.1247 |
| 4.0844 | 3597.3451 | 3466.5983 | 3466.5983 |
| 4.0954 | 3522.9528 | 3456.0718 | 3456.0718 |
| 4.1064 | 3528.5507 | 3445.5453 | 3445.5453 |
| 4.1174 | 3577.6372 | 3435.0188 | 3435.0188 |
| 4.1284 | 3600.0713 | 3424.4923 | 3424.4923 |
| 4.1394 | 3587.0098 | 3413.9658 | 3413.9658 |
| 4.1504 | 3562.4735 | 3403.4393 | 3403.4393 |
| 4.1614 | 3541.0049 | 3392.9128 | 3392.9128 |
| 4.1724 | 3464.6239 | 3382.3864 | 3382.3864 |
| 4.1834 | 3425.1504 | 3371.8599 | 3371.8599 |
| 4.1944 | 3408.7154 | 3361.3334 | 3361.3334 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 25 Etosha22 sub 5-15cm S5 550C | 2.0054 | 29.9894 | 0.0110 | 12/19/2023 1:10:33 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 8.8089 | 2075.02 | 0.1299 | 10.03034 | 100.00 |
| 13.5997 | 27.94 | 0.5196 | 6.50585 | 1.35 |
| 16.1396 | 508.10 | 0.0649 | 5.48728 | 24.49 |
| 17.6792 | 128.39 | 0.1732 | 5.01272 | 6.19 |
| 19.5545 | 35.23 | 0.4330 | 4.53603 | 1.70 |
| 21.1087 | 23.71 | 0.2598 | 4.20543 | 1.14 |
| 22.5399 | 107.39 | 0.2165 | 3.94152 | 5.18 |
| 23.5158 | 57.52 | 0.1732 | 3.78011 | 2.77 |
| 26.4712 | 580.46 | 0.0866 | 3.36440 | 27.97 |
| 27.5836 | 566.46 | 0.0866 | 3.23119 | 27.30 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-015-8194 | 56 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.81 Na0.1 Mg1.88 Ti0.27 Fe0.76 Al1.46 Si2.62 O10.69 ( O H )1.15 F0.16 | Phlogopite-1M | 41 |
| * | 01-076-8341 | 44 | Potassium Sodium Magnesium Manganese Aluminum Iron Titanium Fluoride Aluminum Iron Silicate Hydroxide | ( K0.97 Na0.05 ) ( Fe0.54 Mg0.28 Mn0.01 ) ( Fe0.27 Al0.305 Mg0.355 Ti0.07 )2 ( ( Si2.63 Al1.21 Fe0.16 ) O10.15 ) ( O H )1.78 F0.07 | Biotite-1M | 26 |
| * | 04-013-5979 | 24 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 9 |
| * | 01-075-8689 | No Matching Lines | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | - |
| * | 01-070-3751 | 29 | Potassium Aluminum Silicate | K ( Al Si3 O8 ) | Sanidine | 10 |
| * | 04-011-0528 | 25 | Potassium Sodium Aluminum Silicate | K0.9 Na0.1 Al Si3 O8 | Microcline, Na-bearing | 14 |
| * | 04-025-4215 | No Matching Lines | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | - |
| * | 04-009-8713 | No Matching Lines | Magnesium Sulfate Hydrate | Mg ( S O4 ) ( H2 O )6 | Hexahydrite, syn | - |

Anchor Scan Parameters

Dataset Name	25 Etosha22 sub 5-15cm S5 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 25\25 Etosha22 sub 5-15cm S5 550C.xrdml

Sample Identification	25 Etosha22 sub 5-15cm S5 550C

Measurement Start Date/Time	12/19/2023 1:10:33 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes