25 Etosha 22 sub 5-15 cm S5 regular

Graphics

Graphics

Graphics

Quantitative Results

Phase Silicon Oxide

Weight fraction/ %	5.0

Phase Sodium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	8.0

Phase Titanium Oxide

Weight fraction/ %	4.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	7.0

Phase Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	5.0

Phase Potassium Manganese Silicate Hydroxide Hydrate

Weight fraction/ %	7.0

Phase Potassium Magnesium Aluminum Iron Silicon Oxide Hydroxide

Weight fraction/ %	21.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	24.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	13.0

Phase Copper Arsenate Chloride Hydroxide Hydrate

Weight fraction/ %	3.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Silicon Oxide | Sodium Aluminum Silicon Oxide Hydrate | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Magnesium Silicate Hydroxide Hydrate | Potassium Manganese Silicate Hydroxide Hydrate | Potassium Magnesium Aluminum Iron Silicon Oxide Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Aluminum Silicate | Copper Arsenate Chloride Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 25 Etosha22 Sub 5-15cm S5 | 5.0 | 8.0 | 4.0 | 7.0 | 2.0 | 5.0 | 7.0 | 21.0 | 24.0 | 13.0 | 3.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6795.0000 | 6775.0934 | 6795.0000 |
| 2.0164 | 6570.1967 | 6743.2821 | 6740.6320 |
| 2.0274 | 6583.9597 | 6688.9293 | 6686.2640 |
| 2.0384 | 6509.3053 | 6634.5766 | 6631.8960 |
| 2.0494 | 6659.5457 | 6580.2240 | 6577.5280 |
| 2.0604 | 6383.0728 | 6525.8716 | 6523.1600 |
| 2.0714 | 6422.9941 | 6471.5193 | 6468.7920 |
| 2.0824 | 6334.6559 | 6417.1671 | 6414.4240 |
| 2.0934 | 6322.6421 | 6362.8151 | 6360.0560 |
| 2.1044 | 6240.5796 | 6308.4632 | 6305.6880 |
| 2.1154 | 6211.5034 | 6254.1115 | 6251.3200 |
| 2.1264 | 6266.3274 | 6199.7599 | 6196.9520 |
| 2.1374 | 5973.7316 | 6145.4084 | 6142.5840 |
| 2.1484 | 6080.2424 | 6091.0571 | 6088.2161 |
| 2.1594 | 6042.0914 | 6036.7059 | 6033.8481 |
| 2.1704 | 5900.9720 | 5982.3549 | 5979.4801 |
| 2.1814 | 5887.0836 | 5928.0040 | 5925.1121 |
| 2.1924 | 5861.9852 | 5882.1579 | 5870.7441 |
| 2.2034 | 5850.5221 | 5839.8147 | 5836.8880 |
| 2.2144 | 5847.3417 | 5805.9763 | 5803.0320 |
| 2.2254 | 5782.4484 | 5772.1380 | 5769.1759 |
| 2.2364 | 5798.8879 | 5738.2999 | 5735.3199 |
| 2.2474 | 5621.3815 | 5704.4619 | 5701.4638 |
| 2.2584 | 5746.0093 | 5670.6241 | 5667.6078 |
| 2.2694 | 5609.8466 | 5636.7865 | 5633.7517 |
| 2.2804 | 5528.3909 | 5602.9490 | 5599.8957 |
| 2.2914 | 5517.3609 | 5569.1117 | 5566.0396 |
| 2.3024 | 5562.4602 | 5535.2746 | 5532.1836 |
| 2.3134 | 5626.0590 | 5501.4376 | 5498.3276 |
| 2.3244 | 5559.7325 | 5467.6009 | 5464.4715 |
| 2.3354 | 5522.3510 | 5433.7643 | 5430.6155 |
| 2.3464 | 5465.2817 | 5399.9279 | 5396.7594 |
| 2.3574 | 5425.2802 | 5366.0916 | 5362.9034 |
| 2.3684 | 5348.2360 | 5332.2556 | 5329.0473 |
| 2.3794 | 5284.4464 | 5301.6908 | 5295.1913 |
| 2.3904 | 5260.1362 | 5272.4735 | 5269.2247 |
| 2.4014 | 5197.2655 | 5246.5275 | 5243.2581 |
| 2.4124 | 5228.4449 | 5220.5817 | 5217.2915 |
| 2.4234 | 5228.3530 | 5194.6361 | 5191.3249 |
| 2.4344 | 5203.7094 | 5168.6907 | 5165.3583 |
| 2.4454 | 5164.7158 | 5142.7455 | 5139.3917 |
| 2.4564 | 5124.0477 | 5116.8005 | 5113.4251 |
| 2.4674 | 5161.4690 | 5090.8557 | 5087.4585 |
| 2.4784 | 5115.7571 | 5064.9111 | 5061.4920 |
| 2.4894 | 4955.4395 | 5038.9667 | 5035.5254 |
| 2.5004 | 4937.5929 | 5013.0226 | 5009.5588 |
| 2.5114 | 4952.1308 | 4987.0786 | 4983.5922 |
| 2.5224 | 4925.2714 | 4961.1349 | 4957.6256 |
| 2.5334 | 4837.7434 | 4935.1914 | 4931.6590 |
| 2.5444 | 4874.7144 | 4909.2482 | 4905.6924 |
| 2.5554 | 4931.8437 | 4883.3052 | 4879.7258 |
| 2.5664 | 5011.9823 | 4857.3624 | 4853.7592 |
| 2.5774 | 4875.5683 | 4831.4198 | 4827.7926 |
| 2.5884 | 4784.3771 | 4805.4775 | 4801.8260 |
| 2.5994 | 4836.7965 | 4779.5354 | 4775.8595 |
| 2.6104 | 4793.7512 | 4753.5936 | 4749.8929 |
| 2.6214 | 4700.0531 | 4727.6520 | 4723.9263 |
| 2.6324 | 4704.9277 | 4701.7107 | 4697.9597 |
| 2.6434 | 4691.1976 | 4675.7697 | 4671.9931 |
| 2.6544 | 4677.0993 | 4649.8289 | 4646.0265 |
| 2.6654 | 4643.5516 | 4623.8883 | 4620.0599 |
| 2.6764 | 4707.7252 | 4597.9481 | 4594.0933 |
| 2.6874 | 4661.3677 | 4572.0081 | 4568.1267 |
| 2.6984 | 4515.1062 | 4546.0683 | 4542.1601 |
| 2.7094 | 4516.7581 | 4520.1289 | 4516.1935 |
| 2.7204 | 4508.6249 | 4494.1897 | 4490.2270 |
| 2.7314 | 4598.9115 | 4468.2509 | 4464.2604 |
| 2.7424 | 4481.8284 | 4442.3123 | 4438.2938 |
| 2.7534 | 4345.0187 | 4417.6174 | 4412.3272 |
| 2.7644 | 4405.4159 | 4393.4348 | 4389.3594 |
| 2.7754 | 4273.7365 | 4370.4960 | 4366.3916 |
| 2.7864 | 4330.2852 | 4347.5574 | 4343.4238 |
| 2.7974 | 4338.4602 | 4324.6192 | 4320.4561 |
| 2.8084 | 4320.9523 | 4301.9480 | 4297.4883 |
| 2.8194 | 4342.6480 | 4280.2975 | 4274.5205 |
| 2.8304 | 4124.6829 | 4257.5018 | 4251.5527 |
| 2.8414 | 4275.0757 | 4235.2177 | 4228.5849 |
| 2.8524 | 4220.7512 | 4212.2931 | 4205.6172 |
| 2.8634 | 4108.6667 | 4189.3689 | 4182.6494 |
| 2.8744 | 4069.0442 | 4166.4451 | 4159.6816 |
| 2.8854 | 4101.4317 | 4143.5219 | 4136.7138 |
| 2.8964 | 4108.9690 | 4120.5990 | 4113.7461 |
| 2.9074 | 4218.9538 | 4097.6766 | 4090.7783 |
| 2.9184 | 4087.7660 | 4074.7547 | 4067.8105 |
| 2.9294 | 4120.6519 | 4051.8333 | 4044.8427 |
| 2.9404 | 3991.8948 | 4028.9123 | 4021.8749 |
| 2.9514 | 4016.9882 | 4005.9918 | 3998.9072 |
| 2.9624 | 4106.4336 | 3983.0718 | 3975.9394 |
| 2.9734 | 3990.9764 | 3960.1523 | 3952.9716 |
| 2.9844 | 4119.4400 | 3937.2333 | 3930.0038 |
| 2.9954 | 3956.1593 | 3914.3148 | 3907.0360 |
| 3.0064 | 4002.7866 | 3891.3968 | 3884.0683 |
| 3.0174 | 3953.6686 | 3868.4794 | 3861.1005 |
| 3.0284 | 3864.6843 | 3845.5625 | 3838.1327 |
| 3.0394 | 3754.6519 | 3822.6461 | 3815.1649 |
| 3.0504 | 3834.0944 | 3799.7303 | 3792.1971 |
| 3.0614 | 3891.5074 | 3776.8150 | 3769.2294 |
| 3.0724 | 3804.1863 | 3753.9003 | 3746.2616 |
| 3.0834 | 3851.6381 | 3730.9862 | 3723.2938 |
| 3.0944 | 3773.2566 | 3708.0726 | 3700.3260 |
| 3.1054 | 3717.7089 | 3685.1597 | 3677.3583 |
| 3.1164 | 3685.1362 | 3662.2473 | 3654.3905 |
| 3.1274 | 3626.7876 | 3644.2206 | 3631.4227 |
| 3.1384 | 3630.7404 | 3628.2066 | 3620.2371 |
| 3.1494 | 3491.2960 | 3617.0783 | 3609.0515 |
| 3.1604 | 3546.1844 | 3605.9506 | 3597.8659 |
| 3.1714 | 3589.2576 | 3594.8236 | 3586.6803 |
| 3.1824 | 3544.8117 | 3583.6972 | 3575.4947 |
| 3.1934 | 3575.0354 | 3572.5715 | 3564.3091 |
| 3.2044 | 3568.6219 | 3561.4464 | 3553.1235 |
| 3.2154 | 3594.2734 | 3550.3221 | 3541.9379 |
| 3.2264 | 3584.0604 | 3539.1984 | 3530.7523 |
| 3.2374 | 3472.3894 | 3528.0754 | 3519.5667 |
| 3.2484 | 3512.6111 | 3516.9532 | 3508.3811 |
| 3.2594 | 3517.2537 | 3505.8317 | 3497.1955 |
| 3.2704 | 3442.1731 | 3494.7109 | 3486.0099 |
| 3.2814 | 3503.1613 | 3483.5909 | 3474.8243 |
| 3.2924 | 3542.7566 | 3472.4716 | 3463.6387 |
| 3.3034 | 3530.5841 | 3461.3532 | 3452.4531 |
| 3.3144 | 3490.1597 | 3450.2355 | 3441.2675 |
| 3.3254 | 3465.9617 | 3439.1186 | 3430.0819 |
| 3.3364 | 3467.9415 | 3428.0025 | 3418.8963 |
| 3.3474 | 3372.9971 | 3416.8873 | 3407.7107 |
| 3.3584 | 3373.4410 | 3405.7729 | 3396.5251 |
| 3.3694 | 3335.8859 | 3394.6593 | 3385.3395 |
| 3.3804 | 3449.8958 | 3383.5467 | 3374.1539 |
| 3.3914 | 3427.8583 | 3372.4349 | 3362.9683 |
| 3.4024 | 3383.4130 | 3361.3240 | 3351.7827 |
| 3.4134 | 3363.7443 | 3350.2140 | 3340.5971 |
| 3.4244 | 3270.6239 | 3339.1050 | 3329.4115 |
| 3.4354 | 3236.2389 | 3327.9969 | 3318.2259 |
| 3.4464 | 3280.8609 | 3316.8897 | 3307.0403 |
| 3.4574 | 3241.1770 | 3305.7835 | 3295.8547 |
| 3.4684 | 3240.1603 | 3294.6784 | 3284.6691 |
| 3.4794 | 3235.2379 | 3283.5742 | 3273.4835 |
| 3.4904 | 3216.3628 | 3272.4711 | 3262.2979 |
| 3.5014 | 3261.3393 | 3262.0171 | 3251.1123 |
| 3.5124 | 3279.8968 | 3251.8312 | 3241.4900 |
| 3.5234 | 3243.1917 | 3242.2946 | 3231.8677 |
| 3.5344 | 3230.1254 | 3232.7590 | 3222.2454 |
| 3.5454 | 3193.5211 | 3223.2246 | 3212.6231 |
| 3.5564 | 3209.7876 | 3213.6913 | 3203.0008 |
| 3.5674 | 3177.0256 | 3204.1591 | 3193.3785 |
| 3.5784 | 3214.2758 | 3194.6281 | 3183.7562 |
| 3.5894 | 3192.5044 | 3185.0984 | 3174.1339 |
| 3.6004 | 3139.5433 | 3175.5699 | 3164.5115 |
| 3.6114 | 3130.3835 | 3166.0426 | 3154.8892 |
| 3.6224 | 3178.6003 | 3156.5165 | 3145.2669 |
| 3.6334 | 3081.0629 | 3146.9918 | 3135.6446 |
| 3.6444 | 3108.5448 | 3137.4684 | 3126.0223 |
| 3.6554 | 3119.0000 | 3127.9463 | 3116.4000 |
| 3.6664 | 3107.0167 | 3118.4256 | 3106.7777 |
| 3.6774 | 3058.9833 | 3108.9063 | 3097.1554 |
| 3.6884 | 3103.9513 | 3101.5227 | 3087.5330 |
| 3.6994 | 3033.3245 | 3095.0195 | 3083.0583 |
| 3.7104 | 3185.1102 | 3090.6521 | 3078.5836 |
| 3.7214 | 3093.7463 | 3086.2862 | 3074.1089 |
| 3.7324 | 3113.7503 | 3081.9219 | 3069.6342 |
| 3.7434 | 3022.7433 | 3077.5591 | 3065.1595 |
| 3.7544 | 3000.7773 | 3073.1978 | 3060.6847 |
| 3.7654 | 2923.6411 | 3068.8382 | 3056.2100 |
| 3.7764 | 2895.5496 | 3064.4803 | 3051.7353 |
| 3.7874 | 2893.0177 | 3060.1240 | 3047.2606 |
| 3.7984 | 3023.9277 | 3055.7694 | 3042.7859 |
| 3.8094 | 3004.3688 | 3051.4166 | 3038.3112 |
| 3.8204 | 3088.7109 | 3047.0655 | 3033.8364 |
| 3.8314 | 3041.5005 | 3042.7163 | 3029.3617 |
| 3.8424 | 2983.6834 | 3038.3690 | 3024.8870 |
| 3.8534 | 3016.7906 | 3034.0235 | 3020.4123 |
| 3.8644 | 3048.2006 | 3029.6799 | 3015.9376 |
| 3.8754 | 2959.1957 | 3025.3384 | 3011.4629 |
| 3.8864 | 3101.5088 | 3020.9988 | 3006.9881 |
| 3.8974 | 2918.2842 | 3016.6613 | 3002.5134 |
| 3.9084 | 3019.5634 | 3012.3259 | 2998.0387 |
| 3.9194 | 2915.4986 | 3007.9926 | 2993.5640 |
| 3.9304 | 3019.6603 | 3003.6615 | 2989.0893 |
| 3.9414 | 3015.6155 | 2999.3327 | 2984.6146 |
| 3.9524 | 2954.3717 | 2995.0061 | 2980.1398 |
| 3.9634 | 2980.9243 | 2990.6819 | 2975.6651 |
| 3.9744 | 2950.8024 | 2986.3600 | 2971.1904 |
| 3.9854 | 2965.5398 | 2982.0405 | 2966.7157 |
| 3.9964 | 2937.3166 | 2977.7236 | 2962.2410 |
| 4.0074 | 2876.6204 | 2973.4091 | 2957.7663 |
| 4.0184 | 2856.6151 | 2969.0973 | 2953.2915 |
| 4.0294 | 2983.5378 | 2964.7881 | 2948.8168 |
| 4.0404 | 2945.7847 | 2960.4816 | 2944.3421 |
| 4.0514 | 2935.1593 | 2956.1779 | 2939.8674 |
| 4.0624 | 2941.8117 | 2952.5801 | 2935.3927 |
| 4.0734 | 2905.9823 | 2949.2747 | 2932.6136 |
| 4.0844 | 2942.1681 | 2946.6754 | 2929.8346 |
| 4.0954 | 2935.2291 | 2944.0790 | 2927.0555 |
| 4.1064 | 2926.4169 | 2941.4858 | 2924.2764 |
| 4.1174 | 2967.7227 | 2938.8957 | 2921.4974 |
| 4.1284 | 2936.2522 | 2936.3089 | 2918.7183 |
| 4.1394 | 2894.5437 | 2933.7254 | 2915.9393 |
| 4.1504 | 2909.1048 | 2931.1453 | 2913.1602 |
| 4.1614 | 2983.2252 | 2928.5687 | 2910.3811 |
| 4.1724 | 2902.2949 | 2925.9957 | 2907.6021 |
| 4.1834 | 2817.1770 | 2923.4263 | 2904.8230 |
| 4.1944 | 2933.5521 | 2920.8606 | 2902.0440 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 25 Etosha22 Sub 5-15cm S5 | 2.0054 | 29.9894 | 0.0110 | 12/13/2023 11:37:28 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.8554 | 1031.27 | 0.5196 | 15.08145 | 62.54 |
| 7.1427 | 1648.85 | 0.4330 | 12.36612 | 100.00 |
| 8.7426 | 884.65 | 0.1082 | 10.10626 | 53.65 |
| 13.1974 | 32.24 | 0.6927 | 6.70323 | 1.96 |
| 15.7503 | 754.72 | 0.0974 | 5.62202 | 45.77 |
| 17.6716 | 106.59 | 0.1732 | 5.01487 | 6.46 |
| 18.2403 | 96.66 | 0.0866 | 4.85976 | 5.86 |
| 19.5967 | 53.73 | 0.6061 | 4.52635 | 3.26 |
| 20.8849 | 81.69 | 0.1299 | 4.24997 | 4.95 |
| 22.4053 | 180.79 | 0.1299 | 3.96489 | 10.96 |
| 23.4214 | 94.80 | 0.0866 | 3.79514 | 5.75 |
| 25.9117 | 695.54 | 0.0541 | 3.43577 | 42.18 |
| 26.7095 | 515.24 | 0.1515 | 3.33492 | 31.25 |
| 27.5427 | 407.44 | 0.1515 | 3.23590 | 24.71 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-016-2085 | 52 | Silicon Oxide | Si O2 | Quartz | 5 |
| * | 04-009-3254 | 46 | Sodium Aluminum Silicon Oxide Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 8 |
| * | 04-016-2838 | 51 | Titanium Oxide | Ti O2 | Rutile | 4 |
| * | 04-017-4317 | 37 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 7 |
| * | 04-017-7292 | 35 | Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Ca0.465 Mg2.810 Fe0.065 Al1.190 Si2.895 O10 ( O H )2 ( H2 O )4 | Vermiculite | 2 |
| * | 01-080-5019 | 19 | Magnesium Silicate Hydroxide Hydrate | Mg7.68 ( Si12 O30 ) ( O H )4 ( H2 O )4 ( H2 O )6 | Sepiolite | 5 |
| * | 01-089-6415 | 29 | Potassium Manganese Silicate Hydroxide Hydrate | K3.68 Mn15.904 Si25.472 O64 ( O H )9.376 ( H2 O )7.024 | Ganophyllite | 7 |
| * | 04-020-0786 | 29 | Potassium Magnesium Aluminum Iron Silicon Oxide Hydroxide | K Mg2 Fe Al Si3 O11 ( O H ) | Phlogopite-2M1 | 21 |
| * | 04-025-4215 | 10 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 24 |
| * | 04-025-6511 | 18 | Potassium Aluminum Silicate | K Al Si3 O8 | Microcline | 13 |
| * | 01-083-3890 | 24 | Copper Arsenate Chloride Hydroxide Hydrate | Cu10 ( As O4 )2 ( Cl0.9 ( O H )13.1 ) ( H2 O )4.3 | Parnauite | 3 |

Anchor Scan Parameters

Dataset Name	25 Etosha22 Sub 5-15cm S5

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 25\25 Etosha22 Sub 5-15cm S5.xrdml

Sample Identification	25 Etosha22 Sub 5-15cm S5

Measurement Start Date/Time	12/13/2023 11:37:28 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes