25 Etosha 22 sub 5-15 cm S5 REPLICATE 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	13.0

Phase Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	15.0

Phase Potassium Sodium Aluminum Silicate

Weight fraction/ %	20.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	19.0

Phase Potassium Magnesium Aluminum Iron Silicon Titanium Oxide Chloride Fluoride Hydroxide

Weight fraction/ %	25.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	3.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | Potassium Aluminum Silicate | Potassium Sodium Aluminum Silicate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Magnesium Aluminum Iron Silicon Titanium Oxide Chloride Fluoride Hydroxide | Sodium Magnesium Silicon Oxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 25 400c | 13.0 | 3.0 | 15.0 | 20.0 | 19.0 | 25.0 | 3.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 4606.0000 | 4600.0923 | 4606.0000 |
| 2.0164 | 4542.8156 | 4574.6873 | 4573.1740 |
| 2.0274 | 4525.2960 | 4541.8748 | 4540.3479 |
| 2.0384 | 4416.3776 | 4509.0625 | 4507.5219 |
| 2.0494 | 4374.6391 | 4476.2504 | 4474.6959 |
| 2.0604 | 4383.4970 | 4443.4385 | 4441.8698 |
| 2.0714 | 4325.2065 | 4410.6268 | 4409.0438 |
| 2.0824 | 4271.0226 | 4377.8152 | 4376.2178 |
| 2.0934 | 4335.2950 | 4345.0039 | 4343.3917 |
| 2.1044 | 4335.3451 | 4312.1928 | 4310.5657 |
| 2.1154 | 4300.7257 | 4279.3818 | 4277.7397 |
| 2.1264 | 4222.2242 | 4246.5711 | 4244.9136 |
| 2.1374 | 4300.1888 | 4213.7606 | 4212.0876 |
| 2.1484 | 4163.9425 | 4180.9503 | 4179.2616 |
| 2.1594 | 4203.9518 | 4148.1403 | 4146.4355 |
| 2.1704 | 4078.4027 | 4115.3304 | 4113.6095 |
| 2.1814 | 4090.6981 | 4082.5208 | 4080.7835 |
| 2.1924 | 3998.3722 | 4052.8724 | 4047.9574 |
| 2.2034 | 4065.7168 | 4030.9098 | 4029.1389 |
| 2.2144 | 3988.2090 | 4012.1084 | 4010.3204 |
| 2.2254 | 4081.4661 | 3993.3073 | 3991.5019 |
| 2.2364 | 3883.6814 | 3974.5064 | 3972.6833 |
| 2.2474 | 3923.5565 | 3955.7058 | 3953.8648 |
| 2.2584 | 3886.4636 | 3936.9054 | 3935.0463 |
| 2.2694 | 3933.3156 | 3918.1053 | 3916.2278 |
| 2.2804 | 3891.9381 | 3899.3054 | 3897.4093 |
| 2.2914 | 3839.8368 | 3880.5059 | 3878.5907 |
| 2.3024 | 3827.7965 | 3861.7066 | 3859.7722 |
| 2.3134 | 3897.2861 | 3842.9076 | 3840.9537 |
| 2.3244 | 3886.0797 | 3824.1089 | 3822.1352 |
| 2.3354 | 3841.1239 | 3805.3105 | 3803.3167 |
| 2.3464 | 3729.7739 | 3786.5124 | 3784.4981 |
| 2.3574 | 3765.3835 | 3767.7146 | 3765.6796 |
| 2.3684 | 3685.9867 | 3748.9172 | 3746.8611 |
| 2.3794 | 3732.4326 | 3730.8096 | 3728.0426 |
| 2.3904 | 3749.4641 | 3714.3789 | 3712.2798 |
| 2.4014 | 3735.0088 | 3698.6382 | 3696.5170 |
| 2.4124 | 3671.8948 | 3682.8978 | 3680.7542 |
| 2.4234 | 3603.8387 | 3667.1577 | 3664.9914 |
| 2.4344 | 3600.5133 | 3651.4180 | 3649.2286 |
| 2.4454 | 3656.1908 | 3635.6787 | 3633.4658 |
| 2.4564 | 3667.4410 | 3619.9397 | 3617.7030 |
| 2.4674 | 3637.8024 | 3604.2011 | 3601.9402 |
| 2.4784 | 3606.9582 | 3588.4630 | 3586.1774 |
| 2.4894 | 3575.8269 | 3572.7252 | 3570.4146 |
| 2.5004 | 3604.5664 | 3556.9878 | 3554.6518 |
| 2.5114 | 3616.9921 | 3541.2508 | 3538.8890 |
| 2.5224 | 3564.0723 | 3525.5143 | 3523.1262 |
| 2.5334 | 3544.1298 | 3509.7782 | 3507.3634 |
| 2.5444 | 3494.0010 | 3494.0425 | 3491.6006 |
| 2.5554 | 3432.5742 | 3478.3073 | 3475.8378 |
| 2.5664 | 3446.7153 | 3464.0191 | 3460.0750 |
| 2.5774 | 3491.2045 | 3453.2485 | 3450.7224 |
| 2.5884 | 3466.2630 | 3443.9249 | 3441.3698 |
| 2.5994 | 3471.5487 | 3434.6018 | 3432.0172 |
| 2.6104 | 3453.9036 | 3425.2793 | 3422.6647 |
| 2.6214 | 3389.4425 | 3415.9572 | 3413.3121 |
| 2.6324 | 3352.2876 | 3406.6357 | 3403.9595 |
| 2.6434 | 3387.3471 | 3397.3148 | 3394.6069 |
| 2.6544 | 3396.0231 | 3387.9943 | 3385.2543 |
| 2.6654 | 3449.0472 | 3378.6745 | 3375.9018 |
| 2.6764 | 3414.2679 | 3369.3553 | 3366.5492 |
| 2.6874 | 3400.5723 | 3360.0366 | 3357.1966 |
| 2.6984 | 3403.5487 | 3350.7186 | 3347.8440 |
| 2.7094 | 3322.1907 | 3341.4012 | 3338.4914 |
| 2.7204 | 3369.5059 | 3332.0845 | 3329.1389 |
| 2.7314 | 3335.0826 | 3322.7684 | 3319.7863 |
| 2.7424 | 3360.8810 | 3313.4530 | 3310.4337 |
| 2.7534 | 3262.0187 | 3304.6399 | 3301.0811 |
| 2.7644 | 3293.5811 | 3297.0472 | 3293.9514 |
| 2.7754 | 3258.2606 | 3289.9569 | 3286.8217 |
| 2.7864 | 3341.7571 | 3282.8673 | 3279.6919 |
| 2.7974 | 3321.3717 | 3275.7785 | 3272.5622 |
| 2.8084 | 3245.2202 | 3268.6905 | 3265.4325 |
| 2.8194 | 3340.6873 | 3261.6034 | 3258.3028 |
| 2.8304 | 3327.9543 | 3254.5171 | 3251.1730 |
| 2.8414 | 3252.2045 | 3247.4317 | 3244.0433 |
| 2.8524 | 3309.4631 | 3240.3473 | 3236.9136 |
| 2.8634 | 3186.4513 | 3233.2638 | 3229.7839 |
| 2.8744 | 3248.9695 | 3226.1812 | 3222.6541 |
| 2.8854 | 3147.7551 | 3219.0997 | 3215.5244 |
| 2.8964 | 3249.5398 | 3212.0193 | 3208.3947 |
| 2.9074 | 3276.0393 | 3204.9400 | 3201.2650 |
| 2.9184 | 3278.8432 | 3197.8618 | 3194.1352 |
| 2.9294 | 3174.7139 | 3190.7847 | 3187.0055 |
| 2.9404 | 3198.7739 | 3183.7089 | 3179.8758 |
| 2.9514 | 3256.0039 | 3176.6344 | 3172.7461 |
| 2.9624 | 3225.5649 | 3169.5612 | 3165.6163 |
| 2.9734 | 3256.4090 | 3162.4894 | 3158.4866 |
| 2.9844 | 3213.5585 | 3155.4190 | 3151.3569 |
| 2.9954 | 3192.9735 | 3148.3501 | 3144.2272 |
| 3.0064 | 3215.8673 | 3141.2828 | 3137.0974 |
| 3.0174 | 3188.6224 | 3134.2171 | 3129.9677 |
| 3.0284 | 3111.4263 | 3127.1531 | 3122.8380 |
| 3.0394 | 3118.6234 | 3120.0909 | 3115.7083 |
| 3.0504 | 3189.0496 | 3113.0306 | 3108.5785 |
| 3.0614 | 3091.2596 | 3105.9722 | 3101.4488 |
| 3.0724 | 3093.9243 | 3098.9159 | 3094.3191 |
| 3.0834 | 3062.3884 | 3091.8617 | 3087.1894 |
| 3.0944 | 3024.6903 | 3084.8098 | 3080.0596 |
| 3.1054 | 3138.0865 | 3077.7603 | 3072.9299 |
| 3.1164 | 3079.4125 | 3070.7133 | 3065.8002 |
| 3.1274 | 3028.1033 | 3063.6443 | 3058.6704 |
| 3.1384 | 3047.1382 | 3056.5351 | 3051.4486 |
| 3.1494 | 3061.2006 | 3049.4042 | 3044.2267 |
| 3.1604 | 3097.9248 | 3042.2763 | 3037.0048 |
| 3.1714 | 3055.0973 | 3035.1517 | 3029.7830 |
| 3.1824 | 3033.7817 | 3028.0305 | 3022.5611 |
| 3.1934 | 3056.4071 | 3020.9128 | 3015.3392 |
| 3.2044 | 3057.4631 | 3013.7989 | 3008.1174 |
| 3.2154 | 3010.0964 | 3006.6890 | 3000.8955 |
| 3.2264 | 3061.4307 | 2999.5832 | 2993.6736 |
| 3.2374 | 3059.8485 | 2992.4819 | 2986.4517 |
| 3.2484 | 2930.2222 | 2985.3852 | 2979.2299 |
| 3.2594 | 2897.2035 | 2978.2934 | 2972.0080 |
| 3.2704 | 2937.0394 | 2971.2068 | 2964.7861 |
| 3.2814 | 2986.3166 | 2964.1257 | 2957.5643 |
| 3.2924 | 2948.8982 | 2957.0503 | 2950.3424 |
| 3.3034 | 2909.4503 | 2949.9809 | 2943.1205 |
| 3.3144 | 2923.8791 | 2943.0108 | 2935.8986 |
| 3.3254 | 2939.5251 | 2936.2096 | 2929.0248 |
| 3.3364 | 2962.3864 | 2929.5084 | 2922.1509 |
| 3.3474 | 2959.5270 | 2922.8147 | 2915.2770 |
| 3.3584 | 2902.3156 | 2916.1288 | 2908.4032 |
| 3.3694 | 2866.6627 | 2909.4511 | 2901.5293 |
| 3.3804 | 2864.8274 | 2902.7821 | 2894.6554 |
| 3.3914 | 2938.6814 | 2896.1221 | 2887.7816 |
| 3.4024 | 2923.0747 | 2889.4717 | 2880.9077 |
| 3.4134 | 2812.6873 | 2882.8313 | 2874.0338 |
| 3.4244 | 2797.5929 | 2876.2015 | 2867.1600 |
| 3.4354 | 2833.5329 | 2869.5826 | 2860.2861 |
| 3.4464 | 2856.9823 | 2862.9753 | 2853.4122 |
| 3.4574 | 2839.7257 | 2856.3800 | 2846.5384 |
| 3.4684 | 2818.0182 | 2849.7974 | 2839.6645 |
| 3.4794 | 2806.8830 | 2843.2279 | 2832.7906 |
| 3.4904 | 2816.8451 | 2836.6722 | 2825.9168 |
| 3.5014 | 2787.7345 | 2830.4809 | 2819.0429 |
| 3.5124 | 2825.3938 | 2824.9166 | 2813.4811 |
| 3.5234 | 2896.2508 | 2819.7178 | 2807.9193 |
| 3.5344 | 2770.7664 | 2814.5354 | 2802.3575 |
| 3.5454 | 2788.1200 | 2809.3697 | 2796.7957 |
| 3.5564 | 2751.2935 | 2804.2216 | 2791.2340 |
| 3.5674 | 2683.0256 | 2799.0916 | 2785.6722 |
| 3.5784 | 2771.0364 | 2793.9805 | 2780.1104 |
| 3.5894 | 2795.5310 | 2788.8888 | 2774.5486 |
| 3.6004 | 2839.9322 | 2783.8173 | 2768.9868 |
| 3.6114 | 2761.6332 | 2778.7667 | 2763.4250 |
| 3.6224 | 2786.4071 | 2773.7375 | 2757.8632 |
| 3.6334 | 2744.7601 | 2768.7304 | 2752.3014 |
| 3.6444 | 2836.9209 | 2763.7462 | 2746.7397 |
| 3.6554 | 2824.2537 | 2758.7854 | 2741.1779 |
| 3.6664 | 2792.3215 | 2753.8487 | 2735.6161 |
| 3.6774 | 2752.4022 | 2748.9367 | 2730.0543 |
| 3.6884 | 2777.8186 | 2744.0047 | 2724.4925 |
| 3.6994 | 2679.3254 | 2739.0997 | 2718.8412 |
| 3.7104 | 2807.2926 | 2734.1758 | 2713.1899 |
| 3.7214 | 2679.8023 | 2729.2790 | 2707.5386 |
| 3.7324 | 2631.6716 | 2724.4097 | 2701.8873 |
| 3.7434 | 2670.4474 | 2719.5683 | 2696.2360 |
| 3.7544 | 2689.2227 | 2714.7555 | 2690.5847 |
| 3.7654 | 2702.5654 | 2709.9714 | 2684.9334 |
| 3.7764 | 2610.9872 | 2705.2166 | 2679.2821 |
| 3.7874 | 2598.0973 | 2700.4913 | 2673.6308 |
| 3.7984 | 2741.8520 | 2695.7958 | 2667.9795 |
| 3.8094 | 2699.0629 | 2691.1304 | 2662.3282 |
| 3.8204 | 2700.7301 | 2686.4952 | 2656.6769 |
| 3.8314 | 2625.3058 | 2681.8903 | 2651.0256 |
| 3.8424 | 2704.2630 | 2677.3158 | 2645.3743 |
| 3.8534 | 2699.3952 | 2672.7716 | 2639.7230 |
| 3.8644 | 2571.1116 | 2668.2578 | 2634.0717 |
| 3.8754 | 2693.7001 | 2663.7272 | 2628.4204 |
| 3.8864 | 2709.1681 | 2659.2277 | 2622.6767 |
| 3.8974 | 2681.9361 | 2654.7109 | 2616.9329 |
| 3.9084 | 2601.5595 | 2650.2233 | 2611.1892 |
| 3.9194 | 2632.3746 | 2645.7645 | 2605.4454 |
| 3.9304 | 2593.1505 | 2641.3337 | 2599.7017 |
| 3.9414 | 2633.9400 | 2636.9303 | 2593.9579 |
| 3.9524 | 2600.6283 | 2632.5536 | 2588.2142 |
| 3.9634 | 2568.0659 | 2628.2026 | 2582.4705 |
| 3.9744 | 2584.6037 | 2623.8764 | 2576.7267 |
| 3.9854 | 2609.0531 | 2619.5738 | 2570.9830 |
| 3.9964 | 2581.6077 | 2615.2936 | 2565.2392 |
| 4.0074 | 2566.0806 | 2611.0344 | 2559.4955 |
| 4.0184 | 2568.5221 | 2606.7947 | 2553.7517 |
| 4.0294 | 2553.8466 | 2602.5729 | 2548.0080 |
| 4.0404 | 2583.1200 | 2598.3672 | 2542.2642 |
| 4.0514 | 2607.4366 | 2594.1756 | 2536.5205 |
| 4.0624 | 2587.5762 | 2589.9491 | 2530.7767 |
| 4.0734 | 2498.7463 | 2585.7335 | 2524.9403 |
| 4.0844 | 2503.4558 | 2581.4784 | 2519.1039 |
| 4.0954 | 2553.6234 | 2577.2279 | 2513.2675 |
| 4.1064 | 2510.8451 | 2572.9794 | 2507.4310 |
| 4.1174 | 2544.7316 | 2568.7297 | 2501.5946 |
| 4.1284 | 2638.7079 | 2564.4758 | 2495.7582 |
| 4.1394 | 2564.6814 | 2560.2143 | 2489.9218 |
| 4.1504 | 2548.6932 | 2555.9415 | 2484.0854 |
| 4.1614 | 2484.4061 | 2551.6538 | 2478.2490 |
| 4.1724 | 2549.7016 | 2547.3471 | 2472.4125 |
| 4.1834 | 2588.9027 | 2543.0173 | 2466.5761 |
| 4.1944 | 2555.6509 | 2538.6602 | 2460.7397 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 25 400c | 2.0054 | 29.9894 | 0.0110 | 4/25/2024 2:00:45 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 4.4052 | 84.43 | 0.8659 | 20.04268 | 6.08 |
| 7.0743 | 615.70 | 0.1732 | 12.48552 | 44.31 |
| 8.7607 | 1389.47 | 0.1299 | 10.08550 | 100.00 |
| 13.3074 | 19.82 | 0.5196 | 6.64809 | 1.43 |
| 15.8161 | 670.28 | 0.1082 | 5.59877 | 48.24 |
| 17.6854 | 137.57 | 0.2165 | 5.01097 | 9.90 |
| 18.2580 | 95.68 | 0.1299 | 4.85509 | 6.89 |
| 19.6598 | 41.16 | 0.3464 | 4.51196 | 2.96 |
| 20.9120 | 57.81 | 0.1299 | 4.24452 | 4.16 |
| 22.4701 | 142.21 | 0.1299 | 3.95361 | 10.24 |
| 23.4329 | 79.58 | 0.1299 | 3.79329 | 5.73 |
| 24.3114 | 36.77 | 0.2598 | 3.65818 | 2.65 |
| 25.9674 | 458.20 | 0.1515 | 3.42853 | 32.98 |
| 26.7510 | 498.95 | 0.1299 | 3.32985 | 35.91 |
| 27.5558 | 348.25 | 0.1082 | 3.23439 | 25.06 |
| 29.7849 | 79.24 | 0.1515 | 2.99720 | 5.70 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-024-8347 | 64 | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | K0.19 Na7.69 Ca0.06 Al8 Si16 O48 ( H2 O )8 | Analcime | 13 |
| * | 04-017-7286 | 36 | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | K0.8 Mn4 Al1.08 Si4.92 O16 ( O H )2 ( H2 O )3 | Ganophyllite | 3 |
| * | 01-084-1504 | 26 | Potassium Aluminum Silicate | K ( Al Si3 O8 ) | Sanidine | 15 |
| * | 04-024-2707 | 21 | Potassium Sodium Aluminum Silicate | K0.86 Na0.14 Al Si3 O8 | Microcline | 20 |
| * | 04-025-4215 | 8 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 19 |
| * | 04-019-1410 | 22 | Potassium Magnesium Aluminum Iron Silicon Titanium Oxide Chloride Fluoride Hydroxide | K0.95 Mg1.27 Ti0.38 Fe1.2 Al1.3 Si2.85 Cl0.03 O10.76 ( O H )1.1 F0.11 | Phlogopite-2M1 | 25 |
| * | 01-082-8023 | 17 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 3 |

Anchor Scan Parameters

Dataset Name	25 400c

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\REP 25\25 400c.xrdml

Sample Identification	25 400c

Measurement Start Date/Time	4/25/2024 2:00:45 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes