25 Etosha 22 sub 5-15 cm S5 REPLICATE

Graphics

Graphics

Graphics

Quantitative Results

Phase Silicon Oxide

Weight fraction/ %	4.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	14.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	17.0

Phase Cesium Potassium Sodium Aluminum Silicate

Weight fraction/ %	10.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	2.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	19.0

Phase Potassium Magnesium Aluminum Iron Silicon Titanium Oxide Chloride Fluoride Hydroxide

Weight fraction/ %	20.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	15.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Silicon Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Aluminum Silicate | Cesium Potassium Sodium Aluminum Silicate | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Magnesium Aluminum Iron Silicon Titanium Oxide Chloride Fluoride Hydroxide | Sodium Magnesium Silicon Oxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 25 550c | 4.0 | 14.0 | 17.0 | 10.0 | 2.0 | 19.0 | 20.0 | 15.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 4786.0000 | 4770.5865 | 4786.0000 |
| 2.0164 | 4750.4803 | 4747.7287 | 4746.7073 |
| 2.0274 | 4545.8859 | 4708.4450 | 4707.4146 |
| 2.0384 | 4463.7699 | 4669.1614 | 4668.1218 |
| 2.0494 | 4503.6578 | 4629.8780 | 4628.8291 |
| 2.0604 | 4386.3466 | 4590.5947 | 4589.5364 |
| 2.0714 | 4469.9912 | 4551.3115 | 4550.2437 |
| 2.0824 | 4485.4499 | 4512.0284 | 4510.9509 |
| 2.0934 | 4379.7719 | 4472.7455 | 4471.6582 |
| 2.1044 | 4335.8009 | 4433.4627 | 4432.3655 |
| 2.1154 | 4304.6932 | 4394.1800 | 4393.0728 |
| 2.1264 | 4378.1608 | 4354.8975 | 4353.7801 |
| 2.1374 | 4349.3805 | 4315.6151 | 4314.4873 |
| 2.1484 | 4282.0880 | 4276.3328 | 4275.1946 |
| 2.1594 | 4240.8476 | 4237.0507 | 4235.9019 |
| 2.1704 | 4176.3289 | 4197.7688 | 4196.6092 |
| 2.1814 | 4117.8161 | 4158.4870 | 4157.3164 |
| 2.1924 | 4151.7616 | 4129.4754 | 4118.0237 |
| 2.2034 | 4097.7345 | 4104.4909 | 4103.2980 |
| 2.2144 | 4068.0536 | 4089.7766 | 4088.5723 |
| 2.2254 | 4128.3176 | 4075.0624 | 4073.8466 |
| 2.2364 | 4123.1387 | 4060.3485 | 4059.1210 |
| 2.2474 | 4209.7257 | 4045.6347 | 4044.3953 |
| 2.2584 | 4039.8481 | 4030.9210 | 4029.6696 |
| 2.2694 | 4040.5251 | 4016.2076 | 4014.9439 |
| 2.2804 | 3978.0029 | 4001.4943 | 4000.2182 |
| 2.2914 | 3895.1721 | 3986.7812 | 3985.4925 |
| 2.3024 | 3973.4602 | 3972.0683 | 3970.7668 |
| 2.3134 | 3893.9744 | 3957.3556 | 3956.0411 |
| 2.3244 | 3872.6736 | 3942.6431 | 3941.3154 |
| 2.3354 | 3857.2714 | 3927.9307 | 3926.5897 |
| 2.3464 | 3830.2498 | 3913.2186 | 3911.8640 |
| 2.3574 | 3912.1544 | 3898.5067 | 3897.1383 |
| 2.3684 | 3875.5383 | 3883.7950 | 3882.4126 |
| 2.3794 | 3889.0590 | 3869.4553 | 3867.6869 |
| 2.3904 | 3855.9135 | 3855.2616 | 3853.8506 |
| 2.4014 | 3756.4159 | 3841.4399 | 3840.0144 |
| 2.4124 | 3759.3766 | 3827.6185 | 3826.1781 |
| 2.4234 | 3746.6293 | 3813.7973 | 3812.3418 |
| 2.4344 | 3719.4882 | 3799.9763 | 3798.5055 |
| 2.4454 | 3739.1003 | 3786.1556 | 3784.6692 |
| 2.4564 | 3731.4882 | 3772.3351 | 3770.8329 |
| 2.4674 | 3708.8348 | 3758.5149 | 3756.9966 |
| 2.4784 | 3672.6160 | 3744.6949 | 3743.1603 |
| 2.4894 | 3700.7237 | 3730.8752 | 3729.3240 |
| 2.5004 | 3722.0664 | 3717.0557 | 3715.4877 |
| 2.5114 | 3705.4769 | 3703.2366 | 3701.6514 |
| 2.5224 | 3593.9739 | 3689.4177 | 3687.8151 |
| 2.5334 | 3551.5782 | 3675.5991 | 3673.9788 |
| 2.5444 | 3689.0207 | 3661.7807 | 3660.1425 |
| 2.5554 | 3677.5772 | 3647.9627 | 3646.3062 |
| 2.5664 | 3642.8053 | 3634.1450 | 3632.4699 |
| 2.5774 | 3612.4562 | 3620.3276 | 3618.6336 |
| 2.5884 | 3533.6288 | 3606.5105 | 3604.7973 |
| 2.5994 | 3552.4513 | 3592.6938 | 3590.9610 |
| 2.6104 | 3554.0157 | 3578.8773 | 3577.1247 |
| 2.6214 | 3533.3638 | 3565.0612 | 3563.2884 |
| 2.6324 | 3580.8437 | 3551.2455 | 3549.4521 |
| 2.6434 | 3560.9400 | 3537.4301 | 3535.6158 |
| 2.6544 | 3623.7689 | 3523.6151 | 3521.7795 |
| 2.6654 | 3463.7345 | 3509.8004 | 3507.9432 |
| 2.6764 | 3470.2257 | 3495.9862 | 3494.1069 |
| 2.6874 | 3460.7080 | 3482.1723 | 3480.2706 |
| 2.6984 | 3411.2832 | 3468.3588 | 3466.4343 |
| 2.7094 | 3449.5575 | 3454.5457 | 3452.5980 |
| 2.7204 | 3410.2714 | 3440.7331 | 3438.7618 |
| 2.7314 | 3319.1239 | 3426.9208 | 3424.9255 |
| 2.7424 | 3375.9386 | 3413.1090 | 3411.0892 |
| 2.7534 | 3461.3707 | 3401.4007 | 3397.2529 |
| 2.7644 | 3361.3569 | 3390.5174 | 3388.4471 |
| 2.7754 | 3436.5015 | 3381.7375 | 3379.6414 |
| 2.7864 | 3390.0408 | 3372.9581 | 3370.8356 |
| 2.7974 | 3348.2566 | 3364.1792 | 3362.0299 |
| 2.8084 | 3385.2734 | 3355.4008 | 3353.2241 |
| 2.8194 | 3395.4572 | 3346.6229 | 3344.4183 |
| 2.8304 | 3326.8628 | 3337.8456 | 3335.6126 |
| 2.8414 | 3396.6637 | 3329.0688 | 3326.8068 |
| 2.8524 | 3330.0728 | 3320.2925 | 3318.0011 |
| 2.8634 | 3364.3481 | 3311.5169 | 3309.1953 |
| 2.8744 | 3317.4503 | 3302.7418 | 3300.3896 |
| 2.8854 | 3284.5349 | 3293.9673 | 3291.5838 |
| 2.8964 | 3273.0487 | 3285.1935 | 3282.7781 |
| 2.9074 | 3339.7247 | 3276.4202 | 3273.9723 |
| 2.9184 | 3304.6976 | 3267.6477 | 3265.1666 |
| 2.9294 | 3288.8967 | 3258.8758 | 3256.3608 |
| 2.9404 | 3254.0762 | 3250.1046 | 3247.5551 |
| 2.9514 | 3220.2429 | 3241.3340 | 3238.7493 |
| 2.9624 | 3332.5826 | 3232.5643 | 3229.9436 |
| 2.9734 | 3235.6116 | 3223.7952 | 3221.1378 |
| 2.9844 | 3260.6804 | 3215.0270 | 3212.3321 |
| 2.9954 | 3213.5841 | 3206.2595 | 3203.5263 |
| 3.0064 | 3175.2276 | 3197.4928 | 3194.7206 |
| 3.0174 | 3225.9921 | 3188.7270 | 3185.9148 |
| 3.0284 | 3191.4071 | 3179.9620 | 3177.1091 |
| 3.0394 | 3115.6519 | 3171.1979 | 3168.3033 |
| 3.0504 | 3180.0059 | 3162.4347 | 3159.4976 |
| 3.0614 | 3166.2861 | 3153.6724 | 3150.6918 |
| 3.0724 | 3100.0310 | 3144.9112 | 3141.8861 |
| 3.0834 | 3163.4336 | 3136.1509 | 3133.0803 |
| 3.0944 | 3097.2655 | 3127.3916 | 3124.2746 |
| 3.1054 | 3101.9971 | 3118.6334 | 3115.4688 |
| 3.1164 | 3114.1362 | 3109.8763 | 3106.6630 |
| 3.1274 | 3072.0236 | 3101.5827 | 3097.8573 |
| 3.1384 | 3139.6991 | 3093.4715 | 3090.1575 |
| 3.1494 | 3045.4091 | 3085.8238 | 3082.4577 |
| 3.1604 | 3073.2566 | 3078.1775 | 3074.7579 |
| 3.1714 | 3074.1485 | 3070.5324 | 3067.0581 |
| 3.1824 | 3052.9100 | 3062.8886 | 3059.3583 |
| 3.1934 | 3021.2744 | 3055.2463 | 3051.6584 |
| 3.2044 | 3086.3343 | 3047.6054 | 3043.9586 |
| 3.2154 | 3074.1770 | 3039.9661 | 3036.2588 |
| 3.2264 | 3085.1268 | 3032.3283 | 3028.5590 |
| 3.2374 | 3000.2360 | 3024.6921 | 3020.8592 |
| 3.2484 | 2958.0556 | 3017.0577 | 3013.1594 |
| 3.2594 | 3009.4956 | 3009.4250 | 3005.4596 |
| 3.2704 | 3025.3358 | 3001.7943 | 2997.7598 |
| 3.2814 | 3013.9125 | 2994.1654 | 2990.0600 |
| 3.2924 | 3047.4203 | 2986.5387 | 2982.3602 |
| 3.3034 | 2999.8269 | 2978.9140 | 2974.6604 |
| 3.3144 | 2947.2704 | 2971.7342 | 2966.9606 |
| 3.3254 | 2923.7758 | 2964.7302 | 2960.3193 |
| 3.3364 | 2954.5413 | 2958.1713 | 2953.6780 |
| 3.3474 | 2987.0059 | 2951.6150 | 2947.0368 |
| 3.3584 | 2945.1740 | 2945.0615 | 2940.3955 |
| 3.3694 | 2957.1200 | 2938.5109 | 2933.7543 |
| 3.3804 | 2968.4262 | 2931.9634 | 2927.1130 |
| 3.3914 | 2956.8142 | 2925.4192 | 2920.4717 |
| 3.4024 | 2903.3672 | 2918.8786 | 2913.8305 |
| 3.4134 | 2878.3697 | 2912.3416 | 2907.1892 |
| 3.4244 | 2930.7906 | 2905.8086 | 2900.5480 |
| 3.4354 | 2897.2055 | 2899.2797 | 2893.9067 |
| 3.4464 | 2887.0659 | 2892.7554 | 2887.2654 |
| 3.4574 | 2885.0826 | 2886.2358 | 2880.6242 |
| 3.4684 | 2827.9356 | 2879.7212 | 2873.9829 |
| 3.4794 | 2873.8171 | 2873.2121 | 2867.3417 |
| 3.4904 | 2845.0929 | 2866.7088 | 2860.7004 |
| 3.5014 | 2851.6382 | 2860.2116 | 2854.0591 |
| 3.5124 | 2902.0905 | 2853.7209 | 2847.4179 |
| 3.5234 | 2879.1032 | 2847.2373 | 2840.7766 |
| 3.5344 | 2787.9036 | 2840.7613 | 2834.1354 |
| 3.5454 | 2842.0482 | 2834.2932 | 2827.4941 |
| 3.5564 | 2767.9764 | 2827.8337 | 2820.8528 |
| 3.5674 | 2770.7385 | 2821.3834 | 2814.2116 |
| 3.5784 | 2843.3368 | 2814.9428 | 2807.5703 |
| 3.5894 | 2782.6991 | 2808.5127 | 2800.9291 |
| 3.6004 | 2845.8245 | 2802.0937 | 2794.2878 |
| 3.6114 | 2819.1524 | 2795.6866 | 2787.6465 |
| 3.6224 | 2768.0811 | 2789.2921 | 2781.0053 |
| 3.6334 | 2804.8683 | 2782.9112 | 2774.3640 |
| 3.6444 | 2819.1568 | 2776.5447 | 2767.7227 |
| 3.6554 | 2812.4071 | 2770.1934 | 2761.0815 |
| 3.6664 | 2706.5742 | 2763.8584 | 2754.4402 |
| 3.6774 | 2745.4356 | 2757.5406 | 2747.7990 |
| 3.6884 | 2714.3761 | 2751.3662 | 2741.1577 |
| 3.6994 | 2739.3560 | 2745.2602 | 2734.8155 |
| 3.7104 | 2822.6500 | 2739.2998 | 2728.4733 |
| 3.7214 | 2799.8082 | 2733.3611 | 2722.1311 |
| 3.7324 | 2685.4365 | 2727.4454 | 2715.7889 |
| 3.7434 | 2711.8535 | 2721.5538 | 2709.4467 |
| 3.7544 | 2682.5088 | 2715.6878 | 2703.1044 |
| 3.7654 | 2702.2645 | 2709.8486 | 2696.7622 |
| 3.7764 | 2676.5708 | 2704.0376 | 2690.4200 |
| 3.7874 | 2617.5221 | 2698.2562 | 2684.0778 |
| 3.7984 | 2704.7006 | 2692.5057 | 2677.7356 |
| 3.8094 | 2617.7325 | 2686.7876 | 2671.3934 |
| 3.8204 | 2605.2316 | 2681.1033 | 2665.0512 |
| 3.8314 | 2750.8309 | 2675.4542 | 2658.7090 |
| 3.8424 | 2719.7384 | 2669.8418 | 2652.3668 |
| 3.8534 | 2661.0000 | 2664.2674 | 2646.0246 |
| 3.8644 | 2663.5472 | 2658.7325 | 2639.6824 |
| 3.8754 | 2693.6421 | 2653.2013 | 2633.3401 |
| 3.8864 | 2681.3495 | 2647.6977 | 2626.9091 |
| 3.8974 | 2600.7797 | 2642.2004 | 2620.4780 |
| 3.9084 | 2574.3176 | 2636.7478 | 2614.0469 |
| 3.9194 | 2621.7434 | 2631.3411 | 2607.6158 |
| 3.9304 | 2632.3215 | 2625.9814 | 2601.1847 |
| 3.9414 | 2554.6342 | 2620.6697 | 2594.7537 |
| 3.9524 | 2521.1224 | 2615.4070 | 2588.3226 |
| 3.9634 | 2524.7001 | 2610.1940 | 2581.8915 |
| 3.9744 | 2563.4027 | 2605.0316 | 2575.4604 |
| 3.9854 | 2565.0354 | 2599.9203 | 2569.0293 |
| 3.9964 | 2509.4238 | 2594.8605 | 2562.5982 |
| 4.0074 | 2564.7060 | 2589.8526 | 2556.1672 |
| 4.0184 | 2544.4808 | 2584.8966 | 2549.7361 |
| 4.0294 | 2562.1691 | 2579.9926 | 2543.3050 |
| 4.0404 | 2566.0369 | 2575.1403 | 2536.8739 |
| 4.0514 | 2553.3746 | 2570.3394 | 2530.4428 |
| 4.0624 | 2516.9106 | 2565.5495 | 2524.0118 |
| 4.0734 | 2635.7463 | 2560.7939 | 2517.4859 |
| 4.0844 | 2608.4779 | 2556.0475 | 2510.9601 |
| 4.0954 | 2608.0531 | 2551.3484 | 2504.4343 |
| 4.1064 | 2592.9788 | 2546.6951 | 2497.9084 |
| 4.1174 | 2529.2006 | 2542.0856 | 2491.3826 |
| 4.1284 | 2534.9322 | 2537.5178 | 2484.8568 |
| 4.1394 | 2509.2468 | 2532.9891 | 2478.3309 |
| 4.1504 | 2462.2508 | 2528.4966 | 2471.8051 |
| 4.1614 | 2533.3589 | 2524.0372 | 2465.2793 |
| 4.1724 | 2564.8210 | 2519.6071 | 2458.7534 |
| 4.1834 | 2509.8584 | 2515.2026 | 2452.2276 |
| 4.1944 | 2495.3378 | 2510.8190 | 2445.7018 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 25 550c | 2.0054 | 29.9894 | 0.0110 | 4/25/2024 3:50:58 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 4.4667 | 92.52 | 0.6927 | 19.76673 | 5.55 |
| 8.7800 | 1666.65 | 0.1732 | 10.06330 | 100.00 |
| 13.4655 | 15.50 | 0.8659 | 6.57038 | 0.93 |
| 16.0665 | 387.82 | 0.1515 | 5.51206 | 23.27 |
| 17.6658 | 131.24 | 0.3031 | 5.01650 | 7.87 |
| 19.6780 | 35.75 | 0.3464 | 4.50784 | 2.15 |
| 20.9801 | 33.74 | 0.2598 | 4.23090 | 2.02 |
| 22.4798 | 108.41 | 0.1299 | 3.95192 | 6.50 |
| 23.4434 | 40.56 | 0.2598 | 3.79162 | 2.43 |
| 26.3963 | 472.93 | 0.1732 | 3.37377 | 28.38 |
| 26.7609 | 389.97 | 0.1732 | 3.32863 | 23.40 |
| 27.5446 | 395.85 | 0.1515 | 3.23568 | 23.75 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-006-1757 | 48 | Silicon Oxide | Si O2 | Quartz | 4 |
| * | 04-017-4317 | 43 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 14 |
| * | 01-070-6187 | 30 | Potassium Aluminum Silicate | K ( Al Si3 O8 ) | Microcline | 17 |
| * | 04-022-1039 | 22 | Cesium Potassium Sodium Aluminum Silicate | Cs0.02 K0.83 Na0.15 Al Si3 O8 | Sanidine | 10 |
| * | 04-011-6751 | 8 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 2 |
| * | 04-025-4215 | 3 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 19 |
| * | 04-019-1410 | 20 | Potassium Magnesium Aluminum Iron Silicon Titanium Oxide Chloride Fluoride Hydroxide | K0.95 Mg1.27 Ti0.38 Fe1.2 Al1.3 Si2.85 Cl0.03 O10.76 ( O H )1.1 F0.11 | Phlogopite-2M1 | 20 |
| * | 01-082-8023 | 1 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 15 |

Anchor Scan Parameters

Dataset Name	25 550c

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\REP 25\25 550c.xrdml

Sample Identification	25 550c

Measurement Start Date/Time	4/25/2024 3:50:58 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes