25 Etosha 22 sub 5-15 cm S5 REPLICATE

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	4.0

Phase Potassium Magnesium Manganese Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	13.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	5.0

Phase Silicon Oxide

Weight fraction/ %	6.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	25.0

Phase Potassium Iron Aluminum Silicate

Weight fraction/ %	13.0

Phase Potassium Magnesium Aluminum Hydroxide Fluoride Silicate

Weight fraction/ %	11.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	16.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	3.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Potassium Magnesium Manganese Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Sodium Aluminum Silicate Hydrate | Silicon Oxide | Potassium Aluminum Silicate | Potassium Iron Aluminum Silicate | Potassium Magnesium Aluminum Hydroxide Fluoride Silicate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 25 glycol | 4.0 | 13.0 | 5.0 | 6.0 | 25.0 | 13.0 | 11.0 | 16.0 | 3.0 | 4.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7743.0000 | 7727.3947 | 7743.0000 |
| 2.0164 | 7613.7620 | 7702.3447 | 7689.7443 |
| 2.0274 | 7667.1829 | 7649.3935 | 7636.4885 |
| 2.0384 | 7361.0192 | 7596.4560 | 7583.2328 |
| 2.0494 | 7466.7375 | 7543.5331 | 7529.9771 |
| 2.0604 | 7481.4916 | 7490.6257 | 7476.7213 |
| 2.0714 | 7480.8879 | 7437.7349 | 7423.4656 |
| 2.0824 | 7385.6249 | 7384.8618 | 7370.2099 |
| 2.0934 | 7445.1839 | 7332.0075 | 7316.9541 |
| 2.1044 | 7352.1947 | 7279.1736 | 7263.6984 |
| 2.1154 | 7403.4749 | 7226.3613 | 7210.4427 |
| 2.1264 | 7397.5054 | 7173.5723 | 7157.1869 |
| 2.1374 | 7306.3068 | 7120.8083 | 7103.9312 |
| 2.1484 | 7354.9661 | 7068.0713 | 7050.6755 |
| 2.1594 | 7182.0226 | 7015.3632 | 6997.4197 |
| 2.1704 | 7222.6150 | 6962.6863 | 6944.1640 |
| 2.1814 | 7228.1790 | 6910.0433 | 6890.9083 |
| 2.1924 | 7074.4317 | 6857.3521 | 6837.6526 |
| 2.2034 | 7170.6903 | 6804.7084 | 6784.2354 |
| 2.2144 | 7014.7252 | 6752.0230 | 6730.8182 |
| 2.2254 | 6916.6677 | 6699.3844 | 6677.4011 |
| 2.2364 | 7038.6962 | 6646.7968 | 6623.9839 |
| 2.2474 | 6883.1623 | 6594.2646 | 6570.5667 |
| 2.2584 | 7005.9921 | 6541.7933 | 6517.1496 |
| 2.2694 | 6938.8201 | 6489.3885 | 6463.7324 |
| 2.2804 | 6916.9489 | 6437.0569 | 6410.3152 |
| 2.2914 | 6835.6519 | 6384.8056 | 6356.8981 |
| 2.3024 | 6754.6637 | 6332.6430 | 6303.4809 |
| 2.3134 | 6753.9351 | 6280.5784 | 6250.0637 |
| 2.3244 | 6765.3269 | 6228.6225 | 6196.6466 |
| 2.3354 | 6778.6195 | 6176.7872 | 6143.2294 |
| 2.3464 | 6731.1386 | 6125.0863 | 6089.8122 |
| 2.3574 | 6617.6971 | 6073.5357 | 6036.3951 |
| 2.3684 | 6581.9322 | 6022.1534 | 5982.9779 |
| 2.3794 | 6640.5693 | 5970.8921 | 5929.5607 |
| 2.3904 | 6512.8417 | 5919.8511 | 5876.0130 |
| 2.4014 | 6556.1151 | 5868.9849 | 5822.4652 |
| 2.4124 | 6633.2493 | 5818.3971 | 5768.9174 |
| 2.4234 | 6519.9528 | 5768.1309 | 5715.3697 |
| 2.4344 | 6472.2979 | 5718.2408 | 5661.8219 |
| 2.4454 | 6560.3048 | 5668.7983 | 5608.2741 |
| 2.4564 | 6508.0246 | 5619.8993 | 5554.7264 |
| 2.4674 | 6297.2419 | 5571.6764 | 5501.1786 |
| 2.4784 | 6285.2925 | 5524.3161 | 5447.6308 |
| 2.4894 | 6376.1219 | 5478.0824 | 5394.0830 |
| 2.5004 | 6395.5752 | 5433.3482 | 5340.5353 |
| 2.5114 | 6304.3648 | 5390.6325 | 5286.9875 |
| 2.5224 | 6161.3240 | 5350.6426 | 5233.4397 |
| 2.5334 | 6228.7139 | 5314.3131 | 5179.8920 |
| 2.5444 | 6177.2866 | 5282.8355 | 5126.3442 |
| 2.5554 | 6131.2478 | 5257.6638 | 5072.7964 |
| 2.5664 | 6110.1062 | 5240.4830 | 5019.2487 |
| 2.5774 | 6104.0089 | 5233.1272 | 4965.7009 |
| 2.5884 | 6038.1775 | 5237.4375 | 4912.1531 |
| 2.5994 | 6142.6814 | 5255.0598 | 4858.6054 |
| 2.6104 | 6063.5462 | 5287.1873 | 4805.0576 |
| 2.6214 | 6177.9056 | 5334.2621 | 4751.5098 |
| 2.6324 | 6043.0147 | 5395.6425 | 4697.9621 |
| 2.6434 | 5891.9695 | 5469.2266 | 4644.4143 |
| 2.6544 | 5957.4710 | 5551.0076 | 4590.8665 |
| 2.6654 | 5811.7964 | 5634.5564 | 4537.3187 |
| 2.6764 | 5738.2532 | 5710.5778 | 4483.7710 |
| 2.6874 | 5731.9518 | 5767.0244 | 4430.2232 |
| 2.6984 | 5638.8540 | 5790.5674 | 4376.6754 |
| 2.7094 | 5569.5221 | 5769.8657 | 4323.1277 |
| 2.7204 | 5408.6022 | 5699.5651 | 4269.5799 |
| 2.7314 | 5237.9616 | 5582.5206 | 4216.0321 |
| 2.7424 | 5083.4749 | 5428.5427 | 4162.4844 |
| 2.7534 | 4996.8230 | 5250.6181 | 4108.9366 |
| 2.7644 | 4795.8776 | 5061.4742 | 4055.2582 |
| 2.7754 | 4595.0875 | 4871.2645 | 4001.5799 |
| 2.7864 | 4462.4076 | 4687.3908 | 3947.9015 |
| 2.7974 | 4403.6372 | 4514.6064 | 3894.2231 |
| 2.8084 | 4286.7414 | 4355.5962 | 3840.5447 |
| 2.8194 | 4138.4788 | 4211.4449 | 3786.8664 |
| 2.8304 | 3989.4911 | 4082.0335 | 3733.1880 |
| 2.8414 | 3832.2773 | 3966.3845 | 3679.5096 |
| 2.8524 | 3762.3761 | 3862.9734 | 3625.8313 |
| 2.8634 | 3608.4838 | 3770.0005 | 3572.1529 |
| 2.8744 | 3509.7556 | 3685.6131 | 3518.4745 |
| 2.8854 | 3334.9252 | 3608.0669 | 3464.7961 |
| 2.8964 | 3342.9513 | 3535.8271 | 3411.1178 |
| 2.9074 | 3284.0157 | 3467.6155 | 3357.4394 |
| 2.9184 | 3285.4557 | 3402.4150 | 3303.7610 |
| 2.9294 | 3256.7286 | 3339.4474 | 3250.0827 |
| 2.9404 | 3187.9262 | 3290.8593 | 3196.4043 |
| 2.9514 | 3161.2930 | 3242.3374 | 3167.0004 |
| 2.9624 | 3099.2375 | 3207.4813 | 3137.5965 |
| 2.9734 | 3094.5497 | 3173.3578 | 3108.1926 |
| 2.9844 | 3146.8584 | 3139.8186 | 3078.7887 |
| 2.9954 | 3046.5575 | 3106.7569 | 3049.3848 |
| 3.0064 | 3017.8245 | 3074.0941 | 3019.9809 |
| 3.0174 | 2947.5841 | 3041.7708 | 2990.5770 |
| 3.0284 | 2889.8643 | 3009.7402 | 2961.1731 |
| 3.0394 | 2925.6804 | 2977.9650 | 2931.7692 |
| 3.0504 | 2955.4616 | 2946.9488 | 2902.3653 |
| 3.0614 | 2909.5044 | 2915.7218 | 2872.9614 |
| 3.0724 | 2852.2291 | 2884.8173 | 2843.5575 |
| 3.0834 | 2852.4110 | 2853.8650 | 2814.1536 |
| 3.0944 | 2764.9203 | 2822.9924 | 2784.7497 |
| 3.1054 | 2716.6195 | 2792.2462 | 2755.3458 |
| 3.1164 | 2767.6539 | 2761.6140 | 2725.9420 |
| 3.1274 | 2693.7640 | 2739.2189 | 2696.5381 |
| 3.1384 | 2650.5216 | 2716.1674 | 2682.6531 |
| 3.1494 | 2663.8348 | 2701.3348 | 2668.7680 |
| 3.1604 | 2664.5472 | 2686.5794 | 2654.8830 |
| 3.1714 | 2655.8515 | 2671.8943 | 2640.9980 |
| 3.1824 | 2631.7094 | 2657.2736 | 2627.1130 |
| 3.1934 | 2599.4336 | 2642.7119 | 2613.2280 |
| 3.2044 | 2604.3068 | 2628.2046 | 2599.3430 |
| 3.2154 | 2615.5831 | 2613.7474 | 2585.4580 |
| 3.2264 | 2549.2197 | 2599.3363 | 2571.5730 |
| 3.2374 | 2498.2468 | 2584.9680 | 2557.6880 |
| 3.2484 | 2496.2222 | 2570.6394 | 2543.8030 |
| 3.2594 | 2535.9204 | 2556.3476 | 2529.9180 |
| 3.2704 | 2594.1057 | 2542.0903 | 2516.0330 |
| 3.2814 | 2549.9783 | 2527.8649 | 2502.1480 |
| 3.2924 | 2502.5708 | 2513.6696 | 2488.2630 |
| 3.3034 | 2513.2517 | 2499.5024 | 2474.3780 |
| 3.3144 | 2522.9395 | 2485.3616 | 2460.4930 |
| 3.3254 | 2485.4071 | 2471.2456 | 2446.6080 |
| 3.3364 | 2454.4887 | 2457.1531 | 2432.7230 |
| 3.3474 | 2437.0373 | 2443.0828 | 2418.8380 |
| 3.3584 | 2355.4970 | 2429.0334 | 2404.9530 |
| 3.3694 | 2356.4513 | 2415.0040 | 2391.0679 |
| 3.3804 | 2415.3825 | 2400.9935 | 2377.1829 |
| 3.3914 | 2402.2743 | 2387.0010 | 2363.2979 |
| 3.4024 | 2342.2202 | 2373.0258 | 2349.4129 |
| 3.4134 | 2338.5035 | 2359.0671 | 2335.5279 |
| 3.4244 | 2351.3156 | 2345.1243 | 2321.6429 |
| 3.4354 | 2282.2379 | 2331.1967 | 2307.7579 |
| 3.4464 | 2279.4887 | 2317.2837 | 2293.8729 |
| 3.4574 | 2276.1239 | 2303.3849 | 2279.9879 |
| 3.4684 | 2277.6760 | 2289.4998 | 2266.1029 |
| 3.4794 | 2256.6499 | 2275.6279 | 2252.2179 |
| 3.4904 | 2206.6947 | 2261.7690 | 2238.3329 |
| 3.5014 | 2242.3835 | 2251.2828 | 2224.4479 |
| 3.5124 | 2211.2384 | 2240.4992 | 2216.9735 |
| 3.5234 | 2228.1623 | 2233.0877 | 2209.4990 |
| 3.5344 | 2175.4459 | 2225.6879 | 2202.0246 |
| 3.5454 | 2235.3727 | 2218.2997 | 2194.5502 |
| 3.5564 | 2215.0221 | 2210.9229 | 2187.0757 |
| 3.5674 | 2202.4533 | 2203.5574 | 2179.6013 |
| 3.5784 | 2182.2714 | 2196.2029 | 2172.1269 |
| 3.5894 | 2073.3716 | 2188.8595 | 2164.6524 |
| 3.6004 | 2094.6254 | 2181.5270 | 2157.1780 |
| 3.6114 | 2235.3245 | 2174.2054 | 2149.7036 |
| 3.6224 | 2168.7655 | 2166.8947 | 2142.2291 |
| 3.6334 | 2199.8781 | 2159.5948 | 2134.7547 |
| 3.6444 | 2128.0319 | 2152.3058 | 2127.2803 |
| 3.6554 | 2119.4366 | 2145.0277 | 2119.8058 |
| 3.6664 | 2080.7704 | 2137.7607 | 2112.3314 |
| 3.6774 | 2098.3107 | 2130.5047 | 2104.8570 |
| 3.6884 | 2094.0752 | 2124.2679 | 2097.3825 |
| 3.6994 | 2122.4631 | 2117.9495 | 2091.8311 |
| 3.7104 | 2070.7881 | 2112.6506 | 2086.2796 |
| 3.7214 | 2098.0266 | 2107.3635 | 2080.7282 |
| 3.7324 | 2030.3431 | 2102.0882 | 2075.1767 |
| 3.7434 | 2055.1436 | 2096.8252 | 2069.6253 |
| 3.7544 | 2082.7655 | 2091.5747 | 2064.0738 |
| 3.7654 | 1952.5467 | 2086.3370 | 2058.5224 |
| 3.7764 | 2021.4145 | 2081.1126 | 2052.9709 |
| 3.7874 | 2047.7788 | 2075.9017 | 2047.4195 |
| 3.7984 | 2061.8038 | 2070.7048 | 2041.8680 |
| 3.8094 | 2005.1573 | 2065.5224 | 2036.3166 |
| 3.8204 | 2014.4395 | 2060.3551 | 2030.7651 |
| 3.8314 | 1994.7984 | 2055.2035 | 2025.2137 |
| 3.8424 | 1988.9479 | 2050.0681 | 2019.6622 |
| 3.8534 | 1976.5546 | 2044.9498 | 2014.1108 |
| 3.8644 | 2061.7374 | 2039.8492 | 2008.5593 |
| 3.8754 | 1955.8319 | 2036.3013 | 2003.0078 |
| 3.8864 | 2005.2035 | 2032.6316 | 2000.3833 |
| 3.8974 | 2011.7906 | 2030.5165 | 1997.7587 |
| 3.9084 | 2044.1986 | 2028.4231 | 1995.1341 |
| 3.9194 | 2005.8702 | 2026.3524 | 1992.5095 |
| 3.9304 | 1967.8117 | 2024.3058 | 1989.8850 |
| 3.9414 | 1943.6097 | 2022.2846 | 1987.2604 |
| 3.9524 | 1988.3466 | 2020.2903 | 1984.6358 |
| 3.9634 | 1948.6342 | 2018.3246 | 1982.0112 |
| 3.9744 | 1981.0039 | 2016.3892 | 1979.3867 |
| 3.9854 | 2011.3009 | 2014.4860 | 1976.7621 |
| 3.9964 | 1989.7217 | 2012.6170 | 1974.1375 |
| 4.0074 | 1932.0236 | 2010.7845 | 1971.5129 |
| 4.0184 | 1943.4189 | 2008.9907 | 1968.8883 |
| 4.0294 | 2028.0924 | 2007.2383 | 1966.2638 |
| 4.0404 | 2029.0708 | 2005.5298 | 1963.6392 |
| 4.0514 | 1986.8141 | 2003.8683 | 1961.0146 |
| 4.0624 | 1932.8009 | 2002.2470 | 1958.3900 |
| 4.0734 | 1944.3746 | 2000.6799 | 1955.7466 |
| 4.0844 | 1895.2567 | 1999.1598 | 1953.1032 |
| 4.0954 | 1917.1760 | 1997.7003 | 1950.4598 |
| 4.1064 | 1882.4223 | 1996.3055 | 1947.8164 |
| 4.1174 | 1936.0738 | 1994.9794 | 1945.1731 |
| 4.1284 | 1974.8383 | 1993.7267 | 1942.5297 |
| 4.1394 | 1976.8486 | 1992.5519 | 1939.8863 |
| 4.1504 | 1949.9395 | 1991.4601 | 1937.2429 |
| 4.1614 | 1948.5428 | 1990.4565 | 1934.5995 |
| 4.1724 | 1980.2080 | 1989.5466 | 1931.9561 |
| 4.1834 | 1932.0708 | 1988.7361 | 1929.3127 |
| 4.1944 | 1894.7286 | 1988.0309 | 1926.6693 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 25 glycol | 2.0054 | 29.9894 | 0.0110 | 4/24/2024 1:28:45 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7090 | 1291.25 | 0.1515 | 32.58672 | 100.00 |
| 4.9718 | 526.69 | 0.6927 | 17.75978 | 40.79 |
| 6.9488 | 699.31 | 0.3897 | 12.71059 | 54.16 |
| 8.7196 | 741.81 | 0.1299 | 10.13294 | 57.45 |
| 15.7213 | 703.50 | 0.0758 | 5.63233 | 54.48 |
| 17.5845 | 119.59 | 0.2165 | 5.03951 | 9.26 |
| 18.1942 | 127.57 | 0.1082 | 4.87197 | 9.88 |
| 19.5651 | 32.76 | 0.5196 | 4.53359 | 2.54 |
| 20.8119 | 61.74 | 0.1299 | 4.26473 | 4.78 |
| 22.3663 | 247.44 | 0.0866 | 3.97173 | 19.16 |
| 23.3412 | 69.69 | 0.1732 | 3.80799 | 5.40 |
| 25.8874 | 994.48 | 0.0758 | 3.43894 | 77.02 |
| 26.6524 | 762.18 | 0.1732 | 3.34194 | 59.03 |
| 27.4610 | 386.64 | 0.1299 | 3.24534 | 29.94 |
| 29.6781 | 134.91 | 0.0866 | 3.00775 | 10.45 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-003-0648 | 54 | Titanium Oxide | Ti O2 | Rutile | 4 |
| * | 04-015-8238 | 32 | Potassium Magnesium Manganese Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.99 Mg0.58 Ti0.15 Mn0.05 Fe1.5 Al1.82 Si2.72 O10.32 ( O H )1.57 F0.11 | Biotite-1M | 13 |
| * | 04-011-6751 | 18 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 5 |
| * | 04-006-1757 | 33 | Silicon Oxide | Si O2 | Quartz | 6 |
| * | 01-076-1238 | 23 | Potassium Aluminum Silicate | K ( Al Si3 O8 ) | Microcline | 25 |
| * | 01-077-0992 | 34 | Potassium Iron Aluminum Silicate | K Fe0.28 Al0.72 Si3 O8 | Sanidine, Fe+3-bearing | 13 |
| * | 01-073-1661 | 16 | Potassium Magnesium Aluminum Hydroxide Fluoride Silicate | K Mg3 ( Al Si3 O10 ) ( O H ) F | Phlogopite | 11 |
| * | 04-025-4215 | 21 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 16 |
| * | 01-082-8023 | 23 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 3 |
| * | 04-013-5979 | 13 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 4 |

Anchor Scan Parameters

Dataset Name	25 glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\REP 25\25 glycol.xrdml

Sample Identification	25 glycol

Measurement Start Date/Time	4/24/2024 1:28:45 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes