26 CS2 ground 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Silicon Oxide

Weight fraction/ %	6.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	7.0

Phase Magnesium Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	10.0

Phase Potassium Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	5.0

Phase Potassium Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	25.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	19.0

Phase Titanium Oxide

Weight fraction/ %	13.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	11.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	4.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Silicon Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Aluminum Silicate Hydroxide Hydrate | Potassium Magnesium Aluminum Silicate Hydroxide | Potassium Aluminum Silicate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Titanium Oxide | Magnesium Silicon Oxide Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 26 CS2 ground 400C | 6.0 | 7.0 | 10.0 | 5.0 | 25.0 | 19.0 | 13.0 | 11.0 | 4.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6441.0000 | 6430.6281 | 6441.0000 |
| 2.0164 | 6295.7006 | 6414.1423 | 6400.9729 |
| 2.0274 | 6349.1976 | 6374.5627 | 6360.9459 |
| 2.0384 | 6233.6490 | 6335.0062 | 6320.9188 |
| 2.0494 | 6122.3107 | 6295.4743 | 6280.8917 |
| 2.0604 | 6167.1844 | 6255.9691 | 6240.8647 |
| 2.0714 | 6161.4454 | 6216.4926 | 6200.8376 |
| 2.0824 | 6054.0860 | 6177.0472 | 6160.8105 |
| 2.0934 | 6046.6421 | 6137.6358 | 6120.7835 |
| 2.1044 | 5974.7566 | 6098.2614 | 6080.7564 |
| 2.1154 | 6007.8378 | 6058.9277 | 6040.7293 |
| 2.1264 | 5959.7783 | 6019.6391 | 6000.7023 |
| 2.1374 | 5877.8230 | 5980.4006 | 5960.6752 |
| 2.1484 | 5834.6588 | 5941.2182 | 5920.6481 |
| 2.1594 | 5883.2733 | 5902.0990 | 5880.6210 |
| 2.1704 | 5741.4646 | 5863.0513 | 5840.5940 |
| 2.1814 | 5827.2802 | 5824.0854 | 5800.5669 |
| 2.1924 | 5798.3884 | 5786.3369 | 5760.5398 |
| 2.2034 | 5722.8407 | 5748.3947 | 5722.4586 |
| 2.2144 | 5591.3053 | 5711.7012 | 5684.3775 |
| 2.2254 | 5610.2793 | 5675.1525 | 5646.2963 |
| 2.2364 | 5584.6091 | 5638.7722 | 5608.2151 |
| 2.2474 | 5537.3569 | 5602.5876 | 5570.1339 |
| 2.2584 | 5585.8097 | 5566.6308 | 5532.0527 |
| 2.2694 | 5566.6932 | 5530.9382 | 5493.9715 |
| 2.2804 | 5388.1106 | 5495.5517 | 5455.8903 |
| 2.2914 | 5389.8417 | 5460.5185 | 5417.8091 |
| 2.3024 | 5475.8319 | 5425.8914 | 5379.7279 |
| 2.3134 | 5398.9351 | 5391.7286 | 5341.6467 |
| 2.3244 | 5392.1485 | 5358.0939 | 5303.5655 |
| 2.3354 | 5384.4189 | 5325.0556 | 5265.4843 |
| 2.3464 | 5339.2306 | 5292.6864 | 5227.4031 |
| 2.3574 | 5262.7738 | 5261.0620 | 5189.3219 |
| 2.3684 | 5222.6637 | 5230.2599 | 5151.2407 |
| 2.3794 | 5177.3884 | 5200.2749 | 5113.1595 |
| 2.3904 | 5178.6264 | 5171.2873 | 5074.9352 |
| 2.4014 | 5127.2035 | 5143.2638 | 5036.7109 |
| 2.4124 | 5096.2104 | 5116.3513 | 4998.4866 |
| 2.4234 | 5144.9823 | 5090.6046 | 4960.2623 |
| 2.4344 | 5113.3304 | 5066.0657 | 4922.0380 |
| 2.4454 | 5076.4848 | 5042.7604 | 4883.8137 |
| 2.4564 | 4997.6145 | 5020.6956 | 4845.5894 |
| 2.4674 | 4991.3304 | 4999.8551 | 4807.3651 |
| 2.4784 | 4987.1332 | 4980.1962 | 4769.1408 |
| 2.4894 | 4820.9105 | 4961.6456 | 4730.9165 |
| 2.5004 | 4823.0664 | 4944.0954 | 4692.6922 |
| 2.5114 | 4875.8151 | 4927.3977 | 4654.4679 |
| 2.5224 | 4787.3436 | 4911.3598 | 4616.2436 |
| 2.5334 | 4773.6785 | 4895.7380 | 4578.0193 |
| 2.5444 | 4793.7955 | 4880.2318 | 4539.7950 |
| 2.5554 | 4812.0511 | 4864.4792 | 4501.5707 |
| 2.5664 | 4759.4351 | 4848.0539 | 4463.3464 |
| 2.5774 | 4704.3825 | 4830.4683 | 4425.1221 |
| 2.5884 | 4648.7488 | 4811.1829 | 4386.8978 |
| 2.5994 | 4562.2743 | 4789.6275 | 4348.6735 |
| 2.6104 | 4553.3083 | 4765.2327 | 4310.4492 |
| 2.6214 | 4625.9469 | 4737.4739 | 4272.2249 |
| 2.6324 | 4601.4557 | 4705.9194 | 4234.0006 |
| 2.6434 | 4484.8997 | 4670.2782 | 4195.7763 |
| 2.6544 | 4536.1962 | 4630.4340 | 4157.5519 |
| 2.6654 | 4474.1298 | 4586.4604 | 4119.3276 |
| 2.6764 | 4414.5084 | 4538.6382 | 4081.1033 |
| 2.6874 | 4361.0393 | 4487.3376 | 4042.8790 |
| 2.6984 | 4230.8495 | 4433.0652 | 4004.6547 |
| 2.7094 | 4152.9489 | 4376.3876 | 3966.4304 |
| 2.7204 | 4164.1686 | 4317.8708 | 3928.2061 |
| 2.7314 | 4208.9381 | 4258.0732 | 3889.9818 |
| 2.7424 | 4086.2399 | 4197.4956 | 3851.7575 |
| 2.7534 | 4021.2252 | 4136.4959 | 3813.5332 |
| 2.7644 | 3999.5826 | 4075.5556 | 3775.1658 |
| 2.7754 | 3935.0531 | 4014.8841 | 3736.7984 |
| 2.7864 | 3881.3668 | 3954.8205 | 3698.4310 |
| 2.7974 | 3825.4425 | 3895.5688 | 3660.0636 |
| 2.8084 | 3737.3505 | 3837.2867 | 3621.6962 |
| 2.8194 | 3687.0708 | 3780.0910 | 3583.3287 |
| 2.8304 | 3720.7950 | 3724.0627 | 3544.9613 |
| 2.8414 | 3709.0541 | 3669.2512 | 3506.5939 |
| 2.8524 | 3527.2355 | 3615.6783 | 3468.2265 |
| 2.8634 | 3527.5457 | 3563.3425 | 3429.8591 |
| 2.8744 | 3431.8717 | 3512.2218 | 3391.4917 |
| 2.8854 | 3464.3982 | 3462.2778 | 3353.1243 |
| 2.8964 | 3425.1770 | 3413.4584 | 3314.7569 |
| 2.9074 | 3101.1721 | 3365.7011 | 3276.3894 |
| 2.9184 | 3248.0123 | 3318.9361 | 3238.0220 |
| 2.9294 | 3199.0590 | 3273.0885 | 3199.6546 |
| 2.9404 | 3168.4498 | 3232.4773 | 3161.2872 |
| 2.9514 | 3114.9695 | 3191.4489 | 3130.5324 |
| 2.9624 | 3125.2463 | 3155.5031 | 3099.7776 |
| 2.9734 | 3047.1839 | 3120.1702 | 3069.0229 |
| 2.9844 | 3022.2242 | 3085.3808 | 3038.2681 |
| 2.9954 | 2873.0797 | 3051.0700 | 3007.5133 |
| 3.0064 | 2896.7488 | 3017.1783 | 2976.7585 |
| 3.0174 | 2882.4848 | 2983.6516 | 2946.0037 |
| 3.0284 | 2905.5811 | 2950.4414 | 2915.2490 |
| 3.0394 | 2908.1799 | 2917.5048 | 2884.4942 |
| 3.0504 | 2717.8914 | 2884.8039 | 2853.7394 |
| 3.0614 | 2768.4395 | 2852.3058 | 2822.9846 |
| 3.0724 | 2765.9651 | 2819.9821 | 2792.2298 |
| 3.0834 | 2719.6145 | 2787.8083 | 2761.4751 |
| 3.0944 | 2669.6549 | 2755.7638 | 2730.7203 |
| 3.1054 | 2612.7276 | 2723.8310 | 2699.9655 |
| 3.1164 | 2638.7591 | 2691.9949 | 2669.2107 |
| 3.1274 | 2657.2094 | 2663.5426 | 2638.4559 |
| 3.1384 | 2636.2330 | 2634.2786 | 2613.4145 |
| 3.1494 | 2604.8958 | 2608.3790 | 2588.3731 |
| 3.1604 | 2601.0531 | 2582.5370 | 2563.3316 |
| 3.1714 | 2527.3264 | 2556.7465 | 2538.2902 |
| 3.1824 | 2431.5880 | 2531.0021 | 2513.2487 |
| 3.1934 | 2424.2920 | 2505.2994 | 2488.2073 |
| 3.2044 | 2433.0767 | 2479.6346 | 2463.1659 |
| 3.2154 | 2448.0403 | 2454.0043 | 2438.1244 |
| 3.2264 | 2446.0634 | 2428.4059 | 2413.0830 |
| 3.2374 | 2398.5339 | 2402.8367 | 2388.0415 |
| 3.2484 | 2373.8889 | 2377.2945 | 2363.0001 |
| 3.2594 | 2355.2950 | 2351.7776 | 2337.9587 |
| 3.2704 | 2352.8570 | 2326.2840 | 2312.9172 |
| 3.2814 | 2330.9065 | 2300.8123 | 2287.8758 |
| 3.2924 | 2260.5089 | 2275.3610 | 2262.8343 |
| 3.3034 | 2268.6008 | 2249.9289 | 2237.7929 |
| 3.3144 | 2181.6726 | 2227.4566 | 2212.7514 |
| 3.3254 | 2177.2242 | 2204.2118 | 2192.8044 |
| 3.3364 | 2198.1037 | 2183.9247 | 2172.8574 |
| 3.3474 | 2222.9912 | 2163.6527 | 2152.9104 |
| 3.3584 | 2164.9542 | 2143.3947 | 2132.9634 |
| 3.3694 | 2092.0905 | 2123.1500 | 2113.0163 |
| 3.3804 | 2044.3078 | 2102.9179 | 2093.0693 |
| 3.3914 | 2064.8673 | 2082.6977 | 2073.1223 |
| 3.4024 | 2071.2935 | 2062.4887 | 2053.1753 |
| 3.4134 | 2046.7325 | 2042.2903 | 2033.2283 |
| 3.4244 | 2034.0192 | 2022.1021 | 2013.2812 |
| 3.4354 | 2065.0443 | 2001.9233 | 1993.3342 |
| 3.4464 | 2011.0226 | 1981.7537 | 1973.3872 |
| 3.4574 | 1975.4277 | 1961.5926 | 1953.4402 |
| 3.4684 | 1949.8215 | 1941.4398 | 1933.4932 |
| 3.4794 | 1907.6490 | 1921.2947 | 1913.5461 |
| 3.4904 | 1878.8584 | 1901.1569 | 1893.5991 |
| 3.5014 | 1882.0885 | 1884.5767 | 1873.6521 |
| 3.5124 | 1866.7999 | 1867.0503 | 1859.8531 |
| 3.5234 | 1852.8230 | 1853.0806 | 1846.0540 |
| 3.5344 | 1863.7522 | 1839.1171 | 1832.2550 |
| 3.5454 | 1875.4867 | 1825.1593 | 1818.4559 |
| 3.5564 | 1864.0723 | 1811.2071 | 1804.6569 |
| 3.5674 | 1835.1495 | 1797.2602 | 1790.8578 |
| 3.5784 | 1770.1784 | 1783.4008 | 1777.0588 |
| 3.5894 | 1813.5929 | 1769.4860 | 1763.2597 |
| 3.6004 | 1745.1755 | 1755.5966 | 1749.4607 |
| 3.6114 | 1778.9981 | 1741.6812 | 1735.6616 |
| 3.6224 | 1725.4233 | 1727.7595 | 1721.8626 |
| 3.6334 | 1687.7040 | 1713.8419 | 1708.0635 |
| 3.6444 | 1668.0354 | 1699.9282 | 1694.2645 |
| 3.6554 | 1721.5251 | 1686.0182 | 1680.4655 |
| 3.6664 | 1676.3633 | 1672.1118 | 1666.6664 |
| 3.6774 | 1660.9223 | 1658.2090 | 1652.8674 |
| 3.6884 | 1601.8849 | 1644.3094 | 1639.0683 |
| 3.6994 | 1658.2832 | 1630.4130 | 1625.2693 |
| 3.7104 | 1610.7881 | 1616.5197 | 1611.4702 |
| 3.7214 | 1610.5044 | 1602.6294 | 1597.6712 |
| 3.7324 | 1592.4061 | 1588.7419 | 1583.8721 |
| 3.7434 | 1551.4366 | 1574.8571 | 1570.0731 |
| 3.7544 | 1540.4115 | 1560.9750 | 1556.2740 |
| 3.7654 | 1570.9302 | 1547.0954 | 1542.4750 |
| 3.7764 | 1575.9154 | 1533.2183 | 1528.6759 |
| 3.7874 | 1517.5221 | 1519.3435 | 1514.8769 |
| 3.7984 | 1523.0138 | 1505.4710 | 1501.0779 |
| 3.8094 | 1525.9459 | 1491.6007 | 1487.2788 |
| 3.8204 | 1461.8216 | 1477.7325 | 1473.4798 |
| 3.8314 | 1522.2586 | 1463.8664 | 1459.6807 |
| 3.8424 | 1456.1583 | 1450.0023 | 1445.8817 |
| 3.8534 | 1438.2743 | 1436.1401 | 1432.0826 |
| 3.8644 | 1396.5300 | 1422.2797 | 1418.2836 |
| 3.8754 | 1373.1741 | 1410.6020 | 1404.4845 |
| 3.8864 | 1433.7611 | 1398.3407 | 1394.4618 |
| 3.8974 | 1410.3500 | 1388.2619 | 1384.4391 |
| 3.9084 | 1378.9675 | 1378.1848 | 1374.4164 |
| 3.9194 | 1353.8407 | 1368.1092 | 1364.3937 |
| 3.9304 | 1329.8112 | 1358.0352 | 1354.3709 |
| 3.9414 | 1334.6136 | 1347.9627 | 1344.3482 |
| 3.9524 | 1309.6327 | 1337.8916 | 1334.3255 |
| 3.9634 | 1335.8978 | 1327.8220 | 1324.3028 |
| 3.9744 | 1371.5880 | 1317.7537 | 1314.2801 |
| 3.9854 | 1284.6195 | 1307.6868 | 1304.2573 |
| 3.9964 | 1306.6996 | 1297.6211 | 1294.2346 |
| 4.0074 | 1256.4789 | 1287.5568 | 1284.2119 |
| 4.0184 | 1286.2522 | 1277.4936 | 1274.1892 |
| 4.0294 | 1274.8456 | 1267.4317 | 1264.1665 |
| 4.0404 | 1238.5939 | 1257.3710 | 1254.1438 |
| 4.0514 | 1228.7404 | 1247.3114 | 1244.1210 |
| 4.0624 | 1259.2724 | 1237.5946 | 1234.0983 |
| 4.0734 | 1223.5821 | 1227.7872 | 1224.6673 |
| 4.0844 | 1199.2035 | 1218.3227 | 1215.2363 |
| 4.0954 | 1168.3589 | 1208.8591 | 1205.8053 |
| 4.1064 | 1189.8609 | 1199.3966 | 1196.3743 |
| 4.1174 | 1173.6932 | 1189.9352 | 1186.9433 |
| 4.1284 | 1121.7252 | 1180.4747 | 1177.5123 |
| 4.1394 | 1165.7650 | 1171.0152 | 1168.0813 |
| 4.1504 | 1155.6239 | 1161.5566 | 1158.6503 |
| 4.1614 | 1117.6814 | 1152.0990 | 1149.2193 |
| 4.1724 | 1132.6908 | 1142.6423 | 1139.7883 |
| 4.1834 | 1106.1062 | 1133.1866 | 1130.3573 |
| 4.1944 | 1056.2296 | 1123.7317 | 1120.9263 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 26 CS2 ground 400C | 2.0054 | 29.9894 | 0.0110 | 12/19/2023 7:47:54 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6425 | 423.70 | 0.3031 | 33.40661 | 100.00 |
| 5.3121 | 110.32 | 0.1732 | 16.62274 | 26.04 |
| 7.0065 | 50.72 | 0.4330 | 12.60614 | 11.97 |
| 8.7394 | 181.22 | 0.1082 | 10.11001 | 42.77 |
| 15.7737 | 230.50 | 0.1082 | 5.61370 | 54.40 |
| 17.6266 | 16.33 | 0.2598 | 5.02757 | 3.85 |
| 18.2271 | 24.49 | 0.1299 | 4.86324 | 5.78 |
| 19.6361 | 5.16 | 0.5196 | 4.51736 | 1.22 |
| 25.9080 | 86.80 | 0.1082 | 3.43625 | 20.49 |
| 26.7300 | 113.98 | 0.1515 | 3.33242 | 26.90 |
| 27.5309 | 331.44 | 0.1732 | 3.23726 | 78.23 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-006-1757 | 34 | Silicon Oxide | Si O2 | Quartz | 6 |
| * | 04-017-4317 | 24 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 7 |
| * | 01-082-1872 | 10 | Magnesium Aluminum Silicate Hydroxide Hydrate | ( Mg0.669 Al0.331 )4 ( Si4 O10 )2 ( O H )2 ( H2 O )8 | Palygorskite-M | 10 |
| * | 00-042-1339 | 5 | Potassium Magnesium Aluminum Silicate Hydroxide | K Mg3 ( Si3 Al ) O10 ( O H )2 | Phlogopite-2M1 | 5 |
| * | 00-035-0652 | 11 | Potassium Aluminum Silicate Hydroxide Hydrate | K Al4 ( Si , Al )8 O10 ( O H )4 ·4 H2 O | Illite-montmorillonite (NR) | 25 |
| * | 04-025-4215 | 16 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 19 |
| * | 04-008-7810 | 47 | Titanium Oxide | Ti O2 | Rutile | 13 |
| * | 04-016-3203 | 1 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 11 |
| * | 01-075-8690 | 22 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 4 |

Anchor Scan Parameters

Dataset Name	26 CS2 ground 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 26\26 CS2 ground 400C.xrdml

Sample Identification	26 CS2 ground

Measurement Start Date/Time	12/19/2023 7:47:54 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes