26 CS2 ground 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	4.0

Phase Silicon Oxide

Weight fraction/ %	1.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	11.0

Phase Magnesium Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	5.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	3.0

Phase Potassium Sodium Calcium Aluminum Silicate

Weight fraction/ %	39.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	33.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	3.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Silicon Oxide | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Magnesium Aluminum Silicate Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Potassium Sodium Calcium Aluminum Silicate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Aluminum Silicate Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 26 CS2 ground 550C | 4.0 | 1.0 | 11.0 | 5.0 | 3.0 | 39.0 | 33.0 | 3.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7624.0000 | 7632.3891 | 7624.0000 |
| 2.0164 | 7849.6893 | 7592.8968 | 7572.3663 |
| 2.0274 | 7663.5575 | 7541.9395 | 7520.7326 |
| 2.0384 | 7638.5885 | 7491.0158 | 7469.0988 |
| 2.0494 | 7445.2458 | 7440.1278 | 7417.4651 |
| 2.0604 | 7456.6372 | 7389.2779 | 7365.8314 |
| 2.0714 | 7541.9970 | 7338.4688 | 7314.1977 |
| 2.0824 | 7327.7502 | 7287.7033 | 7262.5639 |
| 2.0934 | 7204.1091 | 7236.9845 | 7210.9302 |
| 2.1044 | 7351.0442 | 7186.3158 | 7159.2965 |
| 2.1154 | 7264.9774 | 7135.7009 | 7107.6628 |
| 2.1264 | 7224.9744 | 7085.1439 | 7056.0290 |
| 2.1374 | 7224.8260 | 7034.6494 | 7004.3953 |
| 2.1484 | 7112.5619 | 6984.2223 | 6952.7616 |
| 2.1594 | 7108.2694 | 6933.8685 | 6901.1279 |
| 2.1704 | 7138.1962 | 6883.5942 | 6849.4942 |
| 2.1814 | 7178.7778 | 6833.4068 | 6797.8604 |
| 2.1924 | 7060.0010 | 6783.2849 | 6746.2267 |
| 2.2034 | 6941.6106 | 6733.1942 | 6694.4595 |
| 2.2144 | 6925.7901 | 6683.1905 | 6642.6924 |
| 2.2254 | 6975.7021 | 6633.3173 | 6590.9252 |
| 2.2364 | 6817.7684 | 6583.5913 | 6539.1580 |
| 2.2474 | 6744.7650 | 6534.0324 | 6487.3908 |
| 2.2584 | 6774.7345 | 6484.6652 | 6435.6236 |
| 2.2694 | 6759.0089 | 6435.5197 | 6383.8565 |
| 2.2804 | 6776.5123 | 6386.6328 | 6332.0893 |
| 2.2914 | 6719.8024 | 6338.0495 | 6280.3221 |
| 2.3024 | 6795.5929 | 6289.8252 | 6228.5549 |
| 2.3134 | 6766.3648 | 6242.0272 | 6176.7878 |
| 2.3244 | 6627.0393 | 6194.7368 | 6125.0206 |
| 2.3354 | 6568.8761 | 6148.0519 | 6073.2534 |
| 2.3464 | 6513.8540 | 6102.0887 | 6021.4862 |
| 2.3574 | 6486.7866 | 6056.9842 | 5969.7191 |
| 2.3684 | 6455.1460 | 6012.8973 | 5917.9519 |
| 2.3794 | 6398.2242 | 5970.0104 | 5866.1847 |
| 2.3904 | 6425.5772 | 5928.5294 | 5814.4175 |
| 2.4014 | 6378.8849 | 5888.6831 | 5762.6503 |
| 2.4124 | 6243.9951 | 5850.7209 | 5710.8832 |
| 2.4234 | 6246.0118 | 5814.9091 | 5659.1160 |
| 2.4344 | 6252.8923 | 5781.5258 | 5607.3488 |
| 2.4454 | 6189.9026 | 5750.8534 | 5555.5816 |
| 2.4564 | 6135.5039 | 5723.1692 | 5503.8145 |
| 2.4674 | 6104.5103 | 5698.7349 | 5452.0473 |
| 2.4784 | 6035.3614 | 5677.7834 | 5400.2801 |
| 2.4894 | 6085.4474 | 5660.5050 | 5348.5129 |
| 2.5004 | 6087.7566 | 5647.0320 | 5296.7458 |
| 2.5114 | 5977.8535 | 5637.4228 | 5244.9786 |
| 2.5224 | 5907.5383 | 5631.6447 | 5193.2114 |
| 2.5334 | 5955.6165 | 5629.5557 | 5141.4442 |
| 2.5444 | 5929.3196 | 5630.8855 | 5089.6770 |
| 2.5554 | 5915.0295 | 5635.2135 | 5037.9099 |
| 2.5664 | 5892.4941 | 5641.9149 | 4986.1427 |
| 2.5774 | 5758.6254 | 5650.1481 | 4934.2421 |
| 2.5884 | 5754.0226 | 5658.9290 | 4882.3414 |
| 2.5994 | 5762.7611 | 5667.0019 | 4830.4408 |
| 2.6104 | 5783.7724 | 5672.8106 | 4778.5402 |
| 2.6214 | 5691.6254 | 5674.5415 | 4726.6395 |
| 2.6324 | 5620.5811 | 5670.1838 | 4674.7389 |
| 2.6434 | 5593.1780 | 5657.6517 | 4622.8383 |
| 2.6544 | 5436.6145 | 5634.9734 | 4570.9376 |
| 2.6654 | 5314.3658 | 5600.5270 | 4519.0370 |
| 2.6764 | 5324.7389 | 5553.2744 | 4467.1364 |
| 2.6874 | 5218.6450 | 5492.9297 | 4415.2357 |
| 2.6984 | 5171.9336 | 5420.0084 | 4363.3351 |
| 2.7094 | 5134.3884 | 5335.7400 | 4311.4345 |
| 2.7204 | 5098.6357 | 5241.8737 | 4259.5339 |
| 2.7314 | 4950.0383 | 5140.4378 | 4207.6332 |
| 2.7424 | 4959.8220 | 5033.5136 | 4155.7326 |
| 2.7534 | 4712.4120 | 4923.0277 | 4103.8320 |
| 2.7644 | 4564.4705 | 4810.6679 | 4051.7664 |
| 2.7754 | 4512.5850 | 4697.9662 | 3999.7008 |
| 2.7864 | 4411.8795 | 4586.1679 | 3947.6352 |
| 2.7974 | 4302.4248 | 4476.2308 | 3895.5696 |
| 2.8084 | 4200.2753 | 4368.8904 | 3843.5040 |
| 2.8194 | 4119.0560 | 4264.6879 | 3791.4384 |
| 2.8304 | 3981.1003 | 4163.9978 | 3739.3728 |
| 2.8414 | 3874.7197 | 4067.0508 | 3687.3072 |
| 2.8524 | 3777.1445 | 3973.9549 | 3635.2416 |
| 2.8634 | 3754.7434 | 3884.7146 | 3583.1761 |
| 2.8744 | 3653.9877 | 3799.2482 | 3531.1105 |
| 2.8854 | 3534.9725 | 3717.4047 | 3479.0449 |
| 2.8964 | 3471.2743 | 3638.9800 | 3426.9793 |
| 2.9074 | 3386.1426 | 3563.7311 | 3374.9137 |
| 2.9184 | 3279.5320 | 3491.3909 | 3322.8481 |
| 2.9294 | 3349.3274 | 3421.6792 | 3270.7825 |
| 2.9404 | 3209.8658 | 3357.6731 | 3218.7169 |
| 2.9514 | 3192.3431 | 3304.1065 | 3181.7374 |
| 2.9624 | 2964.4882 | 3255.7082 | 3144.7579 |
| 2.9734 | 3142.2694 | 3208.8756 | 3107.7785 |
| 2.9844 | 2953.0610 | 3163.3864 | 3070.7990 |
| 2.9954 | 2938.5841 | 3119.0415 | 3033.8195 |
| 3.0064 | 2896.0806 | 3075.6655 | 2996.8400 |
| 3.0174 | 2909.0610 | 3033.1060 | 2959.8605 |
| 3.0284 | 2841.2832 | 2991.2322 | 2922.8810 |
| 3.0394 | 2844.0502 | 2949.9335 | 2885.9015 |
| 3.0504 | 2890.8584 | 2909.1172 | 2848.9220 |
| 3.0614 | 2776.7581 | 2868.7060 | 2811.9425 |
| 3.0724 | 2791.8505 | 2828.6365 | 2774.9630 |
| 3.0834 | 2743.3638 | 2788.8565 | 2737.9835 |
| 3.0944 | 2731.5796 | 2749.3236 | 2701.0041 |
| 3.1054 | 2710.8545 | 2710.0029 | 2664.0246 |
| 3.1164 | 2666.9282 | 2670.8663 | 2627.0451 |
| 3.1274 | 2544.5516 | 2635.4296 | 2590.0656 |
| 3.1384 | 2549.4145 | 2608.9518 | 2568.9812 |
| 3.1494 | 2515.6342 | 2586.1393 | 2547.8967 |
| 3.1604 | 2458.9926 | 2563.4399 | 2526.8123 |
| 3.1714 | 2440.3314 | 2540.8426 | 2505.7279 |
| 3.1824 | 2450.8363 | 2518.3381 | 2484.6434 |
| 3.1934 | 2432.7699 | 2495.9182 | 2463.5590 |
| 3.2044 | 2412.2163 | 2473.5759 | 2442.4746 |
| 3.2154 | 2459.8476 | 2451.3050 | 2421.3901 |
| 3.2264 | 2434.6209 | 2429.1001 | 2400.3057 |
| 3.2374 | 2417.7404 | 2406.9563 | 2379.2213 |
| 3.2484 | 2387.5555 | 2384.8691 | 2358.1368 |
| 3.2594 | 2327.1445 | 2362.8346 | 2337.0524 |
| 3.2704 | 2284.1150 | 2340.8493 | 2315.9680 |
| 3.2814 | 2271.0895 | 2318.9096 | 2294.8835 |
| 3.2924 | 2263.6018 | 2297.0128 | 2273.7991 |
| 3.3034 | 2267.0207 | 2275.1559 | 2252.7147 |
| 3.3144 | 2263.4518 | 2253.3364 | 2231.6303 |
| 3.3254 | 2233.8230 | 2231.5520 | 2210.5458 |
| 3.3364 | 2230.9474 | 2209.8005 | 2189.4614 |
| 3.3474 | 2233.9794 | 2188.0799 | 2168.3770 |
| 3.3584 | 2223.7802 | 2166.3884 | 2147.2925 |
| 3.3694 | 2151.0246 | 2144.7242 | 2126.2081 |
| 3.3804 | 2061.0437 | 2123.0856 | 2105.1237 |
| 3.3914 | 2056.5044 | 2101.4714 | 2084.0392 |
| 3.4024 | 2058.1470 | 2079.8800 | 2062.9548 |
| 3.4134 | 2078.7139 | 2058.3101 | 2041.8704 |
| 3.4244 | 2055.2020 | 2036.7607 | 2020.7859 |
| 3.4354 | 1986.3038 | 2015.2305 | 1999.7015 |
| 3.4464 | 1998.7267 | 1993.7185 | 1978.6171 |
| 3.4574 | 1975.4307 | 1972.2238 | 1957.5327 |
| 3.4684 | 1914.0909 | 1950.7455 | 1936.4482 |
| 3.4794 | 1953.5241 | 1929.2827 | 1915.3638 |
| 3.4904 | 1931.2787 | 1907.8345 | 1894.2794 |
| 3.5014 | 1849.9449 | 1887.9096 | 1873.1949 |
| 3.5124 | 1828.7871 | 1871.7579 | 1858.8890 |
| 3.5234 | 1843.5310 | 1857.1281 | 1844.5831 |
| 3.5344 | 1875.2129 | 1842.5103 | 1830.2772 |
| 3.5454 | 1852.1249 | 1827.9038 | 1815.9712 |
| 3.5564 | 1841.9322 | 1813.3083 | 1801.6653 |
| 3.5674 | 1803.4975 | 1798.7230 | 1787.3594 |
| 3.5784 | 1807.4253 | 1784.2271 | 1773.0535 |
| 3.5894 | 1771.4248 | 1769.6865 | 1758.7475 |
| 3.6004 | 1757.4356 | 1755.1710 | 1744.4416 |
| 3.6114 | 1755.4110 | 1740.6367 | 1730.1357 |
| 3.6224 | 1730.7965 | 1726.0986 | 1715.8298 |
| 3.6334 | 1720.0855 | 1711.5683 | 1701.5238 |
| 3.6444 | 1689.9022 | 1697.0456 | 1687.2179 |
| 3.6554 | 1656.1593 | 1682.5301 | 1672.9120 |
| 3.6664 | 1662.9833 | 1668.0214 | 1658.6061 |
| 3.6774 | 1657.1858 | 1653.5194 | 1644.3001 |
| 3.6884 | 1621.6593 | 1639.0709 | 1629.9942 |
| 3.6994 | 1621.4641 | 1624.7461 | 1615.9003 |
| 3.7104 | 1593.0364 | 1610.4743 | 1601.8065 |
| 3.7214 | 1673.4838 | 1596.2082 | 1587.7126 |
| 3.7324 | 1685.6485 | 1581.9474 | 1573.6187 |
| 3.7434 | 1562.5998 | 1567.6917 | 1559.5248 |
| 3.7544 | 1555.9543 | 1553.4411 | 1545.4309 |
| 3.7654 | 1512.5044 | 1539.1952 | 1531.3371 |
| 3.7764 | 1476.7399 | 1524.9538 | 1517.2432 |
| 3.7874 | 1529.5221 | 1510.7169 | 1503.1493 |
| 3.7984 | 1451.1583 | 1496.4842 | 1489.0554 |
| 3.8094 | 1496.3550 | 1482.2557 | 1474.9616 |
| 3.8204 | 1456.1681 | 1468.0311 | 1460.8677 |
| 3.8314 | 1461.9597 | 1453.8102 | 1446.7738 |
| 3.8424 | 1455.3712 | 1439.5931 | 1432.6799 |
| 3.8534 | 1358.0236 | 1425.3794 | 1418.5861 |
| 3.8644 | 1417.5438 | 1411.1692 | 1404.4922 |
| 3.8754 | 1428.6627 | 1397.5472 | 1390.3983 |
| 3.8864 | 1351.5575 | 1385.3856 | 1378.9314 |
| 3.8974 | 1343.5733 | 1373.8119 | 1367.4644 |
| 3.9084 | 1437.3756 | 1362.2411 | 1355.9975 |
| 3.9194 | 1351.5929 | 1350.6733 | 1344.5306 |
| 3.9304 | 1323.1318 | 1339.1082 | 1333.0636 |
| 3.9414 | 1340.0845 | 1327.5459 | 1321.5967 |
| 3.9524 | 1280.2286 | 1315.9861 | 1310.1298 |
| 3.9634 | 1283.5585 | 1304.4289 | 1298.6628 |
| 3.9744 | 1288.2075 | 1292.8741 | 1287.1959 |
| 3.9854 | 1325.6371 | 1281.3218 | 1275.7290 |
| 3.9964 | 1248.8860 | 1269.7717 | 1264.2620 |
| 4.0074 | 1267.3599 | 1258.2239 | 1252.7951 |
| 4.0184 | 1226.7213 | 1246.6782 | 1241.3281 |
| 4.0294 | 1248.9380 | 1235.1347 | 1229.8612 |
| 4.0404 | 1220.5108 | 1223.5932 | 1218.3943 |
| 4.0514 | 1191.1327 | 1212.0537 | 1206.9273 |
| 4.0624 | 1188.0261 | 1201.0578 | 1195.4604 |
| 4.0734 | 1207.3284 | 1191.4131 | 1186.4261 |
| 4.0844 | 1178.2920 | 1182.3120 | 1177.3918 |
| 4.0954 | 1176.6411 | 1173.2126 | 1168.3575 |
| 4.1064 | 1157.5723 | 1164.1150 | 1159.3232 |
| 4.1174 | 1184.4248 | 1155.0191 | 1150.2889 |
| 4.1284 | 1236.4818 | 1145.9249 | 1141.2546 |
| 4.1394 | 1162.3166 | 1136.8322 | 1132.2203 |
| 4.1504 | 1114.4941 | 1127.7412 | 1123.1860 |
| 4.1614 | 1090.0462 | 1118.6518 | 1114.1517 |
| 4.1724 | 1071.5732 | 1109.5639 | 1105.1174 |
| 4.1834 | 1089.0531 | 1100.4774 | 1096.0831 |
| 4.1944 | 1120.3112 | 1091.3925 | 1087.0488 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 26 CS2 ground 550C | 2.0054 | 29.9894 | 0.0110 | 12/19/2023 1:21:00 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6726 | 969.57 | 0.2598 | 33.03049 | 100.00 |
| 5.3124 | 110.33 | 0.1732 | 16.62173 | 11.38 |
| 8.6897 | 173.18 | 0.1515 | 10.16774 | 17.86 |
| 13.5550 | 28.19 | 0.1299 | 6.52717 | 2.91 |
| 15.8219 | 110.25 | 0.1515 | 5.59674 | 11.37 |
| 26.0741 | 43.18 | 0.2165 | 3.41473 | 4.45 |
| 26.7455 | 38.71 | 0.2165 | 3.33051 | 3.99 |
| 27.5616 | 236.80 | 0.0866 | 3.23373 | 24.42 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-017-4317 | 39 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 4 |
| * | 04-006-1757 | 18 | Silicon Oxide | Si O2 | Quartz | 1 |
| * | 01-073-1660 | 7 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 ( Al Si3 O10 ) ( O H ) F | Phlogopite | 11 |
| * | 01-082-1872 | 0 | Magnesium Aluminum Silicate Hydroxide Hydrate | ( Mg0.669 Al0.331 )4 ( Si4 O10 )2 ( O H )2 ( H2 O )8 | Palygorskite-M | 5 |
| * | 01-075-8690 | 32 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 3 |
| * | 01-077-0982 | 19 | Potassium Sodium Calcium Aluminum Silicate | K0.41 Na0.56 Ca0.03 ( Al1.03 Si2.97 O8 ) | Sanidine | 39 |
| * | 04-025-4215 | 26 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 33 |
| * | 01-075-8690 | 32 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 3 |

Anchor Scan Parameters

Dataset Name	26 CS2 ground 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 26\26 CS2 ground 550C.xrdml

Sample Identification	26 CS2 ground 550C

Measurement Start Date/Time	12/19/2023 1:21:00 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes