26 CS2 ground GLYCOL

Graphics

Graphics

Graphics

Quantitative Results

Phase Silicon Oxide

Weight fraction/ %	4.0

Phase Potassium Sodium Calcium Aluminum Silicate

Weight fraction/ %	50.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	9.0

Phase Potassium Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	17.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	20.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	1.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Silicon Oxide | Potassium Sodium Calcium Aluminum Silicate | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Potassium Aluminum Silicate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Aluminum Silicate Hydrate |
| --- | --- | --- | --- | --- | --- | --- |
| 26 CS2 ground glycol | 4.0 | 50.0 | 9.0 | 17.0 | 20.0 | 1.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8100.0000 | 8079.9470 | 8100.0000 |
| 2.0164 | 8173.7586 | 8046.7780 | 8043.2006 |
| 2.0274 | 8071.7876 | 7990.1015 | 7986.4012 |
| 2.0384 | 7981.3451 | 7933.4314 | 7929.6018 |
| 2.0494 | 7912.8850 | 7876.7682 | 7872.8024 |
| 2.0604 | 7932.2738 | 7820.1123 | 7816.0031 |
| 2.0714 | 7945.9823 | 7763.4644 | 7759.2037 |
| 2.0824 | 7693.2709 | 7706.8250 | 7702.4043 |
| 2.0934 | 7803.6588 | 7650.1947 | 7645.6049 |
| 2.1044 | 7726.8496 | 7593.5744 | 7588.8055 |
| 2.1154 | 7782.0216 | 7536.9647 | 7532.0061 |
| 2.1264 | 7670.0280 | 7480.3665 | 7475.2067 |
| 2.1374 | 7672.2330 | 7423.7808 | 7418.4073 |
| 2.1484 | 7599.9336 | 7367.2086 | 7361.6080 |
| 2.1594 | 7559.3894 | 7310.6511 | 7304.8086 |
| 2.1704 | 7581.9425 | 7254.1096 | 7248.0092 |
| 2.1814 | 7435.3058 | 7197.5855 | 7191.2098 |
| 2.1924 | 7478.6278 | 7141.0111 | 7134.4104 |
| 2.2034 | 7396.0177 | 7084.4288 | 7077.4437 |
| 2.2144 | 7413.2522 | 7027.8000 | 7020.4770 |
| 2.2254 | 7271.2478 | 6971.1962 | 6963.5103 |
| 2.2364 | 7375.2522 | 6914.6200 | 6906.5436 |
| 2.2474 | 7276.6991 | 6858.0743 | 6849.5769 |
| 2.2584 | 7286.9656 | 6801.5622 | 6792.6102 |
| 2.2694 | 7397.5133 | 6745.0875 | 6735.6435 |
| 2.2804 | 7404.1027 | 6688.6543 | 6678.6768 |
| 2.2914 | 7237.4739 | 6632.2674 | 6621.7101 |
| 2.3024 | 7211.4911 | 6575.9324 | 6564.7433 |
| 2.3134 | 7140.6883 | 6519.6555 | 6507.7766 |
| 2.3244 | 7097.4449 | 6463.4441 | 6450.8099 |
| 2.3354 | 7027.3245 | 6407.3067 | 6393.8432 |
| 2.3464 | 7064.4322 | 6351.2532 | 6336.8765 |
| 2.3574 | 7048.0157 | 6295.2952 | 6279.9098 |
| 2.3684 | 7034.0295 | 6239.4466 | 6222.9431 |
| 2.3794 | 7034.6598 | 6183.6675 | 6165.9764 |
| 2.3904 | 6851.4833 | 6128.0100 | 6108.8743 |
| 2.4014 | 6810.2655 | 6072.4646 | 6051.7723 |
| 2.4124 | 6802.3348 | 6017.1153 | 5994.6702 |
| 2.4234 | 6717.0541 | 5961.9962 | 5937.5681 |
| 2.4344 | 6714.3805 | 5907.1490 | 5880.4661 |
| 2.4454 | 6675.9194 | 5852.6251 | 5823.3640 |
| 2.4564 | 6657.7950 | 5798.4883 | 5766.2619 |
| 2.4674 | 6678.4808 | 5744.8194 | 5709.1599 |
| 2.4784 | 6682.0266 | 5691.7206 | 5652.0578 |
| 2.4894 | 6598.9508 | 5639.3254 | 5594.9557 |
| 2.5004 | 6508.4690 | 5587.8125 | 5537.8537 |
| 2.5114 | 6463.8574 | 5537.4364 | 5480.7516 |
| 2.5224 | 6437.6214 | 5488.5892 | 5423.6495 |
| 2.5334 | 6527.7257 | 5441.9321 | 5366.5474 |
| 2.5444 | 6468.1499 | 5398.6498 | 5309.4454 |
| 2.5554 | 6397.6037 | 5360.8888 | 5252.3433 |
| 2.5664 | 6312.1077 | 5332.3831 | 5195.2412 |
| 2.5774 | 6328.3048 | 5319.1187 | 5138.1392 |
| 2.5884 | 6215.5663 | 5329.6278 | 5081.0371 |
| 2.5994 | 6223.6018 | 5374.2837 | 5023.9350 |
| 2.6104 | 6153.4026 | 5462.9991 | 4966.8330 |
| 2.6214 | 6060.1436 | 5601.1574 | 4909.7309 |
| 2.6324 | 6118.6637 | 5784.0173 | 4852.6288 |
| 2.6434 | 6190.9213 | 5989.6892 | 4795.5268 |
| 2.6544 | 6103.3004 | 6171.5241 | 4738.4247 |
| 2.6654 | 5985.8289 | 6261.7530 | 4681.3226 |
| 2.6764 | 5903.2679 | 6203.8096 | 4624.2206 |
| 2.6874 | 5811.0816 | 5997.7585 | 4567.1185 |
| 2.6984 | 5712.1150 | 5700.6412 | 4510.0164 |
| 2.7094 | 5581.4454 | 5380.6203 | 4452.9143 |
| 2.7204 | 5332.2974 | 5083.9599 | 4395.8123 |
| 2.7314 | 5212.9144 | 4832.2664 | 4338.7102 |
| 2.7424 | 5187.2945 | 4630.0510 | 4281.6081 |
| 2.7534 | 5083.0334 | 4471.7500 | 4224.5061 |
| 2.7644 | 4862.0044 | 4347.4318 | 4167.2686 |
| 2.7754 | 4827.7207 | 4246.6883 | 4110.0312 |
| 2.7864 | 4747.7148 | 4161.0690 | 4052.7938 |
| 2.7974 | 4652.8141 | 4084.6224 | 3995.5563 |
| 2.8084 | 4428.4552 | 4013.6449 | 3938.3189 |
| 2.8194 | 4380.3520 | 3946.0121 | 3881.0815 |
| 2.8304 | 4212.9926 | 3880.5524 | 3823.8441 |
| 2.8414 | 4014.9783 | 3816.6122 | 3766.6066 |
| 2.8524 | 3900.7340 | 3753.8031 | 3709.3692 |
| 2.8634 | 3866.2389 | 3691.8727 | 3652.1318 |
| 2.8744 | 3688.2792 | 3630.6431 | 3594.8943 |
| 2.8854 | 3679.0669 | 3569.9819 | 3537.6569 |
| 2.8964 | 3556.5442 | 3509.7869 | 3480.4195 |
| 2.9074 | 3558.0885 | 3449.9779 | 3423.1820 |
| 2.9184 | 3318.4513 | 3390.4913 | 3365.9446 |
| 2.9294 | 3383.1917 | 3331.2758 | 3308.7072 |
| 2.9404 | 3210.5369 | 3279.1838 | 3251.4697 |
| 2.9514 | 3215.6696 | 3230.1526 | 3210.8854 |
| 2.9624 | 3106.9100 | 3188.1831 | 3170.3010 |
| 2.9734 | 3049.7148 | 3146.3582 | 3129.7167 |
| 2.9844 | 3014.4218 | 3104.6585 | 3089.1323 |
| 2.9954 | 2926.9912 | 3063.0679 | 3048.5480 |
| 3.0064 | 2957.5069 | 3021.5727 | 3007.9636 |
| 3.0174 | 2868.3382 | 2980.1612 | 2967.3793 |
| 3.0284 | 2831.1239 | 2938.8236 | 2926.7949 |
| 3.0394 | 2773.4199 | 2897.5513 | 2886.2106 |
| 3.0504 | 2847.3141 | 2856.3371 | 2845.6262 |
| 3.0614 | 2680.6431 | 2815.1746 | 2805.0419 |
| 3.0724 | 2654.5320 | 2774.0584 | 2764.4575 |
| 3.0834 | 2712.3422 | 2732.9836 | 2723.8732 |
| 3.0944 | 2674.8053 | 2691.9462 | 2683.2888 |
| 3.1054 | 2663.3648 | 2650.9423 | 2642.7045 |
| 3.1164 | 2560.4160 | 2609.9689 | 2602.1201 |
| 3.1274 | 2614.6489 | 2576.4586 | 2561.5358 |
| 3.1384 | 2500.9794 | 2546.0636 | 2538.9130 |
| 3.1494 | 2492.6686 | 2523.1271 | 2516.2902 |
| 3.1604 | 2468.9160 | 2500.2113 | 2493.6675 |
| 3.1714 | 2592.4002 | 2477.3146 | 2471.0447 |
| 3.1824 | 2536.8009 | 2454.4352 | 2448.4219 |
| 3.1934 | 2467.3628 | 2431.5718 | 2425.7991 |
| 3.2044 | 2471.4739 | 2408.7231 | 2403.1764 |
| 3.2154 | 2459.5988 | 2385.8879 | 2380.5536 |
| 3.2264 | 2371.6548 | 2363.0651 | 2357.9308 |
| 3.2374 | 2317.3107 | 2340.2539 | 2335.3081 |
| 3.2484 | 2340.6111 | 2317.4533 | 2312.6853 |
| 3.2594 | 2311.1150 | 2294.6626 | 2290.0625 |
| 3.2704 | 2246.4995 | 2271.8811 | 2267.4397 |
| 3.2814 | 2214.7227 | 2249.1081 | 2244.8170 |
| 3.2924 | 2216.9425 | 2226.3430 | 2222.1942 |
| 3.3034 | 2196.7807 | 2203.5853 | 2199.5714 |
| 3.3144 | 2169.7011 | 2183.4347 | 2176.9486 |
| 3.3254 | 2170.2006 | 2164.3712 | 2160.6070 |
| 3.3364 | 2145.0496 | 2147.9140 | 2144.2654 |
| 3.3474 | 2106.5162 | 2131.4625 | 2127.9238 |
| 3.3584 | 2098.7006 | 2115.0162 | 2111.5822 |
| 3.3694 | 2118.5300 | 2098.5748 | 2095.2406 |
| 3.3804 | 2088.7714 | 2082.1381 | 2078.8990 |
| 3.3914 | 2082.5310 | 2065.7058 | 2062.5574 |
| 3.4024 | 2077.3908 | 2049.2775 | 2046.2158 |
| 3.4134 | 2055.0000 | 2032.8532 | 2029.8742 |
| 3.4244 | 2063.7832 | 2016.4324 | 2013.5326 |
| 3.4354 | 2034.7276 | 2000.0152 | 1997.1910 |
| 3.4464 | 2025.0329 | 1983.6011 | 1980.8494 |
| 3.4574 | 2011.5929 | 1967.1902 | 1964.5078 |
| 3.4684 | 1933.8943 | 1950.7821 | 1948.1662 |
| 3.4794 | 1907.9990 | 1934.3768 | 1931.8246 |
| 3.4904 | 1895.5398 | 1917.9741 | 1915.4830 |
| 3.5014 | 1928.9813 | 1901.5739 | 1899.1414 |
| 3.5124 | 1906.2320 | 1885.1760 | 1882.7998 |
| 3.5234 | 1853.9764 | 1868.7803 | 1866.4582 |
| 3.5344 | 1836.4577 | 1851.8388 | 1850.1166 |
| 3.5454 | 1844.3697 | 1834.3930 | 1833.7750 |
| 3.5564 | 1775.4292 | 1817.6484 | 1817.4334 |
| 3.5674 | 1793.7198 | 1801.3081 | 1801.0918 |
| 3.5784 | 1751.4208 | 1784.9679 | 1784.7502 |
| 3.5894 | 1788.4336 | 1768.7386 | 1768.4086 |
| 3.6004 | 1758.8500 | 1752.4002 | 1752.0670 |
| 3.6114 | 1762.6844 | 1736.1175 | 1735.7254 |
| 3.6224 | 1757.3186 | 1719.7798 | 1719.3838 |
| 3.6334 | 1766.4671 | 1703.4419 | 1703.0422 |
| 3.6444 | 1709.1416 | 1687.1041 | 1686.7006 |
| 3.6554 | 1680.1268 | 1670.7663 | 1670.3590 |
| 3.6664 | 1671.0084 | 1654.4286 | 1654.0174 |
| 3.6774 | 1614.4326 | 1638.0909 | 1637.6758 |
| 3.6884 | 1624.4912 | 1623.7397 | 1621.3342 |
| 3.6994 | 1620.7502 | 1610.2141 | 1609.7909 |
| 3.7104 | 1612.7591 | 1598.6749 | 1598.2476 |
| 3.7214 | 1579.8908 | 1587.1358 | 1586.7043 |
| 3.7324 | 1629.0629 | 1575.5968 | 1575.1609 |
| 3.7434 | 1590.6106 | 1564.0578 | 1563.6176 |
| 3.7544 | 1614.7198 | 1552.5190 | 1552.0743 |
| 3.7654 | 1585.0698 | 1540.9801 | 1540.5310 |
| 3.7764 | 1476.3254 | 1529.4414 | 1528.9876 |
| 3.7874 | 1615.7346 | 1517.9028 | 1517.4443 |
| 3.7984 | 1509.9759 | 1506.3642 | 1505.9010 |
| 3.8094 | 1502.8269 | 1494.8257 | 1494.3577 |
| 3.8204 | 1493.8216 | 1483.2873 | 1482.8143 |
| 3.8314 | 1553.5732 | 1471.7490 | 1471.2710 |
| 3.8424 | 1470.5270 | 1460.2108 | 1459.7277 |
| 3.8534 | 1444.6490 | 1448.6726 | 1448.1844 |
| 3.8644 | 1455.2350 | 1437.1346 | 1436.6411 |
| 3.8754 | 1461.7679 | 1426.5199 | 1425.0977 |
| 3.8864 | 1377.3894 | 1416.2890 | 1415.7846 |
| 3.8974 | 1374.3953 | 1406.9815 | 1406.4715 |
| 3.9084 | 1396.0325 | 1397.6741 | 1397.1584 |
| 3.9194 | 1415.3363 | 1388.3667 | 1387.8452 |
| 3.9304 | 1392.6234 | 1379.0595 | 1378.5321 |
| 3.9414 | 1324.1426 | 1369.7525 | 1369.2190 |
| 3.9524 | 1337.0207 | 1360.4455 | 1359.9058 |
| 3.9634 | 1358.9194 | 1351.1386 | 1350.5927 |
| 3.9744 | 1311.4002 | 1341.8319 | 1341.2796 |
| 3.9854 | 1306.8407 | 1332.5253 | 1331.9665 |
| 3.9964 | 1288.2689 | 1323.2189 | 1322.6533 |
| 4.0074 | 1308.6873 | 1313.9126 | 1313.3402 |
| 4.0184 | 1305.5634 | 1304.6064 | 1304.0271 |
| 4.0294 | 1243.8771 | 1295.3004 | 1294.7140 |
| 4.0404 | 1265.1446 | 1285.9945 | 1285.4008 |
| 4.0514 | 1291.4159 | 1276.6888 | 1276.0877 |
| 4.0624 | 1268.5079 | 1267.3832 | 1266.7746 |
| 4.0734 | 1269.3501 | 1258.0778 | 1257.4615 |
| 4.0844 | 1263.4956 | 1248.7726 | 1248.1483 |
| 4.0954 | 1249.7768 | 1239.4675 | 1238.8352 |
| 4.1064 | 1253.6312 | 1230.1627 | 1229.5221 |
| 4.1174 | 1191.0000 | 1220.8580 | 1220.2090 |
| 4.1284 | 1189.8835 | 1211.5535 | 1210.8958 |
| 4.1394 | 1184.5398 | 1202.2492 | 1201.5827 |
| 4.1504 | 1192.0929 | 1192.9452 | 1192.2696 |
| 4.1614 | 1200.9557 | 1183.6413 | 1182.9565 |
| 4.1724 | 1166.8825 | 1174.3377 | 1173.6433 |
| 4.1834 | 1133.7611 | 1165.0343 | 1164.3302 |
| 4.1944 | 1149.3093 | 1155.7311 | 1155.0171 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 26 CS2 ground glycol | 2.0054 | 29.9894 | 0.0110 | 12/20/2023 12:29:11 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6686 | 1451.98 | 0.0866 | 33.07974 | 100.00 |
| 5.3209 | 118.34 | 0.1732 | 16.59534 | 8.15 |
| 6.9711 | 95.31 | 0.4330 | 12.67001 | 6.56 |
| 8.7144 | 250.21 | 0.1299 | 10.13897 | 17.23 |
| 13.5521 | 51.74 | 0.1299 | 6.52858 | 3.56 |
| 15.7232 | 487.29 | 0.0866 | 5.63164 | 33.56 |
| 18.1835 | 77.97 | 0.0866 | 4.87482 | 5.37 |
| 19.7152 | 24.00 | 0.5196 | 4.49941 | 1.65 |
| 20.8154 | 15.95 | 0.5196 | 4.26401 | 1.10 |
| 22.3994 | 31.91 | 0.2598 | 3.96593 | 2.20 |
| 23.3226 | 45.17 | 0.1299 | 3.81099 | 3.11 |
| 24.2041 | 22.04 | 0.2598 | 3.67415 | 1.52 |
| 25.8880 | 357.81 | 0.0974 | 3.43886 | 24.64 |
| 26.6589 | 293.98 | 0.0974 | 3.34113 | 20.25 |
| 27.4848 | 707.89 | 0.0974 | 3.24259 | 48.75 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-075-0443 | 54 | Silicon Oxide | Si O2 | Quartz | 4 |
| * | 04-016-1657 | 54 | Potassium Sodium Calcium Aluminum Silicate | K0.42 Na0.58 Ca0.03 Al Si3 O8 | Sanidine | 50 |
| * | 04-023-1515 | 48 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.93 Na0.05 Mg1.71 Ti0.13 Fe0.97 Al1.44 Si2.75 O10.47 ( O H )1.33 F0.2 | Phlogopite-1M | 9 |
| * | 00-035-0652 | 10 | Potassium Aluminum Silicate Hydroxide Hydrate | K Al4 ( Si , Al )8 O10 ( O H )4 ·4 H2 O | Illite-montmorillonite (NR) | 17 |
| * | 04-025-4215 | 35 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 20 |
| * | 01-075-8690 | 11 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 1 |

Anchor Scan Parameters

Dataset Name	26 CS2 ground glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 26\26 CS2 ground glycol.xrdml

Sample Identification	26 CS2 ground glycol

Measurement Start Date/Time	12/20/2023 12:29:11 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes