26 CS2 ground REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	11.0

Phase Silicon Oxide

Weight fraction/ %	4.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	3.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	9.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	55.0

Phase Potassium Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	16.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Silicon Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Silicate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Aluminum Silicate Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 26 CS2 ground | 11.0 | 4.0 | 3.0 | 2.0 | 9.0 | 55.0 | 16.0 | 0.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8914.0000 | 8943.5166 | 8914.0000 |
| 2.0164 | 8817.8402 | 8882.0701 | 8847.2323 |
| 2.0274 | 8803.4759 | 8816.4314 | 8780.4647 |
| 2.0384 | 8739.2021 | 8750.8477 | 8713.6970 |
| 2.0494 | 8643.6873 | 8685.3226 | 8646.9294 |
| 2.0604 | 8706.8879 | 8619.8600 | 8580.1617 |
| 2.0714 | 8575.9941 | 8554.4641 | 8513.3941 |
| 2.0824 | 8476.8151 | 8489.1395 | 8446.6264 |
| 2.0934 | 8377.5674 | 8423.8911 | 8379.8587 |
| 2.1044 | 8557.6637 | 8358.7243 | 8313.0911 |
| 2.1154 | 8524.8977 | 8293.6451 | 8246.3234 |
| 2.1264 | 8288.6932 | 8228.6600 | 8179.5558 |
| 2.1374 | 8505.4956 | 8163.7760 | 8112.7881 |
| 2.1484 | 8412.6357 | 8099.0012 | 8046.0205 |
| 2.1594 | 8264.1917 | 8034.3443 | 7979.2528 |
| 2.1704 | 8201.6976 | 7969.8151 | 7912.4851 |
| 2.1814 | 8135.1799 | 7905.4250 | 7845.7175 |
| 2.1924 | 8157.5516 | 7841.1732 | 7778.9498 |
| 2.2034 | 8185.5044 | 7776.9050 | 7711.9729 |
| 2.2144 | 8024.0782 | 7712.8070 | 7644.9959 |
| 2.2254 | 7923.7591 | 7648.9125 | 7578.0189 |
| 2.2364 | 7928.6224 | 7585.2455 | 7511.0419 |
| 2.2474 | 8041.8476 | 7521.8347 | 7444.0650 |
| 2.2584 | 7924.3845 | 7458.7151 | 7377.0880 |
| 2.2694 | 7834.5516 | 7395.9291 | 7310.1110 |
| 2.2804 | 7759.7655 | 7333.5288 | 7243.1340 |
| 2.2914 | 7762.4848 | 7271.5780 | 7176.1571 |
| 2.3024 | 7742.0575 | 7210.1549 | 7109.1801 |
| 2.3134 | 7710.1495 | 7149.3555 | 7042.2031 |
| 2.3244 | 7746.4066 | 7089.2964 | 6975.2262 |
| 2.3354 | 7685.6135 | 7030.1191 | 6908.2492 |
| 2.3464 | 7451.0030 | 6971.9933 | 6841.2722 |
| 2.3574 | 7561.5625 | 6915.1213 | 6774.2952 |
| 2.3684 | 7614.5295 | 6859.7410 | 6707.3183 |
| 2.3794 | 7474.6726 | 6806.1185 | 6640.3413 |
| 2.3904 | 7475.4263 | 6754.4344 | 6573.1950 |
| 2.4014 | 7490.4867 | 6705.1850 | 6506.0487 |
| 2.4124 | 7405.1613 | 6658.7804 | 6438.9024 |
| 2.4234 | 7394.2330 | 6615.6563 | 6371.7560 |
| 2.4344 | 7426.5369 | 6576.2793 | 6304.6097 |
| 2.4454 | 7309.7551 | 6541.1366 | 6237.4634 |
| 2.4564 | 7198.4646 | 6510.7240 | 6170.3171 |
| 2.4674 | 7225.4897 | 6485.5297 | 6103.1708 |
| 2.4784 | 7233.8594 | 6466.0153 | 6036.0245 |
| 2.4894 | 7177.1436 | 6452.5935 | 5968.8782 |
| 2.5004 | 7205.8407 | 6445.6037 | 5901.7319 |
| 2.5114 | 7136.2684 | 6445.2851 | 5834.5855 |
| 2.5224 | 7088.9036 | 6451.7487 | 5767.4392 |
| 2.5334 | 7047.8436 | 6464.9474 | 5700.2929 |
| 2.5444 | 6963.2733 | 6484.6445 | 5633.1466 |
| 2.5554 | 6992.6224 | 6510.3797 | 5566.0003 |
| 2.5664 | 7065.1180 | 6541.4317 | 5498.8540 |
| 2.5774 | 7036.5909 | 6576.7752 | 5431.7077 |
| 2.5884 | 6910.5890 | 6615.0332 | 5364.5614 |
| 2.5994 | 6893.5133 | 6654.4258 | 5297.4150 |
| 2.6104 | 6842.7232 | 6692.7234 | 5230.2687 |
| 2.6214 | 6748.0531 | 6727.2207 | 5163.1224 |
| 2.6324 | 6776.7478 | 6754.7561 | 5095.9761 |
| 2.6434 | 6683.3746 | 6771.8111 | 5028.8298 |
| 2.6544 | 6622.2217 | 6774.7186 | 4961.6835 |
| 2.6654 | 6479.8318 | 6759.9891 | 4894.5372 |
| 2.6764 | 6459.4907 | 6724.7237 | 4827.3909 |
| 2.6874 | 6395.0816 | 6667.0297 | 4760.2445 |
| 2.6984 | 6155.9601 | 6586.3268 | 4693.0982 |
| 2.7094 | 6075.6942 | 6483.4462 | 4625.9519 |
| 2.7204 | 5883.2542 | 6360.4889 | 4558.8056 |
| 2.7314 | 5850.6018 | 6220.4916 | 4491.6593 |
| 2.7424 | 5589.6563 | 6067.0032 | 4424.5130 |
| 2.7534 | 5445.2419 | 5903.6383 | 4357.3667 |
| 2.7644 | 5288.9144 | 5733.8338 | 4290.0510 |
| 2.7754 | 5104.8309 | 5560.7603 | 4222.7354 |
| 2.7864 | 5083.3633 | 5386.9649 | 4155.4197 |
| 2.7974 | 4707.8937 | 5214.6827 | 4088.1041 |
| 2.8084 | 4623.1101 | 5045.5579 | 4020.7884 |
| 2.8194 | 4478.0216 | 4880.9317 | 3953.4728 |
| 2.8304 | 4226.1681 | 4721.7717 | 3886.1571 |
| 2.8414 | 4170.5034 | 4568.7498 | 3818.8415 |
| 2.8524 | 4047.8058 | 4422.2836 | 3751.5258 |
| 2.8634 | 3787.9026 | 4282.5737 | 3684.2102 |
| 2.8744 | 3716.7984 | 4149.6365 | 3616.8945 |
| 2.8854 | 3642.2370 | 4023.3362 | 3549.5788 |
| 2.8964 | 3616.1106 | 3903.4134 | 3482.2632 |
| 2.9074 | 3500.4031 | 3789.5140 | 3414.9475 |
| 2.9184 | 3297.1052 | 3681.2146 | 3347.6319 |
| 2.9294 | 3205.6490 | 3578.0475 | 3280.3162 |
| 2.9404 | 3224.5973 | 3487.3465 | 3213.0006 |
| 2.9514 | 3212.5211 | 3414.1429 | 3174.6856 |
| 2.9624 | 3151.8805 | 3352.4257 | 3136.3707 |
| 2.9734 | 3101.8387 | 3293.9087 | 3098.0557 |
| 2.9844 | 3008.0280 | 3238.1623 | 3059.7407 |
| 2.9954 | 2968.5044 | 3184.7940 | 3021.4258 |
| 3.0064 | 2800.5025 | 3133.4521 | 2983.1108 |
| 3.0174 | 2840.8004 | 3083.8265 | 2944.7959 |
| 3.0284 | 2878.2743 | 3035.6473 | 2906.4809 |
| 3.0394 | 2821.7463 | 2988.6832 | 2868.1660 |
| 3.0504 | 2778.2385 | 2942.7381 | 2829.8510 |
| 3.0614 | 2799.9528 | 2897.6475 | 2791.5360 |
| 3.0724 | 2626.6136 | 2853.2748 | 2753.2211 |
| 3.0834 | 2653.3628 | 2809.5072 | 2714.9061 |
| 3.0944 | 2654.8982 | 2766.2522 | 2676.5912 |
| 3.1054 | 2577.8486 | 2723.4343 | 2638.2762 |
| 3.1164 | 2630.1367 | 2680.9920 | 2599.9612 |
| 3.1274 | 2553.9587 | 2646.9403 | 2561.6463 |
| 3.1384 | 2501.9154 | 2614.1137 | 2540.4023 |
| 3.1494 | 2515.7129 | 2589.6029 | 2519.1583 |
| 3.1604 | 2485.4380 | 2565.3151 | 2497.9143 |
| 3.1714 | 2411.9892 | 2541.2269 | 2476.6703 |
| 3.1824 | 2352.7026 | 2517.3190 | 2455.4263 |
| 3.1934 | 2388.0177 | 2493.5746 | 2434.1823 |
| 3.2044 | 2382.6028 | 2469.9795 | 2412.9383 |
| 3.2154 | 2376.0000 | 2446.5213 | 2391.6943 |
| 3.2264 | 2383.6504 | 2423.1890 | 2370.4503 |
| 3.2374 | 2387.2085 | 2399.9730 | 2349.2063 |
| 3.2484 | 2370.6111 | 2376.8646 | 2327.9623 |
| 3.2594 | 2328.2773 | 2353.8561 | 2306.7183 |
| 3.2704 | 2250.2881 | 2330.9405 | 2285.4743 |
| 3.2814 | 2204.5831 | 2308.1113 | 2264.2303 |
| 3.2924 | 2197.5310 | 2285.3628 | 2242.9863 |
| 3.3034 | 2211.8869 | 2262.6896 | 2221.7423 |
| 3.3144 | 2223.8471 | 2241.1237 | 2200.4983 |
| 3.3254 | 2204.0590 | 2219.7447 | 2181.4491 |
| 3.3364 | 2131.7173 | 2199.4645 | 2162.3999 |
| 3.3474 | 2104.0187 | 2179.2422 | 2143.3507 |
| 3.3584 | 2127.9912 | 2159.0743 | 2124.3015 |
| 3.3694 | 2094.0550 | 2138.9575 | 2105.2523 |
| 3.3804 | 2048.5280 | 2118.8889 | 2086.2031 |
| 3.3914 | 2071.8407 | 2098.8656 | 2067.1539 |
| 3.4024 | 2008.8063 | 2078.8849 | 2048.1047 |
| 3.4134 | 1997.1278 | 2058.9446 | 2029.0555 |
| 3.4244 | 2008.8481 | 2039.0422 | 2010.0063 |
| 3.4354 | 2027.6854 | 2019.1757 | 1990.9571 |
| 3.4464 | 1970.9036 | 1999.3431 | 1971.9079 |
| 3.4574 | 1960.8348 | 1979.5427 | 1952.8587 |
| 3.4684 | 1938.6662 | 1959.7726 | 1933.8095 |
| 3.4794 | 1917.8230 | 1940.0314 | 1914.7603 |
| 3.4904 | 1881.4425 | 1920.3174 | 1895.7111 |
| 3.5014 | 1855.6273 | 1901.5636 | 1876.6619 |
| 3.5124 | 1899.5035 | 1882.9433 | 1859.5903 |
| 3.5234 | 1838.1563 | 1865.2807 | 1842.5186 |
| 3.5344 | 1811.9184 | 1847.6402 | 1825.4470 |
| 3.5454 | 1835.4602 | 1830.0209 | 1808.3753 |
| 3.5564 | 1771.8953 | 1812.4216 | 1791.3036 |
| 3.5674 | 1742.2734 | 1794.8415 | 1774.2320 |
| 3.5784 | 1719.0290 | 1777.2795 | 1757.1603 |
| 3.5894 | 1725.8584 | 1759.7350 | 1740.0886 |
| 3.6004 | 1682.2856 | 1742.2070 | 1723.0170 |
| 3.6114 | 1720.6421 | 1724.6948 | 1705.9453 |
| 3.6224 | 1725.1254 | 1707.1977 | 1688.8737 |
| 3.6334 | 1709.0757 | 1689.7150 | 1671.8020 |
| 3.6444 | 1666.9257 | 1672.2461 | 1654.7303 |
| 3.6554 | 1647.1888 | 1654.7903 | 1637.6587 |
| 3.6664 | 1668.1106 | 1637.3472 | 1620.5870 |
| 3.6774 | 1584.3077 | 1619.9161 | 1603.5154 |
| 3.6884 | 1541.0619 | 1605.0895 | 1586.4437 |
| 3.6994 | 1586.1052 | 1590.5763 | 1574.8602 |
| 3.7104 | 1627.2994 | 1578.6666 | 1563.2766 |
| 3.7214 | 1619.9911 | 1566.7671 | 1551.6931 |
| 3.7324 | 1559.4995 | 1554.8773 | 1540.1096 |
| 3.7434 | 1536.1603 | 1542.9969 | 1528.5261 |
| 3.7544 | 1568.3997 | 1531.1255 | 1516.9425 |
| 3.7654 | 1508.1396 | 1519.2627 | 1505.3590 |
| 3.7764 | 1523.6195 | 1507.4082 | 1493.7755 |
| 3.7874 | 1558.6903 | 1495.5617 | 1482.1919 |
| 3.7984 | 1523.6489 | 1483.7228 | 1470.6084 |
| 3.8094 | 1422.7866 | 1471.8913 | 1459.0249 |
| 3.8204 | 1469.6460 | 1460.0670 | 1447.4413 |
| 3.8314 | 1390.1367 | 1448.2494 | 1435.8578 |
| 3.8424 | 1442.3678 | 1436.4385 | 1424.2743 |
| 3.8534 | 1467.0649 | 1424.6339 | 1412.6908 |
| 3.8644 | 1463.7547 | 1412.8354 | 1401.1072 |
| 3.8754 | 1404.9469 | 1401.0427 | 1389.5237 |
| 3.8864 | 1330.5310 | 1389.2558 | 1377.9402 |
| 3.8974 | 1394.8328 | 1377.4744 | 1366.3566 |
| 3.9084 | 1373.0723 | 1365.6982 | 1354.7731 |
| 3.9194 | 1348.9823 | 1353.9271 | 1343.1896 |
| 3.9304 | 1395.4538 | 1342.1610 | 1331.6060 |
| 3.9414 | 1312.7335 | 1330.3996 | 1320.0225 |
| 3.9524 | 1316.2890 | 1318.6428 | 1308.4390 |
| 3.9634 | 1226.5123 | 1306.8904 | 1296.8555 |
| 3.9744 | 1254.5978 | 1295.1424 | 1285.2719 |
| 3.9854 | 1253.9912 | 1283.3985 | 1273.6884 |
| 3.9964 | 1300.8230 | 1271.6586 | 1262.1049 |
| 4.0074 | 1234.3363 | 1259.9226 | 1250.5213 |
| 4.0184 | 1195.7625 | 1248.2612 | 1238.9378 |
| 4.0294 | 1180.9076 | 1236.5981 | 1227.3543 |
| 4.0404 | 1173.0831 | 1224.8899 | 1215.7707 |
| 4.0514 | 1185.4543 | 1213.1709 | 1204.1872 |
| 4.0624 | 1211.3928 | 1202.1318 | 1192.6037 |
| 4.0734 | 1185.5359 | 1191.1750 | 1182.4521 |
| 4.0844 | 1192.5442 | 1180.8978 | 1172.3006 |
| 4.0954 | 1145.0590 | 1170.6237 | 1162.1490 |
| 4.1064 | 1139.9734 | 1160.3526 | 1151.9975 |
| 4.1174 | 1110.6342 | 1150.0845 | 1141.8459 |
| 4.1284 | 1158.7478 | 1139.8192 | 1131.6944 |
| 4.1394 | 1170.8525 | 1129.5566 | 1121.5428 |
| 4.1504 | 1110.0855 | 1119.2968 | 1111.3913 |
| 4.1614 | 1085.2242 | 1109.0395 | 1101.2397 |
| 4.1724 | 1093.9783 | 1098.7848 | 1091.0882 |
| 4.1834 | 1070.3805 | 1088.5325 | 1080.9366 |
| 4.1944 | 1075.1499 | 1078.2827 | 1070.7851 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 26 CS2 ground | 2.0054 | 29.9894 | 0.0110 | 12/13/2023 11:47:56 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6842 | 1701.68 | 0.2598 | 32.88762 | 100.00 |
| 5.3130 | 105.04 | 0.1299 | 16.61979 | 6.17 |
| 7.1000 | 69.74 | 0.4330 | 12.44033 | 4.10 |
| 8.7014 | 171.85 | 0.0649 | 10.15404 | 10.10 |
| 13.3816 | 7.95 | 0.5196 | 6.61136 | 0.47 |
| 15.7133 | 186.44 | 0.0541 | 5.63516 | 10.96 |
| 18.1582 | 30.96 | 0.1299 | 4.88155 | 1.82 |
| 25.8871 | 132.43 | 0.1082 | 3.43898 | 7.78 |
| 26.6822 | 135.73 | 0.1299 | 3.33827 | 7.98 |
| 27.4684 | 350.33 | 0.1732 | 3.24448 | 20.59 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-008-7810 | 60 | Titanium Oxide | Ti O2 | Rutile | 11 |
| * | 01-085-0504 | 38 | Silicon Oxide | Si O2 | Quartz | 4 |
| * | 04-017-4317 | 18 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 3 |
| * | 01-081-8598 | 6 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2 Al2 ) Si8 O20 ( H2 O )4 ( O H )2 ( H2 O )3.84 | Palygorskite-M | 2 |
| * | 01-080-5015 | 1 | Magnesium Silicate Hydroxide Hydrate | Mg7.18 ( Si12 O30 ) ( O H )4 ( H2 O )4 ( H2 O )6 | Sepiolite | 9 |
| * | 04-025-4215 | 24 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 55 |
| * | 00-035-0652 | 5 | Potassium Aluminum Silicate Hydroxide Hydrate | K Al4 ( Si , Al )8 O10 ( O H )4 ·4 H2 O | Illite-montmorillonite (NR) | 16 |
| * | 01-075-8690 | 5 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | - |

Anchor Scan Parameters

Dataset Name	26 CS2 ground

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 26\26 CS2 ground.xrdml

Sample Identification	26 CS2 ground

Measurement Start Date/Time	12/13/2023 11:47:56 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes