27 SS2_63 um 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	8.0

Phase Silicon Oxide

Weight fraction/ %	6.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	49.0

Phase Sodium Aluminum Silicate

Weight fraction/ %	21.0

Phase Potassium Manganese Silicate Hydrate

Weight fraction/ %	4.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	5.0

Phase Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Magnesium Aluminum Iron Silicon Titanium Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Silicon Oxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Aluminum Silicate | Potassium Manganese Silicate Hydrate | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Magnesium Aluminum Iron Silicon Titanium Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 27 SS2 _63 400C | 8.0 | 6.0 | 49.0 | 21.0 | 4.0 | 5.0 | 4.0 | 4.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5543.0000 | 5533.2706 | 5543.0000 |
| 2.0164 | 5485.6067 | 5508.8136 | 5508.8136 |
| 2.0274 | 5453.1888 | 5474.6272 | 5474.6272 |
| 2.0384 | 5421.4056 | 5440.4407 | 5440.4407 |
| 2.0494 | 5441.1937 | 5406.2543 | 5406.2543 |
| 2.0604 | 5604.2507 | 5372.0679 | 5372.0679 |
| 2.0714 | 5373.1740 | 5337.8815 | 5337.8815 |
| 2.0824 | 5285.2016 | 5303.6950 | 5303.6950 |
| 2.0934 | 5145.0108 | 5269.5086 | 5269.5086 |
| 2.1044 | 5283.4115 | 5235.3222 | 5235.3222 |
| 2.1154 | 5138.9272 | 5201.1358 | 5201.1358 |
| 2.1264 | 5117.1352 | 5166.9494 | 5166.9494 |
| 2.1374 | 5097.7935 | 5132.7629 | 5132.7629 |
| 2.1484 | 4993.1436 | 5098.5765 | 5098.5765 |
| 2.1594 | 5043.9223 | 5064.3901 | 5064.3901 |
| 2.1704 | 4990.9558 | 5030.2037 | 5030.2037 |
| 2.1814 | 5022.8073 | 4996.0172 | 4996.0172 |
| 2.1924 | 4955.4484 | 4962.9395 | 4961.8308 |
| 2.2034 | 4903.1593 | 4931.5399 | 4931.5399 |
| 2.2144 | 4921.9405 | 4901.2490 | 4901.2490 |
| 2.2254 | 4842.6155 | 4870.9581 | 4870.9581 |
| 2.2364 | 4881.5428 | 4840.6672 | 4840.6672 |
| 2.2474 | 4789.4031 | 4810.3763 | 4810.3763 |
| 2.2584 | 4751.5575 | 4780.0854 | 4780.0854 |
| 2.2694 | 4730.3628 | 4749.7945 | 4749.7945 |
| 2.2804 | 4782.9921 | 4719.5036 | 4719.5036 |
| 2.2914 | 4658.0934 | 4689.2127 | 4689.2127 |
| 2.3024 | 4655.9159 | 4658.9218 | 4658.9218 |
| 2.3134 | 4703.2920 | 4628.6309 | 4628.6309 |
| 2.3244 | 4683.5737 | 4598.3399 | 4598.3399 |
| 2.3354 | 4572.1209 | 4568.0490 | 4568.0490 |
| 2.3464 | 4505.3825 | 4537.7581 | 4537.7581 |
| 2.3574 | 4502.4808 | 4507.4672 | 4507.4672 |
| 2.3684 | 4431.9779 | 4477.1763 | 4477.1763 |
| 2.3794 | 4423.2517 | 4448.4040 | 4446.8854 |
| 2.3904 | 4479.3397 | 4421.9306 | 4421.9306 |
| 2.4014 | 4451.5398 | 4396.9757 | 4396.9757 |
| 2.4124 | 4472.3717 | 4372.0209 | 4372.0209 |
| 2.4234 | 4454.1681 | 4347.0660 | 4347.0660 |
| 2.4344 | 4374.0900 | 4322.1112 | 4322.1112 |
| 2.4454 | 4366.4484 | 4297.1563 | 4297.1563 |
| 2.4564 | 4396.9764 | 4272.2015 | 4272.2015 |
| 2.4674 | 4297.9823 | 4247.2466 | 4247.2466 |
| 2.4784 | 4253.4523 | 4222.2918 | 4222.2918 |
| 2.4894 | 4283.1839 | 4197.3370 | 4197.3370 |
| 2.5004 | 4231.9646 | 4172.3821 | 4172.3821 |
| 2.5114 | 4149.3766 | 4147.4273 | 4147.4273 |
| 2.5224 | 4111.4223 | 4122.4724 | 4122.4724 |
| 2.5334 | 4121.0295 | 4097.5176 | 4097.5176 |
| 2.5444 | 4100.8982 | 4072.5627 | 4072.5627 |
| 2.5554 | 4024.0029 | 4047.6079 | 4047.6079 |
| 2.5664 | 4053.4454 | 4022.6530 | 4022.6530 |
| 2.5774 | 4007.3559 | 3997.6982 | 3997.6982 |
| 2.5884 | 3973.9828 | 3972.7433 | 3972.7433 |
| 2.5994 | 3983.3274 | 3947.7885 | 3947.7885 |
| 2.6104 | 3962.3677 | 3922.8336 | 3922.8336 |
| 2.6214 | 3934.1042 | 3897.8788 | 3897.8788 |
| 2.6324 | 3816.0074 | 3872.9240 | 3872.9240 |
| 2.6434 | 3835.2979 | 3847.9691 | 3847.9691 |
| 2.6544 | 3806.1617 | 3823.0143 | 3823.0143 |
| 2.6654 | 3829.9853 | 3798.0594 | 3798.0594 |
| 2.6764 | 3773.2738 | 3773.1046 | 3773.1046 |
| 2.6874 | 3767.2891 | 3748.1497 | 3748.1497 |
| 2.6984 | 3708.7301 | 3723.1949 | 3723.1949 |
| 2.7094 | 3675.0541 | 3698.2400 | 3698.2400 |
| 2.7204 | 3693.3697 | 3673.2852 | 3673.2852 |
| 2.7314 | 3699.8112 | 3648.3303 | 3648.3303 |
| 2.7424 | 3673.6480 | 3623.3755 | 3623.3755 |
| 2.7534 | 3608.6588 | 3598.3843 | 3598.4206 |
| 2.7644 | 3517.2802 | 3573.3382 | 3573.3382 |
| 2.7754 | 3525.3697 | 3548.2557 | 3548.2557 |
| 2.7864 | 3549.9440 | 3523.1733 | 3523.1733 |
| 2.7974 | 3530.8761 | 3498.0908 | 3498.0908 |
| 2.8084 | 3579.1431 | 3473.0084 | 3473.0084 |
| 2.8194 | 3411.2782 | 3447.9259 | 3447.9259 |
| 2.8304 | 3471.4336 | 3422.8434 | 3422.8434 |
| 2.8414 | 3509.7601 | 3397.7610 | 3397.7610 |
| 2.8524 | 3344.4852 | 3372.6785 | 3372.6785 |
| 2.8634 | 3355.1327 | 3347.5961 | 3347.5961 |
| 2.8744 | 3273.4656 | 3322.5136 | 3322.5136 |
| 2.8854 | 3338.8466 | 3297.4312 | 3297.4312 |
| 2.8964 | 3257.3672 | 3272.3487 | 3272.3487 |
| 2.9074 | 3154.5585 | 3247.2662 | 3247.2662 |
| 2.9184 | 3226.4312 | 3222.1838 | 3222.1838 |
| 2.9294 | 3287.9852 | 3197.1013 | 3197.1013 |
| 2.9404 | 3054.7714 | 3172.4605 | 3172.0189 |
| 2.9514 | 3177.7719 | 3148.4881 | 3148.4881 |
| 2.9624 | 3167.3451 | 3124.9572 | 3124.9572 |
| 2.9734 | 3080.2852 | 3101.4264 | 3101.4264 |
| 2.9844 | 3090.8815 | 3077.8956 | 3077.8956 |
| 2.9954 | 2953.8142 | 3054.3648 | 3054.3648 |
| 3.0064 | 3025.3933 | 3030.8340 | 3030.8340 |
| 3.0174 | 2996.4533 | 3007.3032 | 3007.3032 |
| 3.0284 | 2925.2743 | 2983.7724 | 2983.7724 |
| 3.0394 | 2898.1092 | 2960.2415 | 2960.2415 |
| 3.0504 | 2973.1642 | 2936.7107 | 2936.7107 |
| 3.0614 | 2839.5369 | 2913.1799 | 2913.1799 |
| 3.0724 | 2861.4700 | 2889.6491 | 2889.6491 |
| 3.0834 | 2795.7473 | 2866.1183 | 2866.1183 |
| 3.0944 | 2886.5796 | 2842.5875 | 2842.5875 |
| 3.1054 | 2847.0678 | 2819.0566 | 2819.0566 |
| 3.1164 | 2784.1037 | 2795.5258 | 2795.5258 |
| 3.1274 | 2792.6873 | 2771.9950 | 2771.9950 |
| 3.1384 | 2749.4125 | 2748.5412 | 2748.4642 |
| 3.1494 | 2671.1219 | 2725.0808 | 2724.9334 |
| 3.1604 | 2681.4793 | 2701.5671 | 2701.4026 |
| 3.1714 | 2671.6342 | 2678.0380 | 2677.8717 |
| 3.1824 | 2633.0437 | 2654.5089 | 2654.3409 |
| 3.1934 | 2550.6460 | 2631.0105 | 2630.8101 |
| 3.2044 | 2586.2439 | 2607.8041 | 2607.2793 |
| 3.2154 | 2534.0541 | 2584.2925 | 2583.7485 |
| 3.2264 | 2497.9882 | 2560.9272 | 2560.2177 |
| 3.2374 | 2535.3402 | 2537.4013 | 2536.6869 |
| 3.2484 | 2473.3889 | 2513.8754 | 2513.1560 |
| 3.2594 | 2501.2803 | 2490.3496 | 2489.6252 |
| 3.2704 | 2515.5378 | 2466.8238 | 2466.0944 |
| 3.2814 | 2475.4454 | 2443.2982 | 2442.5636 |
| 3.2924 | 2426.4425 | 2419.7725 | 2419.0328 |
| 3.3034 | 2385.5634 | 2396.2470 | 2395.5020 |
| 3.3144 | 2354.2596 | 2375.0004 | 2371.9711 |
| 3.3254 | 2351.8909 | 2357.2037 | 2356.4480 |
| 3.3364 | 2379.9715 | 2341.6860 | 2340.9249 |
| 3.3474 | 2341.0000 | 2326.1683 | 2325.4017 |
| 3.3584 | 2293.9144 | 2310.6507 | 2309.8786 |
| 3.3694 | 2294.0718 | 2295.1332 | 2294.3554 |
| 3.3804 | 2264.7340 | 2279.6158 | 2278.8323 |
| 3.3914 | 2251.7345 | 2264.0984 | 2263.3091 |
| 3.4024 | 2228.7330 | 2248.5811 | 2247.7860 |
| 3.4134 | 2208.6627 | 2233.0639 | 2232.2629 |
| 3.4244 | 2251.6652 | 2217.5467 | 2216.7397 |
| 3.4354 | 2233.5211 | 2202.0297 | 2201.2166 |
| 3.4464 | 2217.1013 | 2186.5127 | 2185.6934 |
| 3.4574 | 2199.2153 | 2170.9957 | 2170.1703 |
| 3.4684 | 2182.1917 | 2155.4789 | 2154.6471 |
| 3.4794 | 2116.5939 | 2139.9621 | 2139.1240 |
| 3.4904 | 2140.6770 | 2124.4454 | 2123.6008 |
| 3.5014 | 2139.4356 | 2108.9288 | 2108.0777 |
| 3.5124 | 2110.3225 | 2093.4123 | 2092.5546 |
| 3.5234 | 2078.9380 | 2077.8959 | 2077.0314 |
| 3.5344 | 2070.8338 | 2062.3796 | 2061.5083 |
| 3.5454 | 2087.8564 | 2046.8633 | 2045.9851 |
| 3.5564 | 2011.8997 | 2031.3472 | 2030.4620 |
| 3.5674 | 1981.2547 | 2015.8311 | 2014.9388 |
| 3.5784 | 2026.4572 | 2000.3152 | 1999.4157 |
| 3.5894 | 2021.7522 | 1984.7993 | 1983.8926 |
| 3.6004 | 1969.0678 | 1969.2835 | 1968.3694 |
| 3.6114 | 1973.4789 | 1953.7679 | 1952.8463 |
| 3.6224 | 1940.8879 | 1938.2523 | 1937.3231 |
| 3.6334 | 1878.7601 | 1922.7369 | 1921.8000 |
| 3.6444 | 1924.3643 | 1907.2215 | 1906.2768 |
| 3.6554 | 1979.0266 | 1891.7063 | 1890.7537 |
| 3.6664 | 1883.4302 | 1876.1912 | 1875.2305 |
| 3.6774 | 1848.6352 | 1860.6762 | 1859.7074 |
| 3.6884 | 1789.6460 | 1846.2026 | 1844.1843 |
| 3.6994 | 1856.9971 | 1833.3054 | 1832.3199 |
| 3.7104 | 1880.4818 | 1821.4495 | 1820.4556 |
| 3.7214 | 1882.9174 | 1809.5938 | 1808.5912 |
| 3.7324 | 1792.8195 | 1797.7383 | 1796.7269 |
| 3.7434 | 1816.1436 | 1785.8828 | 1784.8625 |
| 3.7544 | 1741.6578 | 1774.0275 | 1772.9982 |
| 3.7654 | 1697.4041 | 1762.1724 | 1761.1339 |
| 3.7764 | 1764.5202 | 1750.3173 | 1749.2695 |
| 3.7874 | 1769.9646 | 1738.4625 | 1737.4052 |
| 3.7984 | 1733.8864 | 1726.6077 | 1725.5408 |
| 3.8094 | 1701.3461 | 1714.7532 | 1713.6765 |
| 3.8204 | 1723.7286 | 1702.8988 | 1701.8122 |
| 3.8314 | 1748.8791 | 1691.0445 | 1689.9478 |
| 3.8424 | 1741.0024 | 1679.1904 | 1678.0835 |
| 3.8534 | 1651.0649 | 1667.3365 | 1666.2191 |
| 3.8644 | 1655.4735 | 1655.4827 | 1654.3548 |
| 3.8754 | 1688.3205 | 1644.1356 | 1642.4904 |
| 3.8864 | 1598.5752 | 1633.5552 | 1632.4055 |
| 3.8974 | 1591.4749 | 1623.4815 | 1622.3206 |
| 3.9084 | 1634.6318 | 1613.4079 | 1612.2357 |
| 3.9194 | 1628.4631 | 1603.3345 | 1602.1508 |
| 3.9304 | 1579.1500 | 1593.2613 | 1592.0659 |
| 3.9414 | 1654.9833 | 1583.1884 | 1581.9810 |
| 3.9524 | 1578.0000 | 1573.1156 | 1571.8961 |
| 3.9634 | 1576.4975 | 1563.0431 | 1561.8112 |
| 3.9744 | 1572.2011 | 1552.9708 | 1551.7263 |
| 3.9854 | 1573.1416 | 1542.8987 | 1541.6413 |
| 3.9964 | 1545.3481 | 1532.8268 | 1531.5564 |
| 4.0074 | 1528.9095 | 1522.7552 | 1521.4715 |
| 4.0184 | 1455.5162 | 1512.6839 | 1511.3866 |
| 4.0294 | 1451.8161 | 1502.6128 | 1501.3017 |
| 4.0404 | 1491.8338 | 1492.5420 | 1491.2168 |
| 4.0514 | 1487.6932 | 1482.4715 | 1481.1319 |
| 4.0624 | 1462.7434 | 1472.6357 | 1471.0470 |
| 4.0734 | 1481.1642 | 1463.1551 | 1461.7859 |
| 4.0844 | 1431.7610 | 1453.9093 | 1452.5249 |
| 4.0954 | 1368.3825 | 1444.6639 | 1443.2639 |
| 4.1064 | 1428.4489 | 1435.4187 | 1434.0029 |
| 4.1174 | 1456.7374 | 1426.1739 | 1424.7418 |
| 4.1284 | 1379.1200 | 1416.9294 | 1415.4808 |
| 4.1394 | 1385.3166 | 1407.6853 | 1406.2198 |
| 4.1504 | 1349.7935 | 1398.4415 | 1396.9588 |
| 4.1614 | 1360.8171 | 1389.1981 | 1387.6977 |
| 4.1724 | 1369.9439 | 1379.9551 | 1378.4367 |
| 4.1834 | 1371.2389 | 1370.7125 | 1369.1757 |
| 4.1944 | 1355.2448 | 1361.4703 | 1359.9146 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 27 SS2 _63 400C | 2.0054 | 29.9894 | 0.0110 | 12/19/2023 7:58:21 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.3020 | 114.72 | 0.2165 | 16.65428 | 15.09 |
| 7.0996 | 375.74 | 0.3897 | 12.44094 | 49.44 |
| 8.7619 | 267.01 | 0.0974 | 10.08411 | 35.13 |
| 15.7838 | 760.05 | 0.1082 | 5.61015 | 100.00 |
| 18.2611 | 84.84 | 0.1299 | 4.85427 | 11.16 |
| 19.7717 | 37.14 | 0.5196 | 4.48667 | 4.89 |
| 24.2703 | 33.51 | 0.2165 | 3.66429 | 4.41 |
| 25.9589 | 422.22 | 0.0758 | 3.42962 | 55.55 |
| 26.7028 | 151.54 | 0.0758 | 3.33575 | 19.94 |
| 27.5661 | 122.85 | 0.1732 | 3.23320 | 16.16 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-017-4317 | 56 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 8 |
| * | 04-006-1757 | 48 | Silicon Oxide | Si O2 | Quartz | 6 |
| * | 04-025-4215 | 6 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 49 |
| * | 01-073-6448 | 54 | Sodium Aluminum Silicate | Na Al ( Si2 O6 ) | Analcime | 21 |
| * | 01-085-1405 | 51 | Potassium Manganese Silicate Hydrate | K2.16 Mn16 ( Si26.9 O67.8 ) ( O H )8 | Ganophyllite | 4 |
| * | 01-082-8023 | 25 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 5 |
| * | 04-018-3208 | 16 | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Mg1.0 Fe0.08 Al1.0 Si3.99 O10.2 ( O H )0.8 ( H2 O )3.3 | Palygorskite-M | 4 |
| * | 04-017-9666 | 18 | Magnesium Aluminum Iron Silicon Titanium Oxide Hydroxide Hydrate | Mg3.1 Ti0.09 Fe0.14 Al0.34 Si6 O15 ( O H )2 ( H2 O )5 | Sepiolite | 4 |

Anchor Scan Parameters

Dataset Name	27 SS2 _63 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 27\27 SS2 _63 400C.xrdml

Sample Identification	27 SS2 <63

Measurement Start Date/Time	12/19/2023 7:58:21 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes