27 SS2_63 um  GLYCOL

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	9.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	23.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	34.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	4.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	25.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Sodium Aluminum Silicate Hydrate |
| --- | --- | --- | --- | --- | --- | --- |
| 27 SS2 _63um glycol | 9.0 | 4.0 | 23.0 | 34.0 | 4.0 | 25.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8133.0000 | 8108.9809 | 8133.0000 |
| 2.0164 | 8098.9966 | 8079.6782 | 8076.0554 |
| 2.0274 | 7939.0570 | 8022.8614 | 8019.1108 |
| 2.0384 | 7971.9292 | 7966.0514 | 7962.1662 |
| 2.0494 | 7741.2439 | 7909.2489 | 7905.2216 |
| 2.0604 | 7851.3068 | 7852.4542 | 7848.2770 |
| 2.0714 | 7686.3038 | 7795.6681 | 7791.3323 |
| 2.0824 | 7669.5600 | 7738.8911 | 7734.3877 |
| 2.0934 | 7727.5379 | 7682.1241 | 7677.4431 |
| 2.1044 | 7787.0133 | 7625.3677 | 7620.4985 |
| 2.1154 | 7556.8378 | 7568.6229 | 7563.5539 |
| 2.1264 | 7536.3594 | 7511.8907 | 7506.6093 |
| 2.1374 | 7641.2950 | 7455.1720 | 7449.6647 |
| 2.1484 | 7615.6770 | 7398.4681 | 7392.7201 |
| 2.1594 | 7463.7404 | 7341.7803 | 7335.7755 |
| 2.1704 | 7411.4631 | 7285.1100 | 7278.8309 |
| 2.1814 | 7348.1337 | 7228.4590 | 7221.8863 |
| 2.1924 | 7310.1495 | 7171.7684 | 7164.9417 |
| 2.2034 | 7277.8230 | 7115.0966 | 7107.8717 |
| 2.2144 | 7257.8800 | 7058.3897 | 7050.8018 |
| 2.2254 | 7299.9213 | 7001.7107 | 6993.7318 |
| 2.2364 | 7291.9720 | 6945.0626 | 6936.6619 |
| 2.2474 | 7328.5261 | 6888.4487 | 6879.5919 |
| 2.2584 | 7210.2709 | 6831.8729 | 6822.5220 |
| 2.2694 | 7122.6195 | 6775.3394 | 6765.4521 |
| 2.2804 | 7161.8274 | 6718.8532 | 6708.3821 |
| 2.2914 | 7142.1888 | 6662.4201 | 6651.3122 |
| 2.3024 | 7066.5221 | 6606.0465 | 6594.2422 |
| 2.3134 | 7042.8653 | 6549.7402 | 6537.1723 |
| 2.3244 | 6856.9602 | 6493.5099 | 6480.1024 |
| 2.3354 | 6843.4867 | 6437.3662 | 6423.0324 |
| 2.3464 | 6968.3038 | 6381.3212 | 6365.9625 |
| 2.3574 | 7071.7561 | 6325.3894 | 6308.8925 |
| 2.3684 | 6963.5029 | 6269.5880 | 6251.8226 |
| 2.3794 | 6807.0491 | 6213.9373 | 6194.7527 |
| 2.3904 | 6712.5846 | 6158.4622 | 6137.6827 |
| 2.4014 | 6800.3009 | 6103.1925 | 6080.6128 |
| 2.4124 | 6757.9902 | 6048.1646 | 6023.5428 |
| 2.4234 | 6698.0364 | 5993.4232 | 5966.4729 |
| 2.4344 | 6632.5531 | 5939.0238 | 5909.4029 |
| 2.4454 | 6541.1032 | 5885.0359 | 5852.3330 |
| 2.4564 | 6559.6686 | 5831.5472 | 5795.2631 |
| 2.4674 | 6601.6696 | 5778.6703 | 5738.1931 |
| 2.4784 | 6493.8215 | 5726.5534 | 5681.1232 |
| 2.4894 | 6407.5821 | 5675.4000 | 5624.0532 |
| 2.5004 | 6425.2699 | 5625.5090 | 5566.9833 |
| 2.5114 | 6467.1770 | 5577.3614 | 5509.9134 |
| 2.5224 | 6405.1008 | 5531.7987 | 5452.8434 |
| 2.5334 | 6354.0000 | 5490.3567 | 5395.7735 |
| 2.5444 | 6334.7276 | 5455.8005 | 5338.7035 |
| 2.5554 | 6261.7738 | 5432.8108 | 5281.6336 |
| 2.5664 | 6280.4159 | 5428.4887 | 5224.5637 |
| 2.5774 | 6209.1819 | 5452.4309 | 5167.3684 |
| 2.5884 | 6045.1204 | 5515.0482 | 5110.1731 |
| 2.5994 | 6084.5752 | 5624.5819 | 5052.9778 |
| 2.6104 | 6132.3240 | 5782.1176 | 4995.7826 |
| 2.6214 | 6110.6627 | 5975.5442 | 4938.5873 |
| 2.6324 | 6105.9041 | 6171.7978 | 4881.3920 |
| 2.6434 | 6138.6539 | 6310.8205 | 4824.1967 |
| 2.6544 | 6021.9194 | 6321.3207 | 4767.0015 |
| 2.6654 | 5914.0029 | 6172.9212 | 4709.8062 |
| 2.6764 | 5734.8018 | 5906.3617 | 4652.6109 |
| 2.6874 | 5730.7709 | 5593.3831 | 4595.4157 |
| 2.6984 | 5533.8318 | 5289.7226 | 4538.2204 |
| 2.7094 | 5485.3727 | 5024.7521 | 4481.0251 |
| 2.7204 | 5473.0216 | 4808.2070 | 4423.8298 |
| 2.7314 | 5280.7994 | 4637.6118 | 4366.6346 |
| 2.7424 | 5156.2969 | 4504.1955 | 4309.4393 |
| 2.7534 | 5080.4946 | 4397.4184 | 4252.2440 |
| 2.7644 | 4943.4838 | 4308.1320 | 4194.8938 |
| 2.7754 | 4856.4720 | 4229.5021 | 4137.5436 |
| 2.7864 | 4647.9051 | 4157.2537 | 4080.1934 |
| 2.7974 | 4525.1947 | 4088.8438 | 4022.8432 |
| 2.8084 | 4484.2881 | 4022.8657 | 3965.4930 |
| 2.8194 | 4339.1121 | 3958.5455 | 3908.1429 |
| 2.8304 | 4315.7817 | 3895.4361 | 3850.7927 |
| 2.8414 | 4058.1170 | 3833.2559 | 3793.4425 |
| 2.8524 | 3960.5015 | 3771.8112 | 3736.0923 |
| 2.8634 | 3825.6165 | 3710.9599 | 3678.7421 |
| 2.8744 | 3720.9587 | 3650.5935 | 3621.3919 |
| 2.8854 | 3691.4513 | 3590.6273 | 3564.0417 |
| 2.8964 | 3469.9823 | 3530.9941 | 3506.6915 |
| 2.9074 | 3502.5280 | 3471.6402 | 3449.3413 |
| 2.9184 | 3439.5329 | 3412.5223 | 3391.9911 |
| 2.9294 | 3270.3835 | 3353.6050 | 3334.6409 |
| 2.9404 | 3253.7896 | 3304.2591 | 3277.2907 |
| 2.9514 | 3285.2704 | 3255.7109 | 3239.3903 |
| 2.9624 | 3167.6224 | 3216.6901 | 3201.4899 |
| 2.9734 | 3073.3490 | 3177.7802 | 3163.5895 |
| 2.9844 | 2979.1927 | 3138.9671 | 3125.6891 |
| 2.9954 | 2994.7079 | 3100.2389 | 3087.7887 |
| 3.0064 | 2868.6067 | 3061.5854 | 3049.8883 |
| 3.0174 | 2884.9921 | 3022.9979 | 3011.9879 |
| 3.0284 | 2865.2861 | 2984.4689 | 2974.0875 |
| 3.0394 | 2854.2606 | 2945.9921 | 2936.1871 |
| 3.0504 | 2777.1204 | 2907.5618 | 2898.2867 |
| 3.0614 | 2736.0206 | 2869.1732 | 2860.3863 |
| 3.0724 | 2736.9961 | 2830.8220 | 2822.4859 |
| 3.0834 | 2758.7522 | 2792.5046 | 2784.5855 |
| 3.0944 | 2684.7699 | 2754.2175 | 2746.6851 |
| 3.1054 | 2678.6312 | 2715.9581 | 2708.7847 |
| 3.1164 | 2613.7596 | 2677.7236 | 2670.8843 |
| 3.1274 | 2651.1652 | 2647.0101 | 2632.9839 |
| 3.1384 | 2634.7979 | 2616.8361 | 2610.5987 |
| 3.1494 | 2579.9547 | 2594.1792 | 2588.2135 |
| 3.1604 | 2459.3127 | 2571.5397 | 2565.8283 |
| 3.1714 | 2490.2635 | 2548.9160 | 2543.4431 |
| 3.1824 | 2433.5266 | 2526.3070 | 2521.0579 |
| 3.1934 | 2501.4425 | 2503.7114 | 2498.6727 |
| 3.2044 | 2495.4056 | 2481.1281 | 2476.2875 |
| 3.2154 | 2457.9371 | 2458.5563 | 2453.9023 |
| 3.2264 | 2460.8333 | 2435.9951 | 2431.5171 |
| 3.2374 | 2400.2979 | 2413.4436 | 2409.1319 |
| 3.2484 | 2419.7778 | 2390.9012 | 2386.7467 |
| 3.2594 | 2381.2832 | 2368.3673 | 2364.3615 |
| 3.2704 | 2343.0870 | 2345.8411 | 2341.9763 |
| 3.2814 | 2342.7709 | 2323.3223 | 2319.5911 |
| 3.2924 | 2265.6416 | 2300.8103 | 2297.2059 |
| 3.3034 | 2239.2655 | 2278.3046 | 2274.8207 |
| 3.3144 | 2270.9395 | 2259.2777 | 2252.4355 |
| 3.3254 | 2254.3038 | 2240.4965 | 2237.2361 |
| 3.3364 | 2229.9233 | 2225.1933 | 2222.0367 |
| 3.3474 | 2215.0177 | 2209.8950 | 2206.8373 |
| 3.3584 | 2197.0000 | 2194.6012 | 2191.6379 |
| 3.3694 | 2212.7227 | 2179.3118 | 2176.4385 |
| 3.3804 | 2164.2433 | 2164.0264 | 2161.2391 |
| 3.3914 | 2126.4602 | 2148.7448 | 2146.0397 |
| 3.4024 | 2166.9263 | 2133.4667 | 2130.8403 |
| 3.4134 | 2188.5733 | 2118.1921 | 2115.6409 |
| 3.4244 | 2156.2094 | 2102.9206 | 2100.4415 |
| 3.4354 | 2102.5103 | 2087.6522 | 2085.2421 |
| 3.4464 | 2076.5088 | 2072.3865 | 2070.0427 |
| 3.4574 | 2008.2684 | 2057.1236 | 2054.8433 |
| 3.4684 | 1969.6347 | 2042.0458 | 2039.6440 |
| 3.4794 | 2012.7021 | 2026.9956 | 2024.4446 |
| 3.4904 | 2043.2522 | 2011.8000 | 2009.2452 |
| 3.5014 | 2003.3471 | 1996.5493 | 1994.0458 |
| 3.5124 | 1982.6839 | 1981.3008 | 1978.8464 |
| 3.5234 | 1977.4307 | 1964.7960 | 1963.6470 |
| 3.5344 | 1955.1632 | 1948.9265 | 1948.4476 |
| 3.5454 | 1944.8378 | 1933.7132 | 1933.2482 |
| 3.5564 | 1958.6608 | 1918.5169 | 1918.0488 |
| 3.5674 | 1896.1750 | 1903.4122 | 1902.8494 |
| 3.5784 | 1848.7561 | 1888.2621 | 1887.6500 |
| 3.5894 | 1827.1416 | 1873.1139 | 1872.4506 |
| 3.6004 | 1852.7237 | 1857.9428 | 1857.2512 |
| 3.6114 | 1863.3835 | 1842.7493 | 1842.0518 |
| 3.6224 | 1801.8776 | 1827.5559 | 1826.8524 |
| 3.6334 | 1792.7335 | 1812.3626 | 1811.6530 |
| 3.6444 | 1794.0000 | 1797.1694 | 1796.4536 |
| 3.6554 | 1840.4012 | 1781.9763 | 1781.2542 |
| 3.6664 | 1752.2777 | 1766.7833 | 1766.0548 |
| 3.6774 | 1757.7060 | 1751.5903 | 1750.8554 |
| 3.6884 | 1740.7478 | 1738.5429 | 1735.6560 |
| 3.6994 | 1724.6077 | 1725.6439 | 1724.8958 |
| 3.7104 | 1684.0801 | 1714.8904 | 1714.1356 |
| 3.7214 | 1647.8908 | 1704.1371 | 1703.3754 |
| 3.7324 | 1650.5782 | 1693.3838 | 1692.6151 |
| 3.7434 | 1724.4749 | 1682.6307 | 1681.8549 |
| 3.7544 | 1666.9720 | 1671.8777 | 1671.0947 |
| 3.7654 | 1620.5044 | 1661.1247 | 1660.3345 |
| 3.7764 | 1664.0275 | 1650.3719 | 1649.5742 |
| 3.7874 | 1631.3009 | 1639.6192 | 1638.8140 |
| 3.7984 | 1640.8899 | 1628.8667 | 1628.0538 |
| 3.8094 | 1608.7168 | 1618.1142 | 1617.2936 |
| 3.8204 | 1591.5044 | 1607.3619 | 1606.5334 |
| 3.8314 | 1608.7581 | 1596.6098 | 1595.7731 |
| 3.8424 | 1601.1062 | 1585.8577 | 1585.0129 |
| 3.8534 | 1567.5192 | 1575.1058 | 1574.2527 |
| 3.8644 | 1572.4528 | 1564.3540 | 1563.4925 |
| 3.8754 | 1545.4897 | 1554.6569 | 1552.7322 |
| 3.8864 | 1571.4336 | 1545.0329 | 1544.1539 |
| 3.8974 | 1487.7984 | 1536.4634 | 1535.5756 |
| 3.9084 | 1500.9494 | 1527.8942 | 1526.9973 |
| 3.9194 | 1541.6519 | 1519.3251 | 1518.4189 |
| 3.9304 | 1504.6033 | 1510.7561 | 1509.8406 |
| 3.9414 | 1552.0206 | 1502.1874 | 1501.2623 |
| 3.9524 | 1542.4366 | 1493.6188 | 1492.6840 |
| 3.9634 | 1512.1730 | 1485.0504 | 1484.1056 |
| 3.9744 | 1478.4022 | 1476.4822 | 1475.5273 |
| 3.9854 | 1486.2301 | 1467.9141 | 1466.9490 |
| 3.9964 | 1443.0349 | 1459.3463 | 1458.3707 |
| 4.0074 | 1404.7817 | 1450.7787 | 1449.7923 |
| 4.0184 | 1379.1903 | 1442.2112 | 1441.2140 |
| 4.0294 | 1429.7994 | 1433.6440 | 1432.6357 |
| 4.0404 | 1393.6062 | 1425.0770 | 1424.0574 |
| 4.0514 | 1384.0148 | 1416.5102 | 1415.4790 |
| 4.0624 | 1425.1151 | 1408.5992 | 1406.9007 |
| 4.0734 | 1431.9282 | 1400.7338 | 1399.6787 |
| 4.0844 | 1359.4469 | 1393.5241 | 1392.4568 |
| 4.0954 | 1364.4061 | 1386.3146 | 1385.2348 |
| 4.1064 | 1377.1819 | 1379.1055 | 1378.0129 |
| 4.1174 | 1369.3953 | 1371.8966 | 1370.7909 |
| 4.1284 | 1361.5044 | 1364.6880 | 1363.5689 |
| 4.1394 | 1297.3107 | 1357.4796 | 1356.3470 |
| 4.1504 | 1287.7773 | 1350.2716 | 1349.1250 |
| 4.1614 | 1286.6824 | 1343.0639 | 1341.9030 |
| 4.1724 | 1305.5443 | 1335.8565 | 1334.6811 |
| 4.1834 | 1350.6726 | 1328.6494 | 1327.4591 |
| 4.1944 | 1385.1878 | 1321.4427 | 1320.2372 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 27 SS2 _63um glycol | 2.0054 | 29.9894 | 0.0110 | 12/20/2023 12:39:38 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6514 | 1394.57 | 0.0866 | 33.29446 | 100.00 |
| 5.3025 | 145.43 | 0.1732 | 16.65287 | 10.43 |
| 6.9291 | 315.98 | 0.3464 | 12.74680 | 22.66 |
| 8.7296 | 313.11 | 0.1732 | 10.12130 | 22.45 |
| 15.6996 | 576.68 | 0.0758 | 5.64005 | 41.35 |
| 18.1815 | 83.44 | 0.1082 | 4.87535 | 5.98 |
| 19.6772 | 25.49 | 0.7793 | 4.50802 | 1.83 |
| 25.8599 | 495.34 | 0.0866 | 3.44253 | 35.52 |
| 26.7077 | 147.66 | 0.1515 | 3.33515 | 10.59 |
| 27.4967 | 119.73 | 0.1299 | 3.24120 | 8.59 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-015-8228 | 23 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.84 Na0.03 Mg0.89 Ti0.12 Fe1.38 Al1.83 Si2.71 O10.25 ( O H )1.68 F0.07 | Biotite-1M | 9 |
| * | 04-016-3810 | 15 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg0.95 Al0.84 Si3.64 O9 ( O H ) ( H2 O )4 | Palygorskite-M | 4 |
| * | 01-080-5781 | 4 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ( H2 O )3.92 ) ( H2 O )7.72 | Sepiolite | 23 |
| * | 04-025-4215 | 25 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 34 |
| * | 01-082-8023 | 25 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 4 |
| * | 04-011-6756 | 25 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 25 |

Anchor Scan Parameters

Dataset Name	27 SS2 _63um glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 27\27 SS2 _63um glycol.xrdml

Sample Identification	27 SS2 <63um glycol

Measurement Start Date/Time	12/20/2023 12:39:38 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes