27 SS2_63 um 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	29.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	8.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	51.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Deuterate Hydrate

Weight fraction/ %	5.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	6.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Deuterate Hydrate | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- |
| 27 SS2 _63 550C | 29.0 | 8.0 | 51.0 | 5.0 | 0.0 | 6.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8767.0000 | 8768.4895 | 8767.0000 |
| 2.0164 | 8852.1273 | 8724.7535 | 8703.4488 |
| 2.0274 | 8787.7522 | 8661.8644 | 8639.8976 |
| 2.0384 | 9003.6106 | 8599.0063 | 8576.3464 |
| 2.0494 | 8685.0639 | 8536.1811 | 8512.7951 |
| 2.0604 | 8762.2281 | 8473.3911 | 8449.2439 |
| 2.0714 | 8459.6018 | 8410.6384 | 8385.6927 |
| 2.0824 | 8625.2763 | 8347.9255 | 8322.1415 |
| 2.0934 | 8453.8142 | 8285.2551 | 8258.5903 |
| 2.1044 | 8591.9602 | 8222.6300 | 8195.0391 |
| 2.1154 | 8452.0610 | 8160.0533 | 8131.4878 |
| 2.1264 | 8384.4105 | 8097.5285 | 8067.9366 |
| 2.1374 | 8444.3628 | 8035.0593 | 8004.3854 |
| 2.1484 | 8398.6499 | 7972.6496 | 7940.8342 |
| 2.1594 | 8349.1593 | 7910.3039 | 7877.2830 |
| 2.1704 | 8275.4292 | 7848.0270 | 7813.7318 |
| 2.1814 | 8194.3560 | 7785.8242 | 7750.1805 |
| 2.1924 | 8228.1352 | 7723.6379 | 7686.6293 |
| 2.2034 | 8142.1858 | 7661.4549 | 7622.8685 |
| 2.2144 | 8151.8505 | 7599.3019 | 7559.1076 |
| 2.2254 | 8095.6372 | 7537.2502 | 7495.3467 |
| 2.2364 | 8069.5398 | 7475.3087 | 7431.5859 |
| 2.2474 | 7977.9125 | 7413.4874 | 7367.8250 |
| 2.2584 | 7974.5300 | 7351.7979 | 7304.0642 |
| 2.2694 | 7696.9941 | 7290.2533 | 7240.3033 |
| 2.2804 | 7744.9164 | 7228.8691 | 7176.5424 |
| 2.2914 | 7818.6352 | 7167.6637 | 7112.7816 |
| 2.3024 | 7884.9646 | 7106.6592 | 7049.0207 |
| 2.3134 | 7749.6559 | 7045.8820 | 6985.2598 |
| 2.3244 | 7766.1091 | 6985.3652 | 6921.4990 |
| 2.3354 | 7721.7787 | 6925.1490 | 6857.7381 |
| 2.3464 | 7586.5226 | 6865.2842 | 6793.9773 |
| 2.3574 | 7578.7532 | 6805.8337 | 6730.2164 |
| 2.3684 | 7492.5501 | 6746.8763 | 6666.4555 |
| 2.3794 | 7395.5211 | 6688.4591 | 6602.6947 |
| 2.3904 | 7485.0074 | 6630.6878 | 6538.7642 |
| 2.4014 | 7507.0265 | 6573.7285 | 6474.8337 |
| 2.4124 | 7400.2394 | 6517.8150 | 6410.9033 |
| 2.4234 | 7401.2026 | 6463.1678 | 6346.9728 |
| 2.4344 | 7363.6578 | 6410.0489 | 6283.0423 |
| 2.4454 | 7320.3117 | 6358.7649 | 6219.1119 |
| 2.4564 | 7307.5993 | 6309.6694 | 6155.1814 |
| 2.4674 | 7171.8024 | 6263.1615 | 6091.2509 |
| 2.4784 | 7148.3574 | 6219.6831 | 6027.3205 |
| 2.4894 | 7166.5506 | 6179.7117 | 5963.3900 |
| 2.5004 | 7073.3805 | 6143.7493 | 5899.4595 |
| 2.5114 | 7075.0275 | 6112.3075 | 5835.5291 |
| 2.5224 | 7090.1204 | 6085.8873 | 5771.5986 |
| 2.5334 | 7123.7463 | 6064.9556 | 5707.6681 |
| 2.5444 | 7065.9906 | 6049.9168 | 5643.7377 |
| 2.5554 | 6927.6283 | 6041.0824 | 5579.8072 |
| 2.5664 | 6913.5811 | 6038.6365 | 5515.8767 |
| 2.5774 | 6914.0216 | 6042.6012 | 5451.9463 |
| 2.5884 | 6868.5202 | 6052.7977 | 5388.0158 |
| 2.5994 | 6806.5221 | 6068.8063 | 5324.0853 |
| 2.6104 | 6759.9877 | 6089.9207 | 5260.1549 |
| 2.6214 | 6679.8584 | 6115.0967 | 5196.2244 |
| 2.6324 | 6702.9454 | 6142.8933 | 5132.2939 |
| 2.6434 | 6517.8387 | 6171.4111 | 5068.3634 |
| 2.6544 | 6519.5703 | 6198.2379 | 5004.4330 |
| 2.6654 | 6379.4336 | 6220.4296 | 4940.5025 |
| 2.6764 | 6297.0069 | 6234.5632 | 4876.5720 |
| 2.6874 | 6172.6450 | 6236.9119 | 4812.6416 |
| 2.6984 | 6175.4912 | 6223.7733 | 4748.7111 |
| 2.7094 | 5895.1612 | 6191.9341 | 4684.7806 |
| 2.7204 | 5933.4410 | 6139.1818 | 4620.8502 |
| 2.7314 | 5711.5250 | 6064.7130 | 4556.9197 |
| 2.7424 | 5592.0610 | 5969.2919 | 4492.9892 |
| 2.7534 | 5477.8692 | 5855.0462 | 4429.0588 |
| 2.7644 | 5308.7374 | 5725.1498 | 4364.9587 |
| 2.7754 | 5109.9252 | 5583.3097 | 4300.8586 |
| 2.7864 | 5074.1460 | 5433.3037 | 4236.7585 |
| 2.7974 | 4749.9911 | 5278.5633 | 4172.6585 |
| 2.8084 | 4731.3284 | 5122.0462 | 4108.5584 |
| 2.8194 | 4690.3422 | 4966.1798 | 4044.4583 |
| 2.8304 | 4451.8554 | 4812.8787 | 3980.3583 |
| 2.8414 | 4314.3009 | 4663.5975 | 3916.2582 |
| 2.8524 | 4117.6642 | 4519.3925 | 3852.1581 |
| 2.8634 | 4041.8082 | 4380.9801 | 3788.0580 |
| 2.8744 | 3880.7281 | 4248.7887 | 3723.9580 |
| 2.8854 | 3794.3874 | 4123.0041 | 3659.8579 |
| 2.8964 | 3726.2965 | 4003.6104 | 3595.7578 |
| 2.9074 | 3638.5752 | 3890.4279 | 3531.6577 |
| 2.9184 | 3580.9483 | 3783.1490 | 3467.5577 |
| 2.9294 | 3384.1947 | 3681.3715 | 3403.4576 |
| 2.9404 | 3382.5285 | 3591.6101 | 3339.3575 |
| 2.9514 | 3219.8063 | 3515.5488 | 3298.3806 |
| 2.9624 | 3171.1593 | 3450.4919 | 3257.4037 |
| 2.9734 | 3222.1848 | 3388.9572 | 3216.4267 |
| 2.9844 | 3156.0742 | 3330.4665 | 3175.4498 |
| 2.9954 | 3024.1150 | 3274.5769 | 3134.4729 |
| 3.0064 | 2887.4504 | 3220.8876 | 3093.4959 |
| 3.0174 | 2934.6696 | 3169.0440 | 3052.5190 |
| 3.0284 | 2955.6799 | 3118.7378 | 3011.5421 |
| 3.0394 | 2823.6126 | 3069.7056 | 2970.5651 |
| 3.0504 | 2865.5030 | 3021.7260 | 2929.5882 |
| 3.0614 | 2859.9026 | 2974.6149 | 2888.6113 |
| 3.0724 | 2833.5728 | 2928.2215 | 2847.6344 |
| 3.0834 | 2864.5015 | 2882.4231 | 2806.6574 |
| 3.0944 | 2793.1372 | 2837.1208 | 2765.6805 |
| 3.1054 | 2698.4238 | 2792.2352 | 2724.7036 |
| 3.1164 | 2630.7257 | 2747.7028 | 2683.7266 |
| 3.1274 | 2673.8849 | 2709.7532 | 2642.7497 |
| 3.1384 | 2608.7773 | 2680.3113 | 2622.5801 |
| 3.1494 | 2618.5300 | 2657.3784 | 2602.4105 |
| 3.1604 | 2573.4454 | 2634.6471 | 2582.2409 |
| 3.1714 | 2531.6804 | 2612.0953 | 2562.0713 |
| 3.1824 | 2497.8540 | 2589.7045 | 2541.9017 |
| 3.1934 | 2498.7610 | 2567.4591 | 2521.7321 |
| 3.2044 | 2456.1642 | 2545.3459 | 2501.5625 |
| 3.2154 | 2488.4936 | 2523.3532 | 2481.3929 |
| 3.2264 | 2455.9396 | 2501.4710 | 2461.2233 |
| 3.2374 | 2493.4208 | 2479.6904 | 2441.0537 |
| 3.2484 | 2410.5000 | 2458.0033 | 2420.8841 |
| 3.2594 | 2445.4926 | 2436.4028 | 2400.7145 |
| 3.2704 | 2349.6529 | 2414.8824 | 2380.5449 |
| 3.2814 | 2328.8928 | 2393.4362 | 2360.3753 |
| 3.2924 | 2345.3938 | 2372.0589 | 2340.2058 |
| 3.3034 | 2333.4248 | 2350.7458 | 2320.0362 |
| 3.3144 | 2314.2453 | 2330.5268 | 2299.8666 |
| 3.3254 | 2265.9469 | 2311.7219 | 2283.1243 |
| 3.3364 | 2228.5595 | 2294.0034 | 2266.3820 |
| 3.3474 | 2226.4405 | 2276.3335 | 2249.6397 |
| 3.3584 | 2233.2610 | 2258.7091 | 2232.8975 |
| 3.3694 | 2183.0482 | 2241.1272 | 2216.1552 |
| 3.3804 | 2189.3638 | 2223.5851 | 2199.4129 |
| 3.3914 | 2177.5398 | 2206.0805 | 2182.6707 |
| 3.4024 | 2090.5137 | 2188.6111 | 2165.9284 |
| 3.4134 | 2101.2173 | 2171.1747 | 2149.1861 |
| 3.4244 | 2116.2817 | 2153.7694 | 2132.4439 |
| 3.4354 | 2099.9676 | 2136.3933 | 2115.7016 |
| 3.4464 | 2065.1214 | 2119.0448 | 2098.9593 |
| 3.4574 | 2075.7227 | 2101.7224 | 2082.2170 |
| 3.4684 | 2089.7488 | 2084.4246 | 2065.4748 |
| 3.4794 | 2071.4130 | 2067.1499 | 2048.7325 |
| 3.4904 | 2023.1239 | 2049.8972 | 2031.9902 |
| 3.5014 | 2032.8928 | 2032.8540 | 2015.2480 |
| 3.5124 | 2000.1288 | 2016.0783 | 1999.1309 |
| 3.5234 | 1933.4454 | 1999.5099 | 1983.0139 |
| 3.5344 | 1884.9533 | 1982.9592 | 1966.8968 |
| 3.5454 | 1923.4523 | 1966.4252 | 1950.7798 |
| 3.5564 | 1964.2581 | 1949.9072 | 1934.6628 |
| 3.5674 | 1907.1563 | 1933.4873 | 1918.5457 |
| 3.5784 | 1881.9695 | 1917.0306 | 1902.4287 |
| 3.5894 | 1907.1770 | 1900.5991 | 1886.3116 |
| 3.6004 | 1844.6017 | 1884.1549 | 1870.1946 |
| 3.6114 | 1841.6844 | 1867.7078 | 1854.0776 |
| 3.6224 | 1855.6814 | 1851.2724 | 1837.9605 |
| 3.6334 | 1817.8653 | 1834.8484 | 1821.8435 |
| 3.6444 | 1809.8314 | 1818.4352 | 1805.7264 |
| 3.6554 | 1742.5074 | 1802.0323 | 1789.6094 |
| 3.6664 | 1790.7724 | 1785.6393 | 1773.4924 |
| 3.6774 | 1743.6961 | 1769.2556 | 1757.3753 |
| 3.6884 | 1793.1151 | 1753.9017 | 1741.2583 |
| 3.6994 | 1683.1475 | 1739.8966 | 1728.5229 |
| 3.7104 | 1678.9562 | 1726.9204 | 1715.7875 |
| 3.7214 | 1692.8437 | 1713.9522 | 1703.0522 |
| 3.7324 | 1665.1794 | 1700.9915 | 1690.3168 |
| 3.7434 | 1628.1465 | 1688.0381 | 1677.5814 |
| 3.7544 | 1645.0856 | 1675.0916 | 1664.8460 |
| 3.7654 | 1631.5015 | 1662.1518 | 1652.1107 |
| 3.7764 | 1709.3088 | 1649.2184 | 1639.3753 |
| 3.7874 | 1588.0973 | 1636.2911 | 1626.6399 |
| 3.7984 | 1552.1686 | 1623.3698 | 1613.9045 |
| 3.8094 | 1601.0944 | 1610.4542 | 1601.1692 |
| 3.8204 | 1605.7109 | 1597.5440 | 1588.4338 |
| 3.8314 | 1563.1770 | 1584.6391 | 1575.6984 |
| 3.8424 | 1610.0550 | 1571.7392 | 1562.9630 |
| 3.8534 | 1519.5723 | 1558.8443 | 1550.2277 |
| 3.8644 | 1504.3260 | 1545.9540 | 1537.4923 |
| 3.8754 | 1563.4366 | 1533.7233 | 1524.7569 |
| 3.8864 | 1515.7788 | 1522.3569 | 1514.1915 |
| 3.8974 | 1496.2173 | 1511.6498 | 1503.6261 |
| 3.9084 | 1440.0035 | 1500.9467 | 1493.0608 |
| 3.9194 | 1507.0560 | 1490.2475 | 1482.4954 |
| 3.9304 | 1419.1691 | 1479.5522 | 1471.9300 |
| 3.9414 | 1479.7148 | 1468.8605 | 1461.3646 |
| 3.9524 | 1468.3510 | 1458.1723 | 1450.7992 |
| 3.9634 | 1452.1583 | 1447.4876 | 1440.2338 |
| 3.9744 | 1377.0010 | 1436.8062 | 1429.6684 |
| 3.9854 | 1397.5310 | 1426.1280 | 1419.1030 |
| 3.9964 | 1432.7660 | 1415.4530 | 1408.5376 |
| 4.0074 | 1389.4975 | 1404.7809 | 1397.9723 |
| 4.0184 | 1373.5044 | 1394.1118 | 1387.4069 |
| 4.0294 | 1357.2301 | 1383.4455 | 1376.8415 |
| 4.0404 | 1343.7168 | 1372.7820 | 1366.2761 |
| 4.0514 | 1377.4012 | 1362.1211 | 1355.7107 |
| 4.0624 | 1328.0157 | 1351.5261 | 1345.1453 |
| 4.0734 | 1330.3215 | 1341.0014 | 1334.7742 |
| 4.0844 | 1340.9867 | 1330.5423 | 1324.4030 |
| 4.0954 | 1298.5408 | 1320.0857 | 1314.0318 |
| 4.1064 | 1250.7861 | 1309.6314 | 1303.6607 |
| 4.1174 | 1248.9174 | 1299.1793 | 1293.2895 |
| 4.1284 | 1290.5408 | 1288.7294 | 1282.9184 |
| 4.1394 | 1276.6391 | 1278.2817 | 1272.5472 |
| 4.1504 | 1182.3805 | 1267.8361 | 1262.1761 |
| 4.1614 | 1203.5890 | 1257.3926 | 1251.8049 |
| 4.1724 | 1225.2080 | 1246.9510 | 1241.4338 |
| 4.1834 | 1232.5752 | 1236.5114 | 1231.0626 |
| 4.1944 | 1246.7704 | 1226.0737 | 1220.6915 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 27 SS2 _63 550C | 2.0054 | 29.9894 | 0.0110 | 12/19/2023 1:31:27 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7184 | 1356.02 | 0.2381 | 32.47478 | 100.00 |
| 5.3018 | 121.07 | 0.1732 | 16.65489 | 8.93 |
| 8.7174 | 292.17 | 0.1515 | 10.13543 | 21.55 |
| 15.7645 | 472.21 | 0.1732 | 5.61696 | 34.82 |
| 17.8563 | 16.16 | 0.6927 | 4.96339 | 1.19 |
| 18.2824 | 59.27 | 0.1299 | 4.84867 | 4.37 |
| 19.6314 | 21.50 | 0.3464 | 4.51843 | 1.59 |
| 25.9529 | 255.07 | 0.1082 | 3.43041 | 18.81 |
| 26.7095 | 37.99 | 0.2598 | 3.33492 | 2.80 |
| 27.5100 | 133.94 | 0.2165 | 3.23968 | 9.88 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-011-6754 | 69 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 29 |
| * | 04-017-4317 | 43 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 8 |
| * | 04-025-4215 | 36 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 51 |
| * | 04-014-3289 | 7 | Magnesium Aluminum Silicon Oxide Hydroxide Deuterate Hydrate | Mg1.16 Al0.84 Si4 O10 ( O H ) ( H2 O )2 ( D2 O )2.5 | Palygorskite-M | 5 |
| * | 01-082-8023 | No Matching Lines | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | - |
| * | 04-016-3203 | 1 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 6 |

Anchor Scan Parameters

Dataset Name	27 SS2 _63 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 27\27 SS2 _63 550C.xrdml

Sample Identification	27 SS2 <63 550C

Measurement Start Date/Time	12/19/2023 1:31:27 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes