27 SS2_63 um REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Silicon Oxide

Weight fraction/ %	6.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	9.0

Phase Magnesium Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	7.0

Phase Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Sodium Calcium Aluminum Silicate

Weight fraction/ %	2.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	4.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	61.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	5.0

Phase Potassium Manganese Silicate Hydrate

Weight fraction/ %	5.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Silicon Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Aluminum Silicate Hydroxide Hydrate | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Sodium Calcium Aluminum Silicate | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Potassium Manganese Silicate Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 27 SS2 _63um | 6.0 | 9.0 | 7.0 | 2.0 | 2.0 | 4.0 | 61.0 | 5.0 | 5.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8203.0000 | 8202.4996 | 8203.0000 |
| 2.0164 | 8457.1529 | 8171.3906 | 8145.4950 |
| 2.0274 | 8149.3766 | 8114.7429 | 8087.9899 |
| 2.0384 | 8200.2389 | 8058.1379 | 8030.4849 |
| 2.0494 | 8106.8181 | 8001.5785 | 7972.9798 |
| 2.0604 | 8189.3682 | 7945.0679 | 7915.4748 |
| 2.0714 | 8028.9912 | 7888.6093 | 7857.9698 |
| 2.0824 | 8034.0393 | 7832.2065 | 7800.4647 |
| 2.0934 | 7839.7974 | 7775.8634 | 7742.9597 |
| 2.1044 | 7977.5575 | 7719.5844 | 7685.4547 |
| 2.1154 | 7761.6922 | 7663.3742 | 7627.9496 |
| 2.1264 | 7705.0659 | 7607.2379 | 7570.4446 |
| 2.1374 | 7844.9882 | 7551.1813 | 7512.9395 |
| 2.1484 | 7750.7380 | 7495.2106 | 7455.4345 |
| 2.1594 | 7707.1554 | 7439.3327 | 7397.9295 |
| 2.1704 | 7810.6917 | 7383.5552 | 7340.4244 |
| 2.1814 | 7710.8201 | 7327.8867 | 7282.9194 |
| 2.1924 | 7686.3589 | 7272.2516 | 7225.4144 |
| 2.2034 | 7603.5929 | 7216.7248 | 7167.7178 |
| 2.2144 | 7540.1381 | 7161.2546 | 7110.0213 |
| 2.2254 | 7414.2507 | 7105.9406 | 7052.3248 |
| 2.2364 | 7428.8820 | 7050.7994 | 6994.6282 |
| 2.2474 | 7549.0826 | 6995.8509 | 6936.9317 |
| 2.2584 | 7427.6578 | 6941.1190 | 6879.2352 |
| 2.2694 | 7440.1917 | 6886.6325 | 6821.5386 |
| 2.2804 | 7321.6632 | 6832.4269 | 6763.8421 |
| 2.2914 | 7310.0679 | 6778.5463 | 6706.1456 |
| 2.3024 | 7385.6416 | 6725.0455 | 6648.4490 |
| 2.3134 | 7187.8387 | 6671.9928 | 6590.7525 |
| 2.3244 | 7103.3766 | 6619.4739 | 6533.0560 |
| 2.3354 | 7204.8348 | 6567.5952 | 6475.3595 |
| 2.3464 | 7217.7473 | 6516.4891 | 6417.6629 |
| 2.3574 | 7050.0619 | 6466.3180 | 6359.9664 |
| 2.3684 | 7075.9882 | 6417.2800 | 6302.2699 |
| 2.3794 | 7103.7945 | 6369.5450 | 6244.5733 |
| 2.3904 | 6983.3471 | 6323.4481 | 6186.7219 |
| 2.4014 | 7029.3363 | 6279.2694 | 6128.8704 |
| 2.4124 | 7019.0708 | 6237.4593 | 6071.0190 |
| 2.4234 | 6988.2153 | 6198.4485 | 6013.1675 |
| 2.4344 | 6912.6504 | 6162.7131 | 5955.3161 |
| 2.4454 | 6778.0098 | 6130.7665 | 5897.4646 |
| 2.4564 | 6734.4017 | 6103.1477 | 5839.6132 |
| 2.4674 | 6744.7139 | 6080.4048 | 5781.7617 |
| 2.4784 | 6804.0531 | 6063.0730 | 5723.9103 |
| 2.4894 | 6808.2556 | 6051.6490 | 5666.0588 |
| 2.5004 | 6722.7124 | 6046.5608 | 5608.2074 |
| 2.5114 | 6631.5959 | 6048.1342 | 5550.3559 |
| 2.5224 | 6605.9322 | 6056.5567 | 5492.5045 |
| 2.5334 | 6530.1740 | 6071.8391 | 5434.6530 |
| 2.5444 | 6410.7625 | 6093.7750 | 5376.8016 |
| 2.5554 | 6469.1721 | 6121.8965 | 5318.9501 |
| 2.5664 | 6584.6549 | 6155.4262 | 5261.0987 |
| 2.5774 | 6564.8692 | 6193.2207 | 5203.2472 |
| 2.5884 | 6382.2635 | 6233.7078 | 5145.3957 |
| 2.5994 | 6339.8230 | 6274.8200 | 5087.5443 |
| 2.6104 | 6199.7861 | 6313.9372 | 5029.6928 |
| 2.6214 | 6266.1662 | 6347.8685 | 4971.8414 |
| 2.6324 | 6225.2109 | 6372.9153 | 4913.9899 |
| 2.6434 | 6222.0600 | 6385.0679 | 4856.1385 |
| 2.6544 | 6108.4690 | 6380.3687 | 4798.2870 |
| 2.6654 | 6112.8348 | 6355.4192 | 4740.4356 |
| 2.6764 | 6007.5408 | 6307.9314 | 4682.5841 |
| 2.6874 | 5924.0875 | 6237.1552 | 4624.7327 |
| 2.6984 | 5756.9071 | 6144.0281 | 4566.8812 |
| 2.7094 | 5644.3500 | 6030.9880 | 4509.0298 |
| 2.7204 | 5527.7330 | 5901.5217 | 4451.1783 |
| 2.7314 | 5506.2448 | 5759.6130 | 4393.3269 |
| 2.7424 | 5334.8884 | 5609.2488 | 4335.4754 |
| 2.7534 | 5107.4395 | 5454.0072 | 4277.6240 |
| 2.7644 | 5073.3923 | 5297.0680 | 4219.6176 |
| 2.7754 | 4922.5742 | 5140.9359 | 4161.6112 |
| 2.7864 | 4658.0172 | 4987.6899 | 4103.6049 |
| 2.7974 | 4538.0442 | 4838.8522 | 4045.5985 |
| 2.8084 | 4447.1450 | 4695.5232 | 3987.5921 |
| 2.8194 | 4405.2566 | 4558.4442 | 3929.5857 |
| 2.8304 | 4191.8230 | 4428.0522 | 3871.5794 |
| 2.8414 | 4164.6588 | 4304.5280 | 3813.5730 |
| 2.8524 | 4060.8412 | 4187.8396 | 3755.5666 |
| 2.8634 | 3822.9941 | 4077.7825 | 3697.5602 |
| 2.8744 | 3914.9543 | 3974.0182 | 3639.5539 |
| 2.8854 | 3667.2625 | 3876.1096 | 3581.5475 |
| 2.8964 | 3568.4203 | 3783.5545 | 3523.5411 |
| 2.9074 | 3413.3304 | 3695.8150 | 3465.5348 |
| 2.9184 | 3453.2665 | 3612.3434 | 3407.5284 |
| 2.9294 | 3365.4631 | 3532.6027 | 3349.5220 |
| 2.9404 | 3260.7606 | 3464.8688 | 3291.5156 |
| 2.9514 | 3269.1868 | 3402.0647 | 3253.2604 |
| 2.9624 | 3138.0590 | 3350.3707 | 3215.0052 |
| 2.9734 | 3104.7365 | 3300.6250 | 3176.7501 |
| 2.9844 | 3025.1598 | 3252.5014 | 3138.4949 |
| 2.9954 | 3034.2124 | 3205.7215 | 3100.2397 |
| 3.0064 | 2927.2984 | 3160.0514 | 3061.9845 |
| 3.0174 | 2859.7994 | 3115.2969 | 3023.7293 |
| 3.0284 | 2807.3083 | 3071.2993 | 2985.4741 |
| 3.0394 | 2884.2409 | 3027.9292 | 2947.2189 |
| 3.0504 | 2833.5064 | 2985.0825 | 2908.9637 |
| 3.0614 | 2949.5899 | 2942.6760 | 2870.7085 |
| 3.0724 | 2800.8117 | 2900.6426 | 2832.4533 |
| 3.0834 | 2735.0934 | 2858.9289 | 2794.1981 |
| 3.0944 | 2662.4779 | 2817.4919 | 2755.9429 |
| 3.1054 | 2711.2320 | 2776.2970 | 2717.6877 |
| 3.1164 | 2678.3796 | 2735.3158 | 2679.4325 |
| 3.1274 | 2652.4690 | 2702.4452 | 2641.1773 |
| 3.1384 | 2575.8535 | 2671.7107 | 2620.7277 |
| 3.1494 | 2624.5467 | 2649.0509 | 2600.2781 |
| 3.1604 | 2536.1018 | 2626.5314 | 2579.8285 |
| 3.1714 | 2549.7886 | 2604.1401 | 2559.3789 |
| 3.1824 | 2525.8854 | 2582.1282 | 2538.9293 |
| 3.1934 | 2493.7522 | 2560.0298 | 2518.4797 |
| 3.2044 | 2505.3535 | 2538.0967 | 2498.0301 |
| 3.2154 | 2451.1750 | 2516.1581 | 2477.5805 |
| 3.2264 | 2393.1490 | 2494.2719 | 2457.1309 |
| 3.2374 | 2415.1003 | 2472.4647 | 2436.6813 |
| 3.2484 | 2445.8333 | 2450.7310 | 2416.2317 |
| 3.2594 | 2367.2330 | 2429.0655 | 2395.7821 |
| 3.2704 | 2369.1150 | 2407.4636 | 2375.3325 |
| 3.2814 | 2326.7119 | 2385.9209 | 2354.8829 |
| 3.2924 | 2285.2965 | 2364.4337 | 2334.4332 |
| 3.3034 | 2293.3186 | 2342.9982 | 2313.9836 |
| 3.3144 | 2302.6440 | 2322.7145 | 2293.5340 |
| 3.3254 | 2291.8230 | 2302.7500 | 2275.5652 |
| 3.3364 | 2278.2286 | 2283.9315 | 2257.5963 |
| 3.3474 | 2248.5005 | 2265.1528 | 2239.6274 |
| 3.3584 | 2211.1504 | 2246.4116 | 2221.6586 |
| 3.3694 | 2168.6627 | 2227.7057 | 2203.6897 |
| 3.3804 | 2175.4095 | 2209.0329 | 2185.7208 |
| 3.3914 | 2180.4159 | 2190.3913 | 2167.7519 |
| 3.4024 | 2126.1961 | 2171.7791 | 2149.7831 |
| 3.4134 | 2088.5733 | 2153.1947 | 2131.8142 |
| 3.4244 | 2067.3348 | 2134.6365 | 2113.8453 |
| 3.4354 | 2043.0324 | 2116.1031 | 2095.8765 |
| 3.4464 | 2047.3722 | 2097.5931 | 2077.9076 |
| 3.4574 | 2062.7139 | 2079.1053 | 2059.9387 |
| 3.4684 | 2043.2463 | 2060.6384 | 2041.9698 |
| 3.4794 | 2005.7080 | 2042.1915 | 2024.0010 |
| 3.4904 | 1987.7257 | 2023.7634 | 2006.0321 |
| 3.5014 | 1989.0295 | 2006.5752 | 1988.0632 |
| 3.5124 | 1989.6323 | 1989.7073 | 1972.8416 |
| 3.5234 | 1960.4572 | 1974.0775 | 1957.6200 |
| 3.5344 | 1940.2070 | 1958.4630 | 1942.3983 |
| 3.5454 | 1909.6116 | 1942.8632 | 1927.1767 |
| 3.5564 | 1915.8599 | 1927.2773 | 1911.9551 |
| 3.5674 | 1882.4975 | 1911.7653 | 1896.7334 |
| 3.5784 | 1823.5428 | 1896.2466 | 1881.5118 |
| 3.5894 | 1823.6283 | 1880.7306 | 1866.2902 |
| 3.6004 | 1792.0187 | 1865.2163 | 1851.0685 |
| 3.6114 | 1816.1632 | 1849.6929 | 1835.8469 |
| 3.6224 | 1749.1622 | 1834.1799 | 1820.6253 |
| 3.6334 | 1813.7267 | 1818.6770 | 1805.4036 |
| 3.6444 | 1793.7571 | 1803.1837 | 1790.1820 |
| 3.6554 | 1803.7168 | 1787.6996 | 1774.9604 |
| 3.6664 | 1763.3466 | 1772.2244 | 1759.7387 |
| 3.6774 | 1782.9154 | 1756.7575 | 1744.5171 |
| 3.6884 | 1720.9602 | 1742.6716 | 1729.2955 |
| 3.6994 | 1696.8220 | 1728.9340 | 1717.1600 |
| 3.7104 | 1680.5182 | 1716.5767 | 1705.0246 |
| 3.7214 | 1711.1092 | 1704.2265 | 1692.8891 |
| 3.7324 | 1712.1406 | 1691.8832 | 1680.7537 |
| 3.7434 | 1714.8260 | 1679.5465 | 1668.6183 |
| 3.7544 | 1645.3377 | 1667.2160 | 1656.4828 |
| 3.7654 | 1711.5929 | 1654.8917 | 1644.3474 |
| 3.7764 | 1609.2620 | 1642.5733 | 1632.2120 |
| 3.7874 | 1603.0354 | 1630.2605 | 1620.0765 |
| 3.7984 | 1694.5319 | 1617.9531 | 1607.9411 |
| 3.8094 | 1559.4563 | 1605.6509 | 1595.8056 |
| 3.8204 | 1587.4675 | 1593.3538 | 1583.6702 |
| 3.8314 | 1568.1131 | 1581.0616 | 1571.5348 |
| 3.8424 | 1546.8422 | 1568.7740 | 1559.3993 |
| 3.8534 | 1545.3628 | 1556.4909 | 1547.2639 |
| 3.8644 | 1562.6072 | 1544.2123 | 1535.1284 |
| 3.8754 | 1535.7896 | 1531.9378 | 1522.9930 |
| 3.8864 | 1543.7212 | 1519.6674 | 1510.8576 |
| 3.8974 | 1458.5890 | 1507.4010 | 1498.7221 |
| 3.9084 | 1495.1770 | 1495.1383 | 1486.5867 |
| 3.9194 | 1451.7434 | 1482.8794 | 1474.4512 |
| 3.9304 | 1476.6603 | 1470.6240 | 1462.3158 |
| 3.9414 | 1486.6529 | 1458.3720 | 1450.1804 |
| 3.9524 | 1473.3259 | 1446.1234 | 1438.0449 |
| 3.9634 | 1398.5683 | 1433.8781 | 1425.9095 |
| 3.9744 | 1410.1981 | 1421.6358 | 1413.7740 |
| 3.9854 | 1405.8319 | 1409.3967 | 1401.6386 |
| 3.9964 | 1432.5192 | 1397.1605 | 1389.5032 |
| 4.0074 | 1391.6873 | 1384.9271 | 1377.3677 |
| 4.0184 | 1377.8451 | 1372.6966 | 1365.2323 |
| 4.0294 | 1295.6470 | 1360.4687 | 1353.0969 |
| 4.0404 | 1332.6185 | 1348.2435 | 1340.9614 |
| 4.0514 | 1322.4307 | 1336.0209 | 1328.8260 |
| 4.0624 | 1312.5708 | 1325.2571 | 1316.6905 |
| 4.0734 | 1311.1397 | 1314.8573 | 1307.8294 |
| 4.0844 | 1342.1460 | 1305.9162 | 1298.9682 |
| 4.0954 | 1271.6942 | 1296.9774 | 1290.1070 |
| 4.1064 | 1300.4651 | 1288.0409 | 1281.2459 |
| 4.1174 | 1325.8436 | 1279.1065 | 1272.3847 |
| 4.1284 | 1263.9444 | 1270.1743 | 1263.5236 |
| 4.1394 | 1202.6116 | 1261.2442 | 1254.6624 |
| 4.1504 | 1218.3968 | 1252.3162 | 1245.8012 |
| 4.1614 | 1232.9076 | 1243.3901 | 1236.9401 |
| 4.1724 | 1226.0344 | 1234.4660 | 1228.0789 |
| 4.1834 | 1223.6903 | 1225.5439 | 1219.2177 |
| 4.1944 | 1240.0152 | 1216.6236 | 1210.3566 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 27 SS2 _63um | 2.0054 | 29.9894 | 0.0110 | 12/13/2023 11:58:22 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6736 | 1450.97 | 0.2381 | 33.01810 | 100.00 |
| 5.3033 | 107.64 | 0.1732 | 16.65041 | 7.42 |
| 7.0808 | 348.81 | 0.3897 | 12.47394 | 24.04 |
| 8.7099 | 223.68 | 0.1515 | 10.14422 | 15.42 |
| 15.7205 | 604.78 | 0.0974 | 5.63259 | 41.68 |
| 17.5998 | 27.24 | 0.1299 | 5.03515 | 1.88 |
| 18.1881 | 76.71 | 0.1299 | 4.87359 | 5.29 |
| 19.5634 | 35.18 | 0.6061 | 4.53398 | 2.42 |
| 21.0551 | 16.70 | 0.5196 | 4.21600 | 1.15 |
| 22.3631 | 23.63 | 0.2598 | 3.97228 | 1.63 |
| 23.3488 | 40.71 | 0.1299 | 3.80677 | 2.81 |
| 25.9074 | 559.51 | 0.0974 | 3.43632 | 38.56 |
| 26.6719 | 150.12 | 0.1082 | 3.33954 | 10.35 |
| 27.4993 | 174.75 | 0.1299 | 3.24091 | 12.04 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-012-0490 | 39 | Silicon Oxide | Si O2 | Quartz | 6 |
| * | 04-017-4317 | 35 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 9 |
| * | 01-082-1872 | 21 | Magnesium Aluminum Silicate Hydroxide Hydrate | ( Mg0.669 Al0.331 )4 ( Si4 O10 )2 ( O H )2 ( H2 O )8 | Palygorskite-M | 7 |
| * | 04-017-9668 | 10 | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Mg3.84 Ti0.005 Fe0.03 Al0.07 Si6 O15 ( O H )2 ( H2 O )5 | Sepiolite | 2 |
| * | 01-078-0432 | 31 | Sodium Calcium Aluminum Silicate | ( Na0.45 Ca0.55 ) ( Al1.55 Si2.45 O8 ) | Anorthite, Na-bearing, syn | 2 |
| * | 01-075-8690 | 18 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 4 |
| * | 04-025-4215 | 40 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 61 |
| * | 01-082-8023 | 25 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 5 |
| * | 01-085-1405 | 50 | Potassium Manganese Silicate Hydrate | K2.16 Mn16 ( Si26.9 O67.8 ) ( O H )8 | Ganophyllite | 5 |

Anchor Scan Parameters

Dataset Name	27 SS2 _63um

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 27\27 SS2 _63um.xrdml

Sample Identification	27 SS2 <63um

Measurement Start Date/Time	12/13/2023 11:58:22 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes