28 SS2 Ground 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	15.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	17.0

Phase Silicon Oxide

Weight fraction/ %	2.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	11.0

Phase Potassium Magnesium Iron Silicon Oxide Hydroxide

Weight fraction/ %	29.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	8.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	18.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Sodium Aluminum Silicate Hydrate | Silicon Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Magnesium Iron Silicon Oxide Hydroxide | Potassium Aluminum Silicate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 28 SS2 ground 550C | 15.0 | 17.0 | 2.0 | 11.0 | 29.0 | 8.0 | 18.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6955.0000 | 6957.7518 | 6955.0000 |
| 2.0164 | 6682.8569 | 6927.0449 | 6904.5246 |
| 2.0274 | 6592.7207 | 6877.3468 | 6854.0492 |
| 2.0384 | 6656.7596 | 6827.6923 | 6803.5738 |
| 2.0494 | 6548.0649 | 6778.0859 | 6753.0984 |
| 2.0604 | 6584.1898 | 6728.5322 | 6702.6230 |
| 2.0714 | 6526.5900 | 6679.0370 | 6652.1476 |
| 2.0824 | 6513.4371 | 6629.6069 | 6601.6722 |
| 2.0934 | 6304.2429 | 6580.2495 | 6551.1968 |
| 2.1044 | 6385.5708 | 6530.9737 | 6500.7214 |
| 2.1154 | 6368.9390 | 6481.7900 | 6450.2460 |
| 2.1264 | 6431.1814 | 6432.7105 | 6399.7706 |
| 2.1374 | 6312.5959 | 6383.7493 | 6349.2952 |
| 2.1484 | 6235.6480 | 6334.9227 | 6298.8198 |
| 2.1594 | 6350.7080 | 6286.2495 | 6248.3444 |
| 2.1704 | 6270.9705 | 6237.7514 | 6197.8690 |
| 2.1814 | 6104.0039 | 6189.4531 | 6147.3936 |
| 2.1924 | 6038.0752 | 6144.2602 | 6096.9182 |
| 2.2034 | 6018.6903 | 6101.2036 | 6054.0742 |
| 2.2144 | 6161.2876 | 6061.3199 | 6011.2302 |
| 2.2254 | 6101.6922 | 6021.7714 | 5968.3862 |
| 2.2364 | 6012.7965 | 5982.6019 | 5925.5422 |
| 2.2474 | 5882.4179 | 5943.8598 | 5882.6982 |
| 2.2584 | 5906.0516 | 5905.5972 | 5839.8542 |
| 2.2694 | 5856.0118 | 5867.8703 | 5797.0102 |
| 2.2804 | 5952.7684 | 5830.7390 | 5754.1662 |
| 2.2914 | 5828.2370 | 5794.2659 | 5711.3222 |
| 2.3024 | 5780.8982 | 5758.5164 | 5668.4782 |
| 2.3134 | 5704.5644 | 5723.5570 | 5625.6342 |
| 2.3244 | 5751.1583 | 5689.4549 | 5582.7902 |
| 2.3354 | 5722.6195 | 5656.2763 | 5539.9461 |
| 2.3464 | 5685.4263 | 5624.0851 | 5497.1021 |
| 2.3574 | 5609.1495 | 5592.9415 | 5454.2581 |
| 2.3684 | 5573.7006 | 5562.8998 | 5411.4141 |
| 2.3794 | 5579.8830 | 5533.9640 | 5368.5701 |
| 2.3904 | 5539.6337 | 5506.1862 | 5325.6123 |
| 2.4014 | 5499.6106 | 5479.5771 | 5282.6544 |
| 2.4124 | 5438.9489 | 5454.1913 | 5239.6966 |
| 2.4234 | 5429.5103 | 5430.0242 | 5196.7387 |
| 2.4344 | 5388.0516 | 5407.0528 | 5153.7809 |
| 2.4454 | 5426.8191 | 5385.2329 | 5110.8230 |
| 2.4564 | 5363.8977 | 5364.4967 | 5067.8652 |
| 2.4674 | 5333.9646 | 5344.7496 | 5024.9073 |
| 2.4784 | 5286.2891 | 5325.8671 | 4981.9495 |
| 2.4894 | 5216.8987 | 5307.6914 | 4938.9917 |
| 2.5004 | 5195.8274 | 5290.0275 | 4896.0338 |
| 2.5114 | 5113.7109 | 5272.6392 | 4853.0760 |
| 2.5224 | 5153.4922 | 5255.2454 | 4810.1181 |
| 2.5334 | 5122.9056 | 5237.5177 | 4767.1603 |
| 2.5444 | 5116.6691 | 5219.0787 | 4724.2024 |
| 2.5554 | 5148.0216 | 5199.5050 | 4681.2446 |
| 2.5664 | 5058.3908 | 5178.3335 | 4638.2867 |
| 2.5774 | 4994.3825 | 5155.0745 | 4595.3289 |
| 2.5884 | 4998.0285 | 5129.2316 | 4552.3710 |
| 2.5994 | 4982.4336 | 5100.3276 | 4509.4132 |
| 2.6104 | 4895.2871 | 5067.9366 | 4466.4553 |
| 2.6214 | 4874.8309 | 5031.7169 | 4423.4975 |
| 2.6324 | 4774.8097 | 4991.4403 | 4380.5396 |
| 2.6434 | 4802.4268 | 4947.0138 | 4337.5818 |
| 2.6544 | 4690.5914 | 4898.4888 | 4294.6239 |
| 2.6654 | 4716.6460 | 4846.0557 | 4251.6661 |
| 2.6764 | 4648.2817 | 4790.0262 | 4208.7083 |
| 2.6874 | 4593.9007 | 4730.8047 | 4165.7504 |
| 2.6984 | 4576.1593 | 4668.8566 | 4122.7926 |
| 2.7094 | 4453.4326 | 4604.7472 | 4079.8347 |
| 2.7204 | 4389.0433 | 4538.8883 | 4036.8769 |
| 2.7314 | 4298.2566 | 4471.7147 | 3993.9190 |
| 2.7424 | 4264.1770 | 4403.6977 | 3950.9612 |
| 2.7534 | 4210.8525 | 4335.1979 | 3908.0033 |
| 2.7644 | 4117.8879 | 4266.5729 | 3864.9316 |
| 2.7754 | 4179.5733 | 4198.1027 | 3821.8599 |
| 2.7864 | 4079.4262 | 4130.0790 | 3778.7883 |
| 2.7974 | 4054.1504 | 4062.7087 | 3735.7166 |
| 2.8084 | 3889.7011 | 3996.1600 | 3692.6449 |
| 2.8194 | 3859.1760 | 3930.5671 | 3649.5732 |
| 2.8304 | 3821.1268 | 3866.0327 | 3606.5015 |
| 2.8414 | 3690.0255 | 3802.6324 | 3563.4298 |
| 2.8524 | 3635.5723 | 3740.4170 | 3520.3581 |
| 2.8634 | 3665.5959 | 3679.4155 | 3477.2864 |
| 2.8744 | 3516.4960 | 3619.6376 | 3434.2147 |
| 2.8854 | 3451.0364 | 3561.0763 | 3391.1431 |
| 2.8964 | 3368.3628 | 3503.7098 | 3348.0714 |
| 2.9074 | 3311.5909 | 3447.5041 | 3304.9997 |
| 2.9184 | 3259.8387 | 3392.4150 | 3261.9280 |
| 2.9294 | 3247.9764 | 3338.3900 | 3218.8563 |
| 2.9404 | 3129.0738 | 3290.6212 | 3175.7846 |
| 2.9514 | 3150.1750 | 3247.2197 | 3146.6389 |
| 2.9624 | 3116.8805 | 3209.9456 | 3117.4931 |
| 2.9734 | 3059.4936 | 3173.4815 | 3088.3474 |
| 2.9844 | 2899.4612 | 3137.7604 | 3059.2016 |
| 2.9954 | 3032.3097 | 3102.7165 | 3030.0558 |
| 3.0064 | 2966.2842 | 3068.2863 | 3000.9101 |
| 3.0174 | 2901.5851 | 3034.4092 | 2971.7643 |
| 3.0284 | 2935.8333 | 3001.0277 | 2942.6186 |
| 3.0394 | 2833.0964 | 2968.0885 | 2913.4728 |
| 3.0504 | 2791.7792 | 2935.5421 | 2884.3271 |
| 3.0614 | 2753.3776 | 2903.3435 | 2855.1813 |
| 3.0724 | 2772.9670 | 2871.4516 | 2826.0356 |
| 3.0834 | 2732.4071 | 2839.8296 | 2796.8898 |
| 3.0944 | 2777.9823 | 2808.4445 | 2767.7441 |
| 3.1054 | 2675.2940 | 2777.2673 | 2738.5983 |
| 3.1164 | 2669.8982 | 2746.2721 | 2709.4525 |
| 3.1274 | 2735.3599 | 2717.3186 | 2680.3068 |
| 3.1384 | 2669.2310 | 2689.7328 | 2656.1532 |
| 3.1494 | 2583.3658 | 2664.1520 | 2631.9996 |
| 3.1604 | 2592.0649 | 2638.6795 | 2607.8460 |
| 3.1714 | 2553.3304 | 2613.3024 | 2583.6924 |
| 3.1824 | 2625.6440 | 2588.0099 | 2559.5388 |
| 3.1934 | 2507.5487 | 2562.7927 | 2535.3852 |
| 3.2044 | 2501.6357 | 2537.6427 | 2511.2315 |
| 3.2154 | 2456.9597 | 2512.5530 | 2487.0779 |
| 3.2264 | 2437.0782 | 2487.5178 | 2462.9243 |
| 3.2374 | 2441.5703 | 2462.5320 | 2438.7707 |
| 3.2484 | 2437.8889 | 2437.5911 | 2414.6171 |
| 3.2594 | 2405.8496 | 2412.6913 | 2390.4635 |
| 3.2704 | 2403.7109 | 2387.8294 | 2366.3099 |
| 3.2814 | 2378.1986 | 2363.0024 | 2342.1563 |
| 3.2924 | 2349.5663 | 2338.2077 | 2318.0027 |
| 3.3034 | 2298.1062 | 2313.4431 | 2293.8491 |
| 3.3144 | 2278.8540 | 2291.5140 | 2269.6955 |
| 3.3254 | 2221.7286 | 2271.4421 | 2252.9876 |
| 3.3364 | 2216.4631 | 2254.2021 | 2236.2797 |
| 3.3474 | 2209.0285 | 2236.9853 | 2219.5717 |
| 3.3584 | 2184.0944 | 2219.7902 | 2202.8638 |
| 3.3694 | 2182.2350 | 2202.6157 | 2186.1559 |
| 3.3804 | 2171.0998 | 2185.4605 | 2169.4480 |
| 3.3914 | 2148.4425 | 2168.3236 | 2152.7401 |
| 3.4024 | 2139.6096 | 2151.2041 | 2136.0322 |
| 3.4134 | 2116.4838 | 2134.1011 | 2119.3243 |
| 3.4244 | 2086.0457 | 2117.0136 | 2102.6163 |
| 3.4354 | 2055.0865 | 2099.9409 | 2085.9084 |
| 3.4464 | 2024.3569 | 2082.8823 | 2069.2005 |
| 3.4574 | 2019.9794 | 2065.8370 | 2052.4926 |
| 3.4684 | 2002.0546 | 2048.8045 | 2035.7847 |
| 3.4794 | 2010.0570 | 2031.7840 | 2019.0768 |
| 3.4904 | 1949.7964 | 2014.7751 | 2002.3688 |
| 3.5014 | 1960.6824 | 1999.0563 | 1985.6609 |
| 3.5124 | 2036.6583 | 1984.1822 | 1972.3455 |
| 3.5234 | 1985.8141 | 1970.5972 | 1959.0301 |
| 3.5344 | 1988.4228 | 1957.0218 | 1945.7147 |
| 3.5454 | 1937.4120 | 1943.4555 | 1932.3993 |
| 3.5564 | 1947.1859 | 1929.8980 | 1919.0839 |
| 3.5674 | 1910.8082 | 1916.3487 | 1905.7685 |
| 3.5784 | 1951.5792 | 1902.8075 | 1892.4530 |
| 3.5894 | 1911.4867 | 1889.2739 | 1879.1376 |
| 3.6004 | 1850.1966 | 1875.7476 | 1865.8222 |
| 3.6114 | 1815.7542 | 1862.2283 | 1852.5068 |
| 3.6224 | 1788.2168 | 1848.7157 | 1839.1914 |
| 3.6334 | 1829.6873 | 1835.2096 | 1825.8760 |
| 3.6444 | 1762.6829 | 1821.7096 | 1812.5606 |
| 3.6554 | 1746.1563 | 1808.2157 | 1799.2452 |
| 3.6664 | 1758.8392 | 1794.7274 | 1785.9297 |
| 3.6774 | 1809.6215 | 1781.2446 | 1772.6143 |
| 3.6884 | 1852.2213 | 1767.7670 | 1759.2989 |
| 3.6994 | 1786.4670 | 1754.2946 | 1745.9835 |
| 3.7104 | 1730.9341 | 1740.8270 | 1732.6681 |
| 3.7214 | 1764.5310 | 1727.3641 | 1719.3527 |
| 3.7324 | 1675.9601 | 1713.9058 | 1706.0373 |
| 3.7434 | 1738.7070 | 1700.4518 | 1692.7219 |
| 3.7544 | 1666.6578 | 1687.0020 | 1679.4065 |
| 3.7654 | 1573.1091 | 1673.5563 | 1666.0910 |
| 3.7764 | 1726.6175 | 1660.1145 | 1652.7756 |
| 3.7874 | 1662.6017 | 1646.6764 | 1639.4602 |
| 3.7984 | 1592.1549 | 1633.2421 | 1626.1448 |
| 3.8094 | 1636.6224 | 1619.8112 | 1612.8294 |
| 3.8204 | 1612.7198 | 1606.3838 | 1599.5140 |
| 3.8314 | 1601.1455 | 1592.9596 | 1586.1986 |
| 3.8424 | 1559.1568 | 1579.5387 | 1572.8832 |
| 3.8534 | 1595.3392 | 1566.1208 | 1559.5677 |
| 3.8644 | 1553.2178 | 1552.7060 | 1546.2523 |
| 3.8754 | 1512.7424 | 1540.0784 | 1532.9369 |
| 3.8864 | 1551.4336 | 1527.9651 | 1521.7017 |
| 3.8974 | 1464.1485 | 1516.6389 | 1510.4665 |
| 3.9084 | 1450.2129 | 1505.3154 | 1499.2313 |
| 3.9194 | 1502.7021 | 1493.9944 | 1487.9961 |
| 3.9304 | 1482.0374 | 1482.6760 | 1476.7609 |
| 3.9414 | 1510.9400 | 1471.3599 | 1465.5257 |
| 3.9524 | 1478.1549 | 1460.0463 | 1454.2905 |
| 3.9634 | 1448.6293 | 1448.7349 | 1443.0553 |
| 3.9744 | 1460.2001 | 1437.4258 | 1431.8201 |
| 3.9854 | 1451.2301 | 1426.1189 | 1420.5849 |
| 3.9964 | 1422.8638 | 1414.8141 | 1409.3497 |
| 4.0074 | 1436.7296 | 1403.5114 | 1398.1145 |
| 4.0184 | 1382.2846 | 1392.2107 | 1386.8793 |
| 4.0294 | 1368.1859 | 1380.9120 | 1375.6441 |
| 4.0404 | 1424.9877 | 1369.6152 | 1364.4089 |
| 4.0514 | 1386.3834 | 1358.3204 | 1353.1737 |
| 4.0624 | 1329.9946 | 1347.0273 | 1341.9385 |
| 4.0734 | 1363.6391 | 1335.7362 | 1330.7033 |
| 4.0844 | 1330.7699 | 1324.4468 | 1319.4681 |
| 4.0954 | 1328.0236 | 1313.1591 | 1308.2329 |
| 4.1064 | 1336.6952 | 1301.8732 | 1296.9977 |
| 4.1174 | 1304.5309 | 1290.5890 | 1285.7625 |
| 4.1284 | 1243.1391 | 1279.3064 | 1274.5273 |
| 4.1394 | 1254.6096 | 1268.0255 | 1263.2921 |
| 4.1504 | 1279.1903 | 1256.7462 | 1252.0569 |
| 4.1614 | 1266.6834 | 1245.4685 | 1240.8217 |
| 4.1724 | 1238.8373 | 1234.1923 | 1229.5865 |
| 4.1834 | 1246.7788 | 1222.9178 | 1218.3513 |
| 4.1944 | 1224.9621 | 1211.6447 | 1207.1161 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 28 SS2 ground 550C | 2.0054 | 29.9894 | 0.0110 | 12/19/2023 1:41:54 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6319 | 545.39 | 0.3464 | 33.54173 | 100.00 |
| 5.3017 | 102.12 | 0.2598 | 16.65534 | 18.73 |
| 8.7007 | 388.72 | 0.0758 | 10.15492 | 71.28 |
| 13.5674 | 65.71 | 0.1299 | 6.52127 | 12.05 |
| 15.7544 | 316.04 | 0.1732 | 5.62056 | 57.95 |
| 17.6479 | 28.08 | 0.2165 | 5.02154 | 5.15 |
| 18.2639 | 31.30 | 0.2598 | 4.85354 | 5.74 |
| 19.6002 | 24.02 | 0.5196 | 4.52555 | 4.40 |
| 26.0229 | 163.97 | 0.1515 | 3.42134 | 30.07 |
| 26.7158 | 108.26 | 0.2165 | 3.33415 | 19.85 |
| 27.5009 | 534.01 | 0.1948 | 3.24072 | 97.91 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-016-2838 | 58 | Titanium Oxide | Ti O2 | Rutile | 15 |
| * | 01-083-1731 | 54 | Sodium Aluminum Silicate Hydrate | Na14.80 Al14.24 Si33.76 O96 ( H2 O )16 | Analcime | 17 |
| * | 04-006-1757 | 33 | Silicon Oxide | Si O2 | Quartz | 2 |
| * | 04-017-4317 | 28 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 11 |
| * | 01-083-3042 | 15 | Potassium Magnesium Iron Silicon Oxide Hydroxide | K ( Mg2.36 Fe0.64 ) ( Si4 O10 ( O0.88 ( O H )1.12 ) ) | Phlogopite-2M1 | 29 |
| * | 04-013-2099 | 13 | Potassium Aluminum Silicate | K8 Al8 Si16 O48 | Leucite | 8 |
| * | 04-025-4215 | 21 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 18 |

Anchor Scan Parameters

Dataset Name	28 SS2 ground 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 28\28 SS2 ground 550C.xrdml

Sample Identification	28 SS2 ground 550C

Measurement Start Date/Time	12/19/2023 1:41:54 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes