28 SS2 Ground  GLYCOLATED

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	12.0

Phase Silicon Oxide

Weight fraction/ %	8.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	7.0

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	12.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	21.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	33.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Silicon Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 28 SS2 ground glycol | 12.0 | 8.0 | 7.0 | 2.0 | 12.0 | 21.0 | 33.0 | 4.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7242.0000 | 7231.1820 | 7242.0000 |
| 2.0164 | 7006.3397 | 7211.6227 | 7194.0081 |
| 2.0274 | 7113.8525 | 7164.2039 | 7146.0163 |
| 2.0384 | 7107.7050 | 7116.8131 | 7098.0244 |
| 2.0494 | 7092.1829 | 7069.4523 | 7050.0326 |
| 2.0604 | 6938.0501 | 7022.1233 | 7002.0407 |
| 2.0714 | 6894.9912 | 6974.8283 | 6954.0488 |
| 2.0824 | 6921.9789 | 6927.5697 | 6906.0570 |
| 2.0934 | 6937.1003 | 6880.3499 | 6858.0651 |
| 2.1044 | 6890.4115 | 6833.1719 | 6810.0733 |
| 2.1154 | 6914.6018 | 6786.0386 | 6762.0814 |
| 2.1264 | 6659.2960 | 6738.9533 | 6714.0896 |
| 2.1374 | 6643.9174 | 6691.9198 | 6666.0977 |
| 2.1484 | 6650.5261 | 6644.9421 | 6618.1058 |
| 2.1594 | 6612.5457 | 6598.0247 | 6570.1140 |
| 2.1704 | 6551.6652 | 6551.1728 | 6522.1221 |
| 2.1814 | 6584.8869 | 6504.3922 | 6474.1303 |
| 2.1924 | 6559.4031 | 6457.6149 | 6426.1384 |
| 2.2034 | 6478.7257 | 6410.9439 | 6378.0182 |
| 2.2144 | 6278.8859 | 6364.2929 | 6329.8980 |
| 2.2254 | 6356.7040 | 6317.7468 | 6281.7778 |
| 2.2364 | 6342.8024 | 6271.3185 | 6233.6576 |
| 2.2474 | 6326.8614 | 6225.0229 | 6185.5374 |
| 2.2584 | 6403.4189 | 6178.8786 | 6137.4172 |
| 2.2694 | 6250.8260 | 6132.9079 | 6089.2970 |
| 2.2804 | 6194.2453 | 6087.1386 | 6041.1768 |
| 2.2914 | 6201.3176 | 6041.6043 | 5993.0566 |
| 2.3024 | 6252.0708 | 5996.3465 | 5944.9364 |
| 2.3134 | 6172.1632 | 5951.4158 | 5896.8162 |
| 2.3244 | 6128.7630 | 5906.8738 | 5848.6960 |
| 2.3354 | 6223.4808 | 5862.7948 | 5800.5757 |
| 2.3464 | 6182.3707 | 5819.2681 | 5752.4555 |
| 2.3574 | 6068.7945 | 5776.3995 | 5704.3353 |
| 2.3684 | 5999.3348 | 5734.3131 | 5656.2151 |
| 2.3794 | 5926.5978 | 5693.1528 | 5608.0949 |
| 2.3904 | 5928.8451 | 5653.0831 | 5559.9747 |
| 2.4014 | 6002.4336 | 5614.2891 | 5511.8545 |
| 2.4124 | 6015.1711 | 5576.9756 | 5463.7343 |
| 2.4234 | 5909.1327 | 5541.3650 | 5415.6141 |
| 2.4344 | 5837.1740 | 5507.6940 | 5367.4939 |
| 2.4454 | 5833.9095 | 5476.2081 | 5319.3737 |
| 2.4564 | 5810.5118 | 5447.1551 | 5271.2535 |
| 2.4674 | 5797.5457 | 5420.7767 | 5223.1333 |
| 2.4784 | 5736.9621 | 5397.2986 | 5175.0131 |
| 2.4894 | 5689.5919 | 5376.9188 | 5126.8929 |
| 2.5004 | 5628.5841 | 5359.7955 | 5078.7727 |
| 2.5114 | 5617.4887 | 5346.0328 | 5030.6525 |
| 2.5224 | 5634.7571 | 5335.6673 | 4982.5323 |
| 2.5334 | 5547.7640 | 5328.6520 | 4934.4121 |
| 2.5444 | 5460.0801 | 5324.8408 | 4886.2919 |
| 2.5554 | 5440.2291 | 5323.9709 | 4838.1717 |
| 2.5664 | 5430.3437 | 5325.5686 | 4790.0515 |
| 2.5774 | 5435.5044 | 5329.1719 | 4741.8029 |
| 2.5884 | 5356.0118 | 5333.9452 | 4693.5544 |
| 2.5994 | 5367.0797 | 5339.0151 | 4645.3058 |
| 2.6104 | 5271.6145 | 5343.2048 | 4597.0573 |
| 2.6214 | 5353.7896 | 5345.1008 | 4548.8087 |
| 2.6324 | 5334.6298 | 5343.0729 | 4500.5601 |
| 2.6434 | 5298.2871 | 5335.3368 | 4452.3116 |
| 2.6544 | 5197.2011 | 5320.0732 | 4404.0630 |
| 2.6654 | 5035.8436 | 5295.6028 | 4355.8145 |
| 2.6764 | 5049.7311 | 5260.5934 | 4307.5659 |
| 2.6874 | 4992.7955 | 5214.2558 | 4259.3174 |
| 2.6984 | 4906.2788 | 5156.4721 | 4211.0688 |
| 2.7094 | 4865.1878 | 5087.8165 | 4162.8203 |
| 2.7204 | 4755.9395 | 5009.4595 | 4114.5717 |
| 2.7314 | 4665.9144 | 4922.9894 | 4066.3232 |
| 2.7424 | 4615.5895 | 4830.2020 | 4018.0746 |
| 2.7534 | 4602.1495 | 4732.8186 | 3969.8261 |
| 2.7644 | 4487.3569 | 4632.6493 | 3921.4189 |
| 2.7754 | 4405.9135 | 4531.0663 | 3873.0117 |
| 2.7864 | 4192.6691 | 4429.4175 | 3824.6045 |
| 2.7974 | 4111.6726 | 4328.7249 | 3776.1973 |
| 2.8084 | 4086.1578 | 4229.7948 | 3727.7901 |
| 2.8194 | 3956.6647 | 4133.2421 | 3679.3829 |
| 2.8304 | 3950.4528 | 4039.5154 | 3630.9757 |
| 2.8414 | 3852.9174 | 3948.9203 | 3582.5685 |
| 2.8524 | 3790.1617 | 3861.6394 | 3534.1613 |
| 2.8634 | 3675.7905 | 3777.7506 | 3485.7541 |
| 2.8744 | 3633.1313 | 3697.2431 | 3437.3470 |
| 2.8854 | 3484.5074 | 3620.0335 | 3388.9398 |
| 2.8964 | 3497.9292 | 3545.9799 | 3340.5326 |
| 2.9074 | 3354.3628 | 3474.8959 | 3292.1254 |
| 2.9184 | 3272.6696 | 3406.5638 | 3243.7182 |
| 2.9294 | 3206.5074 | 3340.7458 | 3195.3110 |
| 2.9404 | 3157.1681 | 3284.3677 | 3146.9038 |
| 2.9514 | 3058.7335 | 3228.0087 | 3110.8408 |
| 2.9624 | 3120.8480 | 3180.6022 | 3074.7778 |
| 2.9734 | 2915.5074 | 3134.7480 | 3038.7147 |
| 2.9844 | 3031.9474 | 3090.2350 | 3002.6517 |
| 2.9954 | 2911.5221 | 3046.8716 | 2966.5887 |
| 3.0064 | 2949.7060 | 3004.4863 | 2930.5257 |
| 3.0174 | 2868.3835 | 2962.9285 | 2894.4627 |
| 3.0284 | 2738.7153 | 2922.0676 | 2858.3997 |
| 3.0394 | 2750.9233 | 2881.7919 | 2822.3366 |
| 3.0504 | 2794.5030 | 2842.0071 | 2786.2736 |
| 3.0614 | 2785.3038 | 2802.6339 | 2750.2106 |
| 3.0724 | 2733.1534 | 2763.6068 | 2714.1476 |
| 3.0834 | 2699.9587 | 2724.8718 | 2678.0846 |
| 3.0944 | 2550.9159 | 2686.3845 | 2642.0216 |
| 3.1054 | 2559.1426 | 2648.1089 | 2605.9586 |
| 3.1164 | 2595.8963 | 2610.0155 | 2569.8955 |
| 3.1274 | 2549.2596 | 2582.4950 | 2533.8325 |
| 3.1384 | 2469.6824 | 2552.2075 | 2515.6936 |
| 3.1494 | 2523.1652 | 2532.4571 | 2497.5547 |
| 3.1604 | 2508.7965 | 2512.8156 | 2479.4158 |
| 3.1714 | 2486.2684 | 2493.2719 | 2461.2768 |
| 3.1824 | 2484.0914 | 2473.8166 | 2443.1379 |
| 3.1934 | 2441.3628 | 2454.4415 | 2424.9990 |
| 3.2044 | 2439.3589 | 2435.1397 | 2406.8601 |
| 3.2154 | 2403.6303 | 2415.9053 | 2388.7211 |
| 3.2264 | 2333.0000 | 2396.7328 | 2370.5822 |
| 3.2374 | 2335.2596 | 2377.6176 | 2352.4433 |
| 3.2484 | 2319.9444 | 2358.5554 | 2334.3044 |
| 3.2594 | 2310.4602 | 2339.5425 | 2316.1654 |
| 3.2704 | 2343.8943 | 2320.5753 | 2298.0265 |
| 3.2814 | 2336.5044 | 2301.6508 | 2279.8876 |
| 3.2924 | 2299.9734 | 2282.7661 | 2261.7487 |
| 3.3034 | 2254.0855 | 2263.9186 | 2243.6097 |
| 3.3144 | 2220.3594 | 2246.2474 | 2225.4708 |
| 3.3254 | 2207.5251 | 2228.2903 | 2209.2966 |
| 3.3364 | 2159.2527 | 2211.5052 | 2193.1223 |
| 3.3474 | 2170.4396 | 2194.7488 | 2176.9480 |
| 3.3584 | 2199.2448 | 2178.0193 | 2160.7738 |
| 3.3694 | 2206.7827 | 2161.3151 | 2144.5995 |
| 3.3804 | 2154.5698 | 2144.6347 | 2128.4252 |
| 3.3914 | 2072.9646 | 2127.9766 | 2112.2510 |
| 3.4024 | 2063.5123 | 2111.3397 | 2096.0767 |
| 3.4134 | 2052.5477 | 2094.7227 | 2079.9024 |
| 3.4244 | 2048.1711 | 2078.1244 | 2063.7282 |
| 3.4354 | 1995.7925 | 2061.5440 | 2047.5539 |
| 3.4464 | 2049.0787 | 2044.9803 | 2031.3796 |
| 3.4574 | 2006.4129 | 2028.4325 | 2015.2054 |
| 3.4684 | 1979.0049 | 2011.8998 | 1999.0311 |
| 3.4794 | 1981.1780 | 1995.3813 | 1982.8568 |
| 3.4904 | 1993.0974 | 1978.8763 | 1966.6826 |
| 3.5014 | 1963.7050 | 1963.5633 | 1950.5083 |
| 3.5124 | 1904.3353 | 1947.9335 | 1936.3634 |
| 3.5234 | 1888.0885 | 1933.4945 | 1922.2185 |
| 3.5344 | 1862.7871 | 1919.0665 | 1908.0737 |
| 3.5454 | 1812.3589 | 1904.6489 | 1893.9288 |
| 3.5564 | 1843.1814 | 1890.2413 | 1879.7839 |
| 3.5674 | 1873.4159 | 1875.8431 | 1865.6390 |
| 3.5784 | 1888.6067 | 1861.4540 | 1851.4942 |
| 3.5894 | 1768.0442 | 1847.1067 | 1837.3493 |
| 3.6004 | 1798.2694 | 1832.8278 | 1823.2044 |
| 3.6114 | 1840.0403 | 1818.4817 | 1809.0595 |
| 3.6224 | 1794.3658 | 1804.1736 | 1794.9147 |
| 3.6334 | 1788.5526 | 1789.8262 | 1780.7698 |
| 3.6444 | 1689.4046 | 1775.4858 | 1766.6249 |
| 3.6554 | 1767.7080 | 1761.1519 | 1752.4800 |
| 3.6664 | 1709.8205 | 1746.8244 | 1738.3351 |
| 3.6774 | 1764.7227 | 1732.5028 | 1724.1903 |
| 3.6884 | 1720.4071 | 1718.2718 | 1710.0454 |
| 3.6994 | 1679.9656 | 1704.0227 | 1696.0463 |
| 3.7104 | 1609.0216 | 1689.8635 | 1682.0471 |
| 3.7214 | 1670.8053 | 1675.7095 | 1668.0480 |
| 3.7324 | 1605.4134 | 1661.5604 | 1654.0489 |
| 3.7434 | 1611.3038 | 1647.4160 | 1640.0498 |
| 3.7544 | 1617.7257 | 1633.2761 | 1626.0506 |
| 3.7654 | 1557.1062 | 1619.1406 | 1612.0515 |
| 3.7764 | 1586.3235 | 1605.0092 | 1598.0524 |
| 3.7874 | 1561.2301 | 1590.8819 | 1584.0533 |
| 3.7984 | 1543.1136 | 1576.7584 | 1570.0541 |
| 3.8094 | 1574.3638 | 1562.6387 | 1556.0550 |
| 3.8204 | 1473.5133 | 1548.5226 | 1542.0559 |
| 3.8314 | 1525.8791 | 1534.4100 | 1528.0568 |
| 3.8424 | 1519.2124 | 1520.3007 | 1514.0576 |
| 3.8534 | 1453.0767 | 1506.1946 | 1500.0585 |
| 3.8644 | 1484.1578 | 1492.0917 | 1486.0594 |
| 3.8754 | 1492.7207 | 1480.2445 | 1472.0602 |
| 3.8864 | 1441.8496 | 1467.7718 | 1461.9382 |
| 3.8974 | 1465.7453 | 1457.5547 | 1451.8162 |
| 3.9084 | 1455.4946 | 1447.3403 | 1441.6942 |
| 3.9194 | 1444.2360 | 1437.1285 | 1431.5722 |
| 3.9304 | 1389.8117 | 1426.9193 | 1421.4502 |
| 3.9414 | 1374.4238 | 1416.7126 | 1411.3282 |
| 3.9524 | 1458.2035 | 1406.5082 | 1401.2061 |
| 3.9634 | 1382.3097 | 1396.3062 | 1391.0841 |
| 3.9744 | 1380.6028 | 1386.2588 | 1380.9621 |
| 3.9854 | 1406.6106 | 1376.1260 | 1370.8401 |
| 3.9964 | 1398.8800 | 1366.0085 | 1360.7181 |
| 4.0074 | 1335.7158 | 1355.8492 | 1350.5961 |
| 4.0184 | 1360.5192 | 1345.6601 | 1340.4740 |
| 4.0294 | 1350.9390 | 1335.4731 | 1330.3520 |
| 4.0404 | 1381.7384 | 1325.2879 | 1320.2300 |
| 4.0514 | 1358.6696 | 1315.1046 | 1310.1080 |
| 4.0624 | 1289.8638 | 1304.9232 | 1299.9860 |
| 4.0734 | 1285.8033 | 1294.7435 | 1289.8640 |
| 4.0844 | 1253.2743 | 1284.5655 | 1279.7420 |
| 4.0954 | 1243.4582 | 1274.3892 | 1269.6199 |
| 4.1064 | 1187.9464 | 1264.2146 | 1259.4979 |
| 4.1174 | 1227.8761 | 1254.0416 | 1249.3759 |
| 4.1284 | 1278.0295 | 1243.8702 | 1239.2539 |
| 4.1394 | 1291.2448 | 1233.7003 | 1229.1319 |
| 4.1504 | 1233.6032 | 1223.5319 | 1219.0099 |
| 4.1614 | 1219.5015 | 1213.3650 | 1208.8879 |
| 4.1724 | 1181.4611 | 1203.1996 | 1198.7658 |
| 4.1834 | 1172.9115 | 1193.0356 | 1188.6438 |
| 4.1944 | 1190.5408 | 1182.8730 | 1178.5218 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 28 SS2 ground glycol | 2.0054 | 29.9894 | 0.0110 | 12/20/2023 12:50:05 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6815 | 853.62 | 0.2598 | 32.92071 | 100.00 |
| 5.3289 | 134.25 | 0.1732 | 16.57029 | 15.73 |
| 7.0050 | 229.49 | 0.3031 | 12.60889 | 26.88 |
| 8.7292 | 254.85 | 0.1515 | 10.12174 | 29.85 |
| 15.7110 | 588.91 | 0.0866 | 5.63599 | 68.99 |
| 17.5985 | 24.19 | 0.2598 | 5.03553 | 2.83 |
| 18.1867 | 91.72 | 0.0866 | 4.87398 | 10.74 |
| 19.5332 | 34.88 | 0.5196 | 4.54093 | 4.09 |
| 23.3549 | 30.27 | 0.1299 | 3.80579 | 3.55 |
| 24.1359 | 17.20 | 0.2598 | 3.68439 | 2.01 |
| 25.8862 | 462.32 | 0.0974 | 3.43909 | 54.16 |
| 26.7016 | 210.21 | 0.1299 | 3.33589 | 24.63 |
| 27.4840 | 425.30 | 0.0866 | 3.24267 | 49.82 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-008-7810 | 54 | Titanium Oxide | Ti O2 | Rutile | 12 |
| * | 04-016-2085 | 39 | Silicon Oxide | Si O2 | Quartz | 8 |
| * | 04-017-4317 | 28 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 7 |
| * | 04-016-6876 | 25 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 2 |
| * | 04-011-6751 | 19 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 12 |
| * | 04-013-9383 | 13 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 Al Si3 O10 ( O H ) F | Phlogopite-2M1 | 21 |
| * | 04-025-4215 | 21 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 33 |
| * | 01-081-8598 | 11 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2 Al2 ) Si8 O20 ( H2 O )4 ( O H )2 ( H2 O )3.84 | Palygorskite-M | 4 |

Anchor Scan Parameters

Dataset Name	28 SS2 ground glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 28\28 SS2 ground glycol.xrdml

Sample Identification	28 SS2 ground glycol

Measurement Start Date/Time	12/20/2023 12:50:05 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes