28 SS2 Ground  REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	12.0

Phase Silicon Oxide

Weight fraction/ %	5.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	5.0

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	13.0

Phase Potassium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	13.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	10.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	32.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	1.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	3.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Silicon Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Potassium Aluminum Silicate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Silicate Hydroxide Hydrate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 28 SS2 ground | 12.0 | 5.0 | 5.0 | 2.0 | 3.0 | 13.0 | 13.0 | 10.0 | 32.0 | 1.0 | 3.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8403.0000 | 8411.6582 | 8403.0000 |
| 2.0164 | 8336.5206 | 8370.7711 | 8342.1135 |
| 2.0274 | 8297.2134 | 8310.8125 | 8281.2270 |
| 2.0384 | 8257.4823 | 8250.8991 | 8220.3405 |
| 2.0494 | 8047.9794 | 8191.0338 | 8159.4540 |
| 2.0604 | 8294.5138 | 8131.2198 | 8098.5675 |
| 2.0714 | 8222.5339 | 8071.4606 | 8037.6810 |
| 2.0824 | 8169.0197 | 8011.7600 | 7976.7945 |
| 2.0934 | 8070.3746 | 7952.1219 | 7915.9080 |
| 2.1044 | 8103.4867 | 7892.5508 | 7855.0215 |
| 2.1154 | 7842.1013 | 7833.0516 | 7794.1350 |
| 2.1264 | 7949.6991 | 7773.6296 | 7733.2485 |
| 2.1374 | 7894.4454 | 7714.2907 | 7672.3620 |
| 2.1484 | 7845.1598 | 7655.0414 | 7611.4755 |
| 2.1594 | 7848.7532 | 7595.8888 | 7550.5890 |
| 2.1704 | 7828.9985 | 7536.8410 | 7489.7025 |
| 2.1814 | 7713.4818 | 7477.9072 | 7428.8160 |
| 2.1924 | 7837.5821 | 7419.0395 | 7367.9295 |
| 2.2034 | 7763.4336 | 7360.2391 | 7306.8571 |
| 2.2144 | 7564.9813 | 7301.5306 | 7245.7847 |
| 2.2254 | 7689.3156 | 7242.9890 | 7184.7124 |
| 2.2364 | 7506.8083 | 7184.6337 | 7123.6400 |
| 2.2474 | 7520.3982 | 7126.4883 | 7062.5677 |
| 2.2584 | 7489.1981 | 7068.5812 | 7001.4953 |
| 2.2694 | 7522.0944 | 7010.9470 | 6940.4229 |
| 2.2804 | 7520.2724 | 6953.6283 | 6879.3506 |
| 2.2914 | 7447.8043 | 6896.6770 | 6818.2782 |
| 2.3024 | 7430.3805 | 6840.1571 | 6757.2058 |
| 2.3134 | 7396.2665 | 6784.1467 | 6696.1335 |
| 2.3244 | 7317.4646 | 6728.7410 | 6635.0611 |
| 2.3354 | 7224.1622 | 6674.0554 | 6573.9887 |
| 2.3464 | 7223.0934 | 6620.2286 | 6512.9164 |
| 2.3574 | 7170.0285 | 6567.4257 | 6451.8440 |
| 2.3684 | 7047.6976 | 6515.8411 | 6390.7717 |
| 2.3794 | 7060.6529 | 6465.6540 | 6329.6993 |
| 2.3904 | 7130.6947 | 6417.1157 | 6268.4766 |
| 2.4014 | 7030.5221 | 6370.5288 | 6207.2538 |
| 2.4124 | 7051.8240 | 6326.2677 | 6146.0311 |
| 2.4234 | 6984.7316 | 6284.6902 | 6084.8084 |
| 2.4344 | 6892.4794 | 6246.1789 | 6023.5857 |
| 2.4454 | 6896.4415 | 6211.1346 | 5962.3629 |
| 2.4564 | 6841.0398 | 6179.9654 | 5901.1402 |
| 2.4674 | 6765.4484 | 6153.0740 | 5839.9175 |
| 2.4784 | 6820.8781 | 6130.8418 | 5778.6947 |
| 2.4894 | 6780.6244 | 6113.6112 | 5717.4720 |
| 2.5004 | 6682.5973 | 6101.6653 | 5656.2493 |
| 2.5114 | 6688.0039 | 6095.2057 | 5595.0266 |
| 2.5224 | 6674.3151 | 6094.3297 | 5533.8038 |
| 2.5334 | 6723.6667 | 6099.0056 | 5472.5811 |
| 2.5444 | 6597.7532 | 6109.0472 | 5411.3584 |
| 2.5554 | 6511.0403 | 6124.0853 | 5350.1356 |
| 2.5664 | 6489.7625 | 6143.5373 | 5288.9129 |
| 2.5774 | 6502.7915 | 6166.5724 | 5227.6902 |
| 2.5884 | 6500.8515 | 6192.0718 | 5166.4675 |
| 2.5994 | 6480.3717 | 6218.5873 | 5105.2447 |
| 2.6104 | 6419.2153 | 6244.3022 | 5044.0220 |
| 2.6214 | 6252.2753 | 6267.0088 | 4982.7993 |
| 2.6324 | 6297.5915 | 6284.1227 | 4921.5765 |
| 2.6434 | 6242.0580 | 6292.7610 | 4860.3538 |
| 2.6544 | 6214.0531 | 6289.9083 | 4799.1311 |
| 2.6654 | 6137.1416 | 6272.6812 | 4737.9084 |
| 2.6764 | 6003.7842 | 6238.6640 | 4676.6856 |
| 2.6874 | 5933.9459 | 6186.2510 | 4615.4629 |
| 2.6984 | 5820.0133 | 6114.9041 | 4554.2402 |
| 2.7094 | 5679.8722 | 6025.2441 | 4493.0175 |
| 2.7204 | 5684.3535 | 5918.9446 | 4431.7947 |
| 2.7314 | 5478.0295 | 5798.4653 | 4370.5720 |
| 2.7424 | 5190.8318 | 5666.7077 | 4309.3493 |
| 2.7534 | 5201.8486 | 5526.6357 | 4248.1265 |
| 2.7644 | 5108.8377 | 5381.1052 | 4186.7534 |
| 2.7754 | 4958.3628 | 5232.6833 | 4125.3804 |
| 2.7864 | 4703.9985 | 5083.5970 | 4064.0073 |
| 2.7974 | 4725.7522 | 4935.6362 | 4002.6342 |
| 2.8084 | 4550.8589 | 4790.2252 | 3941.2611 |
| 2.8194 | 4389.0216 | 4648.4618 | 3879.8880 |
| 2.8304 | 4207.2271 | 4511.1587 | 3818.5149 |
| 2.8414 | 4112.6657 | 4378.8831 | 3757.1418 |
| 2.8524 | 3899.7360 | 4251.9906 | 3695.7687 |
| 2.8634 | 3876.4956 | 4130.6562 | 3634.3956 |
| 2.8744 | 3742.0029 | 4014.9021 | 3573.0225 |
| 2.8854 | 3553.1425 | 3904.6229 | 3511.6494 |
| 2.8964 | 3499.2257 | 3799.6109 | 3450.2763 |
| 2.9074 | 3553.1435 | 3699.5782 | 3388.9032 |
| 2.9184 | 3318.0929 | 3604.1793 | 3327.5302 |
| 2.9294 | 3270.4307 | 3513.0307 | 3266.1571 |
| 2.9404 | 3165.7896 | 3434.1055 | 3204.7840 |
| 2.9514 | 3197.4415 | 3368.5491 | 3170.0937 |
| 2.9624 | 3084.4941 | 3314.4084 | 3135.4034 |
| 2.9734 | 3032.9774 | 3262.9257 | 3100.7131 |
| 2.9844 | 3107.8947 | 3213.7455 | 3066.0228 |
| 2.9954 | 2862.3717 | 3166.5428 | 3031.3326 |
| 3.0064 | 2913.3933 | 3121.0258 | 2996.6423 |
| 3.0174 | 2882.7532 | 3076.9370 | 2961.9520 |
| 3.0284 | 2811.7198 | 3034.0524 | 2927.2617 |
| 3.0394 | 2830.8928 | 2992.1795 | 2892.5714 |
| 3.0504 | 2811.3176 | 2951.1552 | 2857.8812 |
| 3.0614 | 2767.5899 | 2910.8425 | 2823.1909 |
| 3.0724 | 2646.3009 | 2871.1275 | 2788.5006 |
| 3.0834 | 2686.4808 | 2831.9162 | 2753.8103 |
| 3.0944 | 2584.7168 | 2793.1315 | 2719.1200 |
| 3.1054 | 2651.5477 | 2754.7104 | 2684.4297 |
| 3.1164 | 2593.1391 | 2716.6017 | 2649.7395 |
| 3.1274 | 2633.5546 | 2682.8427 | 2615.0492 |
| 3.1384 | 2599.8515 | 2654.1559 | 2593.3537 |
| 3.1494 | 2607.0954 | 2629.7566 | 2571.6581 |
| 3.1604 | 2578.1888 | 2605.5423 | 2549.9626 |
| 3.1714 | 2544.9203 | 2581.4935 | 2528.2671 |
| 3.1824 | 2499.7394 | 2557.5941 | 2506.5716 |
| 3.1934 | 2479.6460 | 2533.8303 | 2484.8760 |
| 3.2044 | 2449.7753 | 2510.1901 | 2463.1805 |
| 3.2154 | 2471.5605 | 2486.6632 | 2441.4850 |
| 3.2264 | 2484.0782 | 2463.2407 | 2419.7895 |
| 3.2374 | 2426.8082 | 2439.9143 | 2398.0939 |
| 3.2484 | 2329.0555 | 2416.9000 | 2376.3984 |
| 3.2594 | 2302.6283 | 2393.7777 | 2354.7029 |
| 3.2704 | 2312.8653 | 2370.8131 | 2333.0074 |
| 3.2814 | 2307.4258 | 2347.8244 | 2311.3119 |
| 3.2924 | 2297.4867 | 2324.8871 | 2289.6163 |
| 3.3034 | 2251.5752 | 2302.0121 | 2267.9208 |
| 3.3144 | 2254.0998 | 2280.2812 | 2246.2253 |
| 3.3254 | 2255.0324 | 2259.8920 | 2227.9885 |
| 3.3364 | 2160.5865 | 2240.6397 | 2209.7518 |
| 3.3474 | 2121.4956 | 2221.4353 | 2191.5151 |
| 3.3584 | 2190.9986 | 2202.2760 | 2173.2783 |
| 3.3694 | 2203.2114 | 2183.1589 | 2155.0416 |
| 3.3804 | 2127.9626 | 2164.0817 | 2136.8049 |
| 3.3914 | 2098.1593 | 2145.0420 | 2118.5681 |
| 3.4024 | 2098.9267 | 2126.0375 | 2100.3314 |
| 3.4134 | 2077.9233 | 2107.0664 | 2082.0946 |
| 3.4244 | 2029.5516 | 2088.1267 | 2063.8579 |
| 3.4354 | 1998.4346 | 2069.2166 | 2045.6212 |
| 3.4464 | 1994.4405 | 2050.3347 | 2027.3844 |
| 3.4574 | 1954.2979 | 2031.4793 | 2009.1477 |
| 3.4684 | 1970.8909 | 2012.6490 | 1990.9109 |
| 3.4794 | 1980.1190 | 1993.8425 | 1972.6742 |
| 3.4904 | 1952.2212 | 1975.0586 | 1954.4375 |
| 3.5014 | 1925.2104 | 1956.6714 | 1936.2007 |
| 3.5124 | 1915.6323 | 1938.7495 | 1919.1595 |
| 3.5234 | 1931.7080 | 1921.2221 | 1902.1182 |
| 3.5344 | 1889.4080 | 1903.7131 | 1885.0770 |
| 3.5454 | 1927.3806 | 1886.2216 | 1868.0358 |
| 3.5564 | 1895.7551 | 1868.7466 | 1850.9945 |
| 3.5674 | 1808.9203 | 1851.2875 | 1833.9533 |
| 3.5784 | 1788.2729 | 1833.9263 | 1816.9120 |
| 3.5894 | 1842.8938 | 1816.5152 | 1799.8708 |
| 3.6004 | 1800.3348 | 1799.1423 | 1782.8295 |
| 3.6114 | 1797.5064 | 1781.7502 | 1765.7883 |
| 3.6224 | 1821.9764 | 1764.3618 | 1748.7470 |
| 3.6334 | 1743.4542 | 1746.9854 | 1731.7058 |
| 3.6444 | 1632.7183 | 1729.6204 | 1714.6645 |
| 3.6554 | 1775.1387 | 1712.2663 | 1697.6233 |
| 3.6664 | 1734.8122 | 1694.9228 | 1680.5821 |
| 3.6774 | 1678.7197 | 1677.5892 | 1663.5408 |
| 3.6884 | 1690.4912 | 1662.4059 | 1646.4996 |
| 3.6994 | 1544.7915 | 1649.7694 | 1636.2772 |
| 3.7104 | 1583.1170 | 1639.2824 | 1626.0547 |
| 3.7214 | 1624.7788 | 1628.8038 | 1615.8323 |
| 3.7324 | 1625.2109 | 1618.3334 | 1605.6099 |
| 3.7434 | 1634.4199 | 1607.8707 | 1595.3875 |
| 3.7544 | 1589.1947 | 1597.4156 | 1585.1651 |
| 3.7654 | 1595.6991 | 1586.9677 | 1574.9427 |
| 3.7764 | 1607.7463 | 1576.5267 | 1564.7203 |
| 3.7874 | 1507.8938 | 1566.0923 | 1554.4979 |
| 3.7984 | 1552.9415 | 1555.6644 | 1544.2755 |
| 3.8094 | 1535.2291 | 1545.2427 | 1534.0531 |
| 3.8204 | 1486.4956 | 1534.8269 | 1523.8306 |
| 3.8314 | 1470.7739 | 1524.4169 | 1513.6082 |
| 3.8424 | 1510.8958 | 1514.0123 | 1503.3858 |
| 3.8534 | 1473.8437 | 1503.6131 | 1493.1634 |
| 3.8644 | 1484.7650 | 1493.2191 | 1482.9410 |
| 3.8754 | 1472.4159 | 1482.8300 | 1472.7186 |
| 3.8864 | 1503.5133 | 1472.4457 | 1462.4962 |
| 3.8974 | 1544.9174 | 1462.0660 | 1452.2738 |
| 3.9084 | 1427.7075 | 1451.6908 | 1442.0514 |
| 3.9194 | 1466.0265 | 1441.3199 | 1431.8290 |
| 3.9304 | 1377.5280 | 1430.9532 | 1421.6065 |
| 3.9414 | 1400.3884 | 1420.5905 | 1411.3841 |
| 3.9524 | 1386.2979 | 1410.2318 | 1401.1617 |
| 3.9634 | 1379.2438 | 1399.8768 | 1390.9393 |
| 3.9744 | 1366.2016 | 1389.5255 | 1380.7169 |
| 3.9854 | 1362.4336 | 1379.1778 | 1370.4945 |
| 3.9964 | 1310.8860 | 1368.8335 | 1360.2721 |
| 4.0074 | 1349.7394 | 1358.4926 | 1350.0497 |
| 4.0184 | 1363.7537 | 1348.1549 | 1339.8273 |
| 4.0294 | 1354.5074 | 1337.8204 | 1329.6048 |
| 4.0404 | 1325.3078 | 1327.4889 | 1319.3824 |
| 4.0514 | 1309.8879 | 1317.1604 | 1309.1600 |
| 4.0624 | 1339.3195 | 1306.8004 | 1298.9376 |
| 4.0734 | 1292.8358 | 1296.4023 | 1288.6055 |
| 4.0844 | 1312.5221 | 1285.9725 | 1278.2734 |
| 4.0954 | 1287.1288 | 1275.5454 | 1267.9412 |
| 4.1064 | 1245.8073 | 1265.1209 | 1257.6091 |
| 4.1174 | 1276.4071 | 1254.6989 | 1247.2770 |
| 4.1284 | 1235.3948 | 1244.2793 | 1236.9449 |
| 4.1394 | 1243.6873 | 1233.8622 | 1226.6127 |
| 4.1504 | 1231.0693 | 1223.4474 | 1216.2806 |
| 4.1614 | 1187.9538 | 1213.0349 | 1205.9485 |
| 4.1724 | 1192.1013 | 1202.6246 | 1195.6164 |
| 4.1834 | 1206.1151 | 1192.2165 | 1185.2842 |
| 4.1944 | 1190.4080 | 1181.8106 | 1174.9521 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 28 SS2 ground | 2.0054 | 29.9894 | 0.0110 | 12/13/2023 12:08:50 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6848 | 1402.20 | 0.2598 | 32.88019 | 100.00 |
| 5.3118 | 106.73 | 0.1732 | 16.62377 | 7.61 |
| 7.1459 | 270.18 | 0.3897 | 12.36054 | 19.27 |
| 8.6918 | 340.78 | 0.0866 | 10.16530 | 24.30 |
| 13.5419 | 35.38 | 0.1299 | 6.53349 | 2.52 |
| 15.7051 | 506.64 | 0.0974 | 5.63808 | 36.13 |
| 17.6062 | 31.43 | 0.2165 | 5.03335 | 2.24 |
| 18.1920 | 87.27 | 0.0649 | 4.87257 | 6.22 |
| 19.5177 | 31.15 | 0.5196 | 4.54449 | 2.22 |
| 25.8732 | 418.91 | 0.0758 | 3.44078 | 29.87 |
| 26.6636 | 289.91 | 0.1515 | 3.34057 | 20.68 |
| 27.4838 | 663.13 | 0.0758 | 3.24270 | 47.29 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-008-7810 | 55 | Titanium Oxide | Ti O2 | Rutile | 12 |
| * | 01-070-7344 | 45 | Silicon Oxide | Si O2 | Quartz | 5 |
| * | 04-017-4317 | 29 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 5 |
| * | 04-016-6876 | 21 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 2 |
| * | 04-018-3208 | 10 | Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Mg1.0 Fe0.08 Al1.0 Si3.99 O10.2 ( O H )0.8 ( H2 O )3.3 | Palygorskite-M | 3 |
| * | 04-011-6756 | 15 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 13 |
| * | 04-012-1565 | 7 | Potassium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K Mg1.9 Ti0.3 Fe0.5 Al1.2 Si2.8 O10.7 ( O H ) F0.3 | Phlogopite-1M, Fe+2-bearing | 13 |
| * | 04-013-2099 | 15 | Potassium Aluminum Silicate | K8 Al8 Si16 O48 | Leucite | 10 |
| * | 04-025-4215 | 20 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 32 |
| * | 01-075-8323 | 5 | Magnesium Silicate Hydroxide Hydrate | Mg8 ( Si12 O30 ( O H )4 ) ( H2 O )11.82 | Sepiolite | 1 |
| * | 04-013-5980 | 6 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-O | 3 |

Anchor Scan Parameters

Dataset Name	28 SS2 ground

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 28\28 SS2 ground.xrdml

Sample Identification	28 SS2 ground

Measurement Start Date/Time	12/13/2023 12:08:50 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes