28 SS2 Ground 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	13.0

Phase Titanium Oxide

Weight fraction/ %	15.0

Phase Silicon Oxide

Weight fraction/ %	7.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	10.0

Phase Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	12.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	10.0

Phase Potassium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	25.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	3.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | Titanium Oxide | Silicon Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Aluminum Silicate | Potassium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 28 SS2 ground 400C | 13.0 | 15.0 | 7.0 | 10.0 | 2.0 | 12.0 | 10.0 | 25.0 | 3.0 | 3.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6238.0000 | 6228.6326 | 6238.0000 |
| 2.0164 | 6190.5418 | 6208.8450 | 6198.0898 |
| 2.0274 | 5992.8525 | 6169.2513 | 6158.1796 |
| 2.0384 | 5991.9041 | 6129.6722 | 6118.2694 |
| 2.0494 | 6114.6411 | 6090.1086 | 6078.3592 |
| 2.0604 | 6010.2011 | 6050.5618 | 6038.4490 |
| 2.0714 | 5978.6047 | 6011.0328 | 5998.5388 |
| 2.0824 | 5756.0792 | 5971.5231 | 5958.6286 |
| 2.0934 | 5947.3550 | 5932.0343 | 5918.7184 |
| 2.1044 | 5676.3186 | 5892.5680 | 5878.8082 |
| 2.1154 | 5885.4405 | 5853.1265 | 5838.8980 |
| 2.1264 | 5752.5944 | 5813.7119 | 5798.9879 |
| 2.1374 | 5741.8879 | 5774.3269 | 5759.0777 |
| 2.1484 | 5682.8564 | 5734.9749 | 5719.1675 |
| 2.1594 | 5624.3343 | 5695.6592 | 5679.2573 |
| 2.1704 | 5640.2286 | 5656.3843 | 5639.3471 |
| 2.1814 | 5567.3048 | 5617.1550 | 5599.4369 |
| 2.1924 | 5485.7001 | 5579.8613 | 5559.5267 |
| 2.2034 | 5610.3363 | 5542.6515 | 5523.4106 |
| 2.2144 | 5533.3112 | 5507.3918 | 5487.2944 |
| 2.2254 | 5539.8810 | 5472.2070 | 5451.1783 |
| 2.2364 | 5431.9366 | 5437.1077 | 5415.0622 |
| 2.2474 | 5449.5408 | 5402.1058 | 5378.9461 |
| 2.2584 | 5437.4307 | 5367.2152 | 5342.8299 |
| 2.2694 | 5384.4159 | 5332.4515 | 5306.7138 |
| 2.2804 | 5312.9597 | 5297.8324 | 5270.5977 |
| 2.2914 | 5247.8456 | 5263.3780 | 5234.4816 |
| 2.3024 | 5204.1549 | 5229.1104 | 5198.3654 |
| 2.3134 | 5128.4936 | 5195.0545 | 5162.2493 |
| 2.3244 | 5188.9317 | 5161.2372 | 5126.1332 |
| 2.3354 | 5265.3776 | 5127.6881 | 5090.0171 |
| 2.3464 | 5126.7050 | 5094.4391 | 5053.9009 |
| 2.3574 | 5006.4553 | 5061.5240 | 5017.7848 |
| 2.3684 | 4932.8038 | 5028.9787 | 4981.6687 |
| 2.3794 | 4929.9695 | 4997.1660 | 4945.5526 |
| 2.3904 | 4982.1018 | 4965.8031 | 4910.0922 |
| 2.4014 | 4941.8938 | 4935.2499 | 4874.6319 |
| 2.4124 | 4840.9975 | 4905.2191 | 4839.1715 |
| 2.4234 | 4875.6342 | 4875.7481 | 4803.7112 |
| 2.4344 | 4925.8348 | 4846.8722 | 4768.2508 |
| 2.4454 | 4907.8761 | 4818.6240 | 4732.7904 |
| 2.4564 | 4867.8663 | 4791.0316 | 4697.3301 |
| 2.4674 | 4827.7699 | 4764.1183 | 4661.8697 |
| 2.4784 | 4792.7871 | 4737.9009 | 4626.4094 |
| 2.4894 | 4803.7139 | 4712.3883 | 4590.9490 |
| 2.5004 | 4763.2655 | 4687.5807 | 4555.4887 |
| 2.5114 | 4679.9459 | 4663.4679 | 4520.0283 |
| 2.5224 | 4543.8186 | 4640.0279 | 4484.5680 |
| 2.5334 | 4504.7080 | 4617.2255 | 4449.1076 |
| 2.5444 | 4599.8510 | 4595.0106 | 4413.6473 |
| 2.5554 | 4612.6578 | 4573.3163 | 4378.1869 |
| 2.5664 | 4569.1799 | 4551.9863 | 4342.7266 |
| 2.5774 | 4501.9518 | 4530.9840 | 4307.1238 |
| 2.5884 | 4445.2915 | 4510.1100 | 4271.5209 |
| 2.5994 | 4434.3186 | 4489.2805 | 4235.9181 |
| 2.6104 | 4474.5325 | 4468.3134 | 4200.3153 |
| 2.6214 | 4432.4297 | 4446.9989 | 4164.7125 |
| 2.6324 | 4300.6121 | 4425.1000 | 4129.1097 |
| 2.6434 | 4280.9508 | 4402.3554 | 4093.5069 |
| 2.6544 | 4267.7945 | 4378.4862 | 4057.9041 |
| 2.6654 | 4257.5251 | 4353.2061 | 4022.3013 |
| 2.6764 | 4234.5074 | 4326.2354 | 3986.6985 |
| 2.6874 | 4265.8643 | 4297.3186 | 3951.0957 |
| 2.6984 | 4165.7212 | 4266.2435 | 3915.4929 |
| 2.7094 | 4015.7925 | 4232.8586 | 3879.8901 |
| 2.7204 | 4109.4302 | 4197.0878 | 3844.2873 |
| 2.7314 | 4051.7669 | 4158.9368 | 3808.6845 |
| 2.7424 | 3906.6514 | 4118.4935 | 3773.0817 |
| 2.7534 | 3997.0108 | 4075.9187 | 3737.4789 |
| 2.7644 | 3902.1165 | 4031.4321 | 3701.8760 |
| 2.7754 | 3837.9813 | 3985.2937 | 3666.2732 |
| 2.7864 | 3751.5875 | 3937.7851 | 3630.6704 |
| 2.7974 | 3739.1150 | 3889.1924 | 3595.0676 |
| 2.8084 | 3687.8569 | 3839.7926 | 3559.4648 |
| 2.8194 | 3653.8043 | 3789.8437 | 3523.8620 |
| 2.8304 | 3609.5177 | 3739.5791 | 3488.2592 |
| 2.8414 | 3505.1150 | 3689.2045 | 3452.6564 |
| 2.8524 | 3428.9120 | 3638.8980 | 3417.0536 |
| 2.8634 | 3421.1652 | 3588.8105 | 3381.4508 |
| 2.8744 | 3361.7694 | 3539.0683 | 3345.8480 |
| 2.8854 | 3378.6824 | 3489.7745 | 3310.2452 |
| 2.8964 | 3312.2965 | 3441.0120 | 3274.6424 |
| 2.9074 | 3223.4405 | 3392.8450 | 3239.0396 |
| 2.9184 | 3277.2261 | 3345.3216 | 3203.4368 |
| 2.9294 | 3185.4837 | 3298.4749 | 3167.8339 |
| 2.9404 | 3027.7109 | 3256.1569 | 3132.2311 |
| 2.9514 | 3166.8368 | 3214.5969 | 3104.3443 |
| 2.9624 | 3099.8024 | 3177.5728 | 3076.4575 |
| 2.9734 | 3123.3471 | 3141.2425 | 3048.5706 |
| 2.9844 | 3108.0182 | 3105.5884 | 3020.6838 |
| 2.9954 | 3024.5221 | 3070.5865 | 2992.7969 |
| 3.0064 | 2965.8530 | 3036.2078 | 2964.9101 |
| 3.0174 | 2931.5998 | 3002.4193 | 2937.0233 |
| 3.0284 | 2889.1135 | 2969.1855 | 2909.1364 |
| 3.0394 | 2766.7375 | 2936.4686 | 2881.2496 |
| 3.0504 | 2748.3294 | 2904.2303 | 2853.3627 |
| 3.0614 | 2748.0590 | 2872.4318 | 2825.4759 |
| 3.0724 | 2747.3904 | 2841.0349 | 2797.5891 |
| 3.0834 | 2693.1583 | 2810.0026 | 2769.7022 |
| 3.0944 | 2728.8053 | 2779.2993 | 2741.8154 |
| 3.1054 | 2748.2940 | 2748.8913 | 2713.9286 |
| 3.1164 | 2703.3092 | 2718.7472 | 2686.0417 |
| 3.1274 | 2646.6431 | 2693.0162 | 2658.1549 |
| 3.1384 | 2603.1898 | 2667.5501 | 2638.6817 |
| 3.1494 | 2587.5231 | 2646.4459 | 2619.2085 |
| 3.1604 | 2657.6725 | 2625.5033 | 2599.7353 |
| 3.1714 | 2555.1770 | 2604.7028 | 2580.2621 |
| 3.1824 | 2549.1037 | 2584.0268 | 2560.7888 |
| 3.1934 | 2496.9646 | 2563.4600 | 2541.3156 |
| 3.2044 | 2490.8083 | 2542.9889 | 2521.8424 |
| 3.2154 | 2465.0157 | 2522.6016 | 2502.3692 |
| 3.2264 | 2488.2449 | 2502.2880 | 2482.8960 |
| 3.2374 | 2534.0659 | 2482.0391 | 2463.4228 |
| 3.2484 | 2493.5000 | 2461.8473 | 2443.9496 |
| 3.2594 | 2436.3127 | 2441.7062 | 2424.4764 |
| 3.2704 | 2403.5772 | 2421.6099 | 2405.0032 |
| 3.2814 | 2362.9479 | 2401.5537 | 2385.5300 |
| 3.2924 | 2327.1770 | 2381.5335 | 2366.0568 |
| 3.3034 | 2345.7738 | 2361.5456 | 2346.5836 |
| 3.3144 | 2324.3560 | 2342.8066 | 2327.1104 |
| 3.3254 | 2325.2035 | 2324.1109 | 2310.0931 |
| 3.3364 | 2294.6406 | 2306.6592 | 2293.0757 |
| 3.3474 | 2268.0206 | 2289.2299 | 2276.0584 |
| 3.3584 | 2222.9454 | 2271.8213 | 2259.0411 |
| 3.3694 | 2186.8977 | 2254.4317 | 2242.0237 |
| 3.3804 | 2151.3992 | 2237.0598 | 2225.0064 |
| 3.3914 | 2114.5398 | 2219.7045 | 2207.9891 |
| 3.4024 | 2135.2188 | 2202.3647 | 2190.9718 |
| 3.4134 | 2187.2232 | 2185.0393 | 2173.9544 |
| 3.4244 | 2210.6844 | 2167.7276 | 2156.9371 |
| 3.4354 | 2123.1288 | 2150.4286 | 2139.9198 |
| 3.4464 | 2066.2709 | 2133.1417 | 2122.9024 |
| 3.4574 | 2014.2271 | 2115.8662 | 2105.8851 |
| 3.4684 | 2011.4661 | 2098.6014 | 2088.8678 |
| 3.4794 | 2021.8830 | 2081.3468 | 2071.8505 |
| 3.4904 | 2082.6106 | 2064.1019 | 2054.8331 |
| 3.5014 | 2081.0777 | 2046.8661 | 2037.8158 |
| 3.5124 | 2000.3997 | 2029.6390 | 2020.7985 |
| 3.5234 | 2013.4661 | 2012.4202 | 2003.7811 |
| 3.5344 | 2040.5015 | 1995.2091 | 1986.7638 |
| 3.5454 | 1954.6273 | 1978.0056 | 1969.7465 |
| 3.5564 | 1968.3805 | 1960.8091 | 1952.7292 |
| 3.5674 | 1921.9016 | 1943.6497 | 1935.7118 |
| 3.5784 | 1937.1234 | 1926.5432 | 1918.6945 |
| 3.5894 | 1903.5752 | 1909.3827 | 1901.6772 |
| 3.6004 | 1911.1195 | 1892.2516 | 1884.6598 |
| 3.6114 | 1884.4258 | 1875.0881 | 1867.6425 |
| 3.6224 | 1860.6711 | 1857.9299 | 1850.6252 |
| 3.6334 | 1837.3422 | 1840.7769 | 1833.6079 |
| 3.6444 | 1792.2630 | 1823.6288 | 1816.5905 |
| 3.6554 | 1735.9115 | 1806.4854 | 1799.5732 |
| 3.6664 | 1779.2129 | 1789.3466 | 1782.5559 |
| 3.6774 | 1729.8279 | 1772.2121 | 1765.5385 |
| 3.6884 | 1693.7035 | 1757.3428 | 1748.5212 |
| 3.6994 | 1801.6028 | 1742.5083 | 1736.0569 |
| 3.7104 | 1785.1313 | 1729.9387 | 1723.5925 |
| 3.7214 | 1744.3864 | 1717.3728 | 1711.1281 |
| 3.7324 | 1714.9685 | 1704.8104 | 1698.6638 |
| 3.7434 | 1635.7571 | 1692.2514 | 1686.1994 |
| 3.7544 | 1720.7021 | 1679.6957 | 1673.7351 |
| 3.7654 | 1641.8751 | 1667.1431 | 1661.2707 |
| 3.7764 | 1690.8796 | 1654.5935 | 1648.8063 |
| 3.7874 | 1631.5398 | 1642.0469 | 1636.3420 |
| 3.7984 | 1602.9449 | 1629.5030 | 1623.8776 |
| 3.8094 | 1588.1957 | 1616.9619 | 1611.4133 |
| 3.8204 | 1661.7669 | 1604.4234 | 1598.9489 |
| 3.8314 | 1617.3471 | 1591.8874 | 1586.4846 |
| 3.8424 | 1577.4739 | 1579.3538 | 1574.0202 |
| 3.8534 | 1567.4159 | 1566.8226 | 1561.5558 |
| 3.8644 | 1556.0669 | 1554.2936 | 1549.0915 |
| 3.8754 | 1520.1947 | 1543.4606 | 1536.6271 |
| 3.8864 | 1519.1239 | 1532.6527 | 1527.5732 |
| 3.8974 | 1577.5516 | 1523.5407 | 1518.5194 |
| 3.9084 | 1550.8338 | 1514.4306 | 1509.4655 |
| 3.9194 | 1599.7316 | 1505.3225 | 1500.4116 |
| 3.9304 | 1553.1140 | 1496.2162 | 1491.3577 |
| 3.9414 | 1484.4671 | 1487.1118 | 1482.3038 |
| 3.9524 | 1517.2035 | 1478.0091 | 1473.2499 |
| 3.9634 | 1437.5536 | 1468.9082 | 1464.1960 |
| 3.9744 | 1425.2055 | 1459.8089 | 1455.1421 |
| 3.9854 | 1456.4071 | 1450.7113 | 1446.0882 |
| 3.9964 | 1405.1013 | 1441.6152 | 1437.0344 |
| 4.0074 | 1411.2419 | 1432.5207 | 1427.9805 |
| 4.0184 | 1441.4985 | 1423.4277 | 1418.9266 |
| 4.0294 | 1418.6755 | 1414.3362 | 1409.8727 |
| 4.0404 | 1366.1569 | 1405.2461 | 1400.8188 |
| 4.0514 | 1403.2773 | 1396.1574 | 1391.7649 |
| 4.0624 | 1390.1937 | 1387.0143 | 1382.7110 |
| 4.0734 | 1388.0285 | 1377.8718 | 1373.5448 |
| 4.0844 | 1385.7212 | 1368.6748 | 1364.3786 |
| 4.0954 | 1375.8348 | 1359.4790 | 1355.2123 |
| 4.1064 | 1305.0536 | 1350.2846 | 1346.0461 |
| 4.1174 | 1283.4779 | 1341.0913 | 1336.8798 |
| 4.1284 | 1296.1165 | 1331.8993 | 1327.7136 |
| 4.1394 | 1290.3107 | 1322.7085 | 1318.5474 |
| 4.1504 | 1283.1578 | 1313.5188 | 1309.3811 |
| 4.1614 | 1294.2724 | 1304.3303 | 1300.2149 |
| 4.1724 | 1270.7704 | 1295.1429 | 1291.0487 |
| 4.1834 | 1215.0885 | 1285.9567 | 1281.8824 |
| 4.1944 | 1178.2846 | 1276.7715 | 1272.7162 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 28 SS2 ground 400C | 2.0054 | 29.9894 | 0.0110 | 12/19/2023 8:08:48 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7119 | 314.86 | 0.3464 | 32.55205 | 43.60 |
| 5.3067 | 113.45 | 0.1732 | 16.63956 | 15.71 |
| 7.1451 | 293.06 | 0.5196 | 12.36198 | 40.58 |
| 8.7364 | 406.29 | 0.1299 | 10.11353 | 56.25 |
| 13.6007 | 51.73 | 0.1299 | 6.50535 | 7.16 |
| 15.7765 | 559.14 | 0.0866 | 5.61272 | 77.42 |
| 17.6199 | 38.31 | 0.1732 | 5.02946 | 5.30 |
| 18.2364 | 56.23 | 0.1299 | 4.86079 | 7.79 |
| 19.5531 | 27.05 | 0.6061 | 4.53634 | 3.75 |
| 24.2195 | 23.24 | 0.2598 | 3.67186 | 3.22 |
| 25.9607 | 300.90 | 0.1948 | 3.42939 | 41.66 |
| 26.7472 | 256.55 | 0.0866 | 3.33030 | 35.52 |
| 27.5107 | 722.23 | 0.0866 | 3.23959 | 100.00 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-024-8347 | 60 | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | K0.19 Na7.69 Ca0.06 Al8 Si16 O48 ( H2 O )8 | Analcime | 13 |
| * | 04-016-2838 | 57 | Titanium Oxide | Ti O2 | Rutile | 15 |
| * | 04-006-1757 | 37 | Silicon Oxide | Si O2 | Quartz | 7 |
| * | 04-017-4317 | 29 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 10 |
| * | 04-017-7286 | 23 | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | K0.8 Mn4 Al1.08 Si4.92 O16 ( O H )2 ( H2 O )3 | Ganophyllite | 2 |
| * | 04-025-4215 | 9 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 12 |
| * | 04-013-2099 | 15 | Potassium Aluminum Silicate | K8 Al8 Si16 O48 | Leucite | 10 |
| * | 04-012-1565 | 14 | Potassium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K Mg1.9 Ti0.3 Fe0.5 Al1.2 Si2.8 O10.7 ( O H ) F0.3 | Phlogopite-1M, Fe+2-bearing | 25 |
| * | 04-015-2963 | 8 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 3 |
| * | 04-016-3203 | 9 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 3 |

Anchor Scan Parameters

Dataset Name	28 SS2 ground 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 28\28 SS2 ground 400C.xrdml

Sample Identification	28 SS2 ground

Measurement Start Date/Time	12/19/2023 8:08:48 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes