29 RS1_63 um 400 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	9.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	12.0

Phase Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	17.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	46.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	9.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 29 RS1 _63um 400C | 9.0 | 12.0 | 3.0 | 17.0 | 4.0 | 46.0 | 9.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6757.0000 | 6746.6600 | 6757.0000 |
| 2.0164 | 6965.3206 | 6720.2563 | 6714.4509 |
| 2.0274 | 6752.8269 | 6677.9096 | 6671.9018 |
| 2.0384 | 6856.3717 | 6635.5736 | 6629.3528 |
| 2.0494 | 6627.4602 | 6593.2491 | 6586.8037 |
| 2.0604 | 6563.8550 | 6550.9369 | 6544.2546 |
| 2.0714 | 6625.3156 | 6508.6380 | 6501.7055 |
| 2.0824 | 6473.0551 | 6466.3532 | 6459.1565 |
| 2.0934 | 6537.1839 | 6424.0838 | 6416.6074 |
| 2.1044 | 6446.7389 | 6381.8309 | 6374.0583 |
| 2.1154 | 6505.4464 | 6339.5958 | 6331.5092 |
| 2.1264 | 6414.2119 | 6297.3800 | 6288.9602 |
| 2.1374 | 6343.6932 | 6255.1851 | 6246.4111 |
| 2.1484 | 6272.1849 | 6213.0129 | 6203.8620 |
| 2.1594 | 6313.4484 | 6170.8652 | 6161.3129 |
| 2.1704 | 6235.8215 | 6128.7444 | 6118.7639 |
| 2.1814 | 6276.8161 | 6086.6527 | 6076.2148 |
| 2.1924 | 6285.0610 | 6044.5372 | 6033.6657 |
| 2.2034 | 6153.4248 | 6002.4193 | 5990.9678 |
| 2.2144 | 6183.4789 | 5960.2839 | 5948.2699 |
| 2.2254 | 6191.1770 | 5918.1905 | 5905.5720 |
| 2.2364 | 6077.2596 | 5876.1434 | 5862.8742 |
| 2.2474 | 6078.0157 | 5834.1474 | 5820.1763 |
| 2.2584 | 6009.2153 | 5792.2079 | 5777.4784 |
| 2.2694 | 5977.2507 | 5750.3310 | 5734.7805 |
| 2.2804 | 5922.6416 | 5708.5238 | 5692.0826 |
| 2.2914 | 5848.9607 | 5666.7942 | 5649.3847 |
| 2.3024 | 5780.3540 | 5625.1514 | 5606.6868 |
| 2.3134 | 5777.5388 | 5583.6059 | 5563.9889 |
| 2.3244 | 5768.6136 | 5542.1700 | 5521.2910 |
| 2.3354 | 5759.1298 | 5500.8581 | 5478.5931 |
| 2.3464 | 5798.3314 | 5459.6872 | 5435.8952 |
| 2.3574 | 5745.6018 | 5418.6777 | 5393.1974 |
| 2.3684 | 5725.4764 | 5377.8551 | 5350.4995 |
| 2.3794 | 5707.4651 | 5337.2061 | 5307.8016 |
| 2.3904 | 5675.2375 | 5296.7879 | 5264.9833 |
| 2.4014 | 5682.4513 | 5256.6421 | 5222.1650 |
| 2.4124 | 5621.0172 | 5216.8924 | 5179.3467 |
| 2.4234 | 5548.1032 | 5177.6491 | 5136.5284 |
| 2.4344 | 5395.9086 | 5139.0690 | 5093.7102 |
| 2.4454 | 5430.5221 | 5101.3730 | 5050.8919 |
| 2.4564 | 5472.3623 | 5064.8684 | 5008.0736 |
| 2.4674 | 5508.1711 | 5029.9729 | 4965.2553 |
| 2.4784 | 5428.5137 | 4997.2370 | 4922.4370 |
| 2.4894 | 5321.1121 | 4967.3600 | 4879.6187 |
| 2.5004 | 5413.1770 | 4941.1917 | 4836.8004 |
| 2.5114 | 5357.0491 | 4919.7114 | 4793.9822 |
| 2.5224 | 5291.0393 | 4903.9780 | 4751.1639 |
| 2.5334 | 5240.4336 | 4895.0445 | 4708.3456 |
| 2.5444 | 5264.6804 | 4893.8380 | 4665.5273 |
| 2.5554 | 5231.6499 | 4901.0095 | 4622.7090 |
| 2.5664 | 5173.1047 | 4916.7601 | 4579.8907 |
| 2.5774 | 5099.9734 | 4940.6484 | 4537.0724 |
| 2.5884 | 5067.5143 | 4971.3717 | 4494.2542 |
| 2.5994 | 5006.6195 | 5006.5068 | 4451.4359 |
| 2.6104 | 5003.0683 | 5042.2087 | 4408.6176 |
| 2.6214 | 4953.6765 | 5072.9635 | 4365.7993 |
| 2.6324 | 4920.7965 | 5091.6979 | 4322.9810 |
| 2.6434 | 4901.1780 | 5090.7214 | 4280.1627 |
| 2.6544 | 4914.3048 | 5063.7193 | 4237.3444 |
| 2.6654 | 4805.4808 | 5008.0679 | 4194.5262 |
| 2.6764 | 4817.2326 | 4925.9499 | 4151.7079 |
| 2.6874 | 4720.6932 | 4823.3930 | 4108.8896 |
| 2.6984 | 4603.6947 | 4708.0160 | 4066.0713 |
| 2.7094 | 4531.2291 | 4586.9875 | 4023.2530 |
| 2.7204 | 4473.2606 | 4465.9897 | 3980.4347 |
| 2.7314 | 4480.6578 | 4349.0390 | 3937.6165 |
| 2.7424 | 4485.0000 | 4238.7031 | 3894.7982 |
| 2.7534 | 4321.1848 | 4136.3527 | 3851.9799 |
| 2.7644 | 4233.8746 | 4042.5303 | 3809.0412 |
| 2.7754 | 4129.3589 | 3957.0824 | 3766.1025 |
| 2.7864 | 4106.1460 | 3879.4451 | 3723.1638 |
| 2.7974 | 4018.2743 | 3808.7152 | 3680.2252 |
| 2.8084 | 3908.3028 | 3743.8481 | 3637.2865 |
| 2.8194 | 3840.6086 | 3683.7823 | 3594.3478 |
| 2.8304 | 3912.4336 | 3627.5275 | 3551.4091 |
| 2.8414 | 3666.7876 | 3574.2189 | 3508.4704 |
| 2.8524 | 3746.4803 | 3523.1409 | 3465.5318 |
| 2.8634 | 3630.2448 | 3473.7272 | 3422.5931 |
| 2.8744 | 3505.5678 | 3425.5465 | 3379.6544 |
| 2.8854 | 3240.4464 | 3378.2805 | 3336.7157 |
| 2.8964 | 3385.3363 | 3331.6995 | 3293.7770 |
| 2.9074 | 3319.4887 | 3285.6405 | 3250.8384 |
| 2.9184 | 3252.2183 | 3239.9885 | 3207.8997 |
| 2.9294 | 3118.7522 | 3194.6618 | 3164.9610 |
| 2.9404 | 3166.8840 | 3156.9942 | 3122.0223 |
| 2.9514 | 3073.6391 | 3116.6283 | 3090.9471 |
| 2.9624 | 2985.0000 | 3083.8449 | 3059.8718 |
| 2.9734 | 2976.5123 | 3051.2256 | 3028.7966 |
| 2.9844 | 2890.3904 | 3018.7494 | 2997.7214 |
| 2.9954 | 2974.3097 | 2986.3989 | 2966.6461 |
| 3.0064 | 2911.7202 | 2954.1596 | 2935.5709 |
| 3.0174 | 2864.2153 | 2922.0189 | 2904.4956 |
| 3.0284 | 2853.1342 | 2889.9661 | 2873.4204 |
| 3.0394 | 2808.2124 | 2857.9919 | 2842.3452 |
| 3.0504 | 2760.3648 | 2826.0882 | 2811.2699 |
| 3.0614 | 2779.8024 | 2794.2479 | 2780.1947 |
| 3.0724 | 2718.3574 | 2762.4647 | 2749.1194 |
| 3.0834 | 2602.9086 | 2730.7332 | 2718.0442 |
| 3.0944 | 2620.4823 | 2699.0485 | 2686.9690 |
| 3.1054 | 2605.8358 | 2667.4062 | 2655.8937 |
| 3.1164 | 2588.2768 | 2635.8027 | 2624.8185 |
| 3.1274 | 2613.0029 | 2609.2077 | 2593.7432 |
| 3.1384 | 2574.4371 | 2580.6795 | 2570.6493 |
| 3.1494 | 2584.2950 | 2557.1542 | 2547.5554 |
| 3.1604 | 2511.1475 | 2533.6560 | 2524.4614 |
| 3.1714 | 2485.1426 | 2510.1825 | 2501.3675 |
| 3.1824 | 2508.9700 | 2486.7320 | 2478.2736 |
| 3.1934 | 2490.5664 | 2463.3025 | 2455.1796 |
| 3.2044 | 2495.5452 | 2439.8925 | 2432.0857 |
| 3.2154 | 2449.9105 | 2416.5005 | 2408.9918 |
| 3.2264 | 2385.3569 | 2393.1251 | 2385.8978 |
| 3.2374 | 2382.3894 | 2369.7652 | 2362.8039 |
| 3.2484 | 2342.5000 | 2346.4196 | 2339.7100 |
| 3.2594 | 2287.8496 | 2323.0873 | 2316.6160 |
| 3.2704 | 2276.2011 | 2299.7675 | 2293.5221 |
| 3.2814 | 2231.2380 | 2276.4592 | 2270.4282 |
| 3.2924 | 2248.4469 | 2253.1618 | 2247.3342 |
| 3.3034 | 2239.5359 | 2229.8744 | 2224.2403 |
| 3.3144 | 2187.3913 | 2210.9240 | 2201.1464 |
| 3.3254 | 2173.8968 | 2190.2723 | 2184.9974 |
| 3.3364 | 2182.8707 | 2173.9564 | 2168.8484 |
| 3.3474 | 2168.0000 | 2157.6482 | 2152.6994 |
| 3.3584 | 2172.6062 | 2141.3474 | 2136.5504 |
| 3.3694 | 2167.0423 | 2125.0534 | 2120.4014 |
| 3.3804 | 2129.0354 | 2108.7659 | 2104.2524 |
| 3.3914 | 2071.0796 | 2092.4845 | 2088.1034 |
| 3.4024 | 2042.8781 | 2076.2087 | 2071.9544 |
| 3.4134 | 2031.1082 | 2059.9384 | 2055.8054 |
| 3.4244 | 2059.8894 | 2043.6732 | 2039.6564 |
| 3.4354 | 2057.9017 | 2027.4128 | 2023.5074 |
| 3.4464 | 1982.8682 | 2011.1569 | 2007.3584 |
| 3.4574 | 1920.8584 | 1994.9054 | 1991.2094 |
| 3.4684 | 1886.5934 | 1978.6580 | 1975.0604 |
| 3.4794 | 1910.9381 | 1962.4144 | 1958.9114 |
| 3.4904 | 1914.1770 | 1946.1745 | 1942.7624 |
| 3.5014 | 1991.2911 | 1930.1981 | 1926.6134 |
| 3.5124 | 1914.0059 | 1914.1223 | 1910.8818 |
| 3.5234 | 1829.0649 | 1898.3096 | 1895.1501 |
| 3.5344 | 1854.9651 | 1882.5000 | 1879.4184 |
| 3.5454 | 1850.8191 | 1866.6932 | 1863.6867 |
| 3.5564 | 1796.0855 | 1850.8891 | 1847.9550 |
| 3.5674 | 1786.4533 | 1835.0875 | 1832.2234 |
| 3.5784 | 1806.4253 | 1819.3502 | 1816.4917 |
| 3.5894 | 1835.8673 | 1803.5987 | 1800.7600 |
| 3.6004 | 1783.5526 | 1787.8368 | 1785.0283 |
| 3.6114 | 1750.3156 | 1772.0687 | 1769.2966 |
| 3.6224 | 1723.4100 | 1756.2805 | 1753.5650 |
| 3.6334 | 1726.1908 | 1740.4943 | 1737.8333 |
| 3.6444 | 1717.1922 | 1724.7101 | 1722.1016 |
| 3.6554 | 1705.7198 | 1708.9276 | 1706.3699 |
| 3.6664 | 1659.4906 | 1693.1469 | 1690.6382 |
| 3.6774 | 1658.0777 | 1677.3679 | 1674.9066 |
| 3.6884 | 1644.0310 | 1661.7866 | 1659.1749 |
| 3.6994 | 1701.8191 | 1646.1293 | 1643.7578 |
| 3.7104 | 1632.0654 | 1630.6696 | 1628.3408 |
| 3.7214 | 1523.0855 | 1615.2113 | 1612.9238 |
| 3.7324 | 1669.2591 | 1599.7544 | 1597.5067 |
| 3.7434 | 1549.1219 | 1584.2988 | 1582.0897 |
| 3.7544 | 1581.0797 | 1568.8445 | 1566.6726 |
| 3.7654 | 1560.7689 | 1553.3914 | 1551.2556 |
| 3.7764 | 1581.5349 | 1537.9395 | 1535.8386 |
| 3.7874 | 1530.4602 | 1522.4888 | 1520.4215 |
| 3.7984 | 1455.1721 | 1507.0392 | 1505.0045 |
| 3.8094 | 1505.2675 | 1491.5906 | 1489.5875 |
| 3.8204 | 1520.9631 | 1476.1431 | 1474.1704 |
| 3.8314 | 1481.0491 | 1460.6966 | 1458.7534 |
| 3.8424 | 1390.6298 | 1445.2510 | 1443.3363 |
| 3.8534 | 1452.7551 | 1429.8064 | 1427.9193 |
| 3.8644 | 1403.6072 | 1414.3627 | 1412.5023 |
| 3.8754 | 1379.2055 | 1402.1660 | 1397.0852 |
| 3.8864 | 1414.7743 | 1388.6874 | 1386.8777 |
| 3.8974 | 1360.1249 | 1378.4557 | 1376.6701 |
| 3.9084 | 1425.8196 | 1368.2248 | 1366.4625 |
| 3.9194 | 1386.9498 | 1357.9948 | 1356.2550 |
| 3.9304 | 1364.3776 | 1347.7654 | 1346.0474 |
| 3.9414 | 1343.3471 | 1337.5369 | 1335.8398 |
| 3.9524 | 1336.1386 | 1327.3090 | 1325.6323 |
| 3.9634 | 1311.9902 | 1317.0819 | 1315.4247 |
| 3.9744 | 1297.8058 | 1306.8554 | 1305.2172 |
| 3.9854 | 1336.5044 | 1296.6297 | 1295.0096 |
| 3.9964 | 1310.8417 | 1286.4046 | 1284.8020 |
| 4.0074 | 1320.8102 | 1276.1801 | 1274.5945 |
| 4.0184 | 1276.7832 | 1265.9562 | 1264.3869 |
| 4.0294 | 1245.6155 | 1255.7330 | 1254.1793 |
| 4.0404 | 1245.3323 | 1245.5104 | 1243.9718 |
| 4.0514 | 1235.5870 | 1235.2884 | 1233.7642 |
| 4.0624 | 1240.8117 | 1225.2979 | 1223.5567 |
| 4.0734 | 1194.1072 | 1215.1120 | 1213.6150 |
| 4.0844 | 1207.7832 | 1205.1576 | 1203.6733 |
| 4.0954 | 1211.9410 | 1195.2038 | 1193.7317 |
| 4.1064 | 1197.2139 | 1185.2505 | 1183.7900 |
| 4.1174 | 1190.4454 | 1175.2978 | 1173.8483 |
| 4.1284 | 1166.5826 | 1165.3456 | 1163.9067 |
| 4.1394 | 1159.4680 | 1155.3940 | 1153.9650 |
| 4.1504 | 1133.0000 | 1145.4429 | 1144.0233 |
| 4.1614 | 1131.7729 | 1135.4923 | 1134.0817 |
| 4.1724 | 1134.2134 | 1124.9599 | 1124.1400 |
| 4.1834 | 1104.4424 | 1114.6218 | 1114.1983 |
| 4.1944 | 1099.9165 | 1104.6331 | 1104.2567 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 29 RS1 _63um 400C | 2.0054 | 29.9894 | 0.0110 | 12/19/2023 8:19:15 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6529 | 739.83 | 0.1515 | 33.27653 | 100.00 |
| 5.3144 | 112.95 | 0.1732 | 16.61539 | 15.27 |
| 7.1825 | 153.54 | 0.2165 | 12.29756 | 20.75 |
| 8.7150 | 206.60 | 0.0866 | 10.13823 | 27.93 |
| 15.7610 | 256.16 | 0.0974 | 5.61821 | 34.62 |
| 17.7400 | 2.58 | 0.6927 | 4.99568 | 0.35 |
| 19.6579 | 12.85 | 0.5196 | 4.51240 | 1.74 |
| 25.9154 | 118.94 | 0.1732 | 3.43528 | 16.08 |
| 26.6962 | 76.64 | 0.1732 | 3.33655 | 10.36 |
| 27.4799 | 167.13 | 0.1299 | 3.24316 | 22.59 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-003-0648 | 52 | Titanium Oxide | Ti O2 | Rutile | 9 |
| * | 04-017-4317 | 49 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 12 |
| * | 04-017-7286 | 46 | Potassium Manganese Aluminum Silicon Oxide Hydroxide Hydrate | K0.8 Mn4 Al1.08 Si4.92 O16 ( O H )2 ( H2 O )3 | Ganophyllite | 3 |
| * | 04-011-6751 | 35 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 17 |
| * | 04-014-4556 | 11 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 4 |
| * | 04-025-4215 | 50 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 46 |
| * | 04-017-1305 | 9 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )2 | Palygorskite-M | 9 |

Anchor Scan Parameters

Dataset Name	29 RS1 _63um 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 29\29 RS1 _63um 400C.xrdml

Sample Identification	29 RS1 <63um

Measurement Start Date/Time	12/19/2023 8:19:15 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes