29 RS1_63 um 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	19.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	10.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	66.0

Phase Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- |
| 29 RS1 _63um 550C | 19.0 | 10.0 | 66.0 | 4.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7591.0000 | 7585.0539 | 7591.0000 |
| 2.0164 | 7824.3653 | 7544.2832 | 7540.0496 |
| 2.0274 | 7689.9027 | 7493.4785 | 7489.0991 |
| 2.0384 | 7566.5206 | 7442.6815 | 7438.1487 |
| 2.0494 | 7547.1662 | 7391.8927 | 7387.1982 |
| 2.0604 | 7411.1898 | 7341.1127 | 7336.2478 |
| 2.0714 | 7369.4454 | 7290.3421 | 7285.2974 |
| 2.0824 | 7550.1027 | 7239.5816 | 7234.3469 |
| 2.0934 | 7280.4081 | 7188.8321 | 7183.3965 |
| 2.1044 | 7315.8407 | 7138.0943 | 7132.4460 |
| 2.1154 | 7213.5536 | 7087.3691 | 7081.4956 |
| 2.1264 | 7286.8063 | 7036.6577 | 7030.5452 |
| 2.1374 | 7225.6401 | 6985.9612 | 6979.5947 |
| 2.1484 | 7188.3520 | 6935.2807 | 6928.6443 |
| 2.1594 | 7087.0580 | 6884.6177 | 6877.6938 |
| 2.1704 | 7153.1991 | 6833.9737 | 6826.7434 |
| 2.1814 | 6983.5152 | 6783.3504 | 6775.7930 |
| 2.1924 | 7087.6721 | 6732.7230 | 6724.8425 |
| 2.2034 | 7046.7522 | 6682.0379 | 6673.7561 |
| 2.2144 | 7053.6888 | 6631.3531 | 6622.6697 |
| 2.2254 | 6983.4513 | 6580.6981 | 6571.5832 |
| 2.2364 | 6903.0324 | 6530.0760 | 6520.4968 |
| 2.2474 | 6923.3058 | 6479.4900 | 6469.4104 |
| 2.2584 | 6950.2114 | 6428.9441 | 6418.3240 |
| 2.2694 | 6887.6106 | 6378.4425 | 6367.2375 |
| 2.2804 | 6815.5959 | 6327.9903 | 6316.1511 |
| 2.2914 | 6707.2173 | 6277.5932 | 6265.0647 |
| 2.3024 | 6682.9867 | 6227.2576 | 6213.9783 |
| 2.3134 | 6690.7207 | 6176.9910 | 6162.8918 |
| 2.3244 | 6658.3559 | 6126.8021 | 6111.8054 |
| 2.3354 | 6559.7080 | 6076.7009 | 6060.7190 |
| 2.3464 | 6513.5737 | 6026.6992 | 6009.6326 |
| 2.3574 | 6527.3137 | 5976.8106 | 5958.5461 |
| 2.3684 | 6445.2080 | 5927.0512 | 5907.4597 |
| 2.3794 | 6370.9243 | 5877.4401 | 5856.3733 |
| 2.3904 | 6446.2640 | 5827.9999 | 5805.2869 |
| 2.4014 | 6411.1239 | 5778.7577 | 5754.2004 |
| 2.4124 | 6279.8019 | 5729.7462 | 5703.1140 |
| 2.4234 | 6307.7237 | 5681.0048 | 5652.0276 |
| 2.4344 | 6274.2699 | 5632.5823 | 5600.9412 |
| 2.4454 | 6219.3884 | 5584.5396 | 5549.8547 |
| 2.4564 | 6218.9690 | 5536.9548 | 5498.7683 |
| 2.4674 | 6160.2596 | 5489.9330 | 5447.6819 |
| 2.4784 | 6078.6809 | 5443.6230 | 5396.5955 |
| 2.4894 | 5983.3166 | 5398.2489 | 5345.5090 |
| 2.5004 | 6103.8496 | 5354.1647 | 5294.4226 |
| 2.5114 | 6153.1996 | 5311.9437 | 5243.3362 |
| 2.5224 | 6072.7615 | 5272.5105 | 5192.2498 |
| 2.5334 | 6016.9115 | 5237.3108 | 5141.1633 |
| 2.5444 | 5914.6947 | 5208.4894 | 5090.0769 |
| 2.5554 | 5928.6008 | 5189.0093 | 5038.9905 |
| 2.5664 | 5948.4336 | 5182.5817 | 4987.9041 |
| 2.5774 | 5877.4779 | 5193.3419 | 4936.6817 |
| 2.5884 | 5820.2458 | 5225.3081 | 4885.4593 |
| 2.5994 | 5806.3363 | 5281.1991 | 4834.2368 |
| 2.6104 | 5752.5954 | 5361.1035 | 4783.0144 |
| 2.6214 | 5658.8584 | 5460.9196 | 4731.7920 |
| 2.6324 | 5707.8673 | 5570.4049 | 4680.5696 |
| 2.6434 | 5610.1170 | 5671.0562 | 4629.3472 |
| 2.6544 | 5558.4503 | 5736.0142 | 4578.1248 |
| 2.6654 | 5526.5516 | 5736.9766 | 4526.9024 |
| 2.6764 | 5406.2856 | 5658.8624 | 4475.6800 |
| 2.6874 | 5351.7109 | 5509.9520 | 4424.4576 |
| 2.6984 | 5298.7655 | 5315.8308 | 4373.2352 |
| 2.7094 | 5185.0983 | 5104.7079 | 4322.0128 |
| 2.7204 | 4901.5472 | 4897.9330 | 4270.7903 |
| 2.7314 | 4888.9174 | 4708.3111 | 4219.5679 |
| 2.7424 | 4868.0600 | 4541.8037 | 4168.3455 |
| 2.7534 | 4748.1681 | 4399.4891 | 4117.1231 |
| 2.7644 | 4774.3407 | 4279.4557 | 4065.7326 |
| 2.7754 | 4483.5899 | 4177.9986 | 4014.3421 |
| 2.7864 | 4526.6298 | 4090.9958 | 3962.9516 |
| 2.7974 | 4364.7787 | 4014.5156 | 3911.5611 |
| 2.8084 | 4155.3726 | 3945.3253 | 3860.1706 |
| 2.8194 | 4102.1662 | 3881.0150 | 3808.7802 |
| 2.8304 | 4063.9705 | 3819.9219 | 3757.3897 |
| 2.8414 | 3919.0137 | 3760.9646 | 3705.9992 |
| 2.8524 | 3791.6450 | 3703.4657 | 3654.6087 |
| 2.8634 | 3685.2950 | 3647.0075 | 3603.2182 |
| 2.8744 | 3578.0747 | 3591.3282 | 3551.8277 |
| 2.8854 | 3471.7551 | 3536.2573 | 3500.4372 |
| 2.8964 | 3456.0619 | 3481.6768 | 3449.0467 |
| 2.9074 | 3392.1898 | 3427.5006 | 3397.6562 |
| 2.9184 | 3290.5846 | 3373.6624 | 3346.2657 |
| 2.9294 | 3317.7670 | 3320.1100 | 3294.8752 |
| 2.9404 | 3276.3918 | 3271.9676 | 3243.4847 |
| 2.9514 | 3172.2399 | 3225.5861 | 3203.9804 |
| 2.9624 | 3077.8319 | 3184.5511 | 3164.4761 |
| 2.9734 | 3075.7787 | 3143.6716 | 3124.9717 |
| 2.9844 | 2922.6804 | 3102.9275 | 3085.4674 |
| 2.9954 | 2886.0974 | 3062.3016 | 3045.9631 |
| 3.0064 | 2923.1942 | 3021.7797 | 3006.4588 |
| 3.0174 | 2864.3068 | 2981.3492 | 2966.9545 |
| 3.0284 | 2768.0118 | 2940.9997 | 2927.4501 |
| 3.0394 | 2811.1839 | 2900.7220 | 2887.9458 |
| 3.0504 | 2774.1027 | 2860.5083 | 2848.4415 |
| 3.0614 | 2719.4602 | 2820.3517 | 2808.9372 |
| 3.0724 | 2700.2758 | 2780.2463 | 2769.4329 |
| 3.0834 | 2639.2035 | 2740.1869 | 2729.9285 |
| 3.0944 | 2666.3274 | 2700.1690 | 2690.4242 |
| 3.1054 | 2635.9164 | 2660.1885 | 2650.9199 |
| 3.1164 | 2615.5845 | 2620.2420 | 2611.4156 |
| 3.1274 | 2557.4749 | 2587.9535 | 2571.9113 |
| 3.1384 | 2559.3795 | 2557.9847 | 2549.9533 |
| 3.1494 | 2453.4700 | 2535.6688 | 2527.9953 |
| 3.1604 | 2482.8643 | 2513.3762 | 2506.0373 |
| 3.1714 | 2418.1779 | 2491.1049 | 2484.0793 |
| 3.1824 | 2355.9686 | 2468.8532 | 2462.1213 |
| 3.1934 | 2444.6726 | 2446.6195 | 2440.1633 |
| 3.2044 | 2421.2384 | 2424.4023 | 2418.2053 |
| 3.2154 | 2384.3923 | 2402.2004 | 2396.2473 |
| 3.2264 | 2432.9735 | 2380.0126 | 2374.2894 |
| 3.2374 | 2439.0167 | 2357.8378 | 2352.3314 |
| 3.2484 | 2300.5555 | 2335.6750 | 2330.3734 |
| 3.2594 | 2263.3098 | 2313.5234 | 2308.4154 |
| 3.2704 | 2295.0187 | 2291.3822 | 2286.4574 |
| 3.2814 | 2240.1376 | 2269.2507 | 2264.4994 |
| 3.2924 | 2253.1770 | 2247.1282 | 2242.5414 |
| 3.3034 | 2259.1642 | 2225.0140 | 2220.5834 |
| 3.3144 | 2186.7330 | 2203.9642 | 2198.6254 |
| 3.3254 | 2157.6018 | 2183.2390 | 2179.0978 |
| 3.3364 | 2141.5895 | 2163.5772 | 2159.5702 |
| 3.3474 | 2144.4936 | 2143.9218 | 2140.0425 |
| 3.3584 | 2128.9926 | 2124.2724 | 2120.5149 |
| 3.3694 | 2126.8673 | 2104.6286 | 2100.9873 |
| 3.3804 | 2162.2370 | 2084.9901 | 2081.4596 |
| 3.3914 | 2108.3186 | 2065.3566 | 2061.9320 |
| 3.4024 | 2075.1214 | 2045.7278 | 2042.4044 |
| 3.4134 | 2105.4651 | 2026.1034 | 2022.8767 |
| 3.4244 | 2085.8938 | 2006.4831 | 2003.3491 |
| 3.4354 | 2020.5644 | 1986.8668 | 1983.8215 |
| 3.4464 | 1972.3063 | 1967.2542 | 1964.2938 |
| 3.4574 | 1932.3687 | 1947.6450 | 1944.7662 |
| 3.4684 | 1935.9454 | 1928.0392 | 1925.2386 |
| 3.4794 | 1929.8840 | 1908.4366 | 1905.7109 |
| 3.4904 | 1895.6062 | 1888.8369 | 1886.1833 |
| 3.5014 | 1846.7345 | 1871.7524 | 1866.6556 |
| 3.5124 | 1836.5226 | 1855.4254 | 1852.9076 |
| 3.5234 | 1860.1888 | 1841.6133 | 1839.1596 |
| 3.5344 | 1824.3672 | 1827.8037 | 1825.4116 |
| 3.5454 | 1836.2714 | 1813.9963 | 1811.6636 |
| 3.5564 | 1782.0265 | 1800.1912 | 1797.9156 |
| 3.5674 | 1766.1986 | 1786.3881 | 1784.1675 |
| 3.5784 | 1780.3643 | 1772.5869 | 1770.4195 |
| 3.5894 | 1755.5133 | 1758.7877 | 1756.6715 |
| 3.6004 | 1720.4051 | 1744.9902 | 1742.9235 |
| 3.6114 | 1738.4238 | 1731.1945 | 1729.1755 |
| 3.6224 | 1732.0914 | 1717.4004 | 1715.4274 |
| 3.6334 | 1651.1878 | 1703.6078 | 1701.6794 |
| 3.6444 | 1747.8973 | 1689.8168 | 1687.9314 |
| 3.6554 | 1695.0708 | 1676.0271 | 1674.1834 |
| 3.6664 | 1701.5428 | 1662.2388 | 1660.4354 |
| 3.6774 | 1730.1790 | 1648.4519 | 1646.6874 |
| 3.6884 | 1607.2035 | 1635.0559 | 1632.9393 |
| 3.6994 | 1582.8574 | 1621.7783 | 1620.0880 |
| 3.7104 | 1537.6494 | 1608.8917 | 1607.2367 |
| 3.7214 | 1556.8525 | 1596.0061 | 1594.3854 |
| 3.7324 | 1558.0703 | 1583.1216 | 1581.5341 |
| 3.7434 | 1577.7817 | 1570.2381 | 1568.6829 |
| 3.7544 | 1568.5029 | 1556.2491 | 1555.8316 |
| 3.7654 | 1511.9390 | 1542.9803 | 1542.9803 |
| 3.7764 | 1495.3171 | 1530.1290 | 1530.1290 |
| 3.7874 | 1525.7257 | 1517.2777 | 1517.2777 |
| 3.7984 | 1478.2994 | 1504.4264 | 1504.4264 |
| 3.8094 | 1562.9390 | 1491.5751 | 1491.5751 |
| 3.8204 | 1435.6814 | 1478.7238 | 1478.7238 |
| 3.8314 | 1491.0570 | 1465.8725 | 1465.8725 |
| 3.8424 | 1426.5236 | 1453.0212 | 1453.0212 |
| 3.8534 | 1519.0560 | 1440.1699 | 1440.1699 |
| 3.8644 | 1420.9297 | 1427.3186 | 1427.3186 |
| 3.8754 | 1432.4572 | 1415.3749 | 1414.4673 |
| 3.8864 | 1328.9425 | 1403.7039 | 1403.7039 |
| 3.8974 | 1444.0157 | 1392.9405 | 1392.9405 |
| 3.9084 | 1389.7075 | 1382.1770 | 1382.1770 |
| 3.9194 | 1436.4838 | 1371.4136 | 1371.4136 |
| 3.9304 | 1389.2080 | 1360.6502 | 1360.6502 |
| 3.9414 | 1335.4936 | 1349.8868 | 1349.8868 |
| 3.9524 | 1277.7641 | 1339.1234 | 1339.1234 |
| 3.9634 | 1370.9852 | 1328.3599 | 1328.3599 |
| 3.9744 | 1334.0010 | 1317.5965 | 1317.5965 |
| 3.9854 | 1336.9026 | 1306.8770 | 1306.8331 |
| 3.9964 | 1309.4621 | 1296.2052 | 1296.0697 |
| 4.0074 | 1273.8387 | 1285.4785 | 1285.3063 |
| 4.0184 | 1269.4543 | 1274.7180 | 1274.5428 |
| 4.0294 | 1310.7689 | 1263.9577 | 1263.7794 |
| 4.0404 | 1275.1878 | 1253.1974 | 1253.0160 |
| 4.0514 | 1228.2979 | 1242.4372 | 1242.2526 |
| 4.0624 | 1240.3456 | 1231.8761 | 1231.4892 |
| 4.0734 | 1216.5821 | 1221.3749 | 1221.1836 |
| 4.0844 | 1194.1416 | 1211.0728 | 1210.8780 |
| 4.0954 | 1156.2940 | 1200.7708 | 1200.5724 |
| 4.1064 | 1163.1603 | 1190.4689 | 1190.2668 |
| 4.1174 | 1173.6489 | 1180.1671 | 1179.9612 |
| 4.1284 | 1146.5861 | 1169.8655 | 1169.6556 |
| 4.1394 | 1189.5359 | 1159.5639 | 1159.3500 |
| 4.1504 | 1188.0973 | 1149.2624 | 1149.0444 |
| 4.1614 | 1175.7267 | 1138.9611 | 1138.7387 |
| 4.1724 | 1163.7758 | 1128.6599 | 1128.4331 |
| 4.1834 | 1117.7876 | 1118.3588 | 1118.1275 |
| 4.1944 | 1070.3663 | 1108.0579 | 1107.8219 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 29 RS1 _63um 550C | 2.0054 | 29.9894 | 0.0110 | 12/19/2023 1:52:21 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6651 | 1090.61 | 0.1082 | 33.12372 | 100.00 |
| 5.2836 | 118.74 | 0.1299 | 16.71233 | 10.89 |
| 8.7084 | 178.82 | 0.1948 | 10.14598 | 16.40 |
| 15.7775 | 162.58 | 0.1515 | 5.61238 | 14.91 |
| 25.9738 | 74.34 | 0.3031 | 3.42768 | 6.82 |
| 26.8061 | 26.69 | 0.3031 | 3.32313 | 2.45 |
| 27.5145 | 125.88 | 0.1299 | 3.23915 | 11.54 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-011-6751 | 64 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 19 |
| * | 04-017-4317 | 43 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 10 |
| * | 04-025-4215 | 36 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 66 |
| * | 04-015-8329 | 12 | Sodium Calcium Magnesium Aluminum Iron Silicon Oxide Hydroxide Hydrate | Na0.01 Ca0.01 Mg2.04 Fe0.11 Al2.12 Si7.8 O20 ( O H )2 ( H2 O )8 | Palygorskite-M | 4 |

Anchor Scan Parameters

Dataset Name	29 RS1 _63um 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 29\29 RS1 _63um 550C.xrdml

Sample Identification	29 RS1 <63um 550C

Measurement Start Date/Time	12/19/2023 1:52:21 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes