29 RS1_63 um GLYCOLATED

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	15.0

Phase Titanium Oxide

Weight fraction/ %	2.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	11.0

Phase Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	5.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	11.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	49.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	6.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 29 RS1 _63um glycol | 15.0 | 2.0 | 11.0 | 5.0 | 11.0 | 49.0 | 6.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7096.0000 | 7102.4806 | 7096.0000 |
| 2.0164 | 7085.0000 | 7071.5037 | 7049.6732 |
| 2.0274 | 7083.6480 | 7025.8556 | 7003.3463 |
| 2.0384 | 7028.6726 | 6980.2391 | 6957.0195 |
| 2.0494 | 6990.0177 | 6934.6562 | 6910.6926 |
| 2.0604 | 6909.4970 | 6889.1092 | 6864.3658 |
| 2.0714 | 6849.5841 | 6843.6004 | 6818.0389 |
| 2.0824 | 6760.8264 | 6798.1323 | 6771.7121 |
| 2.0934 | 6677.7365 | 6752.7078 | 6725.3852 |
| 2.1044 | 6725.3850 | 6707.3301 | 6679.0584 |
| 2.1154 | 6810.8761 | 6662.0025 | 6632.7315 |
| 2.1264 | 6655.8392 | 6616.7290 | 6586.4047 |
| 2.1374 | 6645.2389 | 6571.5140 | 6540.0779 |
| 2.1484 | 6498.1740 | 6526.3625 | 6493.7510 |
| 2.1594 | 6597.1072 | 6481.2800 | 6447.4242 |
| 2.1704 | 6573.2507 | 6436.2734 | 6401.0973 |
| 2.1814 | 6517.4395 | 6391.3501 | 6354.7705 |
| 2.1924 | 6525.2847 | 6346.4663 | 6308.4436 |
| 2.2034 | 6394.8407 | 6301.6246 | 6261.9503 |
| 2.2144 | 6318.3776 | 6256.8455 | 6215.4569 |
| 2.2254 | 6268.6106 | 6212.1967 | 6168.9635 |
| 2.2364 | 6368.5133 | 6167.6959 | 6122.4702 |
| 2.2474 | 6321.8368 | 6123.3642 | 6075.9768 |
| 2.2584 | 6325.3289 | 6079.2267 | 6029.4835 |
| 2.2694 | 6342.2153 | 6035.3133 | 5982.9901 |
| 2.2804 | 6319.5472 | 5991.6593 | 5936.4967 |
| 2.2914 | 6254.1888 | 5948.3066 | 5890.0034 |
| 2.3024 | 6137.7035 | 5905.3041 | 5843.5100 |
| 2.3134 | 6138.5516 | 5862.7089 | 5797.0167 |
| 2.3244 | 6097.8604 | 5820.5871 | 5750.5233 |
| 2.3354 | 5984.6490 | 5779.0146 | 5704.0299 |
| 2.3464 | 6012.7606 | 5738.0776 | 5657.5366 |
| 2.3574 | 6015.1593 | 5697.8734 | 5611.0432 |
| 2.3684 | 6052.0074 | 5658.5102 | 5564.5498 |
| 2.3794 | 5987.4956 | 5620.0643 | 5518.0565 |
| 2.3904 | 5891.5207 | 5582.6588 | 5471.4284 |
| 2.4014 | 5860.2832 | 5546.4390 | 5424.8003 |
| 2.4124 | 5843.6677 | 5511.5940 | 5378.1723 |
| 2.4234 | 5779.8820 | 5478.2757 | 5331.5442 |
| 2.4344 | 5716.3496 | 5446.6384 | 5284.9161 |
| 2.4454 | 5784.1268 | 5416.8353 | 5238.2880 |
| 2.4564 | 5777.2439 | 5389.0145 | 5191.6600 |
| 2.4674 | 5775.4779 | 5363.3142 | 5145.0319 |
| 2.4784 | 5715.4031 | 5339.8569 | 5098.4038 |
| 2.4894 | 5699.8161 | 5318.7443 | 5051.7757 |
| 2.5004 | 5692.4071 | 5300.0508 | 5005.1477 |
| 2.5114 | 5543.8722 | 5283.8169 | 4958.5196 |
| 2.5224 | 5589.6190 | 5270.0426 | 4911.8915 |
| 2.5334 | 5615.2242 | 5258.6804 | 4865.2634 |
| 2.5444 | 5610.6013 | 5249.6278 | 4818.6354 |
| 2.5554 | 5542.1406 | 5242.7190 | 4772.0073 |
| 2.5664 | 5442.5236 | 5237.7161 | 4725.3792 |
| 2.5774 | 5419.4435 | 5234.2993 | 4678.7511 |
| 2.5884 | 5335.2689 | 5232.0557 | 4632.1231 |
| 2.5994 | 5364.0089 | 5230.4679 | 4585.4950 |
| 2.6104 | 5443.5885 | 5228.9022 | 4538.8669 |
| 2.6214 | 5350.4307 | 5226.6004 | 4492.2388 |
| 2.6324 | 5212.8274 | 5222.6768 | 4445.6108 |
| 2.6434 | 5158.8909 | 5216.1274 | 4398.9827 |
| 2.6544 | 5151.2748 | 5205.8553 | 4352.3546 |
| 2.6654 | 5086.8407 | 5190.7186 | 4305.7265 |
| 2.6764 | 5150.2217 | 5169.6016 | 4259.0984 |
| 2.6874 | 5012.1121 | 5141.5059 | 4212.4704 |
| 2.6984 | 4833.0088 | 5105.6488 | 4165.8423 |
| 2.7094 | 4817.2389 | 5061.5519 | 4119.2142 |
| 2.7204 | 4749.4995 | 5009.1001 | 4072.5861 |
| 2.7314 | 4774.8053 | 4948.5560 | 4025.9581 |
| 2.7424 | 4659.0044 | 4880.5271 | 3979.3300 |
| 2.7534 | 4504.1239 | 4805.8501 | 3932.7019 |
| 2.7644 | 4445.9248 | 4725.5754 | 3885.9391 |
| 2.7754 | 4324.7099 | 4640.8457 | 3839.1763 |
| 2.7864 | 4320.8353 | 4552.8355 | 3792.4136 |
| 2.7974 | 4171.6725 | 4462.6097 | 3745.6508 |
| 2.8084 | 4068.5560 | 4371.1279 | 3698.8880 |
| 2.8194 | 3992.6037 | 4279.2256 | 3652.1252 |
| 2.8304 | 3916.8628 | 4187.6112 | 3605.3624 |
| 2.8414 | 3720.4395 | 4096.8709 | 3558.5996 |
| 2.8524 | 3790.2842 | 4007.4796 | 3511.8368 |
| 2.8634 | 3535.1917 | 3919.8118 | 3465.0740 |
| 2.8744 | 3486.1313 | 3834.1536 | 3418.3112 |
| 2.8854 | 3377.8220 | 3750.7130 | 3371.5484 |
| 2.8964 | 3408.8540 | 3669.6299 | 3324.7857 |
| 2.9074 | 3328.1740 | 3590.9840 | 3278.0229 |
| 2.9184 | 3222.4479 | 3514.8031 | 3231.2601 |
| 2.9294 | 3148.7847 | 3441.0704 | 3184.4973 |
| 2.9404 | 3195.7365 | 3373.5743 | 3137.7345 |
| 2.9514 | 3062.5133 | 3312.8104 | 3103.0829 |
| 2.9624 | 3062.8200 | 3258.0865 | 3068.4313 |
| 2.9734 | 2953.0816 | 3205.4299 | 3033.7797 |
| 2.9844 | 2954.5634 | 3154.6980 | 2999.1282 |
| 2.9954 | 2945.8761 | 3105.7400 | 2964.4766 |
| 3.0064 | 2822.3790 | 3058.4019 | 2929.8250 |
| 3.0174 | 2790.8771 | 3012.5299 | 2895.1734 |
| 3.0284 | 2809.7139 | 2967.9740 | 2860.5218 |
| 3.0394 | 2792.4641 | 2924.5905 | 2825.8702 |
| 3.0504 | 2710.8501 | 2882.2441 | 2791.2186 |
| 3.0614 | 2705.3864 | 2840.8095 | 2756.5671 |
| 3.0724 | 2605.2350 | 2800.1716 | 2721.9155 |
| 3.0834 | 2558.7729 | 2760.2265 | 2687.2639 |
| 3.0944 | 2560.7212 | 2720.8816 | 2652.6123 |
| 3.1054 | 2590.4985 | 2682.0547 | 2617.9607 |
| 3.1164 | 2595.2404 | 2643.6739 | 2583.3091 |
| 3.1274 | 2550.7316 | 2610.3166 | 2548.6575 |
| 3.1384 | 2521.7320 | 2582.7014 | 2528.6275 |
| 3.1494 | 2449.2173 | 2560.0151 | 2508.5975 |
| 3.1604 | 2448.6829 | 2537.5191 | 2488.5675 |
| 3.1714 | 2442.5890 | 2515.2153 | 2468.5374 |
| 3.1824 | 2405.8117 | 2493.0952 | 2448.5074 |
| 3.1934 | 2433.0885 | 2471.1354 | 2428.4774 |
| 3.2044 | 2446.4410 | 2449.3162 | 2408.4473 |
| 3.2154 | 2447.6460 | 2427.6212 | 2388.4173 |
| 3.2264 | 2366.7286 | 2406.0364 | 2368.3873 |
| 3.2374 | 2382.6873 | 2384.5501 | 2348.3573 |
| 3.2484 | 2347.5000 | 2363.1525 | 2328.3272 |
| 3.2594 | 2285.6932 | 2341.8351 | 2308.2972 |
| 3.2704 | 2300.7492 | 2320.5908 | 2288.2672 |
| 3.2814 | 2274.1593 | 2299.4133 | 2268.2371 |
| 3.2924 | 2292.1150 | 2278.2972 | 2248.2071 |
| 3.3034 | 2260.3835 | 2257.2378 | 2228.1771 |
| 3.3144 | 2190.0496 | 2237.3836 | 2208.1470 |
| 3.3254 | 2173.1947 | 2218.9052 | 2191.7493 |
| 3.3364 | 2142.7895 | 2201.6249 | 2175.3515 |
| 3.3474 | 2091.4799 | 2184.3870 | 2158.9537 |
| 3.3584 | 2126.3304 | 2167.1889 | 2142.5560 |
| 3.3694 | 2122.1809 | 2150.0281 | 2126.1582 |
| 3.3804 | 2093.6632 | 2132.9023 | 2109.7604 |
| 3.3914 | 2095.6195 | 2115.8093 | 2093.3626 |
| 3.4024 | 2066.7325 | 2098.7473 | 2076.9649 |
| 3.4134 | 2045.7453 | 2081.7144 | 2060.5671 |
| 3.4244 | 2006.1563 | 2064.7091 | 2044.1693 |
| 3.4354 | 2007.6745 | 2047.7297 | 2027.7715 |
| 3.4464 | 2001.7139 | 2030.7749 | 2011.3738 |
| 3.4574 | 1976.1534 | 2013.8433 | 1994.9760 |
| 3.4684 | 2001.8314 | 1996.9336 | 1978.5782 |
| 3.4794 | 1967.2399 | 1980.0448 | 1962.1805 |
| 3.4904 | 1927.1327 | 1963.1756 | 1945.7827 |
| 3.5014 | 1947.1918 | 1946.5210 | 1929.3849 |
| 3.5124 | 1911.4449 | 1930.1095 | 1913.6041 |
| 3.5234 | 1886.2153 | 1913.9107 | 1897.8234 |
| 3.5344 | 1880.7493 | 1897.7278 | 1882.0426 |
| 3.5454 | 1860.9813 | 1881.5602 | 1866.2618 |
| 3.5564 | 1888.4528 | 1865.4071 | 1850.4811 |
| 3.5674 | 1866.7148 | 1849.2678 | 1834.7003 |
| 3.5784 | 1820.9071 | 1833.1416 | 1818.9195 |
| 3.5894 | 1766.1150 | 1817.0280 | 1803.1387 |
| 3.6004 | 1762.3864 | 1800.9262 | 1787.3580 |
| 3.6114 | 1764.2055 | 1784.8359 | 1771.5772 |
| 3.6224 | 1774.4882 | 1768.7565 | 1755.7964 |
| 3.6334 | 1745.0560 | 1752.6875 | 1740.0157 |
| 3.6444 | 1656.5260 | 1736.6284 | 1724.2349 |
| 3.6554 | 1595.2861 | 1720.5788 | 1708.4541 |
| 3.6664 | 1695.7055 | 1704.5383 | 1692.6733 |
| 3.6774 | 1707.9223 | 1688.5065 | 1676.8926 |
| 3.6884 | 1677.9425 | 1674.6682 | 1661.1118 |
| 3.6994 | 1579.3608 | 1660.3667 | 1649.2301 |
| 3.7104 | 1661.2267 | 1648.2580 | 1637.3484 |
| 3.7214 | 1656.3215 | 1636.1566 | 1625.4668 |
| 3.7324 | 1648.4921 | 1624.0623 | 1613.5851 |
| 3.7434 | 1553.8013 | 1611.9747 | 1601.7034 |
| 3.7544 | 1582.3540 | 1599.8937 | 1589.8218 |
| 3.7654 | 1571.4346 | 1587.8189 | 1577.9401 |
| 3.7764 | 1622.8796 | 1575.7501 | 1566.0584 |
| 3.7874 | 1590.3009 | 1563.6871 | 1554.1767 |
| 3.7984 | 1581.5491 | 1551.6297 | 1542.2951 |
| 3.8094 | 1452.7778 | 1539.5776 | 1530.4134 |
| 3.8204 | 1562.2905 | 1527.5306 | 1518.5317 |
| 3.8314 | 1503.0403 | 1515.4887 | 1506.6500 |
| 3.8424 | 1502.6848 | 1503.4515 | 1494.7684 |
| 3.8534 | 1480.1681 | 1491.4190 | 1482.8867 |
| 3.8644 | 1494.1440 | 1479.3909 | 1471.0050 |
| 3.8754 | 1468.7690 | 1467.3671 | 1459.1234 |
| 3.8864 | 1544.3628 | 1455.3474 | 1447.2417 |
| 3.8974 | 1426.3953 | 1443.3318 | 1435.3600 |
| 3.9084 | 1434.6391 | 1431.3201 | 1423.4783 |
| 3.9194 | 1368.2684 | 1419.3121 | 1411.5967 |
| 3.9304 | 1396.7738 | 1407.3078 | 1399.7150 |
| 3.9414 | 1368.1032 | 1395.3070 | 1387.8333 |
| 3.9524 | 1350.8982 | 1383.3096 | 1375.9516 |
| 3.9634 | 1371.6607 | 1371.3155 | 1364.0700 |
| 3.9744 | 1295.9975 | 1359.3246 | 1352.1883 |
| 3.9854 | 1295.3275 | 1347.3368 | 1340.3066 |
| 3.9964 | 1351.9464 | 1335.3520 | 1328.4250 |
| 4.0074 | 1309.0049 | 1323.3701 | 1316.5433 |
| 4.0184 | 1351.4602 | 1311.3911 | 1304.6616 |
| 4.0294 | 1388.8614 | 1299.4149 | 1292.7799 |
| 4.0404 | 1334.8156 | 1287.4413 | 1280.8983 |
| 4.0514 | 1238.1770 | 1275.4704 | 1269.0166 |
| 4.0624 | 1271.2306 | 1264.8723 | 1257.1349 |
| 4.0734 | 1228.5359 | 1253.9812 | 1247.6984 |
| 4.0844 | 1249.7566 | 1244.4629 | 1238.2618 |
| 4.0954 | 1247.1475 | 1234.9468 | 1228.8252 |
| 4.1064 | 1276.8397 | 1225.4331 | 1219.3887 |
| 4.1174 | 1251.2360 | 1215.9217 | 1209.9521 |
| 4.1284 | 1252.1583 | 1206.4124 | 1200.5155 |
| 4.1394 | 1203.5437 | 1196.9053 | 1191.0790 |
| 4.1504 | 1181.2065 | 1187.4004 | 1181.6424 |
| 4.1614 | 1210.2694 | 1177.8974 | 1172.2058 |
| 4.1724 | 1227.4557 | 1168.3965 | 1162.7693 |
| 4.1834 | 1193.1681 | 1158.8976 | 1153.3327 |
| 4.1944 | 1180.3928 | 1149.4007 | 1143.8961 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 29 RS1 _63um glycol | 2.0054 | 29.9894 | 0.0110 | 12/20/2023 1:00:32 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7050 | 841.24 | 0.3031 | 32.63494 | 100.00 |
| 5.3028 | 116.75 | 0.2165 | 16.65182 | 13.88 |
| 7.0191 | 174.02 | 0.1732 | 12.58349 | 20.69 |
| 8.7316 | 207.53 | 0.1732 | 10.11898 | 24.67 |
| 15.7419 | 370.89 | 0.0758 | 5.62500 | 44.09 |
| 17.5991 | 19.64 | 0.3464 | 5.03535 | 2.33 |
| 18.1810 | 70.02 | 0.0649 | 4.87549 | 8.32 |
| 19.4615 | 13.86 | 0.5196 | 4.55748 | 1.65 |
| 25.8925 | 366.75 | 0.0649 | 3.43827 | 43.60 |
| 26.6486 | 66.17 | 0.2598 | 3.34240 | 7.87 |
| 27.4997 | 58.80 | 0.1732 | 3.24086 | 6.99 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-070-1575 | 35 | Sodium Aluminum Silicate Hydrate | Na ( Al Si2 O6 ) ( H2 O ) | Analcime | 15 |
| * | 04-016-2838 | 31 | Titanium Oxide | Ti O2 | Rutile | 2 |
| * | 04-017-4317 | 27 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 11 |
| * | 04-016-0693 | 24 | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | K0.3 Na0.4 Ca0.3 Mn3.9 Fe0.1 Al1.4 Si5.3 O16 ( O H )2.7 ( H2 O )3.5 | Ganophyllite | 5 |
| * | 01-073-1660 | 8 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 ( Al Si3 O10 ) ( O H ) F | Phlogopite | 11 |
| * | 04-025-4215 | 19 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 49 |
| * | 04-015-2963 | 6 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 6 |

Anchor Scan Parameters

Dataset Name	29 RS1 _63um glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 29\29 RS1 _63um glycol.xrdml

Sample Identification	29 RS1 <63um glycol

Measurement Start Date/Time	12/20/2023 1:00:32 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes