29 RS1_63 um regular

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	6.0

Phase Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	6.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	5.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	36.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	41.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	1.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	1.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Silicate Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 29 RS1 _63um | 6.0 | 3.0 | 6.0 | 5.0 | 36.0 | 41.0 | 1.0 | 1.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7062.0000 | 7058.1362 | 7062.0000 |
| 2.0164 | 6848.1844 | 7026.3797 | 7016.0674 |
| 2.0274 | 6859.6814 | 6980.8358 | 6970.1349 |
| 2.0384 | 6727.6681 | 6935.3142 | 6924.2023 |
| 2.0494 | 6725.3422 | 6889.8165 | 6878.2697 |
| 2.0604 | 6829.6863 | 6844.3447 | 6832.3371 |
| 2.0714 | 6559.9558 | 6798.9007 | 6786.4046 |
| 2.0824 | 6683.7955 | 6753.4868 | 6740.4720 |
| 2.0934 | 6668.8368 | 6708.1057 | 6694.5394 |
| 2.1044 | 6632.7389 | 6662.7599 | 6648.6068 |
| 2.1154 | 6504.7040 | 6617.4527 | 6602.6743 |
| 2.1264 | 6514.9415 | 6572.1874 | 6556.7417 |
| 2.1374 | 6467.9145 | 6526.9678 | 6510.8091 |
| 2.1484 | 6526.0467 | 6481.7981 | 6464.8765 |
| 2.1594 | 6504.3019 | 6436.6830 | 6418.9440 |
| 2.1704 | 6496.4233 | 6391.6279 | 6373.0114 |
| 2.1814 | 6371.9666 | 6346.6385 | 6327.0788 |
| 2.1924 | 6389.4027 | 6301.6812 | 6281.1463 |
| 2.2034 | 6423.4513 | 6256.7504 | 6235.0795 |
| 2.2144 | 6356.1145 | 6211.8678 | 6189.0127 |
| 2.2254 | 6182.9902 | 6167.0834 | 6142.9459 |
| 2.2364 | 6260.0295 | 6122.4085 | 6096.8791 |
| 2.2474 | 6207.5359 | 6077.8559 | 6050.8123 |
| 2.2584 | 6150.0556 | 6033.4409 | 6004.7455 |
| 2.2694 | 6104.9882 | 5989.1817 | 5958.6787 |
| 2.2804 | 6170.4125 | 5945.1004 | 5912.6119 |
| 2.2914 | 6095.8781 | 5901.2247 | 5866.5451 |
| 2.3024 | 6055.9115 | 5857.5896 | 5820.4783 |
| 2.3134 | 6064.6824 | 5814.2414 | 5774.4115 |
| 2.3244 | 5973.2768 | 5771.2412 | 5728.3447 |
| 2.3354 | 5971.6785 | 5728.6718 | 5682.2779 |
| 2.3464 | 6022.8014 | 5686.6452 | 5636.2111 |
| 2.3574 | 5939.5939 | 5645.3135 | 5590.1443 |
| 2.3684 | 5887.9292 | 5604.8805 | 5544.0775 |
| 2.3794 | 5838.0000 | 5565.6162 | 5498.0107 |
| 2.3904 | 5884.4602 | 5527.8710 | 5451.9439 |
| 2.4014 | 5865.9115 | 5492.0883 | 5405.8771 |
| 2.4124 | 5734.9852 | 5458.8132 | 5359.8103 |
| 2.4234 | 5640.6175 | 5428.6933 | 5313.7435 |
| 2.4344 | 5610.9100 | 5402.4685 | 5267.6767 |
| 2.4454 | 5656.4081 | 5380.9452 | 5221.6099 |
| 2.4564 | 5646.8820 | 5364.9536 | 5175.5431 |
| 2.4674 | 5628.3864 | 5355.2860 | 5129.4763 |
| 2.4784 | 5611.7871 | 5352.6177 | 5083.4095 |
| 2.4894 | 5602.1632 | 5357.4136 | 5037.3427 |
| 2.5004 | 5559.1991 | 5369.8228 | 4991.2759 |
| 2.5114 | 5536.5693 | 5389.5640 | 4945.2091 |
| 2.5224 | 5448.7945 | 5415.7977 | 4899.1423 |
| 2.5334 | 5329.8024 | 5446.9789 | 4853.0755 |
| 2.5444 | 5357.2262 | 5480.6843 | 4807.0087 |
| 2.5554 | 5375.4907 | 5513.4355 | 4760.9419 |
| 2.5664 | 5388.3274 | 5540.5615 | 4714.8751 |
| 2.5774 | 5395.6912 | 5556.4276 | 4668.6740 |
| 2.5884 | 5328.4631 | 5555.0780 | 4622.4730 |
| 2.5994 | 5296.9912 | 5531.4320 | 4576.2720 |
| 2.6104 | 5275.0157 | 5482.6324 | 4530.0710 |
| 2.6214 | 5224.7670 | 5409.0210 | 4483.8699 |
| 2.6324 | 5212.6047 | 5314.0200 | 4437.6689 |
| 2.6434 | 5071.7109 | 5203.0377 | 4391.4679 |
| 2.6544 | 5013.2748 | 5082.0497 | 4345.2669 |
| 2.6654 | 5032.9115 | 4956.5072 | 4299.0658 |
| 2.6764 | 4968.0236 | 4830.8071 | 4252.8648 |
| 2.6874 | 5007.2498 | 4708.2010 | 4206.6638 |
| 2.6984 | 4817.1548 | 4590.9193 | 4160.4628 |
| 2.7094 | 4674.9774 | 4480.3513 | 4114.2617 |
| 2.7204 | 4633.0270 | 4377.2122 | 4068.0607 |
| 2.7314 | 4570.4041 | 4281.6864 | 4021.8597 |
| 2.7424 | 4554.5295 | 4193.5520 | 3975.6587 |
| 2.7534 | 4403.5575 | 4112.2435 | 3929.4576 |
| 2.7644 | 4350.2537 | 4037.0384 | 3883.0907 |
| 2.7754 | 4276.3097 | 3967.1475 | 3836.7238 |
| 2.7864 | 4241.4380 | 3901.7908 | 3790.3568 |
| 2.7974 | 3954.8141 | 3840.1727 | 3743.9899 |
| 2.8084 | 4064.2513 | 3781.5706 | 3697.6229 |
| 2.8194 | 3861.8013 | 3725.3572 | 3651.2560 |
| 2.8304 | 3838.1563 | 3671.0085 | 3604.8891 |
| 2.8414 | 3806.2399 | 3618.1008 | 3558.5221 |
| 2.8524 | 3623.2355 | 3566.3012 | 3512.1552 |
| 2.8634 | 3540.1386 | 3515.3543 | 3465.7882 |
| 2.8744 | 3556.4199 | 3465.0676 | 3419.4213 |
| 2.8854 | 3400.6578 | 3415.2984 | 3373.0544 |
| 2.8964 | 3324.3274 | 3365.9411 | 3326.6874 |
| 2.9074 | 3313.4818 | 3316.9180 | 3280.3205 |
| 2.9184 | 3123.6328 | 3268.1713 | 3233.9536 |
| 2.9294 | 3203.7463 | 3219.6575 | 3187.5866 |
| 2.9404 | 3218.8864 | 3174.7785 | 3141.2197 |
| 2.9514 | 3062.5516 | 3134.6297 | 3106.2807 |
| 2.9624 | 2995.9322 | 3098.0681 | 3071.3417 |
| 2.9734 | 3076.4316 | 3061.6408 | 3036.4027 |
| 2.9844 | 2936.6903 | 3025.3331 | 3001.4637 |
| 2.9954 | 2941.8495 | 2989.1325 | 2966.5247 |
| 3.0064 | 2854.2798 | 2953.0280 | 2931.5857 |
| 3.0174 | 2882.5604 | 2917.0102 | 2896.6468 |
| 3.0284 | 2756.8525 | 2881.0708 | 2861.7078 |
| 3.0394 | 2734.1160 | 2845.2024 | 2826.7688 |
| 3.0504 | 2729.0944 | 2809.3986 | 2791.8298 |
| 3.0614 | 2779.1298 | 2773.6536 | 2756.8908 |
| 3.0724 | 2646.2679 | 2737.9622 | 2721.9518 |
| 3.0834 | 2654.2733 | 2702.3198 | 2687.0128 |
| 3.0944 | 2620.7257 | 2666.7224 | 2652.0738 |
| 3.1054 | 2565.3373 | 2631.1661 | 2617.1349 |
| 3.1164 | 2538.4499 | 2595.6477 | 2582.1959 |
| 3.1274 | 2585.4071 | 2564.4004 | 2547.2569 |
| 3.1384 | 2519.4577 | 2538.8049 | 2526.4101 |
| 3.1494 | 2513.1386 | 2517.4810 | 2505.5634 |
| 3.1604 | 2470.8378 | 2496.2803 | 2484.7166 |
| 3.1714 | 2455.5831 | 2475.0539 | 2463.8698 |
| 3.1824 | 2428.8909 | 2453.8025 | 2443.0231 |
| 3.1934 | 2403.2035 | 2432.5729 | 2422.1763 |
| 3.2044 | 2365.7807 | 2411.3638 | 2401.3296 |
| 3.2154 | 2417.9843 | 2390.1736 | 2380.4828 |
| 3.2264 | 2414.7920 | 2369.0012 | 2359.6360 |
| 3.2374 | 2393.7660 | 2347.8452 | 2338.7893 |
| 3.2484 | 2361.8889 | 2326.7047 | 2317.9425 |
| 3.2594 | 2274.3186 | 2305.5786 | 2297.0958 |
| 3.2704 | 2252.0197 | 2284.4661 | 2276.2490 |
| 3.2814 | 2297.7335 | 2263.3663 | 2255.4022 |
| 3.2924 | 2287.5177 | 2242.2783 | 2234.5555 |
| 3.3034 | 2222.1848 | 2221.2015 | 2213.7087 |
| 3.3144 | 2185.9715 | 2200.7941 | 2192.8620 |
| 3.3254 | 2138.7551 | 2181.2706 | 2174.2069 |
| 3.3364 | 2141.9518 | 2162.4153 | 2155.5519 |
| 3.3474 | 2157.0265 | 2143.5687 | 2136.8968 |
| 3.3584 | 2099.2920 | 2124.7305 | 2118.2418 |
| 3.3694 | 2060.5664 | 2105.9000 | 2099.5867 |
| 3.3804 | 2082.5738 | 2087.0770 | 2080.9317 |
| 3.3914 | 2074.9823 | 2068.2610 | 2062.2766 |
| 3.4024 | 2021.1957 | 2049.4516 | 2043.6216 |
| 3.4134 | 2039.9813 | 2030.6485 | 2024.9665 |
| 3.4244 | 2053.1903 | 2011.8514 | 2006.3115 |
| 3.4354 | 1997.7601 | 1993.0599 | 1987.6565 |
| 3.4464 | 1913.0885 | 1974.2737 | 1969.0014 |
| 3.4574 | 1930.2832 | 1955.4927 | 1950.3464 |
| 3.4684 | 1979.1372 | 1936.7165 | 1931.6913 |
| 3.4794 | 1910.7129 | 1917.9450 | 1913.0363 |
| 3.4904 | 1903.6018 | 1899.1778 | 1894.3812 |
| 3.5014 | 1883.7197 | 1881.3298 | 1875.7262 |
| 3.5124 | 1835.5934 | 1864.6997 | 1860.1151 |
| 3.5234 | 1832.4425 | 1848.9884 | 1844.5039 |
| 3.5344 | 1772.5305 | 1833.2808 | 1828.8928 |
| 3.5454 | 1768.3432 | 1817.5766 | 1813.2817 |
| 3.5564 | 1799.7242 | 1801.8758 | 1797.6705 |
| 3.5674 | 1790.8574 | 1786.1781 | 1782.0594 |
| 3.5784 | 1797.8796 | 1770.4834 | 1766.4483 |
| 3.5894 | 1719.6194 | 1754.7917 | 1750.8371 |
| 3.6004 | 1710.6441 | 1739.1028 | 1735.2260 |
| 3.6114 | 1694.3432 | 1723.4165 | 1719.6149 |
| 3.6224 | 1741.4410 | 1707.7327 | 1704.0037 |
| 3.6334 | 1713.0462 | 1692.0515 | 1688.3926 |
| 3.6444 | 1631.6711 | 1676.3726 | 1672.7815 |
| 3.6554 | 1690.3983 | 1660.6959 | 1657.1703 |
| 3.6664 | 1701.4322 | 1645.0215 | 1641.5592 |
| 3.6774 | 1617.6489 | 1629.3491 | 1625.9481 |
| 3.6884 | 1629.6549 | 1615.3907 | 1610.3369 |
| 3.6994 | 1553.5388 | 1601.1215 | 1597.8370 |
| 3.7104 | 1579.2994 | 1588.5662 | 1585.3371 |
| 3.7214 | 1563.7345 | 1576.0126 | 1572.8372 |
| 3.7324 | 1559.2109 | 1563.4608 | 1560.3372 |
| 3.7434 | 1612.6932 | 1550.9107 | 1547.8373 |
| 3.7544 | 1604.5487 | 1538.3622 | 1535.3374 |
| 3.7654 | 1482.2124 | 1525.8153 | 1522.8375 |
| 3.7764 | 1554.3511 | 1513.2698 | 1510.3375 |
| 3.7874 | 1524.2832 | 1500.7259 | 1497.8376 |
| 3.7984 | 1527.8623 | 1488.1833 | 1485.3377 |
| 3.8094 | 1488.5978 | 1475.6421 | 1472.8378 |
| 3.8204 | 1523.0295 | 1463.1023 | 1460.3378 |
| 3.8314 | 1419.3953 | 1450.5637 | 1447.8379 |
| 3.8424 | 1403.7901 | 1438.0264 | 1435.3380 |
| 3.8534 | 1386.4779 | 1425.4903 | 1422.8381 |
| 3.8644 | 1445.7512 | 1412.9554 | 1410.3381 |
| 3.8754 | 1383.9843 | 1400.4026 | 1397.8382 |
| 3.8864 | 1391.4557 | 1387.8544 | 1385.3038 |
| 3.8974 | 1368.8859 | 1375.2883 | 1372.7694 |
| 3.9084 | 1367.4946 | 1362.7233 | 1360.2350 |
| 3.9194 | 1357.3451 | 1350.1593 | 1347.7006 |
| 3.9304 | 1321.2827 | 1337.5963 | 1335.1661 |
| 3.9414 | 1350.8368 | 1325.0342 | 1322.6317 |
| 3.9524 | 1347.8938 | 1312.4732 | 1310.0973 |
| 3.9634 | 1327.8584 | 1299.9130 | 1297.5629 |
| 3.9744 | 1301.0084 | 1287.3538 | 1285.0285 |
| 3.9854 | 1346.9115 | 1274.7955 | 1272.4941 |
| 3.9964 | 1266.3481 | 1262.2380 | 1259.9596 |
| 4.0074 | 1277.6352 | 1249.6814 | 1247.4252 |
| 4.0184 | 1284.7920 | 1237.1257 | 1234.8908 |
| 4.0294 | 1249.8466 | 1224.5708 | 1222.3564 |
| 4.0404 | 1243.2463 | 1212.0167 | 1209.8220 |
| 4.0514 | 1166.1416 | 1199.4634 | 1197.2876 |
| 4.0624 | 1174.4449 | 1189.1204 | 1184.7531 |
| 4.0734 | 1191.5428 | 1178.3745 | 1176.2341 |
| 4.0844 | 1190.1814 | 1169.8389 | 1167.7150 |
| 4.0954 | 1195.1760 | 1161.3041 | 1159.1960 |
| 4.1064 | 1159.0320 | 1152.7700 | 1150.6770 |
| 4.1174 | 1181.2832 | 1144.2366 | 1142.1579 |
| 4.1284 | 1170.6991 | 1135.7041 | 1133.6389 |
| 4.1394 | 1156.2409 | 1127.1722 | 1125.1198 |
| 4.1504 | 1134.8378 | 1118.6411 | 1116.6008 |
| 4.1614 | 1167.4543 | 1110.1107 | 1108.0817 |
| 4.1724 | 1149.9331 | 1101.5810 | 1099.5627 |
| 4.1834 | 1124.9027 | 1093.0521 | 1091.0436 |
| 4.1944 | 1102.3530 | 1084.5238 | 1082.5246 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 29 RS1 _63um | 2.0054 | 29.9894 | 0.0110 | 12/13/2023 12:20:53 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6017 | 857.52 | 0.1732 | 33.93111 | 100.00 |
| 5.3202 | 110.39 | 0.2165 | 16.59730 | 12.87 |
| 7.1388 | 164.59 | 0.1732 | 12.37271 | 19.19 |
| 8.6755 | 178.15 | 0.1515 | 10.18437 | 20.77 |
| 15.7026 | 225.09 | 0.0649 | 5.63897 | 26.25 |
| 18.1834 | 29.81 | 0.2598 | 4.87484 | 3.48 |
| 19.5624 | 12.51 | 0.5196 | 4.53422 | 1.46 |
| 25.8444 | 151.35 | 0.0866 | 3.44456 | 17.65 |
| 26.6863 | 104.46 | 0.0866 | 3.33777 | 12.18 |
| 27.4706 | 166.50 | 0.0758 | 3.24423 | 19.42 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-003-0648 | 58 | Titanium Oxide | Ti O2 | Rutile | 6 |
| * | 04-016-0693 | 18 | Potassium Sodium Calcium Manganese Aluminum Iron Silicon Oxide Hydroxide Hydrate | K0.3 Na0.4 Ca0.3 Mn3.9 Fe0.1 Al1.4 Si5.3 O16 ( O H )2.7 ( H2 O )3.5 | Ganophyllite | 3 |
| * | 01-070-1575 | 19 | Sodium Aluminum Silicate Hydrate | Na ( Al Si2 O6 ) ( H2 O ) | Analcime | 6 |
| * | 04-017-4317 | 18 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 5 |
| * | 04-025-4215 | 28 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 36 |
| * | 01-073-1660 | 8 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 ( Al Si3 O10 ) ( O H ) F | Phlogopite | 41 |
| * | 04-015-2963 | 4 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 1 |
| * | 01-080-5015 | 0 | Magnesium Silicate Hydroxide Hydrate | Mg7.18 ( Si12 O30 ) ( O H )4 ( H2 O )4 ( H2 O )6 | Sepiolite | 1 |

Anchor Scan Parameters

Dataset Name	29 RS1 _63um

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 29\29 RS1 _63um.xrdml

Sample Identification	29 RS1 <63um

Measurement Start Date/Time	12/13/2023 12:20:53 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes