3 Etosha 18 SS 0-2 cm S2 400c

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	39.0

Phase Potassium Iron Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	9.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	45.0

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	2.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Iron Magnesium Aluminum Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- |
| 3 Etosha18 SS 0-2cm S2 400C | 39.0 | 9.0 | 45.0 | 2.0 | 4.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 5623.0000 | 5609.2250 | 5623.0000 |
| 2.0164 | 5615.8692 | 5585.1996 | 5585.1996 |
| 2.0274 | 5521.9272 | 5547.3993 | 5547.3993 |
| 2.0384 | 5403.9454 | 5509.5989 | 5509.5989 |
| 2.0494 | 5497.7571 | 5471.7986 | 5471.7986 |
| 2.0604 | 5319.0615 | 5433.9982 | 5433.9982 |
| 2.0714 | 5317.3451 | 5396.1978 | 5396.1978 |
| 2.0824 | 5287.0973 | 5358.3975 | 5358.3975 |
| 2.0934 | 5306.5290 | 5320.5971 | 5320.5971 |
| 2.1044 | 5195.6106 | 5282.7968 | 5282.7968 |
| 2.1154 | 5287.2901 | 5244.9964 | 5244.9964 |
| 2.1264 | 5181.2252 | 5207.1960 | 5207.1960 |
| 2.1374 | 4951.1622 | 5169.3957 | 5169.3957 |
| 2.1484 | 4997.9371 | 5131.5953 | 5131.5953 |
| 2.1594 | 5082.0098 | 5093.7950 | 5093.7950 |
| 2.1704 | 5030.1608 | 5055.9946 | 5055.9946 |
| 2.1814 | 4938.2684 | 5018.1942 | 5018.1942 |
| 2.1924 | 5038.0010 | 4982.5672 | 4980.3939 |
| 2.2034 | 4930.8938 | 4948.5574 | 4948.5574 |
| 2.2144 | 4918.8264 | 4916.7209 | 4916.7209 |
| 2.2254 | 4888.0669 | 4884.8845 | 4884.8845 |
| 2.2364 | 4873.1608 | 4853.0480 | 4853.0480 |
| 2.2474 | 4837.6893 | 4821.2115 | 4821.2115 |
| 2.2584 | 4764.8481 | 4789.3750 | 4789.3750 |
| 2.2694 | 4749.3009 | 4757.5386 | 4757.5386 |
| 2.2804 | 4693.1726 | 4725.7021 | 4725.7021 |
| 2.2914 | 4665.8348 | 4693.8656 | 4693.8656 |
| 2.3024 | 4655.4159 | 4662.0292 | 4662.0292 |
| 2.3134 | 4636.5841 | 4630.1927 | 4630.1927 |
| 2.3244 | 4673.0693 | 4598.3562 | 4598.3562 |
| 2.3354 | 4629.6460 | 4566.5197 | 4566.5197 |
| 2.3464 | 4479.9867 | 4534.6833 | 4534.6833 |
| 2.3574 | 4431.4366 | 4502.8468 | 4502.8468 |
| 2.3684 | 4508.6077 | 4471.0103 | 4471.0103 |
| 2.3794 | 4461.9852 | 4440.1030 | 4439.1738 |
| 2.3904 | 4394.3436 | 4409.8871 | 4409.8871 |
| 2.4014 | 4354.7080 | 4380.6003 | 4380.6003 |
| 2.4124 | 4334.1465 | 4351.3135 | 4351.3135 |
| 2.4234 | 4218.5752 | 4322.0268 | 4322.0268 |
| 2.4344 | 4251.1505 | 4292.7400 | 4292.7400 |
| 2.4454 | 4248.2704 | 4263.4532 | 4263.4532 |
| 2.4564 | 4184.6062 | 4234.1665 | 4234.1665 |
| 2.4674 | 4139.1504 | 4204.8797 | 4204.8797 |
| 2.4784 | 4120.4676 | 4175.5929 | 4175.5929 |
| 2.4894 | 4121.0924 | 4146.3062 | 4146.3062 |
| 2.5004 | 4029.8407 | 4117.0194 | 4117.0194 |
| 2.5114 | 3961.6037 | 4087.7326 | 4087.7326 |
| 2.5224 | 4026.4091 | 4058.4459 | 4058.4459 |
| 2.5334 | 4045.2419 | 4029.1591 | 4029.1591 |
| 2.5444 | 4002.1367 | 3999.8723 | 3999.8723 |
| 2.5554 | 4014.9676 | 3970.5856 | 3970.5856 |
| 2.5664 | 3954.1519 | 3942.5276 | 3941.2988 |
| 2.5774 | 3868.0954 | 3915.3839 | 3915.3839 |
| 2.5884 | 3834.5772 | 3889.4690 | 3889.4690 |
| 2.5994 | 3850.2389 | 3863.5541 | 3863.5541 |
| 2.6104 | 3906.2925 | 3837.6393 | 3837.6393 |
| 2.6214 | 3795.1583 | 3811.7244 | 3811.7244 |
| 2.6324 | 3758.8201 | 3785.8095 | 3785.8095 |
| 2.6434 | 3728.3658 | 3759.8946 | 3759.8946 |
| 2.6544 | 3789.5934 | 3733.9797 | 3733.9797 |
| 2.6654 | 3727.5546 | 3708.0648 | 3708.0648 |
| 2.6764 | 3618.5251 | 3682.1500 | 3682.1500 |
| 2.6874 | 3656.2498 | 3656.2351 | 3656.2351 |
| 2.6984 | 3590.8230 | 3630.3202 | 3630.3202 |
| 2.7094 | 3543.1878 | 3604.4053 | 3604.4053 |
| 2.7204 | 3541.7935 | 3578.4904 | 3578.4904 |
| 2.7314 | 3547.8673 | 3552.5755 | 3552.5755 |
| 2.7424 | 3566.2935 | 3526.6606 | 3526.6606 |
| 2.7534 | 3503.1367 | 3502.3814 | 3500.7458 |
| 2.7644 | 3419.6091 | 3479.3194 | 3479.3194 |
| 2.7754 | 3474.1092 | 3457.8930 | 3457.8930 |
| 2.7864 | 3471.0374 | 3436.4666 | 3436.4666 |
| 2.7974 | 3475.1947 | 3415.0402 | 3415.0402 |
| 2.8084 | 3359.3579 | 3393.6138 | 3393.6138 |
| 2.8194 | 3389.6578 | 3372.1874 | 3372.1874 |
| 2.8304 | 3465.9027 | 3350.7610 | 3350.7610 |
| 2.8414 | 3379.5221 | 3329.3346 | 3329.3346 |
| 2.8524 | 3392.8746 | 3307.9083 | 3307.9083 |
| 2.8634 | 3370.9911 | 3286.4819 | 3286.4819 |
| 2.8744 | 3346.6962 | 3265.0555 | 3265.0555 |
| 2.8854 | 3242.7551 | 3243.6291 | 3243.6291 |
| 2.8964 | 3329.6062 | 3222.2027 | 3222.2027 |
| 2.9074 | 3325.0796 | 3200.7763 | 3200.7763 |
| 2.9184 | 3208.4557 | 3179.3499 | 3179.3499 |
| 2.9294 | 3181.8053 | 3157.9235 | 3157.9235 |
| 2.9404 | 3169.7812 | 3137.3448 | 3136.4971 |
| 2.9514 | 3039.4523 | 3117.3968 | 3117.3968 |
| 2.9624 | 3085.6844 | 3098.2965 | 3098.2965 |
| 2.9734 | 3155.2261 | 3079.1962 | 3079.1962 |
| 2.9844 | 3079.0939 | 3060.0959 | 3060.0959 |
| 2.9954 | 3070.5487 | 3040.9956 | 3040.9956 |
| 3.0064 | 2989.3412 | 3021.8953 | 3021.8953 |
| 3.0174 | 2963.7915 | 3002.7950 | 3002.7950 |
| 3.0284 | 2897.1741 | 2983.6947 | 2983.6947 |
| 3.0394 | 2991.2192 | 2964.5943 | 2964.5943 |
| 3.0504 | 2840.6623 | 2945.4940 | 2945.4940 |
| 3.0614 | 2969.0029 | 2926.3937 | 2926.3937 |
| 3.0724 | 2916.4661 | 2907.2934 | 2907.2934 |
| 3.0834 | 2861.6598 | 2888.1931 | 2888.1931 |
| 3.0944 | 2835.6991 | 2869.0928 | 2869.0928 |
| 3.1054 | 2817.9410 | 2849.9925 | 2849.9925 |
| 3.1164 | 2793.5531 | 2830.8922 | 2830.8922 |
| 3.1274 | 2832.9292 | 2812.2081 | 2811.7919 |
| 3.1384 | 2796.9917 | 2793.8339 | 2793.8339 |
| 3.1494 | 2838.3205 | 2775.8759 | 2775.8759 |
| 3.1604 | 2725.2153 | 2757.9179 | 2757.9179 |
| 3.1714 | 2723.6795 | 2739.9599 | 2739.9599 |
| 3.1824 | 2788.8486 | 2722.0019 | 2722.0019 |
| 3.1934 | 2759.0796 | 2704.0439 | 2704.0439 |
| 3.2044 | 2703.5069 | 2686.0859 | 2686.0859 |
| 3.2154 | 2637.3658 | 2668.1279 | 2668.1279 |
| 3.2264 | 2576.9661 | 2650.1700 | 2650.1700 |
| 3.2374 | 2625.3510 | 2632.2120 | 2632.2120 |
| 3.2484 | 2624.9444 | 2614.2540 | 2614.2540 |
| 3.2594 | 2610.5162 | 2596.2960 | 2596.2960 |
| 3.2704 | 2575.4425 | 2578.3380 | 2578.3380 |
| 3.2814 | 2574.9302 | 2560.3800 | 2560.3800 |
| 3.2924 | 2549.9248 | 2542.4220 | 2542.4220 |
| 3.3034 | 2557.2655 | 2524.4640 | 2524.4640 |
| 3.3144 | 2542.2134 | 2506.5060 | 2506.5060 |
| 3.3254 | 2492.2006 | 2488.5480 | 2488.5480 |
| 3.3364 | 2475.8196 | 2470.5901 | 2470.5901 |
| 3.3474 | 2438.0246 | 2452.6321 | 2452.6321 |
| 3.3584 | 2421.7006 | 2434.6741 | 2434.6741 |
| 3.3694 | 2453.5841 | 2416.7161 | 2416.7161 |
| 3.3804 | 2426.1893 | 2398.7581 | 2398.7581 |
| 3.3914 | 2338.4602 | 2380.8001 | 2380.8001 |
| 3.4024 | 2336.9017 | 2362.8421 | 2362.8421 |
| 3.4134 | 2367.2930 | 2344.8841 | 2344.8841 |
| 3.4244 | 2376.0266 | 2326.9261 | 2326.9261 |
| 3.4354 | 2331.9774 | 2308.9681 | 2308.9681 |
| 3.4464 | 2278.8658 | 2291.0102 | 2291.0102 |
| 3.4574 | 2305.2124 | 2273.0522 | 2273.0522 |
| 3.4684 | 2310.5934 | 2255.0942 | 2255.0942 |
| 3.4794 | 2268.9439 | 2237.1362 | 2237.1362 |
| 3.4904 | 2196.6194 | 2219.1782 | 2219.1782 |
| 3.5014 | 2213.6677 | 2203.0654 | 2201.2202 |
| 3.5124 | 2181.2900 | 2188.3257 | 2188.3257 |
| 3.5234 | 2135.8112 | 2175.4312 | 2175.4312 |
| 3.5344 | 2122.7493 | 2162.5579 | 2162.5367 |
| 3.5454 | 2073.4307 | 2149.7501 | 2149.6422 |
| 3.5564 | 2067.4617 | 2136.8677 | 2136.7477 |
| 3.5674 | 2083.1799 | 2124.0184 | 2123.8532 |
| 3.5784 | 2076.3933 | 2111.1261 | 2110.9587 |
| 3.5894 | 2140.7522 | 2098.2338 | 2098.0643 |
| 3.6004 | 2115.6322 | 2085.3415 | 2085.1698 |
| 3.6114 | 2015.6057 | 2072.4493 | 2072.2753 |
| 3.6224 | 2041.4071 | 2059.5571 | 2059.3808 |
| 3.6334 | 2048.0855 | 2046.6649 | 2046.4863 |
| 3.6444 | 2022.0590 | 2033.7729 | 2033.5918 |
| 3.6554 | 2060.0266 | 2020.8808 | 2020.6973 |
| 3.6664 | 2068.8559 | 2007.9888 | 2007.8028 |
| 3.6774 | 2039.4798 | 1995.0969 | 1994.9083 |
| 3.6884 | 1959.2743 | 1982.1763 | 1982.0138 |
| 3.6994 | 1932.9292 | 1969.3777 | 1969.0406 |
| 3.7104 | 1942.7665 | 1956.5384 | 1956.0675 |
| 3.7214 | 1930.2389 | 1943.5991 | 1943.0943 |
| 3.7324 | 1895.5310 | 1930.6307 | 1930.1211 |
| 3.7434 | 1930.6795 | 1917.6624 | 1917.1479 |
| 3.7544 | 1862.3835 | 1904.6942 | 1904.1748 |
| 3.7654 | 1871.5654 | 1891.7261 | 1891.2016 |
| 3.7764 | 1882.7675 | 1878.7580 | 1878.2284 |
| 3.7874 | 1865.1593 | 1865.7901 | 1865.2552 |
| 3.7984 | 1879.8038 | 1852.8222 | 1852.2821 |
| 3.8094 | 1821.6784 | 1839.8544 | 1839.3089 |
| 3.8204 | 1742.0546 | 1826.8868 | 1826.3357 |
| 3.8314 | 1848.1209 | 1813.9192 | 1813.3625 |
| 3.8424 | 1846.7915 | 1800.9517 | 1800.3894 |
| 3.8534 | 1770.2861 | 1787.9843 | 1787.4162 |
| 3.8644 | 1759.4597 | 1775.0170 | 1774.4430 |
| 3.8754 | 1758.1003 | 1762.0499 | 1761.4698 |
| 3.8864 | 1799.1106 | 1749.0828 | 1748.4967 |
| 3.8974 | 1707.4484 | 1736.1159 | 1735.5235 |
| 3.9084 | 1728.8594 | 1723.1490 | 1722.5503 |
| 3.9194 | 1642.2979 | 1710.1823 | 1709.5771 |
| 3.9304 | 1661.7551 | 1697.2158 | 1696.6040 |
| 3.9414 | 1616.9194 | 1684.2493 | 1683.6308 |
| 3.9524 | 1607.0575 | 1671.2830 | 1670.6576 |
| 3.9634 | 1651.4877 | 1658.3168 | 1657.6844 |
| 3.9744 | 1636.2085 | 1645.3508 | 1644.7113 |
| 3.9854 | 1676.9646 | 1632.3849 | 1631.7381 |
| 3.9964 | 1584.4587 | 1619.4192 | 1618.7649 |
| 4.0074 | 1619.0236 | 1606.4536 | 1605.7918 |
| 4.0184 | 1596.0206 | 1593.4882 | 1592.8186 |
| 4.0294 | 1562.7070 | 1580.5229 | 1579.8454 |
| 4.0404 | 1557.8491 | 1567.5578 | 1566.8722 |
| 4.0514 | 1592.6489 | 1554.5929 | 1553.8991 |
| 4.0624 | 1488.8638 | 1542.6854 | 1540.9259 |
| 4.0734 | 1533.5861 | 1531.5647 | 1530.8539 |
| 4.0844 | 1573.4203 | 1521.5015 | 1520.7818 |
| 4.0954 | 1535.7355 | 1511.4385 | 1510.7098 |
| 4.1064 | 1538.1445 | 1501.3757 | 1500.6378 |
| 4.1174 | 1503.6785 | 1491.3131 | 1490.5658 |
| 4.1284 | 1499.7183 | 1481.2508 | 1480.4938 |
| 4.1394 | 1487.8427 | 1471.1886 | 1470.4217 |
| 4.1504 | 1482.1622 | 1461.1267 | 1460.3497 |
| 4.1614 | 1478.5880 | 1451.0651 | 1450.2777 |
| 4.1724 | 1484.5570 | 1441.0037 | 1440.2057 |
| 4.1834 | 1459.5133 | 1430.9425 | 1430.1337 |
| 4.1944 | 1440.8539 | 1420.8817 | 1420.0616 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 3 Etosha18 SS 0-2cm S2 400C | 2.0054 | 29.9894 | 0.0110 | 12/5/2023 12:10:35 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.2747 | 114.48 | 0.1732 | 16.74042 | 12.49 |
| 7.1587 | 214.19 | 0.3464 | 12.33838 | 23.37 |
| 8.7615 | 346.80 | 0.1299 | 10.08451 | 37.83 |
| 15.7994 | 916.70 | 0.1082 | 5.60464 | 100.00 |
| 17.6667 | 30.31 | 0.2598 | 5.01623 | 3.31 |
| 18.2652 | 130.97 | 0.1515 | 4.85319 | 14.29 |
| 19.6405 | 35.67 | 0.5196 | 4.51635 | 3.89 |
| 24.3113 | 47.46 | 0.2165 | 3.65819 | 5.18 |
| 25.9939 | 587.64 | 0.0974 | 3.42508 | 64.10 |
| 26.7355 | 115.27 | 0.0866 | 3.33174 | 12.57 |
| 27.5379 | 78.53 | 0.1732 | 3.23645 | 8.57 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-076-0143 | 72 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 39 |
| * | 00-042-1437 | 37 | Potassium Iron Magnesium Aluminum Silicate Hydroxide | K ( Mg , Fe )3 ( Al , Fe ) Si3 O10 ( O H , F )2 | Phlogopite-1M, Fe+2-bearing | 9 |
| * | 04-025-4215 | 6 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 45 |
| * | 04-016-6876 | 21 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 2 |
| * | 01-081-8598 | 11 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2 Al2 ) Si8 O20 ( H2 O )4 ( O H )2 ( H2 O )3.84 | Palygorskite-M | 4 |

Anchor Scan Parameters

Dataset Name	3 Etosha18 SS 0-2cm S2 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 3\3 Etosha18 SS 0-2cm S2 400C.xrdml

Sample Identification	3 Etosha18 SS 0-2cm S2 400C

Measurement Start Date/Time	12/5/2023 12:10:35 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes