3 Etosha 18 SS 0-2 cm S2 GLYCOLATED

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Manganese Silicate Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Potassium Magnesium Aluminum Iron Silicon Titanium Oxide

Weight fraction/ %	11.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	8.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	34.0

Phase Potassium Aluminum Silicate Hydroxide

Weight fraction/ %	44.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Manganese Silicate Hydroxide Hydrate | Potassium Magnesium Aluminum Iron Silicon Titanium Oxide | Sodium Aluminum Silicate Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Aluminum Silicate Hydroxide |
| --- | --- | --- | --- | --- | --- |
| 3 Etosha18 SS 0-2 S2 GLYCOLATED | 3.0 | 11.0 | 8.0 | 34.0 | 44.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7829.0000 | 7809.7683 | 7829.0000 |
| 2.0164 | 7742.9307 | 7781.4555 | 7772.6749 |
| 2.0274 | 7657.7375 | 7725.4066 | 7716.3497 |
| 2.0384 | 7695.4808 | 7669.3709 | 7660.0246 |
| 2.0494 | 7896.5477 | 7613.3493 | 7603.6995 |
| 2.0604 | 7515.0118 | 7557.3426 | 7547.3743 |
| 2.0714 | 7717.3481 | 7501.3518 | 7491.0492 |
| 2.0824 | 7555.0831 | 7445.3781 | 7434.7241 |
| 2.0934 | 7396.8161 | 7389.4226 | 7378.3990 |
| 2.1044 | 7489.4735 | 7333.4866 | 7322.0738 |
| 2.1154 | 7432.9440 | 7277.5714 | 7265.7487 |
| 2.1264 | 7409.6785 | 7221.6786 | 7209.4236 |
| 2.1374 | 7424.4661 | 7165.8099 | 7153.0984 |
| 2.1484 | 7308.9479 | 7109.9669 | 7096.7733 |
| 2.1594 | 7327.9518 | 7054.1518 | 7040.4482 |
| 2.1704 | 7207.5649 | 6998.3666 | 6984.1230 |
| 2.1814 | 7239.7483 | 6942.6138 | 6927.7979 |
| 2.1924 | 7128.2679 | 6886.8061 | 6871.4728 |
| 2.2034 | 7180.4425 | 6831.0337 | 6814.9655 |
| 2.2144 | 7142.5742 | 6775.2125 | 6758.4582 |
| 2.2254 | 7269.0600 | 6719.4359 | 6701.9509 |
| 2.2364 | 7133.9292 | 6663.7077 | 6645.4436 |
| 2.2474 | 7050.8722 | 6608.0324 | 6588.9363 |
| 2.2584 | 7077.7134 | 6552.4147 | 6532.4290 |
| 2.2694 | 7046.0649 | 6496.8600 | 6475.9217 |
| 2.2804 | 7039.0162 | 6441.3745 | 6419.4143 |
| 2.2914 | 6950.0039 | 6385.9648 | 6362.9070 |
| 2.3024 | 6862.8009 | 6330.6386 | 6306.3997 |
| 2.3134 | 6943.7080 | 6275.4045 | 6249.8924 |
| 2.3244 | 6868.6131 | 6220.2722 | 6193.3851 |
| 2.3354 | 6809.9853 | 6165.2526 | 6136.8778 |
| 2.3464 | 6901.0978 | 6110.3583 | 6080.3705 |
| 2.3574 | 6784.3736 | 6055.6036 | 6023.8632 |
| 2.3684 | 6617.6726 | 6001.0047 | 5967.3559 |
| 2.3794 | 6666.0157 | 5946.5080 | 5910.8486 |
| 2.3904 | 6646.9056 | 5892.2056 | 5854.1939 |
| 2.4014 | 6664.4425 | 5838.0525 | 5797.5392 |
| 2.4124 | 6602.2419 | 5784.1515 | 5740.8845 |
| 2.4234 | 6486.8328 | 5730.5386 | 5684.2299 |
| 2.4344 | 6529.2006 | 5677.2581 | 5627.5752 |
| 2.4454 | 6561.5782 | 5624.3658 | 5570.9205 |
| 2.4564 | 6452.6617 | 5571.9338 | 5514.2658 |
| 2.4674 | 6506.5339 | 5520.0593 | 5457.6111 |
| 2.4784 | 6509.2665 | 5468.8755 | 5400.9564 |
| 2.4894 | 6443.9794 | 5418.5696 | 5344.3017 |
| 2.5004 | 6424.5796 | 5369.4063 | 5287.6470 |
| 2.5114 | 6470.1082 | 5321.7599 | 5230.9924 |
| 2.5224 | 6530.9322 | 5276.1527 | 5174.3377 |
| 2.5334 | 6355.4690 | 5233.2986 | 5117.6830 |
| 2.5444 | 6217.3525 | 5194.1460 | 5061.0283 |
| 2.5554 | 6213.3019 | 5159.9116 | 5004.3736 |
| 2.5664 | 6171.4941 | 5132.0904 | 4947.7189 |
| 2.5774 | 6191.6568 | 5112.4309 | 4891.0642 |
| 2.5884 | 6093.5777 | 5102.8573 | 4834.4095 |
| 2.5994 | 6125.2301 | 5105.3303 | 4777.7549 |
| 2.6104 | 6109.4272 | 5121.6436 | 4721.1002 |
| 2.6214 | 6108.9735 | 5153.1601 | 4664.4455 |
| 2.6324 | 6096.3776 | 5200.5024 | 4607.7908 |
| 2.6434 | 6049.3559 | 5263.2046 | 4551.1361 |
| 2.6544 | 5970.4597 | 5339.3229 | 4494.4814 |
| 2.6654 | 5794.0826 | 5425.1110 | 4437.8267 |
| 2.6764 | 5767.7409 | 5514.1200 | 4381.1720 |
| 2.6874 | 5732.8014 | 5596.8851 | 4324.5174 |
| 2.6984 | 5692.6726 | 5661.2330 | 4267.8627 |
| 2.7094 | 5540.2605 | 5693.0522 | 4211.2080 |
| 2.7204 | 5522.5708 | 5679.8411 | 4154.5533 |
| 2.7314 | 5255.4336 | 5614.6166 | 4097.8986 |
| 2.7424 | 5104.7089 | 5498.8257 | 4041.2439 |
| 2.7534 | 4975.6755 | 5341.6429 | 3984.5892 |
| 2.7644 | 4786.9277 | 5156.6079 | 3927.7872 |
| 2.7754 | 4609.8761 | 4957.3232 | 3870.9851 |
| 2.7864 | 4427.1750 | 4755.2383 | 3814.1830 |
| 2.7974 | 4257.0973 | 4558.6738 | 3757.3810 |
| 2.8084 | 4159.0423 | 4373.1268 | 3700.5789 |
| 2.8194 | 4029.9410 | 4201.8015 | 3643.7768 |
| 2.8304 | 3882.4911 | 4046.1214 | 3586.9748 |
| 2.8414 | 3721.5408 | 3906.1626 | 3530.1727 |
| 2.8524 | 3666.5187 | 3781.0290 | 3473.3706 |
| 2.8634 | 3476.0944 | 3669.1878 | 3416.5685 |
| 2.8744 | 3425.2763 | 3568.7666 | 3359.7665 |
| 2.8854 | 3283.3903 | 3477.7980 | 3302.9644 |
| 2.8964 | 3236.1991 | 3394.4035 | 3246.1623 |
| 2.9074 | 3098.1957 | 3316.9111 | 3189.3603 |
| 2.9184 | 3244.9282 | 3243.9152 | 3132.5582 |
| 2.9294 | 3046.8702 | 3174.2885 | 3075.7561 |
| 2.9404 | 3038.7945 | 3116.5604 | 3018.9541 |
| 2.9514 | 2944.0383 | 3060.9659 | 2981.2285 |
| 2.9624 | 2853.4734 | 3016.1523 | 2943.5030 |
| 2.9734 | 2742.1829 | 2972.3866 | 2905.7775 |
| 2.9844 | 2767.7645 | 2929.4318 | 2868.0519 |
| 2.9954 | 2670.1681 | 2887.1203 | 2830.3264 |
| 3.0064 | 2670.2842 | 2845.3318 | 2792.6009 |
| 3.0174 | 2603.1003 | 2803.9785 | 2754.8754 |
| 3.0284 | 2628.1298 | 2762.9939 | 2717.1498 |
| 3.0394 | 2570.9607 | 2722.3266 | 2679.4243 |
| 3.0504 | 2552.6883 | 2681.9350 | 2641.6988 |
| 3.0614 | 2552.6460 | 2641.7853 | 2603.9732 |
| 3.0724 | 2458.8117 | 2601.8489 | 2566.2477 |
| 3.0834 | 2431.3392 | 2562.1017 | 2528.5222 |
| 3.0944 | 2466.2832 | 2522.5229 | 2490.7967 |
| 3.1054 | 2385.4769 | 2483.0945 | 2453.0711 |
| 3.1164 | 2411.8274 | 2443.8009 | 2415.3456 |
| 3.1274 | 2400.1799 | 2413.5110 | 2377.6201 |
| 3.1384 | 2358.8702 | 2383.5953 | 2357.9248 |
| 3.1494 | 2282.3304 | 2362.6607 | 2338.2295 |
| 3.1604 | 2293.3997 | 2341.8154 | 2318.5343 |
| 3.1714 | 2320.0973 | 2321.0510 | 2298.8390 |
| 3.1824 | 2284.6003 | 2300.3603 | 2279.1438 |
| 3.1934 | 2219.7610 | 2279.7367 | 2259.4485 |
| 3.2044 | 2166.2930 | 2259.1743 | 2239.7532 |
| 3.2154 | 2222.9036 | 2238.6681 | 2220.0580 |
| 3.2264 | 2194.5206 | 2218.2132 | 2200.3627 |
| 3.2374 | 2172.1298 | 2197.8055 | 2180.6674 |
| 3.2484 | 2193.8333 | 2177.4412 | 2160.9722 |
| 3.2594 | 2187.2891 | 2157.1170 | 2141.2769 |
| 3.2704 | 2121.4902 | 2136.8296 | 2121.5817 |
| 3.2814 | 2103.3166 | 2116.5764 | 2101.8864 |
| 3.2924 | 2043.9955 | 2096.3548 | 2082.1911 |
| 3.3034 | 2009.3255 | 2076.1624 | 2062.4959 |
| 3.3144 | 2078.2208 | 2056.8655 | 2042.8006 |
| 3.3254 | 2048.3097 | 2037.6197 | 2024.8678 |
| 3.3364 | 2016.0285 | 2019.2658 | 2006.9350 |
| 3.3474 | 1995.0590 | 2000.9337 | 1989.0022 |
| 3.3584 | 1954.4484 | 1982.6221 | 1971.0694 |
| 3.3694 | 1945.2232 | 1964.3296 | 1953.1366 |
| 3.3804 | 1930.7276 | 1946.0549 | 1935.2038 |
| 3.3914 | 1906.5310 | 1927.7970 | 1917.2709 |
| 3.4024 | 1922.1942 | 1909.5547 | 1899.3381 |
| 3.4134 | 1921.6047 | 1891.3271 | 1881.4053 |
| 3.4244 | 1893.6578 | 1873.1133 | 1863.4725 |
| 3.4354 | 1860.3146 | 1854.9125 | 1845.5397 |
| 3.4464 | 1833.5088 | 1836.7238 | 1827.6069 |
| 3.4574 | 1801.3687 | 1818.5467 | 1809.6741 |
| 3.4684 | 1764.9587 | 1800.3804 | 1791.7413 |
| 3.4794 | 1754.6470 | 1782.2243 | 1773.8085 |
| 3.4904 | 1753.0221 | 1764.0778 | 1755.8757 |
| 3.5014 | 1745.9557 | 1749.0067 | 1737.9429 |
| 3.5124 | 1721.7999 | 1734.0357 | 1726.2340 |
| 3.5234 | 1710.6077 | 1722.1391 | 1714.5251 |
| 3.5344 | 1679.5364 | 1710.2502 | 1702.8162 |
| 3.5454 | 1628.8004 | 1698.3687 | 1691.1074 |
| 3.5564 | 1696.1003 | 1686.4940 | 1679.3985 |
| 3.5674 | 1677.5536 | 1674.6260 | 1667.6896 |
| 3.5784 | 1596.6022 | 1662.7643 | 1655.9807 |
| 3.5894 | 1549.8230 | 1650.9085 | 1644.2718 |
| 3.6004 | 1574.8525 | 1639.0583 | 1632.5630 |
| 3.6114 | 1593.5339 | 1627.2136 | 1620.8541 |
| 3.6224 | 1582.2847 | 1615.3740 | 1609.1452 |
| 3.6334 | 1597.0197 | 1603.5393 | 1597.4363 |
| 3.6444 | 1553.6121 | 1591.7093 | 1585.7274 |
| 3.6554 | 1502.6608 | 1579.8837 | 1574.0186 |
| 3.6664 | 1516.3987 | 1568.0623 | 1562.3097 |
| 3.6774 | 1611.1652 | 1556.2451 | 1550.6008 |
| 3.6884 | 1547.5132 | 1544.6473 | 1538.8919 |
| 3.6994 | 1528.0718 | 1533.0597 | 1527.6208 |
| 3.7104 | 1426.5324 | 1521.6913 | 1516.3496 |
| 3.7214 | 1418.7522 | 1510.3263 | 1505.0785 |
| 3.7324 | 1464.5551 | 1498.9646 | 1493.8074 |
| 3.7434 | 1454.8122 | 1487.6060 | 1482.5362 |
| 3.7544 | 1409.1490 | 1476.2504 | 1471.2651 |
| 3.7654 | 1395.4012 | 1464.8976 | 1459.9939 |
| 3.7764 | 1416.5349 | 1453.5476 | 1448.7228 |
| 3.7874 | 1356.5398 | 1442.2003 | 1437.4516 |
| 3.7984 | 1427.6593 | 1430.8555 | 1426.1805 |
| 3.8094 | 1329.9597 | 1419.5131 | 1414.9093 |
| 3.8204 | 1390.9248 | 1408.1731 | 1403.6382 |
| 3.8314 | 1421.7502 | 1396.8354 | 1392.3671 |
| 3.8424 | 1390.3692 | 1385.4998 | 1381.0959 |
| 3.8534 | 1359.6372 | 1374.1663 | 1369.8248 |
| 3.8644 | 1340.6175 | 1362.8349 | 1358.5536 |
| 3.8754 | 1348.0895 | 1351.8687 | 1347.2825 |
| 3.8864 | 1348.5929 | 1340.9152 | 1336.7488 |
| 3.8974 | 1337.2438 | 1330.3269 | 1326.2151 |
| 3.9084 | 1270.0506 | 1319.7402 | 1315.6814 |
| 3.9194 | 1234.3393 | 1309.1553 | 1305.1477 |
| 3.9304 | 1297.7178 | 1298.5720 | 1294.6140 |
| 3.9414 | 1228.3864 | 1287.9903 | 1284.0803 |
| 3.9524 | 1245.8200 | 1277.4101 | 1273.5466 |
| 3.9634 | 1207.0148 | 1266.8313 | 1263.0129 |
| 3.9744 | 1249.8019 | 1256.2540 | 1252.4792 |
| 3.9854 | 1261.1770 | 1245.6781 | 1241.9455 |
| 3.9964 | 1222.7345 | 1235.1035 | 1231.4118 |
| 4.0074 | 1156.5359 | 1224.5302 | 1220.8781 |
| 4.0184 | 1195.5516 | 1213.9582 | 1210.3444 |
| 4.0294 | 1155.0315 | 1203.3874 | 1199.8107 |
| 4.0404 | 1197.7630 | 1192.8177 | 1189.2770 |
| 4.0514 | 1199.2537 | 1182.2492 | 1178.7433 |
| 4.0624 | 1148.5811 | 1173.3047 | 1168.2096 |
| 4.0734 | 1153.8928 | 1164.4098 | 1160.9702 |
| 4.0844 | 1149.9071 | 1157.1387 | 1153.7307 |
| 4.0954 | 1136.8879 | 1149.8688 | 1146.4913 |
| 4.1064 | 1109.4277 | 1142.5998 | 1139.2519 |
| 4.1174 | 1140.5162 | 1135.3317 | 1132.0124 |
| 4.1284 | 1152.0678 | 1128.0646 | 1124.7730 |
| 4.1394 | 1105.4739 | 1120.7984 | 1117.5335 |
| 4.1504 | 1065.7124 | 1113.5331 | 1110.2941 |
| 4.1614 | 1088.9538 | 1106.2687 | 1103.0547 |
| 4.1724 | 1124.7016 | 1099.0051 | 1095.8152 |
| 4.1834 | 1149.1593 | 1091.7424 | 1088.5758 |
| 4.1944 | 1100.6642 | 1084.4804 | 1081.3363 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 3 Etosha18 SS 0-2 S2 GLYCOLATED | 2.0054 | 29.9894 | 0.0110 | 12/1/2023 9:47:40 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7219 | 1370.69 | 0.1515 | 32.43240 | 100.00 |
| 6.9969 | 327.07 | 0.4330 | 12.62336 | 23.86 |
| 8.6814 | 569.85 | 0.1082 | 10.17743 | 41.57 |
| 15.6784 | 1222.64 | 0.0974 | 5.64762 | 89.20 |
| 17.5779 | 60.10 | 0.1732 | 5.04138 | 4.38 |
| 18.1294 | 186.71 | 0.0325 | 4.88925 | 13.62 |
| 19.6763 | 56.09 | 0.5196 | 4.50821 | 4.09 |
| 20.7999 | 35.02 | 0.1299 | 4.26715 | 2.55 |
| 23.3324 | 22.29 | 0.2598 | 3.80940 | 1.63 |
| 24.1610 | 35.01 | 0.1299 | 3.68061 | 2.55 |
| 25.8549 | 1080.29 | 0.1082 | 3.44319 | 78.81 |
| 26.6406 | 224.97 | 0.1515 | 3.34339 | 16.41 |
| 27.4589 | 139.35 | 0.1082 | 3.24558 | 10.17 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-089-6415 | 44 | Potassium Manganese Silicate Hydroxide Hydrate | K3.68 Mn15.904 Si25.472 O64 ( O H )9.376 ( H2 O )7.024 | Ganophyllite | 3 |
| * | 04-012-1345 | 38 | Potassium Magnesium Aluminum Iron Silicon Titanium Oxide | K0.9 Mg1.45 Ti0.25 Fe1.25 Al Si3 O12 | Phlogopite-1M, Fe+2-bearing | 11 |
| * | 01-076-0143 | 19 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 8 |
| * | 04-025-4215 | 30 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 34 |
| * | 00-043-0685 | 12 | Potassium Aluminum Silicate Hydroxide | K Al2 ( Si3 Al ) O10 ( O H )2 | Illite-2M2 (NR) | 44 |

Anchor Scan Parameters

Dataset Name	3 Etosha18 SS 0-2 S2 GLYCOLATED

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 3\3 Etosha18 SS 0-2 S2 GLYCOLATED.xrdml

Sample Identification	3 Etosha18 SS 0-2 S2 GLYCOLATED

Measurement Start Date/Time	12/1/2023 9:47:40 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes