3 Etosha 18 SS 0-2 cm S2

Graphics

Graphics

Graphics

Quantitative Results

Phase Silicon Oxide

Weight fraction/ %	6.0

Phase Potassium Sodium Magnesium Iron Silicon Oxide Hydroxide

Weight fraction/ %	21.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	12.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	46.0

Phase Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	5.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	6.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Silicon Oxide | Potassium Sodium Magnesium Iron Silicon Oxide Hydroxide | Sodium Aluminum Silicate Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 3 Etosha18 SS 0-2cm S2 | 6.0 | 21.0 | 12.0 | 4.0 | 46.0 | 5.0 | 6.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8127.0000 | 8124.8727 | 8127.0000 |
| 2.0164 | 7940.2748 | 8084.5730 | 8066.0778 |
| 2.0274 | 7885.3677 | 8024.2630 | 8005.1557 |
| 2.0384 | 8017.2301 | 7963.9836 | 7944.2335 |
| 2.0494 | 7972.5241 | 7903.7370 | 7883.3113 |
| 2.0604 | 7983.6863 | 7843.5253 | 7822.3892 |
| 2.0714 | 7718.3068 | 7783.3510 | 7761.4670 |
| 2.0824 | 7878.0393 | 7723.2168 | 7700.5448 |
| 2.0934 | 7678.9794 | 7663.1255 | 7639.6226 |
| 2.1044 | 7794.5708 | 7603.0803 | 7578.7005 |
| 2.1154 | 7759.1337 | 7543.0847 | 7517.7783 |
| 2.1264 | 7700.1608 | 7483.1423 | 7456.8561 |
| 2.1374 | 7670.3481 | 7423.2573 | 7395.9340 |
| 2.1484 | 7605.2370 | 7363.4342 | 7335.0118 |
| 2.1594 | 7616.4838 | 7303.6781 | 7274.0896 |
| 2.1704 | 7584.5015 | 7243.9943 | 7213.1675 |
| 2.1814 | 7453.6067 | 7184.3888 | 7152.2453 |
| 2.1924 | 7461.6116 | 7124.8246 | 7091.3231 |
| 2.2034 | 7464.8142 | 7065.3072 | 7030.2675 |
| 2.2144 | 7326.2817 | 7005.8465 | 6969.2119 |
| 2.2254 | 7286.7109 | 6946.4956 | 6908.1563 |
| 2.2364 | 7348.1224 | 6887.2646 | 6847.1007 |
| 2.2474 | 7276.6372 | 6828.1651 | 6786.0451 |
| 2.2584 | 7306.5919 | 6769.2097 | 6724.9895 |
| 2.2694 | 7199.9233 | 6710.4131 | 6663.9339 |
| 2.2804 | 7257.0324 | 6651.7918 | 6602.8783 |
| 2.2914 | 7162.0954 | 6593.3650 | 6541.8227 |
| 2.3024 | 7108.1858 | 6535.1549 | 6480.7671 |
| 2.3134 | 7138.5202 | 6477.1879 | 6419.7115 |
| 2.3244 | 7030.8609 | 6419.4960 | 6358.6559 |
| 2.3354 | 7004.7729 | 6362.1182 | 6297.6003 |
| 2.3464 | 7039.8977 | 6305.1035 | 6236.5447 |
| 2.3574 | 6959.1209 | 6248.5143 | 6175.4891 |
| 2.3684 | 6966.5044 | 6192.5099 | 6114.4335 |
| 2.3794 | 6999.1052 | 6137.4920 | 6053.3779 |
| 2.3904 | 6880.9513 | 6082.9793 | 5992.3223 |
| 2.4014 | 6801.4956 | 6029.1919 | 5931.2667 |
| 2.4124 | 6813.1637 | 5976.5716 | 5870.2111 |
| 2.4234 | 6710.6175 | 5925.4237 | 5809.1555 |
| 2.4344 | 6715.4233 | 5876.1367 | 5748.0999 |
| 2.4454 | 6763.9931 | 5829.1973 | 5687.0443 |
| 2.4564 | 6693.6853 | 5785.2018 | 5625.9887 |
| 2.4674 | 6697.8791 | 5744.8646 | 5564.9331 |
| 2.4784 | 6661.8368 | 5709.0176 | 5503.8775 |
| 2.4894 | 6649.2439 | 5678.6003 | 5442.8219 |
| 2.5004 | 6687.0442 | 5654.6362 | 5381.7663 |
| 2.5114 | 6703.3117 | 5638.1932 | 5320.7107 |
| 2.5224 | 6587.4007 | 5630.3276 | 5259.6550 |
| 2.5334 | 6494.3097 | 5632.0113 | 5198.5994 |
| 2.5444 | 6427.5354 | 5644.0443 | 5137.5438 |
| 2.5554 | 6494.0777 | 5666.9550 | 5076.4882 |
| 2.5664 | 6502.3156 | 5700.8477 | 5015.4326 |
| 2.5774 | 6399.1691 | 5745.3712 | 4954.2436 |
| 2.5884 | 6324.8687 | 5799.5513 | 4893.0546 |
| 2.5994 | 6279.7788 | 5861.6837 | 4831.8655 |
| 2.6104 | 6321.7566 | 5929.0781 | 4770.6765 |
| 2.6214 | 6254.3913 | 5997.9148 | 4709.4875 |
| 2.6324 | 6190.9823 | 6063.0821 | 4648.2984 |
| 2.6434 | 6232.6146 | 6118.1455 | 4587.1094 |
| 2.6544 | 6165.9793 | 6155.6262 | 4525.9204 |
| 2.6654 | 6018.6932 | 6167.7741 | 4464.7313 |
| 2.6764 | 5930.0157 | 6147.8622 | 4403.5423 |
| 2.6874 | 5810.3618 | 6091.6979 | 4342.3533 |
| 2.6984 | 5613.8407 | 5998.7413 | 4281.1642 |
| 2.7094 | 5587.2389 | 5872.2626 | 4219.9752 |
| 2.7204 | 5550.6573 | 5718.4506 | 4158.7862 |
| 2.7314 | 5322.5958 | 5544.9365 | 4097.5971 |
| 2.7424 | 5178.9444 | 5359.3856 | 4036.4081 |
| 2.7534 | 4967.6037 | 5168.5140 | 3975.2190 |
| 2.7644 | 4803.6357 | 4977.7971 | 3913.8651 |
| 2.7754 | 4725.0757 | 4791.3908 | 3852.5111 |
| 2.7864 | 4577.2463 | 4612.3228 | 3791.1571 |
| 2.7974 | 4395.9380 | 4442.5746 | 3729.8032 |
| 2.8084 | 4252.9744 | 4283.3126 | 3668.4492 |
| 2.8194 | 4158.0511 | 4135.0401 | 3607.0953 |
| 2.8304 | 3993.2891 | 3997.7297 | 3545.7413 |
| 2.8414 | 3777.2959 | 3870.9434 | 3484.3873 |
| 2.8524 | 3753.5359 | 3753.9432 | 3423.0334 |
| 2.8634 | 3490.3156 | 3645.7937 | 3361.6794 |
| 2.8744 | 3435.3053 | 3545.4531 | 3300.3254 |
| 2.8854 | 3300.2733 | 3451.8499 | 3238.9715 |
| 2.8964 | 3183.5088 | 3363.9438 | 3177.6175 |
| 2.9074 | 3248.7020 | 3280.7696 | 3116.2635 |
| 2.9184 | 3083.2866 | 3201.4646 | 3054.9096 |
| 2.9294 | 2996.9174 | 3125.2827 | 2993.5556 |
| 2.9404 | 2904.1947 | 3060.7778 | 2932.2016 |
| 2.9514 | 2884.1485 | 3007.8038 | 2898.7612 |
| 2.9624 | 2839.4956 | 2965.5782 | 2865.3207 |
| 2.9734 | 2872.6735 | 2924.5937 | 2831.8803 |
| 2.9844 | 2857.7315 | 2884.5969 | 2798.4399 |
| 2.9954 | 2744.5398 | 2845.3932 | 2764.9994 |
| 3.0064 | 2699.1799 | 2806.8342 | 2731.5590 |
| 3.0174 | 2636.6844 | 2768.8067 | 2698.1185 |
| 3.0284 | 2611.4336 | 2731.2242 | 2664.6781 |
| 3.0394 | 2617.2409 | 2694.0198 | 2631.2376 |
| 3.0504 | 2535.8264 | 2657.1415 | 2597.7972 |
| 3.0614 | 2524.4218 | 2620.5479 | 2564.3568 |
| 3.0724 | 2475.5477 | 2584.2053 | 2530.9163 |
| 3.0834 | 2405.6333 | 2548.0861 | 2497.4759 |
| 3.0944 | 2481.2256 | 2512.1670 | 2464.0354 |
| 3.1054 | 2364.3717 | 2476.4281 | 2430.5950 |
| 3.1164 | 2392.9646 | 2440.8522 | 2397.1546 |
| 3.1274 | 2367.4749 | 2410.5239 | 2363.7141 |
| 3.1384 | 2382.1465 | 2385.6347 | 2345.7775 |
| 3.1494 | 2273.0688 | 2365.9682 | 2327.8409 |
| 3.1604 | 2239.7655 | 2346.4141 | 2309.9044 |
| 3.1714 | 2315.1485 | 2326.9631 | 2291.9678 |
| 3.1824 | 2321.6426 | 2307.6066 | 2274.0312 |
| 3.1934 | 2331.2832 | 2288.3372 | 2256.0946 |
| 3.2044 | 2318.2659 | 2269.1479 | 2238.1580 |
| 3.2154 | 2222.7847 | 2250.0326 | 2220.2214 |
| 3.2264 | 2209.5619 | 2230.9857 | 2202.2848 |
| 3.2374 | 2126.9489 | 2212.0020 | 2184.3482 |
| 3.2484 | 2130.7222 | 2193.0769 | 2166.4117 |
| 3.2594 | 2129.0855 | 2174.2062 | 2148.4751 |
| 3.2704 | 2137.5689 | 2155.3861 | 2130.5385 |
| 3.2814 | 2180.4828 | 2136.6129 | 2112.6019 |
| 3.2924 | 2079.4602 | 2117.8836 | 2094.6653 |
| 3.3034 | 2088.0875 | 2099.1952 | 2076.7287 |
| 3.3144 | 2081.3805 | 2081.2228 | 2058.7921 |
| 3.3254 | 2005.8997 | 2063.9912 | 2042.9165 |
| 3.3364 | 2031.8737 | 2047.4709 | 2027.0410 |
| 3.3474 | 2047.0098 | 2030.9819 | 2011.1654 |
| 3.3584 | 2053.8894 | 2014.5222 | 1995.2898 |
| 3.3694 | 2034.8859 | 1998.0900 | 1979.4142 |
| 3.3804 | 1962.2350 | 1981.6836 | 1963.5386 |
| 3.3914 | 1982.9646 | 1965.3015 | 1947.6630 |
| 3.4024 | 1977.9523 | 1948.9424 | 1931.7874 |
| 3.4134 | 1972.9685 | 1932.6048 | 1915.9118 |
| 3.4244 | 1940.4454 | 1916.2875 | 1900.0362 |
| 3.4354 | 1875.0865 | 1899.9894 | 1884.1607 |
| 3.4464 | 1894.9976 | 1883.7094 | 1868.2851 |
| 3.4574 | 1853.8908 | 1867.4465 | 1852.4095 |
| 3.4684 | 1834.0413 | 1851.1999 | 1836.5339 |
| 3.4794 | 1850.8230 | 1834.9685 | 1820.6583 |
| 3.4904 | 1828.9469 | 1818.7518 | 1804.7827 |
| 3.5014 | 1761.6017 | 1803.4641 | 1788.9071 |
| 3.5124 | 1752.7807 | 1789.1415 | 1775.8142 |
| 3.5234 | 1786.0620 | 1775.7467 | 1762.7213 |
| 3.5344 | 1806.2099 | 1762.3636 | 1749.6284 |
| 3.5454 | 1768.9174 | 1748.9918 | 1736.5355 |
| 3.5564 | 1701.6873 | 1735.6307 | 1723.4426 |
| 3.5674 | 1718.7758 | 1722.2797 | 1710.3497 |
| 3.5784 | 1720.3933 | 1708.9383 | 1697.2568 |
| 3.5894 | 1652.3274 | 1695.6062 | 1684.1639 |
| 3.6004 | 1694.7940 | 1682.2829 | 1671.0710 |
| 3.6114 | 1619.8387 | 1668.9680 | 1657.9781 |
| 3.6224 | 1582.2847 | 1655.6610 | 1644.8852 |
| 3.6334 | 1668.2793 | 1642.3618 | 1631.7923 |
| 3.6444 | 1655.5767 | 1629.0698 | 1618.6994 |
| 3.6554 | 1618.6283 | 1615.7849 | 1605.6065 |
| 3.6664 | 1616.4238 | 1602.5066 | 1592.5136 |
| 3.6774 | 1623.9459 | 1589.2347 | 1579.4207 |
| 3.6884 | 1529.0221 | 1577.0469 | 1566.3278 |
| 3.6994 | 1520.4641 | 1565.9863 | 1556.5120 |
| 3.7104 | 1585.2630 | 1556.0092 | 1546.6962 |
| 3.7214 | 1524.1121 | 1546.0375 | 1536.8804 |
| 3.7324 | 1504.0546 | 1536.0709 | 1527.0645 |
| 3.7434 | 1483.2183 | 1526.1094 | 1517.2487 |
| 3.7544 | 1450.5088 | 1516.1527 | 1507.4329 |
| 3.7654 | 1516.6598 | 1506.2006 | 1497.6171 |
| 3.7764 | 1446.5644 | 1496.2529 | 1487.8013 |
| 3.7874 | 1509.4248 | 1486.3094 | 1477.9855 |
| 3.7984 | 1427.1342 | 1476.3701 | 1468.1697 |
| 3.8094 | 1465.3707 | 1466.4346 | 1458.3538 |
| 3.8204 | 1427.0929 | 1456.5030 | 1448.5380 |
| 3.8314 | 1462.6617 | 1446.5751 | 1438.7222 |
| 3.8424 | 1404.9484 | 1436.6507 | 1428.9064 |
| 3.8534 | 1369.6873 | 1426.7297 | 1419.0906 |
| 3.8644 | 1399.4032 | 1416.8119 | 1409.2748 |
| 3.8754 | 1457.7365 | 1406.9468 | 1399.4590 |
| 3.8864 | 1385.7566 | 1397.1361 | 1389.7934 |
| 3.8974 | 1315.0531 | 1387.3778 | 1380.1278 |
| 3.9084 | 1325.3141 | 1377.6224 | 1370.4623 |
| 3.9194 | 1294.3186 | 1367.8697 | 1360.7967 |
| 3.9304 | 1341.7738 | 1358.1197 | 1351.1311 |
| 3.9414 | 1316.2045 | 1348.3723 | 1341.4656 |
| 3.9524 | 1304.3673 | 1338.6274 | 1331.8000 |
| 3.9634 | 1289.7463 | 1328.8849 | 1322.1344 |
| 3.9744 | 1286.4032 | 1319.1448 | 1312.4689 |
| 3.9854 | 1315.6106 | 1309.4069 | 1302.8033 |
| 3.9964 | 1307.6553 | 1299.6713 | 1293.1377 |
| 4.0074 | 1232.3412 | 1289.9377 | 1283.4722 |
| 4.0184 | 1219.2729 | 1280.2063 | 1273.8066 |
| 4.0294 | 1216.4012 | 1270.4769 | 1264.1411 |
| 4.0404 | 1276.1908 | 1260.7494 | 1254.4755 |
| 4.0514 | 1271.6991 | 1251.0238 | 1244.8099 |
| 4.0624 | 1237.0472 | 1241.3001 | 1235.1444 |
| 4.0734 | 1218.4857 | 1231.5781 | 1225.4788 |
| 4.0844 | 1193.6371 | 1221.8579 | 1215.8132 |
| 4.0954 | 1173.9243 | 1212.1394 | 1206.1477 |
| 4.1064 | 1233.1927 | 1202.4225 | 1196.4821 |
| 4.1174 | 1179.9204 | 1192.7073 | 1186.8165 |
| 4.1284 | 1170.9287 | 1182.9936 | 1177.1510 |
| 4.1394 | 1173.6096 | 1173.2814 | 1167.4854 |
| 4.1504 | 1189.8584 | 1163.5707 | 1157.8198 |
| 4.1614 | 1160.1839 | 1153.8615 | 1148.1543 |
| 4.1724 | 1133.0000 | 1144.1537 | 1138.4887 |
| 4.1834 | 1116.5221 | 1134.4472 | 1128.8232 |
| 4.1944 | 1082.5142 | 1124.7421 | 1119.1576 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 3 Etosha18 SS 0-2cm S2 | 2.0054 | 29.9894 | 0.0110 | 11/30/2023 2:13:21 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6812 | 1566.34 | 0.1948 | 32.92497 | 100.00 |
| 7.1318 | 522.37 | 0.4763 | 12.38490 | 33.35 |
| 8.6953 | 540.59 | 0.1732 | 10.16123 | 34.51 |
| 15.6848 | 1192.26 | 0.0866 | 5.64532 | 76.12 |
| 17.5875 | 56.96 | 0.1732 | 5.03866 | 3.64 |
| 18.1464 | 136.64 | 0.1299 | 4.88471 | 8.72 |
| 19.6389 | 64.71 | 0.2598 | 4.51671 | 4.13 |
| 20.8504 | 31.45 | 0.2598 | 4.25694 | 2.01 |
| 23.3390 | 37.02 | 0.2598 | 3.80834 | 2.36 |
| 24.1387 | 45.18 | 0.1732 | 3.68396 | 2.88 |
| 25.8312 | 940.71 | 0.0660 | 3.44628 | 60.06 |
| 25.8764 | 984.47 | 0.0541 | 3.44037 | 62.85 |
| 26.6773 | 216.77 | 0.0866 | 3.33887 | 13.84 |
| 27.4524 | 118.89 | 0.1732 | 3.24633 | 7.59 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-070-7344 | 51 | Silicon Oxide | Si O2 | Quartz | 6 |
| * | 01-087-8929 | 24 | Potassium Sodium Magnesium Iron Silicon Oxide Hydroxide | K1.91 Na0.09 ( Mg2.62 Fe4.004 ) ( Si7.376 O20 ) ( O H )4 | Phlogopite (Fe-rich) | 21 |
| * | 01-072-4625 | 28 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 12 |
| * | 04-014-4556 | 11 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 4 |
| * | 04-025-4215 | 19 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 46 |
| * | 04-016-6876 | 28 | Potassium Calcium Manganese Aluminum Silicate Hydroxide Hydrate | K0.38 Ca0.12 Mn2 Al0.62 Si2.71 O8 ( O H )1.33 ( H2 O )1.75 | Ganophyllite | 5 |
| * | 04-015-2963 | 15 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 6 |

Anchor Scan Parameters

Dataset Name	3 Etosha18 SS 0-2cm S2

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 3\3 Etosha18 SS 0-2cm S2.xrdml

Sample Identification	3 Etosha18 SS 0-2cm S2

Measurement Start Date/Time	11/30/2023 2:13:21 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes