30 RS1 ground 400 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	12.0

Phase Silicon Oxide

Weight fraction/ %	7.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	7.0

Phase Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	10.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	10.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	38.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	1.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	15.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Silicon Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | Potassium Aluminum Silicate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30 RS1 ground 400C | 12.0 | 7.0 | 7.0 | 10.0 | 10.0 | 38.0 | 1.0 | 15.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8532.0000 | 8536.3060 | 8532.0000 |
| 2.0164 | 8580.2011 | 8495.8823 | 8469.2571 |
| 2.0274 | 8516.0246 | 8433.9544 | 8406.5141 |
| 2.0384 | 8509.6254 | 8372.0640 | 8343.7712 |
| 2.0494 | 8321.8673 | 8310.2134 | 8281.0282 |
| 2.0604 | 8411.0221 | 8248.4053 | 8218.2853 |
| 2.0714 | 8336.8437 | 8186.6421 | 8155.5423 |
| 2.0824 | 8347.0084 | 8124.9269 | 8092.7994 |
| 2.0934 | 8231.9105 | 8063.2628 | 8030.0565 |
| 2.1044 | 8401.5133 | 8001.6532 | 7967.3135 |
| 2.1154 | 8074.0334 | 7940.1017 | 7904.5706 |
| 2.1264 | 8082.4435 | 7878.6124 | 7841.8276 |
| 2.1374 | 8208.5959 | 7817.1896 | 7779.0847 |
| 2.1484 | 8090.5836 | 7755.8380 | 7716.3417 |
| 2.1594 | 8015.1750 | 7694.5629 | 7653.5988 |
| 2.1704 | 8065.7139 | 7633.3699 | 7590.8559 |
| 2.1814 | 7958.7660 | 7572.2654 | 7528.1129 |
| 2.1924 | 7975.7178 | 7511.2078 | 7465.3700 |
| 2.2034 | 7810.4071 | 7450.2090 | 7402.4857 |
| 2.2144 | 7765.5447 | 7389.2737 | 7339.6014 |
| 2.2254 | 7817.1288 | 7328.4601 | 7276.7172 |
| 2.2364 | 7840.2906 | 7267.7797 | 7213.8329 |
| 2.2474 | 7822.6381 | 7207.2455 | 7150.9486 |
| 2.2584 | 7727.9671 | 7146.8727 | 7088.0644 |
| 2.2694 | 7663.4985 | 7086.6795 | 7025.1801 |
| 2.2804 | 7734.6146 | 7026.6873 | 6962.2958 |
| 2.2914 | 7653.8712 | 6966.9220 | 6899.4115 |
| 2.3024 | 7503.8894 | 6907.4152 | 6836.5273 |
| 2.3134 | 7530.9420 | 6848.2051 | 6773.6430 |
| 2.3244 | 7470.9602 | 6789.3390 | 6710.7587 |
| 2.3354 | 7554.4631 | 6730.8744 | 6647.8745 |
| 2.3464 | 7602.2114 | 6672.8821 | 6584.9902 |
| 2.3574 | 7363.8535 | 6615.4486 | 6522.1059 |
| 2.3684 | 7261.6549 | 6558.6791 | 6459.2216 |
| 2.3794 | 7208.0118 | 6502.7006 | 6396.3374 |
| 2.3904 | 7277.7965 | 6447.6654 | 6333.4531 |
| 2.4014 | 7221.0443 | 6393.7544 | 6270.5688 |
| 2.4124 | 7175.4228 | 6341.1796 | 6207.6846 |
| 2.4234 | 7181.6037 | 6290.1869 | 6144.8003 |
| 2.4344 | 7234.3378 | 6241.0573 | 6081.9160 |
| 2.4454 | 7192.9164 | 6194.1072 | 6019.0317 |
| 2.4564 | 7144.5831 | 6149.6867 | 5956.1475 |
| 2.4674 | 7069.2861 | 6108.1761 | 5893.2632 |
| 2.4784 | 7015.2321 | 6069.9799 | 5830.3789 |
| 2.4894 | 7089.2940 | 6035.5179 | 5767.4947 |
| 2.5004 | 7055.3186 | 6005.2141 | 5704.6104 |
| 2.5114 | 6976.7886 | 5979.4821 | 5641.7261 |
| 2.5224 | 6859.7114 | 5958.7080 | 5578.8419 |
| 2.5334 | 6901.6431 | 5943.2310 | 5515.9576 |
| 2.5444 | 7034.7380 | 5933.3220 | 5453.0733 |
| 2.5554 | 6971.7335 | 5929.1602 | 5390.1890 |
| 2.5664 | 6795.3923 | 5930.7577 | 5327.3048 |
| 2.5774 | 6689.7650 | 5938.0473 | 5264.2792 |
| 2.5884 | 6703.5713 | 5950.7684 | 5201.2536 |
| 2.5994 | 6679.8496 | 5968.5242 | 5138.2280 |
| 2.6104 | 6661.7040 | 5990.6338 | 5075.2024 |
| 2.6214 | 6551.4956 | 6016.1460 | 5012.1768 |
| 2.6324 | 6540.2330 | 6043.7972 | 4949.1512 |
| 2.6434 | 6472.8800 | 6071.9687 | 4886.1256 |
| 2.6544 | 6328.7738 | 6098.6503 | 4823.1000 |
| 2.6654 | 6332.7227 | 6121.4276 | 4760.0744 |
| 2.6764 | 6258.2797 | 6137.5142 | 4697.0488 |
| 2.6874 | 6069.4946 | 6143.8597 | 4634.0232 |
| 2.6984 | 6040.1327 | 6137.3518 | 4570.9976 |
| 2.7094 | 5990.1495 | 6115.1148 | 4507.9720 |
| 2.7204 | 5918.2768 | 6074.8646 | 4444.9464 |
| 2.7314 | 5746.6253 | 6015.2437 | 4381.9208 |
| 2.7424 | 5467.8908 | 5936.0425 | 4318.8952 |
| 2.7534 | 5364.1809 | 5838.1718 | 4255.8696 |
| 2.7644 | 5221.6991 | 5723.6429 | 4192.6693 |
| 2.7754 | 5063.7817 | 5595.1539 | 4129.4690 |
| 2.7864 | 4964.3328 | 5455.8385 | 4066.2687 |
| 2.7974 | 4692.8230 | 5308.7994 | 4003.0684 |
| 2.8084 | 4512.7487 | 5156.9329 | 3939.8681 |
| 2.8194 | 4311.3638 | 5002.7902 | 3876.6678 |
| 2.8304 | 4354.7625 | 4848.5219 | 3813.4676 |
| 2.8414 | 4169.4395 | 4695.8787 | 3750.2673 |
| 2.8524 | 3979.9675 | 4546.2417 | 3687.0670 |
| 2.8634 | 3866.4602 | 4400.6649 | 3623.8667 |
| 2.8744 | 3647.4105 | 4259.9173 | 3560.6664 |
| 2.8854 | 3720.6460 | 4124.5232 | 3497.4661 |
| 2.8964 | 3479.0796 | 3994.7961 | 3434.2658 |
| 2.9074 | 3333.9292 | 3870.8702 | 3371.0655 |
| 2.9184 | 3322.1376 | 3752.7283 | 3307.8652 |
| 2.9294 | 3183.5841 | 3640.2283 | 3244.6649 |
| 2.9404 | 3199.6578 | 3542.9267 | 3181.4647 |
| 2.9514 | 3166.4946 | 3458.2172 | 3145.3720 |
| 2.9624 | 3090.6829 | 3388.0155 | 3109.2793 |
| 2.9734 | 3072.1839 | 3322.1167 | 3073.1866 |
| 2.9844 | 3052.2950 | 3260.0987 | 3037.0940 |
| 2.9954 | 2938.0619 | 3201.5386 | 3001.0013 |
| 3.0064 | 2855.3604 | 3146.0255 | 2964.9086 |
| 3.0174 | 2909.3068 | 3093.1699 | 2928.8160 |
| 3.0284 | 2807.5752 | 3042.6107 | 2892.7233 |
| 3.0394 | 2812.2802 | 2994.0196 | 2856.6306 |
| 3.0504 | 2739.0791 | 2947.1033 | 2820.5379 |
| 3.0614 | 2674.1770 | 2901.6039 | 2784.4453 |
| 3.0724 | 2716.5767 | 2857.2980 | 2748.3526 |
| 3.0834 | 2707.1376 | 2813.9941 | 2712.2599 |
| 3.0944 | 2651.4602 | 2771.5306 | 2676.1673 |
| 3.1054 | 2631.4336 | 2729.7721 | 2640.0746 |
| 3.1164 | 2642.3422 | 2688.6062 | 2603.9819 |
| 3.1274 | 2531.1033 | 2653.5146 | 2567.8892 |
| 3.1384 | 2540.5629 | 2623.1199 | 2547.2176 |
| 3.1494 | 2505.6608 | 2598.6617 | 2526.5459 |
| 3.1604 | 2482.7625 | 2574.5154 | 2505.8743 |
| 3.1714 | 2451.0285 | 2550.6398 | 2485.2026 |
| 3.1824 | 2443.5034 | 2527.0013 | 2464.5310 |
| 3.1934 | 2423.4602 | 2503.5722 | 2443.8593 |
| 3.2044 | 2439.8658 | 2480.3295 | 2423.1877 |
| 3.2154 | 2401.0069 | 2457.2542 | 2402.5160 |
| 3.2264 | 2354.6357 | 2434.3300 | 2381.8444 |
| 3.2374 | 2325.7551 | 2411.5432 | 2361.1728 |
| 3.2484 | 2285.6111 | 2388.8819 | 2340.5011 |
| 3.2594 | 2311.2448 | 2366.3358 | 2319.8295 |
| 3.2704 | 2282.7296 | 2343.8957 | 2299.1578 |
| 3.2814 | 2215.9607 | 2321.5537 | 2278.4862 |
| 3.2924 | 2249.8451 | 2299.3024 | 2257.8145 |
| 3.3034 | 2258.2311 | 2277.1353 | 2237.1429 |
| 3.3144 | 2237.2527 | 2255.0466 | 2216.4712 |
| 3.3254 | 2229.9528 | 2233.0309 | 2195.7996 |
| 3.3364 | 2152.9955 | 2211.0832 | 2175.1279 |
| 3.3474 | 2095.9971 | 2189.1992 | 2154.4563 |
| 3.3584 | 2143.5266 | 2167.3747 | 2133.7846 |
| 3.3694 | 2100.5732 | 2145.6058 | 2113.1130 |
| 3.3804 | 2051.9646 | 2123.8892 | 2092.4413 |
| 3.3914 | 2076.4513 | 2102.2216 | 2071.7697 |
| 3.4024 | 2105.7311 | 2080.6000 | 2051.0980 |
| 3.4134 | 2097.4710 | 2059.0217 | 2030.4264 |
| 3.4244 | 2027.1563 | 2037.4840 | 2009.7547 |
| 3.4354 | 2020.3048 | 2015.9847 | 1989.0831 |
| 3.4464 | 2010.5442 | 1994.5215 | 1968.4114 |
| 3.4574 | 1969.9705 | 1973.0923 | 1947.7398 |
| 3.4684 | 2005.5074 | 1951.6954 | 1927.0681 |
| 3.4794 | 1992.5919 | 1930.3288 | 1906.3965 |
| 3.4904 | 1906.0486 | 1908.9909 | 1885.7248 |
| 3.5014 | 1841.4356 | 1890.0914 | 1865.0532 |
| 3.5124 | 1802.7483 | 1873.0657 | 1851.0519 |
| 3.5234 | 1837.2508 | 1858.4756 | 1837.0507 |
| 3.5344 | 1839.2886 | 1843.9085 | 1823.0494 |
| 3.5454 | 1789.4759 | 1829.3634 | 1809.0481 |
| 3.5564 | 1797.9233 | 1814.8392 | 1795.0469 |
| 3.5674 | 1789.1121 | 1800.3347 | 1781.0456 |
| 3.5784 | 1754.2104 | 1785.8490 | 1767.0444 |
| 3.5894 | 1748.8496 | 1771.3812 | 1753.0431 |
| 3.6004 | 1745.3068 | 1756.9304 | 1739.0419 |
| 3.6114 | 1730.4936 | 1742.4959 | 1725.0406 |
| 3.6224 | 1734.2611 | 1728.0767 | 1711.0393 |
| 3.6334 | 1674.5693 | 1713.6724 | 1697.0381 |
| 3.6444 | 1650.1922 | 1699.2820 | 1683.0368 |
| 3.6554 | 1679.2153 | 1684.9051 | 1669.0356 |
| 3.6664 | 1725.2296 | 1670.5410 | 1655.0343 |
| 3.6774 | 1617.3923 | 1656.1891 | 1641.0330 |
| 3.6884 | 1618.4912 | 1642.1100 | 1627.0318 |
| 3.6994 | 1621.8928 | 1628.2424 | 1613.7531 |
| 3.7104 | 1583.0801 | 1614.6466 | 1600.4744 |
| 3.7214 | 1573.4956 | 1601.0611 | 1587.1957 |
| 3.7324 | 1633.4302 | 1587.4854 | 1573.9171 |
| 3.7434 | 1561.6991 | 1573.9208 | 1560.6384 |
| 3.7544 | 1570.3599 | 1560.4579 | 1547.3597 |
| 3.7654 | 1542.0029 | 1546.9573 | 1534.0810 |
| 3.7764 | 1548.8309 | 1533.4190 | 1520.8023 |
| 3.7874 | 1493.4956 | 1519.8887 | 1507.5236 |
| 3.7984 | 1536.9621 | 1506.3661 | 1494.2450 |
| 3.8094 | 1526.1416 | 1492.8509 | 1480.9663 |
| 3.8204 | 1534.3274 | 1479.3428 | 1467.6876 |
| 3.8314 | 1507.7345 | 1465.8415 | 1454.4089 |
| 3.8424 | 1429.6844 | 1452.3467 | 1441.1302 |
| 3.8534 | 1423.9351 | 1438.8583 | 1427.8515 |
| 3.8644 | 1420.8387 | 1425.3760 | 1414.5728 |
| 3.8754 | 1398.1318 | 1412.1132 | 1401.2942 |
| 3.8864 | 1422.0619 | 1399.0198 | 1388.6066 |
| 3.8974 | 1349.4907 | 1386.1455 | 1375.9190 |
| 3.9084 | 1335.0541 | 1373.2765 | 1363.2315 |
| 3.9194 | 1377.7640 | 1360.4126 | 1350.5439 |
| 3.9304 | 1415.2837 | 1347.5535 | 1337.8564 |
| 3.9414 | 1352.7148 | 1334.6992 | 1325.1688 |
| 3.9524 | 1349.7758 | 1321.8495 | 1312.4812 |
| 3.9634 | 1381.0462 | 1309.0041 | 1299.7937 |
| 3.9744 | 1327.7950 | 1296.1630 | 1287.1061 |
| 3.9854 | 1291.6726 | 1283.3261 | 1274.4186 |
| 3.9964 | 1303.8323 | 1270.4931 | 1261.7310 |
| 4.0074 | 1273.6775 | 1257.6640 | 1249.0435 |
| 4.0184 | 1240.4808 | 1244.8386 | 1236.3559 |
| 4.0294 | 1258.9538 | 1232.0168 | 1223.6683 |
| 4.0404 | 1248.8800 | 1219.1986 | 1210.9808 |
| 4.0514 | 1211.1150 | 1206.3837 | 1198.2932 |
| 4.0624 | 1159.2252 | 1195.1324 | 1185.6057 |
| 4.0734 | 1156.3894 | 1185.0802 | 1177.2346 |
| 4.0844 | 1192.4425 | 1176.5914 | 1168.8635 |
| 4.0954 | 1231.6824 | 1168.2044 | 1160.4924 |
| 4.1064 | 1193.2035 | 1159.7493 | 1152.1213 |
| 4.1174 | 1130.0738 | 1151.3197 | 1143.7502 |
| 4.1284 | 1151.3461 | 1142.8573 | 1135.3791 |
| 4.1394 | 1118.0816 | 1134.3842 | 1127.0080 |
| 4.1504 | 1106.1416 | 1125.9137 | 1118.6369 |
| 4.1614 | 1153.8142 | 1117.4458 | 1110.2658 |
| 4.1724 | 1169.9223 | 1108.9803 | 1101.8947 |
| 4.1834 | 1126.8053 | 1100.5173 | 1093.5236 |
| 4.1944 | 1126.2979 | 1092.0567 | 1085.1525 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 30 RS1 ground 400C | 2.0054 | 29.9894 | 0.0110 | 12/19/2023 8:29:43 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7256 | 1459.97 | 0.2598 | 32.38887 | 100.00 |
| 5.2657 | 100.90 | 0.1515 | 16.76911 | 6.91 |
| 7.1249 | 133.55 | 0.3031 | 12.39684 | 9.15 |
| 8.7037 | 338.43 | 0.1082 | 10.15138 | 23.18 |
| 13.5326 | 34.09 | 0.1732 | 6.53793 | 2.34 |
| 15.7438 | 596.07 | 0.1082 | 5.62430 | 40.83 |
| 17.5910 | 36.08 | 0.1732 | 5.03764 | 2.47 |
| 18.2045 | 59.41 | 0.1082 | 4.86924 | 4.07 |
| 19.5907 | 21.45 | 0.3464 | 4.52773 | 1.47 |
| 20.9211 | 14.19 | 0.5196 | 4.24270 | 0.97 |
| 23.3599 | 23.50 | 0.1732 | 3.80499 | 1.61 |
| 24.2197 | 32.14 | 0.1732 | 3.67181 | 2.20 |
| 25.9199 | 302.04 | 0.0866 | 3.43469 | 20.69 |
| 26.6893 | 267.52 | 0.1515 | 3.33740 | 18.32 |
| 27.4621 | 663.11 | 0.0866 | 3.24522 | 45.42 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-008-7810 | 55 | Titanium Oxide | Ti O2 | Rutile | 12 |
| * | 04-016-2085 | 52 | Silicon Oxide | Si O2 | Quartz | 7 |
| * | 04-017-4317 | 46 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 7 |
| * | 04-024-8347 | 41 | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | K0.19 Na7.69 Ca0.06 Al8 Si16 O48 ( H2 O )8 | Analcime | 10 |
| * | 04-013-2099 | 34 | Potassium Aluminum Silicate | K8 Al8 Si16 O48 | Leucite | 10 |
| * | 04-025-4215 | 26 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 38 |
| * | 01-082-8023 | 14 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 1 |
| * | 04-013-9383 | 24 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 Al Si3 O10 ( O H ) F | Phlogopite-2M1 | 15 |

Anchor Scan Parameters

Dataset Name	30 RS1 ground 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 30\30 RS1 ground 400C.xrdml

Sample Identification	30 RS1 ground

Measurement Start Date/Time	12/19/2023 8:29:43 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes