30 RS1 ground 550 C REPORT

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	7.0

Phase Titanium Oxide

Weight fraction/ %	9.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	7.0

Phase Silicon Oxide

Weight fraction/ %	3.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	21.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	32.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	7.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	10.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Silicon Oxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Aluminum Silicate | Sodium Magnesium Silicon Oxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30 RS1 ground 550C | 7.0 | 9.0 | 7.0 | 3.0 | 4.0 | 21.0 | 32.0 | 7.0 | 10.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8371.0000 | 8370.7274 | 8371.0000 |
| 2.0164 | 8236.6637 | 8321.9179 | 8310.6628 |
| 2.0274 | 8289.8033 | 8261.9345 | 8250.3256 |
| 2.0384 | 8280.7463 | 8201.9681 | 8189.9884 |
| 2.0494 | 8241.7561 | 8142.0196 | 8129.6512 |
| 2.0604 | 8123.4582 | 8082.0902 | 8069.3140 |
| 2.0714 | 8153.0354 | 8022.1812 | 8008.9768 |
| 2.0824 | 8066.0777 | 7962.2939 | 7948.6396 |
| 2.0934 | 8180.8112 | 7902.4299 | 7888.3024 |
| 2.1044 | 7948.1593 | 7842.5908 | 7827.9652 |
| 2.1154 | 7869.1121 | 7782.7783 | 7767.6280 |
| 2.1264 | 7932.2729 | 7722.9944 | 7707.2908 |
| 2.1374 | 7960.1003 | 7663.2411 | 7646.9536 |
| 2.1484 | 7914.4956 | 7603.5207 | 7586.6164 |
| 2.1594 | 7849.0098 | 7543.8357 | 7526.2792 |
| 2.1704 | 7820.7596 | 7484.1889 | 7465.9420 |
| 2.1814 | 7791.5772 | 7424.5834 | 7405.6048 |
| 2.1924 | 7746.9105 | 7364.9974 | 7345.2676 |
| 2.2034 | 7751.6106 | 7305.3756 | 7284.7966 |
| 2.2144 | 7769.1440 | 7245.7810 | 7224.3257 |
| 2.2254 | 7656.1721 | 7186.2431 | 7163.8547 |
| 2.2364 | 7589.2920 | 7126.7667 | 7103.3838 |
| 2.2474 | 7617.0816 | 7067.3574 | 7042.9128 |
| 2.2584 | 7620.2827 | 7008.0211 | 6982.4419 |
| 2.2694 | 7606.2507 | 6948.7648 | 6921.9709 |
| 2.2804 | 7573.7655 | 6889.5959 | 6861.5000 |
| 2.2914 | 7544.5280 | 6830.5229 | 6801.0291 |
| 2.3024 | 7457.7168 | 6771.5555 | 6740.5581 |
| 2.3134 | 7367.5467 | 6712.7042 | 6680.0872 |
| 2.3244 | 7273.5747 | 6653.9813 | 6619.6162 |
| 2.3354 | 7302.0767 | 6595.4005 | 6559.1453 |
| 2.3464 | 7260.0030 | 6536.9777 | 6498.6743 |
| 2.3574 | 7234.4759 | 6478.7308 | 6438.2034 |
| 2.3684 | 7107.5442 | 6420.6810 | 6377.7324 |
| 2.3794 | 7111.9676 | 6362.8532 | 6317.2615 |
| 2.3904 | 7187.0379 | 6305.2770 | 6256.7905 |
| 2.4014 | 7079.2035 | 6247.9890 | 6196.3196 |
| 2.4124 | 7040.0246 | 6191.0350 | 6135.8486 |
| 2.4234 | 7078.9823 | 6134.4736 | 6075.3777 |
| 2.4344 | 7008.5029 | 6078.3819 | 6014.9068 |
| 2.4454 | 6925.5516 | 6022.8631 | 5954.4358 |
| 2.4564 | 6906.6141 | 5968.0564 | 5893.9649 |
| 2.4674 | 6849.2448 | 5914.1511 | 5833.4939 |
| 2.4784 | 6793.6273 | 5861.4031 | 5773.0230 |
| 2.4894 | 6855.3766 | 5810.1550 | 5712.5520 |
| 2.5004 | 6767.9159 | 5760.8586 | 5652.0811 |
| 2.5114 | 6764.9007 | 5714.0972 | 5591.6101 |
| 2.5224 | 6777.5669 | 5670.6040 | 5531.1392 |
| 2.5334 | 6645.8141 | 5631.2738 | 5470.6682 |
| 2.5444 | 6670.5098 | 5597.1600 | 5410.1973 |
| 2.5554 | 6618.0678 | 5569.4537 | 5349.7263 |
| 2.5664 | 6490.8230 | 5549.4115 | 5289.2554 |
| 2.5774 | 6530.4179 | 5538.2716 | 5228.6507 |
| 2.5884 | 6526.0973 | 5537.3035 | 5168.0460 |
| 2.5994 | 6418.0354 | 5547.5240 | 5107.4413 |
| 2.6104 | 6401.6883 | 5569.5558 | 5046.8366 |
| 2.6214 | 6369.9489 | 5603.4835 | 4986.2320 |
| 2.6324 | 6360.5089 | 5648.6703 | 4925.6273 |
| 2.6434 | 6297.9892 | 5703.5519 | 4865.0226 |
| 2.6544 | 6243.4435 | 5765.3959 | 4804.4179 |
| 2.6654 | 6059.6961 | 5830.0216 | 4743.8132 |
| 2.6764 | 6072.2257 | 5891.5306 | 4683.2085 |
| 2.6874 | 5988.0275 | 5942.2131 | 4622.6038 |
| 2.6984 | 5940.0619 | 5972.9512 | 4561.9991 |
| 2.7094 | 5767.6617 | 5974.4616 | 4501.3944 |
| 2.7204 | 5705.2227 | 5939.3689 | 4440.7897 |
| 2.7314 | 5568.7728 | 5864.3860 | 4380.1851 |
| 2.7424 | 5508.3540 | 5751.4204 | 4319.5804 |
| 2.7534 | 5327.3195 | 5606.8718 | 4258.9757 |
| 2.7644 | 5136.1047 | 5439.6254 | 4198.2057 |
| 2.7754 | 4851.6086 | 5259.0480 | 4137.4357 |
| 2.7864 | 4873.7045 | 5073.3281 | 4076.6657 |
| 2.7974 | 4738.7522 | 4888.8747 | 4015.8956 |
| 2.8084 | 4517.2222 | 4710.3334 | 3955.1256 |
| 2.8194 | 4362.1170 | 4540.8236 | 3894.3556 |
| 2.8304 | 4181.2271 | 4382.2200 | 3833.5856 |
| 2.8414 | 4238.9272 | 4235.4045 | 3772.8156 |
| 2.8524 | 3887.2030 | 4100.4807 | 3712.0456 |
| 2.8634 | 3920.6873 | 3976.9631 | 3651.2756 |
| 2.8744 | 3895.8122 | 3863.9498 | 3590.5056 |
| 2.8854 | 3674.7443 | 3760.2800 | 3529.7356 |
| 2.8964 | 3580.4026 | 3664.6703 | 3468.9656 |
| 2.9074 | 3452.0718 | 3575.8267 | 3408.1956 |
| 2.9184 | 3335.5644 | 3492.5275 | 3347.4256 |
| 2.9294 | 3360.2743 | 3413.6774 | 3286.6556 |
| 2.9404 | 3272.5128 | 3343.4551 | 3225.8856 |
| 2.9514 | 3124.5329 | 3292.3412 | 3191.7328 |
| 2.9624 | 2973.8923 | 3248.4522 | 3157.5800 |
| 2.9734 | 3050.4700 | 3206.1816 | 3123.4273 |
| 2.9844 | 3006.4120 | 3165.1575 | 3089.2745 |
| 2.9954 | 2854.9381 | 3125.1014 | 3055.1218 |
| 3.0064 | 2850.5025 | 3085.8065 | 3020.9690 |
| 3.0174 | 2874.9764 | 3047.1207 | 2986.8163 |
| 3.0284 | 2816.7168 | 3008.9316 | 2952.6635 |
| 3.0394 | 2821.7178 | 2971.1553 | 2918.5108 |
| 3.0504 | 2785.1204 | 2933.7285 | 2884.3580 |
| 3.0614 | 2734.3038 | 2896.6020 | 2850.2053 |
| 3.0724 | 2688.6893 | 2859.7369 | 2816.0525 |
| 3.0834 | 2712.2055 | 2823.1019 | 2781.8998 |
| 3.0944 | 2671.7124 | 2786.6707 | 2747.7470 |
| 3.1054 | 2662.5172 | 2750.4212 | 2713.5942 |
| 3.1164 | 2698.1027 | 2714.3345 | 2679.4415 |
| 3.1274 | 2653.8082 | 2679.4696 | 2645.2887 |
| 3.1384 | 2601.7011 | 2648.1767 | 2616.7264 |
| 3.1494 | 2561.1042 | 2618.0786 | 2588.1640 |
| 3.1604 | 2548.9661 | 2588.0889 | 2559.6016 |
| 3.1714 | 2514.0177 | 2558.1979 | 2531.0393 |
| 3.1824 | 2433.3397 | 2528.3966 | 2502.4769 |
| 3.1934 | 2418.4779 | 2498.6773 | 2473.9145 |
| 3.2044 | 2438.3014 | 2469.0330 | 2445.3522 |
| 3.2154 | 2435.7040 | 2439.4573 | 2416.7898 |
| 3.2264 | 2422.7920 | 2409.9448 | 2388.2274 |
| 3.2374 | 2390.8446 | 2380.4902 | 2359.6651 |
| 3.2484 | 2342.0555 | 2351.0890 | 2331.1027 |
| 3.2594 | 2285.2035 | 2321.7371 | 2302.5403 |
| 3.2704 | 2247.7202 | 2292.4307 | 2273.9780 |
| 3.2814 | 2217.5457 | 2263.1664 | 2245.4156 |
| 3.2924 | 2206.0044 | 2233.9411 | 2216.8532 |
| 3.3034 | 2174.4710 | 2204.7520 | 2188.2908 |
| 3.3144 | 2171.4518 | 2178.1301 | 2159.7285 |
| 3.3254 | 2123.7758 | 2159.6453 | 2144.3391 |
| 3.3364 | 2135.0526 | 2143.7233 | 2128.9498 |
| 3.3474 | 2122.5300 | 2127.8284 | 2113.5604 |
| 3.3584 | 2090.9764 | 2111.9588 | 2098.1710 |
| 3.3694 | 2073.7532 | 2096.1130 | 2082.7817 |
| 3.3804 | 2043.9813 | 2080.2893 | 2067.3923 |
| 3.3914 | 2022.2212 | 2064.4864 | 2052.0029 |
| 3.4024 | 2017.2439 | 2048.7030 | 2036.6136 |
| 3.4134 | 2025.3058 | 2032.9378 | 2021.2242 |
| 3.4244 | 2009.5059 | 2017.1899 | 2005.8348 |
| 3.4354 | 1989.6195 | 2001.4580 | 1990.4455 |
| 3.4464 | 1926.2074 | 1985.7414 | 1975.0561 |
| 3.4574 | 1941.5280 | 1970.0390 | 1959.6668 |
| 3.4684 | 1951.1504 | 1954.3502 | 1944.2774 |
| 3.4794 | 1877.1819 | 1938.6741 | 1928.8880 |
| 3.4904 | 1907.9514 | 1923.0100 | 1913.4987 |
| 3.5014 | 1916.1514 | 1907.3573 | 1898.1093 |
| 3.5124 | 1904.0000 | 1891.7153 | 1882.7199 |
| 3.5234 | 1915.8348 | 1876.0835 | 1867.3306 |
| 3.5344 | 1917.4577 | 1860.4613 | 1851.9412 |
| 3.5454 | 1849.6912 | 1844.8483 | 1836.5518 |
| 3.5564 | 1829.8643 | 1829.2439 | 1821.1625 |
| 3.5674 | 1816.3481 | 1813.6477 | 1805.7731 |
| 3.5784 | 1732.2074 | 1798.0594 | 1790.3838 |
| 3.5894 | 1719.3186 | 1782.4785 | 1774.9944 |
| 3.6004 | 1668.2458 | 1766.9046 | 1759.6050 |
| 3.6114 | 1760.2567 | 1751.3375 | 1744.2157 |
| 3.6224 | 1790.4204 | 1735.7767 | 1728.8263 |
| 3.6334 | 1679.6057 | 1720.2221 | 1713.4369 |
| 3.6444 | 1645.0236 | 1704.6732 | 1698.0476 |
| 3.6554 | 1554.4159 | 1689.1299 | 1682.6582 |
| 3.6664 | 1619.3152 | 1673.5919 | 1667.2688 |
| 3.6774 | 1672.0708 | 1658.0590 | 1651.8795 |
| 3.6884 | 1664.7920 | 1642.8932 | 1636.4901 |
| 3.6994 | 1614.7876 | 1628.8915 | 1622.9850 |
| 3.7104 | 1564.6494 | 1615.2567 | 1609.4799 |
| 3.7214 | 1582.9351 | 1601.6260 | 1595.9747 |
| 3.7324 | 1566.4061 | 1587.9994 | 1582.4696 |
| 3.7434 | 1547.1023 | 1574.3766 | 1568.9645 |
| 3.7544 | 1563.1770 | 1560.7575 | 1555.4593 |
| 3.7654 | 1510.8387 | 1547.1420 | 1541.9542 |
| 3.7764 | 1486.4862 | 1533.5299 | 1528.4491 |
| 3.7874 | 1491.9469 | 1519.9211 | 1514.9439 |
| 3.7984 | 1516.8382 | 1506.3154 | 1501.4388 |
| 3.8094 | 1470.7866 | 1492.7127 | 1487.9337 |
| 3.8204 | 1516.7773 | 1479.1129 | 1474.4285 |
| 3.8314 | 1406.1691 | 1465.5159 | 1460.9234 |
| 3.8424 | 1435.0521 | 1451.9216 | 1447.4183 |
| 3.8534 | 1451.4041 | 1438.3298 | 1433.9131 |
| 3.8644 | 1418.4769 | 1424.7405 | 1420.4080 |
| 3.8754 | 1459.7414 | 1411.3648 | 1406.9029 |
| 3.8864 | 1335.4071 | 1398.6673 | 1394.4960 |
| 3.8974 | 1345.7296 | 1386.1832 | 1382.0892 |
| 3.9084 | 1391.0506 | 1373.7012 | 1369.6824 |
| 3.9194 | 1343.1386 | 1361.2212 | 1357.2756 |
| 3.9304 | 1337.2080 | 1348.7433 | 1344.8688 |
| 3.9414 | 1308.4671 | 1336.2672 | 1332.4619 |
| 3.9524 | 1357.3510 | 1323.7930 | 1320.0551 |
| 3.9634 | 1356.3707 | 1311.3205 | 1307.6483 |
| 3.9744 | 1342.5988 | 1298.8498 | 1295.2415 |
| 3.9854 | 1324.5044 | 1286.3807 | 1282.8347 |
| 3.9964 | 1290.5285 | 1273.9132 | 1270.4278 |
| 4.0074 | 1284.8437 | 1261.4473 | 1258.0210 |
| 4.0184 | 1293.7507 | 1248.9828 | 1245.6142 |
| 4.0294 | 1278.8761 | 1236.5198 | 1233.2074 |
| 4.0404 | 1230.7847 | 1224.1685 | 1220.8006 |
| 4.0514 | 1217.2979 | 1211.7659 | 1208.3937 |
| 4.0624 | 1212.9321 | 1200.1181 | 1195.9869 |
| 4.0734 | 1162.0787 | 1191.0560 | 1187.7806 |
| 4.0844 | 1162.2345 | 1182.8031 | 1179.5743 |
| 4.0954 | 1143.4415 | 1174.5514 | 1171.3680 |
| 4.1064 | 1175.1337 | 1166.3010 | 1163.1617 |
| 4.1174 | 1158.4425 | 1158.0518 | 1154.9554 |
| 4.1284 | 1137.5565 | 1149.8038 | 1146.7491 |
| 4.1394 | 1122.3087 | 1141.5569 | 1138.5428 |
| 4.1504 | 1109.6681 | 1133.3111 | 1130.3365 |
| 4.1614 | 1096.5910 | 1125.0663 | 1122.1302 |
| 4.1724 | 1123.3869 | 1116.8227 | 1113.9239 |
| 4.1834 | 1157.0973 | 1108.5800 | 1105.7176 |
| 4.1944 | 1142.6357 | 1100.3384 | 1097.5113 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 30 RS1 ground 550C | 2.0054 | 29.9894 | 0.0110 | 12/19/2023 2:02:49 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.7198 | 1341.83 | 0.1732 | 32.45804 | 100.00 |
| 5.3319 | 116.91 | 0.1299 | 16.56107 | 8.71 |
| 8.7203 | 357.23 | 0.0758 | 10.13210 | 26.62 |
| 13.5684 | 67.67 | 0.0866 | 6.52074 | 5.04 |
| 15.7799 | 331.77 | 0.1732 | 5.61155 | 24.73 |
| 17.6304 | 44.04 | 0.1299 | 5.02648 | 3.28 |
| 18.2544 | 37.99 | 0.1299 | 4.85605 | 2.83 |
| 19.6848 | 13.28 | 0.5196 | 4.50629 | 0.99 |
| 23.3846 | 22.13 | 0.2598 | 3.80102 | 1.65 |
| 26.0275 | 161.51 | 0.1515 | 3.42074 | 12.04 |
| 26.6955 | 130.58 | 0.0866 | 3.33664 | 9.73 |
| 27.5694 | 423.16 | 0.1082 | 3.23282 | 31.54 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-075-8689 | 54 | Sodium Aluminum Silicate Hydrate | Na1.71 ( ( Al1.806 Si4.194 ) O12 ) ( H2 O )2.16 | Analcime | 7 |
| * | 04-016-0561 | 53 | Titanium Oxide | Ti O2 | Rutile | 9 |
| * | 04-017-4317 | 28 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 7 |
| * | 04-006-1757 | 33 | Silicon Oxide | Si O2 | Quartz | 3 |
| * | 04-013-5979 | 0 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 4 |
| * | 04-013-9383 | 11 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 Al Si3 O10 ( O H ) F | Phlogopite-2M1 | 21 |
| * | 04-025-4215 | 19 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 32 |
| * | 04-013-2099 | 11 | Potassium Aluminum Silicate | K8 Al8 Si16 O48 | Leucite | 7 |
| * | 01-082-8023 | 1 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 10 |

Anchor Scan Parameters

Dataset Name	30 RS1 ground 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 30\30 RS1 ground 550C.xrdml

Sample Identification	30 RS1 ground 550C

Measurement Start Date/Time	12/19/2023 2:02:49 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes