30 RS1 ground GYCOL

Graphics

Graphics

Graphics

Quantitative Results

Phase Titanium Oxide

Weight fraction/ %	4.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	3.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	15.0

Phase Potassium Magnesium Aluminum Silicate Hydroxide

Weight fraction/ %	4.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	49.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	2.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	2.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	21.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Sodium Aluminum Silicate Hydrate | Potassium Magnesium Aluminum Silicate Hydroxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Sodium Magnesium Silicon Oxide Hydrate | Potassium Aluminum Silicate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30 RS1 ground glycol | 4.0 | 3.0 | 15.0 | 4.0 | 49.0 | 2.0 | 2.0 | 21.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7675.0000 | 8448.0158 | 7675.0000 |
| 2.0164 | 7660.9061 | 8469.8111 | 7622.6486 |
| 2.0274 | 7576.2203 | 8452.6341 | 7570.2972 |
| 2.0384 | 7702.6726 | 8427.2719 | 7517.9458 |
| 2.0494 | 7672.7198 | 8392.2906 | 7465.5944 |
| 2.0604 | 7752.2006 | 8346.7104 | 7413.2430 |
| 2.0714 | 7573.2537 | 8290.1616 | 7360.8916 |
| 2.0824 | 7572.2227 | 8222.9472 | 7308.5402 |
| 2.0934 | 7396.1632 | 8145.9918 | 7256.1888 |
| 2.1044 | 7409.1416 | 8060.6930 | 7203.8374 |
| 2.1154 | 7335.3176 | 7968.7242 | 7151.4860 |
| 2.1264 | 7223.3619 | 7871.8392 | 7099.1346 |
| 2.1374 | 7353.0678 | 7771.7187 | 7046.7832 |
| 2.1484 | 7305.1706 | 7669.8722 | 6994.4318 |
| 2.1594 | 7220.8092 | 7567.5921 | 6942.0804 |
| 2.1704 | 7053.0074 | 7465.9443 | 6889.7290 |
| 2.1814 | 7227.6401 | 7365.7811 | 6837.3776 |
| 2.1924 | 7222.3879 | 7267.6627 | 6785.0262 |
| 2.2034 | 7221.5221 | 7172.2217 | 6732.5131 |
| 2.2144 | 7126.1381 | 7079.6683 | 6680.0000 |
| 2.2254 | 7072.7680 | 6990.3281 | 6627.4869 |
| 2.2364 | 7219.0265 | 6904.3210 | 6574.9738 |
| 2.2474 | 7062.9400 | 6821.6777 | 6522.4607 |
| 2.2584 | 6884.5442 | 6742.3548 | 6469.9476 |
| 2.2694 | 6900.4395 | 6666.2500 | 6417.4345 |
| 2.2804 | 6919.0054 | 6593.2156 | 6364.9214 |
| 2.2914 | 6864.9410 | 6523.0718 | 6312.4083 |
| 2.3024 | 6804.1770 | 6455.6200 | 6259.8952 |
| 2.3134 | 6824.7542 | 6390.6539 | 6207.3821 |
| 2.3244 | 6721.5147 | 6327.9703 | 6154.8690 |
| 2.3354 | 6667.4395 | 6267.3792 | 6102.3559 |
| 2.3464 | 6598.3810 | 6208.7124 | 6049.8428 |
| 2.3574 | 6586.0206 | 6151.8310 | 5997.3297 |
| 2.3684 | 6534.7684 | 6096.6331 | 5944.8166 |
| 2.3794 | 6502.3727 | 6042.9794 | 5892.3035 |
| 2.3904 | 6562.7281 | 5990.9745 | 5839.6596 |
| 2.4014 | 6531.7168 | 5940.5541 | 5787.0157 |
| 2.4124 | 6390.2566 | 5891.9099 | 5734.3718 |
| 2.4234 | 6343.0600 | 5845.2203 | 5681.7279 |
| 2.4344 | 6382.4145 | 5800.7353 | 5629.0840 |
| 2.4454 | 6408.4513 | 5758.7789 | 5576.4400 |
| 2.4564 | 6261.5678 | 5719.7487 | 5523.7961 |
| 2.4674 | 6233.3068 | 5684.1113 | 5471.1522 |
| 2.4784 | 6287.4031 | 5652.3929 | 5418.5083 |
| 2.4894 | 6243.1534 | 5625.1639 | 5365.8644 |
| 2.5004 | 6100.7876 | 5603.0170 | 5313.2205 |
| 2.5114 | 6082.2429 | 5586.5379 | 5260.5766 |
| 2.5224 | 6144.6893 | 5576.2700 | 5207.9327 |
| 2.5334 | 5994.9174 | 5572.6725 | 5155.2887 |
| 2.5444 | 6022.0885 | 5576.0735 | 5102.6448 |
| 2.5554 | 5985.0895 | 5586.6202 | 5050.0009 |
| 2.5664 | 6007.0413 | 5604.2243 | 4997.3570 |
| 2.5774 | 6068.5565 | 5628.5046 | 4944.7131 |
| 2.5884 | 5954.6976 | 5658.7234 | 4892.0692 |
| 2.5994 | 5817.3363 | 5693.7135 | 4839.4253 |
| 2.6104 | 5801.9843 | 5731.7953 | 4786.7813 |
| 2.6214 | 5872.8820 | 5770.6879 | 4734.1374 |
| 2.6324 | 5790.7079 | 5807.4330 | 4681.4935 |
| 2.6434 | 5841.6647 | 5838.3779 | 4628.8496 |
| 2.6544 | 5759.8962 | 5859.2843 | 4576.2057 |
| 2.6654 | 5710.3127 | 5865.6420 | 4523.5618 |
| 2.6764 | 5647.5201 | 5853.2173 | 4470.9179 |
| 2.6874 | 5533.2684 | 5818.7625 | 4418.2739 |
| 2.6984 | 5394.8186 | 5760.6802 | 4365.6300 |
| 2.7094 | 5537.6313 | 5679.3869 | 4312.9861 |
| 2.7204 | 5322.1558 | 5577.2130 | 4260.3422 |
| 2.7314 | 5088.8908 | 5457.8882 | 4207.6983 |
| 2.7424 | 5026.9420 | 5325.8289 | 4155.0544 |
| 2.7534 | 5012.8063 | 5185.3979 | 4102.4105 |
| 2.7644 | 4804.0678 | 5040.7258 | 4049.6357 |
| 2.7754 | 4649.1288 | 4895.0700 | 3996.8610 |
| 2.7864 | 4486.0103 | 4751.1843 | 3944.0863 |
| 2.7974 | 4387.1239 | 4611.0916 | 3891.3115 |
| 2.8084 | 4344.6991 | 4476.2488 | 3838.5368 |
| 2.8194 | 4177.2832 | 4347.6345 | 3785.7621 |
| 2.8304 | 4064.2080 | 4225.8280 | 3732.9874 |
| 2.8414 | 3873.8466 | 4111.0769 | 3680.2126 |
| 2.8524 | 3746.4843 | 4003.3590 | 3627.4379 |
| 2.8634 | 3791.7699 | 3902.4370 | 3574.6632 |
| 2.8744 | 3693.0167 | 3807.9112 | 3521.8884 |
| 2.8854 | 3494.3264 | 3719.2679 | 3469.1137 |
| 2.8964 | 3418.3230 | 3635.9236 | 3416.3390 |
| 2.9074 | 3433.7886 | 3557.2634 | 3363.5643 |
| 2.9184 | 3282.8746 | 3482.6731 | 3310.7895 |
| 2.9294 | 3365.1740 | 3411.5646 | 3258.0148 |
| 2.9404 | 3104.0580 | 3353.5224 | 3205.2401 |
| 2.9514 | 3149.5969 | 3293.9984 | 3168.7942 |
| 2.9624 | 3164.9779 | 3246.6226 | 3132.3483 |
| 2.9734 | 3012.4297 | 3200.8986 | 3095.9024 |
| 2.9844 | 2961.3756 | 3156.5184 | 3059.4565 |
| 2.9954 | 2958.8407 | 3113.2281 | 3023.0107 |
| 3.0064 | 2900.7202 | 3070.8216 | 2986.5648 |
| 3.0174 | 2851.2537 | 3029.1340 | 2950.1189 |
| 3.0284 | 2829.5664 | 2988.0343 | 2913.6730 |
| 3.0394 | 2805.7375 | 2947.4196 | 2877.2271 |
| 3.0504 | 2781.6293 | 2907.2092 | 2840.7813 |
| 3.0614 | 2752.8791 | 2867.3399 | 2804.3354 |
| 3.0724 | 2759.2719 | 2827.7618 | 2767.8895 |
| 3.0834 | 2714.0246 | 2788.4357 | 2731.4436 |
| 3.0944 | 2663.1770 | 2749.3299 | 2694.9977 |
| 3.1054 | 2709.7522 | 2710.4190 | 2658.5519 |
| 3.1164 | 2652.5496 | 2671.7053 | 2622.1060 |
| 3.1274 | 2556.1947 | 2641.6287 | 2585.6601 |
| 3.1384 | 2534.0949 | 2608.3776 | 2562.7558 |
| 3.1494 | 2512.9046 | 2583.6094 | 2539.8514 |
| 3.1604 | 2514.4985 | 2558.9583 | 2516.9471 |
| 3.1714 | 2478.0511 | 2534.4145 | 2494.0428 |
| 3.1824 | 2479.3889 | 2509.9691 | 2471.1384 |
| 3.1934 | 2380.0619 | 2485.6143 | 2448.2341 |
| 3.2044 | 2380.1834 | 2461.3431 | 2425.3298 |
| 3.2154 | 2443.7109 | 2437.1491 | 2402.4254 |
| 3.2264 | 2385.1563 | 2413.0266 | 2379.5211 |
| 3.2374 | 2386.2321 | 2388.9703 | 2356.6168 |
| 3.2484 | 2351.0000 | 2364.9755 | 2333.7125 |
| 3.2594 | 2244.4425 | 2341.0379 | 2310.8081 |
| 3.2704 | 2281.2984 | 2317.1534 | 2287.9038 |
| 3.2814 | 2264.6814 | 2293.3186 | 2264.9995 |
| 3.2924 | 2208.1814 | 2269.5301 | 2242.0951 |
| 3.3034 | 2192.0924 | 2245.7848 | 2219.1908 |
| 3.3144 | 2190.6406 | 2226.0789 | 2196.2865 |
| 3.3254 | 2205.8496 | 2204.8595 | 2179.8287 |
| 3.3364 | 2196.3323 | 2187.6745 | 2163.3708 |
| 3.3474 | 2178.0049 | 2170.5229 | 2146.9130 |
| 3.3584 | 2204.7316 | 2153.4026 | 2130.4552 |
| 3.3694 | 2150.6214 | 2136.3117 | 2113.9974 |
| 3.3804 | 2055.2266 | 2119.2485 | 2097.5396 |
| 3.3914 | 2090.5752 | 2102.2115 | 2081.0818 |
| 3.4024 | 2111.1224 | 2085.1990 | 2064.6239 |
| 3.4134 | 2106.6116 | 2068.2098 | 2048.1661 |
| 3.4244 | 2037.5368 | 2051.2426 | 2031.7083 |
| 3.4354 | 1987.9784 | 2034.2961 | 2015.2505 |
| 3.4464 | 1998.1013 | 2017.3692 | 1998.7927 |
| 3.4574 | 1982.7050 | 2000.4610 | 1982.3349 |
| 3.4684 | 2008.4479 | 1983.5703 | 1965.8770 |
| 3.4794 | 1973.7109 | 1966.6964 | 1949.4192 |
| 3.4904 | 1957.5044 | 1949.8384 | 1932.9614 |
| 3.5014 | 1907.9154 | 1933.6031 | 1916.5036 |
| 3.5124 | 1874.5290 | 1917.1465 | 1901.0254 |
| 3.5234 | 1865.7345 | 1901.3112 | 1885.5473 |
| 3.5344 | 1808.4488 | 1885.4888 | 1870.0692 |
| 3.5454 | 1780.9548 | 1869.6788 | 1854.5910 |
| 3.5564 | 1810.5207 | 1853.8806 | 1839.1129 |
| 3.5674 | 1738.5231 | 1838.0937 | 1823.6347 |
| 3.5784 | 1778.9435 | 1822.3175 | 1808.1566 |
| 3.5894 | 1724.7787 | 1806.5515 | 1792.6784 |
| 3.6004 | 1752.0610 | 1790.7953 | 1777.2003 |
| 3.6114 | 1673.8387 | 1775.0484 | 1761.7221 |
| 3.6224 | 1771.8245 | 1759.3105 | 1746.2440 |
| 3.6334 | 1755.9508 | 1743.5812 | 1730.7658 |
| 3.6444 | 1729.3727 | 1727.8601 | 1715.2877 |
| 3.6554 | 1716.7198 | 1712.1469 | 1699.8096 |
| 3.6664 | 1701.3048 | 1696.4412 | 1684.3314 |
| 3.6774 | 1627.8043 | 1680.7427 | 1668.8533 |
| 3.6884 | 1712.9779 | 1665.4693 | 1653.3751 |
| 3.6994 | 1623.3254 | 1650.0404 | 1638.5710 |
| 3.7104 | 1566.6494 | 1635.0359 | 1623.7669 |
| 3.7214 | 1583.1003 | 1620.0377 | 1608.9628 |
| 3.7324 | 1541.3043 | 1605.0453 | 1594.1587 |
| 3.7434 | 1541.7679 | 1590.0587 | 1579.3545 |
| 3.7544 | 1555.3599 | 1575.0776 | 1564.5504 |
| 3.7654 | 1570.4985 | 1560.1017 | 1549.7463 |
| 3.7764 | 1544.5708 | 1545.1310 | 1534.9422 |
| 3.7874 | 1489.4867 | 1530.1651 | 1520.1381 |
| 3.7984 | 1531.7901 | 1515.2040 | 1505.3340 |
| 3.8094 | 1471.2045 | 1500.2475 | 1490.5298 |
| 3.8204 | 1483.0192 | 1485.2954 | 1475.7257 |
| 3.8314 | 1447.9518 | 1470.3475 | 1460.9216 |
| 3.8424 | 1425.4725 | 1455.4038 | 1446.1175 |
| 3.8534 | 1466.5605 | 1440.4641 | 1431.3134 |
| 3.8644 | 1414.6844 | 1425.5282 | 1416.5093 |
| 3.8754 | 1388.8791 | 1413.8328 | 1401.7051 |
| 3.8864 | 1403.4203 | 1400.8853 | 1392.1187 |
| 3.8974 | 1360.6047 | 1391.1780 | 1382.5323 |
| 3.9084 | 1342.2527 | 1381.4740 | 1372.9458 |
| 3.9194 | 1353.0118 | 1371.7734 | 1363.3594 |
| 3.9304 | 1416.3958 | 1362.0760 | 1353.7729 |
| 3.9414 | 1440.8613 | 1352.3817 | 1344.1865 |
| 3.9524 | 1351.2448 | 1342.6904 | 1334.6001 |
| 3.9634 | 1335.1121 | 1333.0020 | 1325.0136 |
| 3.9744 | 1301.0000 | 1323.3165 | 1315.4272 |
| 3.9854 | 1300.1504 | 1313.6337 | 1305.8408 |
| 3.9964 | 1292.5064 | 1303.9537 | 1296.2543 |
| 4.0074 | 1266.0993 | 1294.2763 | 1286.6679 |
| 4.0184 | 1241.9676 | 1284.6014 | 1277.0814 |
| 4.0294 | 1264.2763 | 1274.9291 | 1267.4950 |
| 4.0404 | 1246.0492 | 1265.2592 | 1257.9086 |
| 4.0514 | 1257.3982 | 1255.5917 | 1248.3221 |
| 4.0624 | 1237.9317 | 1245.9265 | 1238.7357 |
| 4.0734 | 1297.1534 | 1236.2636 | 1229.1492 |
| 4.0844 | 1253.9248 | 1226.6029 | 1219.5628 |
| 4.0954 | 1228.9528 | 1216.9444 | 1209.9764 |
| 4.1064 | 1217.5187 | 1207.2880 | 1200.3899 |
| 4.1174 | 1200.4484 | 1197.6338 | 1190.8035 |
| 4.1284 | 1167.6539 | 1187.9816 | 1181.2171 |
| 4.1394 | 1173.6214 | 1178.3314 | 1171.6306 |
| 4.1504 | 1142.6519 | 1168.6832 | 1162.0442 |
| 4.1614 | 1144.0443 | 1159.0370 | 1152.4577 |
| 4.1724 | 1145.2532 | 1149.3927 | 1142.8713 |
| 4.1834 | 1121.0973 | 1139.7502 | 1133.2849 |
| 4.1944 | 1102.6224 | 1130.1097 | 1123.6984 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 30 RS1 ground glycol | 2.0054 | 29.9894 | 0.0110 | 12/20/2023 1:11:00 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.0593 | 815.39 | 0.2598 | 42.86528 | 65.95 |
| 2.6885 | 1236.38 | 0.2165 | 32.83544 | 100.00 |
| 5.2856 | 122.72 | 0.2165 | 16.70588 | 9.93 |
| 6.9810 | 89.99 | 0.5196 | 12.65207 | 7.28 |
| 8.6955 | 117.43 | 0.1732 | 10.16095 | 9.50 |
| 15.7041 | 257.03 | 0.0541 | 5.63843 | 20.79 |
| 18.2184 | 29.22 | 0.1299 | 4.86557 | 2.36 |
| 19.7868 | 12.54 | 0.4330 | 4.48329 | 1.01 |
| 25.8810 | 171.87 | 0.1299 | 3.43977 | 13.90 |
| 26.6874 | 61.45 | 0.1299 | 3.33763 | 4.97 |
| 27.4832 | 108.30 | 0.1082 | 3.24277 | 8.76 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-003-0648 | 44 | Titanium Oxide | Ti O2 | Rutile | 4 |
| * | 04-017-4317 | 26 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 3 |
| * | 04-011-6756 | 23 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 15 |
| * | 00-042-1339 | 10 | Potassium Magnesium Aluminum Silicate Hydroxide | K Mg3 ( Si3 Al ) O10 ( O H )2 | Phlogopite-2M1 | 4 |
| * | 04-025-4215 | 33 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 49 |
| * | 01-082-8023 | 16 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 2 |
| * | 01-082-8023 | 16 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 2 |
| * | 04-013-2099 | 12 | Potassium Aluminum Silicate | K8 Al8 Si16 O48 | Leucite | 21 |

Anchor Scan Parameters

Dataset Name	30 RS1 ground glycol

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 30\30 RS1 ground glycol.xrdml

Sample Identification	30 RS1 ground glycol

Measurement Start Date/Time	12/20/2023 1:11:00 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes