30 RS1 ground REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Silicon Oxide

Weight fraction/ %	5.0

Phase Titanium Oxide

Weight fraction/ %	10.0

Phase Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide

Weight fraction/ %	4.0

Phase Potassium Aluminum Silicate

Weight fraction/ %	10.0

Phase Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	4.0

Phase Potassium Aluminum Silicate Hydroxide

Weight fraction/ %	22.0

Phase Potassium Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	15.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	3.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	27.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	1.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Silicon Oxide | Titanium Oxide | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | Potassium Aluminum Silicate | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | Potassium Aluminum Silicate Hydroxide | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Sodium Magnesium Silicon Oxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 30 RS1 ground | 5.0 | 10.0 | 4.0 | 10.0 | 4.0 | 22.0 | 15.0 | 3.0 | 27.0 | 1.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 8378.0000 | 8363.4347 | 8378.0000 |
| 2.0164 | 8346.0939 | 8336.2186 | 8316.8372 |
| 2.0274 | 8434.3687 | 8275.6937 | 8255.6745 |
| 2.0384 | 8438.4543 | 8215.2007 | 8194.5117 |
| 2.0494 | 8162.3117 | 8154.7415 | 8133.3490 |
| 2.0604 | 8153.4248 | 8094.3185 | 8072.1862 |
| 2.0714 | 8205.4395 | 8033.9343 | 8011.0235 |
| 2.0824 | 8010.4302 | 7973.5915 | 7949.8607 |
| 2.0934 | 8008.9036 | 7913.2931 | 7888.6980 |
| 2.1044 | 7954.6593 | 7853.0424 | 7827.5352 |
| 2.1154 | 7968.1229 | 7792.8429 | 7766.3725 |
| 2.1264 | 7966.4312 | 7732.6983 | 7705.2097 |
| 2.1374 | 7947.6401 | 7672.6131 | 7644.0470 |
| 2.1484 | 7909.7129 | 7612.5918 | 7582.8842 |
| 2.1594 | 7808.3274 | 7552.6394 | 7521.7214 |
| 2.1704 | 7889.0929 | 7492.7617 | 7460.5587 |
| 2.1814 | 7695.0462 | 7432.9648 | 7399.3959 |
| 2.1924 | 7714.6573 | 7373.1831 | 7338.2332 |
| 2.2034 | 7652.7611 | 7313.5085 | 7276.9376 |
| 2.2144 | 7628.6352 | 7253.8650 | 7215.6421 |
| 2.2254 | 7552.4602 | 7194.3344 | 7154.3465 |
| 2.2364 | 7683.3850 | 7134.9271 | 7093.0509 |
| 2.2474 | 7618.9036 | 7075.6546 | 7031.7554 |
| 2.2584 | 7547.4385 | 7016.5299 | 6970.4598 |
| 2.2694 | 7496.4041 | 6957.5679 | 6909.1642 |
| 2.2804 | 7374.8973 | 6898.7853 | 6847.8687 |
| 2.2914 | 7497.1062 | 6840.2013 | 6786.5731 |
| 2.3024 | 7348.8628 | 6781.8383 | 6725.2775 |
| 2.3134 | 7330.8948 | 6723.7225 | 6663.9820 |
| 2.3244 | 7408.6131 | 6665.8854 | 6602.6864 |
| 2.3354 | 7342.9794 | 6608.3655 | 6541.3908 |
| 2.3464 | 7365.7065 | 6551.2104 | 6480.0953 |
| 2.3574 | 7203.3913 | 6494.4807 | 6418.7997 |
| 2.3684 | 7096.7212 | 6438.2543 | 6357.5041 |
| 2.3794 | 7196.7149 | 6382.6325 | 6296.2086 |
| 2.3904 | 7210.8191 | 6327.7480 | 6234.9130 |
| 2.4014 | 7112.0442 | 6273.7754 | 6173.6174 |
| 2.4124 | 7085.7360 | 6220.9426 | 6112.3219 |
| 2.4234 | 7042.0787 | 6169.5457 | 6051.0263 |
| 2.4344 | 6969.4381 | 6119.9637 | 5989.7308 |
| 2.4454 | 7039.3383 | 6072.6747 | 5928.4352 |
| 2.4564 | 7012.2370 | 6028.2694 | 5867.1396 |
| 2.4674 | 6880.8967 | 5987.4620 | 5805.8441 |
| 2.4784 | 6854.8707 | 5951.0931 | 5744.5485 |
| 2.4894 | 6896.6932 | 5920.1233 | 5683.2529 |
| 2.5004 | 6830.7610 | 5895.6132 | 5621.9574 |
| 2.5114 | 6749.6077 | 5878.6881 | 5560.6618 |
| 2.5224 | 6744.1116 | 5870.4841 | 5499.3662 |
| 2.5334 | 6717.2212 | 5872.0766 | 5438.0707 |
| 2.5444 | 6676.5118 | 5884.3928 | 5376.7751 |
| 2.5554 | 6689.8840 | 5908.1097 | 5315.4795 |
| 2.5664 | 6575.1091 | 5943.4695 | 5254.1840 |
| 2.5774 | 6488.9695 | 5990.3876 | 5192.7556 |
| 2.5884 | 6514.9656 | 6047.9957 | 5131.3272 |
| 2.5994 | 6528.3451 | 6114.8212 | 5069.8988 |
| 2.6104 | 6464.8073 | 6188.3857 | 5008.4705 |
| 2.6214 | 6449.4543 | 6265.0812 | 4947.0421 |
| 2.6324 | 6448.2935 | 6339.9729 | 4885.6137 |
| 2.6434 | 6446.4258 | 6406.6880 | 4824.1853 |
| 2.6544 | 6239.6008 | 6457.5613 | 4762.7570 |
| 2.6654 | 6184.5988 | 6484.2566 | 4701.3286 |
| 2.6764 | 6142.0167 | 6478.9883 | 4639.9002 |
| 2.6874 | 6141.7650 | 6436.1551 | 4578.4718 |
| 2.6984 | 6074.9867 | 6353.7914 | 4517.0434 |
| 2.7094 | 5958.8181 | 6234.1258 | 4455.6151 |
| 2.7204 | 5685.3353 | 6082.9413 | 4394.1867 |
| 2.7314 | 5589.7404 | 5908.0911 | 4332.7583 |
| 2.7424 | 5418.9469 | 5717.8851 | 4271.3299 |
| 2.7534 | 5224.3638 | 5519.8223 | 4209.9016 |
| 2.7644 | 5140.4189 | 5320.2894 | 4148.3090 |
| 2.7754 | 5031.1966 | 5124.0335 | 4086.7165 |
| 2.7864 | 4891.0816 | 4934.6815 | 4025.1239 |
| 2.7974 | 4731.4071 | 4754.6538 | 3963.5314 |
| 2.8084 | 4503.0442 | 4585.4486 | 3901.9389 |
| 2.8194 | 4322.5595 | 4427.8112 | 3840.3463 |
| 2.8304 | 4229.5664 | 4281.8798 | 3778.7538 |
| 2.8414 | 4017.4936 | 4147.3162 | 3717.1612 |
| 2.8524 | 3903.6268 | 4023.4265 | 3655.5687 |
| 2.8634 | 3876.9086 | 3909.2727 | 3593.9762 |
| 2.8744 | 3668.2074 | 3803.7739 | 3532.3836 |
| 2.8854 | 3562.6883 | 3705.7935 | 3470.7911 |
| 2.8964 | 3490.3141 | 3614.2091 | 3409.1985 |
| 2.9074 | 3408.8358 | 3527.9653 | 3347.6060 |
| 2.9184 | 3263.6529 | 3446.1083 | 3286.0135 |
| 2.9294 | 3338.0619 | 3367.8050 | 3224.4209 |
| 2.9404 | 3156.5708 | 3307.6305 | 3162.8284 |
| 2.9514 | 3055.8407 | 3247.1913 | 3129.2717 |
| 2.9624 | 2962.5959 | 3203.8251 | 3095.7149 |
| 2.9734 | 3072.0423 | 3161.8761 | 3062.1582 |
| 2.9844 | 2993.0742 | 3121.0526 | 3028.6015 |
| 2.9954 | 2866.1062 | 3081.1300 | 2995.0448 |
| 3.0064 | 2772.6352 | 3041.9364 | 2961.4881 |
| 3.0174 | 2816.6381 | 3003.3411 | 2927.9314 |
| 3.0284 | 2794.8776 | 2965.2442 | 2894.3747 |
| 3.0394 | 2856.7158 | 2927.5689 | 2860.8179 |
| 3.0504 | 2739.6588 | 2890.2556 | 2827.2612 |
| 3.0614 | 2714.2861 | 2853.2571 | 2793.7045 |
| 3.0724 | 2622.8486 | 2816.5354 | 2760.1478 |
| 3.0834 | 2573.0708 | 2780.0594 | 2726.5911 |
| 3.0944 | 2507.5354 | 2743.8029 | 2693.0344 |
| 3.1054 | 2604.7089 | 2707.7439 | 2659.4777 |
| 3.1164 | 2577.9297 | 2671.8633 | 2625.9209 |
| 3.1274 | 2551.2331 | 2640.3301 | 2592.3642 |
| 3.1384 | 2642.6165 | 2608.2516 | 2566.4865 |
| 3.1494 | 2593.2773 | 2580.4930 | 2540.6088 |
| 3.1604 | 2513.3245 | 2552.8570 | 2514.7311 |
| 3.1714 | 2489.9262 | 2525.3333 | 2488.8533 |
| 3.1824 | 2431.5089 | 2497.9126 | 2462.9756 |
| 3.1934 | 2438.8672 | 2470.5866 | 2437.0979 |
| 3.2044 | 2375.2330 | 2443.3478 | 2411.2202 |
| 3.2154 | 2318.8810 | 2416.1895 | 2385.3424 |
| 3.2264 | 2405.4455 | 2389.1054 | 2359.4647 |
| 3.2374 | 2419.3549 | 2362.0901 | 2333.5870 |
| 3.2484 | 2308.1667 | 2335.1383 | 2307.7093 |
| 3.2594 | 2258.8820 | 2308.2456 | 2281.8315 |
| 3.2704 | 2203.9617 | 2281.4077 | 2255.9538 |
| 3.2814 | 2224.6244 | 2254.6207 | 2230.0761 |
| 3.2924 | 2199.6327 | 2227.8812 | 2204.1984 |
| 3.3034 | 2155.7090 | 2201.1860 | 2178.3206 |
| 3.3144 | 2170.9253 | 2179.8564 | 2152.4429 |
| 3.3254 | 2132.1062 | 2157.6847 | 2136.3333 |
| 3.3364 | 2085.0767 | 2140.8735 | 2120.2236 |
| 3.3474 | 2101.9803 | 2124.0960 | 2104.1140 |
| 3.3584 | 2060.5840 | 2107.3503 | 2088.0044 |
| 3.3694 | 2038.1623 | 2090.6342 | 2071.8947 |
| 3.3804 | 2055.9813 | 2073.9460 | 2055.7851 |
| 3.3914 | 2050.6814 | 2057.2840 | 2039.6755 |
| 3.4024 | 2053.0733 | 2040.6467 | 2023.5659 |
| 3.4134 | 2027.6431 | 2024.0327 | 2007.4562 |
| 3.4244 | 1995.7758 | 2007.4405 | 1991.3466 |
| 3.4354 | 1971.8476 | 1990.8690 | 1975.2370 |
| 3.4464 | 1948.3569 | 1974.3169 | 1959.1273 |
| 3.4574 | 1896.6755 | 1957.7833 | 1943.0177 |
| 3.4684 | 1895.1190 | 1941.2672 | 1926.9081 |
| 3.4794 | 1941.9971 | 1924.7674 | 1910.7984 |
| 3.4904 | 1911.2124 | 1908.2833 | 1894.6888 |
| 3.5014 | 1884.6568 | 1891.8140 | 1878.5792 |
| 3.5124 | 1881.2645 | 1875.3588 | 1862.4695 |
| 3.5234 | 1853.5457 | 1858.9168 | 1846.3599 |
| 3.5344 | 1849.7930 | 1842.4874 | 1830.2503 |
| 3.5454 | 1873.9017 | 1826.0701 | 1814.1407 |
| 3.5564 | 1851.2124 | 1809.6642 | 1798.0310 |
| 3.5674 | 1734.9085 | 1793.2691 | 1781.9214 |
| 3.5784 | 1770.2163 | 1776.8844 | 1765.8118 |
| 3.5894 | 1675.2035 | 1760.5095 | 1749.7021 |
| 3.6004 | 1739.3398 | 1744.1440 | 1733.5925 |
| 3.6114 | 1773.3560 | 1727.7875 | 1717.4829 |
| 3.6224 | 1681.4129 | 1711.4789 | 1701.3732 |
| 3.6334 | 1683.5723 | 1695.1649 | 1685.2636 |
| 3.6444 | 1672.3727 | 1678.8536 | 1669.1540 |
| 3.6554 | 1702.7463 | 1662.5429 | 1653.0443 |
| 3.6664 | 1631.9646 | 1646.2267 | 1636.9347 |
| 3.6774 | 1612.9223 | 1629.9173 | 1620.8251 |
| 3.6884 | 1594.3894 | 1615.8754 | 1604.7155 |
| 3.6994 | 1593.7856 | 1601.4658 | 1592.7538 |
| 3.7104 | 1595.8102 | 1589.3232 | 1580.7922 |
| 3.7214 | 1631.7788 | 1577.1863 | 1568.8306 |
| 3.7324 | 1557.8353 | 1565.0550 | 1556.8690 |
| 3.7434 | 1550.1160 | 1552.9289 | 1544.9073 |
| 3.7544 | 1549.0457 | 1540.8079 | 1532.9457 |
| 3.7654 | 1529.6686 | 1528.6918 | 1520.9841 |
| 3.7764 | 1490.8245 | 1516.5804 | 1509.0225 |
| 3.7874 | 1475.1327 | 1504.4735 | 1497.0608 |
| 3.7984 | 1531.0482 | 1492.3709 | 1485.0992 |
| 3.8094 | 1543.4739 | 1480.2725 | 1473.1376 |
| 3.8204 | 1446.8510 | 1468.1781 | 1461.1760 |
| 3.8314 | 1408.4513 | 1456.0875 | 1449.2143 |
| 3.8424 | 1441.6322 | 1444.0007 | 1437.2527 |
| 3.8534 | 1415.5074 | 1432.0057 | 1425.2911 |
| 3.8644 | 1394.9263 | 1419.9849 | 1413.3295 |
| 3.8754 | 1408.0580 | 1408.9427 | 1401.3678 |
| 3.8864 | 1420.8584 | 1397.7255 | 1391.2206 |
| 3.8974 | 1346.7188 | 1387.4713 | 1381.0733 |
| 3.9084 | 1337.0865 | 1377.2202 | 1370.9260 |
| 3.9194 | 1380.1062 | 1366.9719 | 1360.7787 |
| 3.9304 | 1321.4327 | 1356.7265 | 1350.6314 |
| 3.9414 | 1419.6381 | 1346.4838 | 1340.4841 |
| 3.9524 | 1313.6003 | 1336.2437 | 1330.3368 |
| 3.9634 | 1347.9902 | 1326.0061 | 1320.1895 |
| 3.9744 | 1312.5954 | 1315.7711 | 1310.0422 |
| 3.9854 | 1275.6372 | 1305.5384 | 1299.8949 |
| 3.9964 | 1269.2375 | 1295.3080 | 1289.7477 |
| 4.0074 | 1249.9007 | 1285.0798 | 1279.6004 |
| 4.0184 | 1277.5221 | 1274.8538 | 1269.4531 |
| 4.0294 | 1241.9223 | 1264.6300 | 1259.3058 |
| 4.0404 | 1215.9538 | 1254.4082 | 1249.1585 |
| 4.0514 | 1247.2891 | 1244.1883 | 1239.0112 |
| 4.0624 | 1235.3928 | 1234.3462 | 1228.8639 |
| 4.0734 | 1203.0108 | 1224.4438 | 1219.4061 |
| 4.0844 | 1223.6460 | 1214.9191 | 1209.9483 |
| 4.0954 | 1208.9056 | 1205.3961 | 1200.4904 |
| 4.1064 | 1148.8451 | 1195.8748 | 1191.0326 |
| 4.1174 | 1125.5104 | 1186.3552 | 1181.5748 |
| 4.1284 | 1147.8540 | 1176.8373 | 1172.1169 |
| 4.1394 | 1097.3845 | 1167.3209 | 1162.6591 |
| 4.1504 | 1099.9838 | 1157.8061 | 1153.2013 |
| 4.1614 | 1111.1809 | 1148.2928 | 1143.7434 |
| 4.1724 | 1138.1682 | 1138.7809 | 1134.2856 |
| 4.1834 | 1138.1858 | 1129.2705 | 1124.8278 |
| 4.1944 | 1085.1367 | 1119.7615 | 1115.3699 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 30 RS1 ground | 2.0054 | 29.9894 | 0.0110 | 12/13/2023 12:31:21 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6849 | 1659.52 | 0.1948 | 32.87944 | 100.00 |
| 5.3581 | 68.99 | 0.1732 | 16.48016 | 4.16 |
| 6.8852 | 155.65 | 0.3031 | 12.82785 | 9.38 |
| 8.6998 | 278.13 | 0.1299 | 10.15593 | 16.76 |
| 13.1540 | 28.06 | 0.1299 | 6.72525 | 1.69 |
| 13.5529 | 44.18 | 0.1299 | 6.52818 | 2.66 |
| 15.6972 | 515.71 | 0.0541 | 5.64090 | 31.08 |
| 17.6239 | 33.35 | 0.2165 | 5.02832 | 2.01 |
| 18.1830 | 86.45 | 0.1082 | 4.87496 | 5.21 |
| 19.6938 | 28.53 | 0.3464 | 4.50425 | 1.72 |
| 23.3632 | 32.90 | 0.1299 | 3.80445 | 1.98 |
| 24.1994 | 21.51 | 0.2598 | 3.67486 | 1.30 |
| 25.8650 | 406.39 | 0.0541 | 3.44186 | 24.49 |
| 26.6462 | 289.22 | 0.1082 | 3.34270 | 17.43 |
| 27.4915 | 673.34 | 0.0866 | 3.24181 | 40.57 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-086-1560 | 54 | Silicon Oxide | Si O2 | Quartz | 5 |
| * | 04-016-2838 | 54 | Titanium Oxide | Ti O2 | Rutile | 10 |
| * | 04-017-4317 | 43 | Potassium Magnesium Manganese Iron Aluminum Silicate Hydroxide | K Mg0.2 Mn0.1 Fe2.4 Al1.7 Si2.6 O10 ( O H )2 | Biotite-1M | 4 |
| * | 04-013-2099 | 21 | Potassium Aluminum Silicate | K8 Al8 Si16 O48 | Leucite | 10 |
| * | 04-024-8347 | 15 | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | K0.19 Na7.69 Ca0.06 Al8 Si16 O48 ( H2 O )8 | Analcime | 4 |
| * | 00-043-0685 | 10 | Potassium Aluminum Silicate Hydroxide | K Al2 ( Si3 Al ) O10 ( O H )2 | Illite-2M2 (NR) | 22 |
| * | 04-013-9383 | 14 | Potassium Magnesium Aluminum Silicate Fluoride Hydroxide | K Mg3 Al Si3 O10 ( O H ) F | Phlogopite-2M1 | 15 |
| * | 04-013-5979 | 10 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 3 |
| * | 04-025-4215 | 32 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 27 |
| * | 01-082-8023 | 47 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 1 |

Anchor Scan Parameters

Dataset Name	30 RS1 ground

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 30\30 RS1 ground.xrdml

Sample Identification	30 RS1 ground

Measurement Start Date/Time	12/13/2023 12:31:21 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes