4 Etosha 18 SS 0-2 cm S3 400C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	64.0

Phase Potassium Sodium Barium Iron Magnesium Manganese Titanium Aluminum Fluoride Silicate Hydroxide

Weight fraction/ %	21.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	4.0

Phase Potassium Sodium Copper Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Silicon Oxide

Weight fraction/ %	7.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Sodium Barium Iron Magnesium Manganese Titanium Aluminum Fluoride Silicate Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Potassium Sodium Copper Aluminum Silicate Hydroxide Hydrate | Silicon Oxide | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- | --- |
| 4 Etosha18 SS 0-2cm S3 400C | 64.0 | 21.0 | 4.0 | 4.0 | 7.0 | 0.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 4332.0000 | 4323.6195 | 4332.0000 |
| 2.0164 | 4379.8648 | 4309.9319 | 4309.9319 |
| 2.0274 | 4364.4769 | 4287.8637 | 4287.8637 |
| 2.0384 | 4192.6696 | 4265.7956 | 4265.7956 |
| 2.0494 | 4388.4277 | 4243.7275 | 4243.7275 |
| 2.0604 | 4286.2955 | 4221.6593 | 4221.6593 |
| 2.0714 | 4088.6519 | 4199.5912 | 4199.5912 |
| 2.0824 | 4221.1480 | 4177.5231 | 4177.5231 |
| 2.0934 | 4079.5064 | 4155.4549 | 4155.4549 |
| 2.1044 | 4126.5708 | 4133.3868 | 4133.3868 |
| 2.1154 | 4098.2625 | 4111.3187 | 4111.3187 |
| 2.1264 | 4090.9720 | 4089.2505 | 4089.2505 |
| 2.1374 | 4070.3304 | 4067.1824 | 4067.1824 |
| 2.1484 | 4024.8815 | 4045.1143 | 4045.1143 |
| 2.1594 | 4031.2173 | 4023.0461 | 4023.0461 |
| 2.1704 | 4053.3112 | 4000.9780 | 4000.9780 |
| 2.1814 | 3910.0757 | 3978.9099 | 3978.9099 |
| 2.1924 | 3977.3437 | 3956.8240 | 3956.8417 |
| 2.2034 | 3941.6460 | 3934.7270 | 3934.7270 |
| 2.2144 | 3933.4793 | 3912.6123 | 3912.6123 |
| 2.2254 | 3874.1406 | 3890.4976 | 3890.4976 |
| 2.2364 | 3911.1239 | 3868.3829 | 3868.3829 |
| 2.2474 | 3853.4435 | 3846.2682 | 3846.2682 |
| 2.2584 | 3876.1190 | 3824.1535 | 3824.1535 |
| 2.2694 | 3811.2684 | 3802.0387 | 3802.0387 |
| 2.2804 | 3863.5688 | 3779.9240 | 3779.9240 |
| 2.2914 | 3792.2281 | 3757.8093 | 3757.8093 |
| 2.3024 | 3668.6858 | 3735.6946 | 3735.6946 |
| 2.3134 | 3582.9921 | 3713.5799 | 3713.5799 |
| 2.3244 | 3682.2965 | 3691.4652 | 3691.4652 |
| 2.3354 | 3637.2360 | 3669.3505 | 3669.3505 |
| 2.3464 | 3622.7021 | 3647.2358 | 3647.2358 |
| 2.3574 | 3563.7709 | 3625.1211 | 3625.1211 |
| 2.3684 | 3604.1180 | 3603.0063 | 3603.0063 |
| 2.3794 | 3578.0738 | 3582.6324 | 3580.8916 |
| 2.3904 | 3582.4567 | 3563.3607 | 3563.3607 |
| 2.4014 | 3549.5221 | 3545.8298 | 3545.8298 |
| 2.4124 | 3565.8215 | 3528.2989 | 3528.2989 |
| 2.4234 | 3512.8151 | 3510.7680 | 3510.7680 |
| 2.4344 | 3486.1416 | 3493.2371 | 3493.2371 |
| 2.4454 | 3552.6657 | 3475.7061 | 3475.7061 |
| 2.4564 | 3473.2212 | 3458.1752 | 3458.1752 |
| 2.4674 | 3417.8466 | 3440.6443 | 3440.6443 |
| 2.4784 | 3429.9887 | 3423.1134 | 3423.1134 |
| 2.4894 | 3449.3461 | 3405.5825 | 3405.5825 |
| 2.5004 | 3471.5133 | 3388.0516 | 3388.0516 |
| 2.5114 | 3436.3845 | 3370.5207 | 3370.5207 |
| 2.5224 | 3435.1750 | 3352.9897 | 3352.9897 |
| 2.5334 | 3367.3540 | 3335.4588 | 3335.4588 |
| 2.5444 | 3321.6362 | 3317.9279 | 3317.9279 |
| 2.5554 | 3281.2940 | 3300.3970 | 3300.3970 |
| 2.5664 | 3304.6549 | 3285.2083 | 3282.8661 |
| 2.5774 | 3305.3215 | 3271.5030 | 3271.5030 |
| 2.5884 | 3202.6632 | 3260.1398 | 3260.1398 |
| 2.5994 | 3214.7434 | 3248.7767 | 3248.7767 |
| 2.6104 | 3277.1244 | 3237.4136 | 3237.4136 |
| 2.6214 | 3309.5192 | 3226.0505 | 3226.0505 |
| 2.6324 | 3237.1327 | 3214.6874 | 3214.6874 |
| 2.6434 | 3343.4376 | 3203.3242 | 3203.3242 |
| 2.6544 | 3287.5983 | 3191.9611 | 3191.9611 |
| 2.6654 | 3215.5015 | 3180.5980 | 3180.5980 |
| 2.6764 | 3290.4720 | 3169.2349 | 3169.2349 |
| 2.6874 | 3296.1386 | 3157.8717 | 3157.8717 |
| 2.6984 | 3164.3318 | 3146.5086 | 3146.5086 |
| 2.7094 | 3232.6215 | 3135.1455 | 3135.1455 |
| 2.7204 | 3197.8854 | 3123.7824 | 3123.7824 |
| 2.7314 | 3139.8171 | 3112.4193 | 3112.4193 |
| 2.7424 | 3116.8240 | 3101.0561 | 3101.0561 |
| 2.7534 | 3120.6863 | 3089.6608 | 3089.6930 |
| 2.7644 | 3080.4439 | 3078.2595 | 3078.2595 |
| 2.7754 | 3107.4150 | 3066.8259 | 3066.8259 |
| 2.7864 | 3163.6146 | 3055.3924 | 3055.3924 |
| 2.7974 | 3059.4956 | 3043.9588 | 3043.9588 |
| 2.8084 | 3053.0752 | 3032.5253 | 3032.5253 |
| 2.8194 | 3077.6480 | 3021.0917 | 3021.0917 |
| 2.8304 | 3106.7330 | 3009.6582 | 3009.6582 |
| 2.8414 | 3130.4848 | 2998.2247 | 2998.2247 |
| 2.8524 | 3041.1445 | 2986.7911 | 2986.7911 |
| 2.8634 | 3063.8024 | 2975.3576 | 2975.3576 |
| 2.8744 | 3094.1298 | 2963.9240 | 2963.9240 |
| 2.8854 | 3037.9695 | 2952.4905 | 2952.4905 |
| 2.8964 | 3055.9159 | 2941.0569 | 2941.0569 |
| 2.9074 | 2948.0708 | 2929.6234 | 2929.6234 |
| 2.9184 | 2957.0403 | 2918.1898 | 2918.1898 |
| 2.9294 | 2958.2861 | 2906.7563 | 2906.7563 |
| 2.9404 | 2936.5079 | 2895.3228 | 2895.3228 |
| 2.9514 | 2920.8102 | 2883.8892 | 2883.8892 |
| 2.9624 | 2842.4174 | 2872.4557 | 2872.4557 |
| 2.9734 | 2941.6735 | 2861.0221 | 2861.0221 |
| 2.9844 | 2937.6244 | 2849.5886 | 2849.5886 |
| 2.9954 | 2931.2389 | 2838.1550 | 2838.1550 |
| 3.0064 | 2905.8673 | 2826.7215 | 2826.7215 |
| 3.0174 | 2881.6303 | 2815.2880 | 2815.2880 |
| 3.0284 | 2820.5634 | 2803.8544 | 2803.8544 |
| 3.0394 | 2794.2144 | 2792.4209 | 2792.4209 |
| 3.0504 | 2823.6411 | 2780.9873 | 2780.9873 |
| 3.0614 | 2820.8938 | 2769.5538 | 2769.5538 |
| 3.0724 | 2888.9302 | 2758.1202 | 2758.1202 |
| 3.0834 | 2797.8653 | 2746.6867 | 2746.6867 |
| 3.0944 | 2761.7655 | 2735.2532 | 2735.2532 |
| 3.1054 | 2827.2753 | 2723.8196 | 2723.8196 |
| 3.1164 | 2762.0683 | 2712.3861 | 2712.3861 |
| 3.1274 | 2743.3864 | 2700.9203 | 2700.9525 |
| 3.1384 | 2753.7114 | 2689.4486 | 2689.4486 |
| 3.1494 | 2701.2694 | 2677.9446 | 2677.9446 |
| 3.1604 | 2695.1018 | 2666.4406 | 2666.4406 |
| 3.1714 | 2719.0856 | 2654.9367 | 2654.9367 |
| 3.1824 | 2744.4120 | 2643.4327 | 2643.4327 |
| 3.1934 | 2707.1770 | 2631.9287 | 2631.9287 |
| 3.2044 | 2617.7945 | 2620.4248 | 2620.4248 |
| 3.2154 | 2620.7915 | 2608.9208 | 2608.9208 |
| 3.2264 | 2618.0295 | 2597.4168 | 2597.4168 |
| 3.2374 | 2633.9489 | 2585.9129 | 2585.9129 |
| 3.2484 | 2624.5000 | 2574.4089 | 2574.4089 |
| 3.2594 | 2593.6607 | 2562.9049 | 2562.9049 |
| 3.2704 | 2538.2984 | 2551.4010 | 2551.4010 |
| 3.2814 | 2554.0393 | 2539.8970 | 2539.8970 |
| 3.2924 | 2574.9115 | 2528.3930 | 2528.3930 |
| 3.3034 | 2584.0786 | 2516.8891 | 2516.8891 |
| 3.3144 | 2557.8648 | 2505.3453 | 2505.3851 |
| 3.3254 | 2530.4307 | 2493.7941 | 2493.7941 |
| 3.3364 | 2482.2045 | 2482.2031 | 2482.2031 |
| 3.3474 | 2474.9990 | 2470.6121 | 2470.6121 |
| 3.3584 | 2492.8894 | 2459.0211 | 2459.0211 |
| 3.3694 | 2485.9400 | 2447.4301 | 2447.4301 |
| 3.3804 | 2455.3451 | 2435.8390 | 2435.8390 |
| 3.3914 | 2416.8230 | 2424.2480 | 2424.2480 |
| 3.4024 | 2404.3412 | 2412.6570 | 2412.6570 |
| 3.4134 | 2432.3442 | 2401.0660 | 2401.0660 |
| 3.4244 | 2403.8407 | 2389.4750 | 2389.4750 |
| 3.4354 | 2434.3815 | 2377.8840 | 2377.8840 |
| 3.4464 | 2449.3746 | 2366.2930 | 2366.2930 |
| 3.4574 | 2418.0619 | 2354.7020 | 2354.7020 |
| 3.4684 | 2427.4066 | 2343.1109 | 2343.1109 |
| 3.4794 | 2359.0659 | 2331.5199 | 2331.5199 |
| 3.4904 | 2302.8142 | 2319.9289 | 2319.9289 |
| 3.5014 | 2293.3137 | 2308.5074 | 2308.3379 |
| 3.5124 | 2328.2453 | 2297.1172 | 2297.1172 |
| 3.5234 | 2294.1799 | 2285.8965 | 2285.8965 |
| 3.5344 | 2281.2099 | 2274.6757 | 2274.6757 |
| 3.5454 | 2299.4150 | 2263.4550 | 2263.4550 |
| 3.5564 | 2329.1903 | 2252.2343 | 2252.2343 |
| 3.5674 | 2285.8269 | 2241.0136 | 2241.0136 |
| 3.5784 | 2298.3048 | 2229.7928 | 2229.7928 |
| 3.5894 | 2285.6726 | 2218.5721 | 2218.5721 |
| 3.6004 | 2296.9907 | 2207.3514 | 2207.3514 |
| 3.6114 | 2254.3304 | 2196.1307 | 2196.1307 |
| 3.6224 | 2200.8540 | 2184.9099 | 2184.9099 |
| 3.6334 | 2222.1249 | 2173.6892 | 2173.6892 |
| 3.6444 | 2197.4081 | 2162.4685 | 2162.4685 |
| 3.6554 | 2133.6312 | 2151.2478 | 2151.2478 |
| 3.6664 | 2048.5324 | 2140.0270 | 2140.0270 |
| 3.6774 | 2121.9558 | 2128.8063 | 2128.8063 |
| 3.6884 | 2179.9071 | 2117.6941 | 2117.5856 |
| 3.6994 | 2107.4316 | 2106.6021 | 2106.6021 |
| 3.7104 | 2088.0438 | 2095.6185 | 2095.6185 |
| 3.7214 | 2054.8908 | 2084.6350 | 2084.6350 |
| 3.7324 | 2169.1416 | 2073.6515 | 2073.6515 |
| 3.7434 | 2079.0914 | 2062.6679 | 2062.6679 |
| 3.7544 | 2057.7316 | 2051.6844 | 2051.6844 |
| 3.7654 | 2031.8692 | 2040.7009 | 2040.7009 |
| 3.7764 | 2033.9366 | 2029.7173 | 2029.7173 |
| 3.7874 | 2029.0442 | 2018.7338 | 2018.7338 |
| 3.7984 | 2009.7247 | 2007.7503 | 2007.7503 |
| 3.8094 | 1931.0384 | 1996.7667 | 1996.7667 |
| 3.8204 | 1995.9440 | 1985.7832 | 1985.7832 |
| 3.8314 | 1997.7493 | 1974.7997 | 1974.7997 |
| 3.8424 | 2083.8962 | 1963.8161 | 1963.8161 |
| 3.8534 | 2018.7846 | 1952.8326 | 1952.8326 |
| 3.8644 | 1885.1509 | 1941.8491 | 1941.8491 |
| 3.8754 | 1887.1692 | 1931.6067 | 1930.8655 |
| 3.8864 | 1997.9734 | 1921.5016 | 1921.5016 |
| 3.8974 | 1889.9577 | 1912.1377 | 1912.1377 |
| 3.9084 | 1942.6101 | 1902.7739 | 1902.7739 |
| 3.9194 | 1924.9587 | 1893.4100 | 1893.4100 |
| 3.9304 | 1873.3397 | 1884.0461 | 1884.0461 |
| 3.9414 | 1883.4238 | 1874.6822 | 1874.6822 |
| 3.9524 | 1966.5014 | 1865.3183 | 1865.3183 |
| 3.9634 | 1888.6244 | 1855.9544 | 1855.9544 |
| 3.9744 | 1869.7915 | 1846.5905 | 1846.5905 |
| 3.9854 | 1805.8850 | 1837.2266 | 1837.2266 |
| 3.9964 | 1814.1140 | 1827.8627 | 1827.8627 |
| 4.0074 | 1801.5644 | 1818.4988 | 1818.4988 |
| 4.0184 | 1845.3259 | 1809.2179 | 1809.1349 |
| 4.0294 | 1765.3845 | 1799.9044 | 1799.7710 |
| 4.0404 | 1776.8953 | 1790.5467 | 1790.4072 |
| 4.0514 | 1821.5634 | 1781.1853 | 1781.0433 |
| 4.0624 | 1795.4661 | 1771.8239 | 1771.6794 |
| 4.0734 | 1757.6106 | 1762.4625 | 1762.3155 |
| 4.0844 | 1750.3053 | 1753.1013 | 1752.9516 |
| 4.0954 | 1748.1819 | 1743.7401 | 1743.5877 |
| 4.1064 | 1698.7380 | 1734.3790 | 1734.2238 |
| 4.1174 | 1724.6726 | 1725.0179 | 1724.8599 |
| 4.1284 | 1744.9026 | 1715.6570 | 1715.4960 |
| 4.1394 | 1687.9321 | 1706.2961 | 1706.1321 |
| 4.1504 | 1700.9912 | 1696.9353 | 1696.7682 |
| 4.1614 | 1711.1435 | 1687.5746 | 1687.4043 |
| 4.1724 | 1624.0054 | 1678.2140 | 1678.0404 |
| 4.1834 | 1652.7788 | 1668.8535 | 1668.6766 |
| 4.1944 | 1630.9621 | 1659.4931 | 1659.3127 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 4 Etosha18 SS 0-2cm S3 400C | 2.0054 | 29.9894 | 0.0110 | 12/5/2023 12:21:02 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 5.3108 | 95.37 | 0.1299 | 16.62686 | 10.01 |
| 7.1868 | 617.64 | 0.2598 | 12.29034 | 64.81 |
| 8.8556 | 488.37 | 0.1299 | 9.97759 | 51.25 |
| 10.5564 | 25.55 | 0.4330 | 8.37355 | 2.68 |
| 15.8887 | 952.98 | 0.0649 | 5.57334 | 100.00 |
| 17.7387 | 33.63 | 0.2165 | 4.99605 | 3.53 |
| 18.3616 | 139.68 | 0.0649 | 4.82794 | 14.66 |
| 19.8893 | 53.60 | 0.3031 | 4.46042 | 5.62 |
| 22.5234 | 39.78 | 0.1299 | 3.94438 | 4.17 |
| 23.4808 | 26.65 | 0.1732 | 3.78567 | 2.80 |
| 24.3821 | 51.08 | 0.1732 | 3.64773 | 5.36 |
| 26.0190 | 575.84 | 0.0649 | 3.42183 | 60.43 |
| 26.8142 | 132.23 | 0.2165 | 3.32214 | 13.88 |
| 27.6212 | 56.61 | 0.2165 | 3.22688 | 5.94 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-011-6233 | 62 | Sodium Aluminum Silicate Hydrate | Na8 Al8 Si16 O48 ( H2 O )8 | Analcime | 64 |
| * | 01-076-2507 | 51 | Potassium Sodium Barium Iron Magnesium Manganese Titanium Aluminum Fluoride Silicate Hydroxide | ( Na0.148 K1.793 Ca0.007 Ba0.053 ) ( Al0.034 Fe1.978 Mg3.222 Mn0.019 Ti0.742 ) ( Si5.497 Al2.503 O21.85 ( O H )1.685 F0.465 ) | Phlogopite-1M | 21 |
| * | 01-082-8023 | 21 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 4 |
| * | 01-072-6848 | 44 | Potassium Sodium Copper Aluminum Silicate Hydroxide Hydrate | K2 Na Cu20 Al3 Si29 O76 ( O H )16 ( H2 O )8 | Ajoite | 4 |
| * | 01-085-9814 | 35 | Silicon Oxide | Si O2 | Zeolite SSZ-70 | 7 |
| * | 04-025-4215 | No Matching Lines | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | - |

Anchor Scan Parameters

Dataset Name	4 Etosha18 SS 0-2cm S3 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 4\4 Etosha18 SS 0-2cm S3 400C.xrdml

Sample Identification	4 Etosha18 SS 0-2cm S3 400C

Measurement Start Date/Time	12/5/2023 12:21:02 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes