4 Etosha 18 SS 0-2 cm S3 REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	23.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	12.0

Phase Potassium Sodium Magnesium Manganese Zinc Aluminum Iron Titanium Fluoride Aluminum Iron Silicate Hydroxide

Weight fraction/ %	15.0

Phase Potassium Sodium Copper Aluminum Silicate Hydroxide Hydrate

Weight fraction/ %	7.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	43.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | Sodium Magnesium Silicon Oxide Hydrate | Potassium Sodium Magnesium Manganese Zinc Aluminum Iron Titanium Fluoride Aluminum Iron Silicate Hydroxide | Potassium Sodium Copper Aluminum Silicate Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- | --- |
| 4 Etosha18 SS 0-2cm S3 | 23.0 | 12.0 | 15.0 | 7.0 | 43.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 4737.0000 | 4732.0609 | 4737.0000 |
| 2.0164 | 4682.9754 | 4709.6156 | 4709.6156 |
| 2.0274 | 4677.8043 | 4682.2312 | 4682.2312 |
| 2.0384 | 4555.7935 | 4654.8468 | 4654.8468 |
| 2.0494 | 4670.6264 | 4627.4625 | 4627.4625 |
| 2.0604 | 4467.6032 | 4600.0781 | 4600.0781 |
| 2.0714 | 4430.2625 | 4572.6937 | 4572.6937 |
| 2.0824 | 4425.9902 | 4545.3093 | 4545.3093 |
| 2.0934 | 4472.8053 | 4517.9249 | 4517.9249 |
| 2.1044 | 4411.7965 | 4490.5405 | 4490.5405 |
| 2.1154 | 4379.4749 | 4463.1561 | 4463.1561 |
| 2.1264 | 4379.7247 | 4435.7718 | 4435.7718 |
| 2.1374 | 4332.4366 | 4408.3874 | 4408.3874 |
| 2.1484 | 4431.9695 | 4381.0030 | 4381.0030 |
| 2.1594 | 4398.7856 | 4353.6186 | 4353.6186 |
| 2.1704 | 4402.0664 | 4326.2342 | 4326.2342 |
| 2.1814 | 4309.4513 | 4298.8498 | 4298.8498 |
| 2.1924 | 4197.2389 | 4272.5646 | 4271.4654 |
| 2.2034 | 4225.6991 | 4250.1751 | 4250.1751 |
| 2.2144 | 4320.1863 | 4228.8848 | 4228.8848 |
| 2.2254 | 4147.5703 | 4207.5944 | 4207.5944 |
| 2.2364 | 4159.0929 | 4186.3041 | 4186.3041 |
| 2.2474 | 4118.4690 | 4165.0137 | 4165.0137 |
| 2.2584 | 4150.9287 | 4143.7234 | 4143.7234 |
| 2.2694 | 4087.3156 | 4122.4331 | 4122.4331 |
| 2.2804 | 4064.3746 | 4101.1427 | 4101.1427 |
| 2.2914 | 4042.3323 | 4079.8524 | 4079.8524 |
| 2.3024 | 3966.3053 | 4058.5620 | 4058.5620 |
| 2.3134 | 3993.7984 | 4037.2717 | 4037.2717 |
| 2.3244 | 4015.5841 | 4015.9814 | 4015.9814 |
| 2.3354 | 3981.5074 | 3994.6910 | 3994.6910 |
| 2.3464 | 3927.3781 | 3973.4007 | 3973.4007 |
| 2.3574 | 3905.5398 | 3952.1104 | 3952.1104 |
| 2.3684 | 3932.9027 | 3930.8200 | 3930.8200 |
| 2.3794 | 3933.6578 | 3910.1328 | 3909.5297 |
| 2.3904 | 3884.4076 | 3891.5833 | 3891.5833 |
| 2.4014 | 3860.6283 | 3873.6369 | 3873.6369 |
| 2.4124 | 3834.9975 | 3855.6905 | 3855.6905 |
| 2.4234 | 3795.8387 | 3837.7442 | 3837.7442 |
| 2.4344 | 3803.0590 | 3819.7978 | 3819.7978 |
| 2.4454 | 3827.4179 | 3801.8514 | 3801.8514 |
| 2.4564 | 3793.9371 | 3783.9050 | 3783.9050 |
| 2.4674 | 3797.3569 | 3765.9586 | 3765.9586 |
| 2.4784 | 3813.8137 | 3748.0123 | 3748.0123 |
| 2.4894 | 3764.3786 | 3730.0659 | 3730.0659 |
| 2.5004 | 3692.5575 | 3712.1195 | 3712.1195 |
| 2.5114 | 3707.0541 | 3694.1731 | 3694.1731 |
| 2.5224 | 3762.8840 | 3676.2267 | 3676.2267 |
| 2.5334 | 3748.6018 | 3658.2804 | 3658.2804 |
| 2.5444 | 3686.6598 | 3640.3340 | 3640.3340 |
| 2.5554 | 3600.5447 | 3622.3876 | 3622.3876 |
| 2.5664 | 3577.6711 | 3604.8964 | 3604.4412 |
| 2.5774 | 3599.1436 | 3589.0183 | 3589.0183 |
| 2.5884 | 3606.6514 | 3573.5954 | 3573.5954 |
| 2.5994 | 3545.9380 | 3558.1725 | 3558.1725 |
| 2.6104 | 3471.0595 | 3542.7496 | 3542.7496 |
| 2.6214 | 3568.3874 | 3527.3267 | 3527.3267 |
| 2.6324 | 3563.8510 | 3511.9037 | 3511.9037 |
| 2.6434 | 3571.7925 | 3496.4808 | 3496.4808 |
| 2.6544 | 3534.2379 | 3481.0579 | 3481.0579 |
| 2.6654 | 3415.4425 | 3465.6350 | 3465.6350 |
| 2.6764 | 3379.2502 | 3450.2121 | 3450.2121 |
| 2.6874 | 3384.3343 | 3434.7892 | 3434.7892 |
| 2.6984 | 3319.4071 | 3419.3663 | 3419.3663 |
| 2.7094 | 3518.6824 | 3403.9434 | 3403.9434 |
| 2.7204 | 3416.6185 | 3388.5204 | 3388.5204 |
| 2.7314 | 3382.4897 | 3373.0975 | 3373.0975 |
| 2.7424 | 3397.1760 | 3357.6746 | 3357.6746 |
| 2.7534 | 3394.9852 | 3342.2517 | 3342.2517 |
| 2.7644 | 3385.5192 | 3326.8288 | 3326.8288 |
| 2.7754 | 3379.6981 | 3311.4059 | 3311.4059 |
| 2.7864 | 3344.9661 | 3295.9830 | 3295.9830 |
| 2.7974 | 3288.6726 | 3280.5600 | 3280.5600 |
| 2.8084 | 3304.4312 | 3265.1371 | 3265.1371 |
| 2.8194 | 3258.7945 | 3249.7142 | 3249.7142 |
| 2.8304 | 3233.7198 | 3234.2913 | 3234.2913 |
| 2.8414 | 3195.5693 | 3218.8684 | 3218.8684 |
| 2.8524 | 3288.5875 | 3203.4455 | 3203.4455 |
| 2.8634 | 3181.8318 | 3188.0226 | 3188.0226 |
| 2.8744 | 3249.8245 | 3172.5997 | 3172.5997 |
| 2.8854 | 3244.1337 | 3157.1767 | 3157.1767 |
| 2.8964 | 3153.4026 | 3141.7538 | 3141.7538 |
| 2.9074 | 3233.9616 | 3126.3309 | 3126.3309 |
| 2.9184 | 3101.7502 | 3110.9080 | 3110.9080 |
| 2.9294 | 3043.3038 | 3095.4851 | 3095.4851 |
| 2.9404 | 3109.4051 | 3080.9898 | 3080.0622 |
| 2.9514 | 3057.1937 | 3067.5728 | 3067.5728 |
| 2.9624 | 3108.4749 | 3055.0833 | 3055.0833 |
| 2.9734 | 3086.6126 | 3042.5939 | 3042.5939 |
| 2.9844 | 3063.4877 | 3030.1045 | 3030.1045 |
| 2.9954 | 3002.2567 | 3017.6151 | 3017.6151 |
| 3.0064 | 3088.4690 | 3005.1257 | 3005.1257 |
| 3.0174 | 3022.6460 | 2992.6363 | 2992.6363 |
| 3.0284 | 3004.4248 | 2980.1468 | 2980.1468 |
| 3.0394 | 2981.8535 | 2967.6574 | 2967.6574 |
| 3.0504 | 2934.9528 | 2955.1680 | 2955.1680 |
| 3.0614 | 2892.6608 | 2942.6786 | 2942.6786 |
| 3.0724 | 2890.6505 | 2930.1892 | 2930.1892 |
| 3.0834 | 2923.1141 | 2917.6997 | 2917.6997 |
| 3.0944 | 2917.9735 | 2905.2103 | 2905.2103 |
| 3.1054 | 2945.0649 | 2892.7209 | 2892.7209 |
| 3.1164 | 2913.7930 | 2880.2315 | 2880.2315 |
| 3.1274 | 2907.7168 | 2867.7421 | 2867.7421 |
| 3.1384 | 2924.4061 | 2855.2527 | 2855.2527 |
| 3.1494 | 2959.5034 | 2842.7632 | 2842.7632 |
| 3.1604 | 2904.2109 | 2830.2738 | 2830.2738 |
| 3.1714 | 2910.2694 | 2817.7844 | 2817.7844 |
| 3.1824 | 2813.1937 | 2805.2950 | 2805.2950 |
| 3.1934 | 2816.2655 | 2792.8056 | 2792.8056 |
| 3.2044 | 2793.8137 | 2780.3161 | 2780.3161 |
| 3.2154 | 2813.2242 | 2767.8267 | 2767.8267 |
| 3.2264 | 2796.5914 | 2755.3373 | 2755.3373 |
| 3.2374 | 2772.4533 | 2742.8479 | 2742.8479 |
| 3.2484 | 2778.1111 | 2730.3585 | 2730.3585 |
| 3.2594 | 2711.3186 | 2717.8691 | 2717.8691 |
| 3.2704 | 2672.0674 | 2705.3796 | 2705.3796 |
| 3.2814 | 2665.6332 | 2692.8902 | 2692.8902 |
| 3.2924 | 2667.8938 | 2680.4008 | 2680.4008 |
| 3.3034 | 2686.5497 | 2667.9114 | 2667.9114 |
| 3.3144 | 2649.4518 | 2656.2532 | 2655.4220 |
| 3.3254 | 2618.3982 | 2645.5615 | 2645.5615 |
| 3.3364 | 2673.8751 | 2635.7009 | 2635.7009 |
| 3.3474 | 2671.0472 | 2625.8404 | 2625.8404 |
| 3.3584 | 2648.5900 | 2615.9799 | 2615.9799 |
| 3.3694 | 2635.2655 | 2606.1194 | 2606.1194 |
| 3.3804 | 2602.6091 | 2596.2589 | 2596.2589 |
| 3.3914 | 2610.5841 | 2586.3983 | 2586.3983 |
| 3.4024 | 2586.8299 | 2576.5378 | 2576.5378 |
| 3.4134 | 2561.7070 | 2566.6773 | 2566.6773 |
| 3.4244 | 2542.4336 | 2556.8168 | 2556.8168 |
| 3.4354 | 2562.8810 | 2546.9563 | 2546.9563 |
| 3.4464 | 2534.9695 | 2537.0957 | 2537.0957 |
| 3.4574 | 2517.3156 | 2527.2352 | 2527.2352 |
| 3.4684 | 2532.9818 | 2517.3747 | 2517.3747 |
| 3.4794 | 2540.8820 | 2507.5142 | 2507.5142 |
| 3.4904 | 2444.7655 | 2497.6537 | 2497.6537 |
| 3.5014 | 2464.5163 | 2487.8963 | 2487.7931 |
| 3.5124 | 2521.5679 | 2478.2589 | 2478.2589 |
| 3.5234 | 2509.0265 | 2468.7246 | 2468.7246 |
| 3.5344 | 2390.6062 | 2459.1903 | 2459.1903 |
| 3.5454 | 2390.6863 | 2449.6561 | 2449.6561 |
| 3.5564 | 2461.5118 | 2440.1218 | 2440.1218 |
| 3.5674 | 2428.8269 | 2430.5875 | 2430.5875 |
| 3.5784 | 2377.6647 | 2421.0533 | 2421.0533 |
| 3.5894 | 2374.6991 | 2411.5190 | 2411.5190 |
| 3.6004 | 2420.0212 | 2401.9847 | 2401.9847 |
| 3.6114 | 2460.6018 | 2392.4504 | 2392.4504 |
| 3.6224 | 2375.2197 | 2382.9162 | 2382.9162 |
| 3.6334 | 2360.3717 | 2373.3819 | 2373.3819 |
| 3.6444 | 2362.8314 | 2363.8476 | 2363.8476 |
| 3.6554 | 2400.9646 | 2354.3134 | 2354.3134 |
| 3.6664 | 2360.0668 | 2344.7791 | 2344.7791 |
| 3.6774 | 2293.8279 | 2335.2448 | 2335.2448 |
| 3.6884 | 2359.8452 | 2327.2244 | 2325.7106 |
| 3.6994 | 2303.9311 | 2318.8871 | 2318.8871 |
| 3.7104 | 2330.3943 | 2312.0636 | 2312.0636 |
| 3.7214 | 2220.2419 | 2305.2402 | 2305.2402 |
| 3.7324 | 2326.2119 | 2298.4167 | 2298.4167 |
| 3.7434 | 2324.6381 | 2291.5932 | 2291.5932 |
| 3.7544 | 2237.1607 | 2284.7698 | 2284.7698 |
| 3.7654 | 2280.3619 | 2277.9463 | 2277.9463 |
| 3.7764 | 2239.9090 | 2271.1228 | 2271.1228 |
| 3.7874 | 2163.6725 | 2264.2994 | 2264.2994 |
| 3.7984 | 2247.0069 | 2257.4759 | 2257.4759 |
| 3.8094 | 2250.0698 | 2250.6524 | 2250.6524 |
| 3.8204 | 2315.9631 | 2243.8290 | 2243.8290 |
| 3.8314 | 2281.2498 | 2237.0055 | 2237.0055 |
| 3.8424 | 2309.5796 | 2230.1820 | 2230.1820 |
| 3.8534 | 2281.5339 | 2223.3586 | 2223.3586 |
| 3.8644 | 2241.4459 | 2216.5351 | 2216.5351 |
| 3.8754 | 2193.2635 | 2209.7116 | 2209.7116 |
| 3.8864 | 2247.5354 | 2202.8882 | 2202.8882 |
| 3.8974 | 2163.4297 | 2196.0647 | 2196.0647 |
| 3.9084 | 2164.5595 | 2189.2412 | 2189.2412 |
| 3.9194 | 2203.5546 | 2182.4178 | 2182.4178 |
| 3.9304 | 2199.6042 | 2175.5943 | 2175.5943 |
| 3.9414 | 2156.2045 | 2168.7708 | 2168.7708 |
| 3.9524 | 2132.9587 | 2161.9474 | 2161.9474 |
| 3.9634 | 2086.3442 | 2155.1239 | 2155.1239 |
| 3.9744 | 2156.9936 | 2148.3004 | 2148.3004 |
| 3.9854 | 2105.8496 | 2141.4770 | 2141.4770 |
| 3.9964 | 2109.8987 | 2134.6535 | 2134.6535 |
| 4.0074 | 2114.8958 | 2127.8300 | 2127.8300 |
| 4.0184 | 2109.5339 | 2121.0065 | 2121.0065 |
| 4.0294 | 2083.3697 | 2114.1831 | 2114.1831 |
| 4.0404 | 2114.3938 | 2107.3596 | 2107.3596 |
| 4.0514 | 2127.7050 | 2100.5361 | 2100.5361 |
| 4.0624 | 2097.6755 | 2093.8720 | 2093.7127 |
| 4.0734 | 2068.0393 | 2087.1746 | 2087.1746 |
| 4.0844 | 2056.0044 | 2080.6365 | 2080.6365 |
| 4.0954 | 2017.7001 | 2074.0984 | 2074.0984 |
| 4.1064 | 2056.4597 | 2067.5603 | 2067.5603 |
| 4.1174 | 2080.2891 | 2061.0222 | 2061.0222 |
| 4.1284 | 2017.2296 | 2054.4841 | 2054.4841 |
| 4.1394 | 2015.9145 | 2047.9460 | 2047.9460 |
| 4.1504 | 2051.0000 | 2041.4079 | 2041.4079 |
| 4.1614 | 2046.9095 | 2034.8698 | 2034.8698 |
| 4.1724 | 2010.6637 | 2028.3317 | 2028.3317 |
| 4.1834 | 1964.6637 | 2021.7936 | 2021.7936 |
| 4.1944 | 1943.3928 | 2015.2555 | 2015.2555 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 4 Etosha18 SS 0-2cm S3 | 2.0054 | 29.9894 | 0.0110 | 11/30/2023 2:23:48 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 7.0851 | 2035.03 | 0.1732 | 12.46647 | 100.00 |
| 8.7608 | 477.58 | 0.0866 | 10.08532 | 23.47 |
| 11.5966 | 16.89 | 0.5196 | 7.62472 | 0.83 |
| 13.0094 | 31.34 | 0.5196 | 6.79966 | 1.54 |
| 15.7747 | 1038.60 | 0.1082 | 5.61337 | 51.04 |
| 17.6207 | 68.30 | 0.2598 | 5.02923 | 3.36 |
| 18.2330 | 185.50 | 0.0866 | 4.86169 | 9.12 |
| 19.6364 | 108.63 | 0.6061 | 4.51728 | 5.34 |
| 21.0581 | 19.50 | 0.5196 | 4.21542 | 0.96 |
| 23.4482 | 35.78 | 0.4330 | 3.79086 | 1.76 |
| 24.2299 | 57.86 | 0.1732 | 3.67029 | 2.84 |
| 25.9075 | 1043.69 | 0.0758 | 3.43631 | 51.29 |
| 26.7630 | 145.54 | 0.1732 | 3.32838 | 7.15 |
| 27.4606 | 40.32 | 0.2598 | 3.24539 | 1.98 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-024-8347 | 63 | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | K0.19 Na7.69 Ca0.06 Al8 Si16 O48 ( H2 O )8 | Analcime | 23 |
| * | 01-082-8023 | 22 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 12 |
| * | 01-076-8340 | 30 | Potassium Sodium Magnesium Manganese Zinc Aluminum Iron Titanium Fluoride Aluminum Iron Silicate Hydroxide | ( K0.86 Na0.02 ) ( Fe0.27 Mg0.61 Mn0.03 Zn0.01 ) ( Fe0.165 Al0.24 Mg0.54 Ti0.055 )2 ( ( Si2.75 Al1.20 Fe0.05 ) O10.14 ) ( O H )1.74 F0.12 | Phlogopite-1M | 15 |
| * | 01-072-6848 | 20 | Potassium Sodium Copper Aluminum Silicate Hydroxide Hydrate | K2 Na Cu20 Al3 Si29 O76 ( O H )16 ( H2 O )8 | Ajoite | 7 |
| * | 04-025-4215 | 6 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 43 |

Anchor Scan Parameters

Dataset Name	4 Etosha18 SS 0-2cm S3

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 4\4 Etosha18 SS 0-2cm S3.xrdml

Sample Identification	4 Etosha18 SS 0-2cm S3

Measurement Start Date/Time	11/30/2023 2:23:48 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes