5 Etosha 18 HS 0-2 cm S1

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate

Weight fraction/ %	25.0

Phase Tin Oxide

Weight fraction/ %	2.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	27.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	8.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	9.0

Phase Magnesium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	4.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	19.0

Phase Calcium Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	5.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | Tin Oxide | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Calcium Silicon Oxide Hydroxide Hydrate |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 5 Etosha18 HS 0-2cm S1 400C | 25.0 | 2.0 | 27.0 | 8.0 | 9.0 | 4.0 | 19.0 | 5.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6978.0000 | 6956.5646 | 6978.0000 |
| 2.0164 | 6767.3476 | 6944.8339 | 6933.7263 |
| 2.0274 | 6950.7640 | 6900.9268 | 6889.4525 |
| 2.0384 | 6745.1386 | 6857.0379 | 6845.1788 |
| 2.0494 | 6793.1337 | 6813.1684 | 6800.9050 |
| 2.0604 | 6652.2463 | 6769.3197 | 6756.6313 |
| 2.0714 | 6799.1475 | 6725.4931 | 6712.3575 |
| 2.0824 | 6489.1509 | 6681.6902 | 6668.0838 |
| 2.0934 | 6517.8014 | 6637.9127 | 6623.8100 |
| 2.1044 | 6539.6947 | 6594.1624 | 6579.5363 |
| 2.1154 | 6297.8328 | 6550.4413 | 6535.2626 |
| 2.1264 | 6375.3009 | 6506.7518 | 6490.9888 |
| 2.1374 | 6414.0354 | 6463.0962 | 6446.7151 |
| 2.1484 | 6337.4813 | 6419.4774 | 6402.4413 |
| 2.1594 | 6195.7561 | 6375.8984 | 6358.1676 |
| 2.1704 | 6298.5369 | 6332.3627 | 6313.8938 |
| 2.1814 | 6332.7611 | 6288.8743 | 6269.6201 |
| 2.1924 | 6228.6573 | 6246.6683 | 6225.3463 |
| 2.2034 | 6144.4159 | 6203.7509 | 6182.7646 |
| 2.2144 | 6094.4130 | 6162.1277 | 6140.1828 |
| 2.2254 | 6136.6421 | 6120.5758 | 6097.6010 |
| 2.2364 | 6097.8363 | 6079.1044 | 6055.0192 |
| 2.2474 | 6042.1534 | 6037.7246 | 6012.4374 |
| 2.2584 | 6014.0713 | 5996.4499 | 5969.8556 |
| 2.2694 | 5993.9085 | 5955.2971 | 5927.2739 |
| 2.2804 | 5833.5256 | 5914.2863 | 5884.6921 |
| 2.2914 | 5860.7522 | 5873.4426 | 5842.1103 |
| 2.3024 | 5896.8938 | 5832.7964 | 5799.5285 |
| 2.3134 | 5923.3186 | 5792.3850 | 5756.9467 |
| 2.3244 | 5841.0093 | 5752.2532 | 5714.3649 |
| 2.3354 | 5794.2861 | 5712.4548 | 5671.7832 |
| 2.3464 | 5770.1298 | 5673.0538 | 5629.2014 |
| 2.3574 | 5678.2055 | 5634.1254 | 5586.6196 |
| 2.3684 | 5697.3702 | 5595.7566 | 5544.0378 |
| 2.3794 | 5589.4208 | 5557.9791 | 5501.4560 |
| 2.3904 | 5519.8904 | 5521.0160 | 5458.7805 |
| 2.4014 | 5552.7965 | 5484.8811 | 5416.1049 |
| 2.4124 | 5528.7335 | 5449.7781 | 5373.4294 |
| 2.4234 | 5545.8682 | 5415.8513 | 5330.7538 |
| 2.4344 | 5460.7581 | 5383.2509 | 5288.0783 |
| 2.4454 | 5434.8299 | 5352.1288 | 5245.4028 |
| 2.4564 | 5487.8584 | 5322.6336 | 5202.7272 |
| 2.4674 | 5454.5133 | 5294.9045 | 5160.0517 |
| 2.4784 | 5447.3992 | 5269.0645 | 5117.3761 |
| 2.4894 | 5406.4090 | 5245.2126 | 5074.7006 |
| 2.5004 | 5278.0575 | 5223.4158 | 5032.0250 |
| 2.5114 | 5208.1308 | 5203.6998 | 4989.3495 |
| 2.5224 | 5274.8555 | 5186.0405 | 4946.6740 |
| 2.5334 | 5197.9262 | 5170.3533 | 4903.9984 |
| 2.5444 | 5123.0452 | 5156.4835 | 4861.3229 |
| 2.5554 | 5150.0511 | 5144.1937 | 4818.6473 |
| 2.5664 | 5184.5664 | 5133.1507 | 4775.9718 |
| 2.5774 | 5102.1298 | 5122.9106 | 4733.2962 |
| 2.5884 | 5036.2743 | 5112.9034 | 4690.6207 |
| 2.5994 | 5049.9115 | 5102.4195 | 4647.9452 |
| 2.6104 | 4991.7232 | 5090.6040 | 4605.2696 |
| 2.6214 | 5019.5703 | 5076.4671 | 4562.5941 |
| 2.6324 | 5077.8260 | 5058.9196 | 4519.9185 |
| 2.6434 | 4881.4129 | 5036.8438 | 4477.2430 |
| 2.6544 | 4884.7458 | 5009.1976 | 4434.5674 |
| 2.6654 | 4836.8790 | 4975.1424 | 4391.8919 |
| 2.6764 | 4712.0315 | 4934.1647 | 4349.2164 |
| 2.6874 | 4762.3009 | 4886.1601 | 4306.5408 |
| 2.6984 | 4647.0708 | 4831.4508 | 4263.8653 |
| 2.7094 | 4583.9744 | 4770.7322 | 4221.1897 |
| 2.7204 | 4559.6249 | 4704.9651 | 4178.5142 |
| 2.7314 | 4426.0177 | 4635.2464 | 4135.8386 |
| 2.7424 | 4434.7045 | 4562.6910 | 4093.1631 |
| 2.7534 | 4303.4228 | 4488.2754 | 4050.4875 |
| 2.7644 | 4320.9484 | 4413.0335 | 4007.7182 |
| 2.7754 | 4314.3736 | 4337.6340 | 3964.9489 |
| 2.7864 | 4156.6657 | 4262.7810 | 3922.1796 |
| 2.7974 | 4055.2389 | 4188.9771 | 3879.4103 |
| 2.8084 | 4035.1303 | 4116.6065 | 3836.6410 |
| 2.8194 | 3919.3982 | 4045.9508 | 3793.8717 |
| 2.8304 | 3943.9513 | 3977.2028 | 3751.1024 |
| 2.8414 | 3812.4867 | 3910.4794 | 3708.3331 |
| 2.8524 | 3698.8948 | 3845.8322 | 3665.5638 |
| 2.8634 | 3800.3746 | 3783.2583 | 3622.7945 |
| 2.8744 | 3679.7419 | 3722.7095 | 3580.0252 |
| 2.8854 | 3520.6411 | 3664.1010 | 3537.2559 |
| 2.8964 | 3442.3363 | 3607.3202 | 3494.4866 |
| 2.9074 | 3461.6775 | 3552.2349 | 3451.7173 |
| 2.9184 | 3419.9921 | 3498.7001 | 3408.9480 |
| 2.9294 | 3366.9764 | 3446.5648 | 3366.1787 |
| 2.9404 | 3248.7001 | 3405.7880 | 3323.4094 |
| 2.9514 | 3291.7866 | 3359.7948 | 3294.5448 |
| 2.9624 | 3389.3038 | 3324.8725 | 3265.6803 |
| 2.9734 | 3192.3265 | 3290.7803 | 3236.8157 |
| 2.9844 | 3194.4975 | 3257.3999 | 3207.9512 |
| 2.9954 | 3167.5752 | 3224.6255 | 3179.0866 |
| 3.0064 | 3076.7444 | 3192.3638 | 3150.2221 |
| 3.0174 | 3164.4838 | 3160.5341 | 3121.3575 |
| 3.0284 | 3062.5634 | 3129.0672 | 3092.4930 |
| 3.0394 | 3035.9036 | 3097.9045 | 3063.6284 |
| 3.0504 | 3057.1027 | 3066.9970 | 3034.7638 |
| 3.0614 | 2995.4425 | 3036.3040 | 3005.8993 |
| 3.0724 | 2937.3554 | 3005.7918 | 2977.0347 |
| 3.0834 | 2854.9754 | 2975.4331 | 2948.1702 |
| 3.0944 | 2893.6814 | 2945.2054 | 2919.3056 |
| 3.1054 | 2812.8702 | 2915.0903 | 2890.4411 |
| 3.1164 | 2879.7591 | 2885.0730 | 2861.5765 |
| 3.1274 | 2851.5309 | 2863.9502 | 2832.7120 |
| 3.1384 | 2755.2060 | 2837.4547 | 2815.9619 |
| 3.1494 | 2858.9990 | 2819.8695 | 2799.2118 |
| 3.1604 | 2772.5133 | 2802.2873 | 2782.4618 |
| 3.1714 | 2756.4287 | 2784.7293 | 2765.7117 |
| 3.1824 | 2730.4911 | 2767.2209 | 2748.9617 |
| 3.1934 | 2681.2212 | 2749.7577 | 2732.2116 |
| 3.2044 | 2632.2684 | 2732.3359 | 2715.4615 |
| 3.2154 | 2672.3206 | 2714.9524 | 2698.7115 |
| 3.2264 | 2642.5398 | 2697.6041 | 2681.9614 |
| 3.2374 | 2565.3107 | 2680.2886 | 2665.2114 |
| 3.2484 | 2589.3889 | 2663.0033 | 2648.4613 |
| 3.2594 | 2565.5280 | 2645.7463 | 2631.7112 |
| 3.2704 | 2570.7606 | 2628.5155 | 2614.9612 |
| 3.2814 | 2611.6922 | 2611.3093 | 2598.2111 |
| 3.2924 | 2552.8318 | 2594.1259 | 2581.4611 |
| 3.3034 | 2550.4317 | 2576.9640 | 2564.7110 |
| 3.3144 | 2607.9395 | 2559.8222 | 2547.9609 |
| 3.3254 | 2545.7109 | 2542.6991 | 2531.2109 |
| 3.3364 | 2425.6121 | 2525.5937 | 2514.4608 |
| 3.3474 | 2484.3983 | 2508.5049 | 2497.7108 |
| 3.3584 | 2491.2699 | 2491.4317 | 2480.9607 |
| 3.3694 | 2429.3973 | 2474.3731 | 2464.2106 |
| 3.3804 | 2411.4076 | 2457.3284 | 2447.4606 |
| 3.3914 | 2368.7080 | 2440.2967 | 2430.7105 |
| 3.4024 | 2355.9027 | 2423.2772 | 2413.9605 |
| 3.4134 | 2337.1082 | 2406.2694 | 2397.2104 |
| 3.4244 | 2359.4484 | 2389.2725 | 2380.4603 |
| 3.4354 | 2330.7817 | 2372.2860 | 2363.7103 |
| 3.4464 | 2226.2251 | 2355.3093 | 2346.9602 |
| 3.4574 | 2278.7198 | 2338.3419 | 2330.2102 |
| 3.4684 | 2257.3918 | 2321.3833 | 2313.4601 |
| 3.4794 | 2278.2881 | 2304.4331 | 2296.7101 |
| 3.4904 | 2316.3186 | 2287.4908 | 2279.9600 |
| 3.5014 | 2282.7492 | 2272.0015 | 2263.2099 |
| 3.5124 | 2206.5029 | 2255.6163 | 2248.4478 |
| 3.5234 | 2188.7463 | 2240.6834 | 2233.6856 |
| 3.5344 | 2183.7901 | 2225.7570 | 2218.9234 |
| 3.5454 | 2191.5320 | 2210.8368 | 2204.1613 |
| 3.5564 | 2149.8186 | 2195.9224 | 2189.3991 |
| 3.5674 | 2130.7640 | 2181.0136 | 2174.6369 |
| 3.5784 | 2076.2089 | 2166.1102 | 2159.8748 |
| 3.5894 | 2125.2124 | 2151.2119 | 2145.1126 |
| 3.6004 | 2096.5034 | 2136.3185 | 2130.3504 |
| 3.6114 | 2008.3176 | 2121.4298 | 2115.5883 |
| 3.6224 | 2105.1770 | 2106.5455 | 2100.8261 |
| 3.6334 | 2083.0364 | 2091.6655 | 2086.0639 |
| 3.6444 | 2086.1332 | 2076.7895 | 2071.3018 |
| 3.6554 | 2042.5988 | 2061.9175 | 2056.5396 |
| 3.6664 | 2018.5929 | 2047.0493 | 2041.7774 |
| 3.6774 | 2016.8682 | 2032.1846 | 2027.0153 |
| 3.6884 | 1982.6593 | 2019.7827 | 2012.2531 |
| 3.6994 | 2012.8201 | 2005.8476 | 2000.8731 |
| 3.7104 | 2068.5915 | 1994.3750 | 1989.4930 |
| 3.7214 | 1992.3510 | 1982.9055 | 1978.1130 |
| 3.7324 | 1984.0703 | 1971.4390 | 1966.7329 |
| 3.7434 | 1914.2930 | 1959.9752 | 1955.3529 |
| 3.7544 | 1898.5487 | 1948.5142 | 1943.9729 |
| 3.7654 | 1958.8938 | 1937.0558 | 1932.5928 |
| 3.7764 | 1963.9366 | 1925.6000 | 1921.2128 |
| 3.7874 | 1921.3805 | 1914.1466 | 1909.8327 |
| 3.7984 | 1811.3889 | 1902.6955 | 1898.4527 |
| 3.8094 | 1923.8899 | 1891.2467 | 1887.0727 |
| 3.8204 | 1915.3186 | 1879.8002 | 1875.6926 |
| 3.8314 | 1856.6775 | 1868.3557 | 1864.3126 |
| 3.8424 | 1850.4204 | 1856.9133 | 1852.9325 |
| 3.8534 | 1871.8466 | 1845.4729 | 1841.5525 |
| 3.8644 | 1816.3997 | 1834.0344 | 1830.1725 |
| 3.8754 | 1862.0206 | 1822.6110 | 1818.7924 |
| 3.8864 | 1785.6062 | 1811.1811 | 1807.4305 |
| 3.8974 | 1744.2734 | 1799.7661 | 1796.0686 |
| 3.9084 | 1788.3250 | 1788.3529 | 1784.7067 |
| 3.9194 | 1762.5162 | 1776.9413 | 1773.3448 |
| 3.9304 | 1807.3771 | 1765.5313 | 1761.9829 |
| 3.9414 | 1820.0845 | 1754.1229 | 1750.6209 |
| 3.9524 | 1756.1917 | 1742.7160 | 1739.2590 |
| 3.9634 | 1721.9655 | 1731.3106 | 1727.8971 |
| 3.9744 | 1640.2045 | 1719.9066 | 1716.5352 |
| 3.9854 | 1686.7699 | 1708.5040 | 1705.1733 |
| 3.9964 | 1699.4085 | 1697.1028 | 1693.8114 |
| 4.0074 | 1636.9577 | 1685.7030 | 1682.4495 |
| 4.0184 | 1687.0324 | 1674.3044 | 1671.0876 |
| 4.0294 | 1628.8908 | 1662.9071 | 1659.7257 |
| 4.0404 | 1579.6338 | 1651.5111 | 1648.3638 |
| 4.0514 | 1647.3009 | 1640.1163 | 1637.0018 |
| 4.0624 | 1657.7802 | 1631.2457 | 1625.6399 |
| 4.0734 | 1612.9892 | 1620.8000 | 1617.7477 |
| 4.0844 | 1594.2920 | 1612.8785 | 1609.8555 |
| 4.0954 | 1615.1062 | 1604.9582 | 1601.9634 |
| 4.1064 | 1641.2674 | 1597.0389 | 1594.0712 |
| 4.1174 | 1621.2006 | 1589.1208 | 1586.1790 |
| 4.1284 | 1632.5148 | 1581.2037 | 1578.2868 |
| 4.1394 | 1636.2389 | 1573.2878 | 1570.3946 |
| 4.1504 | 1578.4012 | 1565.3729 | 1562.5024 |
| 4.1614 | 1563.0885 | 1557.4591 | 1554.6102 |
| 4.1724 | 1584.4666 | 1549.5463 | 1546.7180 |
| 4.1834 | 1550.0531 | 1541.6346 | 1538.8258 |
| 4.1944 | 1532.4725 | 1533.7239 | 1530.9336 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 5 Etosha18 HS 0-2cm S1 400C | 2.0054 | 29.9894 | 0.0110 | 12/5/2023 12:31:29 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6714 | 522.60 | 0.2598 | 33.04601 | 62.74 |
| 5.3046 | 123.34 | 0.2165 | 16.64611 | 14.81 |
| 7.1159 | 574.92 | 0.2598 | 12.41259 | 69.02 |
| 8.7168 | 493.48 | 0.1082 | 10.13621 | 59.24 |
| 10.5077 | 19.41 | 0.5196 | 8.41230 | 2.33 |
| 15.7643 | 833.01 | 0.0866 | 5.61706 | 100.00 |
| 17.6351 | 38.48 | 0.1299 | 5.02517 | 4.62 |
| 18.2272 | 99.64 | 0.1082 | 4.86323 | 11.96 |
| 19.5666 | 51.01 | 0.3464 | 4.53324 | 6.12 |
| 24.1783 | 55.27 | 0.1299 | 3.67802 | 6.63 |
| 25.9669 | 511.78 | 0.0974 | 3.42859 | 61.44 |
| 26.7309 | 161.59 | 0.1515 | 3.33230 | 19.40 |
| 27.4965 | 159.74 | 0.1299 | 3.24123 | 19.18 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 04-024-8347 | 63 | Potassium Sodium Calcium Aluminum Silicon Oxide Hydrate | K0.19 Na7.69 Ca0.06 Al8 Si16 O48 ( H2 O )8 | Analcime | 25 |
| * | 01-087-9078 | 50 | Tin Oxide | Sn O2 | Cassiterite | 2 |
| * | 04-024-2561 | 29 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.92 Na0.04 Mg1.74 Ti0.14 Fe1.05 Al1.39 Si2.69 O10.44 ( O H )1.35 F0.21 | Phlogopite-1M | 27 |
| * | 01-082-8023 | 15 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 8 |
| * | 01-081-8598 | 12 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2 Al2 ) Si8 O20 ( H2 O )4 ( O H )2 ( H2 O )3.84 | Palygorskite-M | 9 |
| * | 04-016-3203 | 10 | Magnesium Silicon Oxide Hydroxide Hydrate | Mg4 Si6 O15 ( O H )2 ( H2 O )6 | Sepiolite | 4 |
| * | 04-025-4215 | 18 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 19 |
| * | 01-081-9792 | 26 | Calcium Silicon Oxide Hydroxide Hydrate | Ca7.76 Si6.76 O18.8 ( O H )4.88 ( H2 O )7.84 |  | 5 |

Anchor Scan Parameters

Dataset Name	5 Etosha18 HS 0-2cm S1 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 5\5 Etosha18 HS 0-2cm S1 400C.xrdml

Sample Identification	5 Etosha18 HS 0-2cm S1 400C

Measurement Start Date/Time	12/5/2023 12:31:29 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes