5 Etosha 18 HS 0-2 cm S1 550 C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	43.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	8.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	13.0

Phase Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide

Weight fraction/ %	36.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide |
| --- | --- | --- | --- | --- |
| 5 Etosha18 HS 0-2cm S1 550C | 43.0 | 8.0 | 13.0 | 36.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 7129.0000 | 7123.1267 | 7129.0000 |
| 2.0164 | 7082.5241 | 7094.4801 | 7084.5606 |
| 2.0274 | 7200.4769 | 7050.3807 | 7040.1213 |
| 2.0384 | 7021.3319 | 7006.2988 | 6995.6819 |
| 2.0494 | 7026.1652 | 6962.2358 | 6951.2426 |
| 2.0604 | 6950.2793 | 6918.1929 | 6906.8032 |
| 2.0714 | 6909.1770 | 6874.1716 | 6862.3639 |
| 2.0824 | 6726.5275 | 6830.1735 | 6817.9245 |
| 2.0934 | 6761.2468 | 6786.2003 | 6773.4852 |
| 2.1044 | 6731.3540 | 6742.2538 | 6729.0458 |
| 2.1154 | 6670.7699 | 6698.3362 | 6684.6065 |
| 2.1264 | 6547.4533 | 6654.4496 | 6640.1671 |
| 2.1374 | 6776.0796 | 6610.5967 | 6595.7278 |
| 2.1484 | 6528.6391 | 6566.7801 | 6551.2884 |
| 2.1594 | 6518.7502 | 6523.0028 | 6506.8491 |
| 2.1704 | 6452.0501 | 6479.2682 | 6462.4097 |
| 2.1814 | 6427.0039 | 6435.5801 | 6417.9704 |
| 2.1924 | 6382.5969 | 6391.9031 | 6373.5310 |
| 2.2034 | 6383.1858 | 6348.2471 | 6328.9785 |
| 2.2144 | 6327.9700 | 6304.6122 | 6284.4260 |
| 2.2254 | 6368.0403 | 6261.0439 | 6239.8735 |
| 2.2364 | 6434.4808 | 6217.5492 | 6195.3210 |
| 2.2474 | 6337.2458 | 6174.1364 | 6150.7685 |
| 2.2584 | 6235.5098 | 6130.8150 | 6106.2159 |
| 2.2694 | 6303.8407 | 6087.5969 | 6061.6634 |
| 2.2804 | 6234.9705 | 6044.4963 | 6017.1109 |
| 2.2914 | 6159.5152 | 6001.5313 | 5972.5584 |
| 2.3024 | 6089.0133 | 5958.7241 | 5928.0059 |
| 2.3134 | 5943.0128 | 5916.1033 | 5883.4534 |
| 2.3244 | 5996.0797 | 5873.7052 | 5838.9009 |
| 2.3354 | 5975.4602 | 5831.5764 | 5794.3483 |
| 2.3464 | 5909.5841 | 5789.7759 | 5749.7958 |
| 2.3574 | 5957.6765 | 5748.3789 | 5705.2433 |
| 2.3684 | 5899.7493 | 5707.4794 | 5660.6908 |
| 2.3794 | 5945.4631 | 5667.1944 | 5616.1383 |
| 2.3904 | 5904.3397 | 5627.6670 | 5571.5858 |
| 2.4014 | 5837.6018 | 5589.0693 | 5527.0333 |
| 2.4124 | 5704.3200 | 5551.6044 | 5482.4807 |
| 2.4234 | 5636.2989 | 5515.5070 | 5437.9282 |
| 2.4344 | 5727.4558 | 5481.0417 | 5393.3757 |
| 2.4454 | 5718.0364 | 5448.4988 | 5348.8232 |
| 2.4564 | 5583.4415 | 5418.1866 | 5304.2707 |
| 2.4674 | 5596.1121 | 5390.4209 | 5259.7182 |
| 2.4784 | 5617.9774 | 5365.5097 | 5215.1657 |
| 2.4894 | 5542.5821 | 5343.7359 | 5170.6131 |
| 2.5004 | 5532.0619 | 5325.3352 | 5126.0606 |
| 2.5114 | 5420.5723 | 5310.4731 | 5081.5081 |
| 2.5224 | 5482.8181 | 5299.2187 | 5036.9556 |
| 2.5334 | 5484.4956 | 5291.5174 | 4992.4031 |
| 2.5444 | 5271.4911 | 5287.1613 | 4947.8506 |
| 2.5554 | 5263.1210 | 5285.7564 | 4903.2981 |
| 2.5664 | 5301.4631 | 5286.6457 | 4858.7455 |
| 2.5774 | 5216.6647 | 5288.9500 | 4814.0799 |
| 2.5884 | 5287.6510 | 5291.4677 | 4769.4142 |
| 2.5994 | 5200.3274 | 5292.6926 | 4724.7485 |
| 2.6104 | 5281.8338 | 5290.7246 | 4680.0828 |
| 2.6214 | 5228.9764 | 5283.3736 | 4635.4172 |
| 2.6324 | 5147.8805 | 5268.3321 | 4590.7515 |
| 2.6434 | 5050.3156 | 5243.4678 | 4546.0858 |
| 2.6544 | 4933.0555 | 5207.1917 | 4501.4201 |
| 2.6654 | 4983.8584 | 5158.7900 | 4456.7545 |
| 2.6764 | 5018.9980 | 5098.5877 | 4412.0888 |
| 2.6874 | 4889.9282 | 5027.8718 | 4367.4231 |
| 2.6984 | 4745.2389 | 4948.6081 | 4322.7574 |
| 2.7094 | 4656.0029 | 4863.0735 | 4278.0917 |
| 2.7204 | 4611.2389 | 4773.5265 | 4233.4261 |
| 2.7314 | 4510.7109 | 4681.9893 | 4188.7604 |
| 2.7424 | 4461.0010 | 4590.1457 | 4144.0947 |
| 2.7534 | 4438.2842 | 4499.2752 | 4099.4290 |
| 2.7644 | 4352.7360 | 4410.3843 | 4054.6235 |
| 2.7754 | 4281.2153 | 4324.1829 | 4009.8179 |
| 2.7864 | 4226.6214 | 4241.1962 | 3965.0123 |
| 2.7974 | 4138.5841 | 4161.7005 | 3920.2067 |
| 2.8084 | 4157.6091 | 4085.8066 | 3875.4012 |
| 2.8194 | 4008.1976 | 4013.4901 | 3830.5956 |
| 2.8304 | 3927.5501 | 3944.6201 | 3785.7900 |
| 2.8414 | 3883.7011 | 3878.9852 | 3740.9844 |
| 2.8524 | 3842.1971 | 3816.3184 | 3696.1789 |
| 2.8634 | 3797.8171 | 3756.3191 | 3651.3733 |
| 2.8744 | 3782.4061 | 3698.6728 | 3606.5677 |
| 2.8854 | 3659.0895 | 3643.0669 | 3561.7621 |
| 2.8964 | 3597.2655 | 3589.2031 | 3516.9566 |
| 2.9074 | 3548.0639 | 3536.8063 | 3472.1510 |
| 2.9184 | 3429.1534 | 3485.6299 | 3427.3454 |
| 2.9294 | 3385.8908 | 3435.4585 | 3382.5398 |
| 2.9404 | 3323.4474 | 3391.3858 | 3337.7343 |
| 2.9514 | 3326.8407 | 3352.5863 | 3308.0903 |
| 2.9624 | 3227.0797 | 3319.6048 | 3278.4463 |
| 2.9734 | 3246.4307 | 3287.0610 | 3248.8023 |
| 2.9844 | 3151.9720 | 3254.8729 | 3219.1583 |
| 2.9954 | 3160.6991 | 3222.9754 | 3189.5143 |
| 3.0064 | 3083.5974 | 3191.3175 | 3159.8703 |
| 3.0174 | 3145.9764 | 3159.8591 | 3130.2263 |
| 3.0284 | 3076.2714 | 3128.5690 | 3100.5823 |
| 3.0394 | 3018.9322 | 3097.4225 | 3070.9383 |
| 3.0504 | 3012.4321 | 3066.4001 | 3041.2943 |
| 3.0614 | 2955.8997 | 3035.4862 | 3011.6503 |
| 3.0724 | 2965.7670 | 3004.6682 | 2982.0063 |
| 3.0834 | 2973.8427 | 2973.9355 | 2952.3623 |
| 3.0944 | 2915.5531 | 2943.2794 | 2922.7183 |
| 3.1054 | 2901.9872 | 2912.6926 | 2893.0743 |
| 3.1164 | 2825.8638 | 2882.1686 | 2863.4303 |
| 3.1274 | 2876.6017 | 2854.3520 | 2833.7863 |
| 3.1384 | 2798.3938 | 2828.9006 | 2811.7554 |
| 3.1494 | 2758.8072 | 2806.1473 | 2789.7245 |
| 3.1604 | 2669.7994 | 2783.4382 | 2767.6936 |
| 3.1714 | 2715.0177 | 2760.7696 | 2745.6627 |
| 3.1824 | 2658.6057 | 2738.1385 | 2723.6318 |
| 3.1934 | 2707.2832 | 2715.5420 | 2701.6009 |
| 3.2044 | 2712.2714 | 2692.9776 | 2679.5700 |
| 3.2154 | 2610.9508 | 2670.4428 | 2657.5391 |
| 3.2264 | 2588.1372 | 2647.9356 | 2635.5082 |
| 3.2374 | 2610.5339 | 2625.4540 | 2613.4774 |
| 3.2484 | 2565.6667 | 2602.9962 | 2591.4465 |
| 3.2594 | 2557.0177 | 2580.5606 | 2569.4156 |
| 3.2704 | 2539.1244 | 2558.1457 | 2547.3847 |
| 3.2814 | 2513.3471 | 2535.7502 | 2525.3538 |
| 3.2924 | 2473.4911 | 2513.3726 | 2503.3229 |
| 3.3034 | 2423.9676 | 2491.0120 | 2481.2920 |
| 3.3144 | 2479.2955 | 2471.2576 | 2459.2611 |
| 3.3254 | 2481.5546 | 2453.7787 | 2444.6717 |
| 3.3364 | 2429.0241 | 2438.9042 | 2430.0823 |
| 3.3474 | 2386.0216 | 2424.0427 | 2415.4929 |
| 3.3584 | 2384.4720 | 2409.1936 | 2400.9035 |
| 3.3694 | 2385.1327 | 2394.3560 | 2386.3142 |
| 3.3804 | 2327.7714 | 2379.5293 | 2371.7248 |
| 3.3914 | 2310.0089 | 2364.7129 | 2357.1354 |
| 3.4024 | 2359.3407 | 2349.9062 | 2342.5460 |
| 3.4134 | 2381.8407 | 2335.1086 | 2327.9566 |
| 3.4244 | 2352.2360 | 2320.3197 | 2313.3672 |
| 3.4354 | 2344.1632 | 2305.5390 | 2298.7778 |
| 3.4464 | 2336.3569 | 2290.7660 | 2284.1884 |
| 3.4574 | 2319.5310 | 2276.0004 | 2269.5990 |
| 3.4684 | 2294.0546 | 2261.2417 | 2255.0097 |
| 3.4794 | 2208.8889 | 2246.4896 | 2240.4203 |
| 3.4904 | 2247.4558 | 2231.7437 | 2225.8309 |
| 3.5014 | 2243.6755 | 2217.7827 | 2211.2415 |
| 3.5124 | 2172.7610 | 2204.5071 | 2198.8896 |
| 3.5234 | 2145.8230 | 2192.0369 | 2186.5377 |
| 3.5344 | 2203.5103 | 2179.6554 | 2174.1858 |
| 3.5454 | 2168.8987 | 2167.1863 | 2161.8339 |
| 3.5564 | 2124.7419 | 2154.7640 | 2149.4819 |
| 3.5674 | 2102.0934 | 2142.2941 | 2137.1300 |
| 3.5784 | 2125.7896 | 2129.8285 | 2124.7781 |
| 3.5894 | 2149.6283 | 2117.3669 | 2112.4262 |
| 3.6004 | 2157.9110 | 2104.9092 | 2100.0743 |
| 3.6114 | 2070.0167 | 2092.4553 | 2087.7224 |
| 3.6224 | 2096.2139 | 2080.0048 | 2075.3705 |
| 3.6334 | 2118.6480 | 2067.5578 | 2063.0186 |
| 3.6444 | 2061.9729 | 2055.1141 | 2050.6667 |
| 3.6554 | 2054.2183 | 2042.6734 | 2038.3148 |
| 3.6664 | 2034.4572 | 2030.2358 | 2025.9629 |
| 3.6774 | 2078.7532 | 2017.8010 | 2013.6110 |
| 3.6884 | 2027.8849 | 2005.3690 | 2001.2591 |
| 3.6994 | 2027.1426 | 1992.9396 | 1988.9071 |
| 3.7104 | 1929.3426 | 1980.5128 | 1976.5552 |
| 3.7214 | 1966.7050 | 1968.0884 | 1964.2033 |
| 3.7324 | 2026.7817 | 1955.6664 | 1951.8514 |
| 3.7434 | 2028.1740 | 1943.2467 | 1939.4995 |
| 3.7544 | 1946.8864 | 1930.8291 | 1927.1476 |
| 3.7654 | 1910.1367 | 1918.4136 | 1914.7957 |
| 3.7764 | 1782.7271 | 1906.0002 | 1902.4438 |
| 3.7874 | 1933.6284 | 1893.5887 | 1890.0919 |
| 3.7984 | 1908.0069 | 1881.1791 | 1877.7400 |
| 3.8094 | 1909.0246 | 1868.7713 | 1865.3881 |
| 3.8204 | 1848.2242 | 1856.3652 | 1853.0362 |
| 3.8314 | 1856.4838 | 1843.9609 | 1840.6842 |
| 3.8424 | 1867.1583 | 1831.5582 | 1828.3323 |
| 3.8534 | 1849.9233 | 1819.1571 | 1815.9804 |
| 3.8644 | 1817.7615 | 1806.7576 | 1803.6285 |
| 3.8754 | 1787.5103 | 1795.3206 | 1791.2766 |
| 3.8864 | 1754.4425 | 1784.7238 | 1781.6856 |
| 3.8974 | 1769.6126 | 1775.0895 | 1772.0946 |
| 3.9084 | 1716.4621 | 1765.4565 | 1762.5035 |
| 3.9194 | 1708.4986 | 1755.8249 | 1752.9125 |
| 3.9304 | 1798.0196 | 1746.1945 | 1743.3215 |
| 3.9414 | 1725.1632 | 1736.5654 | 1733.7305 |
| 3.9524 | 1737.9351 | 1726.9376 | 1724.1395 |
| 3.9634 | 1779.1632 | 1717.3109 | 1714.5484 |
| 3.9744 | 1720.8029 | 1707.6853 | 1704.9574 |
| 3.9854 | 1746.1239 | 1698.0609 | 1695.3664 |
| 3.9964 | 1756.2468 | 1688.4376 | 1685.7754 |
| 4.0074 | 1728.2173 | 1678.8154 | 1676.1844 |
| 4.0184 | 1639.1726 | 1669.1942 | 1666.5933 |
| 4.0294 | 1702.5683 | 1659.5741 | 1657.0023 |
| 4.0404 | 1654.0708 | 1649.9550 | 1647.4113 |
| 4.0514 | 1635.8496 | 1640.3368 | 1637.8203 |
| 4.0624 | 1628.9685 | 1631.3011 | 1628.2292 |
| 4.0734 | 1626.2212 | 1622.7739 | 1620.3086 |
| 4.0844 | 1600.6283 | 1614.8290 | 1612.3880 |
| 4.0954 | 1625.3353 | 1606.8850 | 1604.4674 |
| 4.1064 | 1646.1603 | 1598.9420 | 1596.5468 |
| 4.1174 | 1639.3746 | 1590.9999 | 1588.6262 |
| 4.1284 | 1555.5339 | 1583.0586 | 1580.7056 |
| 4.1394 | 1550.3068 | 1575.1182 | 1572.7850 |
| 4.1504 | 1570.6637 | 1567.1787 | 1564.8644 |
| 4.1614 | 1592.7276 | 1559.2401 | 1556.9438 |
| 4.1724 | 1568.1971 | 1551.3023 | 1549.0232 |
| 4.1834 | 1551.8407 | 1543.3653 | 1541.1026 |
| 4.1944 | 1573.1347 | 1535.4292 | 1533.1820 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 5 Etosha18 HS 0-2cm S1 550C | 2.0054 | 29.9894 | 0.0110 | 12/7/2023 11:46:42 AM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 2.6544 | 631.25 | 0.2165 | 33.25742 | 98.89 |
| 5.2640 | 133.77 | 0.1732 | 16.77437 | 20.96 |
| 8.7463 | 581.92 | 0.1515 | 10.10210 | 91.16 |
| 15.8233 | 638.32 | 0.1082 | 5.59623 | 100.00 |
| 17.6100 | 23.88 | 0.2598 | 5.03226 | 3.74 |
| 18.2965 | 54.65 | 0.1299 | 4.84496 | 8.56 |
| 19.7240 | 20.64 | 0.5196 | 4.49742 | 3.23 |
| 24.3600 | 24.64 | 0.2598 | 3.65099 | 3.86 |
| 26.1040 | 279.71 | 0.1732 | 3.41089 | 43.82 |
| 26.7154 | 113.97 | 0.1732 | 3.33420 | 17.86 |
| 27.4384 | 117.33 | 0.1299 | 3.24796 | 18.38 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-076-6569 | 59 | Sodium Aluminum Silicate Hydrate | Na0.9 ( ( Al0.9 Si2 ) O6 ) ( H2 O ) | Analcime | 43 |
| * | 01-081-8598 | 25 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | ( Mg2 Al2 ) Si8 O20 ( H2 O )4 ( O H )2 ( H2 O )3.84 | Palygorskite-M | 8 |
| * | 04-025-4215 | 42 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 13 |
| * | 04-024-2561 | 55 | Potassium Sodium Magnesium Aluminum Iron Silicon Titanium Oxide Fluoride Hydroxide | K0.92 Na0.04 Mg1.74 Ti0.14 Fe1.05 Al1.39 Si2.69 O10.44 ( O H )1.35 F0.21 | Phlogopite-1M | 36 |

Anchor Scan Parameters

Dataset Name	5 Etosha18 HS 0-2cm S1 550C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 5\5 Etosha18 HS 0-2cm S1 550C.xrdml

Sample Identification	5 Etosha18 HS 0-2cm S1 550C

Measurement Start Date/Time	12/7/2023 11:46:42 AM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes