5 Etosha 18 HS 0-2 cm S1 REGULAR

Graphics

Graphics

Graphics

Quantitative Results

Phase Potassium Sodium Iron Magnesium Aluminum Silicate Fluoride Hydroxide

Weight fraction/ %	39.0

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	28.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	15.0

Phase Magnesium Silicate Hydroxide Hydrate

Weight fraction/ %	12.0

Phase Magnesium Aluminum Silicon Oxide Hydroxide Hydrate

Weight fraction/ %	6.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Potassium Sodium Iron Magnesium Aluminum Silicate Fluoride Hydroxide | Sodium Aluminum Silicate Hydrate | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Magnesium Silicate Hydroxide Hydrate | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Tin Oxide |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 5 Etosha18 HS 0-2cm S1 | 39.0 | 28.0 | 15.0 | 0.0 | 12.0 | 6.0 | 0.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 4901.0000 | 4901.0000 | 4901.0000 |
| 2.0164 | 4904.3977 | 4871.5802 | 4871.5802 |
| 2.0274 | 4856.8604 | 4842.1603 | 4842.1603 |
| 2.0384 | 4885.6534 | 4812.7405 | 4812.7405 |
| 2.0494 | 4743.4435 | 4783.3207 | 4783.3207 |
| 2.0604 | 4688.7148 | 4753.9009 | 4753.9009 |
| 2.0714 | 4613.0885 | 4724.4810 | 4724.4810 |
| 2.0824 | 4669.4287 | 4695.0612 | 4695.0612 |
| 2.0934 | 4596.4730 | 4665.6414 | 4665.6414 |
| 2.1044 | 4655.2655 | 4636.2215 | 4636.2215 |
| 2.1154 | 4579.3353 | 4606.8017 | 4606.8017 |
| 2.1264 | 4585.4543 | 4577.3819 | 4577.3819 |
| 2.1374 | 4512.5428 | 4547.9621 | 4547.9621 |
| 2.1484 | 4477.0054 | 4518.5422 | 4518.5422 |
| 2.1594 | 4463.3992 | 4489.1224 | 4489.1224 |
| 2.1704 | 4464.3392 | 4459.7026 | 4459.7026 |
| 2.1814 | 4354.6578 | 4430.2827 | 4430.2827 |
| 2.1924 | 4494.3446 | 4400.8629 | 4400.8629 |
| 2.2034 | 4343.7965 | 4374.2422 | 4374.2422 |
| 2.2144 | 4305.4135 | 4347.6215 | 4347.6215 |
| 2.2254 | 4249.3864 | 4321.0008 | 4321.0008 |
| 2.2364 | 4302.0944 | 4294.3800 | 4294.3800 |
| 2.2474 | 4218.7611 | 4267.7593 | 4267.7593 |
| 2.2584 | 4147.1465 | 4241.1386 | 4241.1386 |
| 2.2694 | 4268.4307 | 4214.5179 | 4214.5179 |
| 2.2804 | 4201.2778 | 4187.8972 | 4187.8972 |
| 2.2914 | 4129.3913 | 4161.2765 | 4161.2765 |
| 2.3024 | 4164.2389 | 4134.6557 | 4134.6557 |
| 2.3134 | 4191.8574 | 4108.0350 | 4108.0350 |
| 2.3244 | 4117.7320 | 4081.4143 | 4081.4143 |
| 2.3354 | 3969.2596 | 4054.7936 | 4054.7936 |
| 2.3464 | 3876.7183 | 4028.1729 | 4028.1729 |
| 2.3574 | 3943.8584 | 4001.5522 | 4001.5522 |
| 2.3684 | 4011.6578 | 3974.9314 | 3974.9314 |
| 2.3794 | 3993.4494 | 3948.3107 | 3948.3107 |
| 2.3904 | 3878.3776 | 3929.4880 | 3929.4880 |
| 2.4014 | 3872.3894 | 3910.6652 | 3910.6652 |
| 2.4124 | 3877.3274 | 3891.8425 | 3891.8425 |
| 2.4234 | 3783.3953 | 3873.0197 | 3873.0197 |
| 2.4344 | 3853.6962 | 3854.1970 | 3854.1970 |
| 2.4454 | 3932.5752 | 3835.3742 | 3835.3742 |
| 2.4564 | 3892.2207 | 3816.5515 | 3816.5515 |
| 2.4674 | 3835.8348 | 3797.7287 | 3797.7287 |
| 2.4784 | 3800.6731 | 3778.9060 | 3778.9060 |
| 2.4894 | 3857.3048 | 3760.0832 | 3760.0832 |
| 2.5004 | 3801.4026 | 3741.2605 | 3741.2605 |
| 2.5114 | 3700.6499 | 3722.4377 | 3722.4377 |
| 2.5224 | 3657.4508 | 3703.6150 | 3703.6150 |
| 2.5334 | 3619.3805 | 3684.7922 | 3684.7922 |
| 2.5444 | 3720.4071 | 3665.9695 | 3665.9695 |
| 2.5554 | 3749.5959 | 3647.1467 | 3647.1467 |
| 2.5664 | 3676.6136 | 3628.3240 | 3628.3240 |
| 2.5774 | 3713.5526 | 3609.5012 | 3609.5012 |
| 2.5884 | 3599.5206 | 3590.6785 | 3590.6785 |
| 2.5994 | 3627.1859 | 3571.8557 | 3571.8557 |
| 2.6104 | 3614.3992 | 3553.0330 | 3553.0330 |
| 2.6214 | 3552.4031 | 3534.2102 | 3534.2102 |
| 2.6324 | 3455.6298 | 3515.3875 | 3515.3875 |
| 2.6434 | 3485.5851 | 3496.5647 | 3496.5647 |
| 2.6544 | 3559.1362 | 3477.7420 | 3477.7420 |
| 2.6654 | 3562.9882 | 3458.9192 | 3458.9192 |
| 2.6764 | 3499.5192 | 3440.0965 | 3440.0965 |
| 2.6874 | 3475.4277 | 3421.2737 | 3421.2737 |
| 2.6984 | 3357.0752 | 3402.4510 | 3402.4510 |
| 2.7094 | 3330.8663 | 3383.6282 | 3383.6282 |
| 2.7204 | 3423.2778 | 3364.8055 | 3364.8055 |
| 2.7314 | 3410.3068 | 3345.9827 | 3345.9827 |
| 2.7424 | 3305.6504 | 3327.1600 | 3327.1600 |
| 2.7534 | 3246.5536 | 3308.9396 | 3308.3372 |
| 2.7644 | 3322.9602 | 3293.8602 | 3293.8602 |
| 2.7754 | 3313.0492 | 3279.3831 | 3279.3831 |
| 2.7864 | 3272.3481 | 3264.9061 | 3264.9061 |
| 2.7974 | 3245.7611 | 3250.4290 | 3250.4290 |
| 2.8084 | 3234.0275 | 3235.9520 | 3235.9520 |
| 2.8194 | 3285.7532 | 3221.4750 | 3221.4750 |
| 2.8304 | 3194.2080 | 3206.9979 | 3206.9979 |
| 2.8414 | 3200.9459 | 3192.5209 | 3192.5209 |
| 2.8524 | 3169.8220 | 3178.0438 | 3178.0438 |
| 2.8634 | 3050.0796 | 3163.5668 | 3163.5668 |
| 2.8744 | 3164.4322 | 3149.0898 | 3149.0898 |
| 2.8854 | 3124.7355 | 3134.6127 | 3134.6127 |
| 2.8964 | 3102.0973 | 3120.1357 | 3120.1357 |
| 2.9074 | 3186.7168 | 3105.6586 | 3105.6586 |
| 2.9184 | 3149.6091 | 3091.1816 | 3091.1816 |
| 2.9294 | 3079.9882 | 3076.7045 | 3076.7045 |
| 2.9404 | 3020.4027 | 3062.2944 | 3062.2275 |
| 2.9514 | 3033.3343 | 3048.2334 | 3048.2334 |
| 2.9624 | 3098.2758 | 3034.2393 | 3034.2393 |
| 2.9734 | 3019.9971 | 3020.2452 | 3020.2452 |
| 2.9844 | 3134.1534 | 3006.2510 | 3006.2510 |
| 2.9954 | 2943.6195 | 2992.2569 | 2992.2569 |
| 3.0064 | 3031.2227 | 2978.2628 | 2978.2628 |
| 3.0174 | 3018.9154 | 2964.2687 | 2964.2687 |
| 3.0284 | 3004.6843 | 2950.2746 | 2950.2746 |
| 3.0394 | 2895.4287 | 2936.2805 | 2936.2805 |
| 3.0504 | 2952.7733 | 2922.2864 | 2922.2864 |
| 3.0614 | 2902.3599 | 2908.2923 | 2908.2923 |
| 3.0724 | 2903.2311 | 2894.2981 | 2894.2981 |
| 3.0834 | 2898.3638 | 2880.3040 | 2880.3040 |
| 3.0944 | 2888.9646 | 2866.3099 | 2866.3099 |
| 3.1054 | 2889.6844 | 2852.3158 | 2852.3158 |
| 3.1164 | 2902.6878 | 2838.3217 | 2838.3217 |
| 3.1274 | 2801.9882 | 2824.4168 | 2824.3276 |
| 3.1384 | 2758.0433 | 2810.9775 | 2810.9775 |
| 3.1494 | 2787.4523 | 2797.6274 | 2797.6274 |
| 3.1604 | 2807.1357 | 2784.2773 | 2784.2773 |
| 3.1714 | 2787.9321 | 2770.9272 | 2770.9272 |
| 3.1824 | 2733.6111 | 2757.5772 | 2757.5772 |
| 3.1934 | 2787.7522 | 2744.2271 | 2744.2271 |
| 3.2044 | 2748.1534 | 2730.8770 | 2730.8770 |
| 3.2154 | 2761.8879 | 2717.5269 | 2717.5269 |
| 3.2264 | 2726.3053 | 2704.1768 | 2704.1768 |
| 3.2374 | 2709.4130 | 2690.8268 | 2690.8268 |
| 3.2484 | 2746.9444 | 2677.4767 | 2677.4767 |
| 3.2594 | 2663.0737 | 2664.1266 | 2664.1266 |
| 3.2704 | 2664.7419 | 2650.7765 | 2650.7765 |
| 3.2814 | 2697.1160 | 2637.4264 | 2637.4264 |
| 3.2924 | 2607.5531 | 2624.0764 | 2624.0764 |
| 3.3034 | 2601.6028 | 2610.7263 | 2610.7263 |
| 3.3144 | 2618.4912 | 2597.5287 | 2597.3762 |
| 3.3254 | 2603.0796 | 2585.1260 | 2585.1260 |
| 3.3364 | 2528.5865 | 2572.8758 | 2572.8758 |
| 3.3474 | 2521.4641 | 2560.6255 | 2560.6255 |
| 3.3584 | 2585.1254 | 2548.3753 | 2548.3753 |
| 3.3694 | 2573.2655 | 2536.1251 | 2536.1251 |
| 3.3804 | 2457.4700 | 2523.8749 | 2523.8749 |
| 3.3914 | 2442.4160 | 2511.6247 | 2511.6247 |
| 3.4024 | 2499.2193 | 2499.3744 | 2499.3744 |
| 3.4134 | 2463.2861 | 2487.1242 | 2487.1242 |
| 3.4244 | 2461.0339 | 2474.8740 | 2474.8740 |
| 3.4354 | 2466.8584 | 2462.6238 | 2462.6238 |
| 3.4464 | 2454.1696 | 2450.3736 | 2450.3736 |
| 3.4574 | 2459.2242 | 2438.1233 | 2438.1233 |
| 3.4684 | 2477.5983 | 2425.8731 | 2425.8731 |
| 3.4794 | 2460.1200 | 2413.6229 | 2413.6229 |
| 3.4904 | 2434.7920 | 2401.3727 | 2401.3727 |
| 3.5014 | 2426.9852 | 2389.1225 | 2389.1225 |
| 3.5124 | 2463.6131 | 2376.8723 | 2376.8723 |
| 3.5234 | 2407.9026 | 2364.6220 | 2364.6220 |
| 3.5344 | 2385.2099 | 2352.3718 | 2352.3718 |
| 3.5454 | 2372.4228 | 2340.1216 | 2340.1216 |
| 3.5564 | 2330.8141 | 2327.8714 | 2327.8714 |
| 3.5674 | 2265.8269 | 2315.6212 | 2315.6212 |
| 3.5784 | 2270.7286 | 2303.3709 | 2303.3709 |
| 3.5894 | 2283.3894 | 2291.1207 | 2291.1207 |
| 3.6004 | 2274.0492 | 2278.8705 | 2278.8705 |
| 3.6114 | 2259.8771 | 2266.6203 | 2266.6203 |
| 3.6224 | 2183.5826 | 2254.3701 | 2254.3701 |
| 3.6334 | 2237.2596 | 2242.1198 | 2242.1198 |
| 3.6444 | 2322.8348 | 2229.8696 | 2229.8696 |
| 3.6554 | 2203.7020 | 2217.6194 | 2217.6194 |
| 3.6664 | 2246.6200 | 2205.3692 | 2205.3692 |
| 3.6774 | 2144.2605 | 2193.1190 | 2193.1190 |
| 3.6884 | 2166.6239 | 2181.6267 | 2180.8687 |
| 3.6994 | 2172.0000 | 2174.0864 | 2174.0864 |
| 3.7104 | 2276.9931 | 2167.3040 | 2167.3040 |
| 3.7214 | 2244.8820 | 2160.5217 | 2160.5217 |
| 3.7324 | 2237.2812 | 2153.7393 | 2153.7393 |
| 3.7434 | 2231.3481 | 2146.9570 | 2146.9570 |
| 3.7544 | 2235.7714 | 2140.1746 | 2140.1746 |
| 3.7654 | 2142.2428 | 2133.3923 | 2133.3923 |
| 3.7764 | 2155.6406 | 2126.6099 | 2126.6099 |
| 3.7874 | 2239.2567 | 2119.8276 | 2119.8276 |
| 3.7984 | 2163.8899 | 2113.0452 | 2113.0452 |
| 3.8094 | 2133.3845 | 2106.2629 | 2106.2629 |
| 3.8204 | 2220.0000 | 2099.4805 | 2099.4805 |
| 3.8314 | 2216.2104 | 2092.6982 | 2092.6982 |
| 3.8424 | 2126.6839 | 2085.9158 | 2085.9158 |
| 3.8534 | 2138.7404 | 2079.1335 | 2079.1335 |
| 3.8644 | 2129.8284 | 2072.3511 | 2072.3511 |
| 3.8754 | 2074.2635 | 2065.5688 | 2065.5688 |
| 3.8864 | 2143.0885 | 2058.7864 | 2058.7864 |
| 3.8974 | 2178.7610 | 2052.0041 | 2052.0041 |
| 3.9084 | 2113.1913 | 2045.2217 | 2045.2217 |
| 3.9194 | 2140.0560 | 2038.4394 | 2038.4394 |
| 3.9304 | 2042.8112 | 2031.6570 | 2031.6570 |
| 3.9414 | 2054.3058 | 2024.8747 | 2024.8747 |
| 3.9524 | 2068.0207 | 2018.0923 | 2018.0923 |
| 3.9634 | 2088.9803 | 2011.3100 | 2011.3100 |
| 3.9744 | 2010.3869 | 2004.5276 | 2004.5276 |
| 3.9854 | 1929.0620 | 1997.7453 | 1997.7453 |
| 3.9964 | 2012.3387 | 1990.9629 | 1990.9629 |
| 4.0074 | 1988.2419 | 1984.1806 | 1984.1806 |
| 4.0184 | 2039.1873 | 1977.3982 | 1977.3982 |
| 4.0294 | 2070.8289 | 1970.6159 | 1970.6159 |
| 4.0404 | 1981.3692 | 1963.8335 | 1963.8335 |
| 4.0514 | 1983.8555 | 1957.0512 | 1957.0512 |
| 4.0624 | 1971.7488 | 1950.2539 | 1950.2688 |
| 4.0734 | 1946.8928 | 1943.3790 | 1943.3790 |
| 4.0844 | 1950.6593 | 1936.4892 | 1936.4892 |
| 4.0954 | 1944.8348 | 1929.5993 | 1929.5993 |
| 4.1064 | 1904.6416 | 1922.7095 | 1922.7095 |
| 4.1174 | 1947.3156 | 1915.8197 | 1915.8197 |
| 4.1284 | 1970.6278 | 1908.9298 | 1908.9298 |
| 4.1394 | 1965.3864 | 1902.0400 | 1902.0400 |
| 4.1504 | 1946.4941 | 1895.1502 | 1895.1502 |
| 4.1614 | 1942.0895 | 1888.2603 | 1888.2603 |
| 4.1724 | 1926.4503 | 1881.3705 | 1881.3705 |
| 4.1834 | 1909.7876 | 1874.4807 | 1874.4807 |
| 4.1944 | 1891.5845 | 1867.5908 | 1867.5908 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 5 Etosha18 HS 0-2cm S1 | 2.0054 | 29.9894 | 0.0110 | 11/30/2023 2:34:15 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 7.1979 | 1464.73 | 0.1299 | 12.27138 | 100.00 |
| 8.7463 | 412.59 | 0.0866 | 10.10207 | 28.17 |
| 12.9654 | 15.91 | 0.5196 | 6.82264 | 1.09 |
| 15.7347 | 978.73 | 0.0974 | 5.62754 | 66.82 |
| 17.6471 | 50.51 | 0.2165 | 5.02178 | 3.45 |
| 18.2181 | 143.40 | 0.1082 | 4.86564 | 9.79 |
| 19.6404 | 76.70 | 0.5196 | 4.51639 | 5.24 |
| 23.4484 | 26.66 | 0.3464 | 3.79082 | 1.82 |
| 24.1947 | 34.11 | 0.1299 | 3.67556 | 2.33 |
| 25.9210 | 914.16 | 0.0866 | 3.43455 | 62.41 |
| 26.6883 | 176.79 | 0.3031 | 3.33752 | 12.07 |
| 27.5383 | 77.04 | 0.1732 | 3.23641 | 5.26 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-085-2271 | 56 | Potassium Sodium Iron Magnesium Aluminum Silicate Fluoride Hydroxide | ( K0.93 Na0.04 ) ( Mg2.48 Fe0.24 Al0.24 ) ( Si2.74 Al1.26 O10 ) ( ( O H )1.94 F0.06 ) | Phlogopite-1M | 39 |
| * | 01-070-1575 | 55 | Sodium Aluminum Silicate Hydrate | Na ( Al Si2 O6 ) ( H2 O ) | Analcime | 28 |
| * | 01-082-8023 | 22 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 15 |
| * | 04-025-4215 | No Matching Lines | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | - |
| * | 01-080-5019 | 30 | Magnesium Silicate Hydroxide Hydrate | Mg7.68 ( Si12 O30 ) ( O H )4 ( H2 O )4 ( H2 O )6 | Sepiolite | 12 |
| * | 04-015-2962 | 23 | Magnesium Aluminum Silicon Oxide Hydroxide Hydrate | Mg Al Si4 O10 ( O H ) ( H2 O )4 | Palygorskite-M | 6 |
| * | 01-087-9078 | No Matching Lines | Tin Oxide | Sn O2 | Cassiterite | - |

Anchor Scan Parameters

Dataset Name	5 Etosha18 HS 0-2cm S1

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 5\5 Etosha18 HS 0-2cm S1.xrdml

Sample Identification	5 Etosha18 HS 0-2cm S1

Measurement Start Date/Time	11/30/2023 2:34:15 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes