6 Etosha 18 Ssub 2-5 cm S1 400C

Graphics

Graphics

Graphics

Quantitative Results

Phase Sodium Aluminum Silicate Hydrate

Weight fraction/ %	25.0

Phase Potassium Sodium Magnesium Aluminum Iron Titanium Silicate Hydroxide

Weight fraction/ %	25.0

Phase Sodium Magnesium Silicon Oxide Hydrate

Weight fraction/ %	8.0

Phase Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide

Weight fraction/ %	42.0

Multiple Quantitative Results

Scans vs Phases Matrix

| Scan name | Sodium Aluminum Silicate Hydrate | Potassium Sodium Magnesium Aluminum Iron Titanium Silicate Hydroxide | Sodium Magnesium Silicon Oxide Hydrate | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide |
| --- | --- | --- | --- | --- |
| 6 Etosha18 Ssub 2-5cm S1 400C | 25.0 | 25.0 | 8.0 | 42.0 |

Anchor Scan Data

| Pos. [°2θ] | Iobs [cts] | Icalc [cts] | Iback [cts] |
| --- | --- | --- | --- |
| 2.0054 | 6904.0000 | 6893.2140 | 6904.0000 |
| 2.0164 | 6863.0123 | 6862.8846 | 6861.1965 |
| 2.0274 | 6858.5428 | 6820.0884 | 6818.3929 |
| 2.0384 | 6642.0369 | 6777.2922 | 6775.5894 |
| 2.0494 | 6637.9361 | 6734.4961 | 6732.7858 |
| 2.0604 | 6539.3240 | 6691.7001 | 6689.9823 |
| 2.0714 | 6539.9882 | 6648.9041 | 6647.1787 |
| 2.0824 | 6671.1170 | 6606.1081 | 6604.3752 |
| 2.0934 | 6573.6145 | 6563.3122 | 6561.5716 |
| 2.1044 | 6362.0575 | 6520.5164 | 6518.7681 |
| 2.1154 | 6438.4739 | 6477.7206 | 6475.9646 |
| 2.1264 | 6279.4263 | 6434.9248 | 6433.1610 |
| 2.1374 | 6221.7139 | 6392.1291 | 6390.3575 |
| 2.1484 | 6313.3736 | 6349.3335 | 6347.5539 |
| 2.1594 | 6124.6165 | 6306.5379 | 6304.7504 |
| 2.1704 | 6222.6873 | 6263.7424 | 6261.9468 |
| 2.1814 | 6221.6942 | 6220.9469 | 6219.1433 |
| 2.1924 | 6159.7758 | 6180.7778 | 6176.3397 |
| 2.2034 | 6171.9823 | 6144.3733 | 6142.5534 |
| 2.2144 | 6075.5811 | 6110.5952 | 6108.7671 |
| 2.2254 | 5973.2389 | 6076.8172 | 6074.9808 |
| 2.2364 | 5912.6180 | 6043.0392 | 6041.1945 |
| 2.2474 | 5997.1377 | 6009.2613 | 6007.4082 |
| 2.2584 | 5993.4730 | 5975.4834 | 5973.6218 |
| 2.2694 | 5970.8289 | 5941.7056 | 5939.8355 |
| 2.2804 | 5950.4828 | 5907.9279 | 5906.0492 |
| 2.2914 | 5826.6264 | 5874.1502 | 5872.2629 |
| 2.3024 | 5857.5708 | 5840.3725 | 5838.4766 |
| 2.3134 | 5682.8908 | 5806.5950 | 5804.6902 |
| 2.3244 | 5599.1986 | 5772.8175 | 5770.9039 |
| 2.3354 | 5643.9705 | 5739.0400 | 5737.1176 |
| 2.3464 | 5608.0044 | 5705.2626 | 5703.3313 |
| 2.3574 | 5643.8535 | 5671.4853 | 5669.5450 |
| 2.3684 | 5631.6991 | 5637.7080 | 5635.7586 |
| 2.3794 | 5593.8368 | 5603.9159 | 5601.9723 |
| 2.3904 | 5570.1962 | 5570.1025 | 5568.1349 |
| 2.4014 | 5542.0973 | 5536.2743 | 5534.2974 |
| 2.4124 | 5515.7434 | 5502.4462 | 5500.4599 |
| 2.4234 | 5470.4621 | 5468.6181 | 5466.6224 |
| 2.4344 | 5374.9587 | 5434.7900 | 5432.7850 |
| 2.4454 | 5314.0531 | 5400.9621 | 5398.9475 |
| 2.4564 | 5388.5816 | 5367.1342 | 5365.1100 |
| 2.4674 | 5394.3953 | 5333.3064 | 5331.2725 |
| 2.4784 | 5263.5438 | 5299.4786 | 5297.4351 |
| 2.4894 | 5241.9390 | 5265.6509 | 5263.5976 |
| 2.5004 | 5232.7655 | 5231.8233 | 5229.7601 |
| 2.5114 | 5192.5959 | 5197.9958 | 5195.9226 |
| 2.5224 | 5190.6170 | 5164.1683 | 5162.0852 |
| 2.5334 | 5225.9794 | 5130.3409 | 5128.2477 |
| 2.5444 | 5190.4326 | 5096.5136 | 5094.4102 |
| 2.5554 | 5035.0167 | 5062.6863 | 5060.5728 |
| 2.5664 | 5004.8938 | 5030.2569 | 5026.7353 |
| 2.5774 | 4973.9213 | 4999.8310 | 4997.6968 |
| 2.5884 | 4979.7370 | 4970.8029 | 4968.6582 |
| 2.5994 | 5038.8319 | 4941.7749 | 4939.6197 |
| 2.6104 | 4924.8264 | 4912.7470 | 4910.5812 |
| 2.6214 | 4834.1563 | 4883.7191 | 4881.5426 |
| 2.6324 | 4881.5502 | 4854.6914 | 4852.5041 |
| 2.6434 | 4924.1091 | 4825.6637 | 4823.4656 |
| 2.6544 | 4798.2935 | 4796.6361 | 4794.4270 |
| 2.6654 | 4767.1740 | 4767.6085 | 4765.3885 |
| 2.6764 | 4839.2286 | 4738.5811 | 4736.3500 |
| 2.6874 | 4806.8948 | 4709.5537 | 4707.3114 |
| 2.6984 | 4676.1725 | 4680.5264 | 4678.2729 |
| 2.7094 | 4681.5447 | 4651.4992 | 4649.2344 |
| 2.7204 | 4731.9459 | 4622.4721 | 4620.1959 |
| 2.7314 | 4571.6460 | 4593.4451 | 4591.1573 |
| 2.7424 | 4569.0575 | 4564.4182 | 4562.1188 |
| 2.7534 | 4583.6863 | 4535.3913 | 4533.0803 |
| 2.7644 | 4462.8761 | 4506.3646 | 4504.0417 |
| 2.7754 | 4550.2675 | 4477.3379 | 4475.0032 |
| 2.7864 | 4510.4041 | 4448.3113 | 4445.9647 |
| 2.7974 | 4432.0885 | 4419.2848 | 4416.9261 |
| 2.8084 | 4479.5266 | 4390.2585 | 4387.8876 |
| 2.8194 | 4254.9774 | 4361.2322 | 4358.8491 |
| 2.8304 | 4287.3097 | 4332.2059 | 4329.8105 |
| 2.8414 | 4193.9174 | 4303.1798 | 4300.7720 |
| 2.8524 | 4450.1023 | 4274.1538 | 4271.7335 |
| 2.8634 | 4243.5398 | 4245.1279 | 4242.6950 |
| 2.8744 | 4140.7846 | 4216.1021 | 4213.6564 |
| 2.8854 | 4108.5015 | 4187.0764 | 4184.6179 |
| 2.8964 | 4024.3717 | 4158.0508 | 4155.5794 |
| 2.9074 | 4076.5271 | 4129.0253 | 4126.5408 |
| 2.9184 | 4141.3672 | 4099.9999 | 4097.5023 |
| 2.9294 | 4061.9351 | 4070.9746 | 4068.4638 |
| 2.9404 | 4057.8972 | 4043.4492 | 4039.4252 |
| 2.9514 | 4005.0727 | 4015.7178 | 4013.1802 |
| 2.9624 | 3881.2095 | 3989.4863 | 3986.9352 |
| 2.9734 | 3972.7768 | 3963.2549 | 3960.6902 |
| 2.9844 | 3911.1829 | 3937.0237 | 3934.4451 |
| 2.9954 | 3881.9823 | 3910.7925 | 3908.2001 |
| 3.0064 | 3845.6868 | 3884.5615 | 3881.9551 |
| 3.0174 | 3722.2704 | 3858.3306 | 3855.7101 |
| 3.0284 | 3843.5516 | 3832.0998 | 3829.4651 |
| 3.0394 | 3733.7925 | 3805.8691 | 3803.2200 |
| 3.0504 | 3588.2444 | 3779.6385 | 3776.9750 |
| 3.0614 | 3668.3953 | 3753.4080 | 3750.7300 |
| 3.0724 | 3716.1224 | 3727.1777 | 3724.4850 |
| 3.0834 | 3634.8643 | 3700.9475 | 3698.2400 |
| 3.0944 | 3618.1549 | 3674.7174 | 3671.9949 |
| 3.1054 | 3636.4395 | 3648.4874 | 3645.7499 |
| 3.1164 | 3607.1377 | 3622.2576 | 3619.5049 |
| 3.1274 | 3601.3422 | 3599.5520 | 3593.2599 |
| 3.1384 | 3592.6042 | 3576.3621 | 3573.5787 |
| 3.1494 | 3513.9390 | 3556.6965 | 3553.8975 |
| 3.1604 | 3514.7168 | 3537.0310 | 3534.2163 |
| 3.1714 | 3518.1317 | 3517.3656 | 3514.5351 |
| 3.1824 | 3520.8048 | 3497.7004 | 3494.8539 |
| 3.1934 | 3512.8583 | 3478.0353 | 3475.1727 |
| 3.2044 | 3372.3422 | 3458.3703 | 3455.4916 |
| 3.2154 | 3447.9891 | 3438.7055 | 3435.8104 |
| 3.2264 | 3391.3820 | 3419.0409 | 3416.1292 |
| 3.2374 | 3495.7532 | 3399.3763 | 3396.4480 |
| 3.2484 | 3414.9444 | 3379.7119 | 3376.7668 |
| 3.2594 | 3335.7463 | 3360.0477 | 3357.0856 |
| 3.2704 | 3418.6829 | 3340.3836 | 3337.4045 |
| 3.2814 | 3376.9282 | 3320.7196 | 3317.7233 |
| 3.2924 | 3293.9248 | 3301.0558 | 3298.0421 |
| 3.3034 | 3250.3766 | 3281.3922 | 3278.3609 |
| 3.3144 | 3234.7439 | 3265.5295 | 3258.6797 |
| 3.3254 | 3267.5988 | 3249.1446 | 3246.0778 |
| 3.3364 | 3288.6677 | 3236.5607 | 3233.4759 |
| 3.3474 | 3237.5634 | 3223.9769 | 3220.8740 |
| 3.3584 | 3185.7950 | 3211.3933 | 3208.2721 |
| 3.3694 | 3222.1082 | 3198.8099 | 3195.6702 |
| 3.3804 | 3210.2080 | 3186.2267 | 3183.0683 |
| 3.3914 | 3211.1770 | 3173.6436 | 3170.4664 |
| 3.4024 | 3209.6347 | 3161.0606 | 3157.8645 |
| 3.4134 | 3148.8722 | 3148.4779 | 3145.2626 |
| 3.4244 | 3165.8437 | 3135.8953 | 3132.6607 |
| 3.4354 | 3176.2822 | 3123.3129 | 3120.0588 |
| 3.4464 | 3099.3771 | 3110.7307 | 3107.4569 |
| 3.4574 | 3074.3156 | 3098.1486 | 3094.8550 |
| 3.4684 | 3037.9356 | 3085.5667 | 3082.2531 |
| 3.4794 | 3065.7011 | 3072.9850 | 3069.6512 |
| 3.4904 | 3119.3938 | 3060.4035 | 3057.0493 |
| 3.5014 | 3147.4464 | 3047.7738 | 3044.4474 |
| 3.5124 | 2991.5540 | 3035.1509 | 3031.7553 |
| 3.5234 | 2933.4041 | 3022.4798 | 3019.0632 |
| 3.5344 | 3009.7203 | 3009.8089 | 3006.3712 |
| 3.5454 | 2968.8082 | 2997.1382 | 2993.6791 |
| 3.5564 | 3007.2404 | 2984.4677 | 2980.9871 |
| 3.5674 | 3000.4415 | 2971.7974 | 2968.2950 |
| 3.5784 | 2980.9086 | 2959.1274 | 2955.6030 |
| 3.5894 | 2854.8141 | 2946.4575 | 2942.9109 |
| 3.6004 | 2913.4287 | 2933.7878 | 2930.2188 |
| 3.6114 | 2914.5762 | 2921.1183 | 2917.5268 |
| 3.6224 | 2908.8068 | 2908.4491 | 2904.8347 |
| 3.6334 | 2901.6283 | 2895.7800 | 2892.1427 |
| 3.6444 | 2845.9611 | 2883.1112 | 2879.4506 |
| 3.6554 | 2833.3127 | 2870.4426 | 2866.7586 |
| 3.6664 | 2844.9833 | 2857.7743 | 2854.0665 |
| 3.6774 | 2866.9695 | 2845.1061 | 2841.3744 |
| 3.6884 | 2797.7964 | 2832.4382 | 2828.6824 |
| 3.6994 | 2846.9263 | 2819.7706 | 2815.9903 |
| 3.7104 | 2837.7080 | 2807.1031 | 2803.2983 |
| 3.7214 | 2841.5044 | 2794.4360 | 2790.6062 |
| 3.7324 | 2840.1406 | 2781.7690 | 2777.9142 |
| 3.7434 | 2772.1770 | 2769.1023 | 2765.2221 |
| 3.7544 | 2663.9837 | 2756.4359 | 2752.5300 |
| 3.7654 | 2691.8633 | 2743.7697 | 2739.8380 |
| 3.7764 | 2714.5349 | 2731.1037 | 2727.1459 |
| 3.7874 | 2715.0000 | 2718.4381 | 2714.4539 |
| 3.7984 | 2687.0998 | 2705.7726 | 2701.7618 |
| 3.8094 | 2716.4405 | 2693.1075 | 2689.0698 |
| 3.8204 | 2744.0000 | 2680.4426 | 2676.3777 |
| 3.8314 | 2742.9115 | 2667.7780 | 2663.6856 |
| 3.8424 | 2713.6858 | 2655.1137 | 2650.9936 |
| 3.8534 | 2646.4070 | 2642.4497 | 2638.3015 |
| 3.8644 | 2548.4238 | 2629.7859 | 2625.6095 |
| 3.8754 | 2674.0835 | 2618.4258 | 2612.9174 |
| 3.8864 | 2575.5177 | 2606.8868 | 2602.6529 |
| 3.8974 | 2675.7345 | 2596.6515 | 2592.3883 |
| 3.9084 | 2599.6642 | 2586.4164 | 2582.1238 |
| 3.9194 | 2634.2891 | 2576.1817 | 2571.8593 |
| 3.9304 | 2674.1897 | 2565.9473 | 2561.5947 |
| 3.9414 | 2570.2458 | 2555.7132 | 2551.3302 |
| 3.9524 | 2540.9956 | 2545.4794 | 2541.0657 |
| 3.9634 | 2503.2026 | 2535.2459 | 2530.8011 |
| 3.9744 | 2541.7994 | 2525.0128 | 2520.5366 |
| 3.9854 | 2515.9734 | 2514.7799 | 2510.2721 |
| 3.9964 | 2442.4936 | 2504.5475 | 2500.0075 |
| 4.0074 | 2473.4032 | 2494.3154 | 2489.7430 |
| 4.0184 | 2490.5958 | 2484.0836 | 2479.4785 |
| 4.0294 | 2410.0010 | 2473.8521 | 2469.2139 |
| 4.0404 | 2434.4493 | 2463.6211 | 2458.9494 |
| 4.0514 | 2376.8643 | 2453.3904 | 2448.6849 |
| 4.0624 | 2403.6229 | 2444.1382 | 2438.4203 |
| 4.0734 | 2487.0935 | 2434.7520 | 2429.9777 |
| 4.0844 | 2556.2699 | 2426.3444 | 2421.5352 |
| 4.0954 | 2475.3471 | 2417.9371 | 2413.0926 |
| 4.1064 | 2453.2355 | 2409.5302 | 2404.6500 |
| 4.1174 | 2382.8466 | 2401.1238 | 2396.2074 |
| 4.1284 | 2347.7443 | 2392.7177 | 2387.7648 |
| 4.1394 | 2358.9961 | 2384.3120 | 2379.3222 |
| 4.1504 | 2401.1859 | 2375.9068 | 2370.8796 |
| 4.1614 | 2450.4081 | 2367.5019 | 2362.4370 |
| 4.1724 | 2413.4395 | 2359.0975 | 2353.9944 |
| 4.1834 | 2347.4690 | 2350.6936 | 2345.5518 |
| 4.1944 | 2397.9297 | 2342.2900 | 2337.1093 |

Scan List

| Vis. | Dataset Name | Start pos. [°2θ] | End pos. [°2θ] | Step [°2θ] | Meas.Date/Time |
| --- | --- | --- | --- | --- | --- |
| * | 6 Etosha18 Ssub 2-5cm S1 400C | 2.0054 | 29.9894 | 0.0110 | 12/5/2023 12:41:57 PM |

Peak List

| Pos. [°2θ] | Height [cts] | FWHM Left [°2θ] | d-spacing [Å] | Rel. Int. [%] |
| --- | --- | --- | --- | --- |
| 7.0671 | 1134.63 | 0.5196 | 12.49813 | 100.00 |
| 8.7169 | 879.26 | 0.2165 | 10.13606 | 77.49 |
| 10.5660 | 67.31 | 0.5196 | 8.36595 | 5.93 |
| 13.0819 | 21.63 | 0.5196 | 6.76216 | 1.91 |
| 15.7635 | 1133.24 | 0.1407 | 5.61734 | 99.88 |
| 17.6060 | 83.73 | 0.2598 | 5.03341 | 7.38 |
| 18.2619 | 129.77 | 0.1299 | 4.85406 | 11.44 |
| 19.6454 | 116.82 | 0.3464 | 4.51523 | 10.30 |
| 22.3684 | 13.01 | 0.3464 | 3.97136 | 1.15 |
| 24.2695 | 56.98 | 0.2165 | 3.66440 | 5.02 |
| 25.9510 | 901.09 | 0.0649 | 3.43065 | 79.42 |
| 26.7244 | 283.03 | 0.2598 | 3.33309 | 24.94 |
| 27.5420 | 128.28 | 0.1732 | 3.23599 | 11.31 |

Pattern List

| Visible | Ref.Code | Score | Compound Name | Chem. Formula | Mineral Name | SemiQuant[%] |
| --- | --- | --- | --- | --- | --- | --- |
| * | 01-072-4625 | 67 | Sodium Aluminum Silicate Hydrate | Na Al ( Si2 O6 ) ( H2 O ) | Analcime | 25 |
| * | 04-013-2149 | 33 | Potassium Sodium Magnesium Aluminum Iron Titanium Silicate Hydroxide | K0.78 Na0.22 Mg1.65 Ti0.5 Fe0.85 Al1.16 Si2.84 O10.84 ( O H )1.16 | Biotite-1M | 25 |
| * | 01-082-8023 | 24 | Sodium Magnesium Silicon Oxide Hydrate | Na2 Mg3 ( Si6 O16 ) ( H2 O )7 | Loughlinite | 8 |
| * | 04-025-4215 | 7 | Magnesium Manganese Aluminum Arsenic Iron Phosphorus Silicon Vanadium Oxide Hydroxide | Mg10.4 V0.36 Mn33.5 Fe0.14 Al0.69 Si6.77 As6.5 P0.3 O54 ( O H )42 | Carlfrancisite | 42 |

Anchor Scan Parameters

Dataset Name	6 Etosha18 Ssub 2-5cm S1 400C

File name	C:\aeris_data\XRD data\Goldstein\Etosha 2023\Etosha Clay Data\Sample 6\6 Etosha18 Ssub 2-5cm S1 400C.xrdml

Sample Identification	6 Etosha18 Ssub 2-5cm S1 400C

Measurement Start Date/Time	12/5/2023 12:41:57 PM

Operator	Instrument

Raw Data Origin	XRD measurement (*.XRDML)

Scan Axis	Gonio

Start Position [°2θ]	2.0054

End Position [°2θ]	29.9894

Step Size [°2θ]	0.0110

Scan Step Time [s]	48.1950

Scan Type	Continuous

PSD Mode	Scanning

PSD Length [°2θ]	5.54

Offset [°2θ]	0.0000

Divergence Slit Type	Fixed

Divergence Slit Size [°]	0.0603

Specimen Length [mm]	10.00

Measurement Temperature [°C]	25.00

Anode Material	Cu

K-α1 [Å]	1.54060

K-α2 [Å]	1.54443

K-β1 [Å]	1.39225

K-A2 / K-A1 Ratio	0.50000

Generator Settings	15 mA, 40 kV

Diffractometer Type	2082464

Diffractometer Number	0

Goniometer Radius [mm]	145.00

Dist. Focus-Diverg. Slit [mm]	95.00

Incident Beam Monochromator	No

Spinning	Yes